Discharge Test for Bluefin Battery #0182/B6

MBARI took delivery of three Bluefin pressure tolerant batteries in June of 2005, serial numbers #0179, #0180, and #0182. These units have been used in both the MBARI CTD vehicle and mapping vehicle over the last year. The first runs with these batteries occurred on August 18th of 2005. To date, the batteries have seen 16 discharge cycles to ~85% depth of discharge, and ~20 discharge cycles to <50% depth of discharge. The batteries have seen >2000 pressure cycles to depths of 100m or more, as well as two pressure cycles to a depth of 500m. The typical configuration of the MBARI vehicles contains three batteries.

Early in the use of #0182, after approximately 5 discharge cycles and 1100 pressure cycles to >100m,  one of the temperature sensors began exhibiting intermittent full scale readings. Further analysis of the data showed these readings to be cyclic with depth; as the vehicle descended, the temperature sensors would read properly, and as the vehicle ascended shallower than ~10m, it would read full scale. Further in-lab checking showed the sensor leads to be open circuit in the lab, indicating that the internal connections had broken. The most likely cause of this, based on past experience, was fatigue stress on the lead caused by the battery compressing and expanding with pressure.

A second anomaly occurred during the fall of 2005, when it was noticed that Cell5 of battery #0179 was 30mV lower than the other cells in the battery after a charge. Although this imbalance can be removed by balancing the battery, the balance history of the battery up to that point had been excellent. The ongoing concern is that a one of the cells of the quanta has become internally detached, again due to fatigue stress building up when the battery is pressure cycled. A similar problem has been noted in one of the Scripps Institute of Oceanography batteries (again on cell 5).

Beginning in 2006, MBARI began operating its CTD AUV without ship escort. The nominal flight profile is a 19 to 20 hour survey during which the vehicle undulates between 2m and 100m or 250m, depending on the survey. After 7 of these surveys, a noticeable loss in capacity occurred between these three batteries. To quantify this, we are performing constant current discharge tests on the batteries. We’re still in the process of performing these tests, but the testing for #0182 is complete and will be presented here.

Battery #0182 Test 5/26/2006 to 5/27/2006

Battery #0182 was discharged at a rate of 4.0A using a programmable DC load. The battery had been fully charged prior to the test using a 4A/3A/2A charge profile, to a cell voltage between 4.14V and 4.16V. The discharge test was interrupted at ~3 hours elapsed time, for ~25 minutes, due to a computer glitch; the discharge current was set to 0A during this period. The discharge test ended after an elapsed time of 15:10, when the battery turned off due to low voltage on Cell 5. A graph of the discharge is shown in Figure 1. 

Battery #0179 Test 5/27/2006 to 5/28/2006

Battery #0179 was discharged at a rate of 4.0A using a programmable DC load. The battery had been fully charged prior to the test using a 4A/3A/2A charge profile, to a cell voltage between 4.14V and 4.16V. The discharge logging was interrupted for 30 minutes at 3.5 hours elapsed time due to a problem with the logging program. During the glitch, discharge was maintained at 4.0A. Discharge ended after an elapsed time of 14:57, when the battery turned off due to low voltage on Cell 5. A graph of the discharge is shown in Figure 2. 

Battery #0180 Test 5/28/2006 to 5/29/2006

Battery #0180 was discharged using the same procedure as the other two batteries. Initial cells voltages were between 4.13V and 4.14V. There were no interruptions in the discharge. Data is plotted in Figure 3.

Conclusions

	Battery S/N
	As-Delivered Capacity 
	Measured Capacity 
	Cell Voltage @ End of Discharge

	
	Ah
	Wh
	Ah
	Wh
	Cell 1
	Cell 2
	Cell 3
	Cell 4
	Cell 5
	Cell 6
	Cell 7
	Cell 8

	#0179
	80.71
	2434.1
	60.01
	1834.8
	3.42
	3.65
	3.62
	3.43
	3.15
	3.64
	3.64
	3.28

	#0180
	77.21
	2345.4
	64.63
	1977.7
	3.64
	3.64
	3.64
	3.48
	3.14
	3.56
	3.63
	3.33

	#0182
	76.80
	2332.4
	62.02
	1907.3
	3.61
	3.66
	3.65
	3.62
	3.16
	3.65
	3.66
	3.50


Table 1 Discharge Test Results

Based on the data collected during this discharge, battery #0182 retains a capacity of 62Ah/1900Whr. The original test data for the battery showed a capacity of 76.8Ah/2332Whr. A capacity loss of almost 20% has occurred. Similar overall capacity changes have occurred in the other two batteries. This is well outside of what would be expected from the limited number of discharge cycles the unit has undergone. A review of operational discharges shows that this change has accelerated with unattended operations. These runs incur substantially more undulations. It should also be kept in mind that our discharge test was done at a substantially lower current than the data reported in the acceptance test. Had we conducted our test at higher current, the measured capacity would have been slightly lower due to cell impedance.

The discharge tests show that cell 5 and cell 8 of batteries #0179, #0180, and  #0182 are the most affected. Other cells (highlighted in Table 1) show a lesser degree of capacity decrease. To date, MBARI has now seen problems with low voltage/capacity cells 5 and 8 in four batteries (MBARI #0179, #0180, #0182, and SIO #0162/Cell 5) that underwent cyclic pressure service. It is my conclusion that there exists a flaw in design, assembly or construction of the batteries which is aggravated by a large number of pressure cycles.

Past testing has shown that the individual Li Polymer cells making up these batteries can compress and change volume by 1% to 2%, translating to almost 1 inch of dimensional change in the battery. Although we haven’t repeated that test with these particular batteries or cells, its not unreasonable to expect that some compression still occurs. This cyclic dimensional change can exert substantial fatigue stress on the internal components of the batteries (which are all bonded together by the urethane potting), in particular the tabs joining the cells together. Fracture of these tabs would lead to exactly the problem we have documented here. If this is the failure mode, then we may likely see an accelerating trend of damage (and capacity loss), since the cell tabs at this point have been exposed to a large number of fatigue cycles and fracture may be imminent.
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Figure 1 #0182 Discharge
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Figure 2 #0179 Discharge
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Figure 3 #0180 Discharge
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		S1148753507:		#B3q0		1148753507:		$B3q0		d-		32.99		3.96		21.48		4.12		4.14		0		-27483.78		0:05:00		m

		S1148753537:		#B3q0		1148753537:		$B3q0		d-		32.95		4		21.48		4.12		4.13		0		-27484.8		0:05:30		m

		S1148753567:		#B3q0		1148753567:		$B3q0		d-		32.95		4		21.48		4.11		4.13		0		-27485.97		0:06:00		m

		S1148753597:		#B3q0		1148753597:		$B3q0		d-		32.95		3.96		21.58		4.11		4.13		0		-27486.99		0:06:30		m
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		S1148753657:		#B3q0		1148753657:		$B3q0		d-		32.91		3.96		21.67		4.11		4.13		0		-27489.18		0:07:30		m

		S1148753687:		#B3q0		1148753687:		$B3q0		d-		32.91		4		21.67		4.11		4.13		0		-27490.34		0:08:00		m

		S1148753717:		#B3q0		1148753717:		$B3q0		d-		32.91		4		21.67		4.11		4.13		0		-27491.37		0:08:30		m

		S1148753747:		#B3q0		1148753747:		$B3q0		d-		32.91		3.96		21.87		4.11		4.13		0		-27492.53		0:09:00		m
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		S1148753927:		#B3q0		1148753927:		$B3q0		d-		32.95		3.96		21.97		4.1		4.12		0		-27499.09		0:12:00		m

		S1148753957:		#B3q0		1148753957:		$B3q0		d-		32.91		4.04		22.07		4.1		4.12		0		-27500.11		0:12:30		m

		S1148753987:		#B3q0		1148753987:		$B3q0		d-		32.91		3.96		22.07		4.1		4.12		0		-27501.28		0:13:00		m

		S1148754017:		#B3q0		1148754017:		$B3q0		d-		32.91		4.04		22.16		4.1		4.12		0		-27502.3		0:13:30		m

		S1148754047:		#B3q0		1148754047:		$B3q0		d-		32.88		4		22.16		4.1		4.12		0		-27503.47		0:14:00		m

		S1148754077:		#B3q0		1148754077:		$B3q0		d-		32.88		4		22.26		4.1		4.12		0		-27504.49		0:14:30		m

		S1148754107:		#B3q0		1148754107:		$B3q0		d-		32.91		3.96		22.26		4.1		4.12		0		-27505.66		0:15:00		m
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		S1148754467:		#B3q0		1148754467:		$B3q0		d-		32.84		4		22.55		4.09		4.12		0		-27518.79		0:21:00		m

		S1148754497:		#B3q0		1148754497:		$B3q0		d-		32.88		4		22.65		4.09		4.11		0		-27519.81		0:21:30		m

		S1148754527:		#B3q0		1148754527:		$B3q0		d-		32.84		4		22.65		4.09		4.11		0		-27520.98		0:22:00		m

		S1148754557:		#B3q0		1148754557:		$B3q0		d-		32.84		4.04		22.65		4.09		4.11		0		-27522		0:22:30		m

		S1148754587:		#B3q0		1148754587:		$B3q0		d-		32.84		4.04		22.65		4.09		4.11		0		-27523.17		0:23:00		m

		S1148754617:		#B3q0		1148754617:		$B3q0		d-		32.84		4		22.75		4.09		4.11		0		-27524.19		0:23:30		m

		S1148754647:		#B3q0		1148754647:		$B3q0		d-		32.76		3.96		22.75		4.09		4.11		0		-27525.37		0:24:00		m

		S1148754677:		#B3q0		1148754677:		$B3q0		d-		32.8		4		22.75		4.09		4.11		0		-27526.39		0:24:30		m

		S1148754707:		#B3q0		1148754707:		$B3q0		d-		32.84		4		22.85		4.09		4.11		0		-27527.56		0:25:00		m
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		S1148754827:		#B3q0		1148754827:		$B3q0		d-		32.76		4.04		22.85		4.09		4.11		0		-27531.94		0:27:00		m

		S1148754857:		#B3q0		1148754857:		$B3q0		d-		32.76		4		22.85		4.08		4.11		0		-27532.97		0:27:30		m

		S1148754887:		#B3q0		1148754887:		$B3q0		d-		32.8		4		23.04		4.08		4.11		0		-27534.14		0:28:00		m

		S1148754917:		#B3q0		1148754917:		$B3q0		d-		32.76		4		23.04		4.08		4.11		0		-27535.16		0:28:30		m

		S1148754947:		#B3q0		1148754947:		$B3q0		d-		32.76		4		23.04		4.08		4.11		0		-27536.33		0:29:00		m

		S1148754977:		#B3q0		1148754977:		$B3q0		d-		32.73		3.96		23.04		4.08		4.1		0		-27537.36		0:29:30		m

		S1148755007:		#B3q0		1148755007:		$B3q0		d-		32.76		4		23.04		4.08		4.1		0		-27538.53		0:30:00		m

		S1148755037:		#B3q0		1148755037:		$B3q0		d-		32.76		3.96		23.04		4.08		4.1		0		-27539.55		0:30:30		m

		S1148755067:		#B3q0		1148755067:		$B3q0		d-		32.73		4		23.04		4.08		4.1		0		-27540.72		0:31:00		m
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		S1148755277:		#B3q0		1148755277:		$B3q0		d-		32.73		4		23.24		4.08		4.1		0		-27548.32		0:34:30		m

		S1148755307:		#B3q0		1148755307:		$B3q0		d-		32.73		4.04		23.24		4.08		4.1		0		-27549.5		0:35:00		m

		S1148755337:		#B3q0		1148755337:		$B3q0		d-		32.69		4.04		23.24		4.08		4.1		0		-27550.52		0:35:30		m

		S1148755367:		#B3q0		1148755368:		$B3q0		d-		32.73		4		23.24		4.08		4.1		0		-27551.69		0:36:01		m

		S1148755397:		#B3q0		1148755397:		$B3q0		d-		32.73		4.04		23.33		4.08		4.1		0		-27552.71		0:36:30		m

		S1148755427:		#B3q0		1148755427:		$B3q0		d-		32.69		4		23.33		4.08		4.1		0		-27553.88		0:37:00		m

		S1148755457:		#B3q0		1148755457:		$B3q0		d-		32.73		4.04		23.33		4.08		4.1		0		-27554.9		0:37:30		m

		S1148755487:		#B3q0		1148755487:		$B3q0		d-		32.69		4.04		23.33		4.08		4.1		0		-27556.07		0:38:00		m

		S1148755517:		#B3q0		1148755517:		$B3q0		d-		32.73		4		23.43		4.07		4.1		0		-27557.09		0:38:30		m

		S1148755547:		#B3q0		1148755547:		$B3q0		d-		32.73		4		23.33		4.07		4.1		0		-27558.26		0:39:00		m

		S1148755577:		#B3q0		1148755577:		$B3q0		d-		32.69		4.04		23.43		4.07		4.1		0		-27559.28		0:39:30		m

		S1148755607:		#B3q0		1148755608:		$B3q0		d-		32.69		4		23.53		4.07		4.1		0		-27560.45		0:40:01		m

		S1148755637:		#B3q0		1148755637:		$B3q0		d-		32.73		4.04		23.43		4.07		4.1		0		-27561.47		0:40:30		m

		S1148755667:		#B3q0		1148755667:		$B3q0		d-		32.69		4.04		23.43		4.07		4.1		0		-27562.64		0:41:00		m

		S1148755697:		#B3q0		1148755697:		$B3q0		d-		32.73		4		23.53		4.07		4.1		0		-27563.65		0:41:30		m

		S1148755727:		#B3q0		1148755727:		$B3q0		d-		32.73		4.04		23.53		4.07		4.1		0		-27564.82		0:42:00		m

		S1148755757:		#B3q0		1148755757:		$B3q0		d-		32.69		4		23.63		4.07		4.09		0		-27565.84		0:42:30		m

		S1148755787:		#B3q0		1148755787:		$B3q0		d-		32.69		4.04		23.63		4.07		4.09		0		-27567.01		0:43:00		m

		S1148755817:		#B3q0		1148755818:		$B3q0		d-		32.69		4		23.53		4.07		4.09		0		-27568.03		0:43:31		m

		S1148755847:		#B3q0		1148755847:		$B3q0		d-		32.69		4		23.63		4.07		4.09		0		-27569.2		0:44:00		m

		S1148755877:		#B3q0		1148755877:		$B3q0		d-		32.61		4		23.53		4.07		4.09		0		-27570.22		0:44:30		m

		S1148755907:		#B3q0		1148755907:		$B3q0		d-		32.69		4		23.63		4.07		4.09		0		-27571.39		0:45:00		m

		S1148755937:		#B3q0		1148755937:		$B3q0		d-		32.69		4.04		23.53		4.07		4.09		0		-27572.42		0:45:30		m

		S1148755967:		#B3q0		1148755967:		$B3q0		d-		32.61		4		23.63		4.07		4.09		0		-27573.58		0:46:00		m

		S1148755997:		#B3q0		1148755997:		$B3q0		d-		32.65		4.04		23.63		4.07		4.09		0		-27574.61		0:46:30		m

		S1148756027:		#B3q0		1148756027:		$B3q0		d-		32.61		4		23.73		4.07		4.09		0		-27575.77		0:47:00		m

		S1148756057:		#B3q0		1148756057:		$B3q0		d-		32.61		4.04		23.73		4.07		4.09		0		-27576.79		0:47:30		m

		S1148756087:		#B3q0		1148756087:		$B3q0		d-		32.65		4		23.63		4.07		4.09		0		-27577.96		0:48:00		m

		S1148756117:		#B3q0		1148756117:		$B3q0		d-		32.61		4		23.82		4.07		4.09		0		-27578.98		0:48:30		m

		S1148756147:		#B3q0		1148756147:		$B3q0		d-		32.61		4		23.73		4.07		4.09		0		-27580.14		0:49:00		m

		S1148756177:		#B3q0		1148756177:		$B3q0		d-		32.61		4		23.82		4.07		4.09		0		-27581.17		0:49:30		m

		S1148756207:		#B3q0		1148756207:		$B3q0		d-		32.61		4		23.73		4.07		4.09		0		-27582.34		0:50:00		m

		S1148756237:		#B3q0		1148756237:		$B3q0		d-		32.61		4		23.73		4.06		4.09		0		-27583.36		0:50:30		m

		S1148756267:		#B3q0		1148756267:		$B3q0		d-		32.61		4		23.73		4.06		4.09		0		-27584.52		0:51:00		m

		S1148756297:		#B3q0		1148756297:		$B3q0		d-		32.61		4.04		23.92		4.06		4.08		0		-27585.53		0:51:30		m

		S1148756327:		#B3q0		1148756327:		$B3q0		d-		32.61		4		23.82		4.06		4.08		0		-27586.7		0:52:00		m

		S1148756357:		#B3q0		1148756357:		$B3q0		d-		32.61		4.04		23.82		4.06		4.08		0		-27587.72		0:52:30		m

		S1148756387:		#B3q0		1148756387:		$B3q0		d-		32.65		4		23.92		4.06		4.08		0		-27588.89		0:53:00		m

		S1148756417:		#B3q0		1148756417:		$B3q0		d-		32.61		4.04		23.92		4.06		4.08		0		-27589.91		0:53:30		m

		S1148756447:		#B3q0		1148756447:		$B3q0		d-		32.61		4		23.82		4.06		4.08		0		-27591.07		0:54:00		m

		S1148756477:		#B3q0		1148756477:		$B3q0		d-		32.61		4		23.82		4.06		4.08		0		-27592.09		0:54:30		m

		S1148756507:		#B3q0		1148756507:		$B3q0		d-		32.61		4.04		23.82		4.06		4.08		0		-27593.26		0:55:00		m

		S1148756537:		#B3q0		1148756537:		$B3q0		d-		32.57		4.08		23.92		4.06		4.08		0		-27594.29		0:55:30		m

		S1148756567:		#B3q0		1148756567:		$B3q0		d-		32.57		4.08		24.02		4.06		4.08		0		-27595.45		0:56:00		m

		S1148756597:		#B3q0		1148756597:		$B3q0		d-		32.53		4.04		23.92		4.06		4.08		0		-27596.48		0:56:30		m

		S1148756627:		#B3q0		1148756627:		$B3q0		d-		32.61		4		24.02		4.06		4.08		0		-27597.64		0:57:00		m

		S1148756657:		#B3q0		1148756657:		$B3q0		d-		32.53		4		24.02		4.06		4.08		0		-27598.66		0:57:30		m

		S1148756687:		#B3q0		1148756687:		$B3q0		d-		32.57		4.08		24.02		4.06		4.08		0		-27599.83		0:58:00		m

		S1148756717:		#B3q0		1148756717:		$B3q0		d-		32.57		4.04		23.92		4.05		4.08		0		-27600.85		0:58:30		m

		S1148756747:		#B3q0		1148756747:		$B3q0		d-		32.57		4.04		23.92		4.05		4.08		0		-27602.01		0:59:00		m

		S1148756777:		#B3q0		1148756777:		$B3q0		d-		32.53		4.04		24.02		4.05		4.08		0		-27603.04		0:59:30		m

		S1148756807:		#B3q0		1148756807:		$B3q0		d-		32.53		4		24.02		4.05		4.08		0		-27604.2		1:00:00		m

		S1148756837:		#B3q0		1148756837:		$B3q0		d-		32.53		4.04		24.02		4.05		4.08		0		-27605.23		1:00:30		m

		S1148756867:		#B3q0		1148756867:		$B3q0		d-		32.53		4.04		24.02		4.05		4.08		0		-27606.39		1:01:00		m

		S1148756897:		#B3q0		1148756898:		$B3q0		d-		32.53		4.04		24.02		4.05		4.08		0		-27607.41		1:01:30		m

		S1148756927:		#B3q0		1148756927:		$B3q0		d-		32.53		4.08		24.02		4.05		4.08		0		-27608.59		1:02:00		m

		S1148756957:		#B3q0		1148756957:		$B3q0		d-		32.53		4.04		24.12		4.05		4.08		0		-27609.61		1:02:30		m

		S1148756987:		#B3q0		1148756987:		$B3q0		d-		32.53		4.04		24.12		4.05		4.08		0		-27610.77		1:03:00		m

		S1148757017:		#B3q0		1148757017:		$B3q0		d-		32.5		4.08		24.12		4.05		4.08		0		-27611.79		1:03:30		m

		S1148757047:		#B3q0		1148757047:		$B3q0		d-		32.53		4.08		24.21		4.05		4.08		0		-27612.96		1:04:00		m

		S1148757077:		#B3q0		1148757077:		$B3q0		d-		32.53		4.04		24.21		4.05		4.07		0		-27613.98		1:04:30		m

		S1148757107:		#B3q0		1148757107:		$B3q0		d-		32.53		4.04		24.12		4.05		4.07		0		-27615.14		1:05:00		m

		S1148757137:		#B3q0		1148757137:		$B3q0		d-		32.5		4.04		24.12		4.05		4.07		0		-27616.16		1:05:30		m

		S1148757167:		#B3q0		1148757167:		$B3q0		d-		32.53		4		24.12		4.05		4.07		0		-27617.33		1:06:00		m

		S1148757197:		#B3q0		1148757197:		$B3q0		d-		32.5		4.04		24.31		4.05		4.07		0		-27618.35		1:06:30		m

		S1148757227:		#B3q0		1148757227:		$B3q0		d-		32.53		4		24.21		4.05		4.07		0		-27619.51		1:07:00		m

		S1148757257:		#B3q0		1148757257:		$B3q0		d-		32.46		4		24.21		4.05		4.07		0		-27620.53		1:07:31		m

		S1148757287:		#B3q0		1148757287:		$B3q0		d-		32.5		4		24.31		4.05		4.07		0		-27621.69		1:08:00		m

		S1148757317:		#B3q0		1148757317:		$B3q0		d-		32.5		4.04		24.31		4.05		4.07		0		-27622.71		1:08:30		m

		S1148757347:		#B3q0		1148757347:		$B3q0		d-		32.5		4		24.31		4.05		4.07		0		-27623.87		1:09:00		m

		S1148757377:		#B3q0		1148757377:		$B3q0		d-		32.5		4.04		24.31		4.05		4.07		0		-27624.89		1:09:30		m

		S1148757407:		#B3q0		1148757407:		$B3q0		d-		32.46		4.04		24.31		4.05		4.07		0		-27626.05		1:10:00		m

		S1148757437:		#B3q0		1148757437:		$B3q0		d-		32.46		4.04		24.31		4.04		4.07		0		-27627.07		1:10:30		m

		S1148757467:		#B3q0		1148757467:		$B3q0		d-		32.5		4.04		24.31		4.04		4.07		0		-27628.24		1:11:00		m

		S1148757497:		#B3q0		1148757497:		$B3q0		d-		32.46		4.04		24.31		4.04		4.07		0		-27629.26		1:11:30		m

		S1148757527:		#B3q0		1148757528:		$B3q0		d-		32.46		4.08		24.41		4.04		4.07		0		-27630.42		1:12:01		m

		S1148757557:		#B3q0		1148757557:		$B3q0		d-		32.42		4.04		24.41		4.04		4.07		0		-27631.44		1:12:30		m

		S1148757587:		#B3q0		1148757587:		$B3q0		d-		32.42		4		24.31		4.04		4.07		0		-27632.6		1:13:00		m

		S1148757617:		#B3q0		1148757617:		$B3q0		d-		32.42		4.08		24.41		4.04		4.07		0		-27633.62		1:13:30		m

		S1148757647:		#B3q0		1148757647:		$B3q0		d-		32.5		4.08		24.41		4.04		4.07		0		-27634.78		1:14:00		m

		S1148757677:		#B3q0		1148757677:		$B3q0		d-		32.42		4.04		24.31		4.04		4.07		0		-27635.8		1:14:30		m

		S1148757707:		#B3q0		1148757707:		$B3q0		d-		32.42		4.04		24.41		4.04		4.07		0		-27636.97		1:15:00		m

		S1148757737:		#B3q0		1148757737:		$B3q0		d-		32.42		4.04		24.51		4.04		4.07		0		-27637.99		1:15:30		m

		S1148757767:		#B3q0		1148757767:		$B3q0		d-		32.42		4.04		24.41		4.04		4.07		0		-27639.15		1:16:00		m

		S1148757797:		#B3q0		1148757797:		$B3q0		d-		32.42		4		24.41		4.04		4.07		0		-27640.17		1:16:30		m

		S1148757827:		#B3q0		1148757827:		$B3q0		d-		32.42		4.04		24.51		4.04		4.07		0		-27641.33		1:17:00		m

		S1148757857:		#B3q0		1148757857:		$B3q0		d-		32.42		4.08		24.41		4.04		4.07		0		-27642.35		1:17:30		m

		S1148757887:		#B3q0		1148757887:		$B3q0		d-		32.42		4		24.51		4.04		4.06		0		-27643.51		1:18:00		m

		S1148757917:		#B3q0		1148757917:		$B3q0		d-		32.42		4		24.51		4.04		4.07		0		-27644.53		1:18:30		m

		S1148757947:		#B3q0		1148757947:		$B3q0		d-		32.38		4		24.51		4.03		4.06		0		-27645.69		1:19:00		m

		S1148757977:		#B3q0		1148757977:		$B3q0		d-		32.42		4.04		24.41		4.03		4.06		0		-27646.7		1:19:30		m

		S1148758007:		#B3q0		1148758007:		$B3q0		d-		32.42		4.04		24.51		4.03		4.06		0		-27647.86		1:20:01		m

		S1148758037:		#B3q0		1148758037:		$B3q0		d-		32.42		4.04		24.51		4.03		4.06		0		-27648.88		1:20:31		m

		S1148758067:		#B3q0		1148758067:		$B3q0		d-		32.38		4.04		24.51		4.03		4.06		0		-27650.04		1:21:00		m

		S1148758097:		#B3q0		1148758097:		$B3q0		d-		32.42		4.04		24.51		4.03		4.06		0		-27651.06		1:21:30		m

		S1148758127:		#B3q0		1148758127:		$B3q0		d-		32.42		4.04		24.51		4.03		4.06		0		-27652.22		1:22:00		m

		S1148758157:		#B3q0		1148758157:		$B3q0		d-		32.42		4.04		24.51		4.03		4.06		0		-27653.24		1:22:30		m

		S1148758187:		#B3q0		1148758187:		$B3q0		d-		32.38		4.04		24.51		4.03		4.06		0		-27654.4		1:23:00		m

		S1148758217:		#B3q0		1148758217:		$B3q0		d-		32.42		4.04		24.6		4.03		4.06		0		-27655.41		1:23:30		m

		S1148758247:		#B3q0		1148758247:		$B3q0		d-		32.38		4		24.51		4.03		4.06		0		-27656.57		1:24:00		m

		S1148758277:		#B3q0		1148758277:		$B3q0		d-		32.38		4		24.51		4.03		4.06		0		-27657.59		1:24:30		m

		S1148758307:		#B3q0		1148758307:		$B3q0		d-		32.38		4		24.51		4.03		4.06		0		-27658.75		1:25:00		m

		S1148758337:		#B3q0		1148758337:		$B3q0		d-		32.38		4		24.51		4.03		4.06		0		-27659.76		1:25:30		m

		S1148758367:		#B3q0		1148758367:		$B3q0		d-		32.35		4		24.51		4.03		4.06		0		-27660.92		1:26:00		m

		S1148758397:		#B3q0		1148758397:		$B3q0		d-		32.35		4		24.6		4.03		4.06		0		-27661.93		1:26:30		m

		S1148758427:		#B3q0		1148758427:		$B3q0		d-		32.35		4		24.6		4.03		4.06		0		-27663.09		1:27:00		m

		S1148758457:		#B3q0		1148758457:		$B3q0		d-		32.38		4.04		24.7		4.03		4.06		0		-27664.1		1:27:30		m

		S1148758487:		#B3q0		1148758487:		$B3q0		d-		32.35		4.04		24.7		4.03		4.05		0		-27665.26		1:28:00		m

		S1148758517:		#B3q0		1148758517:		$B3q0		d-		32.35		4.04		24.7		4.03		4.05		0		-27666.27		1:28:30		m

		S1148758547:		#B3q0		1148758547:		$B3q0		d-		32.31		4		24.7		4.03		4.05		0		-27667.44		1:29:00		m

		S1148758577:		#B3q0		1148758577:		$B3q0		d-		32.35		4.04		24.7		4.03		4.05		0		-27668.45		1:29:30		m

		S1148758607:		#B3q0		1148758607:		$B3q0		d-		32.31		4		24.6		4.03		4.05		0		-27669.6		1:30:00		m

		S1148758637:		#B3q0		1148758637:		$B3q0		d-		32.31		4		24.7		4.03		4.05		0		-27670.62		1:30:30		m

		S1148758667:		#B3q0		1148758667:		$B3q0		d-		32.35		4		24.7		4.03		4.05		0		-27671.77		1:31:00		m

		S1148758697:		#B3q0		1148758697:		$B3q0		d-		32.35		4.04		24.7		4.03		4.05		0		-27672.78		1:31:30		m

		S1148758727:		#B3q0		1148758727:		$B3q0		d-		32.31		4		24.7		4.02		4.05		0		-27673.94		1:32:01		m

		S1148758757:		#B3q0		1148758757:		$B3q0		d-		32.31		4		24.7		4.02		4.05		0		-27674.95		1:32:30		m

		S1148758787:		#B3q0		1148758787:		$B3q0		d-		32.35		4		24.8		4.02		4.05		0		-27676.1		1:33:00		m

		S1148758817:		#B3q0		1148758818:		$B3q0		d-		32.35		4.04		24.8		4.02		4.05		0		-27677.12		1:33:31		m

		S1148758847:		#B3q0		1148758847:		$B3q0		d-		32.31		4.04		24.8		4.02		4.05		0		-27678.28		1:34:00		m

		S1148758877:		#B3q0		1148758877:		$B3q0		d-		32.31		4		24.8		4.02		4.05		0		-27679.29		1:34:30		m

		S1148758907:		#B3q0		1148758907:		$B3q0		d-		32.31		4.04		24.8		4.02		4.05		0		-27680.45		1:35:00		m

		S1148758937:		#B3q0		1148758937:		$B3q0		d-		32.31		4		24.7		4.02		4.05		0		-27681.46		1:35:30		m

		S1148758967:		#B3q0		1148758967:		$B3q0		d-		32.27		4		24.7		4.02		4.05		0		-27682.62		1:36:00		m

		S1148758997:		#B3q0		1148758997:		$B3q0		d-		32.27		4.04		24.7		4.02		4.05		0		-27683.63		1:36:30		m

		S1148759027:		#B3q0		1148759027:		$B3q0		d-		32.27		4.08		24.7		4.02		4.05		0		-27684.79		1:37:00		m

		S1148759057:		#B3q0		1148759057:		$B3q0		d-		32.27		4.04		24.8		4.02		4.05		0		-27685.8		1:37:30		m

		S1148759087:		#B3q0		1148759087:		$B3q0		d-		32.27		4.04		24.7		4.02		4.05		0		-27686.96		1:38:00		m

		S1148759117:		#B3q0		1148759117:		$B3q0		d-		32.27		4		24.8		4.02		4.05		0		-27687.97		1:38:30		m

		S1148759147:		#B3q0		1148759147:		$B3q0		d-		32.31		4.08		24.8		4.02		4.05		0		-27689.13		1:39:00		m

		S1148759177:		#B3q0		1148759177:		$B3q0		d-		32.27		4.04		24.9		4.02		4.05		0		-27690.14		1:39:30		m

		S1148759207:		#B3q0		1148759207:		$B3q0		d-		32.27		4.04		24.8		4.02		4.05		0		-27691.29		1:40:00		m

		S1148759237:		#B3q0		1148759237:		$B3q0		d-		32.27		4		24.8		4.01		4.05		0		-27692.3		1:40:30		m

		S1148759267:		#B3q0		1148759267:		$B3q0		d-		32.23		4.08		24.9		4.01		4.05		0		-27693.46		1:41:00		m

		S1148759297:		#B3q0		1148759297:		$B3q0		d-		32.27		4.04		24.8		4.01		4.05		0		-27694.47		1:41:30		m

		S1148759327:		#B3q0		1148759327:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27695.63		1:42:00		m

		S1148759357:		#B3q0		1148759357:		$B3q0		d-		32.23		4		24.8		4.01		4.04		0		-27696.64		1:42:30		m

		S1148759387:		#B3q0		1148759388:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27697.79		1:43:01		m

		S1148759417:		#B3q0		1148759417:		$B3q0		d-		32.27		4		24.9		4.01		4.04		0		-27698.8		1:43:30		m

		S1148759447:		#B3q0		1148759447:		$B3q0		d-		32.27		4		24.9		4.01		4.04		0		-27699.95		1:44:01		m

		S1148759477:		#B3q0		1148759477:		$B3q0		d-		32.23		4.04		24.9		4.01		4.04		0		-27700.96		1:44:30		m

		S1148759507:		#B3q0		1148759507:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27702.11		1:45:00		m

		S1148759537:		#B3q0		1148759537:		$B3q0		d-		32.27		4.04		24.9		4.01		4.04		0		-27703.12		1:45:30		m

		S1148759567:		#B3q0		1148759567:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27704.28		1:46:00		m

		S1148759597:		#B3q0		1148759597:		$B3q0		d-		32.27		4		24.9		4.01		4.04		0		-27705.29		1:46:30		m

		S1148759627:		#B3q0		1148759627:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27706.44		1:47:00		m

		S1148759657:		#B3q0		1148759657:		$B3q0		d-		32.19		4.08		24.9		4.01		4.04		0		-27707.45		1:47:30		m

		S1148759687:		#B3q0		1148759687:		$B3q0		d-		32.23		4.04		24.9		4.01		4.04		0		-27708.6		1:48:00		m

		S1148759717:		#B3q0		1148759717:		$B3q0		d-		32.19		4		24.9		4.01		4.04		0		-27709.61		1:48:30		m

		S1148759747:		#B3q0		1148759747:		$B3q0		d-		32.19		4		24.9		4.01		4.04		0		-27710.77		1:49:00		m

		S1148759777:		#B3q0		1148759777:		$B3q0		d-		32.19		4.04		24.9		4.01		4.04		0		-27711.78		1:49:30		m

		S1148759807:		#B3q0		1148759807:		$B3q0		d-		32.23		4		24.9		4.01		4.04		0		-27712.94		1:50:00		m

		S1148759837:		#B3q0		1148759837:		$B3q0		d-		32.19		4.04		24.9		4.01		4.04		0		-27713.94		1:50:30		m

		S1148759867:		#B3q0		1148759867:		$B3q0		d-		32.19		4.04		24.9		4.01		4.04		0		-27715.09		1:51:00		m

		S1148759897:		#B3q0		1148759897:		$B3q0		d-		32.16		4		25		4.01		4.03		0		-27716.1		1:51:30		m

		S1148759927:		#B3q0		1148759927:		$B3q0		d-		32.16		4		24.9		4.01		4.03		0		-27717.25		1:52:00		m

		S1148759957:		#B3q0		1148759957:		$B3q0		d-		32.19		4		24.9		4.01		4.03		0		-27718.25		1:52:30		m

		S1148759987:		#B3q0		1148759987:		$B3q0		d-		32.19		4.08		24.9		4.01		4.03		0		-27719.4		1:53:00		m

		S1148760017:		#B3q0		1148760017:		$B3q0		d-		32.19		4.08		25		4		4.03		0		-27720.41		1:53:30		m

		S1148760047:		#B3q0		1148760047:		$B3q0		d-		32.19		4		25.09		4		4.03		0		-27721.56		1:54:00		m

		S1148760077:		#B3q0		1148760077:		$B3q0		d-		32.12		4		25		4		4.03		0		-27722.57		1:54:30		m

		S1148760107:		#B3q0		1148760107:		$B3q0		d-		32.19		4.08		25		4		4.03		0		-27723.72		1:55:00		m

		S1148760137:		#B3q0		1148760137:		$B3q0		d-		32.16		4.04		25.09		4		4.03		0		-27724.73		1:55:30		m

		S1148760167:		#B3q0		1148760168:		$B3q0		d-		32.16		4		25		4		4.03		0		-27725.89		1:56:01		m

		S1148760197:		#B3q0		1148760197:		$B3q0		d-		32.16		4.08		25		4		4.03		0		-27726.9		1:56:30		m

		S1148760227:		#B3q0		1148760227:		$B3q0		d-		32.12		4		25		4		4.03		0		-27728.06		1:57:00		m

		S1148760257:		#B3q0		1148760257:		$B3q0		d-		32.16		4.04		25.09		4		4.03		0		-27729.07		1:57:31		m

		S1148760287:		#B3q0		1148760287:		$B3q0		d-		32.16		4		25		4		4.03		0		-27730.21		1:58:00		m

		S1148760317:		#B3q0		1148760317:		$B3q0		d-		32.16		4.04		25.09		4		4.03		0		-27731.22		1:58:30		m

		S1148760347:		#B3q0		1148760347:		$B3q0		d-		32.12		4		25		4		4.03		0		-27732.38		1:59:00		m

		S1148760377:		#B3q0		1148760377:		$B3q0		d-		32.12		4.04		25		4		4.03		0		-27733.38		1:59:30		m

		S1148760407:		#B3q0		1148760407:		$B3q0		d-		32.12		4		25.09		4		4.03		0		-27734.54		2:00:00		m

		S1148760437:		#B3q0		1148760437:		$B3q0		d-		32.16		4.08		25.09		4		4.03		0		-27735.55		2:00:30		m

		S1148760467:		#B3q0		1148760467:		$B3q0		d-		32.12		4.04		25.09		4		4.03		0		-27736.7		2:01:00		m

		S1148760497:		#B3q0		1148760497:		$B3q0		d-		32.16		4		25.09		4		4.03		0		-27737.71		2:01:30		m

		S1148760527:		#B3q0		1148760527:		$B3q0		d-		32.12		4.04		25		4		4.03		0		-27738.86		2:02:00		m

		S1148760557:		#B3q0		1148760558:		$B3q0		d-		32.12		4		25.09		4		4.03		0		-27739.86		2:02:31		m

		S1148760587:		#B3q0		1148760587:		$B3q0		d-		32.12		4.04		25.19		4		4.03		0		-27741.01		2:03:00		m

		S1148760617:		#B3q0		1148760617:		$B3q0		d-		32.12		4.08		25.09		4		4.03		0		-27742.02		2:03:30		m

		S1148760647:		#B3q0		1148760647:		$B3q0		d-		32.12		4.04		25.19		4		4.03		0		-27743.17		2:04:00		m

		S1148760677:		#B3q0		1148760677:		$B3q0		d-		32.12		4.04		25.09		4		4.03		0		-27744.18		2:04:30		m

		S1148760707:		#B3q0		1148760707:		$B3q0		d-		32.08		4		25.19		4		4.03		0		-27745.33		2:05:00		m

		S1148760737:		#B3q0		1148760737:		$B3q0		d-		32.08		4.04		25.09		4		4.03		0		-27746.34		2:05:30		m

		S1148760767:		#B3q0		1148760767:		$B3q0		d-		32.08		4		25.09		3.99		4.03		0		-27747.49		2:06:00		m

		S1148760797:		#B3q0		1148760797:		$B3q0		d-		32.08		4		25.19		3.99		4.03		0		-27748.5		2:06:30		m

		S1148760827:		#B3q0		1148760827:		$B3q0		d-		32.08		4.04		25.09		3.99		4.02		0		-27749.64		2:07:01		m

		S1148760857:		#B3q0		1148760857:		$B3q0		d-		32.08		4.04		25.29		3.99		4.02		0		-27750.65		2:07:30		m

		S1148760887:		#B3q0		1148760887:		$B3q0		d-		32.04		4		25.09		3.99		4.02		0		-27751.8		2:08:00		m

		S1148760917:		#B3q0		1148760917:		$B3q0		d-		32.08		4.04		25.09		3.99		4.02		0		-27752.81		2:08:30		m

		S1148760947:		#B3q0		1148760947:		$B3q0		d-		32.04		4.04		25.19		3.99		4.02		0		-27753.95		2:09:00		m

		S1148760977:		#B3q0		1148760977:		$B3q0		d-		32.08		4		25.19		3.99		4.02		0		-27754.95		2:09:30		m

		S1148761007:		#B3q0		1148761007:		$B3q0		d-		32.04		4.08		25.19		3.99		4.02		0		-27756.1		2:10:00		m

		S1148761037:		#B3q0		1148761037:		$B3q0		d-		32.08		4		25.19		3.99		4.02		0		-27757.11		2:10:30		m

		S1148761067:		#B3q0		1148761067:		$B3q0		d-		32.08		4		25.29		3.99		4.02		0		-27758.25		2:11:00		m

		S1148761097:		#B3q0		1148761097:		$B3q0		d-		32.08		4.04		25.19		3.99		4.02		0		-27759.25		2:11:30		m

		S1148761127:		#B3q0		1148761127:		$B3q0		d-		32.04		4		25.29		3.99		4.02		0		-27760.4		2:12:01		m

		S1148761157:		#B3q0		1148761157:		$B3q0		d-		32.08		4		25.29		3.99		4.02		0		-27761.41		2:12:30		m

		S1148761187:		#B3q0		1148761187:		$B3q0		d-		32.04		4.04		25.29		3.99		4.02		0		-27762.56		2:13:00		m

		S1148761217:		#B3q0		1148761217:		$B3q0		d-		32.04		4.04		25.19		3.99		4.02		0		-27763.56		2:13:30		m

		S1148761247:		#B3q0		1148761247:		$B3q0		d-		32.04		4.04		25.19		3.99		4.02		0		-27764.71		2:14:00		m

		S1148761277:		#B3q0		1148761277:		$B3q0		d-		32		4		25.19		3.99		4.02		0		-27765.71		2:14:30		m

		S1148761307:		#B3q0		1148761307:		$B3q0		d-		32.04		4.04		25.19		3.98		4.02		0		-27766.86		2:15:00		m

		S1148761337:		#B3q0		1148761337:		$B3q0		d-		32.04		4.04		25.19		3.98		4.02		0		-27767.87		2:15:31		m

		S1148761367:		#B3q0		1148761367:		$B3q0		d-		32.04		4		25.29		3.98		4.02		0		-27769.02		2:16:00		m

		S1148761397:		#B3q0		1148761397:		$B3q0		d-		32.04		4		25.29		3.98		4.01		0		-27770.02		2:16:31		m

		S1148761427:		#B3q0		1148761427:		$B3q0		d-		32		4.08		25.39		3.98		4.01		0		-27771.16		2:17:00		m

		S1148761457:		#B3q0		1148761457:		$B3q0		d-		32		4.08		25.29		3.98		4.01		0		-27772.17		2:17:30		m

		S1148761487:		#B3q0		1148761487:		$B3q0		d-		32		4		25.29		3.98		4.01		0		-27773.32		2:18:00		m

		S1148761517:		#B3q0		1148761517:		$B3q0		d-		32		4.08		25.29		3.98		4.01		0		-27774.32		2:18:30		m

		S1148761547:		#B3q0		1148761547:		$B3q0		d-		32		4.04		25.29		3.98		4.01		0		-27775.47		2:19:00		m

		S1148761577:		#B3q0		1148761577:		$B3q0		d-		32		4		25.29		3.98		4.01		0		-27776.48		2:19:30		m

		S1148761607:		#B3q0		1148761607:		$B3q0		d-		32		4.08		25.29		3.98		4.01		0		-27777.62		2:20:00		m

		S1148761637:		#B3q0		1148761637:		$B3q0		d-		32		4.04		25.39		3.98		4.01		0		-27778.62		2:20:30		m

		S1148761667:		#B3q0		1148761667:		$B3q0		d-		31.97		4		25.29		3.98		4.01		0		-27779.77		2:21:00		m

		S1148761697:		#B3q0		1148761697:		$B3q0		d-		32		4		25.29		3.98		4.01		0		-27780.77		2:21:31		m

		S1148761727:		#B3q0		1148761727:		$B3q0		d-		31.97		4.08		25.29		3.98		4.01		0		-27781.91		2:22:01		m

		S1148761757:		#B3q0		1148761757:		$B3q0		d-		32		3.96		25.29		3.98		4.01		0		-27782.91		2:22:30		m

		S1148761787:		#B3q0		1148761787:		$B3q0		d-		31.97		4		25.29		3.98		4.01		0		-27784.06		2:23:00		m

		S1148761817:		#B3q0		1148761817:		$B3q0		d-		31.97		4.04		25.39		3.98		4.01		0		-27785.06		2:23:31		m

		S1148761847:		#B3q0		1148761847:		$B3q0		d-		31.97		4.04		25.39		3.98		4.01		0		-27786.2		2:24:00		m

		S1148761877:		#B3q0		1148761877:		$B3q0		d-		31.97		4.04		25.39		3.98		4.01		0		-27787.21		2:24:30		m

		S1148761907:		#B3q0		1148761907:		$B3q0		d-		32		4		25.29		3.98		4.01		0		-27788.35		2:25:00		m

		S1148761937:		#B3q0		1148761937:		$B3q0		d-		31.97		4.04		25.29		3.98		4.01		0		-27789.36		2:25:30		m

		S1148761967:		#B3q0		1148761967:		$B3q0		d-		31.97		4.04		25.39		3.98		4.01		0		-27790.5		2:26:00		m

		S1148761997:		#B3q0		1148761997:		$B3q0		d-		31.97		4.04		25.39		3.98		4.01		0		-27791.5		2:26:30		m

		S1148762027:		#B3q0		1148762027:		$B3q0		d-		31.97		4		25.39		3.98		4.01		0		-27792.65		2:27:00		m

		S1148762057:		#B3q0		1148762057:		$B3q0		d-		31.93		4.08		25.39		3.98		4.01		0		-27793.66		2:27:30		m

		S1148762087:		#B3q0		1148762087:		$B3q0		d-		31.97		4		25.48		3.98		4.01		0		-27794.8		2:28:00		m

		S1148762117:		#B3q0		1148762117:		$B3q0		d-		31.97		4.04		25.29		3.97		4.01		0		-27795.8		2:28:30		m

		S1148762147:		#B3q0		1148762147:		$B3q0		d-		31.97		4		25.39		3.97		4.01		0		-27796.95		2:29:00		m

		S1148762177:		#B3q0		1148762177:		$B3q0		d-		31.93		4.04		25.48		3.97		4.01		0		-27797.96		2:29:30		m

		S1148762207:		#B3q0		1148762207:		$B3q0		d-		31.93		4.04		25.39		3.97		4.01		0		-27799.1		2:30:00		m

		S1148762237:		#B3q0		1148762237:		$B3q0		d-		31.93		4.08		25.48		3.97		4.01		0		-27800.1		2:30:30		m

		S1148762267:		#B3q0		1148762267:		$B3q0		d-		31.93		4		25.48		3.97		4.01		0		-27801.25		2:31:00		m

		S1148762297:		#B3q0		1148762297:		$B3q0		d-		31.93		4.04		25.39		3.97		4		0		-27802.25		2:31:30		m

		S1148762327:		#B3q0		1148762327:		$B3q0		d-		31.93		4.04		25.48		3.97		4		0		-27803.39		2:32:00		m

		S1148762357:		#B3q0		1148762357:		$B3q0		d-		31.89		4.04		25.48		3.97		4		0		-27804.4		2:32:30		m

		S1148762387:		#B3q0		1148762387:		$B3q0		d-		31.93		4		25.39		3.97		4		0		-27805.54		2:33:01		m

		S1148762417:		#B3q0		1148762417:		$B3q0		d-		31.93		4		25.48		3.97		4		0		-27806.54		2:33:30		m

		S1148762447:		#B3q0		1148762447:		$B3q0		d-		31.93		4		25.48		3.97		4		0		-27807.69		2:34:00		m

		S1148762477:		#B3q0		1148762477:		$B3q0		d-		31.89		4.04		25.39		3.97		4		0		-27808.68		2:34:30		m

		S1148762507:		#B3q0		1148762507:		$B3q0		d-		31.93		4		25.48		3.97		4		0		-27809.83		2:35:00		m

		S1148762537:		#B3q0		1148762537:		$B3q0		d-		31.93		4.04		25.48		3.97		4		0		-27810.83		2:35:30		m

		S1148762567:		#B3q0		1148762567:		$B3q0		d-		31.89		4.04		25.39		3.97		4		0		-27811.97		2:36:00		m

		S1148762597:		#B3q0		1148762597:		$B3q0		d-		31.89		4		25.48		3.97		4		0		-27812.97		2:36:30		m

		S1148762627:		#B3q0		1148762627:		$B3q0		d-		31.89		4		25.39		3.97		4		0		-27814.12		2:37:01		m

		S1148762657:		#B3q0		1148762657:		$B3q0		d-		31.89		4.04		25.48		3.97		4		0		-27815.12		2:37:30		m

		S1148762687:		#B3q0		1148762687:		$B3q0		d-		31.89		4.04		25.48		3.96		4		0		-27816.26		2:38:01		m

		S1148762717:		#B3q0		1148762717:		$B3q0		d-		31.85		4		25.39		3.96		4		0		-27817.26		2:38:31		m

		S1148762747:		#B3q0		1148762747:		$B3q0		d-		31.85		4		25.48		3.96		4		0		-27818.4		2:39:01		m

		S1148762777:		#B3q0		1148762777:		$B3q0		d-		31.89		4		25.39		3.96		4		0		-27819.4		2:39:30		m

		S1148762807:		#B3q0		1148762807:		$B3q0		d-		31.85		4.04		25.48		3.96		4		0		-27820.54		2:40:01		m

		S1148762837:		#B3q0		1148762837:		$B3q0		d-		31.85		4.08		25.58		3.96		4		0		-27821.54		2:40:30		m

		S1148762867:		#B3q0		1148762867:		$B3q0		d-		31.82		4.04		25.48		3.96		4		0		-27822.68		2:41:00		m

		S1148762897:		#B3q0		1148762897:		$B3q0		d-		31.85		4.04		25.58		3.96		4		0		-27823.68		2:41:30		m

		S1148762927:		#B3q0		1148762927:		$B3q0		d-		31.82		4		25.58		3.96		4		0		-27824.82		2:42:01		m

		S1148762957:		#B3q0		1148762957:		$B3q0		d-		31.85		4		25.48		3.96		4		0		-27825.82		2:42:30		m

		S1148762987:		#B3q0		1148762987:		$B3q0		d-		31.85		4		25.48		3.96		4		0		-27826.97		2:43:00		m

		S1148763017:		#B3q0		1148763017:		$B3q0		d-		31.85		4.04		25.48		3.96		4		0		-27827.96		2:43:30		m

		S1148763047:		#B3q0		1148763047:		$B3q0		d-		31.85		4.08		25.48		3.96		4		0		-27829.11		2:44:00		m

		S1148763077:		#B3q0		1148763077:		$B3q0		d-		31.82		4.04		25.58		3.96		4		0		-27830.1		2:44:30		m

		S1148763107:		#B3q0		1148763107:		$B3q0		d-		31.82		4.08		25.58		3.96		4		0		-27831.24		2:45:00		m

		S1148763137:		#B3q0		1148763137:		$B3q0		d-		31.82		4		25.58		3.96		4		0		-27832.24		2:45:31		m

		S1148763167:		#B3q0		1148763167:		$B3q0		d-		31.82		4		25.58		3.96		4		0		-27833.38		2:46:01		m

		S1148763197:		#B3q0		1148763197:		$B3q0		d-		31.85		4.04		25.58		3.96		4		0		-27834.38		2:46:30		m

		S1148763227:		#B3q0		1148763227:		$B3q0		d-		31.85		4.04		25.58		3.96		3.99		0		-27835.52		2:47:00		m

		S1148763257:		#B3q0		1148763257:		$B3q0		d-		31.82		4.04		25.48		3.96		3.99		0		-27836.52		2:47:31		m

		S1148763287:		#B3q0		1148763287:		$B3q0		d-		31.82		4.04		25.48		3.96		3.99		0		-27837.66		2:48:01		m

		S1148763317:		#B3q0		1148763317:		$B3q0		d-		31.82		4		25.68		3.96		3.99		0		-27838.65		2:48:30		m

		S1148763347:		#B3q0		1148763347:		$B3q0		d-		31.82		4.04		25.58		3.96		3.99		0		-27839.79		2:49:00		m

		S1148763377:		#B3q0		1148763377:		$B3q0		d-		31.82		4.04		25.58		3.96		3.99		0		-27840.78		2:49:30		m

		S1148763407:		#B3q0		1148763407:		$B3q0		d-		31.82		3.96		25.68		3.96		3.99		0		-27841.92		2:50:00		m

		S1148763437:		#B3q0		1148763437:		$B3q0		d-		31.78		4		25.58		3.96		3.99		0		-27842.92		2:50:31		m

		S1148763467:		#B3q0		1148763467:		$B3q0		d-		31.82		4		25.48		3.96		3.99		0		-27844.06		2:51:00		m

		S1148763497:		#B3q0		1148763497:		$B3q0		d-		31.82		4		25.58		3.96		3.99		0		-27845.06		2:51:30		m

		S1148763527:		#B3q0		1148763527:		$B3q0		d-		31.78		4.04		25.58		3.95		3.99		0		-27846.2		2:52:00		m

		S1148763557:		#B3q0		1148763557:		$B3q0		d-		31.82		4		25.58		3.95		3.99		0		-27847.19		2:52:30		m

		S1148763587:		#B3q0		1148763587:		$B3q0		d-		31.78		4.04		25.58		3.95		3.99		0		-27848.33		2:53:00		m

		S1148763617:		#B3q0		1148763617:		$B3q0		d-		31.82		4		25.58		3.95		3.99		0		-27849.33		2:53:30		m

		S1148763647:		#B3q0		1148763647:		$B3q0		d-		31.82		4		25.58		3.95		3.99		0		-27850.47		2:54:00		m

		S1148763677:		#B3q0		1148763677:		$B3q0		d-		31.78		4.04		25.58		3.95		3.99		0		-27851.47		2:54:31		m

		S1148763707:		#B3q0		1148763707:		$B3q0		d-		31.78		4.04		25.58		3.95		3.99		0		-27852.61		2:55:00		m

		S1148763737:		#B3q0		1148763737:		$B3q0		d-		31.78		4		25.68		3.95		3.99		0		-27853.6		2:55:30		m

		S1148763767:		#B3q0		1148763767:		$B3q0		d-		31.74		4.04		25.68		3.95		3.99		0		-27854.74		2:56:00		m

		S1148763797:		#B3q0		1148763797:		$B3q0		d-		31.78		4		25.58		3.95		3.99		0		-27855.74		2:56:31		m

		S1148763827:		#B3q0		1148763827:		$B3q0		d-		31.74		4.08		25.58		3.95		3.99		0		-27856.87		2:57:00		m

		S1148763857:		#B3q0		1148763857:		$B3q0		d-		31.78		4		25.68		3.95		3.99		0		-27857.86		2:57:30		m

		S1148763887:		#B3q0		1148763887:		$B3q0		d-		31.74		4.04		25.68		3.95		3.98		0		-27859		2:58:00		m

		S1148763917:		#B3q0		1148763917:		$B3q0		d-		31.78		4.04		25.58		3.95		3.98		0		-27859.99		2:58:30		m

		S1148763947:		#B3q0		1148763947:		$B3q0		d-		31.74		4.04		25.58		3.95		3.98		0		-27861.13		2:59:00		m

		S1148763977:		#B3q0		1148763977:		$B3q0		d-		31.74		4.04		25.68		3.95		3.98		0		-27862.12		2:59:30		m

		S1148764007:		#B3q0		1148764007:		$B3q0		d-		31.74		4.08		25.68		3.95		3.98		0		-27863.26		3:00:00		m

		S1148764037:		#B3q0		1148764037:		$B3q0		d-		31.74		4		25.68		3.95		3.98		0		-27864.25		3:00:30		m

		S1148764067:		#B3q0		1148764067:		$B3q0		d-		31.74		4		25.68		3.95		3.98		0		-27865.39		3:01:00		m

		S1148764097:		#B3q0		1148764097:		$B3q0		d-		31.74		4.04		25.58		3.95		3.98		0		-27866.39		3:01:30		m

		S1148764127:		#B3q0		1148764127:		$B3q0		d-		31.74		4		25.68		3.94		3.98		0		-27867.52		3:02:01		m

		S1148764157:		#B3q0		1148764157:		$B3q0		d-		31.7		4.08		25.58		3.94		3.98		0		-27868.52		3:02:31		m

		S1148764187:		#B3q0		1148764187:		$B3q0		d-		31.7		4.04		25.78		3.94		3.98		0		-27869.65		3:03:00		m

		S1148764217:		#B3q0		1148764217:		$B3q0		d-		31.74		4		25.68		3.94		3.98		0		-27870.65		3:03:30		m

		S1148764247:		#B3q0		1148764247:		$B3q0		d-		31.7		4		25.68		3.94		3.98		0		-27871.79		3:04:00		m

		S1148764277:		#B3q0		1148764277:		$B3q0		d-		31.7		4		25.68		3.94		3.98		0		-27872.78		3:04:30		m

		S1148764307:		#B3q0		1148764307:		$B3q0		d-		31.7		4.04		25.68		3.94		3.98		0		-27873.92		3:05:00		m

		S1148764337:		#B3q0		1148764337:		$B3q0		d-		31.74		4		25.68		3.94		3.98		0		-27874.91		3:05:30		m

		S1148764367:		#B3q0		1148764367:		$B3q0		d-		31.7		4		25.78		3.94		3.98		0		-27876.05		3:06:00		m

		S1148764397:		#B3q0		1148764397:		$B3q0		d-		31.7		4.04		25.78		3.94		3.98		0		-27877.04		3:06:30		m

		S1148764427:		#B3q0		1148764427:		$B3q0		d-		31.7		4		25.78		3.94		3.98		0		-27878.18		3:07:00		m

		S1148764457:		#B3q0		1148764457:		$B3q0		d-		31.7		4.04		25.78		3.94		3.98		0		-27879.17		3:07:30		m

		S1148764487:		#B3q0		1148764487:		$B3q0		d-		31.66		4.04		25.78		3.94		3.98		0		-27880.3		3:08:00		m

		S1148764517:		#B3q0		1148764517:		$B3q0		d-		31.7		4		25.68		3.94		3.98		0		-27881.29		3:08:30		m

		S1148764547:		#B3q0		1148764547:		$B3q0		d-		31.66		4.04		25.68		3.94		3.98		0		-27882.43		3:09:01		m

		S1148764577:		#B3q0		1148764577:		$B3q0		d-		31.7		4.04		25.78		3.94		3.98		0		-27883.42		3:09:30		m

		S1148764607:		#B3q0		1148764607:		$B3q0		d-		31.66		4.04		25.78		3.94		3.98		0		-27884.55		3:10:00		m

		S1148764637:		#B3q0		1148764637:		$B3q0		d-		31.66		4		25.78		3.94		3.98		0		-27885.55		3:10:30		m

		S1148764667:		#B3q0		1148764667:		$B3q0		d-		31.7		4		25.78		3.94		3.98		0		-27886.68		3:11:00		m

		S1148764697:		#B3q0		1148764697:		$B3q0		d-		31.66		4.04		25.68		3.94		3.98		0		-27887.67		3:11:30		m

		S1148764727:		#B3q0		1148764727:		$B3q0		d-		31.66		4.08		25.68		3.94		3.98		0		-27888.8		3:12:01		m

		S1148764757:		#B3q0		1148764757:		$B3q0		d-		31.66		4.04		25.78		3.94		3.98		0		-27889.8		3:12:30		m

		S1148764787:		#B3q0		1148764787:		$B3q0		d-		31.66		4.04		25.78		3.94		3.98		0		-27890.93		3:13:00		m

		S1148764817:		#B3q0		1148764817:		$B3q0		d-		31.66		4.04		25.78		3.94		3.97		0		-27891.92		3:13:30		m

		S1148764847:		#B3q0		1148764847:		$B3q0		d-		31.66		4		25.78		3.94		3.97		0		-27893.05		3:14:01		m

		S1148764877:		#B3q0		1148764877:		$B3q0		d-		31.66		4		25.87		3.94		3.97		0		-27894.05		3:14:30		m

		S1148764907:		#B3q0		1148764907:		$B3q0		d-		31.66		4		25.68		3.94		3.97		0		-27895.18		3:15:00		m

		S1148764937:		#B3q0		1148764937:		$B3q0		d-		31.62		4		25.78		3.94		3.97		0		-27896.17		3:15:30		m

		S1148764967:		#B3q0		1148764967:		$B3q0		d-		31.62		4.04		25.87		3.94		3.97		0		-27897.31		3:16:00		m

		S1148764997:		#B3q0		1148764997:		$B3q0		d-		31.62		4.04		25.78		3.94		3.97		0		-27898.3		3:16:30		m

		S1148765027:		#B3q0		1148765027:		$B3q0		d-		31.62		4.08		25.78		3.93		3.97		0		-27899.44		3:17:00		m

		S1148765057:		#B3q0		1148765057:		$B3q0		d-		31.62		4		25.78		3.93		3.97		0		-27900.43		3:17:30		m

		S1148765087:		#B3q0		1148765087:		$B3q0		d-		31.62		4.04		25.78		3.93		3.97		0		-27901.56		3:18:00		m

		S1148765117:		#B3q0		1148765117:		$B3q0		d-		31.62		4.08		25.78		3.93		3.97		0		-27902.56		3:18:30		m

		S1148765147:		#B3q0		1148765147:		$B3q0		d-		31.62		4.08		25.78		3.93		3.97		0		-27903.69		3:19:01		m

		S1148765177:		#B3q0		1148765177:		$B3q0		d-		31.62		4		25.87		3.93		3.97		0		-27904.68		3:19:30		m

		S1148765207:		#B3q0		1148765207:		$B3q0		d-		31.62		4.04		25.78		3.93		3.97		0		-27905.81		3:20:00		m

		S1148765237:		#B3q0		1148765237:		$B3q0		d-		31.59		4.08		25.78		3.93		3.97		0		-27906.8		3:20:31		m

		S1148765267:		#B3q0		1148765267:		$B3q0		d-		31.59		4		25.87		3.93		3.97		0		-27907.93		3:21:00		m

		S1148765297:		#B3q0		1148765297:		$B3q0		d-		31.62		4.04		25.87		3.93		3.97		0		-27908.92		3:21:31		m

		S1148765327:		#B3q0		1148765327:		$B3q0		d-		31.59		4		25.78		3.93		3.97		0		-27910.05		3:22:01		m

		S1148765357:		#B3q0		1148765357:		$B3q0		d-		31.59		4.04		25.78		3.93		3.97		0		-27911.04		3:22:31		m

		S1148765387:		#B3q0		1148765387:		$B3q0		d-		31.59		4.04		25.78		3.93		3.96		0		-27912.17		3:23:01		m

		S1148765417:		#B3q0		1148765417:		$B3q0		d-		31.59		4		25.78		3.93		3.97		0		-27913.16		3:23:30		m

		S1148765447:		#B3q0		1148765447:		$B3q0		d-		31.59		4.08		25.87		3.93		3.96		0		-27914.3		3:24:00		m

		S1148768612:		#B3q0		1148768612:		$B3q0		d-		31.28		4.04		26.17		3.89		3.93		0		-28025.79		4:16:45		m

		S1148768641:		#B3q0		1148768641:		$B3q0		d-		31.28		4.04		26.17		3.89		3.93		0		-28026.78		4:17:14		m

		S1148768671:		#B3q0		1148768671:		$B3q0		d-		31.28		4		26.17		3.89		3.93		0		-28027.9		4:17:45		m

		S1148768701:		#B3q0		1148768701:		$B3q0		d-		31.28		4.04		26.17		3.89		3.93		0		-28028.88		4:18:14		m

		S1148768731:		#B3q0		1148768731:		$B3q0		d-		31.28		4.04		26.26		3.89		3.93		0		-28030		4:18:45		m

		S1148768761:		#B3q0		1148768761:		$B3q0		d-		31.28		4.04		26.26		3.89		3.93		0		-28030.99		4:19:15		m

		S1148768791:		#B3q0		1148768791:		$B3q0		d-		31.28		4		26.17		3.89		3.93		0		-28032.11		4:19:45		m

		S1148768821:		#B3q0		1148768821:		$B3q0		d-		31.28		4.08		26.17		3.89		3.93		0		-28033.09		4:20:15		m

		S1148768851:		#B3q0		1148768851:		$B3q0		d-		31.25		4.04		26.26		3.89		3.92		0		-28034.21		4:20:44		m

		S1148768881:		#B3q0		1148768881:		$B3q0		d-		31.25		4.04		26.07		3.89		3.92		0		-28035.19		4:21:15		m

		S1148768911:		#B3q0		1148768911:		$B3q0		d-		31.28		4.04		26.17		3.88		3.92		0		-28036.31		4:21:45		m

		S1148768941:		#B3q0		1148768942:		$B3q0		d-		31.25		4.04		26.17		3.88		3.92		0		-28037.29		4:22:15		m

		S1148768971:		#B3q0		1148768971:		$B3q0		d-		31.25		4.04		26.17		3.88		3.92		0		-28038.41		4:22:45		m

		S1148769001:		#B3q0		1148769001:		$B3q0		d-		31.28		4		26.17		3.88		3.92		0		-28039.39		4:23:15		m

		S1148769031:		#B3q0		1148769031:		$B3q0		d-		31.25		4.04		26.17		3.88		3.92		0		-28040.52		4:23:44		m

		S1148769061:		#B3q0		1148769061:		$B3q0		d-		31.25		4.04		26.17		3.88		3.92		0		-28041.5		4:24:15		m

		S1148769091:		#B3q0		1148769091:		$B3q0		d-		31.25		4		26.17		3.88		3.92		0		-28042.62		4:24:44		m

		S1148769121:		#B3q0		1148769121:		$B3q0		d-		31.21		4.04		26.26		3.88		3.92		0		-28043.6		4:25:15		m

		S1148769151:		#B3q0		1148769151:		$B3q0		d-		31.21		4.04		26.26		3.88		3.92		0		-28044.72		4:25:44		m

		S1148769181:		#B3q0		1148769181:		$B3q0		d-		31.21		4		26.17		3.88		3.92		0		-28045.7		4:26:14		m

		S1148769211:		#B3q0		1148769211:		$B3q0		d-		31.21		4.04		26.26		3.88		3.92		0		-28046.82		4:26:45		m

		S1148769241:		#B3q0		1148769241:		$B3q0		d-		31.25		4.04		26.26		3.88		3.92		0		-28047.81		4:27:15		m

		S1148769271:		#B3q0		1148769271:		$B3q0		d-		31.21		4.04		26.26		3.88		3.92		0		-28048.93		4:27:45		m

		S1148769301:		#B3q0		1148769301:		$B3q0		d-		31.21		4.04		26.26		3.88		3.92		0		-28049.9		4:28:15		m

		S1148769331:		#B3q0		1148769331:		$B3q0		d-		31.21		4.08		26.26		3.88		3.92		0		-28051.02		4:28:44		m

		S1148769361:		#B3q0		1148769361:		$B3q0		d-		31.21		4		26.26		3.88		3.92		0		-28052		4:29:15		m

		S1148769391:		#B3q0		1148769391:		$B3q0		d-		31.21		4		26.17		3.88		3.92		0		-28053.13		4:29:45		m

		S1148769421:		#B3q0		1148769421:		$B3q0		d-		31.21		4.08		26.26		3.88		3.92		0		-28054.1		4:30:15		m

		S1148769451:		#B3q0		1148769451:		$B3q0		d-		31.21		4		26.26		3.88		3.92		0		-28055.22		4:30:44		m

		S1148769481:		#B3q0		1148769481:		$B3q0		d-		31.21		4		26.26		3.88		3.92		0		-28056.2		4:31:15		m

		S1148769511:		#B3q0		1148769511:		$B3q0		d-		31.21		4		26.26		3.87		3.92		0		-28057.32		4:31:45		m

		S1148769541:		#B3q0		1148769541:		$B3q0		d-		31.21		4.04		26.26		3.87		3.92		0		-28058.3		4:32:15		m

		S1148769571:		#B3q0		1148769571:		$B3q0		d-		31.17		4.04		26.17		3.87		3.92		0		-28059.41		4:32:44		m

		S1148769601:		#B3q0		1148769601:		$B3q0		d-		31.17		4.08		26.26		3.87		3.92		0		-28060.39		4:33:15		m

		S1148769631:		#B3q0		1148769631:		$B3q0		d-		31.21		4.04		26.26		3.87		3.92		0		-28061.51		4:33:45		m

		S1148769661:		#B3q0		1148769661:		$B3q0		d-		31.21		4.04		26.17		3.87		3.92		0		-28062.49		4:34:15		m

		S1148769691:		#B3q0		1148769691:		$B3q0		d-		31.17		3.96		26.26		3.87		3.92		0		-28063.61		4:34:45		m

		S1148769721:		#B3q0		1148769721:		$B3q0		d-		31.21		4.04		26.26		3.87		3.92		0		-28064.58		4:35:14		m

		S1148769751:		#B3q0		1148769751:		$B3q0		d-		31.17		4		26.26		3.87		3.92		0		-28065.7		4:35:44		m

		S1148769781:		#B3q0		1148769781:		$B3q0		d-		31.17		4.04		26.26		3.87		3.92		0		-28066.68		4:36:15		m

		S1148769811:		#B3q0		1148769811:		$B3q0		d-		31.17		4.04		26.26		3.87		3.92		0		-28067.8		4:36:44		m

		S1148769841:		#B3q0		1148769841:		$B3q0		d-		31.17		4.04		26.26		3.87		3.92		0		-28068.78		4:37:14		m

		S1148769871:		#B3q0		1148769871:		$B3q0		d-		31.17		4		26.26		3.87		3.92		0		-28069.9		4:37:45		m

		S1148769901:		#B3q0		1148769901:		$B3q0		d-		31.17		4.04		26.26		3.87		3.92		0		-28070.88		4:38:14		m

		S1148769931:		#B3q0		1148769931:		$B3q0		d-		31.13		4.04		26.26		3.87		3.92		0		-28071.99		4:38:45		m

		S1148769961:		#B3q0		1148769961:		$B3q0		d-		31.13		4.04		26.17		3.87		3.92		0		-28072.97		4:39:15		m

		S1148769991:		#B3q0		1148769991:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28074.09		4:39:44		m

		S1148770021:		#B3q0		1148770021:		$B3q0		d-		31.13		4		26.26		3.87		3.91		0		-28075.07		4:40:14		m

		S1148770051:		#B3q0		1148770051:		$B3q0		d-		31.17		4.04		26.26		3.87		3.91		0		-28076.19		4:40:45		m

		S1148770081:		#B3q0		1148770081:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28077.17		4:41:15		m

		S1148770111:		#B3q0		1148770111:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28078.29		4:41:45		m

		S1148770141:		#B3q0		1148770141:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28079.26		4:42:15		m

		S1148770171:		#B3q0		1148770171:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28080.38		4:42:45		m

		S1148770201:		#B3q0		1148770201:		$B3q0		d-		31.13		4.08		26.26		3.87		3.91		0		-28081.35		4:43:14		m

		S1148770231:		#B3q0		1148770231:		$B3q0		d-		31.13		4		26.17		3.87		3.91		0		-28082.47		4:43:45		m

		S1148770261:		#B3q0		1148770261:		$B3q0		d-		31.09		4.04		26.36		3.87		3.91		0		-28083.44		4:44:15		m

		S1148770291:		#B3q0		1148770291:		$B3q0		d-		31.13		4.08		26.26		3.87		3.91		0		-28084.56		4:44:45		m

		S1148770321:		#B3q0		1148770321:		$B3q0		d-		31.13		4.04		26.26		3.87		3.91		0		-28085.53		4:45:14		m

		S1148770351:		#B3q0		1148770351:		$B3q0		d-		31.09		4.08		26.26		3.87		3.91		0		-28086.65		4:45:45		m

		S1148770381:		#B3q0		1148770381:		$B3q0		d-		31.09		4.04		26.26		3.87		3.91		0		-28087.62		4:46:15		m

		S1148770411:		#B3q0		1148770411:		$B3q0		d-		31.09		4.08		26.26		3.86		3.91		0		-28088.74		4:46:45		m

		S1148770441:		#B3q0		1148770441:		$B3q0		d-		31.09		4.04		26.26		3.86		3.91		0		-28089.72		4:47:15		m

		S1148770471:		#B3q0		1148770471:		$B3q0		d-		31.09		4.04		26.26		3.86		3.91		0		-28090.84		4:47:45		m

		S1148770501:		#B3q0		1148770501:		$B3q0		d-		31.13		4		26.26		3.86		3.91		0		-28091.81		4:48:14		m

		S1148770531:		#B3q0		1148770531:		$B3q0		d-		31.09		4		26.26		3.86		3.91		0		-28092.92		4:48:45		m

		S1148770561:		#B3q0		1148770561:		$B3q0		d-		31.09		3.96		26.26		3.86		3.91		0		-28093.9		4:49:15		m

		S1148770591:		#B3q0		1148770591:		$B3q0		d-		31.09		4.04		26.26		3.86		3.91		0		-28095.02		4:49:45		m

		S1148770621:		#B3q0		1148770621:		$B3q0		d-		31.09		4		26.36		3.86		3.91		0		-28095.99		4:50:15		m

		S1148770651:		#B3q0		1148770651:		$B3q0		d-		31.09		4.04		26.36		3.86		3.91		0		-28097.11		4:50:45		m

		S1148770681:		#B3q0		1148770681:		$B3q0		d-		31.06		4.04		26.36		3.86		3.91		0		-28098.09		4:51:15		m

		S1148770711:		#B3q0		1148770711:		$B3q0		d-		31.09		4.04		26.36		3.86		3.91		0		-28099.2		4:51:45		m

		S1148770741:		#B3q0		1148770741:		$B3q0		d-		31.06		4		26.36		3.86		3.91		0		-28100.17		4:52:15		m

		S1148770771:		#B3q0		1148770771:		$B3q0		d-		31.09		4.04		26.36		3.86		3.91		0		-28101.28		4:52:45		m

		S1148770801:		#B3q0		1148770801:		$B3q0		d-		31.09		4.04		26.26		3.86		3.91		0		-28102.26		4:53:15		m

		S1148770831:		#B3q0		1148770831:		$B3q0		d-		31.06		4		26.26		3.86		3.91		0		-28103.38		4:53:44		m

		S1148770861:		#B3q0		1148770861:		$B3q0		d-		31.06		4		26.26		3.86		3.91		0		-28104.35		4:54:14		m

		S1148770891:		#B3q0		1148770891:		$B3q0		d-		31.06		4.08		26.26		3.86		3.91		0		-28105.47		4:54:45		m

		S1148770921:		#B3q0		1148770921:		$B3q0		d-		31.06		4.04		26.26		3.86		3.91		0		-28106.44		4:55:15		m

		S1148770951:		#B3q0		1148770951:		$B3q0		d-		31.06		4		26.36		3.86		3.91		0		-28107.56		4:55:45		m

		S1148770981:		#B3q0		1148770981:		$B3q0		d-		31.06		4.04		26.26		3.86		3.91		0		-28108.53		4:56:15		m

		S1148771011:		#B3q0		1148771011:		$B3q0		d-		31.06		4.04		26.26		3.86		3.9		0		-28109.65		4:56:45		m

		S1148771041:		#B3q0		1148771041:		$B3q0		d-		31.06		4.04		26.26		3.86		3.9		0		-28110.63		4:57:15		m

		S1148771071:		#B3q0		1148771071:		$B3q0		d-		31.06		4		26.26		3.85		3.9		0		-28111.74		4:57:45		m

		S1148771101:		#B3q0		1148771101:		$B3q0		d-		31.06		4		26.36		3.85		3.9		0		-28112.71		4:58:15		m

		S1148771131:		#B3q0		1148771131:		$B3q0		d-		31.02		4.04		26.36		3.85		3.9		0		-28113.82		4:58:45		m

		S1148771161:		#B3q0		1148771161:		$B3q0		d-		31.02		4		26.26		3.85		3.9		0		-28114.8		4:59:15		m

		S1148771191:		#B3q0		1148771191:		$B3q0		d-		31.06		4.04		26.36		3.85		3.9		0		-28115.91		4:59:45		m

		S1148771221:		#B3q0		1148771221:		$B3q0		d-		31.02		4.04		26.26		3.85		3.9		0		-28116.89		5:00:15		m

		S1148771251:		#B3q0		1148771251:		$B3q0		d-		31.02		4.04		26.36		3.85		3.9		0		-28118		5:00:45		m

		S1148771281:		#B3q0		1148771281:		$B3q0		d-		31.02		4.04		26.26		3.85		3.9		0		-28118.97		5:01:15		m

		S1148771311:		#B3q0		1148771311:		$B3q0		d-		31.02		4		26.26		3.85		3.9		0		-28120.07		5:01:44		m

		S1148771341:		#B3q0		1148771341:		$B3q0		d-		31.02		4		26.26		3.85		3.9		0		-28121.04		5:02:15		m

		S1148771371:		#B3q0		1148771371:		$B3q0		d-		31.02		4.04		26.26		3.85		3.9		0		-28122.16		5:02:45		m

		S1148771401:		#B3q0		1148771401:		$B3q0		d-		30.98		4		26.26		3.85		3.9		0		-28123.13		5:03:15		m

		S1148771431:		#B3q0		1148771431:		$B3q0		d-		30.98		4.04		26.36		3.85		3.9		0		-28124.24		5:03:45		m

		S1148771461:		#B3q0		1148771461:		$B3q0		d-		31.02		4		26.26		3.85		3.9		0		-28125.21		5:04:14		m

		S1148771491:		#B3q0		1148771491:		$B3q0		d-		31.02		4		26.36		3.85		3.9		0		-28126.32		5:04:45		m

		S1148771521:		#B3q0		1148771521:		$B3q0		d-		31.02		4		26.26		3.85		3.9		0		-28127.29		5:05:15		m

		S1148771551:		#B3q0		1148771551:		$B3q0		d-		30.98		4.04		26.36		3.85		3.9		0		-28128.4		5:05:45		m

		S1148771581:		#B3q0		1148771581:		$B3q0		d-		30.98		4.04		26.26		3.85		3.9		0		-28129.37		5:06:15		m

		S1148771611:		#B3q0		1148771611:		$B3q0		d-		30.98		4		26.36		3.85		3.9		0		-28130.48		5:06:45		m

		S1148771641:		#B3q0		1148771641:		$B3q0		d-		31.02		4.08		26.36		3.85		3.9		0		-28131.45		5:07:15		m

		S1148771671:		#B3q0		1148771671:		$B3q0		d-		30.98		4		26.36		3.85		3.9		0		-28132.56		5:07:45		m

		S1148771701:		#B3q0		1148771701:		$B3q0		d-		30.98		4.04		26.26		3.85		3.89		0		-28133.54		5:08:15		m

		S1148771731:		#B3q0		1148771731:		$B3q0		d-		30.98		4.04		26.36		3.85		3.89		0		-28134.65		5:08:44		m

		S1148771761:		#B3q0		1148771761:		$B3q0		d-		30.98		4.08		26.26		3.85		3.89		0		-28135.62		5:09:15		m

		S1148771791:		#B3q0		1148771791:		$B3q0		d-		30.98		4		26.36		3.85		3.89		0		-28136.74		5:09:45		m

		S1148771821:		#B3q0		1148771821:		$B3q0		d-		30.98		4.04		26.36		3.85		3.89		0		-28137.71		5:10:15		m

		S1148771851:		#B3q0		1148771851:		$B3q0		d-		30.98		4.04		26.26		3.85		3.89		0		-28138.81		5:10:45		m

		S1148771881:		#B3q0		1148771881:		$B3q0		d-		30.98		4.08		26.36		3.85		3.89		0		-28139.79		5:11:15		m

		S1148771911:		#B3q0		1148771911:		$B3q0		d-		30.94		4.04		26.26		3.85		3.89		0		-28140.89		5:11:45		m

		S1148771941:		#B3q0		1148771941:		$B3q0		d-		30.94		4		26.26		3.85		3.89		0		-28141.87		5:12:15		m

		S1148771971:		#B3q0		1148771971:		$B3q0		d-		30.91		4		26.26		3.85		3.89		0		-28142.98		5:12:45		m

		S1148772001:		#B3q0		1148772001:		$B3q0		d-		30.94		4.04		26.36		3.85		3.89		0		-28143.95		5:13:15		m

		S1148772031:		#B3q0		1148772031:		$B3q0		d-		30.94		4.04		26.36		3.85		3.89		0		-28145.06		5:13:45		m

		S1148772061:		#B3q0		1148772061:		$B3q0		d-		30.91		4		26.36		3.84		3.89		0		-28146.03		5:14:15		m

		S1148772091:		#B3q0		1148772091:		$B3q0		d-		30.94		4		26.26		3.84		3.89		0		-28147.15		5:14:45		m

		S1148772121:		#B3q0		1148772121:		$B3q0		d-		30.91		4		26.36		3.84		3.89		0		-28148.12		5:15:15		m

		S1148772151:		#B3q0		1148772151:		$B3q0		d-		30.94		4.04		26.26		3.84		3.89		0		-28149.23		5:15:45		m

		S1148772181:		#B3q0		1148772181:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28150.2		5:16:15		m

		S1148772211:		#B3q0		1148772211:		$B3q0		d-		30.94		4.04		26.36		3.84		3.89		0		-28151.31		5:16:45		m

		S1148772241:		#B3q0		1148772241:		$B3q0		d-		30.94		4.04		26.36		3.84		3.89		0		-28152.28		5:17:15		m

		S1148772271:		#B3q0		1148772271:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28153.39		5:17:45		m

		S1148772301:		#B3q0		1148772301:		$B3q0		d-		30.94		4.04		26.36		3.84		3.89		0		-28154.36		5:18:15		m

		S1148772331:		#B3q0		1148772331:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28155.47		5:18:45		m

		S1148772361:		#B3q0		1148772361:		$B3q0		d-		30.94		4.04		26.26		3.84		3.89		0		-28156.44		5:19:15		m

		S1148772391:		#B3q0		1148772391:		$B3q0		d-		30.94		4.04		26.26		3.84		3.89		0		-28157.55		5:19:44		m

		S1148772421:		#B3q0		1148772421:		$B3q0		d-		30.94		4.04		26.26		3.84		3.89		0		-28158.52		5:20:15		m

		S1148772451:		#B3q0		1148772451:		$B3q0		d-		30.91		4.04		26.26		3.84		3.89		0		-28159.63		5:20:45		m

		S1148772481:		#B3q0		1148772481:		$B3q0		d-		30.91		4		26.36		3.84		3.89		0		-28160.61		5:21:15		m

		S1148772511:		#B3q0		1148772511:		$B3q0		d-		30.91		4.08		26.36		3.84		3.89		0		-28161.72		5:21:45		m

		S1148772541:		#B3q0		1148772541:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28162.68		5:22:15		m

		S1148772571:		#B3q0		1148772571:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28163.79		5:22:45		m

		S1148772601:		#B3q0		1148772601:		$B3q0		d-		30.91		4.04		26.26		3.84		3.89		0		-28164.76		5:23:15		m

		S1148772631:		#B3q0		1148772631:		$B3q0		d-		30.91		4		26.36		3.84		3.89		0		-28165.87		5:23:45		m

		S1148772661:		#B3q0		1148772661:		$B3q0		d-		30.91		4.04		26.36		3.84		3.89		0		-28166.84		5:24:15		m

		S1148772691:		#B3q0		1148772691:		$B3q0		d-		30.91		4.04		26.36		3.84		3.88		0		-28167.96		5:24:45		m

		S1148772721:		#B3q0		1148772721:		$B3q0		d-		30.87		4.04		26.36		3.84		3.88		0		-28168.93		5:25:15		m

		S1148772751:		#B3q0		1148772751:		$B3q0		d-		30.87		4.04		26.46		3.84		3.88		0		-28170.03		5:25:45		m

		S1148772781:		#B3q0		1148772781:		$B3q0		d-		30.87		4.04		26.36		3.83		3.88		0		-28171.01		5:26:15		m

		S1148772811:		#B3q0		1148772811:		$B3q0		d-		30.87		4.08		26.46		3.83		3.88		0		-28172.11		5:26:45		m

		S1148772841:		#B3q0		1148772841:		$B3q0		d-		30.87		4.04		26.36		3.83		3.88		0		-28173.08		5:27:15		m

		S1148772871:		#B3q0		1148772871:		$B3q0		d-		30.91		4.08		26.36		3.83		3.88		0		-28174.19		5:27:45		m

		S1148772901:		#B3q0		1148772901:		$B3q0		d-		30.87		4.04		26.46		3.83		3.88		0		-28175.15		5:28:15		m

		S1148772931:		#B3q0		1148772931:		$B3q0		d-		30.87		4.04		26.36		3.83		3.88		0		-28176.26		5:28:45		m

		S1148772961:		#B3q0		1148772961:		$B3q0		d-		30.87		4		26.46		3.83		3.88		0		-28177.23		5:29:15		m

		S1148772991:		#B3q0		1148772991:		$B3q0		d-		30.87		4.04		26.36		3.83		3.88		0		-28178.33		5:29:44		m

		S1148773021:		#B3q0		1148773021:		$B3q0		d-		30.87		4		26.36		3.83		3.88		0		-28179.29		5:30:15		m

		S1148773051:		#B3q0		1148773051:		$B3q0		d-		30.87		4		26.46		3.83		3.88		0		-28180.39		5:30:45		m

		S1148773081:		#B3q0		1148773081:		$B3q0		d-		30.87		4		26.36		3.83		3.88		0		-28181.36		5:31:15		m

		S1148773111:		#B3q0		1148773111:		$B3q0		d-		30.83		4		26.26		3.83		3.88		0		-28182.47		5:31:45		m

		S1148773141:		#B3q0		1148773141:		$B3q0		d-		30.83		4.04		26.36		3.83		3.88		0		-28183.71		5:32:20		m

		S1148773171:		#B3q0		1148773171:		$B3q0		d-		30.83		4.04		26.36		3.83		3.88		0		-28184.67		5:32:50		m

		S1148773201:		#B3q0		1148773201:		$B3q0		d-		30.83		4.08		26.36		3.83		3.88		0		-28185.78		5:33:20		m

		S1148773231:		#B3q0		1148773231:		$B3q0		d-		30.83		4.04		26.36		3.83		3.88		0		-28186.75		5:33:50		m

		S1148773261:		#B3q0		1148773261:		$B3q0		d-		30.87		4.04		26.46		3.83		3.88		0		-28187.85		5:34:20		m

		S1148773291:		#B3q0		1148773291:		$B3q0		d-		30.83		4.04		26.26		3.83		3.88		0		-28188.82		5:34:50		m

		S1148773321:		#B3q0		1148773321:		$B3q0		d-		30.83		4.04		26.36		3.83		3.87		0		-28189.93		5:35:20		m

		S1148773351:		#B3q0		1148773351:		$B3q0		d-		30.83		4		26.36		3.83		3.87		0		-28190.9		5:35:50		m

		S1148773381:		#B3q0		1148773381:		$B3q0		d-		30.83		4.04		26.36		3.83		3.87		0		-28192		5:36:20		m

		S1148773411:		#B3q0		1148773411:		$B3q0		d-		30.83		4.04		26.46		3.83		3.87		0		-28192.97		5:36:50		m

		S1148773441:		#B3q0		1148773441:		$B3q0		d-		30.83		4.04		26.36		3.83		3.87		0		-28194.08		5:37:20		m

		S1148773471:		#B3q0		1148773471:		$B3q0		d-		30.83		4		26.36		3.83		3.87		0		-28195.04		5:37:50		m

		S1148773501:		#B3q0		1148773501:		$B3q0		d-		30.83		4.04		26.36		3.83		3.87		0		-28196.15		5:38:20		m

		S1148773531:		#B3q0		1148773531:		$B3q0		d-		30.83		4		26.46		3.83		3.87		0		-28197.12		5:38:50		m

		S1148773561:		#B3q0		1148773561:		$B3q0		d-		30.83		4		26.36		3.83		3.87		0		-28198.22		5:39:20		m

		S1148773591:		#B3q0		1148773591:		$B3q0		d-		30.83		4.04		26.46		3.83		3.87		0		-28199.19		5:39:50		m

		S1148773621:		#B3q0		1148773621:		$B3q0		d-		30.79		4.08		26.46		3.83		3.87		0		-28200.3		5:40:20		m

		S1148773651:		#B3q0		1148773651:		$B3q0		d-		30.79		4		26.46		3.83		3.87		0		-28201.26		5:40:50		m

		S1148773681:		#B3q0		1148773681:		$B3q0		d-		30.79		4.04		26.46		3.83		3.87		0		-28202.37		5:41:20		m

		S1148773711:		#B3q0		1148773711:		$B3q0		d-		30.79		4.04		26.46		3.83		3.87		0		-28203.34		5:41:50		m

		S1148773741:		#B3q0		1148773741:		$B3q0		d-		30.79		4.04		26.36		3.83		3.87		0		-28204.44		5:42:20		m

		S1148773771:		#B3q0		1148773771:		$B3q0		d-		30.79		4.04		26.36		3.83		3.87		0		-28205.4		5:42:50		m

		S1148773801:		#B3q0		1148773801:		$B3q0		d-		30.83		4.08		26.36		3.83		3.87		0		-28206.51		5:43:20		m

		S1148773831:		#B3q0		1148773831:		$B3q0		d-		30.79		4.04		26.36		3.83		3.87		0		-28207.47		5:43:50		m

		S1148773861:		#B3q0		1148773861:		$B3q0		d-		30.75		4.04		26.36		3.83		3.87		0		-28208.57		5:44:20		m

		S1148773891:		#B3q0		1148773891:		$B3q0		d-		30.79		4		26.36		3.83		3.87		0		-28209.54		5:44:50		m

		S1148773921:		#B3q0		1148773921:		$B3q0		d-		30.79		4		26.36		3.83		3.87		0		-28210.65		5:45:20		m

		S1148773951:		#B3q0		1148773951:		$B3q0		d-		30.79		4.04		26.36		3.82		3.87		0		-28211.61		5:45:50		m

		S1148773981:		#B3q0		1148773981:		$B3q0		d-		30.79		4.04		26.46		3.82		3.87		0		-28212.71		5:46:20		m

		S1148774011:		#B3q0		1148774011:		$B3q0		d-		30.79		4.04		26.36		3.82		3.87		0		-28213.68		5:46:50		m

		S1148774041:		#B3q0		1148774041:		$B3q0		d-		30.79		4		26.36		3.82		3.87		0		-28214.5		5:47:15		m

		S1148774071:		#B3q0		1148774071:		$B3q0		d-		30.75		4		26.46		3.82		3.87		0		-28215.6		5:47:45		m

		S1148774101:		#B3q0		1148774101:		$B3q0		d-		30.79		4.04		26.36		3.82		3.87		0		-28216.56		5:48:15		m

		S1148774131:		#B3q0		1148774131:		$B3q0		d-		30.75		4		26.36		3.82		3.87		0		-28217.67		5:48:45		m

		S1148774161:		#B3q0		1148774161:		$B3q0		d-		30.75		4.04		26.36		3.82		3.87		0		-28218.63		5:49:14		m

		S1148774191:		#B3q0		1148774191:		$B3q0		d-		30.79		4.04		26.46		3.82		3.87		0		-28219.74		5:49:44		m

		S1148774221:		#B3q0		1148774221:		$B3q0		d-		30.75		4		26.46		3.82		3.87		0		-28220.71		5:50:15		m

		S1148774251:		#B3q0		1148774251:		$B3q0		d-		30.75		4.04		26.46		3.82		3.87		0		-28221.81		5:50:45		m

		S1148774281:		#B3q0		1148774281:		$B3q0		d-		30.75		4.04		26.46		3.82		3.87		0		-28222.77		5:51:15		m

		S1148774311:		#B3q0		1148774311:		$B3q0		d-		30.75		4		26.46		3.82		3.87		0		-28223.88		5:51:45		m

		S1148774341:		#B3q0		1148774341:		$B3q0		d-		30.79		4.04		26.36		3.82		3.86		0		-28224.84		5:52:15		m

		S1148774371:		#B3q0		1148774371:		$B3q0		d-		30.75		4.08		26.46		3.82		3.86		0		-28225.95		5:52:45		m

		S1148774401:		#B3q0		1148774401:		$B3q0		d-		30.75		4		26.36		3.82		3.86		0		-28226.91		5:53:15		m

		S1148774431:		#B3q0		1148774431:		$B3q0		d-		30.75		4.04		26.36		3.82		3.86		0		-28228.01		5:53:45		m

		S1148774461:		#B3q0		1148774461:		$B3q0		d-		30.71		4.04		26.46		3.82		3.86		0		-28228.98		5:54:15		m

		S1148774491:		#B3q0		1148774491:		$B3q0		d-		30.75		4.04		26.36		3.82		3.86		0		-28230.08		5:54:45		m

		S1148774521:		#B3q0		1148774521:		$B3q0		d-		30.75		4.04		26.36		3.82		3.86		0		-28231.05		5:55:15		m

		S1148774551:		#B3q0		1148774551:		$B3q0		d-		30.71		4.04		26.36		3.82		3.86		0		-28232.16		5:55:45		m

		S1148774581:		#B3q0		1148774581:		$B3q0		d-		30.71		4.04		26.46		3.82		3.86		0		-28233.13		5:56:15		m

		S1148774611:		#B3q0		1148774611:		$B3q0		d-		30.71		4.08		26.46		3.82		3.86		0		-28234.23		5:56:45		m

		S1148774641:		#B3q0		1148774641:		$B3q0		d-		30.75		4		26.46		3.82		3.86		0		-28235.19		5:57:15		m

		S1148774671:		#B3q0		1148774671:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28236.3		5:57:45		m

		S1148774701:		#B3q0		1148774701:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28237.27		5:58:15		m

		S1148774731:		#B3q0		1148774731:		$B3q0		d-		30.71		4.04		26.46		3.82		3.86		0		-28238.37		5:58:45		m

		S1148774761:		#B3q0		1148774761:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28239.33		5:59:15		m

		S1148774791:		#B3q0		1148774791:		$B3q0		d-		30.71		4.04		26.46		3.82		3.86		0		-28240.44		5:59:45		m

		S1148774821:		#B3q0		1148774821:		$B3q0		d-		30.71		4.04		26.36		3.82		3.86		0		-28241.4		6:00:15		m

		S1148774851:		#B3q0		1148774851:		$B3q0		d-		30.71		4.04		26.36		3.82		3.86		0		-28242.51		6:00:45		m

		S1148774881:		#B3q0		1148774881:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28243.47		6:01:15		m

		S1148774911:		#B3q0		1148774911:		$B3q0		d-		30.71		4.04		26.46		3.82		3.86		0		-28244.58		6:01:45		m

		S1148774941:		#B3q0		1148774941:		$B3q0		d-		30.68		4.04		26.46		3.82		3.86		0		-28245.54		6:02:15		m

		S1148774971:		#B3q0		1148774971:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28246.64		6:02:45		m

		S1148775001:		#B3q0		1148775001:		$B3q0		d-		30.68		4		26.46		3.82		3.86		0		-28247.61		6:03:15		m

		S1148775031:		#B3q0		1148775031:		$B3q0		d-		30.71		4		26.46		3.82		3.86		0		-28248.71		6:03:45		m

		S1148775061:		#B3q0		1148775061:		$B3q0		d-		30.68		4.04		26.46		3.82		3.85		0		-28249.67		6:04:15		m

		S1148775091:		#B3q0		1148775091:		$B3q0		d-		30.68		4.04		26.46		3.82		3.85		0		-28250.77		6:04:45		m

		S1148775121:		#B3q0		1148775121:		$B3q0		d-		30.68		4		26.46		3.82		3.85		0		-28251.74		6:05:15		m

		S1148775151:		#B3q0		1148775151:		$B3q0		d-		30.71		4		26.46		3.82		3.85		0		-28252.84		6:05:45		m

		S1148775181:		#B3q0		1148775181:		$B3q0		d-		30.68		4.04		26.36		3.82		3.85		0		-28253.8		6:06:15		m

		S1148775211:		#B3q0		1148775211:		$B3q0		d-		30.68		4.04		26.46		3.82		3.85		0		-28254.9		6:06:45		m

		S1148775241:		#B3q0		1148775241:		$B3q0		d-		30.68		4.04		26.46		3.81		3.85		0		-28255.86		6:07:15		m

		S1148775271:		#B3q0		1148775271:		$B3q0		d-		30.68		4		26.46		3.81		3.85		0		-28256.96		6:07:45		m

		S1148775301:		#B3q0		1148775301:		$B3q0		d-		30.68		4.04		26.36		3.81		3.85		0		-28257.92		6:08:15		m

		S1148775331:		#B3q0		1148775331:		$B3q0		d-		30.68		4.04		26.46		3.81		3.85		0		-28259.02		6:08:45		m

		S1148775361:		#B3q0		1148775361:		$B3q0		d-		30.68		4.04		26.36		3.81		3.85		0		-28259.98		6:09:15		m

		S1148775391:		#B3q0		1148775391:		$B3q0		d-		30.68		4		26.46		3.81		3.85		0		-28261.08		6:09:45		m

		S1148775421:		#B3q0		1148775421:		$B3q0		d-		30.64		4		26.46		3.81		3.85		0		-28262.04		6:10:15		m

		S1148775451:		#B3q0		1148775451:		$B3q0		d-		30.64		4.08		26.46		3.81		3.85		0		-28263.14		6:10:45		m

		S1148775481:		#B3q0		1148775481:		$B3q0		d-		30.64		4		26.46		3.81		3.85		0		-28264.1		6:11:15		m

		S1148775511:		#B3q0		1148775511:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28265.2		6:11:45		m

		S1148775541:		#B3q0		1148775541:		$B3q0		d-		30.68		4		26.46		3.81		3.85		0		-28266.17		6:12:15		m

		S1148775571:		#B3q0		1148775571:		$B3q0		d-		30.64		4		26.46		3.81		3.85		0		-28267.27		6:12:45		m

		S1148775601:		#B3q0		1148775601:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28268.23		6:13:15		m

		S1148775631:		#B3q0		1148775631:		$B3q0		d-		30.68		4		26.36		3.81		3.85		0		-28269.32		6:13:45		m

		S1148775661:		#B3q0		1148775661:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28270.28		6:14:15		m

		S1148775691:		#B3q0		1148775691:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28271.38		6:14:45		m

		S1148775721:		#B3q0		1148775721:		$B3q0		d-		30.64		4		26.46		3.81		3.85		0		-28272.34		6:15:15		m

		S1148775751:		#B3q0		1148775751:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28273.44		6:15:45		m

		S1148775781:		#B3q0		1148775781:		$B3q0		d-		30.64		4.04		26.36		3.81		3.85		0		-28274.41		6:16:15		m

		S1148775811:		#B3q0		1148775811:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28275.5		6:16:45		m

		S1148775841:		#B3q0		1148775841:		$B3q0		d-		30.6		4.04		26.46		3.81		3.85		0		-28276.47		6:17:15		m

		S1148775871:		#B3q0		1148775871:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28277.56		6:17:45		m

		S1148775901:		#B3q0		1148775901:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28278.53		6:18:15		m

		S1148775931:		#B3q0		1148775931:		$B3q0		d-		30.64		4.08		26.46		3.81		3.85		0		-28279.63		6:18:45		m

		S1148775961:		#B3q0		1148775961:		$B3q0		d-		30.64		4		26.46		3.81		3.85		0		-28280.59		6:19:15		m

		S1148775991:		#B3q0		1148775991:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28281.69		6:19:45		m

		S1148776021:		#B3q0		1148776021:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28282.65		6:20:15		m

		S1148776051:		#B3q0		1148776051:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28283.75		6:20:45		m

		S1148776081:		#B3q0		1148776081:		$B3q0		d-		30.64		4.04		26.46		3.81		3.85		0		-28284.71		6:21:15		m

		S1148776111:		#B3q0		1148776111:		$B3q0		d-		30.64		4		26.36		3.81		3.85		0		-28285.81		6:21:45		m

		S1148776141:		#B3q0		1148776141:		$B3q0		d-		30.6		4.04		26.46		3.81		3.85		0		-28286.77		6:22:15		m

		S1148776171:		#B3q0		1148776171:		$B3q0		d-		30.6		4.04		26.36		3.8		3.85		0		-28287.87		6:22:45		m

		S1148776201:		#B3q0		1148776201:		$B3q0		d-		30.6		4		26.46		3.8		3.85		0		-28288.83		6:23:15		m

		S1148776231:		#B3q0		1148776231:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28289.93		6:23:45		m

		S1148776261:		#B3q0		1148776261:		$B3q0		d-		30.64		4.04		26.46		3.8		3.84		0		-28290.9		6:24:15		m

		S1148776291:		#B3q0		1148776291:		$B3q0		d-		30.6		4		26.46		3.8		3.84		0		-28291.99		6:24:45		m

		S1148776321:		#B3q0		1148776321:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28292.95		6:25:15		m

		S1148776351:		#B3q0		1148776351:		$B3q0		d-		30.6		4		26.46		3.8		3.84		0		-28294.05		6:25:45		m

		S1148776381:		#B3q0		1148776381:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28295.01		6:26:15		m

		S1148776411:		#B3q0		1148776411:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28296.11		6:26:45		m

		S1148776441:		#B3q0		1148776441:		$B3q0		d-		30.6		4		26.46		3.8		3.84		0		-28297.07		6:27:15		m

		S1148776471:		#B3q0		1148776471:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28298.16		6:27:45		m

		S1148776501:		#B3q0		1148776501:		$B3q0		d-		30.6		4		26.46		3.8		3.84		0		-28299.13		6:28:15		m

		S1148776531:		#B3q0		1148776531:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28300.23		6:28:45		m

		S1148776561:		#B3q0		1148776561:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28301.19		6:29:15		m

		S1148776591:		#B3q0		1148776591:		$B3q0		d-		30.6		4		26.46		3.8		3.84		0		-28302.28		6:29:45		m

		S1148776621:		#B3q0		1148776621:		$B3q0		d-		30.56		4		26.46		3.8		3.84		0		-28303.24		6:30:15		m

		S1148776651:		#B3q0		1148776651:		$B3q0		d-		30.56		4.08		26.46		3.8		3.84		0		-28304.34		6:30:45		m

		S1148776681:		#B3q0		1148776681:		$B3q0		d-		30.6		4.08		26.46		3.8		3.84		0		-28305.3		6:31:15		m

		S1148776711:		#B3q0		1148776711:		$B3q0		d-		30.56		4.04		26.46		3.8		3.84		0		-28306.4		6:31:45		m

		S1148776741:		#B3q0		1148776741:		$B3q0		d-		30.56		4		26.46		3.8		3.84		0		-28307.36		6:32:15		m

		S1148776771:		#B3q0		1148776771:		$B3q0		d-		30.56		4.04		26.36		3.8		3.84		0		-28308.46		6:32:45		m

		S1148776801:		#B3q0		1148776801:		$B3q0		d-		30.6		4.04		26.46		3.8		3.84		0		-28309.42		6:33:15		m

		S1148776831:		#B3q0		1148776831:		$B3q0		d-		30.56		4.08		26.46		3.8		3.84		0		-28310.52		6:33:45		m

		S1148776861:		#B3q0		1148776861:		$B3q0		d-		30.56		4.04		26.46		3.8		3.84		0		-28311.48		6:34:15		m

		S1148776891:		#B3q0		1148776891:		$B3q0		d-		30.56		4.08		26.46		3.8		3.84		0		-28312.57		6:34:45		m

		S1148776921:		#B3q0		1148776921:		$B3q0		d-		30.56		4.04		26.46		3.8		3.84		0		-28313.53		6:35:15		m

		S1148776951:		#B3q0		1148776951:		$B3q0		d-		30.56		4		26.46		3.8		3.84		0		-28314.63		6:35:45		m

		S1148776981:		#B3q0		1148776981:		$B3q0		d-		30.56		4.04		26.56		3.8		3.84		0		-28315.59		6:36:15		m

		S1148777011:		#B3q0		1148777011:		$B3q0		d-		30.56		4.04		26.46		3.8		3.84		0		-28316.69		6:36:45		m

		S1148777041:		#B3q0		1148777041:		$B3q0		d-		30.56		4.04		26.46		3.8		3.84		0		-28317.65		6:37:15		m

		S1148777071:		#B3q0		1148777071:		$B3q0		d-		30.56		4		26.46		3.8		3.83		0		-28318.74		6:37:45		m

		S1148777101:		#B3q0		1148777101:		$B3q0		d-		30.56		4		26.46		3.8		3.83		0		-28319.7		6:38:15		m

		S1148777131:		#B3q0		1148777131:		$B3q0		d-		30.56		4.04		26.46		3.8		3.83		0		-28320.79		6:38:45		m

		S1148777161:		#B3q0		1148777161:		$B3q0		d-		30.56		4.04		26.56		3.8		3.83		0		-28321.75		6:39:15		m

		S1148777191:		#B3q0		1148777191:		$B3q0		d-		30.56		4.04		26.46		3.8		3.83		0		-28322.85		6:39:45		m

		S1148777221:		#B3q0		1148777221:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28323.8		6:40:15		m

		S1148777251:		#B3q0		1148777251:		$B3q0		d-		30.53		4		26.46		3.8		3.83		0		-28324.9		6:40:45		m

		S1148777281:		#B3q0		1148777281:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28325.86		6:41:15		m

		S1148777311:		#B3q0		1148777311:		$B3q0		d-		30.56		4.04		26.56		3.8		3.83		0		-28326.95		6:41:45		m

		S1148777341:		#B3q0		1148777341:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28327.91		6:42:15		m

		S1148777371:		#B3q0		1148777371:		$B3q0		d-		30.53		4.08		26.46		3.8		3.83		0		-28329.01		6:42:45		m

		S1148777401:		#B3q0		1148777401:		$B3q0		d-		30.56		4.04		26.46		3.8		3.83		0		-28329.96		6:43:15		m

		S1148777431:		#B3q0		1148777431:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28331.06		6:43:45		m

		S1148777461:		#B3q0		1148777461:		$B3q0		d-		30.53		4		26.46		3.8		3.83		0		-28332.01		6:44:15		m

		S1148777491:		#B3q0		1148777491:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28333.11		6:44:45		m

		S1148777521:		#B3q0		1148777521:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28334.07		6:45:15		m

		S1148777551:		#B3q0		1148777551:		$B3q0		d-		30.53		4.08		26.46		3.8		3.83		0		-28335.16		6:45:45		m

		S1148777581:		#B3q0		1148777581:		$B3q0		d-		30.53		4		26.46		3.8		3.83		0		-28336.12		6:46:15		m

		S1148777611:		#B3q0		1148777611:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28337.21		6:46:45		m

		S1148777641:		#B3q0		1148777641:		$B3q0		d-		30.53		4.04		26.46		3.8		3.83		0		-28338.16		6:47:15		m

		S1148777671:		#B3q0		1148777671:		$B3q0		d-		30.53		4		26.56		3.79		3.83		0		-28339.26		6:47:45		m

		S1148777701:		#B3q0		1148777701:		$B3q0		d-		30.53		4		26.46		3.79		3.83		0		-28340.22		6:48:15		m

		S1148777731:		#B3q0		1148777731:		$B3q0		d-		30.53		4		26.46		3.79		3.83		0		-28341.31		6:48:45		m

		S1148777761:		#B3q0		1148777761:		$B3q0		d-		30.49		4		26.46		3.79		3.83		0		-28342.27		6:49:15		m

		S1148777791:		#B3q0		1148777791:		$B3q0		d-		30.49		4.08		26.46		3.79		3.83		0		-28343.36		6:49:45		m

		S1148777821:		#B3q0		1148777821:		$B3q0		d-		30.53		4.04		26.46		3.79		3.83		0		-28344.32		6:50:15		m

		S1148777851:		#B3q0		1148777851:		$B3q0		d-		30.49		4.04		26.56		3.79		3.83		0		-28345.4		6:50:45		m

		S1148777881:		#B3q0		1148777881:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28346.37		6:51:15		m

		S1148777911:		#B3q0		1148777911:		$B3q0		d-		30.53		4.04		26.46		3.79		3.83		0		-28347.46		6:51:45		m

		S1148777941:		#B3q0		1148777941:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28348.42		6:52:15		m

		S1148777971:		#B3q0		1148777971:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28349.51		6:52:45		m

		S1148778001:		#B3q0		1148778001:		$B3q0		d-		30.49		4		26.46		3.79		3.83		0		-28350.47		6:53:15		m

		S1148778031:		#B3q0		1148778031:		$B3q0		d-		30.49		4		26.46		3.79		3.83		0		-28351.57		6:53:45		m

		S1148778061:		#B3q0		1148778061:		$B3q0		d-		30.45		4.04		26.56		3.79		3.83		0		-28352.53		6:54:15		m

		S1148778091:		#B3q0		1148778091:		$B3q0		d-		30.49		4		26.46		3.79		3.83		0		-28353.62		6:54:45		m

		S1148778121:		#B3q0		1148778121:		$B3q0		d-		30.49		4		26.56		3.79		3.83		0		-28354.59		6:55:15		m

		S1148778151:		#B3q0		1148778151:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28355.68		6:55:45		m

		S1148778181:		#B3q0		1148778181:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28356.64		6:56:15		m

		S1148778211:		#B3q0		1148778211:		$B3q0		d-		30.49		4		26.46		3.79		3.83		0		-28357.73		6:56:45		m

		S1148778241:		#B3q0		1148778241:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28358.69		6:57:15		m

		S1148778271:		#B3q0		1148778271:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28359.79		6:57:45		m

		S1148778301:		#B3q0		1148778301:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28360.74		6:58:15		m

		S1148778331:		#B3q0		1148778331:		$B3q0		d-		30.49		4.04		26.46		3.79		3.83		0		-28361.84		6:58:45		m

		S1148778361:		#B3q0		1148778361:		$B3q0		d-		30.45		4.08		26.46		3.79		3.83		0		-28362.79		6:59:15		m

		S1148778391:		#B3q0		1148778391:		$B3q0		d-		30.49		4.04		26.56		3.79		3.83		0		-28363.88		6:59:45		m

		S1148778421:		#B3q0		1148778421:		$B3q0		d-		30.45		4.04		26.56		3.79		3.83		0		-28364.84		7:00:15		m

		S1148778451:		#B3q0		1148778451:		$B3q0		d-		30.49		4		26.46		3.79		3.82		0		-28365.94		7:00:45		m

		S1148778481:		#B3q0		1148778481:		$B3q0		d-		30.45		4		26.46		3.79		3.82		0		-28366.89		7:01:15		m

		S1148778511:		#B3q0		1148778511:		$B3q0		d-		30.45		4.08		26.46		3.79		3.82		0		-28367.99		7:01:45		m

		S1148778541:		#B3q0		1148778541:		$B3q0		d-		30.49		4.04		26.56		3.79		3.82		0		-28368.95		7:02:15		m

		S1148778571:		#B3q0		1148778571:		$B3q0		d-		30.45		4		26.56		3.79		3.82		0		-28370.04		7:02:45		m

		S1148778601:		#B3q0		1148778601:		$B3q0		d-		30.49		4.04		26.46		3.79		3.82		0		-28371		7:03:15		m

		S1148778631:		#B3q0		1148778631:		$B3q0		d-		30.45		4.04		26.46		3.79		3.82		0		-28372.09		7:03:45		m

		S1148778661:		#B3q0		1148778661:		$B3q0		d-		30.49		4		26.46		3.79		3.82		0		-28373.05		7:04:15		m

		S1148778691:		#B3q0		1148778691:		$B3q0		d-		30.45		4.04		26.56		3.79		3.82		0		-28374.14		7:04:45		m

		S1148778721:		#B3q0		1148778721:		$B3q0		d-		30.45		4.04		26.56		3.78		3.82		0		-28375.1		7:05:15		m

		S1148778751:		#B3q0		1148778751:		$B3q0		d-		30.45		4.04		26.56		3.78		3.82		0		-28376.19		7:05:45		m

		S1148778781:		#B3q0		1148778781:		$B3q0		d-		30.45		4		26.46		3.78		3.82		0		-28377.15		7:06:15		m

		S1148778811:		#B3q0		1148778811:		$B3q0		d-		30.45		4		26.46		3.78		3.82		0		-28378.24		7:06:45		m

		S1148778841:		#B3q0		1148778841:		$B3q0		d-		30.45		4.08		26.46		3.78		3.82		0		-28379.2		7:07:15		m

		S1148778871:		#B3q0		1148778871:		$B3q0		d-		30.45		4.04		26.56		3.78		3.82		0		-28380.3		7:07:45		m

		S1148778901:		#B3q0		1148778901:		$B3q0		d-		30.45		4		26.46		3.78		3.82		0		-28381.26		7:08:15		m

		S1148778931:		#B3q0		1148778931:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28382.35		7:08:45		m

		S1148778961:		#B3q0		1148778961:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28383.31		7:09:15		m

		S1148778991:		#B3q0		1148778991:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28384.4		7:09:45		m

		S1148779021:		#B3q0		1148779021:		$B3q0		d-		30.45		4.04		26.46		3.78		3.82		0		-28385.36		7:10:15		m

		S1148779051:		#B3q0		1148779051:		$B3q0		d-		30.41		4.08		26.56		3.78		3.82		0		-28386.45		7:10:45		m

		S1148779081:		#B3q0		1148779081:		$B3q0		d-		30.41		4		26.56		3.78		3.82		0		-28387.4		7:11:15		m

		S1148779111:		#B3q0		1148779111:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28388.49		7:11:45		m

		S1148779141:		#B3q0		1148779141:		$B3q0		d-		30.45		4		26.56		3.78		3.82		0		-28389.44		7:12:15		m

		S1148779171:		#B3q0		1148779171:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28390.54		7:12:45		m

		S1148779201:		#B3q0		1148779201:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28391.49		7:13:15		m

		S1148779231:		#B3q0		1148779231:		$B3q0		d-		30.45		4.04		26.46		3.78		3.82		0		-28392.58		7:13:45		m

		S1148779261:		#B3q0		1148779261:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28393.54		7:14:15		m

		S1148779291:		#B3q0		1148779291:		$B3q0		d-		30.45		4.04		26.46		3.78		3.82		0		-28394.63		7:14:45		m

		S1148779321:		#B3q0		1148779321:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28395.58		7:15:15		m

		S1148779351:		#B3q0		1148779351:		$B3q0		d-		30.41		4.08		26.56		3.78		3.82		0		-28396.68		7:15:45		m

		S1148779381:		#B3q0		1148779381:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28397.63		7:16:15		m

		S1148779411:		#B3q0		1148779411:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28398.72		7:16:45		m

		S1148779441:		#B3q0		1148779441:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28399.68		7:17:15		m

		S1148779471:		#B3q0		1148779471:		$B3q0		d-		30.41		4.04		26.46		3.78		3.82		0		-28400.76		7:17:45		m

		S1148779501:		#B3q0		1148779501:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28401.72		7:18:15		m

		S1148779531:		#B3q0		1148779531:		$B3q0		d-		30.41		4.08		26.46		3.78		3.82		0		-28402.81		7:18:45		m

		S1148779561:		#B3q0		1148779561:		$B3q0		d-		30.41		4		26.46		3.78		3.82		0		-28403.76		7:19:15		m

		S1148779591:		#B3q0		1148779591:		$B3q0		d-		30.37		4		26.46		3.78		3.82		0		-28404.85		7:19:45		m

		S1148779621:		#B3q0		1148779621:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28405.8		7:20:15		m

		S1148779651:		#B3q0		1148779651:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28406.9		7:20:45		m

		S1148779681:		#B3q0		1148779681:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28407.85		7:21:15		m

		S1148779711:		#B3q0		1148779711:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28408.94		7:21:45		m

		S1148779741:		#B3q0		1148779741:		$B3q0		d-		30.37		4.04		26.46		3.78		3.82		0		-28409.89		7:22:15		m

		S1148779771:		#B3q0		1148779771:		$B3q0		d-		30.41		4.08		26.46		3.78		3.82		0		-28410.98		7:22:45		m

		S1148779801:		#B3q0		1148779801:		$B3q0		d-		30.37		4.08		26.56		3.78		3.82		0		-28411.93		7:23:15		m

		S1148779831:		#B3q0		1148779831:		$B3q0		d-		30.41		4.04		26.56		3.78		3.82		0		-28413.02		7:23:45		m

		S1148779861:		#B3q0		1148779861:		$B3q0		d-		30.37		4		26.46		3.78		3.82		0		-28413.97		7:24:15		m

		S1148779891:		#B3q0		1148779891:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28415.06		7:24:45		m

		S1148779921:		#B3q0		1148779921:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28416.01		7:25:15		m

		S1148779951:		#B3q0		1148779951:		$B3q0		d-		30.37		4.04		26.46		3.78		3.82		0		-28417.1		7:25:45		m

		S1148779981:		#B3q0		1148779981:		$B3q0		d-		30.37		4.04		26.56		3.78		3.82		0		-28418.06		7:26:15		m

		S1148780011:		#B3q0		1148780011:		$B3q0		d-		30.37		4		26.56		3.78		3.81		0		-28419.15		7:26:45		m

		S1148780041:		#B3q0		1148780041:		$B3q0		d-		30.37		4.04		26.56		3.78		3.81		0		-28420.1		7:27:15		m

		S1148780071:		#B3q0		1148780071:		$B3q0		d-		30.37		4.04		26.56		3.78		3.81		0		-28421.19		7:27:45		m

		S1148780101:		#B3q0		1148780101:		$B3q0		d-		30.33		4.08		26.46		3.78		3.81		0		-28422.14		7:28:15		m

		S1148780131:		#B3q0		1148780131:		$B3q0		d-		30.37		4.04		26.56		3.78		3.81		0		-28423.23		7:28:45		m

		S1148780161:		#B3q0		1148780161:		$B3q0		d-		30.37		4.04		26.56		3.78		3.81		0		-28424.18		7:29:15		m

		S1148780191:		#B3q0		1148780191:		$B3q0		d-		30.37		4		26.56		3.78		3.81		0		-28425.28		7:29:45		m

		S1148780221:		#B3q0		1148780221:		$B3q0		d-		30.33		4.04		26.46		3.78		3.81		0		-28426.23		7:30:15		m

		S1148780251:		#B3q0		1148780251:		$B3q0		d-		30.33		4.04		26.56		3.78		3.81		0		-28427.31		7:30:45		m

		S1148780281:		#B3q0		1148780281:		$B3q0		d-		30.33		4.04		26.56		3.78		3.81		0		-28428.27		7:31:15		m

		S1148780311:		#B3q0		1148780311:		$B3q0		d-		30.33		4		26.46		3.78		3.81		0		-28429.36		7:31:45		m

		S1148780341:		#B3q0		1148780341:		$B3q0		d-		30.33		4.04		26.56		3.78		3.81		0		-28430.31		7:32:15		m

		S1148780371:		#B3q0		1148780371:		$B3q0		d-		30.33		4.04		26.56		3.78		3.81		0		-28431.4		7:32:45		m

		S1148780401:		#B3q0		1148780401:		$B3q0		d-		30.33		4.04		26.56		3.78		3.81		0		-28432.35		7:33:15		m

		S1148780431:		#B3q0		1148780431:		$B3q0		d-		30.3		4.08		26.46		3.78		3.81		0		-28433.44		7:33:45		m

		S1148780461:		#B3q0		1148780461:		$B3q0		d-		30.33		4		26.46		3.77		3.81		0		-28434.39		7:34:15		m

		S1148780491:		#B3q0		1148780491:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28435.48		7:34:45		m

		S1148780521:		#B3q0		1148780521:		$B3q0		d-		30.33		4		26.56		3.77		3.81		0		-28436.43		7:35:15		m

		S1148780551:		#B3q0		1148780551:		$B3q0		d-		30.33		4		26.56		3.77		3.81		0		-28437.52		7:35:45		m

		S1148780581:		#B3q0		1148780581:		$B3q0		d-		30.33		4		26.56		3.77		3.81		0		-28438.47		7:36:15		m

		S1148780611:		#B3q0		1148780611:		$B3q0		d-		30.33		4.08		26.56		3.77		3.81		0		-28439.56		7:36:45		m

		S1148780641:		#B3q0		1148780641:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28440.51		7:37:15		m

		S1148780671:		#B3q0		1148780671:		$B3q0		d-		30.33		4.04		26.66		3.77		3.81		0		-28441.6		7:37:45		m

		S1148780701:		#B3q0		1148780701:		$B3q0		d-		30.33		4.08		26.56		3.77		3.81		0		-28442.56		7:38:15		m

		S1148780731:		#B3q0		1148780731:		$B3q0		d-		30.33		4.04		26.46		3.77		3.81		0		-28443.64		7:38:45		m

		S1148780761:		#B3q0		1148780761:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28444.59		7:39:15		m

		S1148780791:		#B3q0		1148780791:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28445.68		7:39:45		m

		S1148780821:		#B3q0		1148780821:		$B3q0		d-		30.3		4.04		26.56		3.77		3.81		0		-28446.62		7:40:15		m

		S1148780851:		#B3q0		1148780851:		$B3q0		d-		30.3		4.04		26.46		3.77		3.81		0		-28447.71		7:40:45		m

		S1148780881:		#B3q0		1148780881:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28448.66		7:41:15		m

		S1148780911:		#B3q0		1148780911:		$B3q0		d-		30.33		4		26.46		3.77		3.81		0		-28449.75		7:41:45		m

		S1148780941:		#B3q0		1148780941:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28450.7		7:42:15		m

		S1148780971:		#B3q0		1148780971:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28451.79		7:42:45		m

		S1148781001:		#B3q0		1148781001:		$B3q0		d-		30.3		4.04		26.56		3.77		3.81		0		-28452.74		7:43:15		m

		S1148781031:		#B3q0		1148781031:		$B3q0		d-		30.33		4		26.56		3.77		3.81		0		-28453.83		7:43:45		m

		S1148781061:		#B3q0		1148781061:		$B3q0		d-		30.33		4.04		26.56		3.77		3.81		0		-28454.79		7:44:15		m

		S1148781091:		#B3q0		1148781091:		$B3q0		d-		30.3		4.04		26.56		3.77		3.81		0		-28455.87		7:44:45		m

		S1148781121:		#B3q0		1148781121:		$B3q0		d-		30.3		4		26.56		3.77		3.81		0		-28456.83		7:45:15		m

		S1148781151:		#B3q0		1148781151:		$B3q0		d-		30.33		4		26.56		3.77		3.8		0		-28457.91		7:45:45		m

		S1148781181:		#B3q0		1148781181:		$B3q0		d-		30.33		4.04		26.46		3.77		3.8		0		-28458.87		7:46:15		m

		S1148781211:		#B3q0		1148781211:		$B3q0		d-		30.3		4		26.56		3.77		3.8		0		-28459.96		7:46:45		m

		S1148781241:		#B3q0		1148781241:		$B3q0		d-		30.33		4		26.56		3.77		3.8		0		-28460.91		7:47:15		m

		S1148781271:		#B3q0		1148781271:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28462		7:47:45		m

		S1148781301:		#B3q0		1148781301:		$B3q0		d-		30.33		4		26.56		3.77		3.8		0		-28462.95		7:48:15		m

		S1148781331:		#B3q0		1148781331:		$B3q0		d-		30.33		4.04		26.46		3.77		3.8		0		-28464.03		7:48:45		m

		S1148781361:		#B3q0		1148781361:		$B3q0		d-		30.3		4		26.46		3.77		3.8		0		-28464.98		7:49:15		m

		S1148781391:		#B3q0		1148781391:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28466.07		7:49:45		m

		S1148781421:		#B3q0		1148781421:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28467.02		7:50:15		m

		S1148781451:		#B3q0		1148781451:		$B3q0		d-		30.33		4.04		26.56		3.77		3.8		0		-28468.11		7:50:45		m

		S1148781481:		#B3q0		1148781481:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28469.06		7:51:15		m

		S1148781511:		#B3q0		1148781511:		$B3q0		d-		30.3		4		26.46		3.77		3.8		0		-28470.15		7:51:45		m

		S1148781541:		#B3q0		1148781541:		$B3q0		d-		30.3		4.08		26.66		3.77		3.8		0		-28471.1		7:52:15		m

		S1148781571:		#B3q0		1148781571:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28472.18		7:52:45		m

		S1148781601:		#B3q0		1148781601:		$B3q0		d-		30.3		4.08		26.56		3.77		3.8		0		-28473.13		7:53:15		m

		S1148781631:		#B3q0		1148781631:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28474.22		7:53:45		m

		S1148781661:		#B3q0		1148781661:		$B3q0		d-		30.3		4.04		26.56		3.77		3.8		0		-28475.17		7:54:15		m

		S1148781691:		#B3q0		1148781691:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28476.25		7:54:45		m

		S1148781721:		#B3q0		1148781721:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28477.21		7:55:15		m

		S1148781751:		#B3q0		1148781751:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28478.3		7:55:45		m

		S1148781781:		#B3q0		1148781781:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28479.25		7:56:15		m

		S1148781811:		#B3q0		1148781811:		$B3q0		d-		30.26		4		26.46		3.76		3.8		0		-28480.33		7:56:45		m

		S1148781841:		#B3q0		1148781841:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28481.28		7:57:15		m

		S1148781871:		#B3q0		1148781871:		$B3q0		d-		30.26		4.04		26.46		3.76		3.8		0		-28482.37		7:57:45		m

		S1148781901:		#B3q0		1148781901:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28483.33		7:58:15		m

		S1148781931:		#B3q0		1148781931:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28484.41		7:58:45		m

		S1148781961:		#B3q0		1148781961:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28485.36		7:59:15		m

		S1148781991:		#B3q0		1148781991:		$B3q0		d-		30.3		4.04		26.46		3.76		3.8		0		-28486.44		7:59:45		m

		S1148782021:		#B3q0		1148782021:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28487.39		8:00:15		m

		S1148782051:		#B3q0		1148782051:		$B3q0		d-		30.26		4.04		26.46		3.76		3.8		0		-28488.48		8:00:45		m

		S1148782081:		#B3q0		1148782081:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28489.44		8:01:15		m

		S1148782111:		#B3q0		1148782111:		$B3q0		d-		30.3		4.04		26.56		3.76		3.8		0		-28490.53		8:01:45		m

		S1148782141:		#B3q0		1148782141:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28491.48		8:02:15		m

		S1148782171:		#B3q0		1148782171:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28492.57		8:02:45		m

		S1148782201:		#B3q0		1148782201:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28493.52		8:03:15		m

		S1148782231:		#B3q0		1148782231:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28494.6		8:03:45		m

		S1148782261:		#B3q0		1148782261:		$B3q0		d-		30.26		4.04		26.66		3.76		3.8		0		-28495.55		8:04:15		m

		S1148782291:		#B3q0		1148782291:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28496.63		8:04:45		m

		S1148782321:		#B3q0		1148782321:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28497.58		8:05:15		m

		S1148782351:		#B3q0		1148782351:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28498.66		8:05:45		m

		S1148782381:		#B3q0		1148782381:		$B3q0		d-		30.22		4		26.56		3.76		3.8		0		-28499.62		8:06:15		m

		S1148782411:		#B3q0		1148782411:		$B3q0		d-		30.26		4.08		26.46		3.76		3.8		0		-28500.7		8:06:45		m

		S1148782441:		#B3q0		1148782441:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28501.65		8:07:15		m

		S1148782471:		#B3q0		1148782471:		$B3q0		d-		30.26		4		26.56		3.76		3.8		0		-28502.74		8:07:45		m

		S1148782501:		#B3q0		1148782501:		$B3q0		d-		30.26		4.04		26.46		3.76		3.8		0		-28503.69		8:08:15		m

		S1148782531:		#B3q0		1148782531:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28504.77		8:08:45		m

		S1148782561:		#B3q0		1148782561:		$B3q0		d-		30.22		4.04		26.56		3.76		3.8		0		-28505.72		8:09:15		m

		S1148782591:		#B3q0		1148782591:		$B3q0		d-		30.22		4.04		26.56		3.76		3.8		0		-28506.8		8:09:45		m

		S1148782621:		#B3q0		1148782621:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28507.75		8:10:15		m

		S1148782651:		#B3q0		1148782651:		$B3q0		d-		30.22		4.08		26.56		3.76		3.8		0		-28508.84		8:10:45		m

		S1148782681:		#B3q0		1148782681:		$B3q0		d-		30.22		4.04		26.56		3.76		3.8		0		-28509.78		8:11:15		m

		S1148782711:		#B3q0		1148782711:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28510.87		8:11:45		m

		S1148782741:		#B3q0		1148782741:		$B3q0		d-		30.22		4.04		26.56		3.76		3.8		0		-28511.82		8:12:15		m

		S1148782771:		#B3q0		1148782771:		$B3q0		d-		30.26		4.04		26.56		3.76		3.8		0		-28512.9		8:12:45		m

		S1148782801:		#B3q0		1148782801:		$B3q0		d-		30.22		4		26.56		3.76		3.8		0		-28513.85		8:13:15		m

		S1148782831:		#B3q0		1148782831:		$B3q0		d-		30.22		4.04		26.56		3.76		3.8		0		-28514.93		8:13:45		m

		S1148782861:		#B3q0		1148782861:		$B3q0		d-		30.22		4		26.56		3.76		3.79		0		-28515.88		8:14:15		m

		S1148782891:		#B3q0		1148782891:		$B3q0		d-		30.22		4		26.56		3.76		3.79		0		-28516.96		8:14:45		m

		S1148782921:		#B3q0		1148782921:		$B3q0		d-		30.22		4.04		26.66		3.76		3.79		0		-28517.91		8:15:15		m

		S1148782951:		#B3q0		1148782951:		$B3q0		d-		30.26		4		26.46		3.76		3.79		0		-28519		8:15:45		m

		S1148782981:		#B3q0		1148782981:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28519.95		8:16:15		m

		S1148783011:		#B3q0		1148783011:		$B3q0		d-		30.22		4.08		26.56		3.76		3.79		0		-28521.04		8:16:45		m

		S1148783041:		#B3q0		1148783041:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28521.98		8:17:15		m

		S1148783071:		#B3q0		1148783071:		$B3q0		d-		30.22		4		26.46		3.76		3.79		0		-28523.06		8:17:45		m

		S1148783101:		#B3q0		1148783101:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28524.01		8:18:15		m

		S1148783131:		#B3q0		1148783131:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28525.1		8:18:45		m

		S1148783161:		#B3q0		1148783161:		$B3q0		d-		30.22		4		26.56		3.76		3.79		0		-28526.05		8:19:15		m

		S1148783191:		#B3q0		1148783191:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28527.13		8:19:45		m

		S1148783221:		#B3q0		1148783221:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28528.08		8:20:15		m

		S1148783251:		#B3q0		1148783251:		$B3q0		d-		30.22		4.04		26.46		3.76		3.79		0		-28529.17		8:20:45		m

		S1148783281:		#B3q0		1148783281:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28530.12		8:21:15		m

		S1148783311:		#B3q0		1148783311:		$B3q0		d-		30.18		4.04		26.66		3.76		3.79		0		-28531.2		8:21:45		m

		S1148783341:		#B3q0		1148783341:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28532.15		8:22:15		m

		S1148783371:		#B3q0		1148783371:		$B3q0		d-		30.18		4.08		26.56		3.76		3.79		0		-28533.24		8:22:45		m

		S1148783401:		#B3q0		1148783401:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28534.19		8:23:15		m

		S1148783431:		#B3q0		1148783431:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28535.27		8:23:45		m

		S1148783461:		#B3q0		1148783461:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28536.22		8:24:15		m

		S1148783491:		#B3q0		1148783491:		$B3q0		d-		30.22		4.04		26.56		3.76		3.79		0		-28537.3		8:24:45		m

		S1148783521:		#B3q0		1148783521:		$B3q0		d-		30.18		4.04		26.66		3.76		3.79		0		-28538.26		8:25:15		m

		S1148783551:		#B3q0		1148783551:		$B3q0		d-		30.18		4		26.56		3.76		3.79		0		-28539.34		8:25:45		m

		S1148783581:		#B3q0		1148783581:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28540.29		8:26:15		m

		S1148783611:		#B3q0		1148783611:		$B3q0		d-		30.18		4		26.56		3.76		3.79		0		-28541.37		8:26:45		m

		S1148783641:		#B3q0		1148783641:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28542.32		8:27:15		m

		S1148783671:		#B3q0		1148783671:		$B3q0		d-		30.18		4		26.46		3.76		3.79		0		-28543.4		8:27:45		m

		S1148783701:		#B3q0		1148783701:		$B3q0		d-		30.18		4.04		26.56		3.76		3.79		0		-28544.35		8:28:15		m

		S1148783731:		#B3q0		1148783731:		$B3q0		d-		30.18		4.04		26.56		3.75		3.79		0		-28545.43		8:28:45		m

		S1148783761:		#B3q0		1148783761:		$B3q0		d-		30.18		4.04		26.56		3.75		3.79		0		-28546.38		8:29:15		m

		S1148783791:		#B3q0		1148783791:		$B3q0		d-		30.18		4.04		26.56		3.75		3.79		0		-28547.47		8:29:45		m

		S1148783821:		#B3q0		1148783821:		$B3q0		d-		30.18		4		26.56		3.75		3.79		0		-28548.42		8:30:15		m

		S1148783851:		#B3q0		1148783851:		$B3q0		d-		30.18		4		26.56		3.75		3.79		0		-28549.5		8:30:45		m

		S1148783881:		#B3q0		1148783881:		$B3q0		d-		30.18		4		26.56		3.75		3.79		0		-28550.45		8:31:15		m

		S1148783911:		#B3q0		1148783911:		$B3q0		d-		30.18		4.04		26.56		3.75		3.79		0		-28551.53		8:31:45		m

		S1148783941:		#B3q0		1148783941:		$B3q0		d-		30.18		4.04		26.56		3.75		3.79		0		-28552.48		8:32:15		m

		S1148783971:		#B3q0		1148783971:		$B3q0		d-		30.18		4.04		26.46		3.75		3.79		0		-28553.56		8:32:45		m

		S1148784001:		#B3q0		1148784001:		$B3q0		d-		30.15		4.04		26.56		3.75		3.79		0		-28554.51		8:33:15		m

		S1148784031:		#B3q0		1148784031:		$B3q0		d-		30.15		4		26.56		3.75		3.79		0		-28555.59		8:33:45		m

		S1148784061:		#B3q0		1148784061:		$B3q0		d-		30.18		4		26.56		3.75		3.79		0		-28556.54		8:34:15		m

		S1148784091:		#B3q0		1148784091:		$B3q0		d-		30.18		4		26.56		3.75		3.79		0		-28557.62		8:34:45		m

		S1148784121:		#B3q0		1148784121:		$B3q0		d-		30.15		4.04		26.56		3.75		3.79		0		-28558.57		8:35:15		m

		S1148784151:		#B3q0		1148784151:		$B3q0		d-		30.18		4.04		26.56		3.75		3.78		0		-28559.65		8:35:45		m

		S1148784181:		#B3q0		1148784181:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28560.6		8:36:15		m

		S1148784211:		#B3q0		1148784211:		$B3q0		d-		30.15		4		26.46		3.75		3.78		0		-28561.68		8:36:45		m

		S1148784241:		#B3q0		1148784241:		$B3q0		d-		30.18		4.04		26.56		3.75		3.78		0		-28562.63		8:37:15		m

		S1148784271:		#B3q0		1148784271:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28563.71		8:37:45		m

		S1148784301:		#B3q0		1148784301:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28564.66		8:38:15		m

		S1148784331:		#B3q0		1148784331:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28565.75		8:38:45		m

		S1148784361:		#B3q0		1148784361:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28566.69		8:39:15		m

		S1148784391:		#B3q0		1148784391:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28567.78		8:39:45		m

		S1148784421:		#B3q0		1148784421:		$B3q0		d-		30.18		4.04		26.56		3.75		3.78		0		-28568.73		8:40:15		m

		S1148784451:		#B3q0		1148784451:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28569.81		8:40:45		m

		S1148784481:		#B3q0		1148784481:		$B3q0		d-		30.15		4.08		26.56		3.75		3.78		0		-28570.75		8:41:15		m

		S1148784511:		#B3q0		1148784511:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28571.84		8:41:45		m

		S1148784541:		#B3q0		1148784541:		$B3q0		d-		30.15		4		26.46		3.75		3.78		0		-28572.79		8:42:15		m

		S1148784571:		#B3q0		1148784571:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28573.87		8:42:45		m

		S1148784601:		#B3q0		1148784601:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28574.82		8:43:15		m

		S1148784631:		#B3q0		1148784631:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28575.9		8:43:45		m

		S1148784661:		#B3q0		1148784661:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28576.84		8:44:15		m

		S1148784691:		#B3q0		1148784691:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28577.92		8:44:45		m

		S1148784721:		#B3q0		1148784721:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28578.87		8:45:15		m

		S1148784751:		#B3q0		1148784751:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28579.95		8:45:45		m

		S1148784781:		#B3q0		1148784781:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28580.9		8:46:15		m

		S1148784811:		#B3q0		1148784811:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28581.99		8:46:45		m

		S1148784841:		#B3q0		1148784841:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28582.93		8:47:15		m

		S1148784871:		#B3q0		1148784871:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28584.01		8:47:45		m

		S1148784901:		#B3q0		1148784901:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28584.96		8:48:15		m

		S1148784931:		#B3q0		1148784931:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28586.04		8:48:45		m

		S1148784961:		#B3q0		1148784961:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28586.98		8:49:15		m

		S1148784991:		#B3q0		1148784991:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28588.06		8:49:45		m

		S1148785021:		#B3q0		1148785021:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28589.01		8:50:15		m

		S1148785051:		#B3q0		1148785051:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28590.09		8:50:45		m

		S1148785081:		#B3q0		1148785081:		$B3q0		d-		30.15		4		26.66		3.75		3.78		0		-28591.03		8:51:15		m

		S1148785111:		#B3q0		1148785111:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28592.12		8:51:45		m

		S1148785141:		#B3q0		1148785141:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28593.06		8:52:15		m

		S1148785171:		#B3q0		1148785171:		$B3q0		d-		30.15		4.04		26.56		3.75		3.78		0		-28594.14		8:52:45		m

		S1148785201:		#B3q0		1148785201:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28595.09		8:53:15		m

		S1148785231:		#B3q0		1148785231:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28596.17		8:53:45		m

		S1148785261:		#B3q0		1148785261:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28597.11		8:54:15		m

		S1148785291:		#B3q0		1148785291:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28598.19		8:54:45		m

		S1148785321:		#B3q0		1148785321:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28599.14		8:55:15		m

		S1148785351:		#B3q0		1148785351:		$B3q0		d-		30.15		4		26.56		3.75		3.78		0		-28600.22		8:55:45		m

		S1148785381:		#B3q0		1148785381:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28601.17		8:56:15		m

		S1148785411:		#B3q0		1148785411:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28602.25		8:56:45		m

		S1148785441:		#B3q0		1148785441:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28603.19		8:57:15		m

		S1148785471:		#B3q0		1148785471:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28604.27		8:57:45		m

		S1148785501:		#B3q0		1148785501:		$B3q0		d-		30.11		4.08		26.56		3.75		3.78		0		-28605.21		8:58:15		m

		S1148785531:		#B3q0		1148785531:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28606.29		8:58:45		m

		S1148785561:		#B3q0		1148785561:		$B3q0		d-		30.07		4		26.56		3.75		3.78		0		-28607.24		8:59:15		m

		S1148785591:		#B3q0		1148785591:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28608.32		8:59:45		m

		S1148785621:		#B3q0		1148785621:		$B3q0		d-		30.11		4.04		26.46		3.75		3.78		0		-28609.27		9:00:15		m

		S1148785651:		#B3q0		1148785651:		$B3q0		d-		30.07		4		26.56		3.75		3.78		0		-28610.35		9:00:45		m

		S1148785681:		#B3q0		1148785681:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28611.29		9:01:15		m

		S1148785711:		#B3q0		1148785711:		$B3q0		d-		30.11		4		26.56		3.75		3.78		0		-28612.37		9:01:45		m

		S1148785741:		#B3q0		1148785741:		$B3q0		d-		30.11		4.04		26.56		3.75		3.78		0		-28613.32		9:02:15		m

		S1148785771:		#B3q0		1148785771:		$B3q0		d-		30.11		4.04		26.46		3.74		3.78		0		-28614.4		9:02:45		m

		S1148785801:		#B3q0		1148785801:		$B3q0		d-		30.11		4.04		26.56		3.74		3.78		0		-28615.34		9:03:15		m

		S1148785831:		#B3q0		1148785831:		$B3q0		d-		30.11		4.04		26.56		3.74		3.78		0		-28616.42		9:03:45		m

		S1148785861:		#B3q0		1148785861:		$B3q0		d-		30.07		4.04		26.56		3.74		3.78		0		-28617.36		9:04:15		m

		S1148785891:		#B3q0		1148785891:		$B3q0		d-		30.07		4		26.56		3.74		3.78		0		-28618.44		9:04:45		m

		S1148785921:		#B3q0		1148785921:		$B3q0		d-		30.07		4		26.56		3.74		3.78		0		-28619.38		9:05:15		m

		S1148785951:		#B3q0		1148785951:		$B3q0		d-		30.11		4		26.46		3.74		3.78		0		-28620.46		9:05:45		m

		S1148785981:		#B3q0		1148785981:		$B3q0		d-		30.11		4		26.56		3.74		3.78		0		-28621.41		9:06:15		m

		S1148786011:		#B3q0		1148786011:		$B3q0		d-		30.07		4.04		26.56		3.74		3.78		0		-28622.49		9:06:45		m

		S1148786041:		#B3q0		1148786041:		$B3q0		d-		30.07		4.08		26.56		3.74		3.78		0		-28623.44		9:07:15		m

		S1148786071:		#B3q0		1148786071:		$B3q0		d-		30.11		4.08		26.56		3.74		3.78		0		-28624.51		9:07:45		m

		S1148786101:		#B3q0		1148786101:		$B3q0		d-		30.11		4.04		26.56		3.74		3.78		0		-28625.46		9:08:15		m

		S1148786131:		#B3q0		1148786131:		$B3q0		d-		30.11		4		26.46		3.74		3.78		0		-28626.54		9:08:45		m

		S1148786161:		#B3q0		1148786161:		$B3q0		d-		30.07		4.08		26.56		3.74		3.78		0		-28627.48		9:09:15		m

		S1148786191:		#B3q0		1148786191:		$B3q0		d-		30.07		4.04		26.46		3.74		3.77		0		-28628.56		9:09:45		m

		S1148786221:		#B3q0		1148786221:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28629.5		9:10:15		m

		S1148786251:		#B3q0		1148786251:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28630.58		9:10:45		m

		S1148786281:		#B3q0		1148786281:		$B3q0		d-		30.07		4.04		26.46		3.74		3.77		0		-28631.53		9:11:15		m

		S1148786311:		#B3q0		1148786311:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28632.61		9:11:45		m

		S1148786341:		#B3q0		1148786341:		$B3q0		d-		30.07		4.08		26.56		3.74		3.77		0		-28633.56		9:12:15		m

		S1148786371:		#B3q0		1148786371:		$B3q0		d-		30.07		4.04		26.46		3.74		3.77		0		-28634.63		9:12:45		m

		S1148786401:		#B3q0		1148786401:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28635.58		9:13:15		m

		S1148786431:		#B3q0		1148786431:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28636.66		9:13:45		m

		S1148786461:		#B3q0		1148786461:		$B3q0		d-		30.07		4.04		26.46		3.74		3.77		0		-28637.6		9:14:15		m

		S1148786491:		#B3q0		1148786491:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28638.68		9:14:45		m

		S1148786521:		#B3q0		1148786521:		$B3q0		d-		30.07		4.04		26.56		3.74		3.77		0		-28639.63		9:15:15		m

		S1148786551:		#B3q0		1148786551:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28640.71		9:15:45		m

		S1148786581:		#B3q0		1148786581:		$B3q0		d-		30.03		4		26.56		3.74		3.77		0		-28641.65		9:16:15		m

		S1148786611:		#B3q0		1148786611:		$B3q0		d-		30.07		4.04		26.46		3.74		3.77		0		-28642.73		9:16:45		m

		S1148786641:		#B3q0		1148786641:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28643.68		9:17:15		m

		S1148786671:		#B3q0		1148786671:		$B3q0		d-		30.07		4		26.56		3.74		3.77		0		-28644.76		9:17:45		m

		S1148786701:		#B3q0		1148786701:		$B3q0		d-		30.07		4		26.56		3.74		3.77		0		-28645.7		9:18:15		m

		S1148786731:		#B3q0		1148786731:		$B3q0		d-		30.03		4		26.56		3.74		3.77		0		-28646.78		9:18:45		m

		S1148786761:		#B3q0		1148786761:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28647.73		9:19:15		m

		S1148786791:		#B3q0		1148786791:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28648.8		9:19:45		m

		S1148786821:		#B3q0		1148786821:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28649.75		9:20:15		m

		S1148786851:		#B3q0		1148786851:		$B3q0		d-		30.03		4		26.56		3.74		3.77		0		-28650.82		9:20:45		m

		S1148786881:		#B3q0		1148786881:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28651.76		9:21:15		m

		S1148786911:		#B3q0		1148786911:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28652.84		9:21:45		m

		S1148786941:		#B3q0		1148786941:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28653.78		9:22:15		m

		S1148786971:		#B3q0		1148786971:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28654.86		9:22:45		m

		S1148787001:		#B3q0		1148787001:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28655.8		9:23:15		m

		S1148787031:		#B3q0		1148787031:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28656.87		9:23:45		m

		S1148787061:		#B3q0		1148787061:		$B3q0		d-		30.03		4.08		26.56		3.74		3.77		0		-28657.82		9:24:15		m

		S1148787091:		#B3q0		1148787091:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28658.89		9:24:45		m

		S1148787121:		#B3q0		1148787121:		$B3q0		d-		30.03		4.04		26.56		3.74		3.77		0		-28659.84		9:25:15		m

		S1148787151:		#B3q0		1148787151:		$B3q0		d-		30.03		4.04		26.46		3.74		3.77		0		-28660.92		9:25:45		m

		S1148787181:		#B3q0		1148787181:		$B3q0		d-		30		4.08		26.56		3.73		3.77		0		-28661.86		9:26:15		m

		S1148787211:		#B3q0		1148787211:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28662.94		9:26:45		m

		S1148787241:		#B3q0		1148787241:		$B3q0		d-		30.03		4.08		26.56		3.74		3.77		0		-28663.88		9:27:15		m

		S1148787271:		#B3q0		1148787271:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28664.95		9:27:45		m

		S1148787301:		#B3q0		1148787301:		$B3q0		d-		30.03		4		26.56		3.73		3.77		0		-28665.9		9:28:15		m

		S1148787331:		#B3q0		1148787331:		$B3q0		d-		30		4.04		26.56		3.73		3.77		0		-28666.97		9:28:45		m

		S1148787361:		#B3q0		1148787361:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28667.91		9:29:15		m

		S1148787391:		#B3q0		1148787391:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28668.99		9:29:45		m

		S1148787421:		#B3q0		1148787421:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28669.93		9:30:15		m

		S1148787451:		#B3q0		1148787451:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28671		9:30:45		m

		S1148787481:		#B3q0		1148787481:		$B3q0		d-		30.03		4		26.46		3.73		3.77		0		-28671.94		9:31:15		m

		S1148787511:		#B3q0		1148787511:		$B3q0		d-		30.03		4.04		26.56		3.73		3.77		0		-28673.02		9:31:45		m

		S1148787541:		#B3q0		1148787541:		$B3q0		d-		30.03		4		26.56		3.73		3.77		0		-28673.95		9:32:15		m

		S1148787571:		#B3q0		1148787571:		$B3q0		d-		30.03		4.04		26.46		3.73		3.77		0		-28675.03		9:32:45		m

		S1148787601:		#B3q0		1148787601:		$B3q0		d-		30		4.04		26.56		3.73		3.77		0		-28675.97		9:33:15		m

		S1148787631:		#B3q0		1148787631:		$B3q0		d-		30		4		26.56		3.73		3.77		0		-28677.05		9:33:45		m

		S1148787661:		#B3q0		1148787661:		$B3q0		d-		30		4.08		26.46		3.73		3.76		0		-28677.99		9:34:15		m

		S1148787691:		#B3q0		1148787691:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28679.06		9:34:45		m

		S1148787721:		#B3q0		1148787721:		$B3q0		d-		30.03		4.04		26.56		3.73		3.76		0		-28680		9:35:15		m

		S1148787751:		#B3q0		1148787751:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28681.08		9:35:45		m

		S1148787781:		#B3q0		1148787781:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28682.02		9:36:15		m

		S1148787811:		#B3q0		1148787811:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28683.09		9:36:45		m

		S1148787841:		#B3q0		1148787841:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28684.03		9:37:15		m

		S1148787871:		#B3q0		1148787871:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28685.11		9:37:45		m

		S1148787901:		#B3q0		1148787901:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28686.05		9:38:15		m

		S1148787931:		#B3q0		1148787931:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28687.12		9:38:45		m

		S1148787961:		#B3q0		1148787961:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28688.06		9:39:15		m

		S1148787991:		#B3q0		1148787991:		$B3q0		d-		30		4		26.66		3.73		3.76		0		-28689.15		9:39:45		m

		S1148788021:		#B3q0		1148788021:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28690.09		9:40:15		m

		S1148788051:		#B3q0		1148788051:		$B3q0		d-		30.03		4.04		26.56		3.73		3.76		0		-28691.17		9:40:45		m

		S1148788081:		#B3q0		1148788081:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28692.11		9:41:15		m

		S1148788111:		#B3q0		1148788111:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28693.19		9:41:45		m

		S1148788141:		#B3q0		1148788141:		$B3q0		d-		30		4.04		26.46		3.73		3.76		0		-28694.13		9:42:15		m

		S1148788171:		#B3q0		1148788171:		$B3q0		d-		30.03		4.08		26.56		3.73		3.76		0		-28695.21		9:42:45		m

		S1148788201:		#B3q0		1148788201:		$B3q0		d-		30		4.08		26.56		3.73		3.76		0		-28696.15		9:43:15		m

		S1148788231:		#B3q0		1148788231:		$B3q0		d-		30.03		4.04		26.56		3.73		3.76		0		-28697.22		9:43:45		m

		S1148788261:		#B3q0		1148788261:		$B3q0		d-		30.03		4		26.56		3.73		3.76		0		-28698.16		9:44:15		m

		S1148788291:		#B3q0		1148788291:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28699.23		9:44:45		m

		S1148788321:		#B3q0		1148788321:		$B3q0		d-		30		4.08		26.56		3.73		3.76		0		-28700.17		9:45:15		m

		S1148788351:		#B3q0		1148788351:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28701.25		9:45:45		m

		S1148788381:		#B3q0		1148788381:		$B3q0		d-		30		4.04		26.66		3.73		3.76		0		-28702.19		9:46:15		m

		S1148788411:		#B3q0		1148788411:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28703.26		9:46:45		m

		S1148788441:		#B3q0		1148788441:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28704.2		9:47:15		m

		S1148788471:		#B3q0		1148788471:		$B3q0		d-		30		4.08		26.56		3.73		3.76		0		-28705.28		9:47:45		m

		S1148788501:		#B3q0		1148788501:		$B3q0		d-		30		4.08		26.56		3.73		3.76		0		-28706.22		9:48:15		m

		S1148788531:		#B3q0		1148788531:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28707.29		9:48:45		m

		S1148788561:		#B3q0		1148788561:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28708.23		9:49:15		m

		S1148788591:		#B3q0		1148788591:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28709.31		9:49:45		m

		S1148788621:		#B3q0		1148788621:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28710.25		9:50:15		m

		S1148788651:		#B3q0		1148788651:		$B3q0		d-		30		4.04		26.56		3.73		3.76		0		-28711.33		9:50:45		m

		S1148788681:		#B3q0		1148788681:		$B3q0		d-		29.96		4.08		26.46		3.73		3.76		0		-28712.27		9:51:15		m

		S1148788711:		#B3q0		1148788711:		$B3q0		d-		29.96		4		26.56		3.73		3.76		0		-28713.35		9:51:45		m

		S1148788741:		#B3q0		1148788741:		$B3q0		d-		29.96		4		26.56		3.73		3.76		0		-28714.29		9:52:15		m

		S1148788771:		#B3q0		1148788771:		$B3q0		d-		29.96		4		26.56		3.73		3.76		0		-28715.36		9:52:45		m

		S1148788801:		#B3q0		1148788801:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28716.3		9:53:15		m

		S1148788831:		#B3q0		1148788831:		$B3q0		d-		30		4		26.56		3.73		3.76		0		-28717.38		9:53:45		m

		S1148788861:		#B3q0		1148788861:		$B3q0		d-		30		4.04		26.66		3.73		3.76		0		-28718.32		9:54:15		m

		S1148788891:		#B3q0		1148788891:		$B3q0		d-		29.96		4		26.56		3.73		3.76		0		-28719.4		9:54:45		m

		S1148788921:		#B3q0		1148788921:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28720.34		9:55:15		m

		S1148788951:		#B3q0		1148788951:		$B3q0		d-		29.96		4		26.56		3.73		3.76		0		-28721.41		9:55:45		m

		S1148788981:		#B3q0		1148788981:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28722.35		9:56:15		m

		S1148789011:		#B3q0		1148789011:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28723.42		9:56:45		m

		S1148789041:		#B3q0		1148789041:		$B3q0		d-		29.92		4.04		26.56		3.73		3.76		0		-28724.36		9:57:15		m

		S1148789071:		#B3q0		1148789071:		$B3q0		d-		29.96		4.04		26.66		3.73		3.76		0		-28725.44		9:57:45		m

		S1148789101:		#B3q0		1148789101:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28726.38		9:58:15		m

		S1148789131:		#B3q0		1148789131:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28727.45		9:58:45		m

		S1148789161:		#B3q0		1148789161:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28728.39		9:59:15		m

		S1148789191:		#B3q0		1148789191:		$B3q0		d-		29.96		4.04		26.56		3.73		3.76		0		-28729.46		9:59:45		m

		S1148789221:		#B3q0		1148789221:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28730.4		10:00:15		m

		S1148789251:		#B3q0		1148789251:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28731.48		10:00:45		m

		S1148789281:		#B3q0		1148789281:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28732.42		10:01:15		m

		S1148789311:		#B3q0		1148789311:		$B3q0		d-		29.96		4		26.66		3.72		3.76		0		-28733.49		10:01:45		m

		S1148789341:		#B3q0		1148789341:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28734.43		10:02:15		m

		S1148789371:		#B3q0		1148789371:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28735.5		10:02:45		m

		S1148789401:		#B3q0		1148789401:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28736.44		10:03:15		m

		S1148789431:		#B3q0		1148789431:		$B3q0		d-		29.92		4		26.56		3.72		3.76		0		-28737.52		10:03:45		m

		S1148789461:		#B3q0		1148789461:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28738.45		10:04:15		m

		S1148789491:		#B3q0		1148789491:		$B3q0		d-		29.92		4.04		26.66		3.72		3.76		0		-28739.53		10:04:45		m

		S1148789521:		#B3q0		1148789521:		$B3q0		d-		29.92		4.08		26.56		3.72		3.76		0		-28740.47		10:05:15		m

		S1148789551:		#B3q0		1148789551:		$B3q0		d-		29.96		4		26.56		3.72		3.76		0		-28741.54		10:05:45		m

		S1148789581:		#B3q0		1148789581:		$B3q0		d-		29.92		4.04		26.66		3.72		3.76		0		-28742.48		10:06:15		m

		S1148789611:		#B3q0		1148789611:		$B3q0		d-		29.92		4.04		26.66		3.72		3.76		0		-28743.56		10:06:45		m

		S1148789641:		#B3q0		1148789641:		$B3q0		d-		29.92		4.08		26.66		3.72		3.76		0		-28744.5		10:07:15		m

		S1148789671:		#B3q0		1148789671:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28745.57		10:07:45		m

		S1148789701:		#B3q0		1148789701:		$B3q0		d-		29.92		4.04		26.66		3.72		3.76		0		-28746.51		10:08:15		m

		S1148789731:		#B3q0		1148789731:		$B3q0		d-		29.96		4.04		26.56		3.72		3.76		0		-28747.58		10:08:45		m

		S1148789761:		#B3q0		1148789761:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28748.52		10:09:15		m

		S1148789791:		#B3q0		1148789791:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28749.59		10:09:45		m

		S1148789821:		#B3q0		1148789821:		$B3q0		d-		29.92		4		26.56		3.72		3.76		0		-28750.53		10:10:15		m

		S1148789851:		#B3q0		1148789851:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28751.6		10:10:45		m

		S1148789881:		#B3q0		1148789881:		$B3q0		d-		29.92		4.04		26.66		3.72		3.76		0		-28752.54		10:11:15		m

		S1148789911:		#B3q0		1148789911:		$B3q0		d-		29.92		4		26.66		3.72		3.76		0		-28753.61		10:11:45		m

		S1148789941:		#B3q0		1148789941:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28754.55		10:12:15		m

		S1148789971:		#B3q0		1148789971:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28755.63		10:12:45		m

		S1148790001:		#B3q0		1148790001:		$B3q0		d-		29.88		4		26.56		3.72		3.76		0		-28756.57		10:13:15		m

		S1148790031:		#B3q0		1148790031:		$B3q0		d-		29.92		4.04		26.56		3.72		3.76		0		-28757.64		10:13:45		m

		S1148790061:		#B3q0		1148790061:		$B3q0		d-		29.88		4		26.56		3.72		3.75		0		-28758.58		10:14:15		m

		S1148790091:		#B3q0		1148790091:		$B3q0		d-		29.88		4		26.56		3.72		3.75		0		-28759.66		10:14:45		m

		S1148790121:		#B3q0		1148790121:		$B3q0		d-		29.92		4		26.56		3.72		3.75		0		-28760.6		10:15:15		m

		S1148790151:		#B3q0		1148790151:		$B3q0		d-		29.88		4		26.56		3.72		3.75		0		-28761.67		10:15:45		m

		S1148790181:		#B3q0		1148790181:		$B3q0		d-		29.92		4		26.66		3.72		3.75		0		-28762.61		10:16:15		m

		S1148790211:		#B3q0		1148790211:		$B3q0		d-		29.88		4.04		26.56		3.72		3.75		0		-28763.69		10:16:45		m

		S1148790241:		#B3q0		1148790241:		$B3q0		d-		29.92		4.04		26.56		3.72		3.75		0		-28764.63		10:17:15		m

		S1148790271:		#B3q0		1148790271:		$B3q0		d-		29.88		4.04		26.56		3.72		3.75		0		-28765.7		10:17:45		m

		S1148790301:		#B3q0		1148790301:		$B3q0		d-		29.92		4		26.56		3.72		3.75		0		-28766.63		10:18:15		m

		S1148790331:		#B3q0		1148790331:		$B3q0		d-		29.88		4.04		26.56		3.72		3.75		0		-28767.71		10:18:45		m

		S1148790361:		#B3q0		1148790361:		$B3q0		d-		29.88		4.04		26.56		3.72		3.75		0		-28768.65		10:19:15		m

		S1148790391:		#B3q0		1148790391:		$B3q0		d-		29.88		4.04		26.56		3.72		3.75		0		-28769.72		10:19:45		m

		S1148790421:		#B3q0		1148790421:		$B3q0		d-		29.88		4		26.66		3.71		3.75		0		-28770.65		10:20:15		m

		S1148790451:		#B3q0		1148790451:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28771.73		10:20:45		m

		S1148790481:		#B3q0		1148790481:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28772.67		10:21:15		m

		S1148790511:		#B3q0		1148790511:		$B3q0		d-		29.88		4		26.66		3.71		3.75		0		-28773.74		10:21:45		m

		S1148790541:		#B3q0		1148790541:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28774.68		10:22:15		m

		S1148790571:		#B3q0		1148790571:		$B3q0		d-		29.88		4		26.66		3.71		3.75		0		-28775.75		10:22:45		m

		S1148790601:		#B3q0		1148790601:		$B3q0		d-		29.92		4		26.56		3.71		3.75		0		-28776.69		10:23:15		m

		S1148790631:		#B3q0		1148790631:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28777.76		10:23:45		m

		S1148790661:		#B3q0		1148790661:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28778.69		10:24:15		m

		S1148790691:		#B3q0		1148790691:		$B3q0		d-		29.88		4		26.56		3.71		3.75		0		-28779.77		10:24:45		m

		S1148790721:		#B3q0		1148790721:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28780.7		10:25:15		m

		S1148790751:		#B3q0		1148790751:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28781.78		10:25:45		m

		S1148790781:		#B3q0		1148790781:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28782.71		10:26:15		m

		S1148790811:		#B3q0		1148790811:		$B3q0		d-		29.88		4.08		26.66		3.71		3.75		0		-28783.78		10:26:45		m

		S1148790841:		#B3q0		1148790841:		$B3q0		d-		29.88		4.04		26.66		3.71		3.75		0		-28784.72		10:27:15		m

		S1148790871:		#B3q0		1148790871:		$B3q0		d-		29.88		4		26.66		3.71		3.75		0		-28785.79		10:27:45		m

		S1148790901:		#B3q0		1148790901:		$B3q0		d-		29.88		4		26.56		3.71		3.75		0		-28786.73		10:28:15		m

		S1148790931:		#B3q0		1148790931:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28787.8		10:28:45		m

		S1148790961:		#B3q0		1148790961:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28788.74		10:29:15		m

		S1148790991:		#B3q0		1148790991:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28789.81		10:29:45		m

		S1148791021:		#B3q0		1148791021:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28790.74		10:30:15		m

		S1148791051:		#B3q0		1148791051:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28791.81		10:30:45		m

		S1148791081:		#B3q0		1148791081:		$B3q0		d-		29.84		4		26.56		3.71		3.75		0		-28792.75		10:31:15		m

		S1148791111:		#B3q0		1148791111:		$B3q0		d-		29.88		4.04		26.56		3.71		3.75		0		-28793.82		10:31:45		m

		S1148791141:		#B3q0		1148791141:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28794.75		10:32:15		m

		S1148791171:		#B3q0		1148791171:		$B3q0		d-		29.84		4		26.66		3.71		3.75		0		-28795.82		10:32:45		m

		S1148791201:		#B3q0		1148791201:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28796.76		10:33:15		m

		S1148791231:		#B3q0		1148791231:		$B3q0		d-		29.84		4		26.66		3.71		3.75		0		-28797.83		10:33:45		m

		S1148791261:		#B3q0		1148791261:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28798.77		10:34:15		m

		S1148791291:		#B3q0		1148791291:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28799.85		10:34:45		m

		S1148791321:		#B3q0		1148791321:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28800.78		10:35:15		m

		S1148791351:		#B3q0		1148791351:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28801.86		10:35:45		m

		S1148791381:		#B3q0		1148791381:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28802.79		10:36:15		m

		S1148791411:		#B3q0		1148791411:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28803.87		10:36:45		m

		S1148791441:		#B3q0		1148791441:		$B3q0		d-		29.84		4		26.66		3.71		3.75		0		-28804.81		10:37:15		m

		S1148791471:		#B3q0		1148791471:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28805.88		10:37:45		m

		S1148791501:		#B3q0		1148791501:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28806.81		10:38:15		m

		S1148791531:		#B3q0		1148791531:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28807.88		10:38:45		m

		S1148791561:		#B3q0		1148791561:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28808.82		10:39:15		m

		S1148791591:		#B3q0		1148791591:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28809.88		10:39:45		m

		S1148791621:		#B3q0		1148791621:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28810.82		10:40:15		m

		S1148791651:		#B3q0		1148791651:		$B3q0		d-		29.8		4.04		26.66		3.71		3.75		0		-28811.89		10:40:45		m

		S1148791681:		#B3q0		1148791681:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28812.83		10:41:15		m

		S1148791711:		#B3q0		1148791711:		$B3q0		d-		29.8		4		26.66		3.71		3.75		0		-28813.9		10:41:45		m

		S1148791741:		#B3q0		1148791741:		$B3q0		d-		29.8		4		26.66		3.71		3.75		0		-28814.84		10:42:15		m

		S1148791771:		#B3q0		1148791771:		$B3q0		d-		29.84		4.04		26.56		3.71		3.75		0		-28815.91		10:42:45		m

		S1148791801:		#B3q0		1148791801:		$B3q0		d-		29.8		4.08		26.56		3.71		3.75		0		-28816.85		10:43:15		m

		S1148791831:		#B3q0		1148791831:		$B3q0		d-		29.8		4		26.56		3.71		3.75		0		-28817.92		10:43:45		m

		S1148791861:		#B3q0		1148791861:		$B3q0		d-		29.8		4.04		26.66		3.71		3.75		0		-28818.86		10:44:15		m

		S1148791891:		#B3q0		1148791891:		$B3q0		d-		29.8		4		26.56		3.71		3.75		0		-28819.93		10:44:45		m

		S1148791921:		#B3q0		1148791921:		$B3q0		d-		29.8		4		26.66		3.71		3.75		0		-28820.86		10:45:15		m

		S1148791951:		#B3q0		1148791951:		$B3q0		d-		29.84		4.04		26.66		3.71		3.75		0		-28821.93		10:45:45		m

		S1148791981:		#B3q0		1148791981:		$B3q0		d-		29.84		4.04		26.66		3.7		3.75		0		-28822.87		10:46:15		m

		S1148792011:		#B3q0		1148792011:		$B3q0		d-		29.8		4.04		26.56		3.7		3.75		0		-28823.94		10:46:45		m

		S1148792041:		#B3q0		1148792041:		$B3q0		d-		29.8		4.08		26.66		3.7		3.75		0		-28824.88		10:47:15		m

		S1148792071:		#B3q0		1148792071:		$B3q0		d-		29.8		4.04		26.56		3.7		3.75		0		-28825.95		10:47:45		m

		S1148792101:		#B3q0		1148792101:		$B3q0		d-		29.8		4.04		26.66		3.7		3.75		0		-28826.89		10:48:15		m

		S1148792131:		#B3q0		1148792131:		$B3q0		d-		29.8		4		26.66		3.7		3.75		0		-28827.96		10:48:45		m

		S1148792161:		#B3q0		1148792161:		$B3q0		d-		29.8		4.08		26.66		3.7		3.75		0		-28828.89		10:49:15		m

		S1148792191:		#B3q0		1148792191:		$B3q0		d-		29.8		4.04		26.66		3.7		3.75		0		-28829.96		10:49:45		m

		S1148792221:		#B3q0		1148792221:		$B3q0		d-		29.8		4.04		26.66		3.7		3.75		0		-28830.9		10:50:15		m

		S1148792251:		#B3q0		1148792251:		$B3q0		d-		29.8		4.08		26.66		3.7		3.75		0		-28831.97		10:50:45		m

		S1148792281:		#B3q0		1148792281:		$B3q0		d-		29.77		4.04		26.66		3.7		3.75		0		-28832.91		10:51:15		m

		S1148792311:		#B3q0		1148792311:		$B3q0		d-		29.8		4.04		26.66		3.7		3.75		0		-28833.97		10:51:45		m

		S1148792341:		#B3q0		1148792341:		$B3q0		d-		29.8		4.04		26.66		3.7		3.75		0		-28834.91		10:52:15		m

		S1148792371:		#B3q0		1148792371:		$B3q0		d-		29.8		4.08		26.66		3.7		3.75		0		-28835.98		10:52:45		m

		S1148792401:		#B3q0		1148792401:		$B3q0		d-		29.77		4.04		26.56		3.7		3.75		0		-28836.91		10:53:15		m

		S1148792431:		#B3q0		1148792431:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28837.98		10:53:45		m

		S1148792461:		#B3q0		1148792461:		$B3q0		d-		29.8		4.04		26.56		3.7		3.75		0		-28838.92		10:54:15		m

		S1148792491:		#B3q0		1148792491:		$B3q0		d-		29.77		3.96		26.56		3.7		3.74		0		-28839.99		10:54:45		m

		S1148792521:		#B3q0		1148792521:		$B3q0		d-		29.77		4.04		26.56		3.7		3.74		0		-28840.92		10:55:15		m

		S1148792551:		#B3q0		1148792551:		$B3q0		d-		29.8		4.04		26.66		3.7		3.74		0		-28841.99		10:55:45		m

		S1148792581:		#B3q0		1148792581:		$B3q0		d-		29.77		4.08		26.56		3.7		3.74		0		-28842.93		10:56:15		m

		S1148792611:		#B3q0		1148792611:		$B3q0		d-		29.8		4.04		26.66		3.7		3.74		0		-28843.99		10:56:45		m

		S1148792641:		#B3q0		1148792641:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28844.93		10:57:15		m

		S1148792671:		#B3q0		1148792671:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28846		10:57:45		m

		S1148792701:		#B3q0		1148792701:		$B3q0		d-		29.8		4.04		26.56		3.7		3.74		0		-28846.93		10:58:15		m

		S1148792731:		#B3q0		1148792731:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28848		10:58:45		m

		S1148792761:		#B3q0		1148792761:		$B3q0		d-		29.77		4		26.66		3.7		3.74		0		-28848.94		10:59:15		m

		S1148792791:		#B3q0		1148792791:		$B3q0		d-		29.77		4.08		26.66		3.7		3.74		0		-28850.01		10:59:45		m

		S1148792821:		#B3q0		1148792821:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28850.94		11:00:15		m

		S1148792851:		#B3q0		1148792851:		$B3q0		d-		29.77		4.04		26.56		3.7		3.74		0		-28852.01		11:00:45		m

		S1148792881:		#B3q0		1148792881:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28852.94		11:01:15		m

		S1148792911:		#B3q0		1148792911:		$B3q0		d-		29.77		4.04		26.56		3.7		3.74		0		-28854		11:01:45		m

		S1148792941:		#B3q0		1148792941:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28854.94		11:02:15		m

		S1148792971:		#B3q0		1148792971:		$B3q0		d-		29.77		4		26.66		3.7		3.74		0		-28856.01		11:02:45		m

		S1148793001:		#B3q0		1148793001:		$B3q0		d-		29.77		4.04		26.66		3.7		3.74		0		-28856.94		11:03:15		m

		S1148793031:		#B3q0		1148793031:		$B3q0		d-		29.73		4.04		26.66		3.7		3.74		0		-28858.01		11:03:45		m

		S1148793061:		#B3q0		1148793061:		$B3q0		d-		29.73		4		26.66		3.7		3.74		0		-28858.94		11:04:15		m

		S1148793091:		#B3q0		1148793091:		$B3q0		d-		29.73		4.04		26.56		3.69		3.74		0		-28860.01		11:04:45		m

		S1148793121:		#B3q0		1148793121:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28860.94		11:05:15		m

		S1148793151:		#B3q0		1148793151:		$B3q0		d-		29.73		4.08		26.66		3.69		3.74		0		-28862.01		11:05:45		m

		S1148793181:		#B3q0		1148793181:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28862.95		11:06:15		m

		S1148793211:		#B3q0		1148793211:		$B3q0		d-		29.73		4.08		26.66		3.69		3.74		0		-28864.01		11:06:45		m

		S1148793241:		#B3q0		1148793241:		$B3q0		d-		29.77		4.04		26.66		3.69		3.74		0		-28864.95		11:07:15		m

		S1148793271:		#B3q0		1148793271:		$B3q0		d-		29.73		4.08		26.56		3.69		3.74		0		-28866.02		11:07:45		m

		S1148793301:		#B3q0		1148793301:		$B3q0		d-		29.73		4		26.66		3.69		3.74		0		-28866.95		11:08:15		m

		S1148793331:		#B3q0		1148793331:		$B3q0		d-		29.77		4		26.66		3.69		3.74		0		-28868.02		11:08:45		m

		S1148793361:		#B3q0		1148793361:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28868.96		11:09:15		m

		S1148793391:		#B3q0		1148793391:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28870.02		11:09:45		m

		S1148793421:		#B3q0		1148793421:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28870.96		11:10:15		m

		S1148793451:		#B3q0		1148793451:		$B3q0		d-		29.73		4		26.66		3.69		3.74		0		-28872.03		11:10:45		m

		S1148793481:		#B3q0		1148793481:		$B3q0		d-		29.73		4		26.66		3.69		3.74		0		-28872.97		11:11:15		m

		S1148793511:		#B3q0		1148793511:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28874.03		11:11:45		m

		S1148793541:		#B3q0		1148793541:		$B3q0		d-		29.73		4.08		26.66		3.69		3.74		0		-28874.96		11:12:15		m

		S1148793571:		#B3q0		1148793571:		$B3q0		d-		29.73		4.04		26.56		3.69		3.74		0		-28876.02		11:12:45		m

		S1148793601:		#B3q0		1148793601:		$B3q0		d-		29.73		4		26.66		3.69		3.74		0		-28876.96		11:13:15		m

		S1148793631:		#B3q0		1148793631:		$B3q0		d-		29.73		4.08		26.66		3.69		3.74		0		-28878.02		11:13:45		m

		S1148793661:		#B3q0		1148793661:		$B3q0		d-		29.73		4.08		26.66		3.69		3.74		0		-28878.96		11:14:15		m

		S1148793691:		#B3q0		1148793691:		$B3q0		d-		29.69		4.04		26.66		3.69		3.74		0		-28880.03		11:14:45		m

		S1148793721:		#B3q0		1148793721:		$B3q0		d-		29.73		4		26.66		3.69		3.74		0		-28880.96		11:15:15		m

		S1148793751:		#B3q0		1148793751:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28882.03		11:15:45		m

		S1148793781:		#B3q0		1148793781:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28882.96		11:16:15		m

		S1148793811:		#B3q0		1148793811:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28884.03		11:16:45		m

		S1148793841:		#B3q0		1148793841:		$B3q0		d-		29.73		4.04		26.75		3.69		3.74		0		-28884.97		11:17:15		m

		S1148793871:		#B3q0		1148793871:		$B3q0		d-		29.69		4.04		26.66		3.69		3.74		0		-28886.04		11:17:45		m

		S1148793901:		#B3q0		1148793901:		$B3q0		d-		29.69		4		26.66		3.69		3.74		0		-28886.97		11:18:15		m

		S1148793931:		#B3q0		1148793931:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28888.04		11:18:45		m

		S1148793961:		#B3q0		1148793961:		$B3q0		d-		29.73		4.04		26.66		3.69		3.74		0		-28888.97		11:19:15		m

		S1148793991:		#B3q0		1148793991:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28890.04		11:19:45		m

		S1148794021:		#B3q0		1148794021:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28890.97		11:20:15		m

		S1148794051:		#B3q0		1148794051:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28892.04		11:20:45		m

		S1148794081:		#B3q0		1148794081:		$B3q0		d-		29.73		4.08		26.66		3.69		3.73		0		-28892.98		11:21:15		m

		S1148794111:		#B3q0		1148794111:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28894.04		11:21:45		m

		S1148794141:		#B3q0		1148794141:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28894.97		11:22:15		m

		S1148794171:		#B3q0		1148794171:		$B3q0		d-		29.73		4		26.66		3.69		3.73		0		-28896.04		11:22:45		m

		S1148794201:		#B3q0		1148794201:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28896.97		11:23:15		m

		S1148794231:		#B3q0		1148794231:		$B3q0		d-		29.73		4		26.66		3.69		3.73		0		-28898.03		11:23:45		m

		S1148794261:		#B3q0		1148794261:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28898.96		11:24:15		m

		S1148794291:		#B3q0		1148794291:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28900.03		11:24:45		m

		S1148794321:		#B3q0		1148794321:		$B3q0		d-		29.69		4		26.66		3.69		3.73		0		-28900.97		11:25:15		m

		S1148794351:		#B3q0		1148794351:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28902.03		11:25:45		m

		S1148794381:		#B3q0		1148794381:		$B3q0		d-		29.69		4.04		26.75		3.69		3.73		0		-28902.96		11:26:15		m

		S1148794411:		#B3q0		1148794411:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28904.03		11:26:45		m

		S1148794441:		#B3q0		1148794441:		$B3q0		d-		29.69		4		26.56		3.69		3.73		0		-28904.96		11:27:15		m

		S1148794471:		#B3q0		1148794471:		$B3q0		d-		29.73		4		26.66		3.69		3.73		0		-28906.02		11:27:45		m

		S1148794501:		#B3q0		1148794501:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28906.95		11:28:15		m

		S1148794531:		#B3q0		1148794531:		$B3q0		d-		29.69		4.08		26.66		3.69		3.73		0		-28908.02		11:28:45		m

		S1148794561:		#B3q0		1148794561:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28908.94		11:29:15		m

		S1148794591:		#B3q0		1148794591:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28910.01		11:29:45		m

		S1148794621:		#B3q0		1148794621:		$B3q0		d-		29.73		4.04		26.66		3.69		3.73		0		-28910.94		11:30:15		m

		S1148794651:		#B3q0		1148794651:		$B3q0		d-		29.65		4		26.66		3.69		3.73		0		-28912		11:30:45		m

		S1148794681:		#B3q0		1148794681:		$B3q0		d-		29.69		4.04		26.75		3.69		3.73		0		-28912.93		11:31:15		m

		S1148794711:		#B3q0		1148794711:		$B3q0		d-		29.65		4		26.66		3.69		3.73		0		-28914		11:31:45		m

		S1148794741:		#B3q0		1148794741:		$B3q0		d-		29.65		4.04		26.66		3.69		3.73		0		-28914.93		11:32:15		m

		S1148794771:		#B3q0		1148794771:		$B3q0		d-		29.69		4.08		26.66		3.69		3.73		0		-28915.99		11:32:45		m

		S1148794801:		#B3q0		1148794801:		$B3q0		d-		29.65		4		26.66		3.69		3.73		0		-28916.92		11:33:15		m

		S1148794831:		#B3q0		1148794831:		$B3q0		d-		29.69		4.04		26.66		3.69		3.73		0		-28917.98		11:33:45		m

		S1148794861:		#B3q0		1148794861:		$B3q0		d-		29.65		4		26.66		3.69		3.73		0		-28918.92		11:34:15		m

		S1148794891:		#B3q0		1148794891:		$B3q0		d-		29.65		4.04		26.75		3.69		3.73		0		-28919.99		11:34:45		m

		S1148794921:		#B3q0		1148794921:		$B3q0		d-		29.65		4.08		26.66		3.69		3.73		0		-28920.92		11:35:15		m

		S1148794951:		#B3q0		1148794951:		$B3q0		d-		29.65		4		26.66		3.68		3.73		0		-28921.98		11:35:45		m

		S1148794981:		#B3q0		1148794981:		$B3q0		d-		29.65		4		26.66		3.68		3.73		0		-28922.91		11:36:15		m

		S1148795011:		#B3q0		1148795011:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28923.98		11:36:45		m

		S1148795041:		#B3q0		1148795041:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28924.91		11:37:15		m

		S1148795071:		#B3q0		1148795071:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28925.98		11:37:45		m

		S1148795101:		#B3q0		1148795101:		$B3q0		d-		29.69		4.04		26.66		3.68		3.73		0		-28926.91		11:38:15		m

		S1148795131:		#B3q0		1148795131:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28927.97		11:38:45		m

		S1148795161:		#B3q0		1148795161:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28928.91		11:39:15		m

		S1148795191:		#B3q0		1148795191:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28929.97		11:39:45		m

		S1148795221:		#B3q0		1148795221:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28930.9		11:40:15		m

		S1148795251:		#B3q0		1148795251:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28931.96		11:40:45		m

		S1148795281:		#B3q0		1148795281:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28932.9		11:41:15		m

		S1148795311:		#B3q0		1148795311:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28933.96		11:41:45		m

		S1148795341:		#B3q0		1148795341:		$B3q0		d-		29.65		4.08		26.75		3.68		3.73		0		-28934.89		11:42:15		m

		S1148795371:		#B3q0		1148795371:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28935.96		11:42:45		m

		S1148795401:		#B3q0		1148795401:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28936.89		11:43:15		m

		S1148795431:		#B3q0		1148795431:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28937.96		11:43:45		m

		S1148795461:		#B3q0		1148795461:		$B3q0		d-		29.65		4		26.66		3.68		3.73		0		-28938.89		11:44:15		m

		S1148795491:		#B3q0		1148795491:		$B3q0		d-		29.62		4.04		26.66		3.68		3.73		0		-28939.95		11:44:45		m

		S1148795521:		#B3q0		1148795521:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28940.88		11:45:15		m

		S1148795551:		#B3q0		1148795551:		$B3q0		d-		29.65		4.04		26.66		3.68		3.73		0		-28941.95		11:45:45		m

		S1148795581:		#B3q0		1148795581:		$B3q0		d-		29.62		4.04		26.66		3.68		3.73		0		-28942.88		11:46:15		m

		S1148795611:		#B3q0		1148795611:		$B3q0		d-		29.62		4.04		26.66		3.68		3.73		0		-28943.94		11:46:45		m

		S1148795641:		#B3q0		1148795641:		$B3q0		d-		29.62		4.04		26.75		3.68		3.73		0		-28944.87		11:47:15		m

		S1148795671:		#B3q0		1148795671:		$B3q0		d-		29.62		4.04		26.75		3.68		3.73		0		-28945.93		11:47:45		m

		S1148795701:		#B3q0		1148795701:		$B3q0		d-		29.65		4		26.66		3.68		3.73		0		-28946.86		11:48:15		m

		S1148795731:		#B3q0		1148795731:		$B3q0		d-		29.62		4.04		26.75		3.68		3.73		0		-28947.92		11:48:45		m

		S1148795761:		#B3q0		1148795761:		$B3q0		d-		29.62		4		26.75		3.68		3.73		0		-28948.85		11:49:15		m

		S1148795791:		#B3q0		1148795791:		$B3q0		d-		29.65		4.04		26.75		3.68		3.73		0		-28949.92		11:49:45		m

		S1148795821:		#B3q0		1148795821:		$B3q0		d-		29.62		4.04		26.75		3.68		3.73		0		-28950.85		11:50:15		m

		S1148795851:		#B3q0		1148795851:		$B3q0		d-		29.62		4.04		26.66		3.68		3.73		0		-28951.91		11:50:45		m

		S1148795881:		#B3q0		1148795881:		$B3q0		d-		29.62		4.04		26.75		3.68		3.73		0		-28952.84		11:51:15		m

		S1148795911:		#B3q0		1148795911:		$B3q0		d-		29.62		4.04		26.66		3.68		3.73		0		-28953.9		11:51:45		m

		S1148795941:		#B3q0		1148795941:		$B3q0		d-		29.62		4		26.75		3.68		3.73		0		-28954.83		11:52:15		m

		S1148795971:		#B3q0		1148795971:		$B3q0		d-		29.62		4.08		26.66		3.68		3.73		0		-28955.9		11:52:45		m

		S1148796001:		#B3q0		1148796001:		$B3q0		d-		29.62		4.04		26.66		3.67		3.73		0		-28956.82		11:53:15		m

		S1148796031:		#B3q0		1148796031:		$B3q0		d-		29.62		4.04		26.75		3.67		3.73		0		-28957.89		11:53:45		m

		S1148796061:		#B3q0		1148796061:		$B3q0		d-		29.62		4.04		26.75		3.67		3.73		0		-28958.82		11:54:15		m

		S1148796091:		#B3q0		1148796091:		$B3q0		d-		29.62		4.04		26.75		3.67		3.73		0		-28959.88		11:54:45		m

		S1148796121:		#B3q0		1148796121:		$B3q0		d-		29.58		4.04		26.66		3.67		3.72		0		-28960.81		11:55:15		m

		S1148796151:		#B3q0		1148796151:		$B3q0		d-		29.62		4.04		26.75		3.67		3.72		0		-28961.87		11:55:45		m

		S1148796181:		#B3q0		1148796181:		$B3q0		d-		29.62		4.04		26.75		3.67		3.72		0		-28962.81		11:56:15		m

		S1148796211:		#B3q0		1148796211:		$B3q0		d-		29.58		4.04		26.66		3.67		3.72		0		-28963.87		11:56:45		m

		S1148796241:		#B3q0		1148796241:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28964.8		11:57:15		m

		S1148796271:		#B3q0		1148796271:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28965.86		11:57:45		m

		S1148796301:		#B3q0		1148796301:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28966.79		11:58:15		m

		S1148796331:		#B3q0		1148796331:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28967.85		11:58:45		m

		S1148796361:		#B3q0		1148796361:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28968.78		11:59:15		m

		S1148796391:		#B3q0		1148796391:		$B3q0		d-		29.62		4.04		26.75		3.67		3.72		0		-28969.85		11:59:45		m

		S1148796421:		#B3q0		1148796421:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28970.78		12:00:15		m

		S1148796451:		#B3q0		1148796451:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28971.84		12:00:45		m

		S1148796481:		#B3q0		1148796481:		$B3q0		d-		29.62		4.08		26.75		3.67		3.72		0		-28972.77		12:01:15		m

		S1148796511:		#B3q0		1148796511:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28973.83		12:01:45		m

		S1148796541:		#B3q0		1148796541:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28974.76		12:02:15		m

		S1148796571:		#B3q0		1148796571:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28975.82		12:02:45		m

		S1148796601:		#B3q0		1148796601:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28976.75		12:03:15		m

		S1148796631:		#B3q0		1148796631:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28977.81		12:03:45		m

		S1148796661:		#B3q0		1148796661:		$B3q0		d-		29.58		4.04		26.66		3.67		3.72		0		-28978.74		12:04:15		m

		S1148796691:		#B3q0		1148796691:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28979.8		12:04:45		m

		S1148796721:		#B3q0		1148796721:		$B3q0		d-		29.54		4		26.75		3.67		3.72		0		-28980.73		12:05:15		m

		S1148796751:		#B3q0		1148796751:		$B3q0		d-		29.58		4.04		26.85		3.67		3.72		0		-28981.79		12:05:45		m

		S1148796781:		#B3q0		1148796781:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28982.71		12:06:15		m

		S1148796811:		#B3q0		1148796811:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28983.77		12:06:45		m

		S1148796841:		#B3q0		1148796841:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28984.7		12:07:15		m

		S1148796871:		#B3q0		1148796871:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28985.76		12:07:45		m

		S1148796901:		#B3q0		1148796901:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28986.69		12:08:15		m

		S1148796931:		#B3q0		1148796931:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28987.75		12:08:45		m

		S1148796961:		#B3q0		1148796961:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28988.68		12:09:15		m

		S1148796991:		#B3q0		1148796991:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28989.74		12:09:45		m

		S1148797021:		#B3q0		1148797021:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28990.67		12:10:15		m

		S1148797051:		#B3q0		1148797051:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28991.73		12:10:45		m

		S1148797081:		#B3q0		1148797081:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28992.66		12:11:15		m

		S1148797111:		#B3q0		1148797111:		$B3q0		d-		29.58		4		26.75		3.67		3.72		0		-28993.72		12:11:45		m

		S1148797141:		#B3q0		1148797141:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28994.65		12:12:15		m

		S1148797171:		#B3q0		1148797171:		$B3q0		d-		29.58		4.04		26.75		3.67		3.72		0		-28995.71		12:12:45		m

		S1148797201:		#B3q0		1148797201:		$B3q0		d-		29.54		4		26.75		3.67		3.72		0		-28996.64		12:13:15		m

		S1148797231:		#B3q0		1148797231:		$B3q0		d-		29.54		4.04		26.75		3.67		3.72		0		-28997.7		12:13:45		m

		S1148797261:		#B3q0		1148797261:		$B3q0		d-		29.54		4		26.85		3.67		3.71		0		-28998.63		12:14:15		m

		S1148797291:		#B3q0		1148797291:		$B3q0		d-		29.54		4.04		26.75		3.67		3.71		0		-28999.69		12:14:45		m

		S1148797321:		#B3q0		1148797321:		$B3q0		d-		29.54		4.08		26.75		3.67		3.71		0		-29000.62		12:15:15		m

		S1148797351:		#B3q0		1148797351:		$B3q0		d-		29.54		4.04		26.75		3.67		3.71		0		-29001.68		12:15:45		m

		S1148797381:		#B3q0		1148797381:		$B3q0		d-		29.54		4.04		26.85		3.67		3.71		0		-29002.6		12:16:15		m

		S1148797411:		#B3q0		1148797411:		$B3q0		d-		29.54		4.04		26.75		3.67		3.71		0		-29003.66		12:16:45		m

		S1148797441:		#B3q0		1148797441:		$B3q0		d-		29.54		4		26.75		3.67		3.71		0		-29004.59		12:17:15		m

		S1148797471:		#B3q0		1148797471:		$B3q0		d-		29.5		4.04		26.85		3.66		3.71		0		-29005.65		12:17:45		m

		S1148797501:		#B3q0		1148797501:		$B3q0		d-		29.54		4.08		26.75		3.66		3.71		0		-29006.58		12:18:15		m

		S1148797531:		#B3q0		1148797531:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29007.64		12:18:45		m

		S1148797561:		#B3q0		1148797561:		$B3q0		d-		29.5		4		26.75		3.66		3.71		0		-29008.56		12:19:15		m

		S1148797591:		#B3q0		1148797591:		$B3q0		d-		29.54		4		26.75		3.66		3.71		0		-29009.62		12:19:45		m

		S1148797621:		#B3q0		1148797621:		$B3q0		d-		29.54		4		26.85		3.66		3.71		0		-29010.55		12:20:15		m

		S1148797651:		#B3q0		1148797651:		$B3q0		d-		29.54		4.04		26.75		3.66		3.71		0		-29011.61		12:20:45		m

		S1148797681:		#B3q0		1148797681:		$B3q0		d-		29.54		4.04		26.75		3.66		3.71		0		-29012.53		12:21:15		m

		S1148797711:		#B3q0		1148797711:		$B3q0		d-		29.54		4.04		26.75		3.66		3.71		0		-29013.59		12:21:45		m

		S1148797741:		#B3q0		1148797741:		$B3q0		d-		29.5		4		26.75		3.66		3.71		0		-29014.52		12:22:15		m

		S1148797771:		#B3q0		1148797771:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29015.58		12:22:45		m

		S1148797801:		#B3q0		1148797801:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29016.51		12:23:15		m

		S1148797831:		#B3q0		1148797831:		$B3q0		d-		29.5		4.04		26.85		3.66		3.71		0		-29017.57		12:23:45		m

		S1148797861:		#B3q0		1148797861:		$B3q0		d-		29.5		4		26.75		3.66		3.71		0		-29018.49		12:24:15		m

		S1148797891:		#B3q0		1148797891:		$B3q0		d-		29.5		4.04		26.85		3.66		3.71		0		-29019.55		12:24:45		m

		S1148797921:		#B3q0		1148797921:		$B3q0		d-		29.5		4.08		26.75		3.66		3.71		0		-29020.48		12:25:15		m

		S1148797951:		#B3q0		1148797951:		$B3q0		d-		29.5		4		26.85		3.66		3.71		0		-29021.54		12:25:45		m

		S1148797981:		#B3q0		1148797981:		$B3q0		d-		29.5		4.04		26.85		3.66		3.71		0		-29022.47		12:26:15		m

		S1148798011:		#B3q0		1148798011:		$B3q0		d-		29.46		4.08		26.85		3.66		3.71		0		-29023.53		12:26:45		m

		S1148798041:		#B3q0		1148798041:		$B3q0		d-		29.5		4.04		26.85		3.66		3.71		0		-29024.46		12:27:15		m

		S1148798071:		#B3q0		1148798071:		$B3q0		d-		29.5		4.08		26.85		3.66		3.71		0		-29025.51		12:27:45		m

		S1148798101:		#B3q0		1148798101:		$B3q0		d-		29.5		4		26.85		3.66		3.71		0		-29026.44		12:28:15		m

		S1148798131:		#B3q0		1148798131:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29027.5		12:28:45		m

		S1148798161:		#B3q0		1148798161:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29028.43		12:29:15		m

		S1148798191:		#B3q0		1148798191:		$B3q0		d-		29.46		4		26.85		3.66		3.71		0		-29029.48		12:29:45		m

		S1148798221:		#B3q0		1148798221:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29030.41		12:30:15		m

		S1148798251:		#B3q0		1148798251:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29031.47		12:30:45		m

		S1148798281:		#B3q0		1148798281:		$B3q0		d-		29.5		4		26.85		3.66		3.71		0		-29032.4		12:31:15		m

		S1148798311:		#B3q0		1148798311:		$B3q0		d-		29.5		4.04		26.75		3.66		3.71		0		-29033.46		12:31:45		m

		S1148798341:		#B3q0		1148798341:		$B3q0		d-		29.46		4		26.85		3.66		3.71		0		-29034.38		12:32:15		m

		S1148798371:		#B3q0		1148798371:		$B3q0		d-		29.46		4		26.75		3.66		3.71		0		-29035.44		12:32:45		m

		S1148798401:		#B3q0		1148798401:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29036.37		12:33:15		m

		S1148798431:		#B3q0		1148798431:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29037.43		12:33:45		m

		S1148798461:		#B3q0		1148798461:		$B3q0		d-		29.46		4.04		26.75		3.66		3.71		0		-29038.36		12:34:15		m

		S1148798491:		#B3q0		1148798491:		$B3q0		d-		29.46		4.08		26.85		3.66		3.71		0		-29039.42		12:34:45		m

		S1148798521:		#B3q0		1148798521:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29040.34		12:35:15		m

		S1148798551:		#B3q0		1148798551:		$B3q0		d-		29.46		4.08		26.85		3.66		3.71		0		-29041.4		12:35:45		m

		S1148798581:		#B3q0		1148798581:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29042.33		12:36:15		m

		S1148798611:		#B3q0		1148798611:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29043.38		12:36:45		m

		S1148798641:		#B3q0		1148798641:		$B3q0		d-		29.46		4.08		26.85		3.66		3.71		0		-29044.31		12:37:15		m

		S1148798671:		#B3q0		1148798671:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29045.36		12:37:45		m

		S1148798701:		#B3q0		1148798701:		$B3q0		d-		29.42		4.04		26.75		3.66		3.71		0		-29046.29		12:38:15		m

		S1148798731:		#B3q0		1148798731:		$B3q0		d-		29.42		4.04		26.85		3.66		3.71		0		-29047.34		12:38:45		m

		S1148798761:		#B3q0		1148798761:		$B3q0		d-		29.42		4.04		26.85		3.66		3.71		0		-29048.27		12:39:15		m

		S1148798791:		#B3q0		1148798791:		$B3q0		d-		29.46		4.04		26.85		3.66		3.71		0		-29049.33		12:39:45		m

		S1148798821:		#B3q0		1148798821:		$B3q0		d-		29.46		4.04		26.85		3.65		3.71		0		-29050.26		12:40:15		m

		S1148798851:		#B3q0		1148798851:		$B3q0		d-		29.42		4		26.85		3.65		3.71		0		-29051.31		12:40:45		m

		S1148798881:		#B3q0		1148798881:		$B3q0		d-		29.42		4.04		26.85		3.65		3.71		0		-29052.24		12:41:15		m

		S1148798911:		#B3q0		1148798911:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29053.29		12:41:45		m

		S1148798941:		#B3q0		1148798941:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29054.22		12:42:15		m

		S1148798971:		#B3q0		1148798971:		$B3q0		d-		29.42		4		26.85		3.65		3.7		0		-29055.27		12:42:45		m

		S1148799001:		#B3q0		1148799001:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29056.19		12:43:15		m

		S1148799031:		#B3q0		1148799031:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29057.25		12:43:45		m

		S1148799061:		#B3q0		1148799061:		$B3q0		d-		29.42		4		26.85		3.65		3.7		0		-29058.17		12:44:15		m

		S1148799091:		#B3q0		1148799091:		$B3q0		d-		29.42		4		26.85		3.65		3.7		0		-29059.23		12:44:45		m

		S1148799121:		#B3q0		1148799121:		$B3q0		d-		29.42		4		26.85		3.65		3.7		0		-29060.16		12:45:15		m

		S1148799151:		#B3q0		1148799151:		$B3q0		d-		29.42		4		26.85		3.65		3.7		0		-29061.21		12:45:45		m

		S1148799181:		#B3q0		1148799181:		$B3q0		d-		29.42		4.08		26.85		3.65		3.7		0		-29062.14		12:46:15		m

		S1148799211:		#B3q0		1148799211:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29063.19		12:46:45		m

		S1148799241:		#B3q0		1148799241:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29064.12		12:47:15		m

		S1148799271:		#B3q0		1148799271:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29065.17		12:47:45		m

		S1148799301:		#B3q0		1148799301:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29066.1		12:48:15		m

		S1148799331:		#B3q0		1148799331:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29067.15		12:48:45		m

		S1148799361:		#B3q0		1148799361:		$B3q0		d-		29.39		4.08		26.85		3.65		3.7		0		-29068.08		12:49:15		m

		S1148799391:		#B3q0		1148799391:		$B3q0		d-		29.39		4.04		26.95		3.65		3.7		0		-29069.13		12:49:45		m

		S1148799421:		#B3q0		1148799421:		$B3q0		d-		29.42		4.04		26.85		3.65		3.7		0		-29070.05		12:50:15		m

		S1148799451:		#B3q0		1148799451:		$B3q0		d-		29.39		4		26.95		3.65		3.7		0		-29071.11		12:50:45		m

		S1148799481:		#B3q0		1148799481:		$B3q0		d-		29.39		4		26.85		3.64		3.7		0		-29072.03		12:51:15		m

		S1148799511:		#B3q0		1148799511:		$B3q0		d-		29.42		4		26.85		3.64		3.7		0		-29073.09		12:51:45		m

		S1148799541:		#B3q0		1148799541:		$B3q0		d-		29.39		4.04		26.95		3.64		3.7		0		-29074.02		12:52:15		m

		S1148799571:		#B3q0		1148799571:		$B3q0		d-		29.39		4.04		26.95		3.64		3.7		0		-29075.07		12:52:45		m

		S1148799601:		#B3q0		1148799601:		$B3q0		d-		29.42		4.04		26.95		3.64		3.7		0		-29075.99		12:53:15		m

		S1148799631:		#B3q0		1148799631:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29077.05		12:53:45		m

		S1148799661:		#B3q0		1148799661:		$B3q0		d-		29.39		4		26.85		3.64		3.7		0		-29077.97		12:54:15		m

		S1148799691:		#B3q0		1148799691:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29079.03		12:54:45		m

		S1148799721:		#B3q0		1148799721:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29079.95		12:55:15		m

		S1148799751:		#B3q0		1148799751:		$B3q0		d-		29.39		4		26.85		3.64		3.7		0		-29081.01		12:55:45		m

		S1148799781:		#B3q0		1148799781:		$B3q0		d-		29.39		4.08		26.85		3.64		3.7		0		-29081.93		12:56:15		m

		S1148799811:		#B3q0		1148799811:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29082.98		12:56:45		m

		S1148799841:		#B3q0		1148799841:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29083.9		12:57:15		m

		S1148799871:		#B3q0		1148799871:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29084.96		12:57:45		m

		S1148799901:		#B3q0		1148799901:		$B3q0		d-		29.35		4.04		26.95		3.64		3.7		0		-29085.88		12:58:15		m

		S1148799931:		#B3q0		1148799931:		$B3q0		d-		29.35		4		26.85		3.64		3.7		0		-29086.94		12:58:45		m

		S1148799961:		#B3q0		1148799961:		$B3q0		d-		29.39		4.04		26.95		3.64		3.7		0		-29087.87		12:59:15		m

		S1148799991:		#B3q0		1148799991:		$B3q0		d-		29.35		4.04		26.95		3.64		3.7		0		-29088.92		12:59:45		m

		S1148800021:		#B3q0		1148800021:		$B3q0		d-		29.39		4.08		26.95		3.64		3.7		0		-29089.84		13:00:15		m

		S1148800051:		#B3q0		1148800051:		$B3q0		d-		29.39		4.04		26.95		3.64		3.7		0		-29090.9		13:00:45		m

		S1148800081:		#B3q0		1148800081:		$B3q0		d-		29.35		4.04		26.85		3.64		3.7		0		-29091.82		13:01:15		m

		S1148800111:		#B3q0		1148800111:		$B3q0		d-		29.39		4.04		26.85		3.64		3.7		0		-29092.88		13:01:45		m

		S1148800141:		#B3q0		1148800141:		$B3q0		d-		29.35		4		26.95		3.64		3.7		0		-29093.8		13:02:15		m

		S1148800171:		#B3q0		1148800171:		$B3q0		d-		29.35		4.04		26.85		3.64		3.7		0		-29094.85		13:02:45		m

		S1148800201:		#B3q0		1148800201:		$B3q0		d-		29.35		4		26.85		3.64		3.7		0		-29095.77		13:03:15		m

		S1148800231:		#B3q0		1148800231:		$B3q0		d-		29.35		4.04		26.85		3.64		3.7		0		-29096.83		13:03:45		m

		S1148800261:		#B3q0		1148800261:		$B3q0		d-		29.35		4		26.95		3.64		3.69		0		-29097.75		13:04:15		m

		S1148800291:		#B3q0		1148800291:		$B3q0		d-		29.35		4		26.85		3.64		3.69		0		-29098.8		13:04:45		m

		S1148800321:		#B3q0		1148800321:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29099.72		13:05:15		m

		S1148800351:		#B3q0		1148800351:		$B3q0		d-		29.35		4		26.95		3.64		3.69		0		-29100.77		13:05:45		m

		S1148800381:		#B3q0		1148800381:		$B3q0		d-		29.35		4.04		26.85		3.64		3.69		0		-29101.69		13:06:15		m

		S1148800411:		#B3q0		1148800411:		$B3q0		d-		29.35		4		26.95		3.64		3.69		0		-29102.75		13:06:45		m

		S1148800441:		#B3q0		1148800441:		$B3q0		d-		29.35		4.04		26.85		3.64		3.69		0		-29103.67		13:07:15		m

		S1148800471:		#B3q0		1148800471:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29104.72		13:07:45		m

		S1148800501:		#B3q0		1148800501:		$B3q0		d-		29.35		4		26.95		3.64		3.69		0		-29105.64		13:08:15		m

		S1148800531:		#B3q0		1148800531:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29106.7		13:08:45		m

		S1148800561:		#B3q0		1148800561:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29107.62		13:09:15		m

		S1148800591:		#B3q0		1148800591:		$B3q0		d-		29.35		4.08		26.95		3.64		3.69		0		-29108.67		13:09:45		m

		S1148800621:		#B3q0		1148800621:		$B3q0		d-		29.31		4		26.85		3.64		3.69		0		-29109.59		13:10:15		m

		S1148800651:		#B3q0		1148800651:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29110.64		13:10:45		m

		S1148800681:		#B3q0		1148800681:		$B3q0		d-		29.31		4.04		26.85		3.64		3.69		0		-29111.56		13:11:15		m

		S1148800711:		#B3q0		1148800711:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29112.61		13:11:45		m

		S1148800741:		#B3q0		1148800741:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29113.53		13:12:15		m

		S1148800771:		#B3q0		1148800771:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29114.59		13:12:45		m

		S1148800801:		#B3q0		1148800801:		$B3q0		d-		29.31		4.08		26.95		3.64		3.69		0		-29115.5		13:13:15		m

		S1148800831:		#B3q0		1148800831:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29116.56		13:13:45		m

		S1148800861:		#B3q0		1148800861:		$B3q0		d-		29.35		4		26.95		3.64		3.69		0		-29117.48		13:14:15		m

		S1148800891:		#B3q0		1148800891:		$B3q0		d-		29.31		4		26.95		3.64		3.69		0		-29118.53		13:14:45		m

		S1148800921:		#B3q0		1148800921:		$B3q0		d-		29.35		4		26.85		3.64		3.69		0		-29119.46		13:15:15		m

		S1148800951:		#B3q0		1148800951:		$B3q0		d-		29.31		4		26.95		3.64		3.69		0		-29120.51		13:15:45		m

		S1148800981:		#B3q0		1148800981:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29121.43		13:16:15		m

		S1148801011:		#B3q0		1148801011:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29122.48		13:16:45		m

		S1148801041:		#B3q0		1148801041:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29123.41		13:17:15		m

		S1148801071:		#B3q0		1148801071:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29124.46		13:17:45		m

		S1148801101:		#B3q0		1148801101:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29125.38		13:18:15		m

		S1148801131:		#B3q0		1148801131:		$B3q0		d-		29.35		4.04		26.95		3.64		3.69		0		-29126.43		13:18:45		m

		S1148801161:		#B3q0		1148801161:		$B3q0		d-		29.31		4		26.95		3.64		3.69		0		-29127.35		13:19:15		m

		S1148801191:		#B3q0		1148801191:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29128.4		13:19:45		m

		S1148801221:		#B3q0		1148801221:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29129.32		13:20:15		m

		S1148801251:		#B3q0		1148801251:		$B3q0		d-		29.31		4		26.95		3.64		3.69		0		-29130.37		13:20:45		m

		S1148801281:		#B3q0		1148801281:		$B3q0		d-		29.27		4.04		26.95		3.64		3.69		0		-29131.29		13:21:15		m

		S1148801311:		#B3q0		1148801311:		$B3q0		d-		29.31		4.04		26.95		3.64		3.69		0		-29132.35		13:21:45		m

		S1148801341:		#B3q0		1148801341:		$B3q0		d-		29.31		4.04		26.85		3.63		3.69		0		-29133.26		13:22:15		m

		S1148801371:		#B3q0		1148801371:		$B3q0		d-		29.31		4.04		26.95		3.63		3.69		0		-29134.31		13:22:45		m

		S1148801401:		#B3q0		1148801401:		$B3q0		d-		29.31		4.08		26.95		3.63		3.69		0		-29135.23		13:23:15		m

		S1148801431:		#B3q0		1148801431:		$B3q0		d-		29.31		4		27.05		3.63		3.69		0		-29136.28		13:23:45		m

		S1148801461:		#B3q0		1148801461:		$B3q0		d-		29.27		4		26.95		3.63		3.69		0		-29137.2		13:24:15		m

		S1148801491:		#B3q0		1148801491:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29138.25		13:24:45		m

		S1148801521:		#B3q0		1148801521:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29139.18		13:25:15		m

		S1148801551:		#B3q0		1148801551:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29140.23		13:25:45		m

		S1148801581:		#B3q0		1148801581:		$B3q0		d-		29.31		4		26.95		3.63		3.69		0		-29141.15		13:26:15		m

		S1148801611:		#B3q0		1148801611:		$B3q0		d-		29.31		4.04		26.95		3.63		3.69		0		-29142.2		13:26:45		m

		S1148801641:		#B3q0		1148801641:		$B3q0		d-		29.31		4.04		26.95		3.63		3.69		0		-29143.12		13:27:15		m

		S1148801671:		#B3q0		1148801671:		$B3q0		d-		29.27		4		27.05		3.63		3.69		0		-29144.17		13:27:45		m

		S1148801701:		#B3q0		1148801701:		$B3q0		d-		29.31		4.04		26.95		3.63		3.69		0		-29145.09		13:28:15		m

		S1148801731:		#B3q0		1148801731:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29146.14		13:28:45		m

		S1148801761:		#B3q0		1148801761:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29147.06		13:29:15		m

		S1148801791:		#B3q0		1148801791:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29148.11		13:29:45		m

		S1148801821:		#B3q0		1148801821:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29149.03		13:30:15		m

		S1148801851:		#B3q0		1148801851:		$B3q0		d-		29.31		4		26.95		3.63		3.69		0		-29150.08		13:30:45		m

		S1148801881:		#B3q0		1148801881:		$B3q0		d-		29.27		4.08		27.05		3.63		3.69		0		-29151		13:31:15		m

		S1148801911:		#B3q0		1148801911:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29152.05		13:31:45		m

		S1148801941:		#B3q0		1148801941:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29152.97		13:32:15		m

		S1148801971:		#B3q0		1148801971:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29154.02		13:32:45		m

		S1148802001:		#B3q0		1148802001:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29154.94		13:33:15		m

		S1148802031:		#B3q0		1148802031:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29155.99		13:33:45		m

		S1148802061:		#B3q0		1148802061:		$B3q0		d-		29.27		4.04		26.95		3.63		3.69		0		-29156.91		13:34:15		m

		S1148802091:		#B3q0		1148802091:		$B3q0		d-		29.24		4		27.05		3.63		3.69		0		-29157.96		13:34:45		m

		S1148802121:		#B3q0		1148802121:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29158.88		13:35:15		m

		S1148802151:		#B3q0		1148802151:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29159.93		13:35:45		m

		S1148802181:		#B3q0		1148802181:		$B3q0		d-		29.27		4.08		26.95		3.63		3.69		0		-29160.85		13:36:15		m

		S1148802211:		#B3q0		1148802211:		$B3q0		d-		29.24		4		26.95		3.63		3.69		0		-29161.9		13:36:45		m

		S1148802241:		#B3q0		1148802241:		$B3q0		d-		29.27		4.04		27.05		3.63		3.69		0		-29162.81		13:37:15		m

		S1148802271:		#B3q0		1148802271:		$B3q0		d-		29.24		4.08		26.95		3.63		3.69		0		-29163.86		13:37:45		m

		S1148802301:		#B3q0		1148802301:		$B3q0		d-		29.27		4.04		27.05		3.63		3.68		0		-29164.78		13:38:15		m

		S1148802331:		#B3q0		1148802331:		$B3q0		d-		29.24		4		27.05		3.63		3.68		0		-29165.83		13:38:45		m

		S1148802361:		#B3q0		1148802361:		$B3q0		d-		29.27		4.04		27.05		3.62		3.68		0		-29166.75		13:39:15		m

		S1148802391:		#B3q0		1148802391:		$B3q0		d-		29.27		4.04		26.95		3.62		3.68		0		-29167.8		13:39:45		m

		S1148802421:		#B3q0		1148802421:		$B3q0		d-		29.24		4.04		27.05		3.62		3.68		0		-29168.72		13:40:15		m

		S1148802451:		#B3q0		1148802451:		$B3q0		d-		29.24		4.08		26.95		3.62		3.68		0		-29169.77		13:40:45		m

		S1148802481:		#B3q0		1148802481:		$B3q0		d-		29.24		4.04		26.95		3.62		3.68		0		-29170.69		13:41:15		m

		S1148802511:		#B3q0		1148802511:		$B3q0		d-		29.24		4.04		27.05		3.62		3.68		0		-29171.74		13:41:45		m

		S1148802541:		#B3q0		1148802541:		$B3q0		d-		29.24		4		27.05		3.62		3.68		0		-29172.66		13:42:15		m

		S1148802571:		#B3q0		1148802571:		$B3q0		d-		29.24		4.04		27.05		3.62		3.68		0		-29173.7		13:42:45		m

		S1148802601:		#B3q0		1148802601:		$B3q0		d-		29.24		4.04		27.05		3.62		3.68		0		-29174.62		13:43:15		m

		S1148802631:		#B3q0		1148802631:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29175.67		13:43:45		m

		S1148802661:		#B3q0		1148802661:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29176.59		13:44:15		m

		S1148802691:		#B3q0		1148802691:		$B3q0		d-		29.2		4.04		26.95		3.62		3.68		0		-29177.64		13:44:45		m

		S1148802721:		#B3q0		1148802721:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29178.56		13:45:15		m

		S1148802751:		#B3q0		1148802751:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29179.61		13:45:45		m

		S1148802781:		#B3q0		1148802781:		$B3q0		d-		29.2		4		26.95		3.62		3.68		0		-29180.53		13:46:15		m

		S1148802811:		#B3q0		1148802811:		$B3q0		d-		29.2		4.08		27.05		3.62		3.68		0		-29181.57		13:46:45		m

		S1148802841:		#B3q0		1148802841:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29182.49		13:47:15		m

		S1148802871:		#B3q0		1148802871:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29183.54		13:47:45		m

		S1148802901:		#B3q0		1148802901:		$B3q0		d-		29.2		4.04		27.05		3.62		3.68		0		-29184.45		13:48:15		m

		S1148802931:		#B3q0		1148802931:		$B3q0		d-		29.2		4		26.95		3.62		3.68		0		-29185.5		13:48:45		m

		S1148802961:		#B3q0		1148802961:		$B3q0		d-		29.2		4.04		27.05		3.61		3.68		0		-29186.41		13:49:15		m

		S1148802991:		#B3q0		1148802991:		$B3q0		d-		29.2		4		27.05		3.61		3.68		0		-29187.46		13:49:45		m

		S1148803021:		#B3q0		1148803021:		$B3q0		d-		29.2		4.04		27.05		3.61		3.68		0		-29188.38		13:50:15		m

		S1148803051:		#B3q0		1148803051:		$B3q0		d-		29.2		4		26.95		3.61		3.68		0		-29189.43		13:50:45		m

		S1148803081:		#B3q0		1148803081:		$B3q0		d-		29.16		4.04		27.05		3.61		3.68		0		-29190.35		13:51:15		m

		S1148803111:		#B3q0		1148803111:		$B3q0		d-		29.16		4.08		27.05		3.61		3.68		0		-29191.4		13:51:45		m

		S1148803141:		#B3q0		1148803141:		$B3q0		d-		29.16		4.04		27.05		3.61		3.68		0		-29192.32		13:52:15		m

		S1148803171:		#B3q0		1148803171:		$B3q0		d-		29.2		4.04		27.05		3.61		3.68		0		-29193.36		13:52:45		m

		S1148803201:		#B3q0		1148803201:		$B3q0		d-		29.16		4.04		27.05		3.6		3.68		0		-29194.28		13:53:15		m

		S1148803231:		#B3q0		1148803231:		$B3q0		d-		29.16		4.08		27.05		3.6		3.68		0		-29195.33		13:53:45		m

		S1148803261:		#B3q0		1148803261:		$B3q0		d-		29.16		4		27.05		3.6		3.68		0		-29196.24		13:54:15		m

		S1148803291:		#B3q0		1148803291:		$B3q0		d-		29.16		4.04		27.05		3.6		3.68		0		-29197.29		13:54:45		m

		S1148803321:		#B3q0		1148803321:		$B3q0		d-		29.16		4.04		27.05		3.6		3.68		0		-29198.21		13:55:15		m

		S1148803351:		#B3q0		1148803351:		$B3q0		d-		29.12		4.04		27.05		3.6		3.68		0		-29199.25		13:55:45		m

		S1148803381:		#B3q0		1148803381:		$B3q0		d-		29.16		4.04		27.05		3.6		3.68		0		-29200.17		13:56:15		m

		S1148803411:		#B3q0		1148803411:		$B3q0		d-		29.12		4		26.95		3.6		3.68		0		-29201.21		13:56:45		m

		S1148803441:		#B3q0		1148803441:		$B3q0		d-		29.12		4		27.05		3.59		3.68		0		-29202.13		13:57:15		m

		S1148803471:		#B3q0		1148803471:		$B3q0		d-		29.12		4.04		27.05		3.59		3.68		0		-29203.18		13:57:45		m

		S1148803501:		#B3q0		1148803501:		$B3q0		d-		29.12		4.04		27.05		3.59		3.68		0		-29204.09		13:58:15		m

		S1148803531:		#B3q0		1148803531:		$B3q0		d-		29.08		4.04		27.05		3.59		3.68		0		-29205.14		13:58:45		m

		S1148803561:		#B3q0		1148803561:		$B3q0		d-		29.12		4.04		27.05		3.59		3.67		0		-29206.05		13:59:15		m

		S1148803591:		#B3q0		1148803591:		$B3q0		d-		29.08		4.04		27.14		3.58		3.67		0		-29207.1		13:59:45		m

		S1148803621:		#B3q0		1148803621:		$B3q0		d-		29.12		4		27.05		3.58		3.67		0		-29208.01		14:00:15		m

		S1148803651:		#B3q0		1148803651:		$B3q0		d-		29.12		4.08		27.14		3.58		3.67		0		-29209.06		14:00:45		m

		S1148803681:		#B3q0		1148803681:		$B3q0		d-		29.12		4.04		27.05		3.58		3.67		0		-29209.97		14:01:15		m

		S1148803711:		#B3q0		1148803711:		$B3q0		d-		29.12		4.04		27.05		3.58		3.67		0		-29211.02		14:01:45		m

		S1148803741:		#B3q0		1148803741:		$B3q0		d-		29.08		4.04		27.14		3.58		3.67		0		-29211.93		14:02:15		m

		S1148803771:		#B3q0		1148803771:		$B3q0		d-		29.08		4.04		27.05		3.58		3.67		0		-29212.98		14:02:45		m

		S1148803801:		#B3q0		1148803801:		$B3q0		d-		29.08		4.04		27.05		3.57		3.67		0		-29213.89		14:03:15		m

		S1148803831:		#B3q0		1148803831:		$B3q0		d-		29.08		4.04		27.05		3.57		3.67		0		-29214.93		14:03:45		m

		S1148803861:		#B3q0		1148803861:		$B3q0		d-		29.05		4		27.14		3.57		3.67		0		-29215.85		14:04:15		m

		S1148803891:		#B3q0		1148803891:		$B3q0		d-		29.05		4.04		27.05		3.57		3.67		0		-29216.89		14:04:45		m

		S1148803921:		#B3q0		1148803921:		$B3q0		d-		29.05		4.04		27.14		3.57		3.67		0		-29217.81		14:05:15		m

		S1148803951:		#B3q0		1148803951:		$B3q0		d-		29.05		4.08		27.05		3.57		3.67		0		-29218.85		14:05:45		m

		S1148803981:		#B3q0		1148803981:		$B3q0		d-		29.05		4.08		27.14		3.56		3.67		0		-29219.76		14:06:15		m

		S1148804011:		#B3q0		1148804011:		$B3q0		d-		29.05		4		27.05		3.56		3.67		0		-29220.81		14:06:45		m

		S1148804041:		#B3q0		1148804041:		$B3q0		d-		29.05		4.04		27.14		3.56		3.67		0		-29221.72		14:07:15		m

		S1148804071:		#B3q0		1148804071:		$B3q0		d-		29.01		4.04		27.14		3.56		3.67		0		-29222.76		14:07:45		m

		S1148804101:		#B3q0		1148804101:		$B3q0		d-		29.01		4.04		27.05		3.55		3.67		0		-29223.67		14:08:15		m

		S1148804131:		#B3q0		1148804131:		$B3q0		d-		29.01		4.04		27.14		3.55		3.67		0		-29224.71		14:08:45		m

		S1148804161:		#B3q0		1148804161:		$B3q0		d-		29.01		4.04		27.05		3.55		3.67		0		-29225.63		14:09:15		m

		S1148804191:		#B3q0		1148804191:		$B3q0		d-		28.97		4.04		27.05		3.55		3.67		0		-29226.67		14:09:45		m

		S1148804221:		#B3q0		1148804221:		$B3q0		d-		29.01		4		27.05		3.55		3.67		0		-29227.58		14:10:15		m

		S1148804251:		#B3q0		1148804251:		$B3q0		d-		28.97		4.04		27.05		3.55		3.67		0		-29228.62		14:10:45		m

		S1148804281:		#B3q0		1148804281:		$B3q0		d-		28.97		4.04		27.05		3.54		3.67		0		-29229.53		14:11:15		m

		S1148804311:		#B3q0		1148804311:		$B3q0		d-		28.97		4.04		27.05		3.54		3.67		0		-29230.57		14:11:45		m

		S1148804341:		#B3q0		1148804341:		$B3q0		d-		28.97		4.04		27.05		3.54		3.67		0		-29231.48		14:12:15		m

		S1148804371:		#B3q0		1148804371:		$B3q0		d-		28.93		4.04		27.14		3.54		3.67		0		-29232.52		14:12:45		m

		S1148804401:		#B3q0		1148804401:		$B3q0		d-		28.93		4		27.05		3.53		3.67		0		-29233.43		14:13:15		m

		S1148804431:		#B3q0		1148804431:		$B3q0		d-		28.93		4		27.14		3.53		3.67		0		-29234.46		14:13:45		m

		S1148804461:		#B3q0		1148804461:		$B3q0		d-		28.93		4.04		27.14		3.53		3.67		0		-29235.37		14:14:15		m

		S1148804491:		#B3q0		1148804491:		$B3q0		d-		28.93		4.04		27.14		3.53		3.67		0		-29236.41		14:14:45		m

		S1148804521:		#B3q0		1148804521:		$B3q0		d-		28.93		4.04		27.14		3.53		3.67		0		-29237.32		14:15:15		m

		S1148804551:		#B3q0		1148804551:		$B3q0		d-		28.89		4.04		27.14		3.53		3.67		0		-29238.36		14:15:45		m

		S1148804581:		#B3q0		1148804581:		$B3q0		d-		28.89		4.04		27.05		3.52		3.67		0		-29239.27		14:16:15		m

		S1148804611:		#B3q0		1148804611:		$B3q0		d-		28.89		4		27.05		3.52		3.67		0		-29240.31		14:16:45		m

		S1148804641:		#B3q0		1148804641:		$B3q0		d-		28.89		4.08		27.14		3.52		3.67		0		-29241.22		14:17:15		m

		S1148804671:		#B3q0		1148804671:		$B3q0		d-		28.85		4.04		27.14		3.51		3.67		0		-29242.26		14:17:45		m

		S1148804701:		#B3q0		1148804701:		$B3q0		d-		28.85		4.04		27.14		3.51		3.67		0		-29243.16		14:18:15		m

		S1148804731:		#B3q0		1148804731:		$B3q0		d-		28.85		4.04		27.14		3.51		3.67		0		-29244.2		14:18:45		m

		S1148804761:		#B3q0		1148804761:		$B3q0		d-		28.85		4.04		27.14		3.51		3.67		0		-29245.11		14:19:15		m

		S1148804791:		#B3q0		1148804791:		$B3q0		d-		28.82		4.04		27.05		3.51		3.67		0		-29246.14		14:19:45		m

		S1148804821:		#B3q0		1148804821:		$B3q0		d-		28.85		4		27.05		3.5		3.67		0		-29247.05		14:20:15		m

		S1148804851:		#B3q0		1148804851:		$B3q0		d-		28.82		4		27.14		3.5		3.67		0		-29248.08		14:20:45		m

		S1148804881:		#B3q0		1148804881:		$B3q0		d-		28.82		4.04		27.14		3.5		3.67		0		-29248.98		14:21:15		m

		S1148804911:		#B3q0		1148804911:		$B3q0		d-		28.82		4.04		27.14		3.5		3.67		0		-29250.02		14:21:45		m

		S1148804941:		#B3q0		1148804941:		$B3q0		d-		28.82		4.04		27.14		3.5		3.67		0		-29250.92		14:22:15		m

		S1148804971:		#B3q0		1148804971:		$B3q0		d-		28.78		4.04		27.14		3.49		3.67		0		-29251.96		14:22:45		m

		S1148805001:		#B3q0		1148805001:		$B3q0		d-		28.78		4.04		27.14		3.49		3.67		0		-29252.86		14:23:15		m

		S1148805031:		#B3q0		1148805031:		$B3q0		d-		28.78		4.04		27.14		3.49		3.67		0		-29253.9		14:23:45		m

		S1148805061:		#B3q0		1148805061:		$B3q0		d-		28.78		4.04		27.14		3.48		3.67		0		-29254.8		14:24:15		m

		S1148805091:		#B3q0		1148805091:		$B3q0		d-		28.74		4.04		27.14		3.48		3.67		0		-29255.83		14:24:45		m

		S1148805121:		#B3q0		1148805121:		$B3q0		d-		28.74		4.04		27.14		3.48		3.67		0		-29256.73		14:25:15		m

		S1148805151:		#B3q0		1148805151:		$B3q0		d-		28.74		4.04		27.14		3.48		3.67		0		-29257.76		14:25:45		m

		S1148805181:		#B3q0		1148805181:		$B3q0		d-		28.74		4.04		27.14		3.47		3.67		0		-29258.67		14:26:15		m

		S1148805211:		#B3q0		1148805211:		$B3q0		d-		28.71		4		27.14		3.47		3.67		0		-29259.7		14:26:45		m

		S1148805241:		#B3q0		1148805241:		$B3q0		d-		28.67		4.04		27.14		3.47		3.66		0		-29260.6		14:27:15		m

		S1148805271:		#B3q0		1148805271:		$B3q0		d-		28.67		4.04		27.14		3.46		3.66		0		-29261.63		14:27:45		m

		S1148805301:		#B3q0		1148805301:		$B3q0		d-		28.67		4.04		27.14		3.46		3.66		0		-29262.53		14:28:15		m

		S1148805331:		#B3q0		1148805331:		$B3q0		d-		28.67		4.04		27.14		3.46		3.66		0		-29263.56		14:28:45		m

		S1148805361:		#B3q0		1148805361:		$B3q0		d-		28.67		4.04		27.14		3.46		3.66		0		-29264.46		14:29:15		m

		S1148805391:		#B3q0		1148805391:		$B3q0		d-		28.67		4.04		27.14		3.45		3.66		0		-29265.49		14:29:45		m

		S1148805421:		#B3q0		1148805421:		$B3q0		d-		28.63		4.04		27.14		3.45		3.66		0		-29266.39		14:30:15		m

		S1148805451:		#B3q0		1148805451:		$B3q0		d-		28.63		4.04		27.14		3.45		3.66		0		-29267.42		14:30:45		m

		S1148805481:		#B3q0		1148805481:		$B3q0		d-		28.63		4.08		27.14		3.44		3.66		0		-29268.32		14:31:15		m

		S1148805511:		#B3q0		1148805511:		$B3q0		d-		28.59		4.04		27.24		3.44		3.66		0		-29269.35		14:31:45		m

		S1148805541:		#B3q0		1148805541:		$B3q0		d-		28.59		4.04		27.14		3.44		3.66		0		-29270.24		14:32:15		m

		S1148805571:		#B3q0		1148805571:		$B3q0		d-		28.59		4		27.14		3.44		3.66		0		-29271.27		14:32:45		m

		S1148805601:		#B3q0		1148805601:		$B3q0		d-		28.59		4.04		27.14		3.43		3.66		0		-29272.17		14:33:15		m

		S1148805631:		#B3q0		1148805631:		$B3q0		d-		28.55		4.04		27.14		3.43		3.66		0		-29273.19		14:33:45		m

		S1148805661:		#B3q0		1148805661:		$B3q0		d-		28.55		4.04		27.14		3.42		3.66		0		-29274.09		14:34:15		m

		S1148805691:		#B3q0		1148805691:		$B3q0		d-		28.55		4.04		27.14		3.42		3.66		0		-29275.12		14:34:45		m

		S1148805721:		#B3q0		1148805721:		$B3q0		d-		28.51		4.04		27.24		3.42		3.66		0		-29276.01		14:35:15		m

		S1148805751:		#B3q0		1148805751:		$B3q0		d-		28.51		4.08		27.14		3.41		3.66		0		-29277.04		14:35:45		m

		S1148805781:		#B3q0		1148805781:		$B3q0		d-		28.51		4.04		27.14		3.41		3.66		0		-29277.94		14:36:15		m

		S1148805811:		#B3q0		1148805811:		$B3q0		d-		28.48		4.04		27.14		3.41		3.66		0		-29278.96		14:36:45		m

		S1148805841:		#B3q0		1148805841:		$B3q0		d-		28.48		4		27.14		3.4		3.66		0		-29279.86		14:37:15		m

		S1148805871:		#B3q0		1148805871:		$B3q0		d-		28.48		4.04		27.14		3.4		3.66		0		-29280.88		14:37:45		m

		S1148805901:		#B3q0		1148805901:		$B3q0		d-		28.48		4.04		27.14		3.39		3.66		0		-29281.77		14:38:15		m

		S1148805931:		#B3q0		1148805931:		$B3q0		d-		28.44		4.04		27.14		3.39		3.66		0		-29282.79		14:38:45		m

		S1148805961:		#B3q0		1148805961:		$B3q0		d-		28.44		4.04		27.14		3.39		3.66		0		-29283.68		14:39:15		m

		S1148805991:		#B3q0		1148805991:		$B3q0		d-		28.44		4.04		27.14		3.38		3.66		0		-29284.7		14:39:45		m

		S1148806021:		#B3q0		1148806021:		$B3q0		d-		28.4		4		27.14		3.38		3.66		0		-29285.59		14:40:15		m

		S1148806051:		#B3q0		1148806051:		$B3q0		d-		28.4		4		27.24		3.37		3.66		0		-29286.61		14:40:45		m

		S1148806081:		#B3q0		1148806081:		$B3q0		d-		28.4		4.08		27.14		3.37		3.66		0		-29287.51		14:41:15		m

		S1148806111:		#B3q0		1148806111:		$B3q0		d-		28.4		4.04		27.24		3.37		3.66		0		-29288.53		14:41:45		m

		S1148806141:		#B3q0		1148806141:		$B3q0		d-		28.36		4.04		27.24		3.36		3.66		0		-29289.42		14:42:15		m

		S1148806171:		#B3q0		1148806171:		$B3q0		d-		28.36		4.04		27.24		3.35		3.66		0		-29290.44		14:42:45		m

		S1148806201:		#B3q0		1148806201:		$B3q0		d-		28.33		4.08		27.24		3.35		3.66		0		-29291.33		14:43:15		m

		S1148806231:		#B3q0		1148806231:		$B3q0		d-		28.33		4.08		27.14		3.35		3.66		0		-29292.35		14:43:45		m

		S1148806261:		#B3q0		1148806261:		$B3q0		d-		28.29		4.04		27.24		3.34		3.66		0		-29293.24		14:44:15		m

		S1148806291:		#B3q0		1148806291:		$B3q0		d-		28.29		4.04		27.24		3.33		3.66		0		-29294.25		14:44:45		m

		S1148806321:		#B3q0		1148806321:		$B3q0		d-		28.29		4		27.24		3.33		3.66		0		-29295.14		14:45:15		m

		S1148806351:		#B3q0		1148806351:		$B3q0		d-		28.29		4		27.24		3.32		3.66		0		-29296.16		14:45:45		m

		S1148806381:		#B3q0		1148806381:		$B3q0		d-		28.25		4		27.14		3.32		3.66		0		-29297.05		14:46:15		m

		S1148806411:		#B3q0		1148806411:		$B3q0		d-		28.25		4.04		27.14		3.32		3.66		0		-29298.06		14:46:45		m

		S1148806441:		#B3q0		1148806441:		$B3q0		d-		28.21		4		27.24		3.31		3.66		0		-29298.95		14:47:15		m

		S1148806471:		#B3q0		1148806471:		$B3q0		d-		28.21		4.04		27.24		3.3		3.66		0		-29299.96		14:47:45		m

		S1148806501:		#B3q0		1148806501:		$B3q0		d-		28.21		4.04		27.14		3.3		3.66		0		-29300.85		14:48:15		m

		S1148806531:		#B3q0		1148806531:		$B3q0		d-		28.17		4.04		27.24		3.29		3.66		0		-29301.86		14:48:45		m

		S1148806561:		#B3q0		1148806561:		$B3q0		d-		28.17		4.04		27.14		3.28		3.66		0		-29302.74		14:49:15		m

		S1148806591:		#B3q0		1148806591:		$B3q0		d-		28.14		4		27.24		3.28		3.66		0		-29303.76		14:49:45		m

		S1148806621:		#B3q0		1148806621:		$B3q0		d-		28.14		4.04		27.24		3.27		3.65		0		-29304.64		14:50:15		m

		S1148806651:		#B3q0		1148806651:		$B3q0		d-		28.1		4.08		27.24		3.26		3.65		0		-29305.65		14:50:45		m

		S1148806681:		#B3q0		1148806681:		$B3q0		d-		28.1		4.04		27.14		3.26		3.65		0		-29306.53		14:51:15		m

		S1148806711:		#B3q0		1148806711:		$B3q0		d-		28.06		4		27.24		3.25		3.65		0		-29307.54		14:51:45		m

		S1148806741:		#B3q0		1148806741:		$B3q0		d-		28.06		4.04		27.14		3.24		3.65		0		-29308.42		14:52:15		m

		S1148806771:		#B3q0		1148806771:		$B3q0		d-		28.06		4.04		27.24		3.23		3.65		0		-29309.43		14:52:45		m

		S1148806801:		#B3q0		1148806801:		$B3q0		d-		28.06		4.04		27.14		3.23		3.65		0		-29310.31		14:53:15		m

		S1148806831:		#B3q0		1148806831:		$B3q0		d-		28.02		4.04		27.14		3.22		3.65		0		-29311.32		14:53:45		m

		S1148806861:		#B3q0		1148806861:		$B3q0		d-		27.98		4.04		27.24		3.21		3.65		0		-29312.2		14:54:15		m

		S1148806891:		#B3q0		1148806891:		$B3q0		d-		27.98		4.04		27.24		3.2		3.65		0		-29313.2		14:54:45		m

		S1148806921:		#B3q0		1148806921:		$B3q0		d-		27.94		4.04		27.24		3.19		3.65		0		-29314.08		14:55:15		m

		S1148806951:		#B3q0		1148806951:		$B3q0		d-		27.94		4		27.14		3.18		3.65		0		-29315.09		14:55:45		m

		S1148806981:		#B3q0		1148806981:		$B3q0		d-		27.91		4.04		27.14		3.17		3.65		0		-29315.97		14:56:15		m

		S1148807011:		#B3q0		1148807011:		$B3q0		d-		27.91		4.08		27.24		3.16		3.65		0		-29316.97		14:56:45		m

		S1148807041:		#B3q0		1148807041:		$B3q0		d-		27.87		4.04		27.14		3.15		3.65		0		-29317.85		14:57:15		m

		S1148807071:		#B3q0		1148807071:		$B3q0		fc		28.02		0		27.24		3.14		3.65		0		-29318.84		14:57:45		m

		S1148807101:		#B3q0		1148807101:		$B3q0		fc		28.06		0		27.14		3.17		3.67		0		-29318.84		14:58:15		m

		S1148807131:		#B3q0		1148807131:		$B3q0		fc		28.06		0		27.14		3.17		3.67		0		-29318.84		14:58:45		m

		S1148807161:		#B3q0		1148807161:		$B3q0		fc		28.1		0		27.14		3.18		3.67		0		-29318.84		14:59:15		m

		S1148807191:		#B3q0		1148807191:		$B3q0		fc		28.1		0		27.14		3.18		3.67		0		-29318.84		14:59:45		m

		S1148807221:		#B3q0		1148807221:		$B3q0		fc		28.14		0		27.14		3.18		3.67		0		-29318.84		15:00:15		m

		S1148807251:		#B3q0		1148807251:		$B3q0		fc		28.14		0		27.05		3.19		3.67		0		-29318.84		15:00:45		m

		S1148807281:		#B3q0		1148807281:		$B3q0		fc		28.14		0		27.05		3.19		3.67		0		-29318.84		15:01:15		m

		S1148807311:		#B3q0		1148807311:		$B3q0		fc		28.14		0		27.05		3.19		3.67		0		-29318.84		15:01:45		m

		S1148807341:		#B3q0		1148807341:		$B3q0		fc		28.14		0		27.05		3.2		3.67		0		-29318.84		15:02:15		m

		S1148807371:		#B3q0		1148807371:		$B3q0		fc		28.17		0		27.14		3.21		3.67		0		-29318.84		15:02:45		m

		S1148807401:		#B3q0		1148807401:		$B3q0		fc		28.17		0		27.05		3.21		3.67		0		-29318.84		15:03:15		m

		S1148807431:		#B3q0		1148807431:		$B3q0		fc		28.17		0		26.95		3.22		3.67		0		-29318.84		15:03:45		m

		S1148807461:		#B3q0		1148807461:		$B3q0		fc		28.21		0		27.05		3.22		3.67		0		-29318.84		15:04:15		m

		S1148807491:		#B3q0		1148807491:		$B3q0		fc		28.21		0		27.05		3.23		3.67		0		-29318.84		15:04:45		m

		S1148807521:		#B3q0		1148807521:		$B3q0		fc		28.21		0		27.05		3.23		3.67		0		-29318.84		15:05:15		m

		S1148807551:		#B3q0		1148807551:		$B3q0		fc		28.21		0		27.05		3.23		3.67		0		-29318.84		15:05:45		m

		S1148807581:		#B3q0		1148807581:		$B3q0		fc		28.21		0		27.05		3.24		3.67		0		-29318.84		15:06:15		m

		S1148807611:		#B3q0		1148807611:		$B3q0		fc		28.25		0		26.95		3.25		3.68		0		-29318.84		15:06:45		m

		S1148807641:		#B3q0		1148807641:		$B3q0		fc		28.25		0		26.95		3.26		3.67		0		-29318.84		15:07:15		m

		S1148807671:		#B3q0		1148807671:		$B3q0		fc		28.29		0		26.95		3.26		3.67		0		-29318.84		15:07:45		m

		S1148807701:		#B3q0		1148807701:		$B3q0		fc		28.29		0		26.95		3.26		3.67		0		-29318.84		15:08:15		m

		S1148807731:		#B3q0		1148807731:		$B3q0		fc		28.33		0		26.95		3.27		3.67		0		-29318.84		15:08:45		m

		S1148807761:		#B3q0		1148807761:		$B3q0		fc		28.29		0		26.95		3.28		3.68		0		-29318.84		15:09:15		m

		S1148807791:		#B3q0		1148807791:		$B3q0		fc		28.33		0		26.95		3.28		3.68		0		-29318.84		15:09:45		m

		S1148807821:		#B3q0		1148807821:		$B3q0		fc		28.29		0		26.85		3.28		3.67		0		-29318.84		15:10:15		m

		S1148807851:		#B3q0		1148807851:		$B3q0		fc		28.33		0		26.95		3.29		3.68		0		-29318.84		15:10:45		m

		S1148807881:		#B3q0		1148807881:		$B3q0		fc		28.33		0		26.85		3.29		3.67		0		-29318.84		15:11:15		m

		S1148807911:		#B3q0		1148807911:		$B3q0		fc		28.36		0		26.85		3.29		3.68		0		-29318.84		15:11:45		m

		S1148807941:		#B3q0		1148807941:		$B3q0		fc		28.36		0		26.85		3.3		3.68		0		-29318.84		15:12:15		m

		S1148807971:		#B3q0		1148807971:		$B3q0		fc		28.36		0		26.85		3.3		3.68		0		-29318.84		15:12:45		m

		S1148808001:		#B3q0		1148808001:		$B3q0		fc		28.36		0		26.75		3.3		3.68		0		-29318.84		15:13:15		m

		S1148808031:		#B3q0		1148808031:		$B3q0		fc		28.36		0		26.85		3.31		3.68		0		-29318.84		15:13:45		m

		S1148808061:		#B3q0		1148808061:		$B3q0		fc		28.36		0		26.75		3.31		3.68		0		-29318.84		15:14:15		m

		S1148808091:		#B3q0		1148808091:		$B3q0		fc		28.36		0		26.75		3.31		3.68		0		-29318.84		15:14:45		m

		S1148808121:		#B3q0		1148808121:		$B3q0		fc		28.36		0		26.75		3.32		3.68		0		-29318.84		15:15:15		m

		S1148808151:		#B3q0		1148808151:		$B3q0		fc		28.4		0		26.85		3.32		3.68		0		-29318.84		15:15:45		m

		S1148808181:		#B3q0		1148808181:		$B3q0		fc		28.4		0		26.75		3.32		3.68		0		-29318.84		15:16:15		m

		S1148808211:		#B3q0		1148808211:		$B3q0		fc		28.4		0		26.75		3.32		3.68		0		-29318.84		15:16:45		m

		S1148808241:		#B3q0		1148808241:		$B3q0		fc		28.44		0		26.75		3.32		3.68		0		-29318.84		15:17:15		m

		S1148808271:		#B3q0		1148808271:		$B3q0		fc		28.4		0		26.75		3.32		3.68		0		-29318.84		15:17:45		m

		S1148808301:		#B3q0		1148808301:		$B3q0		fc		28.4		0		26.75		3.33		3.68		0		-29318.84		15:18:15		m

		S1148808331:		#B3q0		1148808331:		$B3q0		fc		28.4		0		26.66		3.33		3.68		0		-29318.84		15:18:45		m

		S1148808361:		#B3q0		1148808361:		$B3q0		fc		28.44		0		26.66		3.33		3.68		0		-29318.84		15:19:15		m

		S1148808391:		#B3q0		1148808391:		$B3q0		fc		28.44		0		26.66		3.33		3.68		0		-29318.84		15:19:45		m

		S1148808421:		#B3q0		1148808421:		$B3q0		fc		28.44		0		26.66		3.33		3.68		0		-29318.84		15:20:15		m

		S1148808451:		#B3q0		1148808451:		$B3q0		fc		28.4		0		26.56		3.33		3.68		0		-29318.84		15:20:45		m

		S1148808481:		#B3q0		1148808481:		$B3q0		fc		28.44		0		26.66		3.34		3.68		0		-29318.84		15:21:15		m

		S1148808511:		#B3q0		1148808511:		$B3q0		fc		28.44		0		26.66		3.34		3.68		0		-29318.84		15:21:45		m

		S1148808541:		#B3q0		1148808541:		$B3q0		fc		28.48		0		26.56		3.34		3.68		0		-29318.84		15:22:15		m

		S1148808571:		#B3q0		1148808571:		$B3q0		fc		28.44		0		26.56		3.34		3.68		0		-29318.84		15:22:45		m

		S1148808601:		#B3q0		1148808601:		$B3q0		fc		28.44		0		26.56		3.34		3.68		0		-29318.84		15:23:15		m

		S1148808631:		#B3q0		1148808631:		$B3q0		fc		28.48		0		26.56		3.35		3.68		0		-29318.84		15:23:45		m

		S1148808661:		#B3q0		1148808661:		$B3q0		fc		28.48		0		26.56		3.35		3.68		0		-29318.84		15:24:15		m

		S1148808691:		#B3q0		1148808691:		$B3q0		fc		28.48		0		26.56		3.35		3.68		0		-29318.84		15:24:45		m

		S1148808721:		#B3q0		1148808721:		$B3q0		fc		28.48		0		26.56		3.35		3.68		0		-29318.84		15:25:15		m

		S1148808751:		#B3q0		1148808751:		$B3q0		fc		28.48		0		26.56		3.35		3.68		0		-29318.84		15:25:45		m

		S1148808781:		#B3q0		1148808781:		$B3q0		fc		28.48		0		26.46		3.35		3.68		0		-29318.84		15:26:15		m

		S1148808811:		#B3q0		1148808811:		$B3q0		fc		28.48		0		26.46		3.35		3.68		0		-29318.84		15:26:45		m

		S1148808841:		#B3q0		1148808841:		$B3q0		fc		28.51		0		26.56		3.35		3.68		0		-29318.84		15:27:15		m

		S1148808871:		#B3q0		1148808871:		$B3q0		fc		28.51		0		26.56		3.35		3.68		0		-29318.84		15:27:45		m

		S1148808901:		#B3q0		1148808901:		$B3q0		fc		28.51		0		26.46		3.35		3.68		0		-29318.84		15:28:15		m

		S1148808931:		#B3q0		1148808931:		$B3q0		fc		28.48		0		26.46		3.35		3.68		0		-29318.84		15:28:45		m

		S1148808961:		#B3q0		1148808961:		$B3q0		fc		28.51		0		26.46		3.36		3.68		0		-29318.84		15:29:15		m

		S1148808991:		#B3q0		1148808991:		$B3q0		fc		28.51		0		26.46		3.36		3.68		0		-29318.84		15:29:45		m

		S1148809021:		#B3q0		1148809021:		$B3q0		fc		28.48		0		26.46		3.36		3.68		0		-29318.84		15:30:15		m

		S1148809051:		#B3q0		1148809051:		$B3q0		fc		28.51		0		26.46		3.36		3.68		0		-29318.84		15:30:45		m

		S1148809081:		#B3q0		1148809081:		$B3q0		fc		28.51		0		26.36		3.36		3.68		0		-29318.84		15:31:15		m

		S1148809111:		#B3q0		1148809111:		$B3q0		fc		28.51		0		26.46		3.36		3.68		0		-29318.84		15:31:45		m

		S1148809141:		#B3q0		1148809141:		$B3q0		fc		28.51		0		26.36		3.36		3.68		0		-29318.84		15:32:15		m

		S1148809171:		#B3q0		1148809171:		$B3q0		fc		28.55		0		26.36		3.36		3.68		0		-29318.84		15:32:45		m

		S1148809201:		#B3q0		1148809201:		$B3q0		fc		28.51		0		26.36		3.37		3.68		0		-29318.84		15:33:15		m

		S1148809231:		#B3q0		1148809231:		$B3q0		fc		28.55		0		26.36		3.37		3.68		0		-29318.84		15:33:45		m

		S1148809261:		#B3q0		1148809261:		$B3q0		fc		28.51		0		26.36		3.37		3.68		0		-29318.84		15:34:15		m

		S1148809291:		#B3q0		1148809291:		$B3q0		fc		28.55		0		26.36		3.37		3.68		0		-29318.84		15:34:45		m

		S1148809321:		#B3q0		1148809321:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:35:15		m

		S1148809351:		#B3q0		1148809351:		$B3q0		fc		28.55		0		26.36		3.37		3.68		0		-29318.84		15:35:45		m

		S1148809381:		#B3q0		1148809381:		$B3q0		fc		28.51		0		26.26		3.37		3.68		0		-29318.84		15:36:15		m

		S1148809411:		#B3q0		1148809411:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:36:45		m

		S1148809441:		#B3q0		1148809441:		$B3q0		fc		28.55		0		26.36		3.37		3.68		0		-29318.84		15:37:15		m

		S1148809471:		#B3q0		1148809471:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:37:45		m

		S1148809501:		#B3q0		1148809501:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:38:15		m

		S1148809531:		#B3q0		1148809531:		$B3q0		fc		28.59		0		26.26		3.37		3.68		0		-29318.84		15:38:45		m

		S1148809561:		#B3q0		1148809561:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:39:15		m

		S1148809591:		#B3q0		1148809591:		$B3q0		fc		28.59		0		26.26		3.37		3.68		0		-29318.84		15:39:45		m

		S1148809621:		#B3q0		1148809621:		$B3q0		fc		28.59		0		26.26		3.37		3.68		0		-29318.84		15:40:15		m

		S1148809651:		#B3q0		1148809651:		$B3q0		fc		28.59		0		26.26		3.37		3.68		0		-29318.84		15:40:45		m

		S1148809681:		#B3q0		1148809681:		$B3q0		fc		28.55		0		26.17		3.37		3.68		0		-29318.84		15:41:15		m

		S1148809711:		#B3q0		1148809711:		$B3q0		fc		28.55		0		26.26		3.37		3.68		0		-29318.84		15:41:45		m

		S1148809741:		#B3q0		1148809741:		$B3q0		fc		28.59		0		26.17		3.37		3.68		0		-29318.84		15:42:15		m

		S1148809771:		#B3q0		1148809771:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:42:45		m

		S1148809801:		#B3q0		1148809801:		$B3q0		fc		28.55		0		26.17		3.38		3.68		0		-29318.84		15:43:15		m

		S1148809831:		#B3q0		1148809831:		$B3q0		fc		28.59		0		26.26		3.38		3.68		0		-29318.84		15:43:45		m

		S1148809861:		#B3q0		1148809861:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:44:15		m

		S1148809891:		#B3q0		1148809891:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:44:45		m

		S1148809921:		#B3q0		1148809921:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:45:15		m

		S1148809951:		#B3q0		1148809951:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:45:45		m

		S1148809981:		#B3q0		1148809981:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:46:15		m

		S1148810011:		#B3q0		1148810011:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:46:45		m

		S1148810041:		#B3q0		1148810041:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:47:15		m

		S1148810071:		#B3q0		1148810071:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:47:45		m

		S1148810101:		#B3q0		1148810101:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:48:15		m

		S1148810131:		#B3q0		1148810131:		$B3q0		fc		28.63		0		26.17		3.38		3.68		0		-29318.84		15:48:45		m

		S1148810161:		#B3q0		1148810161:		$B3q0		fc		28.59		0		26.17		3.38		3.68		0		-29318.84		15:49:15		m

		S1148810191:		#B3q0		1148810191:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:49:45		m

		S1148810221:		#B3q0		1148810221:		$B3q0		fc		28.63		0		26.17		3.38		3.68		0		-29318.84		15:50:15		m

		S1148810251:		#B3q0		1148810251:		$B3q0		fc		28.59		0		25.97		3.38		3.68		0		-29318.84		15:50:45		m

		S1148810281:		#B3q0		1148810281:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:51:15		m

		S1148810311:		#B3q0		1148810311:		$B3q0		fc		28.59		0		26.07		3.38		3.68		0		-29318.84		15:51:45		m

		S1148810341:		#B3q0		1148810341:		$B3q0		fc		28.63		0		26.07		3.38		3.68		0		-29318.84		15:52:15		m

		S1148810371:		#B3q0		1148810371:		$B3q0		fc		28.63		0		25.97		3.38		3.68		0		-29318.84		15:52:45		m

		S1148810401:		#B3q0		1148810401:		$B3q0		fc		28.63		0		25.97		3.38		3.68		0		-29318.84		15:53:15		m

		S1148810431:		#B3q0		1148810431:		$B3q0		fc		28.63		0		26.07		3.38		3.68		0		-29318.84		15:53:45		m

		S1148810461:		#B3q0		1148810461:		$B3q0		fc		28.63		0		25.97		3.38		3.68		0		-29318.84		15:54:15		m

		S1148810491:		#B3q0		1148810491:		$B3q0		fc		28.63		0		25.97		3.38		3.68		0		-29318.84		15:54:45		m

		S1148810521:		#B3q0		1148810521:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		15:55:15		m

		S1148810551:		#B3q0		1148810551:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		15:55:45		m

		S1148810581:		#B3q0		1148810581:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		15:56:15		m

		S1148810611:		#B3q0		1148810611:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		15:56:45		m

		S1148810641:		#B3q0		1148810641:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		15:57:15		m

		S1148810671:		#B3q0		1148810671:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		15:57:45		m

		S1148810701:		#B3q0		1148810701:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		15:58:15		m

		S1148810731:		#B3q0		1148810731:		$B3q0		fc		28.67		0		25.97		3.39		3.68		0		-29318.84		15:58:45		m

		S1148810761:		#B3q0		1148810761:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		15:59:15		m

		S1148810791:		#B3q0		1148810791:		$B3q0		fc		28.67		0		25.97		3.39		3.68		0		-29318.84		15:59:45		m

		S1148810821:		#B3q0		1148810821:		$B3q0		fc		28.63		0		25.97		3.39		3.68		0		-29318.84		16:00:15		m

		S1148810851:		#B3q0		1148810851:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		16:00:45		m

		S1148810881:		#B3q0		1148810881:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:01:15		m

		S1148810911:		#B3q0		1148810911:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		16:01:45		m

		S1148810941:		#B3q0		1148810941:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		16:02:15		m

		S1148810971:		#B3q0		1148810971:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:02:45		m

		S1148811001:		#B3q0		1148811001:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:03:15		m

		S1148811031:		#B3q0		1148811031:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:03:45		m

		S1148811061:		#B3q0		1148811061:		$B3q0		fc		28.63		0		25.87		3.39		3.68		0		-29318.84		16:04:15		m

		S1148811091:		#B3q0		1148811091:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:04:45		m

		S1148811121:		#B3q0		1148811121:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:05:15		m

		S1148811151:		#B3q0		1148811151:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:05:45		m

		S1148811181:		#B3q0		1148811181:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:06:15		m

		S1148811211:		#B3q0		1148811211:		$B3q0		fc		28.63		0		25.78		3.39		3.68		0		-29318.84		16:06:45		m

		S1148811241:		#B3q0		1148811241:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:07:15		m

		S1148811271:		#B3q0		1148811271:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:07:45		m

		S1148811301:		#B3q0		1148811301:		$B3q0		fc		28.67		0		25.87		3.39		3.68		0		-29318.84		16:08:15		m

		S1148811331:		#B3q0		1148811331:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:08:45		m

		S1148811361:		#B3q0		1148811361:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:09:15		m

		S1148811391:		#B3q0		1148811391:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:09:45		m

		S1148811421:		#B3q0		1148811421:		$B3q0		fc		28.67		0		25.68		3.39		3.68		0		-29318.84		16:10:15		m

		S1148811451:		#B3q0		1148811451:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:10:45		m

		S1148811481:		#B3q0		1148811481:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:11:15		m

		S1148811511:		#B3q0		1148811511:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:11:45		m

		S1148811541:		#B3q0		1148811541:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:12:15		m

		S1148811571:		#B3q0		1148811571:		$B3q0		fc		28.67		0		25.78		3.39		3.68		0		-29318.84		16:12:45		m

		S1148811601:		#B3q0		1148811601:		$B3q0		fc		28.67		0		25.68		3.39		3.68		0		-29318.84		16:13:15		m

		S1148811631:		#B3q0		1148811631:		$B3q0		fc		28.67		0		25.68		3.39		3.68		0		-29318.84		16:13:45		m

		S1148811661:		#B3q0		1148811661:		$B3q0		fc		28.71		0		25.78		3.39		3.68		0		-29318.84		16:14:15		m

		S1148811691:		#B3q0		1148811691:		$B3q0		fc		28.67		0		25.68		3.39		3.68		0		-29318.84		16:14:45		m

		S1148811721:		#B3q0		1148811721:		$B3q0		fc		28.71		0		25.78		3.39		3.68		0		-29318.84		16:15:15		m

		S1148811751:		#B3q0		1148811751:		$B3q0		fc		28.71		0		25.78		3.39		3.68		0		-29318.84		16:15:45		m

		S1148811781:		#B3q0		1148811781:		$B3q0		fc		28.67		0		25.68		3.39		3.68		0		-29318.84		16:16:15		m

		S1148811811:		#B3q0		1148811811:		$B3q0		fc		28.71		0		25.68		3.39		3.68		0		-29318.84		16:16:45		m

		S1148811841:		#B3q0		1148811841:		$B3q0		fc		28.71		0		25.68		3.39		3.68		0		-29318.84		16:17:15		m

		S1148811871:		#B3q0		1148811871:		$B3q0		fc		28.71		0		25.78		3.39		3.68		0		-29318.84		16:17:45		m

		S1148811901:		#B3q0		1148811901:		$B3q0		fc		28.71		0		25.68		3.39		3.68		0		-29318.84		16:18:15		m

		S1148811931:		#B3q0		1148811931:		$B3q0		fc		28.71		0		25.68		3.39		3.68		0		-29318.84		16:18:45		m

		S1148811961:		#B3q0		1148811961:		$B3q0		fc		28.71		0		25.58		3.39		3.68		0		-29318.84		16:19:15		m

		S1148811991:		#B3q0		1148811991:		$B3q0		fc		28.71		0		25.68		3.39		3.68		0		-29318.84		16:19:45		m

		S1148812021:		#B3q0		1148812021:		$B3q0		fc		28.71		0		25.58		3.39		3.68		0		-29318.84		16:20:15		m

		S1148812051:		#B3q0		1148812051:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:20:45		m

		S1148812081:		#B3q0		1148812081:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:21:15		m

		S1148812111:		#B3q0		1148812111:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:21:45		m

		S1148812141:		#B3q0		1148812141:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:22:15		m

		S1148812171:		#B3q0		1148812171:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:22:45		m

		S1148812201:		#B3q0		1148812201:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:23:15		m

		S1148812231:		#B3q0		1148812231:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:23:45		m

		S1148812261:		#B3q0		1148812261:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:24:15		m

		S1148812291:		#B3q0		1148812291:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:24:45		m

		S1148812321:		#B3q0		1148812321:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:25:15		m

		S1148812351:		#B3q0		1148812351:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:25:45		m

		S1148812381:		#B3q0		1148812381:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:26:15		m

		S1148812411:		#B3q0		1148812411:		$B3q0		fc		28.71		0		25.68		3.4		3.68		0		-29318.84		16:26:45		m

		S1148812441:		#B3q0		1148812441:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:27:15		m

		S1148812471:		#B3q0		1148812471:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:27:45		m

		S1148812501:		#B3q0		1148812501:		$B3q0		fc		28.74		0		25.58		3.4		3.68		0		-29318.84		16:28:15		m

		S1148812531:		#B3q0		1148812531:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:28:45		m

		S1148812561:		#B3q0		1148812561:		$B3q0		fc		28.74		0		25.58		3.4		3.68		0		-29318.84		16:29:15		m

		S1148812591:		#B3q0		1148812591:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:29:45		m

		S1148812621:		#B3q0		1148812621:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:30:15		m

		S1148812651:		#B3q0		1148812651:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:30:45		m

		S1148812681:		#B3q0		1148812681:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:31:15		m

		S1148812711:		#B3q0		1148812711:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:31:45		m

		S1148812741:		#B3q0		1148812741:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:32:15		m

		S1148812771:		#B3q0		1148812771:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:32:45		m

		S1148812801:		#B3q0		1148812801:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:33:15		m

		S1148812831:		#B3q0		1148812831:		$B3q0		fc		28.74		0		25.58		3.4		3.68		0		-29318.84		16:33:45		m

		S1148812861:		#B3q0		1148812861:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:34:15		m

		S1148812891:		#B3q0		1148812891:		$B3q0		fc		28.71		0		25.58		3.4		3.68		0		-29318.84		16:34:45		m

		S1148812921:		#B3q0		1148812921:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:35:15		m

		S1148812951:		#B3q0		1148812951:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:35:45		m

		S1148812981:		#B3q0		1148812981:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:36:15		m

		S1148813011:		#B3q0		1148813011:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:36:45		m

		S1148813041:		#B3q0		1148813041:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:37:15		m

		S1148813071:		#B3q0		1148813071:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:37:45		m

		S1148813101:		#B3q0		1148813101:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:38:15		m

		S1148813131:		#B3q0		1148813131:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:38:45		m

		S1148813161:		#B3q0		1148813161:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:39:15		m

		S1148813191:		#B3q0		1148813191:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:39:45		m

		S1148813221:		#B3q0		1148813221:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:40:15		m

		S1148813251:		#B3q0		1148813251:		$B3q0		fc		28.71		0		25.48		3.4		3.68		0		-29318.84		16:40:45		m

		S1148813281:		#B3q0		1148813281:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:41:15		m

		S1148813311:		#B3q0		1148813311:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:41:45		m

		S1148813341:		#B3q0		1148813341:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:42:15		m

		S1148813371:		#B3q0		1148813371:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:42:45		m

		S1148813401:		#B3q0		1148813401:		$B3q0		fc		28.74		0		25.48		3.4		3.68		0		-29318.84		16:43:15		m

		S1148813431:		#B3q0		1148813431:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:43:45		m

		S1148813461:		#B3q0		1148813461:		$B3q0		fc		28.71		0		25.48		3.41		3.68		0		-29318.84		16:44:15		m

		S1148813491:		#B3q0		1148813491:		$B3q0		fc		28.74		0		25.39		3.4		3.68		0		-29318.84		16:44:45		m

		S1148813521:		#B3q0		1148813521:		$B3q0		fc		28.78		0		25.39		3.41		3.68		0		-29318.84		16:45:15		m

		S1148813551:		#B3q0		1148813551:		$B3q0		fc		28.78		0		25.39		3.41		3.68		0		-29318.84		16:45:45		m

		S1148813581:		#B3q0		1148813581:		$B3q0		fc		28.78		0		25.39		3.41		3.68		0		-29318.84		16:46:15		m

		S1148813611:		#B3q0		1148813611:		$B3q0		fc		28.78		0		25.39		3.42		3.68		0		-29318.84		16:46:45		m

		S1148813641:		#B3q0		1148813641:		$B3q0		fc		28.78		0		25.39		3.42		3.68		0		-29318.84		16:47:15		m

		S1148813671:		#B3q0		1148813671:		$B3q0		fc		28.74		0		25.29		3.42		3.68		0		-29318.84		16:47:45		m

		S1148813701:		#B3q0		1148813701:		$B3q0		fc		28.78		0		25.29		3.42		3.68		0		-29318.84		16:48:15		m

		S1148813731:		#B3q0		1148813731:		$B3q0		fc		28.74		0		25.39		3.42		3.68		0		-29318.84		16:48:45		m

		S1148813761:		#B3q0		1148813761:		$B3q0		fc		28.78		0		25.39		3.42		3.68		0		-29318.84		16:49:15		m

		S1148813791:		#B3q0		1148813791:		$B3q0		fc		28.78		0		25.29		3.42		3.68		0		-29318.84		16:49:45		m

		S1148813821:		#B3q0		1148813821:		$B3q0		fc		28.74		0		25.29		3.42		3.68		0		-29318.84		16:50:15		m

		S1148813851:		#B3q0		1148813851:		$B3q0		fc		28.78		0		25.29		3.42		3.68		0		-29318.84		16:50:45		m

		S1148813881:		#B3q0		1148813881:		$B3q0		fc		28.78		0		25.29		3.42		3.68		0		-29318.84		16:51:15		m

		S1148813911:		#B3q0		1148813911:		$B3q0		fc		28.78		0		25.29		3.42		3.68		0		-29318.84		16:51:45		m

		S1148813941:		#B3q0		1148813941:		$B3q0		fc		28.78		0		25.39		3.42		3.68		0		-29318.84		16:52:15		m

		S1148813971:		#B3q0		1148813971:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:52:45		m

		S1148814001:		#B3q0		1148814001:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:53:15		m

		S1148814031:		#B3q0		1148814031:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:53:45		m

		S1148814061:		#B3q0		1148814061:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:54:15		m

		S1148814091:		#B3q0		1148814091:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:54:45		m

		S1148814121:		#B3q0		1148814121:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:55:15		m

		S1148814151:		#B3q0		1148814151:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:55:45		m

		S1148814181:		#B3q0		1148814181:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:56:15		m

		S1148814211:		#B3q0		1148814211:		$B3q0		fc		28.78		0		25.39		3.43		3.68		0		-29318.84		16:56:45		m

		S1148814241:		#B3q0		1148814241:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:57:15		m

		S1148814271:		#B3q0		1148814271:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:57:45		m

		S1148814301:		#B3q0		1148814301:		$B3q0		fc		28.78		0		25.29		3.43		3.68		0		-29318.84		16:58:15		m

		S1148814331:		#B3q0		1148814331:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		16:58:45		m

		S1148814361:		#B3q0		1148814361:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		16:59:15		m

		S1148814391:		#B3q0		1148814391:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		16:59:45		m

		S1148814421:		#B3q0		1148814421:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		17:00:15		m

		S1148814451:		#B3q0		1148814451:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		17:00:45		m

		S1148814481:		#B3q0		1148814481:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		17:01:15		m

		S1148814511:		#B3q0		1148814511:		$B3q0		fc		28.82		0		25.29		3.44		3.68		0		-29318.84		17:01:45		m

		S1148814541:		#B3q0		1148814541:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		17:02:15		m

		S1148814571:		#B3q0		1148814571:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:02:45		m

		S1148814601:		#B3q0		1148814601:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		17:03:15		m

		S1148814631:		#B3q0		1148814631:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:03:45		m

		S1148814661:		#B3q0		1148814661:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		17:04:15		m

		S1148814691:		#B3q0		1148814691:		$B3q0		fc		28.82		0		25.29		3.44		3.68		0		-29318.84		17:04:45		m

		S1148814721:		#B3q0		1148814721:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:05:15		m

		S1148814751:		#B3q0		1148814751:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		17:05:45		m

		S1148814781:		#B3q0		1148814781:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:06:15		m

		S1148814811:		#B3q0		1148814811:		$B3q0		fc		28.82		0		25.09		3.44		3.68		0		-29318.84		17:06:45		m

		S1148814841:		#B3q0		1148814841:		$B3q0		fc		28.78		0		25.19		3.44		3.68		0		-29318.84		17:07:15		m

		S1148814871:		#B3q0		1148814871:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:07:45		m

		S1148814901:		#B3q0		1148814901:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:08:15		m

		S1148814931:		#B3q0		1148814931:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:08:45		m

		S1148814961:		#B3q0		1148814961:		$B3q0		fc		28.78		0		25.29		3.44		3.68		0		-29318.84		17:09:15		m

		S1148814991:		#B3q0		1148814991:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:09:45		m

		S1148815021:		#B3q0		1148815021:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:10:15		m

		S1148815051:		#B3q0		1148815051:		$B3q0		fc		28.82		0		25.19		3.44		3.68		0		-29318.84		17:10:45		m

		S1148815081:		#B3q0		1148815081:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:11:15		m

		S1148815111:		#B3q0		1148815111:		$B3q0		fc		28.78		0		25.19		3.45		3.68		0		-29318.84		17:11:45		m

		S1148815141:		#B3q0		1148815141:		$B3q0		fc		28.82		0		25.19		3.45		3.68		0		-29318.84		17:12:15		m

		S1148815171:		#B3q0		1148815171:		$B3q0		fc		28.78		0		25.19		3.45		3.68		0		-29318.84		17:12:45		m

		S1148815201:		#B3q0		1148815201:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:13:15		m

		S1148815231:		#B3q0		1148815231:		$B3q0		fc		28.78		0		25.09		3.45		3.68		0		-29318.84		17:13:45		m

		S1148815261:		#B3q0		1148815261:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:14:15		m

		S1148815291:		#B3q0		1148815291:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:14:45		m

		S1148815321:		#B3q0		1148815321:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:15:15		m

		S1148815351:		#B3q0		1148815351:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:15:45		m

		S1148815381:		#B3q0		1148815381:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:16:15		m

		S1148815411:		#B3q0		1148815411:		$B3q0		fc		28.85		0		25.09		3.45		3.68		0		-29318.84		17:16:45		m

		S1148815441:		#B3q0		1148815441:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:17:15		m

		S1148815471:		#B3q0		1148815471:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:17:45		m

		S1148815501:		#B3q0		1148815501:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:18:15		m

		S1148815531:		#B3q0		1148815531:		$B3q0		fc		28.82		0		25		3.45		3.68		0		-29318.84		17:18:45		m

		S1148815561:		#B3q0		1148815561:		$B3q0		fc		28.85		0		25.19		3.45		3.68		0		-29318.84		17:19:15		m

		S1148815591:		#B3q0		1148815591:		$B3q0		fc		28.82		0		25		3.45		3.68		0		-29318.84		17:19:45		m

		S1148815621:		#B3q0		1148815621:		$B3q0		fc		28.85		0		25.09		3.45		3.68		0		-29318.84		17:20:15		m

		S1148815651:		#B3q0		1148815651:		$B3q0		fc		28.78		0		25.09		3.45		3.68		0		-29318.84		17:20:45		m

		S1148815681:		#B3q0		1148815681:		$B3q0		fc		28.78		0		25		3.45		3.68		0		-29318.84		17:21:15		m

		S1148815711:		#B3q0		1148815711:		$B3q0		fc		28.82		0		25.09		3.45		3.68		0		-29318.84		17:21:45		m

		S1148815741:		#B3q0		1148815741:		$B3q0		fc		28.78		0		25.09		3.46		3.68		0		-29318.84		17:22:15		m

		S1148815771:		#B3q0		1148815771:		$B3q0		fc		28.78		0		25		3.46		3.68		0		-29318.84		17:22:45		m

		S1148815801:		#B3q0		1148815801:		$B3q0		fc		28.85		0		25.09		3.46		3.68		0		-29318.84		17:23:15		m

		S1148815831:		#B3q0		1148815831:		$B3q0		fc		28.82		0		25.09		3.46		3.68		0		-29318.84		17:23:45		m

		S1148815861:		#B3q0		1148815861:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:24:15		m

		S1148815891:		#B3q0		1148815891:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:24:45		m

		S1148815921:		#B3q0		1148815921:		$B3q0		fc		28.78		0		25.09		3.46		3.68		0		-29318.84		17:25:15		m

		S1148815951:		#B3q0		1148815951:		$B3q0		fc		28.85		0		25.09		3.46		3.68		0		-29318.84		17:25:45		m

		S1148815981:		#B3q0		1148815981:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:26:15		m

		S1148816011:		#B3q0		1148816011:		$B3q0		fc		28.85		0		25.09		3.46		3.68		0		-29318.84		17:26:45		m

		S1148816041:		#B3q0		1148816041:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:27:15		m

		S1148816071:		#B3q0		1148816071:		$B3q0		fc		28.85		0		25.09		3.46		3.68		0		-29318.84		17:27:45		m

		S1148816101:		#B3q0		1148816101:		$B3q0		fc		28.78		0		25.09		3.46		3.68		0		-29318.84		17:28:15		m

		S1148816131:		#B3q0		1148816131:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:28:45		m

		S1148816161:		#B3q0		1148816161:		$B3q0		fc		28.82		0		25.09		3.46		3.68		0		-29318.84		17:29:15		m

		S1148816191:		#B3q0		1148816191:		$B3q0		fc		28.82		0		25.09		3.46		3.68		0		-29318.84		17:29:45		m

		S1148816221:		#B3q0		1148816221:		$B3q0		fc		28.78		0		25		3.46		3.68		0		-29318.84		17:30:15		m

		S1148816251:		#B3q0		1148816251:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:30:45		m

		S1148816281:		#B3q0		1148816281:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:31:15		m

		S1148816311:		#B3q0		1148816311:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:31:45		m

		S1148816341:		#B3q0		1148816341:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:32:15		m

		S1148816371:		#B3q0		1148816371:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:32:45		m

		S1148816401:		#B3q0		1148816401:		$B3q0		fc		28.78		0		24.9		3.46		3.68		0		-29318.84		17:33:15		m

		S1148816431:		#B3q0		1148816431:		$B3q0		fc		28.85		0		25.09		3.46		3.68		0		-29318.84		17:33:45		m

		S1148816461:		#B3q0		1148816461:		$B3q0		fc		28.82		0		24.9		3.46		3.68		0		-29318.84		17:34:15		m

		S1148816491:		#B3q0		1148816491:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:34:45		m

		S1148816521:		#B3q0		1148816521:		$B3q0		fc		28.82		0		25		3.46		3.68		0		-29318.84		17:35:15		m

		S1148816551:		#B3q0		1148816551:		$B3q0		fc		28.82		0		24.9		3.46		3.68		0		-29318.84		17:35:45		m

		S1148816581:		#B3q0		1148816581:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:36:15		m

		S1148816611:		#B3q0		1148816611:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:36:45		m

		S1148816641:		#B3q0		1148816641:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:37:15		m

		S1148816671:		#B3q0		1148816671:		$B3q0		fc		28.82		0		24.9		3.46		3.68		0		-29318.84		17:37:45		m

		S1148816701:		#B3q0		1148816701:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:38:15		m

		S1148816731:		#B3q0		1148816731:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:38:45		m

		S1148816761:		#B3q0		1148816761:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:39:15		m

		S1148816791:		#B3q0		1148816791:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:39:45		m

		S1148816821:		#B3q0		1148816821:		$B3q0		fc		28.85		0		25		3.46		3.68		0		-29318.84		17:40:15		m

		S1148816851:		#B3q0		1148816851:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:40:45		m

		S1148816881:		#B3q0		1148816881:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:41:15		m

		S1148816911:		#B3q0		1148816911:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:41:45		m

		S1148816941:		#B3q0		1148816941:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:42:15		m

		S1148816971:		#B3q0		1148816971:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:42:45		m

		S1148817001:		#B3q0		1148817001:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:43:15		m

		S1148817031:		#B3q0		1148817031:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:43:45		m

		S1148817061:		#B3q0		1148817061:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:44:15		m

		S1148817091:		#B3q0		1148817091:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:44:45		m

		S1148817121:		#B3q0		1148817121:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:45:15		m

		S1148817151:		#B3q0		1148817151:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:45:45		m

		S1148817181:		#B3q0		1148817181:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:46:15		m

		S1148817211:		#B3q0		1148817211:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:46:45		m

		S1148817241:		#B3q0		1148817241:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:47:15		m

		S1148817271:		#B3q0		1148817271:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:47:45		m

		S1148817301:		#B3q0		1148817301:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:48:15		m

		S1148817331:		#B3q0		1148817331:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:48:45		m

		S1148817361:		#B3q0		1148817361:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:49:15		m

		S1148817391:		#B3q0		1148817391:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:49:45		m

		S1148817421:		#B3q0		1148817421:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:50:15		m

		S1148817451:		#B3q0		1148817451:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:50:45		m

		S1148817481:		#B3q0		1148817481:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:51:15		m

		S1148817511:		#B3q0		1148817511:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:51:45		m

		S1148817541:		#B3q0		1148817541:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:52:15		m

		S1148817571:		#B3q0		1148817571:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:52:45		m

		S1148817601:		#B3q0		1148817601:		$B3q0		fc		28.85		0		24.9		3.46		3.68		0		-29318.84		17:53:15		m

		S1148817631:		#B3q0		1148817631:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		17:53:45		m

		S1148817661:		#B3q0		1148817661:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		17:54:15		m

		S1148817691:		#B3q0		1148817691:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		17:54:45		m

		S1148817721:		#B3q0		1148817721:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:55:15		m

		S1148817751:		#B3q0		1148817751:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:55:45		m

		S1148817781:		#B3q0		1148817781:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		17:56:15		m

		S1148817811:		#B3q0		1148817811:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:56:45		m

		S1148817841:		#B3q0		1148817841:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:57:15		m

		S1148817871:		#B3q0		1148817871:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		17:57:45		m

		S1148817901:		#B3q0		1148817901:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		17:58:15		m

		S1148817931:		#B3q0		1148817931:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:58:45		m

		S1148817961:		#B3q0		1148817961:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		17:59:15		m

		S1148817991:		#B3q0		1148817991:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		17:59:45		m

		S1148818021:		#B3q0		1148818021:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		18:00:15		m

		S1148818051:		#B3q0		1148818051:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		18:00:45		m

		S1148818081:		#B3q0		1148818081:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		18:01:15		m

		S1148818111:		#B3q0		1148818111:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		18:01:45		m

		S1148818141:		#B3q0		1148818141:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:02:15		m

		S1148818171:		#B3q0		1148818171:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		18:02:45		m

		S1148818201:		#B3q0		1148818201:		$B3q0		fc		28.85		0		24.9		3.47		3.68		0		-29318.84		18:03:15		m

		S1148818231:		#B3q0		1148818231:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		18:03:45		m

		S1148818261:		#B3q0		1148818261:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:04:15		m

		S1148818291:		#B3q0		1148818291:		$B3q0		fc		28.85		0		24.7		3.47		3.68		0		-29318.84		18:04:45		m

		S1148818321:		#B3q0		1148818321:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:05:15		m

		S1148818351:		#B3q0		1148818351:		$B3q0		fc		28.89		0		24.9		3.47		3.68		0		-29318.84		18:05:45		m

		S1148818381:		#B3q0		1148818381:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:06:15		m

		S1148818411:		#B3q0		1148818411:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:06:45		m

		S1148818441:		#B3q0		1148818441:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:07:15		m

		S1148818471:		#B3q0		1148818471:		$B3q0		fc		28.85		0		24.7		3.47		3.68		0		-29318.84		18:07:45		m

		S1148818501:		#B3q0		1148818501:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:08:15		m

		S1148818531:		#B3q0		1148818531:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:08:45		m

		S1148818561:		#B3q0		1148818561:		$B3q0		fc		28.85		0		24.7		3.47		3.69		0		-29318.84		18:09:15		m

		S1148818591:		#B3q0		1148818591:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:09:45		m

		S1148818621:		#B3q0		1148818621:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:10:15		m

		S1148818651:		#B3q0		1148818651:		$B3q0		fc		28.85		0		24.7		3.47		3.68		0		-29318.84		18:10:45		m

		S1148818681:		#B3q0		1148818681:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:11:15		m

		S1148818711:		#B3q0		1148818711:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:11:45		m

		S1148818741:		#B3q0		1148818741:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:12:15		m

		S1148818771:		#B3q0		1148818771:		$B3q0		fc		28.89		0		24.8		3.47		3.68		0		-29318.84		18:12:45		m

		S1148818801:		#B3q0		1148818801:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:13:15		m

		S1148818831:		#B3q0		1148818831:		$B3q0		fc		28.85		0		24.8		3.47		3.68		0		-29318.84		18:13:45		m

		S1148818861:		#B3q0		1148818861:		$B3q0		fc		28.85		0		24.7		3.47		3.68		0		-29318.84		18:14:15		m

		S1148818891:		#B3q0		1148818891:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:14:45		m

		S1148818921:		#B3q0		1148818921:		$B3q0		fc		28.85		0		24.7		3.47		3.69		0		-29318.84		18:15:15		m

		S1148818951:		#B3q0		1148818951:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:15:45		m

		S1148818981:		#B3q0		1148818981:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:16:15		m

		S1148819011:		#B3q0		1148819011:		$B3q0		fc		28.85		0		24.7		3.47		3.69		0		-29318.84		18:16:45		m

		S1148819041:		#B3q0		1148819041:		$B3q0		fc		28.89		0		24.7		3.47		3.68		0		-29318.84		18:17:15		m

		S1148819071:		#B3q0		1148819071:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:17:45		m

		S1148819101:		#B3q0		1148819101:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:18:15		m

		S1148819131:		#B3q0		1148819131:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:18:45		m

		S1148819161:		#B3q0		1148819161:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:19:15		m

		S1148819191:		#B3q0		1148819191:		$B3q0		fc		28.89		0		24.7		3.47		3.68		0		-29318.84		18:19:45		m

		S1148819221:		#B3q0		1148819221:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:20:15		m

		S1148819251:		#B3q0		1148819251:		$B3q0		fc		28.93		0		24.8		3.47		3.69		0		-29318.84		18:20:45		m

		S1148819281:		#B3q0		1148819281:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:21:15		m

		S1148819311:		#B3q0		1148819311:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:21:45		m

		S1148819341:		#B3q0		1148819341:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:22:15		m

		S1148819371:		#B3q0		1148819371:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:22:45		m

		S1148819401:		#B3q0		1148819401:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:23:15		m

		S1148819431:		#B3q0		1148819431:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:23:45		m

		S1148819461:		#B3q0		1148819461:		$B3q0		fc		28.85		0		24.7		3.47		3.69		0		-29318.84		18:24:15		m

		S1148819491:		#B3q0		1148819491:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:24:45		m

		S1148819521:		#B3q0		1148819521:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:25:15		m

		S1148819551:		#B3q0		1148819551:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:25:45		m

		S1148819581:		#B3q0		1148819581:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:26:15		m

		S1148819611:		#B3q0		1148819611:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:26:45		m

		S1148819641:		#B3q0		1148819641:		$B3q0		fc		28.89		0		24.7		3.47		3.68		0		-29318.84		18:27:15		m

		S1148819671:		#B3q0		1148819671:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:27:45		m

		S1148819701:		#B3q0		1148819701:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:28:15		m

		S1148819731:		#B3q0		1148819731:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:28:45		m

		S1148819761:		#B3q0		1148819761:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:29:15		m

		S1148819791:		#B3q0		1148819791:		$B3q0		fc		28.89		0		24.8		3.47		3.69		0		-29318.84		18:29:45		m

		S1148819821:		#B3q0		1148819821:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:30:15		m

		S1148819851:		#B3q0		1148819851:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:30:45		m

		S1148819881:		#B3q0		1148819881:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:31:15		m

		S1148819911:		#B3q0		1148819911:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:31:45		m

		S1148819941:		#B3q0		1148819941:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:32:15		m

		S1148819971:		#B3q0		1148819971:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:32:45		m

		S1148820001:		#B3q0		1148820001:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:33:15		m

		S1148820031:		#B3q0		1148820031:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:33:45		m

		S1148820061:		#B3q0		1148820061:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:34:15		m

		S1148820091:		#B3q0		1148820091:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:34:45		m

		S1148820121:		#B3q0		1148820121:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:35:15		m

		S1148820151:		#B3q0		1148820151:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:35:45		m

		S1148820181:		#B3q0		1148820181:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:36:15		m

		S1148820211:		#B3q0		1148820211:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:36:45		m

		S1148820241:		#B3q0		1148820241:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:37:15		m

		S1148820271:		#B3q0		1148820271:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:37:45		m

		S1148820301:		#B3q0		1148820301:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:38:15		m

		S1148820331:		#B3q0		1148820331:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:38:45		m

		S1148820361:		#B3q0		1148820361:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:39:15		m

		S1148820391:		#B3q0		1148820391:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:39:45		m

		S1148820421:		#B3q0		1148820421:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:40:15		m

		S1148820451:		#B3q0		1148820451:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:40:45		m

		S1148820481:		#B3q0		1148820481:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:41:15		m

		S1148820511:		#B3q0		1148820511:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:41:45		m

		S1148820541:		#B3q0		1148820541:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:42:15		m

		S1148820571:		#B3q0		1148820571:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:42:45		m

		S1148820601:		#B3q0		1148820601:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:43:15		m

		S1148820631:		#B3q0		1148820631:		$B3q0		fc		28.89		0		24.51		3.47		3.69		0		-29318.84		18:43:45		m

		S1148820661:		#B3q0		1148820661:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:44:15		m

		S1148820691:		#B3q0		1148820691:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:44:45		m

		S1148820721:		#B3q0		1148820721:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:45:15		m

		S1148820751:		#B3q0		1148820751:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:45:45		m

		S1148820781:		#B3q0		1148820781:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:46:15		m

		S1148820811:		#B3q0		1148820811:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:46:45		m

		S1148820841:		#B3q0		1148820841:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:47:15		m

		S1148820871:		#B3q0		1148820871:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:47:45		m

		S1148820901:		#B3q0		1148820901:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:48:15		m

		S1148820931:		#B3q0		1148820931:		$B3q0		fc		28.89		0		24.51		3.47		3.69		0		-29318.84		18:48:45		m

		S1148820961:		#B3q0		1148820961:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:49:15		m

		S1148820991:		#B3q0		1148820991:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:49:45		m

		S1148821021:		#B3q0		1148821021:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:50:15		m

		S1148821051:		#B3q0		1148821051:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:50:45		m

		S1148821081:		#B3q0		1148821081:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:51:15		m

		S1148821111:		#B3q0		1148821111:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:51:45		m

		S1148821141:		#B3q0		1148821141:		$B3q0		fc		28.89		0		24.7		3.47		3.69		0		-29318.84		18:52:15		m

		S1148821171:		#B3q0		1148821171:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:52:45		m

		S1148821201:		#B3q0		1148821201:		$B3q0		fc		28.93		0		24.7		3.47		3.69		0		-29318.84		18:53:15		m

		S1148821231:		#B3q0		1148821231:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:53:45		m

		S1148821261:		#B3q0		1148821261:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:54:15		m

		S1148821291:		#B3q0		1148821291:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:54:45		m

		S1148821321:		#B3q0		1148821321:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:55:15		m

		S1148821351:		#B3q0		1148821351:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:55:45		m

		S1148821381:		#B3q0		1148821381:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:56:15		m

		S1148821411:		#B3q0		1148821411:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:56:45		m

		S1148821441:		#B3q0		1148821441:		$B3q0		fc		28.89		0		24.51		3.47		3.69		0		-29318.84		18:57:15		m

		S1148821471:		#B3q0		1148821471:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		18:57:45		m

		S1148821501:		#B3q0		1148821501:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:58:15		m

		S1148821531:		#B3q0		1148821531:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:58:45		m

		S1148821561:		#B3q0		1148821561:		$B3q0		fc		28.93		0		24.51		3.47		3.69		0		-29318.84		18:59:15		m

		S1148821591:		#B3q0		1148821591:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		18:59:45		m

		S1148821621:		#B3q0		1148821621:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:00:15		m

		S1148821651:		#B3q0		1148821651:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		19:00:45		m

		S1148821681:		#B3q0		1148821681:		$B3q0		fc		28.89		0		24.6		3.47		3.69		0		-29318.84		19:01:15		m

		S1148821711:		#B3q0		1148821711:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:01:45		m

		S1148821741:		#B3q0		1148821741:		$B3q0		fc		28.93		0		24.6		3.47		3.69		0		-29318.84		19:02:15		m

		S1148821771:		#B3q0		1148821771:		$B3q0		fc		28.89		0		24.51		3.48		3.69		0		-29318.84		19:02:45		m

		S1148821801:		#B3q0		1148821801:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:03:15		m

		S1148821831:		#B3q0		1148821831:		$B3q0		fc		28.89		0		24.6		3.48		3.69		0		-29318.84		19:03:45		m

		S1148821861:		#B3q0		1148821861:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:04:15		m

		S1148821891:		#B3q0		1148821891:		$B3q0		fc		28.89		0		24.51		3.48		3.69		0		-29318.84		19:04:45		m

		S1148821921:		#B3q0		1148821921:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:05:15		m

		S1148821951:		#B3q0		1148821951:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:05:45		m

		S1148821981:		#B3q0		1148821981:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:06:15		m

		S1148822011:		#B3q0		1148822011:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:06:45		m

		S1148822041:		#B3q0		1148822041:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:07:15		m

		S1148822071:		#B3q0		1148822071:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:07:45		m

		S1148822101:		#B3q0		1148822101:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:08:15		m

		S1148822131:		#B3q0		1148822131:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:08:45		m

		S1148822161:		#B3q0		1148822161:		$B3q0		fc		28.97		0		24.6		3.48		3.69		0		-29318.84		19:09:15		m

		S1148822191:		#B3q0		1148822191:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:09:45		m

		S1148822221:		#B3q0		1148822221:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:10:15		m

		S1148822251:		#B3q0		1148822251:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:10:45		m

		S1148822281:		#B3q0		1148822281:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:11:15		m

		S1148822311:		#B3q0		1148822311:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:11:45		m

		S1148822341:		#B3q0		1148822341:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:12:15		m

		S1148822371:		#B3q0		1148822371:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:12:45		m

		S1148822401:		#B3q0		1148822401:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:13:15		m

		S1148822431:		#B3q0		1148822431:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:13:45		m

		S1148822461:		#B3q0		1148822461:		$B3q0		fc		28.89		0		24.51		3.48		3.69		0		-29318.84		19:14:15		m

		S1148822491:		#B3q0		1148822491:		$B3q0		fc		28.97		0		24.6		3.48		3.69		0		-29318.84		19:14:45		m

		S1148822521:		#B3q0		1148822521:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:15:15		m

		S1148822551:		#B3q0		1148822551:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:15:45		m

		S1148822581:		#B3q0		1148822581:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:16:15		m

		S1148822611:		#B3q0		1148822611:		$B3q0		fc		28.93		0		24.6		3.48		3.69		0		-29318.84		19:16:45		m

		S1148822641:		#B3q0		1148822641:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:17:15		m

		S1148822671:		#B3q0		1148822671:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:17:45		m

		S1148822701:		#B3q0		1148822701:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:18:15		m

		S1148822731:		#B3q0		1148822731:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:18:45		m

		S1148822761:		#B3q0		1148822761:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:19:15		m

		S1148822791:		#B3q0		1148822791:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:19:45		m

		S1148822821:		#B3q0		1148822821:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:20:15		m

		S1148822851:		#B3q0		1148822851:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:20:45		m

		S1148822881:		#B3q0		1148822881:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:21:15		m

		S1148822911:		#B3q0		1148822911:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:21:45		m

		S1148822941:		#B3q0		1148822941:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:22:15		m

		S1148822971:		#B3q0		1148822971:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:22:45		m

		S1148823001:		#B3q0		1148823001:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:23:15		m

		S1148823031:		#B3q0		1148823031:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:23:45		m

		S1148823061:		#B3q0		1148823061:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:24:15		m

		S1148823091:		#B3q0		1148823091:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:24:45		m

		S1148823121:		#B3q0		1148823121:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:25:15		m

		S1148823151:		#B3q0		1148823151:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:25:45		m

		S1148823181:		#B3q0		1148823181:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:26:15		m

		S1148823211:		#B3q0		1148823211:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:26:45		m

		S1148823241:		#B3q0		1148823241:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:27:15		m

		S1148823271:		#B3q0		1148823271:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:27:45		m

		S1148823301:		#B3q0		1148823301:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:28:15		m

		S1148823331:		#B3q0		1148823331:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:28:45		m

		S1148823361:		#B3q0		1148823361:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:29:15		m

		S1148823391:		#B3q0		1148823391:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:29:45		m

		S1148823421:		#B3q0		1148823421:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:30:15		m

		S1148823451:		#B3q0		1148823451:		$B3q0		fc		28.93		0		24.31		3.48		3.69		0		-29318.84		19:30:45		m

		S1148823481:		#B3q0		1148823481:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:31:15		m

		S1148823511:		#B3q0		1148823511:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:31:45		m

		S1148823541:		#B3q0		1148823541:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:32:15		m

		S1148823571:		#B3q0		1148823571:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:32:45		m

		S1148823601:		#B3q0		1148823601:		$B3q0		fc		28.93		0		24.31		3.48		3.69		0		-29318.84		19:33:15		m

		S1148823631:		#B3q0		1148823631:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:33:45		m

		S1148823661:		#B3q0		1148823661:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:34:15		m

		S1148823691:		#B3q0		1148823691:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:34:45		m

		S1148823721:		#B3q0		1148823721:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:35:15		m

		S1148823751:		#B3q0		1148823751:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:35:45		m

		S1148823781:		#B3q0		1148823781:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:36:15		m

		S1148823811:		#B3q0		1148823811:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:36:45		m

		S1148823841:		#B3q0		1148823841:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:37:15		m

		S1148823871:		#B3q0		1148823871:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:37:45		m

		S1148823901:		#B3q0		1148823901:		$B3q0		fc		28.97		0		24.51		3.48		3.69		0		-29318.84		19:38:15		m

		S1148823931:		#B3q0		1148823931:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:38:45		m

		S1148823961:		#B3q0		1148823961:		$B3q0		fc		28.93		0		24.51		3.48		3.69		0		-29318.84		19:39:15		m

		S1148823991:		#B3q0		1148823991:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:39:45		m

		S1148824021:		#B3q0		1148824021:		$B3q0		fc		28.93		0		24.41		3.48		3.69		0		-29318.84		19:40:15		m

		S1148824051:		#B3q0		1148824051:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:40:45		m

		S1148824081:		#B3q0		1148824081:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:41:15		m

		S1148824111:		#B3q0		1148824111:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:41:45		m

		S1148824141:		#B3q0		1148824141:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:42:15		m

		S1148824171:		#B3q0		1148824171:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:42:45		m

		S1148824201:		#B3q0		1148824201:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:43:15		m

		S1148824231:		#B3q0		1148824231:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:43:45		m

		S1148824261:		#B3q0		1148824261:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		19:44:15		m

		S1148824291:		#B3q0		1148824291:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:44:45		m

		S1148824321:		#B3q0		1148824321:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:45:15		m

		S1148824351:		#B3q0		1148824351:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:45:45		m

		S1148824381:		#B3q0		1148824381:		$B3q0		fc		29.01		0		24.51		3.48		3.69		0		-29318.84		19:46:15		m

		S1148824411:		#B3q0		1148824411:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:46:45		m

		S1148824441:		#B3q0		1148824441:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		19:47:15		m

		S1148824471:		#B3q0		1148824471:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:47:45		m

		S1148824501:		#B3q0		1148824501:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:48:15		m

		S1148824531:		#B3q0		1148824531:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:48:45		m

		S1148824561:		#B3q0		1148824561:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:49:15		m

		S1148824591:		#B3q0		1148824591:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:49:45		m

		S1148824621:		#B3q0		1148824621:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:50:15		m

		S1148824651:		#B3q0		1148824651:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:50:45		m

		S1148824681:		#B3q0		1148824681:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:51:15		m

		S1148824711:		#B3q0		1148824711:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:51:45		m

		S1148824741:		#B3q0		1148824741:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		19:52:15		m

		S1148824771:		#B3q0		1148824771:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:52:45		m

		S1148824801:		#B3q0		1148824801:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		19:53:15		m

		S1148824831:		#B3q0		1148824831:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:53:45		m

		S1148824861:		#B3q0		1148824861:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		19:54:15		m

		S1148824891:		#B3q0		1148824891:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:54:45		m

		S1148824921:		#B3q0		1148824921:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:55:15		m

		S1148824951:		#B3q0		1148824951:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:55:45		m

		S1148824981:		#B3q0		1148824981:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:56:15		m

		S1148825011:		#B3q0		1148825011:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:56:45		m

		S1148825041:		#B3q0		1148825041:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:57:15		m

		S1148825071:		#B3q0		1148825071:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		19:57:45		m

		S1148825101:		#B3q0		1148825101:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:58:15		m

		S1148825131:		#B3q0		1148825131:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:58:45		m

		S1148825161:		#B3q0		1148825161:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		19:59:15		m

		S1148825191:		#B3q0		1148825191:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		19:59:45		m

		S1148825221:		#B3q0		1148825221:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		20:00:15		m

		S1148825251:		#B3q0		1148825251:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:00:45		m

		S1148825281:		#B3q0		1148825281:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:01:15		m

		S1148825311:		#B3q0		1148825311:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:01:45		m

		S1148825341:		#B3q0		1148825341:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:02:15		m

		S1148825371:		#B3q0		1148825371:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:02:45		m

		S1148825401:		#B3q0		1148825401:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		20:03:15		m

		S1148825431:		#B3q0		1148825431:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:03:45		m

		S1148825461:		#B3q0		1148825461:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:04:15		m

		S1148825491:		#B3q0		1148825491:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		20:04:45		m

		S1148825521:		#B3q0		1148825521:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:05:15		m

		S1148825551:		#B3q0		1148825551:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:05:45		m

		S1148825581:		#B3q0		1148825581:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:06:15		m

		S1148825611:		#B3q0		1148825611:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		20:06:45		m

		S1148825641:		#B3q0		1148825641:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:07:15		m

		S1148825671:		#B3q0		1148825671:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:07:45		m

		S1148825701:		#B3q0		1148825701:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:08:15		m

		S1148825731:		#B3q0		1148825731:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:08:45		m

		S1148825761:		#B3q0		1148825761:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		20:09:15		m

		S1148825791:		#B3q0		1148825791:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:09:45		m

		S1148825821:		#B3q0		1148825821:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:10:15		m

		S1148825851:		#B3q0		1148825851:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:10:45		m

		S1148825881:		#B3q0		1148825881:		$B3q0		fc		29.01		0		24.41		3.48		3.69		0		-29318.84		20:11:15		m

		S1148825911:		#B3q0		1148825911:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:11:45		m

		S1148825941:		#B3q0		1148825941:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:12:15		m

		S1148825971:		#B3q0		1148825971:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:12:45		m

		S1148826001:		#B3q0		1148826001:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:13:15		m

		S1148826031:		#B3q0		1148826031:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:13:45		m

		S1148826061:		#B3q0		1148826061:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:14:15		m

		S1148826091:		#B3q0		1148826091:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:14:45		m

		S1148826121:		#B3q0		1148826121:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:15:15		m

		S1148826151:		#B3q0		1148826151:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:15:45		m

		S1148826181:		#B3q0		1148826181:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:16:15		m

		S1148826211:		#B3q0		1148826211:		$B3q0		fc		28.97		0		24.41		3.48		3.69		0		-29318.84		20:16:45		m

		S1148826241:		#B3q0		1148826241:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:17:15		m

		S1148826271:		#B3q0		1148826271:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:17:45		m

		S1148826301:		#B3q0		1148826301:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:18:15		m

		S1148826331:		#B3q0		1148826331:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:18:45		m

		S1148826361:		#B3q0		1148826361:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:19:15		m

		S1148826391:		#B3q0		1148826391:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:19:45		m

		S1148826421:		#B3q0		1148826421:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:20:15		m

		S1148826451:		#B3q0		1148826451:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:20:45		m

		S1148826481:		#B3q0		1148826481:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:21:15		m

		S1148826511:		#B3q0		1148826511:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:21:45		m

		S1148826541:		#B3q0		1148826541:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:22:15		m

		S1148826571:		#B3q0		1148826571:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:22:45		m

		S1148826601:		#B3q0		1148826601:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:23:15		m

		S1148826631:		#B3q0		1148826631:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:23:45		m

		S1148826661:		#B3q0		1148826661:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:24:15		m

		S1148826691:		#B3q0		1148826691:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:24:45		m

		S1148826721:		#B3q0		1148826721:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:25:15		m

		S1148826751:		#B3q0		1148826751:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:25:45		m

		S1148826781:		#B3q0		1148826781:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:26:15		m

		S1148826811:		#B3q0		1148826811:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:26:45		m

		S1148826841:		#B3q0		1148826841:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:27:15		m

		S1148826871:		#B3q0		1148826871:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:27:45		m

		S1148826901:		#B3q0		1148826901:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:28:15		m

		S1148826931:		#B3q0		1148826931:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:28:45		m

		S1148826961:		#B3q0		1148826961:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:29:15		m

		S1148826991:		#B3q0		1148826991:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:29:45		m

		S1148827021:		#B3q0		1148827021:		$B3q0		fc		29.01		0		24.12		3.48		3.69		0		-29318.84		20:30:15		m

		S1148827051:		#B3q0		1148827051:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:30:45		m

		S1148827081:		#B3q0		1148827081:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:31:15		m

		S1148827111:		#B3q0		1148827111:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:31:45		m

		S1148827141:		#B3q0		1148827141:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:32:15		m

		S1148827171:		#B3q0		1148827171:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:32:45		m

		S1148827201:		#B3q0		1148827201:		$B3q0		fc		29.05		0		24.31		3.48		3.69		0		-29318.84		20:33:15		m

		S1148827231:		#B3q0		1148827231:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:33:45		m

		S1148827261:		#B3q0		1148827261:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:34:15		m

		S1148827291:		#B3q0		1148827291:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:34:45		m

		S1148827321:		#B3q0		1148827321:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:35:15		m

		S1148827351:		#B3q0		1148827351:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:35:45		m

		S1148827381:		#B3q0		1148827381:		$B3q0		fc		28.97		0		24.31		3.48		3.69		0		-29318.84		20:36:15		m

		S1148827411:		#B3q0		1148827411:		$B3q0		fc		29.01		0		24.31		3.48		3.69		0		-29318.84		20:36:45		m

		S1148827441:		#B3q0		1148827441:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:37:15		m

		S1148827471:		#B3q0		1148827471:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:37:45		m

		S1148827501:		#B3q0		1148827501:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:38:15		m

		S1148827531:		#B3q0		1148827531:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:38:45		m

		S1148827561:		#B3q0		1148827561:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:39:15		m

		S1148827591:		#B3q0		1148827591:		$B3q0		fc		29.01		0		24.12		3.48		3.69		0		-29318.84		20:39:45		m

		S1148827621:		#B3q0		1148827621:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:40:15		m

		S1148827651:		#B3q0		1148827651:		$B3q0		fc		29.05		0		24.12		3.48		3.69		0		-29318.84		20:40:45		m

		S1148827681:		#B3q0		1148827681:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:41:15		m

		S1148827711:		#B3q0		1148827711:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:41:45		m

		S1148827741:		#B3q0		1148827741:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:42:15		m

		S1148827771:		#B3q0		1148827771:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:42:45		m

		S1148827801:		#B3q0		1148827801:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:43:15		m

		S1148827831:		#B3q0		1148827831:		$B3q0		fc		28.97		0		24.12		3.48		3.69		0		-29318.84		20:43:45		m

		S1148827861:		#B3q0		1148827861:		$B3q0		fc		29.01		0		24.12		3.48		3.69		0		-29318.84		20:44:15		m

		S1148827891:		#B3q0		1148827891:		$B3q0		fc		29.01		0		24.21		3.48		3.69		0		-29318.84		20:44:45		m

		S1148827921:		#B3q0		1148827921:		$B3q0		fc		29.01		0		24.31		3.49		3.69		0		-29318.84		20:45:15		m

		S1148827951:		#B3q0		1148827951:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		20:45:45		m

		S1148827981:		#B3q0		1148827981:		$B3q0		fc		28.97		0		24.21		3.48		3.69		0		-29318.84		20:46:15		m

		S1148828011:		#B3q0		1148828011:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:46:45		m

		S1148828041:		#B3q0		1148828041:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		20:47:15		m

		S1148828071:		#B3q0		1148828071:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:47:45		m

		S1148828101:		#B3q0		1148828101:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:48:15		m

		S1148828131:		#B3q0		1148828131:		$B3q0		fc		28.97		0		24.21		3.49		3.69		0		-29318.84		20:48:45		m

		S1148828161:		#B3q0		1148828161:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:49:15		m

		S1148828191:		#B3q0		1148828191:		$B3q0		fc		28.97		0		24.31		3.49		3.69		0		-29318.84		20:49:45		m

		S1148828221:		#B3q0		1148828221:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:50:15		m

		S1148828251:		#B3q0		1148828251:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:50:45		m

		S1148828281:		#B3q0		1148828281:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:51:15		m

		S1148828311:		#B3q0		1148828311:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:51:45		m

		S1148828341:		#B3q0		1148828341:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:52:15		m

		S1148828371:		#B3q0		1148828371:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:52:45		m

		S1148828401:		#B3q0		1148828401:		$B3q0		fc		28.97		0		24.21		3.49		3.69		0		-29318.84		20:53:15		m

		S1148828431:		#B3q0		1148828431:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		20:53:45		m

		S1148828461:		#B3q0		1148828461:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:54:15		m

		S1148828491:		#B3q0		1148828491:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		20:54:45		m

		S1148828521:		#B3q0		1148828521:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:55:15		m

		S1148828551:		#B3q0		1148828551:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:55:45		m

		S1148828581:		#B3q0		1148828581:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		20:56:15		m

		S1148828611:		#B3q0		1148828611:		$B3q0		fc		28.97		0		24.21		3.49		3.69		0		-29318.84		20:56:45		m

		S1148828641:		#B3q0		1148828641:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:57:15		m

		S1148828671:		#B3q0		1148828671:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:57:45		m

		S1148828701:		#B3q0		1148828701:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		20:58:15		m

		S1148828731:		#B3q0		1148828731:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:58:45		m

		S1148828761:		#B3q0		1148828761:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		20:59:15		m

		S1148828791:		#B3q0		1148828791:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		20:59:45		m

		S1148828821:		#B3q0		1148828821:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:00:15		m

		S1148828851:		#B3q0		1148828851:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:00:45		m

		S1148828881:		#B3q0		1148828881:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:01:15		m

		S1148828911:		#B3q0		1148828911:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:01:45		m

		S1148828941:		#B3q0		1148828941:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:02:15		m

		S1148828971:		#B3q0		1148828971:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:02:45		m

		S1148829001:		#B3q0		1148829001:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:03:15		m

		S1148829031:		#B3q0		1148829031:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:03:45		m

		S1148829061:		#B3q0		1148829061:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:04:15		m

		S1148829091:		#B3q0		1148829091:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:04:45		m

		S1148829121:		#B3q0		1148829121:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:05:15		m

		S1148829151:		#B3q0		1148829151:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:05:45		m

		S1148829181:		#B3q0		1148829181:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:06:15		m

		S1148829211:		#B3q0		1148829211:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:06:45		m

		S1148829241:		#B3q0		1148829241:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:07:15		m

		S1148829271:		#B3q0		1148829271:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:07:45		m

		S1148829301:		#B3q0		1148829301:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:08:15		m

		S1148829331:		#B3q0		1148829331:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:08:45		m

		S1148829361:		#B3q0		1148829361:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:09:15		m

		S1148829391:		#B3q0		1148829391:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:09:45		m

		S1148829421:		#B3q0		1148829421:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:10:15		m

		S1148829451:		#B3q0		1148829451:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		21:10:45		m

		S1148829481:		#B3q0		1148829481:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:11:15		m

		S1148829511:		#B3q0		1148829511:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:11:45		m

		S1148829541:		#B3q0		1148829541:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:12:15		m

		S1148829571:		#B3q0		1148829571:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:12:45		m

		S1148829601:		#B3q0		1148829601:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:13:15		m

		S1148829631:		#B3q0		1148829631:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:13:45		m

		S1148829661:		#B3q0		1148829661:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:14:15		m

		S1148829691:		#B3q0		1148829691:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:14:45		m

		S1148829721:		#B3q0		1148829721:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:15:15		m

		S1148829751:		#B3q0		1148829751:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		21:15:45		m

		S1148829781:		#B3q0		1148829781:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:16:15		m

		S1148829811:		#B3q0		1148829811:		$B3q0		fc		28.97		0		24.21		3.49		3.69		0		-29318.84		21:16:45		m

		S1148829841:		#B3q0		1148829841:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:17:15		m

		S1148829871:		#B3q0		1148829871:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:17:45		m

		S1148829901:		#B3q0		1148829901:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:18:15		m

		S1148829931:		#B3q0		1148829931:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:18:45		m

		S1148829961:		#B3q0		1148829961:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:19:15		m

		S1148829991:		#B3q0		1148829991:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:19:45		m

		S1148830021:		#B3q0		1148830021:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:20:15		m

		S1148830051:		#B3q0		1148830051:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:20:45		m

		S1148830081:		#B3q0		1148830081:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:21:15		m

		S1148830111:		#B3q0		1148830111:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:21:45		m

		S1148830141:		#B3q0		1148830141:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		21:22:15		m

		S1148830171:		#B3q0		1148830171:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		21:22:45		m

		S1148830201:		#B3q0		1148830201:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:23:15		m

		S1148830231:		#B3q0		1148830231:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:23:45		m

		S1148830261:		#B3q0		1148830261:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:24:15		m

		S1148830291:		#B3q0		1148830291:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:24:45		m

		S1148830321:		#B3q0		1148830321:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:25:15		m

		S1148830351:		#B3q0		1148830351:		$B3q0		fc		28.97		0		24.12		3.49		3.69		0		-29318.84		21:25:45		m

		S1148830381:		#B3q0		1148830381:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:26:15		m

		S1148830411:		#B3q0		1148830411:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:26:45		m

		S1148830441:		#B3q0		1148830441:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:27:15		m

		S1148830471:		#B3q0		1148830471:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:27:45		m

		S1148830501:		#B3q0		1148830501:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:28:15		m

		S1148830531:		#B3q0		1148830531:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:28:45		m

		S1148830561:		#B3q0		1148830561:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:29:15		m

		S1148830591:		#B3q0		1148830591:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:29:45		m

		S1148830621:		#B3q0		1148830621:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:30:15		m

		S1148830651:		#B3q0		1148830651:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:30:45		m

		S1148830681:		#B3q0		1148830681:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:31:15		m

		S1148830711:		#B3q0		1148830711:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:31:45		m

		S1148830741:		#B3q0		1148830741:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:32:15		m

		S1148830771:		#B3q0		1148830771:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:32:45		m

		S1148830801:		#B3q0		1148830801:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:33:15		m

		S1148830831:		#B3q0		1148830831:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:33:45		m

		S1148830861:		#B3q0		1148830861:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:34:15		m

		S1148830891:		#B3q0		1148830891:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:34:45		m

		S1148830921:		#B3q0		1148830921:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:35:15		m

		S1148830951:		#B3q0		1148830951:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:35:45		m

		S1148830981:		#B3q0		1148830981:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:36:15		m

		S1148831011:		#B3q0		1148831011:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:36:45		m

		S1148831041:		#B3q0		1148831041:		$B3q0		fc		29.01		0		24.21		3.49		3.69		0		-29318.84		21:37:15		m

		S1148831071:		#B3q0		1148831071:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:37:45		m

		S1148831101:		#B3q0		1148831101:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:38:15		m

		S1148831131:		#B3q0		1148831131:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:38:45		m

		S1148831161:		#B3q0		1148831161:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:39:15		m

		S1148831191:		#B3q0		1148831191:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:39:45		m

		S1148831221:		#B3q0		1148831221:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:40:15		m

		S1148831251:		#B3q0		1148831251:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:40:45		m

		S1148831281:		#B3q0		1148831281:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:41:15		m

		S1148831311:		#B3q0		1148831311:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:41:45		m

		S1148831341:		#B3q0		1148831341:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:42:15		m

		S1148831371:		#B3q0		1148831371:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:42:45		m

		S1148831401:		#B3q0		1148831401:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:43:15		m

		S1148831431:		#B3q0		1148831431:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:43:45		m

		S1148831461:		#B3q0		1148831461:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:44:15		m

		S1148831491:		#B3q0		1148831491:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:44:45		m

		S1148831521:		#B3q0		1148831521:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:45:15		m

		S1148831551:		#B3q0		1148831551:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:45:45		m

		S1148831581:		#B3q0		1148831581:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:46:15		m

		S1148831611:		#B3q0		1148831611:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:46:45		m

		S1148831641:		#B3q0		1148831641:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:47:15		m

		S1148831671:		#B3q0		1148831671:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:47:45		m

		S1148831701:		#B3q0		1148831701:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:48:15		m

		S1148831731:		#B3q0		1148831731:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:48:45		m

		S1148831761:		#B3q0		1148831761:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:49:15		m

		S1148831791:		#B3q0		1148831791:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:49:45		m

		S1148831821:		#B3q0		1148831821:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:50:15		m

		S1148831851:		#B3q0		1148831851:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:50:45		m

		S1148831881:		#B3q0		1148831881:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:51:15		m

		S1148831911:		#B3q0		1148831911:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:51:45		m

		S1148831941:		#B3q0		1148831941:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:52:15		m

		S1148831971:		#B3q0		1148831971:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:52:45		m

		S1148832001:		#B3q0		1148832001:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:53:15		m

		S1148832031:		#B3q0		1148832031:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:53:45		m

		S1148832061:		#B3q0		1148832061:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:54:15		m

		S1148832091:		#B3q0		1148832091:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		21:54:45		m

		S1148832121:		#B3q0		1148832121:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:55:15		m

		S1148832151:		#B3q0		1148832151:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:55:45		m

		S1148832181:		#B3q0		1148832181:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:56:15		m

		S1148832211:		#B3q0		1148832211:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:56:45		m

		S1148832241:		#B3q0		1148832241:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		21:57:15		m

		S1148832271:		#B3q0		1148832271:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:57:45		m

		S1148832301:		#B3q0		1148832301:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:58:15		m

		S1148832331:		#B3q0		1148832331:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		21:58:45		m

		S1148832361:		#B3q0		1148832361:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		21:59:15		m

		S1148832391:		#B3q0		1148832391:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		21:59:45		m

		S1148832421:		#B3q0		1148832421:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		22:00:15		m

		S1148832451:		#B3q0		1148832451:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:00:45		m

		S1148832481:		#B3q0		1148832481:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:01:15		m

		S1148832511:		#B3q0		1148832511:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:01:45		m

		S1148832541:		#B3q0		1148832541:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:02:15		m

		S1148832571:		#B3q0		1148832571:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:02:45		m

		S1148832601:		#B3q0		1148832601:		$B3q0		fc		29.05		0		24.21		3.49		3.69		0		-29318.84		22:03:15		m

		S1148832631:		#B3q0		1148832631:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:03:45		m

		S1148832661:		#B3q0		1148832661:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:04:15		m

		S1148832691:		#B3q0		1148832691:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:04:45		m

		S1148832721:		#B3q0		1148832721:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:05:15		m

		S1148832751:		#B3q0		1148832751:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:05:45		m

		S1148832781:		#B3q0		1148832781:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:06:15		m

		S1148832811:		#B3q0		1148832811:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:06:45		m

		S1148832841:		#B3q0		1148832841:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:07:15		m

		S1148832871:		#B3q0		1148832871:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:07:45		m

		S1148832901:		#B3q0		1148832901:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:08:15		m

		S1148832931:		#B3q0		1148832931:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:08:45		m

		S1148832961:		#B3q0		1148832961:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:09:15		m

		S1148832991:		#B3q0		1148832991:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:09:45		m

		S1148833021:		#B3q0		1148833021:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:10:15		m

		S1148833051:		#B3q0		1148833051:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:10:45		m

		S1148833081:		#B3q0		1148833081:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:11:15		m

		S1148833111:		#B3q0		1148833111:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:11:45		m

		S1148833141:		#B3q0		1148833141:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:12:15		m

		S1148833171:		#B3q0		1148833171:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:12:45		m

		S1148833201:		#B3q0		1148833201:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:13:15		m

		S1148833231:		#B3q0		1148833231:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:13:45		m

		S1148833261:		#B3q0		1148833261:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:14:15		m

		S1148833291:		#B3q0		1148833291:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:14:45		m

		S1148833321:		#B3q0		1148833321:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:15:15		m

		S1148833351:		#B3q0		1148833351:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:15:45		m

		S1148833381:		#B3q0		1148833381:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:16:15		m

		S1148833411:		#B3q0		1148833411:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:16:45		m

		S1148833441:		#B3q0		1148833441:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:17:15		m

		S1148833471:		#B3q0		1148833471:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:17:45		m

		S1148833501:		#B3q0		1148833501:		$B3q0		fc		29.05		0		24.12		3.49		3.69		0		-29318.84		22:18:15		m

		S1148833531:		#B3q0		1148833531:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:18:45		m

		S1148833561:		#B3q0		1148833561:		$B3q0		fc		29.01		0		23.92		3.49		3.69		0		-29318.84		22:19:15		m

		S1148833591:		#B3q0		1148833591:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:19:45		m

		S1148833621:		#B3q0		1148833621:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:20:15		m

		S1148833651:		#B3q0		1148833651:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:20:45		m

		S1148833681:		#B3q0		1148833681:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:21:15		m

		S1148833711:		#B3q0		1148833711:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:21:45		m

		S1148833741:		#B3q0		1148833741:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:22:15		m

		S1148833771:		#B3q0		1148833771:		$B3q0		fc		29.01		0		24.12		3.49		3.69		0		-29318.84		22:22:45		m

		S1148833801:		#B3q0		1148833801:		$B3q0		fc		29.05		0		23.92		3.49		3.69		0		-29318.84		22:23:15		m

		S1148833831:		#B3q0		1148833831:		$B3q0		fc		29.01		0		24.02		3.49		3.69		0		-29318.84		22:23:45		m

		S1148833861:		#B3q0		1148833861:		$B3q0		fc		29.05		0		24.02		3.49		3.69		0		-29318.84		22:24:15		m





B3_q1

		S1148753357:		#B3q1		1148753357:		$B3q1		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15

		S1148753387:		#B3q1		1148753387:		$B3q1		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15

		S1148753417:		#B3q1		1148753417:		$B3q1		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15

		S1148753447:		#B3q1		1148753447:		$B3q1		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15

		S1148753477:		#B3q1		1148753477:		$B3q1		4.12		4.14		4.12		4.12		4.13		4.13		4.13		4.13

		S1148753507:		#B3q1		1148753507:		$B3q1		4.12		4.14		4.12		4.12		4.13		4.13		4.13		4.12

		S1148753537:		#B3q1		1148753537:		$B3q1		4.12		4.13		4.12		4.12		4.13		4.13		4.13		4.12

		S1148753567:		#B3q1		1148753567:		$B3q1		4.12		4.13		4.11		4.11		4.12		4.12		4.13		4.12

		S1148753597:		#B3q1		1148753597:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12

		S1148753627:		#B3q1		1148753627:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12

		S1148753657:		#B3q1		1148753657:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12

		S1148753687:		#B3q1		1148753687:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12

		S1148753717:		#B3q1		1148753717:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12

		S1148753747:		#B3q1		1148753747:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12

		S1148753777:		#B3q1		1148753777:		$B3q1		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12

		S1148753807:		#B3q1		1148753807:		$B3q1		4.11		4.12		4.11		4.11		4.12		4.12		4.12		4.11

		S1148753837:		#B3q1		1148753837:		$B3q1		4.11		4.12		4.11		4.10		4.12		4.12		4.12		4.11

		S1148753867:		#B3q1		1148753867:		$B3q1		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11

		S1148753897:		#B3q1		1148753897:		$B3q1		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11

		S1148753927:		#B3q1		1148753927:		$B3q1		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11

		S1148753957:		#B3q1		1148753957:		$B3q1		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11

		S1148753987:		#B3q1		1148753987:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11

		S1148754017:		#B3q1		1148754017:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11

		S1148754047:		#B3q1		1148754047:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11

		S1148754077:		#B3q1		1148754077:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11

		S1148754107:		#B3q1		1148754107:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11

		S1148754137:		#B3q1		1148754137:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11

		S1148754167:		#B3q1		1148754167:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10

		S1148754197:		#B3q1		1148754197:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10

		S1148754227:		#B3q1		1148754227:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10

		S1148754257:		#B3q1		1148754257:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10

		S1148754287:		#B3q1		1148754287:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10

		S1148754317:		#B3q1		1148754317:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.11		4.10

		S1148754347:		#B3q1		1148754347:		$B3q1		4.10		4.12		4.10		4.10		4.11		4.11		4.11		4.10

		S1148754377:		#B3q1		1148754377:		$B3q1		4.10		4.12		4.10		4.10		4.10		4.11		4.11		4.10

		S1148754407:		#B3q1		1148754407:		$B3q1		4.10		4.12		4.10		4.09		4.10		4.11		4.11		4.10

		S1148754437:		#B3q1		1148754437:		$B3q1		4.10		4.12		4.10		4.09		4.10		4.11		4.11		4.10

		S1148754467:		#B3q1		1148754467:		$B3q1		4.09		4.12		4.10		4.09		4.10		4.11		4.11		4.10

		S1148754497:		#B3q1		1148754497:		$B3q1		4.09		4.11		4.10		4.09		4.10		4.11		4.11		4.10

		S1148754527:		#B3q1		1148754527:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754557:		#B3q1		1148754557:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754587:		#B3q1		1148754587:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754617:		#B3q1		1148754617:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754647:		#B3q1		1148754647:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754677:		#B3q1		1148754677:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754707:		#B3q1		1148754707:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754737:		#B3q1		1148754737:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10

		S1148754767:		#B3q1		1148754767:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.10

		S1148754797:		#B3q1		1148754797:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.10

		S1148754827:		#B3q1		1148754827:		$B3q1		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.09

		S1148754857:		#B3q1		1148754857:		$B3q1		4.09		4.11		4.09		4.08		4.10		4.10		4.10		4.09

		S1148754887:		#B3q1		1148754887:		$B3q1		4.09		4.11		4.09		4.08		4.10		4.10		4.10		4.09

		S1148754917:		#B3q1		1148754917:		$B3q1		4.08		4.11		4.09		4.08		4.10		4.10		4.10		4.09

		S1148754947:		#B3q1		1148754947:		$B3q1		4.08		4.11		4.09		4.08		4.10		4.10		4.10		4.09

		S1148754977:		#B3q1		1148754977:		$B3q1		4.08		4.10		4.08		4.08		4.10		4.10		4.10		4.09

		S1148755007:		#B3q1		1148755007:		$B3q1		4.08		4.10		4.08		4.08		4.10		4.10		4.10		4.09

		S1148755037:		#B3q1		1148755037:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755067:		#B3q1		1148755067:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755097:		#B3q1		1148755097:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755127:		#B3q1		1148755127:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755157:		#B3q1		1148755157:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755187:		#B3q1		1148755187:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755217:		#B3q1		1148755217:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09

		S1148755247:		#B3q1		1148755247:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755277:		#B3q1		1148755277:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755307:		#B3q1		1148755307:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755337:		#B3q1		1148755337:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755367:		#B3q1		1148755367:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755397:		#B3q1		1148755397:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755427:		#B3q1		1148755427:		$B3q1		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08

		S1148755457:		#B3q1		1148755457:		$B3q1		4.08		4.10		4.08		4.08		4.08		4.09		4.10		4.08

		S1148755487:		#B3q1		1148755487:		$B3q1		4.08		4.10		4.08		4.08		4.08		4.09		4.10		4.08

		S1148755517:		#B3q1		1148755517:		$B3q1		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755547:		#B3q1		1148755547:		$B3q1		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755577:		#B3q1		1148755577:		$B3q1		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755607:		#B3q1		1148755607:		$B3q1		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755637:		#B3q1		1148755637:		$B3q1		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755667:		#B3q1		1148755667:		$B3q1		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755697:		#B3q1		1148755697:		$B3q1		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08

		S1148755727:		#B3q1		1148755727:		$B3q1		4.07		4.10		4.07		4.07		4.08		4.09		4.09		4.08

		S1148755757:		#B3q1		1148755757:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.09		4.09		4.08

		S1148755787:		#B3q1		1148755787:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08

		S1148755817:		#B3q1		1148755817:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08

		S1148755847:		#B3q1		1148755847:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08

		S1148755877:		#B3q1		1148755877:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08

		S1148755907:		#B3q1		1148755907:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08

		S1148755937:		#B3q1		1148755937:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07

		S1148755967:		#B3q1		1148755967:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07

		S1148755997:		#B3q1		1148755997:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07

		S1148756027:		#B3q1		1148756027:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07

		S1148756057:		#B3q1		1148756057:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.08		4.07

		S1148756087:		#B3q1		1148756087:		$B3q1		4.07		4.09		4.07		4.07		4.08		4.08		4.08		4.07

		S1148756117:		#B3q1		1148756117:		$B3q1		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07

		S1148756147:		#B3q1		1148756147:		$B3q1		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07

		S1148756177:		#B3q1		1148756177:		$B3q1		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07

		S1148756207:		#B3q1		1148756207:		$B3q1		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07

		S1148756237:		#B3q1		1148756237:		$B3q1		4.07		4.09		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756267:		#B3q1		1148756267:		$B3q1		4.07		4.09		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756297:		#B3q1		1148756297:		$B3q1		4.07		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756327:		#B3q1		1148756327:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756357:		#B3q1		1148756357:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756387:		#B3q1		1148756387:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756417:		#B3q1		1148756417:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756447:		#B3q1		1148756447:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756477:		#B3q1		1148756477:		$B3q1		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07

		S1148756507:		#B3q1		1148756507:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07

		S1148756537:		#B3q1		1148756537:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07

		S1148756567:		#B3q1		1148756567:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07

		S1148756597:		#B3q1		1148756597:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.07

		S1148756627:		#B3q1		1148756627:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.07

		S1148756657:		#B3q1		1148756657:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.06

		S1148756687:		#B3q1		1148756687:		$B3q1		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.06

		S1148756717:		#B3q1		1148756717:		$B3q1		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06

		S1148756747:		#B3q1		1148756747:		$B3q1		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06

		S1148756777:		#B3q1		1148756777:		$B3q1		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06

		S1148756807:		#B3q1		1148756807:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.08		4.06

		S1148756837:		#B3q1		1148756837:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.08		4.06

		S1148756867:		#B3q1		1148756867:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148756897:		#B3q1		1148756897:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148756927:		#B3q1		1148756927:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148756957:		#B3q1		1148756957:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148756987:		#B3q1		1148756987:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148757017:		#B3q1		1148757017:		$B3q1		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06

		S1148757047:		#B3q1		1148757047:		$B3q1		4.05		4.08		4.05		4.05		4.06		4.07		4.07		4.06

		S1148757077:		#B3q1		1148757077:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.06

		S1148757107:		#B3q1		1148757107:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.06

		S1148757137:		#B3q1		1148757137:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757167:		#B3q1		1148757167:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757197:		#B3q1		1148757197:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757227:		#B3q1		1148757227:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757257:		#B3q1		1148757257:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757287:		#B3q1		1148757287:		$B3q1		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05

		S1148757317:		#B3q1		1148757317:		$B3q1		4.05		4.07		4.05		4.05		4.05		4.07		4.07		4.05

		S1148757347:		#B3q1		1148757347:		$B3q1		4.05		4.07		4.05		4.05		4.05		4.07		4.07		4.05

		S1148757377:		#B3q1		1148757377:		$B3q1		4.05		4.07		4.05		4.05		4.05		4.06		4.07		4.05

		S1148757407:		#B3q1		1148757407:		$B3q1		4.05		4.07		4.05		4.05		4.05		4.06		4.07		4.05

		S1148757437:		#B3q1		1148757437:		$B3q1		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757467:		#B3q1		1148757467:		$B3q1		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757497:		#B3q1		1148757497:		$B3q1		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757527:		#B3q1		1148757527:		$B3q1		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757557:		#B3q1		1148757557:		$B3q1		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757587:		#B3q1		1148757587:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757617:		#B3q1		1148757617:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757647:		#B3q1		1148757647:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757677:		#B3q1		1148757677:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05

		S1148757707:		#B3q1		1148757707:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05

		S1148757737:		#B3q1		1148757737:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05

		S1148757767:		#B3q1		1148757767:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05

		S1148757797:		#B3q1		1148757797:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05

		S1148757827:		#B3q1		1148757827:		$B3q1		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05

		S1148757857:		#B3q1		1148757857:		$B3q1		4.04		4.07		4.04		4.04		4.05		4.06		4.06		4.05

		S1148757887:		#B3q1		1148757887:		$B3q1		4.04		4.06		4.04		4.04		4.05		4.06		4.06		4.04

		S1148757917:		#B3q1		1148757917:		$B3q1		4.04		4.07		4.04		4.04		4.05		4.06		4.06		4.04

		S1148757947:		#B3q1		1148757947:		$B3q1		4.04		4.06		4.04		4.03		4.05		4.05		4.06		4.04

		S1148757977:		#B3q1		1148757977:		$B3q1		4.04		4.06		4.04		4.03		4.05		4.05		4.06		4.04

		S1148758007:		#B3q1		1148758007:		$B3q1		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758037:		#B3q1		1148758037:		$B3q1		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758067:		#B3q1		1148758067:		$B3q1		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758097:		#B3q1		1148758097:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758127:		#B3q1		1148758127:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758157:		#B3q1		1148758157:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758187:		#B3q1		1148758187:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758217:		#B3q1		1148758217:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04

		S1148758247:		#B3q1		1148758247:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04

		S1148758277:		#B3q1		1148758277:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04

		S1148758307:		#B3q1		1148758307:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04

		S1148758337:		#B3q1		1148758337:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04

		S1148758367:		#B3q1		1148758367:		$B3q1		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04

		S1148758397:		#B3q1		1148758397:		$B3q1		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03

		S1148758427:		#B3q1		1148758427:		$B3q1		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03

		S1148758457:		#B3q1		1148758457:		$B3q1		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03

		S1148758487:		#B3q1		1148758487:		$B3q1		4.03		4.05		4.03		4.03		4.04		4.05		4.05		4.03

		S1148758517:		#B3q1		1148758517:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758547:		#B3q1		1148758547:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758577:		#B3q1		1148758577:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758607:		#B3q1		1148758607:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758637:		#B3q1		1148758637:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758667:		#B3q1		1148758667:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758697:		#B3q1		1148758697:		$B3q1		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03

		S1148758727:		#B3q1		1148758727:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.05		4.05		4.03

		S1148758757:		#B3q1		1148758757:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.05		4.05		4.03

		S1148758787:		#B3q1		1148758787:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758817:		#B3q1		1148758817:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758847:		#B3q1		1148758847:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758877:		#B3q1		1148758877:		$B3q1		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758907:		#B3q1		1148758907:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758937:		#B3q1		1148758937:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758967:		#B3q1		1148758967:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148758997:		#B3q1		1148758997:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148759027:		#B3q1		1148759027:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03

		S1148759057:		#B3q1		1148759057:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03

		S1148759087:		#B3q1		1148759087:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03

		S1148759117:		#B3q1		1148759117:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03

		S1148759147:		#B3q1		1148759147:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02

		S1148759177:		#B3q1		1148759177:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02

		S1148759207:		#B3q1		1148759207:		$B3q1		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02

		S1148759237:		#B3q1		1148759237:		$B3q1		4.02		4.05		4.03		4.01		4.03		4.04		4.04		4.02

		S1148759267:		#B3q1		1148759267:		$B3q1		4.02		4.05		4.02		4.01		4.02		4.04		4.04		4.02

		S1148759297:		#B3q1		1148759297:		$B3q1		4.02		4.05		4.02		4.01		4.02		4.04		4.04		4.02

		S1148759327:		#B3q1		1148759327:		$B3q1		4.02		4.04		4.02		4.01		4.02		4.04		4.04		4.02

		S1148759357:		#B3q1		1148759357:		$B3q1		4.02		4.04		4.02		4.01		4.02		4.04		4.04		4.02

		S1148759387:		#B3q1		1148759387:		$B3q1		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759417:		#B3q1		1148759417:		$B3q1		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759447:		#B3q1		1148759447:		$B3q1		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759477:		#B3q1		1148759477:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759507:		#B3q1		1148759507:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759537:		#B3q1		1148759537:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759567:		#B3q1		1148759567:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759597:		#B3q1		1148759597:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759627:		#B3q1		1148759627:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759657:		#B3q1		1148759657:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02

		S1148759687:		#B3q1		1148759687:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.02

		S1148759717:		#B3q1		1148759717:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.01

		S1148759747:		#B3q1		1148759747:		$B3q1		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.01

		S1148759777:		#B3q1		1148759777:		$B3q1		4.01		4.04		4.02		4.01		4.01		4.03		4.03		4.01

		S1148759807:		#B3q1		1148759807:		$B3q1		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759837:		#B3q1		1148759837:		$B3q1		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759867:		#B3q1		1148759867:		$B3q1		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759897:		#B3q1		1148759897:		$B3q1		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759927:		#B3q1		1148759927:		$B3q1		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759957:		#B3q1		1148759957:		$B3q1		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01

		S1148759987:		#B3q1		1148759987:		$B3q1		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01

		S1148760017:		#B3q1		1148760017:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760047:		#B3q1		1148760047:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760077:		#B3q1		1148760077:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760107:		#B3q1		1148760107:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760137:		#B3q1		1148760137:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760167:		#B3q1		1148760167:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760197:		#B3q1		1148760197:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760227:		#B3q1		1148760227:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760257:		#B3q1		1148760257:		$B3q1		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01

		S1148760287:		#B3q1		1148760287:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760317:		#B3q1		1148760317:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760347:		#B3q1		1148760347:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760377:		#B3q1		1148760377:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760407:		#B3q1		1148760407:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760437:		#B3q1		1148760437:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760467:		#B3q1		1148760467:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01

		S1148760497:		#B3q1		1148760497:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.00

		S1148760527:		#B3q1		1148760527:		$B3q1		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.00

		S1148760557:		#B3q1		1148760557:		$B3q1		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00

		S1148760587:		#B3q1		1148760587:		$B3q1		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00

		S1148760617:		#B3q1		1148760617:		$B3q1		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00

		S1148760647:		#B3q1		1148760647:		$B3q1		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00

		S1148760677:		#B3q1		1148760677:		$B3q1		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00

		S1148760707:		#B3q1		1148760707:		$B3q1		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00

		S1148760737:		#B3q1		1148760737:		$B3q1		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00

		S1148760767:		#B3q1		1148760767:		$B3q1		4.00		4.03		4.00		3.99		4.00		4.02		4.02		4.00

		S1148760797:		#B3q1		1148760797:		$B3q1		4.00		4.03		4.00		3.99		4.00		4.02		4.02		4.00

		S1148760827:		#B3q1		1148760827:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.02		4.02		4.00

		S1148760857:		#B3q1		1148760857:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.02		4.02		4.00

		S1148760887:		#B3q1		1148760887:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148760917:		#B3q1		1148760917:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148760947:		#B3q1		1148760947:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148760977:		#B3q1		1148760977:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761007:		#B3q1		1148761007:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761037:		#B3q1		1148761037:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761067:		#B3q1		1148761067:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761097:		#B3q1		1148761097:		$B3q1		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761127:		#B3q1		1148761127:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761157:		#B3q1		1148761157:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.02		4.00

		S1148761187:		#B3q1		1148761187:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00

		S1148761217:		#B3q1		1148761217:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00

		S1148761247:		#B3q1		1148761247:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00

		S1148761277:		#B3q1		1148761277:		$B3q1		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00

		S1148761307:		#B3q1		1148761307:		$B3q1		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761337:		#B3q1		1148761337:		$B3q1		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761367:		#B3q1		1148761367:		$B3q1		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761397:		#B3q1		1148761397:		$B3q1		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761427:		#B3q1		1148761427:		$B3q1		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761457:		#B3q1		1148761457:		$B3q1		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761487:		#B3q1		1148761487:		$B3q1		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99

		S1148761517:		#B3q1		1148761517:		$B3q1		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761547:		#B3q1		1148761547:		$B3q1		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761577:		#B3q1		1148761577:		$B3q1		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761607:		#B3q1		1148761607:		$B3q1		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761637:		#B3q1		1148761637:		$B3q1		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761667:		#B3q1		1148761667:		$B3q1		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761697:		#B3q1		1148761697:		$B3q1		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761727:		#B3q1		1148761727:		$B3q1		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761757:		#B3q1		1148761757:		$B3q1		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99

		S1148761787:		#B3q1		1148761787:		$B3q1		3.98		4.01		3.99		3.98		3.99		4.00		4.01		3.99

		S1148761817:		#B3q1		1148761817:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761847:		#B3q1		1148761847:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761877:		#B3q1		1148761877:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761907:		#B3q1		1148761907:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761937:		#B3q1		1148761937:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761967:		#B3q1		1148761967:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148761997:		#B3q1		1148761997:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148762027:		#B3q1		1148762027:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98

		S1148762057:		#B3q1		1148762057:		$B3q1		3.98		4.01		3.99		3.98		3.98		4.00		4.00		3.98

		S1148762087:		#B3q1		1148762087:		$B3q1		3.98		4.01		3.98		3.98		3.98		4.00		4.00		3.98

		S1148762117:		#B3q1		1148762117:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762147:		#B3q1		1148762147:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762177:		#B3q1		1148762177:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762207:		#B3q1		1148762207:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762237:		#B3q1		1148762237:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762267:		#B3q1		1148762267:		$B3q1		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762297:		#B3q1		1148762297:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762327:		#B3q1		1148762327:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762357:		#B3q1		1148762357:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762387:		#B3q1		1148762387:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762417:		#B3q1		1148762417:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762447:		#B3q1		1148762447:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762477:		#B3q1		1148762477:		$B3q1		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762507:		#B3q1		1148762507:		$B3q1		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762537:		#B3q1		1148762537:		$B3q1		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762567:		#B3q1		1148762567:		$B3q1		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762597:		#B3q1		1148762597:		$B3q1		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98

		S1148762627:		#B3q1		1148762627:		$B3q1		3.97		4.00		3.98		3.97		3.97		4.00		4.00		3.98

		S1148762657:		#B3q1		1148762657:		$B3q1		3.97		4.00		3.98		3.97		3.97		4.00		4.00		3.97

		S1148762687:		#B3q1		1148762687:		$B3q1		3.97		4.00		3.98		3.96		3.97		4.00		4.00		3.97

		S1148762717:		#B3q1		1148762717:		$B3q1		3.97		4.00		3.98		3.96		3.97		4.00		4.00		3.97

		S1148762747:		#B3q1		1148762747:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762777:		#B3q1		1148762777:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762807:		#B3q1		1148762807:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762837:		#B3q1		1148762837:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762867:		#B3q1		1148762867:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762897:		#B3q1		1148762897:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762927:		#B3q1		1148762927:		$B3q1		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97

		S1148762957:		#B3q1		1148762957:		$B3q1		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148762987:		#B3q1		1148762987:		$B3q1		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763017:		#B3q1		1148763017:		$B3q1		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763047:		#B3q1		1148763047:		$B3q1		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763077:		#B3q1		1148763077:		$B3q1		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763107:		#B3q1		1148763107:		$B3q1		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763137:		#B3q1		1148763137:		$B3q1		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763167:		#B3q1		1148763167:		$B3q1		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97

		S1148763197:		#B3q1		1148763197:		$B3q1		3.96		4.00		3.97		3.96		3.96		3.99		3.99		3.96

		S1148763227:		#B3q1		1148763227:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96

		S1148763257:		#B3q1		1148763257:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96

		S1148763287:		#B3q1		1148763287:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96

		S1148763317:		#B3q1		1148763317:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96

		S1148763347:		#B3q1		1148763347:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763377:		#B3q1		1148763377:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763407:		#B3q1		1148763407:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763437:		#B3q1		1148763437:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763467:		#B3q1		1148763467:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763497:		#B3q1		1148763497:		$B3q1		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96

		S1148763527:		#B3q1		1148763527:		$B3q1		3.96		3.99		3.97		3.95		3.96		3.98		3.98		3.96

		S1148763557:		#B3q1		1148763557:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763587:		#B3q1		1148763587:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763617:		#B3q1		1148763617:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763647:		#B3q1		1148763647:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763677:		#B3q1		1148763677:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763707:		#B3q1		1148763707:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763737:		#B3q1		1148763737:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763767:		#B3q1		1148763767:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763797:		#B3q1		1148763797:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763827:		#B3q1		1148763827:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763857:		#B3q1		1148763857:		$B3q1		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763887:		#B3q1		1148763887:		$B3q1		3.96		3.98		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763917:		#B3q1		1148763917:		$B3q1		3.96		3.98		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763947:		#B3q1		1148763947:		$B3q1		3.95		3.98		3.96		3.95		3.96		3.98		3.98		3.96

		S1148763977:		#B3q1		1148763977:		$B3q1		3.95		3.98		3.96		3.95		3.96		3.98		3.98		3.96

		S1148764007:		#B3q1		1148764007:		$B3q1		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.96

		S1148764037:		#B3q1		1148764037:		$B3q1		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.96

		S1148764067:		#B3q1		1148764067:		$B3q1		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.95

		S1148764097:		#B3q1		1148764097:		$B3q1		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.95

		S1148764127:		#B3q1		1148764127:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764157:		#B3q1		1148764157:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764187:		#B3q1		1148764187:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764217:		#B3q1		1148764217:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764247:		#B3q1		1148764247:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764277:		#B3q1		1148764277:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95

		S1148764307:		#B3q1		1148764307:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95

		S1148764337:		#B3q1		1148764337:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95

		S1148764367:		#B3q1		1148764367:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95

		S1148764397:		#B3q1		1148764397:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95

		S1148764427:		#B3q1		1148764427:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95

		S1148764457:		#B3q1		1148764457:		$B3q1		3.95		3.98		3.96		3.94		3.95		3.97		3.97		3.95

		S1148764487:		#B3q1		1148764487:		$B3q1		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95

		S1148764517:		#B3q1		1148764517:		$B3q1		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95

		S1148764547:		#B3q1		1148764547:		$B3q1		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95

		S1148764577:		#B3q1		1148764577:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.95

		S1148764607:		#B3q1		1148764607:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.95

		S1148764637:		#B3q1		1148764637:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764667:		#B3q1		1148764667:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764697:		#B3q1		1148764697:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764727:		#B3q1		1148764727:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764757:		#B3q1		1148764757:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764787:		#B3q1		1148764787:		$B3q1		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764817:		#B3q1		1148764817:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764847:		#B3q1		1148764847:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764877:		#B3q1		1148764877:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94

		S1148764907:		#B3q1		1148764907:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94

		S1148764937:		#B3q1		1148764937:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94

		S1148764967:		#B3q1		1148764967:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94

		S1148764997:		#B3q1		1148764997:		$B3q1		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94

		S1148765027:		#B3q1		1148765027:		$B3q1		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94

		S1148765057:		#B3q1		1148765057:		$B3q1		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94

		S1148765087:		#B3q1		1148765087:		$B3q1		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94

		S1148765117:		#B3q1		1148765117:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765147:		#B3q1		1148765147:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765177:		#B3q1		1148765177:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765207:		#B3q1		1148765207:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765237:		#B3q1		1148765237:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765267:		#B3q1		1148765267:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765297:		#B3q1		1148765297:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765327:		#B3q1		1148765327:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765357:		#B3q1		1148765357:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765387:		#B3q1		1148765387:		$B3q1		3.94		3.96		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765417:		#B3q1		1148765417:		$B3q1		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94

		S1148765447:		#B3q1		1148765447:		$B3q1		3.94		3.96		3.94		3.93		3.93		3.96		3.96		3.94

		S1148768611:		#B3q1		1148768612:		$B3q1		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89

		S1148768641:		#B3q1		1148768641:		$B3q1		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768671:		#B3q1		1148768671:		$B3q1		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89

		S1148768701:		#B3q1		1148768701:		$B3q1		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89

		S1148768731:		#B3q1		1148768731:		$B3q1		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768761:		#B3q1		1148768761:		$B3q1		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768791:		#B3q1		1148768791:		$B3q1		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768821:		#B3q1		1148768821:		$B3q1		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768851:		#B3q1		1148768851:		$B3q1		3.89		3.92		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768881:		#B3q1		1148768881:		$B3q1		3.89		3.92		3.90		3.89		3.89		3.92		3.92		3.89

		S1148768911:		#B3q1		1148768911:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148768941:		#B3q1		1148768941:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148768971:		#B3q1		1148768971:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769001:		#B3q1		1148769001:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769031:		#B3q1		1148769031:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769061:		#B3q1		1148769061:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769091:		#B3q1		1148769091:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769121:		#B3q1		1148769121:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769151:		#B3q1		1148769151:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769181:		#B3q1		1148769181:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769211:		#B3q1		1148769211:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769241:		#B3q1		1148769241:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769271:		#B3q1		1148769271:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769301:		#B3q1		1148769301:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769331:		#B3q1		1148769331:		$B3q1		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89

		S1148769361:		#B3q1		1148769361:		$B3q1		3.89		3.92		3.89		3.88		3.89		3.91		3.92		3.89

		S1148769391:		#B3q1		1148769391:		$B3q1		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.89

		S1148769421:		#B3q1		1148769421:		$B3q1		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.89

		S1148769451:		#B3q1		1148769451:		$B3q1		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.88

		S1148769481:		#B3q1		1148769481:		$B3q1		3.88		3.92		3.89		3.88		3.88		3.91		3.92		3.88

		S1148769511:		#B3q1		1148769511:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.92		3.88

		S1148769541:		#B3q1		1148769541:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769571:		#B3q1		1148769571:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769601:		#B3q1		1148769601:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769631:		#B3q1		1148769631:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769661:		#B3q1		1148769661:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769691:		#B3q1		1148769691:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769721:		#B3q1		1148769721:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769751:		#B3q1		1148769751:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769781:		#B3q1		1148769781:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769811:		#B3q1		1148769811:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769841:		#B3q1		1148769841:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769871:		#B3q1		1148769871:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769901:		#B3q1		1148769901:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769931:		#B3q1		1148769931:		$B3q1		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88

		S1148769961:		#B3q1		1148769961:		$B3q1		3.88		3.92		3.89		3.87		3.87		3.91		3.91		3.88

		S1148769991:		#B3q1		1148769991:		$B3q1		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.88

		S1148770021:		#B3q1		1148770021:		$B3q1		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770051:		#B3q1		1148770051:		$B3q1		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770081:		#B3q1		1148770081:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770111:		#B3q1		1148770111:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770141:		#B3q1		1148770141:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770171:		#B3q1		1148770171:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770201:		#B3q1		1148770201:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770231:		#B3q1		1148770231:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770261:		#B3q1		1148770261:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770291:		#B3q1		1148770291:		$B3q1		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87

		S1148770321:		#B3q1		1148770321:		$B3q1		3.87		3.91		3.88		3.87		3.87		3.91		3.91		3.87

		S1148770351:		#B3q1		1148770351:		$B3q1		3.87		3.91		3.88		3.87		3.87		3.91		3.91		3.87

		S1148770381:		#B3q1		1148770381:		$B3q1		3.87		3.91		3.88		3.87		3.87		3.90		3.91		3.87

		S1148770411:		#B3q1		1148770411:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770441:		#B3q1		1148770441:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770471:		#B3q1		1148770471:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770501:		#B3q1		1148770501:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770531:		#B3q1		1148770531:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770561:		#B3q1		1148770561:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770591:		#B3q1		1148770591:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87

		S1148770621:		#B3q1		1148770621:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770651:		#B3q1		1148770651:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770681:		#B3q1		1148770681:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770711:		#B3q1		1148770711:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770741:		#B3q1		1148770741:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770771:		#B3q1		1148770771:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770801:		#B3q1		1148770801:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770831:		#B3q1		1148770831:		$B3q1		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87

		S1148770861:		#B3q1		1148770861:		$B3q1		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.87

		S1148770891:		#B3q1		1148770891:		$B3q1		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.86

		S1148770921:		#B3q1		1148770921:		$B3q1		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.86

		S1148770951:		#B3q1		1148770951:		$B3q1		3.87		3.91		3.87		3.86		3.86		3.90		3.90		3.86

		S1148770981:		#B3q1		1148770981:		$B3q1		3.87		3.91		3.87		3.86		3.86		3.90		3.90		3.86

		S1148771011:		#B3q1		1148771011:		$B3q1		3.87		3.90		3.87		3.86		3.86		3.90		3.90		3.86

		S1148771041:		#B3q1		1148771041:		$B3q1		3.87		3.90		3.87		3.86		3.86		3.89		3.90		3.86

		S1148771071:		#B3q1		1148771071:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771101:		#B3q1		1148771101:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771131:		#B3q1		1148771131:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771161:		#B3q1		1148771161:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771191:		#B3q1		1148771191:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771221:		#B3q1		1148771221:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771251:		#B3q1		1148771251:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86

		S1148771281:		#B3q1		1148771281:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771311:		#B3q1		1148771311:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771341:		#B3q1		1148771341:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771371:		#B3q1		1148771371:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771401:		#B3q1		1148771401:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771431:		#B3q1		1148771431:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771461:		#B3q1		1148771461:		$B3q1		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86

		S1148771491:		#B3q1		1148771491:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.86

		S1148771521:		#B3q1		1148771521:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771551:		#B3q1		1148771551:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771581:		#B3q1		1148771581:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771611:		#B3q1		1148771611:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771641:		#B3q1		1148771641:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771671:		#B3q1		1148771671:		$B3q1		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771701:		#B3q1		1148771701:		$B3q1		3.86		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771731:		#B3q1		1148771731:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771761:		#B3q1		1148771761:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771791:		#B3q1		1148771791:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771821:		#B3q1		1148771821:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771851:		#B3q1		1148771851:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771881:		#B3q1		1148771881:		$B3q1		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85

		S1148771911:		#B3q1		1148771911:		$B3q1		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85

		S1148771941:		#B3q1		1148771941:		$B3q1		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85

		S1148771971:		#B3q1		1148771971:		$B3q1		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85

		S1148772001:		#B3q1		1148772001:		$B3q1		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85

		S1148772031:		#B3q1		1148772031:		$B3q1		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85

		S1148772061:		#B3q1		1148772061:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772091:		#B3q1		1148772091:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772121:		#B3q1		1148772121:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772151:		#B3q1		1148772151:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772181:		#B3q1		1148772181:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772211:		#B3q1		1148772211:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772241:		#B3q1		1148772241:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772271:		#B3q1		1148772271:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85

		S1148772301:		#B3q1		1148772301:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85

		S1148772331:		#B3q1		1148772331:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85

		S1148772361:		#B3q1		1148772361:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85

		S1148772391:		#B3q1		1148772391:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85

		S1148772421:		#B3q1		1148772421:		$B3q1		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85

		S1148772451:		#B3q1		1148772451:		$B3q1		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.85

		S1148772481:		#B3q1		1148772481:		$B3q1		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.85

		S1148772511:		#B3q1		1148772511:		$B3q1		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84

		S1148772541:		#B3q1		1148772541:		$B3q1		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84

		S1148772571:		#B3q1		1148772571:		$B3q1		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84

		S1148772601:		#B3q1		1148772601:		$B3q1		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84

		S1148772631:		#B3q1		1148772631:		$B3q1		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84

		S1148772661:		#B3q1		1148772661:		$B3q1		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84

		S1148772691:		#B3q1		1148772691:		$B3q1		3.85		3.88		3.85		3.84		3.84		3.87		3.88		3.84

		S1148772721:		#B3q1		1148772721:		$B3q1		3.85		3.88		3.85		3.84		3.84		3.87		3.88		3.84

		S1148772751:		#B3q1		1148772751:		$B3q1		3.84		3.88		3.85		3.84		3.84		3.87		3.88		3.84

		S1148772781:		#B3q1		1148772781:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84

		S1148772811:		#B3q1		1148772811:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84

		S1148772841:		#B3q1		1148772841:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84

		S1148772871:		#B3q1		1148772871:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84

		S1148772901:		#B3q1		1148772901:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84

		S1148772931:		#B3q1		1148772931:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148772961:		#B3q1		1148772961:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148772991:		#B3q1		1148772991:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773021:		#B3q1		1148773021:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773051:		#B3q1		1148773051:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773081:		#B3q1		1148773081:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773111:		#B3q1		1148773111:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773141:		#B3q1		1148773141:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773171:		#B3q1		1148773171:		$B3q1		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84

		S1148773201:		#B3q1		1148773201:		$B3q1		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773231:		#B3q1		1148773231:		$B3q1		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773261:		#B3q1		1148773261:		$B3q1		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773291:		#B3q1		1148773291:		$B3q1		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773321:		#B3q1		1148773321:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773351:		#B3q1		1148773351:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773381:		#B3q1		1148773381:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773411:		#B3q1		1148773411:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773441:		#B3q1		1148773441:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773471:		#B3q1		1148773471:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773501:		#B3q1		1148773501:		$B3q1		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773531:		#B3q1		1148773531:		$B3q1		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773561:		#B3q1		1148773561:		$B3q1		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773591:		#B3q1		1148773591:		$B3q1		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773621:		#B3q1		1148773621:		$B3q1		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773651:		#B3q1		1148773651:		$B3q1		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83

		S1148773681:		#B3q1		1148773681:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773711:		#B3q1		1148773711:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773741:		#B3q1		1148773741:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773771:		#B3q1		1148773771:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773801:		#B3q1		1148773801:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773831:		#B3q1		1148773831:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773861:		#B3q1		1148773861:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773891:		#B3q1		1148773891:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773921:		#B3q1		1148773921:		$B3q1		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83

		S1148773951:		#B3q1		1148773951:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148773981:		#B3q1		1148773981:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774011:		#B3q1		1148774011:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774041:		#B3q1		1148774041:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774071:		#B3q1		1148774071:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774101:		#B3q1		1148774101:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774131:		#B3q1		1148774131:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774161:		#B3q1		1148774161:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774191:		#B3q1		1148774191:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774221:		#B3q1		1148774221:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774251:		#B3q1		1148774251:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774281:		#B3q1		1148774281:		$B3q1		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83

		S1148774311:		#B3q1		1148774311:		$B3q1		3.83		3.87		3.84		3.82		3.82		3.86		3.86		3.83

		S1148774341:		#B3q1		1148774341:		$B3q1		3.83		3.86		3.84		3.82		3.82		3.86		3.86		3.83

		S1148774371:		#B3q1		1148774371:		$B3q1		3.83		3.86		3.84		3.82		3.82		3.86		3.86		3.83

		S1148774401:		#B3q1		1148774401:		$B3q1		3.83		3.86		3.84		3.82		3.82		3.85		3.86		3.82

		S1148774431:		#B3q1		1148774431:		$B3q1		3.83		3.86		3.84		3.82		3.82		3.85		3.86		3.82

		S1148774461:		#B3q1		1148774461:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774491:		#B3q1		1148774491:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774521:		#B3q1		1148774521:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774551:		#B3q1		1148774551:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774581:		#B3q1		1148774581:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774611:		#B3q1		1148774611:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774641:		#B3q1		1148774641:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774671:		#B3q1		1148774671:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82

		S1148774701:		#B3q1		1148774701:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774731:		#B3q1		1148774731:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774761:		#B3q1		1148774761:		$B3q1		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774791:		#B3q1		1148774791:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774821:		#B3q1		1148774821:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774851:		#B3q1		1148774851:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774881:		#B3q1		1148774881:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774911:		#B3q1		1148774911:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774941:		#B3q1		1148774941:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148774971:		#B3q1		1148774971:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775001:		#B3q1		1148775001:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775031:		#B3q1		1148775031:		$B3q1		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775061:		#B3q1		1148775061:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775091:		#B3q1		1148775091:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775121:		#B3q1		1148775121:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775151:		#B3q1		1148775151:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775181:		#B3q1		1148775181:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775211:		#B3q1		1148775211:		$B3q1		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82

		S1148775241:		#B3q1		1148775241:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775271:		#B3q1		1148775271:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775301:		#B3q1		1148775301:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775331:		#B3q1		1148775331:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775361:		#B3q1		1148775361:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775391:		#B3q1		1148775391:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775421:		#B3q1		1148775421:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775451:		#B3q1		1148775451:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775481:		#B3q1		1148775481:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775511:		#B3q1		1148775511:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82

		S1148775541:		#B3q1		1148775541:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.84		3.85		3.82

		S1148775571:		#B3q1		1148775571:		$B3q1		3.82		3.85		3.83		3.81		3.82		3.84		3.85		3.82

		S1148775601:		#B3q1		1148775601:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.82

		S1148775631:		#B3q1		1148775631:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.82

		S1148775661:		#B3q1		1148775661:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81

		S1148775691:		#B3q1		1148775691:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81

		S1148775721:		#B3q1		1148775721:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81

		S1148775751:		#B3q1		1148775751:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81

		S1148775781:		#B3q1		1148775781:		$B3q1		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81

		S1148775811:		#B3q1		1148775811:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775841:		#B3q1		1148775841:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775871:		#B3q1		1148775871:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775901:		#B3q1		1148775901:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775931:		#B3q1		1148775931:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775961:		#B3q1		1148775961:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148775991:		#B3q1		1148775991:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776021:		#B3q1		1148776021:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776051:		#B3q1		1148776051:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776081:		#B3q1		1148776081:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776111:		#B3q1		1148776111:		$B3q1		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776141:		#B3q1		1148776141:		$B3q1		3.81		3.85		3.82		3.81		3.81		3.84		3.84		3.81

		S1148776171:		#B3q1		1148776171:		$B3q1		3.81		3.85		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776201:		#B3q1		1148776201:		$B3q1		3.81		3.85		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776231:		#B3q1		1148776231:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776261:		#B3q1		1148776261:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776291:		#B3q1		1148776291:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776321:		#B3q1		1148776321:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776351:		#B3q1		1148776351:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81

		S1148776381:		#B3q1		1148776381:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81

		S1148776411:		#B3q1		1148776411:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81

		S1148776441:		#B3q1		1148776441:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81

		S1148776471:		#B3q1		1148776471:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81

		S1148776501:		#B3q1		1148776501:		$B3q1		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81

		S1148776531:		#B3q1		1148776531:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.81

		S1148776561:		#B3q1		1148776561:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.81

		S1148776591:		#B3q1		1148776591:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80

		S1148776621:		#B3q1		1148776621:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80

		S1148776651:		#B3q1		1148776651:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80

		S1148776681:		#B3q1		1148776681:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776711:		#B3q1		1148776711:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776741:		#B3q1		1148776741:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776771:		#B3q1		1148776771:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776801:		#B3q1		1148776801:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776831:		#B3q1		1148776831:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776861:		#B3q1		1148776861:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776891:		#B3q1		1148776891:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776921:		#B3q1		1148776921:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776951:		#B3q1		1148776951:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148776981:		#B3q1		1148776981:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777011:		#B3q1		1148777011:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777041:		#B3q1		1148777041:		$B3q1		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777071:		#B3q1		1148777071:		$B3q1		3.81		3.83		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777101:		#B3q1		1148777101:		$B3q1		3.81		3.83		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777131:		#B3q1		1148777131:		$B3q1		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777161:		#B3q1		1148777161:		$B3q1		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777191:		#B3q1		1148777191:		$B3q1		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80

		S1148777221:		#B3q1		1148777221:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777251:		#B3q1		1148777251:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777281:		#B3q1		1148777281:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777311:		#B3q1		1148777311:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777341:		#B3q1		1148777341:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777371:		#B3q1		1148777371:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777401:		#B3q1		1148777401:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777431:		#B3q1		1148777431:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777461:		#B3q1		1148777461:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777491:		#B3q1		1148777491:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777521:		#B3q1		1148777521:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777551:		#B3q1		1148777551:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777581:		#B3q1		1148777581:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777611:		#B3q1		1148777611:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777641:		#B3q1		1148777641:		$B3q1		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80

		S1148777671:		#B3q1		1148777671:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80

		S1148777701:		#B3q1		1148777701:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80

		S1148777731:		#B3q1		1148777731:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80

		S1148777761:		#B3q1		1148777761:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777791:		#B3q1		1148777791:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777821:		#B3q1		1148777821:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777851:		#B3q1		1148777851:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777881:		#B3q1		1148777881:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777911:		#B3q1		1148777911:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777941:		#B3q1		1148777941:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148777971:		#B3q1		1148777971:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80

		S1148778001:		#B3q1		1148778001:		$B3q1		3.80		3.83		3.81		3.79		3.80		3.82		3.82		3.80

		S1148778031:		#B3q1		1148778031:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.80

		S1148778061:		#B3q1		1148778061:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.80

		S1148778091:		#B3q1		1148778091:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79

		S1148778121:		#B3q1		1148778121:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79

		S1148778151:		#B3q1		1148778151:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79

		S1148778181:		#B3q1		1148778181:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79

		S1148778211:		#B3q1		1148778211:		$B3q1		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79

		S1148778241:		#B3q1		1148778241:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778271:		#B3q1		1148778271:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778301:		#B3q1		1148778301:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778331:		#B3q1		1148778331:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778361:		#B3q1		1148778361:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778391:		#B3q1		1148778391:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778421:		#B3q1		1148778421:		$B3q1		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778451:		#B3q1		1148778451:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778481:		#B3q1		1148778481:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778511:		#B3q1		1148778511:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778541:		#B3q1		1148778541:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778571:		#B3q1		1148778571:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778601:		#B3q1		1148778601:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778631:		#B3q1		1148778631:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778661:		#B3q1		1148778661:		$B3q1		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778691:		#B3q1		1148778691:		$B3q1		3.79		3.82		3.80		3.79		3.79		3.82		3.82		3.79

		S1148778721:		#B3q1		1148778721:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778751:		#B3q1		1148778751:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778781:		#B3q1		1148778781:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778811:		#B3q1		1148778811:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778841:		#B3q1		1148778841:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778871:		#B3q1		1148778871:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778901:		#B3q1		1148778901:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778931:		#B3q1		1148778931:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778961:		#B3q1		1148778961:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148778991:		#B3q1		1148778991:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148779021:		#B3q1		1148779021:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148779051:		#B3q1		1148779051:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148779081:		#B3q1		1148779081:		$B3q1		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79

		S1148779111:		#B3q1		1148779111:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.79

		S1148779141:		#B3q1		1148779141:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779171:		#B3q1		1148779171:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779201:		#B3q1		1148779201:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779231:		#B3q1		1148779231:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779261:		#B3q1		1148779261:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779291:		#B3q1		1148779291:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78

		S1148779321:		#B3q1		1148779321:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779351:		#B3q1		1148779351:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779381:		#B3q1		1148779381:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779411:		#B3q1		1148779411:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779441:		#B3q1		1148779441:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779471:		#B3q1		1148779471:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779501:		#B3q1		1148779501:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78

		S1148779531:		#B3q1		1148779531:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779561:		#B3q1		1148779561:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779591:		#B3q1		1148779591:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779621:		#B3q1		1148779621:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779651:		#B3q1		1148779651:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779681:		#B3q1		1148779681:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779711:		#B3q1		1148779711:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779741:		#B3q1		1148779741:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779771:		#B3q1		1148779771:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779801:		#B3q1		1148779801:		$B3q1		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779831:		#B3q1		1148779831:		$B3q1		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779861:		#B3q1		1148779861:		$B3q1		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779891:		#B3q1		1148779891:		$B3q1		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78

		S1148779921:		#B3q1		1148779921:		$B3q1		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78

		S1148779951:		#B3q1		1148779951:		$B3q1		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78

		S1148779981:		#B3q1		1148779981:		$B3q1		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780011:		#B3q1		1148780011:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780041:		#B3q1		1148780041:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780071:		#B3q1		1148780071:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780101:		#B3q1		1148780101:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780131:		#B3q1		1148780131:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780161:		#B3q1		1148780161:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780191:		#B3q1		1148780191:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780221:		#B3q1		1148780221:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780251:		#B3q1		1148780251:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780281:		#B3q1		1148780281:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780311:		#B3q1		1148780311:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780341:		#B3q1		1148780341:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78

		S1148780371:		#B3q1		1148780371:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78

		S1148780401:		#B3q1		1148780401:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78

		S1148780431:		#B3q1		1148780431:		$B3q1		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78

		S1148780461:		#B3q1		1148780461:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780491:		#B3q1		1148780491:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780521:		#B3q1		1148780521:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780551:		#B3q1		1148780551:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780581:		#B3q1		1148780581:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780611:		#B3q1		1148780611:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78

		S1148780641:		#B3q1		1148780641:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78

		S1148780671:		#B3q1		1148780671:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78

		S1148780701:		#B3q1		1148780701:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78

		S1148780731:		#B3q1		1148780731:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78

		S1148780761:		#B3q1		1148780761:		$B3q1		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78

		S1148780791:		#B3q1		1148780791:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78

		S1148780821:		#B3q1		1148780821:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78

		S1148780851:		#B3q1		1148780851:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78

		S1148780881:		#B3q1		1148780881:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148780911:		#B3q1		1148780911:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148780941:		#B3q1		1148780941:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148780971:		#B3q1		1148780971:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148781001:		#B3q1		1148781001:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148781031:		#B3q1		1148781031:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148781061:		#B3q1		1148781061:		$B3q1		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77

		S1148781091:		#B3q1		1148781091:		$B3q1		3.78		3.81		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781121:		#B3q1		1148781121:		$B3q1		3.78		3.81		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781151:		#B3q1		1148781151:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781181:		#B3q1		1148781181:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781211:		#B3q1		1148781211:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781241:		#B3q1		1148781241:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781271:		#B3q1		1148781271:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781301:		#B3q1		1148781301:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781331:		#B3q1		1148781331:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781361:		#B3q1		1148781361:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781391:		#B3q1		1148781391:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781421:		#B3q1		1148781421:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781451:		#B3q1		1148781451:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781481:		#B3q1		1148781481:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781511:		#B3q1		1148781511:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781541:		#B3q1		1148781541:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781571:		#B3q1		1148781571:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781601:		#B3q1		1148781601:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781631:		#B3q1		1148781631:		$B3q1		3.78		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781661:		#B3q1		1148781661:		$B3q1		3.77		3.80		3.78		3.77		3.77		3.80		3.80		3.77

		S1148781691:		#B3q1		1148781691:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781721:		#B3q1		1148781721:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781751:		#B3q1		1148781751:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781781:		#B3q1		1148781781:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781811:		#B3q1		1148781811:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781841:		#B3q1		1148781841:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781871:		#B3q1		1148781871:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781901:		#B3q1		1148781901:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781931:		#B3q1		1148781931:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781961:		#B3q1		1148781961:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148781991:		#B3q1		1148781991:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148782021:		#B3q1		1148782021:		$B3q1		3.77		3.80		3.78		3.76		3.77		3.80		3.80		3.77

		S1148782051:		#B3q1		1148782051:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.80		3.80		3.76

		S1148782081:		#B3q1		1148782081:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.80		3.80		3.76

		S1148782111:		#B3q1		1148782111:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782141:		#B3q1		1148782141:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782171:		#B3q1		1148782171:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782201:		#B3q1		1148782201:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782231:		#B3q1		1148782231:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782261:		#B3q1		1148782261:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782291:		#B3q1		1148782291:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782321:		#B3q1		1148782321:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782351:		#B3q1		1148782351:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782381:		#B3q1		1148782381:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.80		3.76

		S1148782411:		#B3q1		1148782411:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782441:		#B3q1		1148782441:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782471:		#B3q1		1148782471:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782501:		#B3q1		1148782501:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782531:		#B3q1		1148782531:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782561:		#B3q1		1148782561:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782591:		#B3q1		1148782591:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782621:		#B3q1		1148782621:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782651:		#B3q1		1148782651:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782681:		#B3q1		1148782681:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782711:		#B3q1		1148782711:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782741:		#B3q1		1148782741:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782771:		#B3q1		1148782771:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782801:		#B3q1		1148782801:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782831:		#B3q1		1148782831:		$B3q1		3.77		3.80		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782861:		#B3q1		1148782861:		$B3q1		3.77		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782891:		#B3q1		1148782891:		$B3q1		3.77		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782921:		#B3q1		1148782921:		$B3q1		3.76		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782951:		#B3q1		1148782951:		$B3q1		3.76		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148782981:		#B3q1		1148782981:		$B3q1		3.76		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148783011:		#B3q1		1148783011:		$B3q1		3.76		3.79		3.78		3.76		3.76		3.79		3.79		3.76

		S1148783041:		#B3q1		1148783041:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783071:		#B3q1		1148783071:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783101:		#B3q1		1148783101:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783131:		#B3q1		1148783131:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783161:		#B3q1		1148783161:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783191:		#B3q1		1148783191:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783221:		#B3q1		1148783221:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783251:		#B3q1		1148783251:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783281:		#B3q1		1148783281:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783311:		#B3q1		1148783311:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783341:		#B3q1		1148783341:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783371:		#B3q1		1148783371:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.79		3.79		3.76

		S1148783401:		#B3q1		1148783401:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783431:		#B3q1		1148783431:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783461:		#B3q1		1148783461:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783491:		#B3q1		1148783491:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783521:		#B3q1		1148783521:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783551:		#B3q1		1148783551:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783581:		#B3q1		1148783581:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783611:		#B3q1		1148783611:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783641:		#B3q1		1148783641:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783671:		#B3q1		1148783671:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783701:		#B3q1		1148783701:		$B3q1		3.76		3.79		3.77		3.76		3.76		3.78		3.79		3.76

		S1148783731:		#B3q1		1148783731:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.79		3.76

		S1148783761:		#B3q1		1148783761:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783791:		#B3q1		1148783791:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783821:		#B3q1		1148783821:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783851:		#B3q1		1148783851:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783881:		#B3q1		1148783881:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783911:		#B3q1		1148783911:		$B3q1		3.76		3.79		3.77		3.75		3.76		3.78		3.78		3.76

		S1148783941:		#B3q1		1148783941:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.76

		S1148783971:		#B3q1		1148783971:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.76

		S1148784001:		#B3q1		1148784001:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.76

		S1148784031:		#B3q1		1148784031:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.76

		S1148784061:		#B3q1		1148784061:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784091:		#B3q1		1148784091:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784121:		#B3q1		1148784121:		$B3q1		3.76		3.79		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784151:		#B3q1		1148784151:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784181:		#B3q1		1148784181:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784211:		#B3q1		1148784211:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784241:		#B3q1		1148784241:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784271:		#B3q1		1148784271:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784301:		#B3q1		1148784301:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784331:		#B3q1		1148784331:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784361:		#B3q1		1148784361:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784391:		#B3q1		1148784391:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784421:		#B3q1		1148784421:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784451:		#B3q1		1148784451:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784481:		#B3q1		1148784481:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784511:		#B3q1		1148784511:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784541:		#B3q1		1148784541:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784571:		#B3q1		1148784571:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784601:		#B3q1		1148784601:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784631:		#B3q1		1148784631:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784661:		#B3q1		1148784661:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784691:		#B3q1		1148784691:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784721:		#B3q1		1148784721:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784751:		#B3q1		1148784751:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784781:		#B3q1		1148784781:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784811:		#B3q1		1148784811:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784841:		#B3q1		1148784841:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784871:		#B3q1		1148784871:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784901:		#B3q1		1148784901:		$B3q1		3.76		3.78		3.77		3.75		3.75		3.78		3.78		3.75

		S1148784931:		#B3q1		1148784931:		$B3q1		3.76		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784961:		#B3q1		1148784961:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148784991:		#B3q1		1148784991:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785021:		#B3q1		1148785021:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785051:		#B3q1		1148785051:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785081:		#B3q1		1148785081:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785111:		#B3q1		1148785111:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785141:		#B3q1		1148785141:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785171:		#B3q1		1148785171:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785201:		#B3q1		1148785201:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785231:		#B3q1		1148785231:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785261:		#B3q1		1148785261:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785291:		#B3q1		1148785291:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785321:		#B3q1		1148785321:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785351:		#B3q1		1148785351:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785381:		#B3q1		1148785381:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785411:		#B3q1		1148785411:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785441:		#B3q1		1148785441:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.78		3.78		3.75

		S1148785471:		#B3q1		1148785471:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785501:		#B3q1		1148785501:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785531:		#B3q1		1148785531:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785561:		#B3q1		1148785561:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785591:		#B3q1		1148785591:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785621:		#B3q1		1148785621:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785651:		#B3q1		1148785651:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785681:		#B3q1		1148785681:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785711:		#B3q1		1148785711:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785741:		#B3q1		1148785741:		$B3q1		3.75		3.78		3.76		3.75		3.75		3.77		3.78		3.75

		S1148785771:		#B3q1		1148785771:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785801:		#B3q1		1148785801:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785831:		#B3q1		1148785831:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785861:		#B3q1		1148785861:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785891:		#B3q1		1148785891:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785921:		#B3q1		1148785921:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785951:		#B3q1		1148785951:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148785981:		#B3q1		1148785981:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148786011:		#B3q1		1148786011:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148786041:		#B3q1		1148786041:		$B3q1		3.75		3.78		3.76		3.74		3.75		3.77		3.77		3.75

		S1148786071:		#B3q1		1148786071:		$B3q1		3.75		3.78		3.76		3.74		3.74		3.77		3.77		3.75

		S1148786101:		#B3q1		1148786101:		$B3q1		3.75		3.78		3.76		3.74		3.74		3.77		3.77		3.75

		S1148786131:		#B3q1		1148786131:		$B3q1		3.75		3.78		3.76		3.74		3.74		3.77		3.77		3.75

		S1148786161:		#B3q1		1148786161:		$B3q1		3.75		3.78		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786191:		#B3q1		1148786191:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786221:		#B3q1		1148786221:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786251:		#B3q1		1148786251:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786281:		#B3q1		1148786281:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786311:		#B3q1		1148786311:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786341:		#B3q1		1148786341:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786371:		#B3q1		1148786371:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786401:		#B3q1		1148786401:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786431:		#B3q1		1148786431:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786461:		#B3q1		1148786461:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786491:		#B3q1		1148786491:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786521:		#B3q1		1148786521:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786551:		#B3q1		1148786551:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786581:		#B3q1		1148786581:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786611:		#B3q1		1148786611:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786641:		#B3q1		1148786641:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786671:		#B3q1		1148786671:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786701:		#B3q1		1148786701:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786731:		#B3q1		1148786731:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786761:		#B3q1		1148786761:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786791:		#B3q1		1148786791:		$B3q1		3.75		3.77		3.76		3.74		3.74		3.77		3.77		3.74

		S1148786821:		#B3q1		1148786821:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.77		3.77		3.74

		S1148786851:		#B3q1		1148786851:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.77		3.77		3.74

		S1148786881:		#B3q1		1148786881:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.77		3.77		3.74

		S1148786911:		#B3q1		1148786911:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.77		3.77		3.74

		S1148786941:		#B3q1		1148786941:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148786971:		#B3q1		1148786971:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787001:		#B3q1		1148787001:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787031:		#B3q1		1148787031:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787061:		#B3q1		1148787061:		$B3q1		3.75		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787091:		#B3q1		1148787091:		$B3q1		3.74		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787121:		#B3q1		1148787121:		$B3q1		3.74		3.77		3.75		3.74		3.74		3.76		3.77		3.74

		S1148787151:		#B3q1		1148787151:		$B3q1		3.74		3.77		3.75		3.74		3.74		3.76		3.76		3.74

		S1148787181:		#B3q1		1148787181:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787211:		#B3q1		1148787211:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787241:		#B3q1		1148787241:		$B3q1		3.74		3.77		3.75		3.74		3.74		3.76		3.76		3.74

		S1148787271:		#B3q1		1148787271:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787301:		#B3q1		1148787301:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787331:		#B3q1		1148787331:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787361:		#B3q1		1148787361:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787391:		#B3q1		1148787391:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787421:		#B3q1		1148787421:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787451:		#B3q1		1148787451:		$B3q1		3.74		3.77		3.75		3.73		3.74		3.76		3.76		3.74

		S1148787481:		#B3q1		1148787481:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.74

		S1148787511:		#B3q1		1148787511:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.74

		S1148787541:		#B3q1		1148787541:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787571:		#B3q1		1148787571:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787601:		#B3q1		1148787601:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787631:		#B3q1		1148787631:		$B3q1		3.74		3.77		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787661:		#B3q1		1148787661:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787691:		#B3q1		1148787691:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787721:		#B3q1		1148787721:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787751:		#B3q1		1148787751:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787781:		#B3q1		1148787781:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787811:		#B3q1		1148787811:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787841:		#B3q1		1148787841:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787871:		#B3q1		1148787871:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787901:		#B3q1		1148787901:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787931:		#B3q1		1148787931:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787961:		#B3q1		1148787961:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148787991:		#B3q1		1148787991:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788021:		#B3q1		1148788021:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788051:		#B3q1		1148788051:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788081:		#B3q1		1148788081:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788111:		#B3q1		1148788111:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788141:		#B3q1		1148788141:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788171:		#B3q1		1148788171:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788201:		#B3q1		1148788201:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788231:		#B3q1		1148788231:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788261:		#B3q1		1148788261:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788291:		#B3q1		1148788291:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788321:		#B3q1		1148788321:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788351:		#B3q1		1148788351:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788381:		#B3q1		1148788381:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788411:		#B3q1		1148788411:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788441:		#B3q1		1148788441:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788471:		#B3q1		1148788471:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788501:		#B3q1		1148788501:		$B3q1		3.74		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788531:		#B3q1		1148788531:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788561:		#B3q1		1148788561:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788591:		#B3q1		1148788591:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788621:		#B3q1		1148788621:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788651:		#B3q1		1148788651:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788681:		#B3q1		1148788681:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788711:		#B3q1		1148788711:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788741:		#B3q1		1148788741:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788771:		#B3q1		1148788771:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788801:		#B3q1		1148788801:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788831:		#B3q1		1148788831:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788861:		#B3q1		1148788861:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788891:		#B3q1		1148788891:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788921:		#B3q1		1148788921:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788951:		#B3q1		1148788951:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148788981:		#B3q1		1148788981:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148789011:		#B3q1		1148789011:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148789041:		#B3q1		1148789041:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148789071:		#B3q1		1148789071:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148789101:		#B3q1		1148789101:		$B3q1		3.73		3.76		3.75		3.73		3.73		3.76		3.76		3.73

		S1148789131:		#B3q1		1148789131:		$B3q1		3.73		3.76		3.74		3.73		3.73		3.76		3.76		3.73

		S1148789161:		#B3q1		1148789161:		$B3q1		3.73		3.76		3.74		3.73		3.73		3.76		3.76		3.73

		S1148789191:		#B3q1		1148789191:		$B3q1		3.73		3.76		3.74		3.73		3.73		3.76		3.76		3.73

		S1148789221:		#B3q1		1148789221:		$B3q1		3.73		3.76		3.74		3.72		3.73		3.75		3.76		3.73

		S1148789251:		#B3q1		1148789251:		$B3q1		3.73		3.76		3.74		3.72		3.73		3.76		3.76		3.73

		S1148789281:		#B3q1		1148789281:		$B3q1		3.73		3.76		3.74		3.72		3.73		3.75		3.76		3.73

		S1148789311:		#B3q1		1148789311:		$B3q1		3.73		3.76		3.74		3.72		3.73		3.75		3.76		3.73

		S1148789341:		#B3q1		1148789341:		$B3q1		3.73		3.76		3.74		3.72		3.73		3.75		3.76		3.73

		S1148789371:		#B3q1		1148789371:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.73

		S1148789401:		#B3q1		1148789401:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.73

		S1148789431:		#B3q1		1148789431:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.73

		S1148789461:		#B3q1		1148789461:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.72

		S1148789491:		#B3q1		1148789491:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.72

		S1148789521:		#B3q1		1148789521:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.76		3.72

		S1148789551:		#B3q1		1148789551:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789581:		#B3q1		1148789581:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789611:		#B3q1		1148789611:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789641:		#B3q1		1148789641:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789671:		#B3q1		1148789671:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789701:		#B3q1		1148789701:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789731:		#B3q1		1148789731:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789761:		#B3q1		1148789761:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789791:		#B3q1		1148789791:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789821:		#B3q1		1148789821:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789851:		#B3q1		1148789851:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789881:		#B3q1		1148789881:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789911:		#B3q1		1148789911:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789941:		#B3q1		1148789941:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148789971:		#B3q1		1148789971:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790001:		#B3q1		1148790001:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790031:		#B3q1		1148790031:		$B3q1		3.73		3.76		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790061:		#B3q1		1148790061:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790091:		#B3q1		1148790091:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790121:		#B3q1		1148790121:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790151:		#B3q1		1148790151:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790181:		#B3q1		1148790181:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790211:		#B3q1		1148790211:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790241:		#B3q1		1148790241:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790271:		#B3q1		1148790271:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790301:		#B3q1		1148790301:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790331:		#B3q1		1148790331:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790361:		#B3q1		1148790361:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790391:		#B3q1		1148790391:		$B3q1		3.73		3.75		3.74		3.72		3.72		3.75		3.75		3.72

		S1148790421:		#B3q1		1148790421:		$B3q1		3.73		3.75		3.74		3.71		3.72		3.75		3.75		3.72

		S1148790451:		#B3q1		1148790451:		$B3q1		3.73		3.75		3.74		3.71		3.72		3.75		3.75		3.72

		S1148790481:		#B3q1		1148790481:		$B3q1		3.73		3.75		3.74		3.71		3.72		3.75		3.75		3.72

		S1148790511:		#B3q1		1148790511:		$B3q1		3.72		3.75		3.74		3.71		3.71		3.75		3.75		3.72

		S1148790541:		#B3q1		1148790541:		$B3q1		3.72		3.75		3.74		3.71		3.71		3.75		3.75		3.72

		S1148790571:		#B3q1		1148790571:		$B3q1		3.72		3.75		3.74		3.71		3.71		3.75		3.75		3.72

		S1148790601:		#B3q1		1148790601:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790631:		#B3q1		1148790631:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790661:		#B3q1		1148790661:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790691:		#B3q1		1148790691:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790721:		#B3q1		1148790721:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790751:		#B3q1		1148790751:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790781:		#B3q1		1148790781:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790811:		#B3q1		1148790811:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790841:		#B3q1		1148790841:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790871:		#B3q1		1148790871:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790901:		#B3q1		1148790901:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790931:		#B3q1		1148790931:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790961:		#B3q1		1148790961:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148790991:		#B3q1		1148790991:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791021:		#B3q1		1148791021:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791051:		#B3q1		1148791051:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791081:		#B3q1		1148791081:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791111:		#B3q1		1148791111:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791141:		#B3q1		1148791141:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791171:		#B3q1		1148791171:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791201:		#B3q1		1148791201:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791231:		#B3q1		1148791231:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791261:		#B3q1		1148791261:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791291:		#B3q1		1148791291:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791321:		#B3q1		1148791321:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791351:		#B3q1		1148791351:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791381:		#B3q1		1148791381:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791411:		#B3q1		1148791411:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791441:		#B3q1		1148791441:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791471:		#B3q1		1148791471:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791501:		#B3q1		1148791501:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.75		3.75		3.71

		S1148791531:		#B3q1		1148791531:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791561:		#B3q1		1148791561:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791591:		#B3q1		1148791591:		$B3q1		3.72		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791621:		#B3q1		1148791621:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791651:		#B3q1		1148791651:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791681:		#B3q1		1148791681:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791711:		#B3q1		1148791711:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791741:		#B3q1		1148791741:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791771:		#B3q1		1148791771:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791801:		#B3q1		1148791801:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791831:		#B3q1		1148791831:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791861:		#B3q1		1148791861:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791891:		#B3q1		1148791891:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791921:		#B3q1		1148791921:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.74		3.71

		S1148791951:		#B3q1		1148791951:		$B3q1		3.71		3.75		3.73		3.71		3.71		3.74		3.75		3.71

		S1148791981:		#B3q1		1148791981:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.71

		S1148792011:		#B3q1		1148792011:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.71

		S1148792041:		#B3q1		1148792041:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.71

		S1148792071:		#B3q1		1148792071:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.71

		S1148792101:		#B3q1		1148792101:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.71

		S1148792131:		#B3q1		1148792131:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792161:		#B3q1		1148792161:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792191:		#B3q1		1148792191:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792221:		#B3q1		1148792221:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792251:		#B3q1		1148792251:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792281:		#B3q1		1148792281:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792311:		#B3q1		1148792311:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792341:		#B3q1		1148792341:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792371:		#B3q1		1148792371:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792401:		#B3q1		1148792401:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792431:		#B3q1		1148792431:		$B3q1		3.71		3.74		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792461:		#B3q1		1148792461:		$B3q1		3.71		3.75		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792491:		#B3q1		1148792491:		$B3q1		3.71		3.74		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792521:		#B3q1		1148792521:		$B3q1		3.71		3.74		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792551:		#B3q1		1148792551:		$B3q1		3.71		3.74		3.73		3.70		3.70		3.74		3.74		3.70

		S1148792581:		#B3q1		1148792581:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792611:		#B3q1		1148792611:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792641:		#B3q1		1148792641:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792671:		#B3q1		1148792671:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792701:		#B3q1		1148792701:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792731:		#B3q1		1148792731:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792761:		#B3q1		1148792761:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792791:		#B3q1		1148792791:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792821:		#B3q1		1148792821:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792851:		#B3q1		1148792851:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792881:		#B3q1		1148792881:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792911:		#B3q1		1148792911:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792941:		#B3q1		1148792941:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148792971:		#B3q1		1148792971:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148793001:		#B3q1		1148793001:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148793031:		#B3q1		1148793031:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148793061:		#B3q1		1148793061:		$B3q1		3.71		3.74		3.72		3.70		3.70		3.74		3.74		3.70

		S1148793091:		#B3q1		1148793091:		$B3q1		3.71		3.74		3.72		3.70		3.69		3.74		3.74		3.70

		S1148793121:		#B3q1		1148793121:		$B3q1		3.71		3.74		3.72		3.69		3.69		3.73		3.74		3.70

		S1148793151:		#B3q1		1148793151:		$B3q1		3.71		3.74		3.72		3.69		3.69		3.73		3.74		3.70

		S1148793181:		#B3q1		1148793181:		$B3q1		3.71		3.74		3.72		3.69		3.69		3.73		3.74		3.70

		S1148793211:		#B3q1		1148793211:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793241:		#B3q1		1148793241:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793271:		#B3q1		1148793271:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793301:		#B3q1		1148793301:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793331:		#B3q1		1148793331:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793361:		#B3q1		1148793361:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793391:		#B3q1		1148793391:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.74		3.69

		S1148793421:		#B3q1		1148793421:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793451:		#B3q1		1148793451:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793481:		#B3q1		1148793481:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793511:		#B3q1		1148793511:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793541:		#B3q1		1148793541:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793571:		#B3q1		1148793571:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793601:		#B3q1		1148793601:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793631:		#B3q1		1148793631:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793661:		#B3q1		1148793661:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793691:		#B3q1		1148793691:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793721:		#B3q1		1148793721:		$B3q1		3.70		3.74		3.72		3.69		3.69		3.73		3.73		3.69

		S1148793751:		#B3q1		1148793751:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793781:		#B3q1		1148793781:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793811:		#B3q1		1148793811:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793841:		#B3q1		1148793841:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793871:		#B3q1		1148793871:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793901:		#B3q1		1148793901:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793931:		#B3q1		1148793931:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793961:		#B3q1		1148793961:		$B3q1		3.70		3.74		3.71		3.69		3.69		3.73		3.73		3.69

		S1148793991:		#B3q1		1148793991:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794021:		#B3q1		1148794021:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794051:		#B3q1		1148794051:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794081:		#B3q1		1148794081:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794111:		#B3q1		1148794111:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794141:		#B3q1		1148794141:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794171:		#B3q1		1148794171:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794201:		#B3q1		1148794201:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794231:		#B3q1		1148794231:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794261:		#B3q1		1148794261:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794291:		#B3q1		1148794291:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794321:		#B3q1		1148794321:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794351:		#B3q1		1148794351:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794381:		#B3q1		1148794381:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794411:		#B3q1		1148794411:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794441:		#B3q1		1148794441:		$B3q1		3.70		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794471:		#B3q1		1148794471:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794501:		#B3q1		1148794501:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794531:		#B3q1		1148794531:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794561:		#B3q1		1148794561:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794591:		#B3q1		1148794591:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794621:		#B3q1		1148794621:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794651:		#B3q1		1148794651:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794681:		#B3q1		1148794681:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794711:		#B3q1		1148794711:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794741:		#B3q1		1148794741:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794771:		#B3q1		1148794771:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794801:		#B3q1		1148794801:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794831:		#B3q1		1148794831:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794861:		#B3q1		1148794861:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794891:		#B3q1		1148794891:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794921:		#B3q1		1148794921:		$B3q1		3.69		3.73		3.71		3.69		3.69		3.73		3.73		3.69

		S1148794951:		#B3q1		1148794951:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.69

		S1148794981:		#B3q1		1148794981:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.69

		S1148795011:		#B3q1		1148795011:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.69

		S1148795041:		#B3q1		1148795041:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.69

		S1148795071:		#B3q1		1148795071:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.68

		S1148795101:		#B3q1		1148795101:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.68

		S1148795131:		#B3q1		1148795131:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.73		3.73		3.68

		S1148795161:		#B3q1		1148795161:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795191:		#B3q1		1148795191:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795221:		#B3q1		1148795221:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795251:		#B3q1		1148795251:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795281:		#B3q1		1148795281:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795311:		#B3q1		1148795311:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795341:		#B3q1		1148795341:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.73		3.68

		S1148795371:		#B3q1		1148795371:		$B3q1		3.69		3.73		3.71		3.68		3.68		3.72		3.73		3.68

		S1148795401:		#B3q1		1148795401:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.73		3.68

		S1148795431:		#B3q1		1148795431:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.73		3.68

		S1148795461:		#B3q1		1148795461:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.73		3.68

		S1148795491:		#B3q1		1148795491:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795521:		#B3q1		1148795521:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795551:		#B3q1		1148795551:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795581:		#B3q1		1148795581:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795611:		#B3q1		1148795611:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795641:		#B3q1		1148795641:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795671:		#B3q1		1148795671:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795701:		#B3q1		1148795701:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795731:		#B3q1		1148795731:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795761:		#B3q1		1148795761:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795791:		#B3q1		1148795791:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795821:		#B3q1		1148795821:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795851:		#B3q1		1148795851:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795881:		#B3q1		1148795881:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795911:		#B3q1		1148795911:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795941:		#B3q1		1148795941:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148795971:		#B3q1		1148795971:		$B3q1		3.69		3.73		3.70		3.68		3.68		3.72		3.72		3.68

		S1148796001:		#B3q1		1148796001:		$B3q1		3.69		3.73		3.70		3.68		3.67		3.72		3.72		3.68

		S1148796031:		#B3q1		1148796031:		$B3q1		3.69		3.73		3.70		3.68		3.67		3.72		3.72		3.68

		S1148796061:		#B3q1		1148796061:		$B3q1		3.69		3.73		3.70		3.68		3.67		3.72		3.72		3.67

		S1148796091:		#B3q1		1148796091:		$B3q1		3.69		3.73		3.70		3.68		3.67		3.72		3.72		3.67

		S1148796121:		#B3q1		1148796121:		$B3q1		3.69		3.72		3.70		3.68		3.67		3.72		3.72		3.67

		S1148796151:		#B3q1		1148796151:		$B3q1		3.69		3.72		3.70		3.68		3.67		3.72		3.72		3.67

		S1148796181:		#B3q1		1148796181:		$B3q1		3.69		3.72		3.70		3.67		3.67		3.72		3.72		3.67

		S1148796211:		#B3q1		1148796211:		$B3q1		3.69		3.72		3.70		3.67		3.67		3.72		3.72		3.67

		S1148796241:		#B3q1		1148796241:		$B3q1		3.69		3.72		3.70		3.67		3.67		3.72		3.72		3.67

		S1148796271:		#B3q1		1148796271:		$B3q1		3.69		3.72		3.70		3.67		3.67		3.72		3.72		3.67

		S1148796301:		#B3q1		1148796301:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796331:		#B3q1		1148796331:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796361:		#B3q1		1148796361:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796391:		#B3q1		1148796391:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796421:		#B3q1		1148796421:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796451:		#B3q1		1148796451:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796481:		#B3q1		1148796481:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796511:		#B3q1		1148796511:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796541:		#B3q1		1148796541:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796571:		#B3q1		1148796571:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796601:		#B3q1		1148796601:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796631:		#B3q1		1148796631:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796661:		#B3q1		1148796661:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.72		3.67

		S1148796691:		#B3q1		1148796691:		$B3q1		3.68		3.72		3.70		3.67		3.67		3.71		3.71		3.67

		S1148796721:		#B3q1		1148796721:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796751:		#B3q1		1148796751:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796781:		#B3q1		1148796781:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796811:		#B3q1		1148796811:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796841:		#B3q1		1148796841:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796871:		#B3q1		1148796871:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796901:		#B3q1		1148796901:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796931:		#B3q1		1148796931:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796961:		#B3q1		1148796961:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148796991:		#B3q1		1148796991:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797021:		#B3q1		1148797021:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797051:		#B3q1		1148797051:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797081:		#B3q1		1148797081:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797111:		#B3q1		1148797111:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797141:		#B3q1		1148797141:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797171:		#B3q1		1148797171:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797201:		#B3q1		1148797201:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797231:		#B3q1		1148797231:		$B3q1		3.68		3.72		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797261:		#B3q1		1148797261:		$B3q1		3.68		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797291:		#B3q1		1148797291:		$B3q1		3.68		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797321:		#B3q1		1148797321:		$B3q1		3.68		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797351:		#B3q1		1148797351:		$B3q1		3.68		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797381:		#B3q1		1148797381:		$B3q1		3.68		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797411:		#B3q1		1148797411:		$B3q1		3.67		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797441:		#B3q1		1148797441:		$B3q1		3.67		3.71		3.69		3.67		3.67		3.71		3.71		3.67

		S1148797471:		#B3q1		1148797471:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.67

		S1148797501:		#B3q1		1148797501:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.67

		S1148797531:		#B3q1		1148797531:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.67

		S1148797561:		#B3q1		1148797561:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.66

		S1148797591:		#B3q1		1148797591:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.67

		S1148797621:		#B3q1		1148797621:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.66

		S1148797651:		#B3q1		1148797651:		$B3q1		3.67		3.71		3.69		3.67		3.66		3.71		3.71		3.66

		S1148797681:		#B3q1		1148797681:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.71		3.71		3.66

		S1148797711:		#B3q1		1148797711:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.71		3.71		3.66

		S1148797741:		#B3q1		1148797741:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.71		3.71		3.66

		S1148797771:		#B3q1		1148797771:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797801:		#B3q1		1148797801:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797831:		#B3q1		1148797831:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797861:		#B3q1		1148797861:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797891:		#B3q1		1148797891:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797921:		#B3q1		1148797921:		$B3q1		3.67		3.71		3.69		3.66		3.67		3.71		3.71		3.66

		S1148797951:		#B3q1		1148797951:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148797981:		#B3q1		1148797981:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.71		3.71		3.66

		S1148798011:		#B3q1		1148798011:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.71		3.71		3.66

		S1148798041:		#B3q1		1148798041:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798071:		#B3q1		1148798071:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798101:		#B3q1		1148798101:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798131:		#B3q1		1148798131:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798161:		#B3q1		1148798161:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798191:		#B3q1		1148798191:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798221:		#B3q1		1148798221:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798251:		#B3q1		1148798251:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798281:		#B3q1		1148798281:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.71		3.66

		S1148798311:		#B3q1		1148798311:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798341:		#B3q1		1148798341:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798371:		#B3q1		1148798371:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798401:		#B3q1		1148798401:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798431:		#B3q1		1148798431:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798461:		#B3q1		1148798461:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798491:		#B3q1		1148798491:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798521:		#B3q1		1148798521:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798551:		#B3q1		1148798551:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798581:		#B3q1		1148798581:		$B3q1		3.67		3.71		3.69		3.66		3.66		3.70		3.70		3.66

		S1148798611:		#B3q1		1148798611:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798641:		#B3q1		1148798641:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798671:		#B3q1		1148798671:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798701:		#B3q1		1148798701:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798731:		#B3q1		1148798731:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798761:		#B3q1		1148798761:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798791:		#B3q1		1148798791:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.66

		S1148798821:		#B3q1		1148798821:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.65

		S1148798851:		#B3q1		1148798851:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.65

		S1148798881:		#B3q1		1148798881:		$B3q1		3.67		3.71		3.68		3.66		3.66		3.70		3.70		3.65

		S1148798911:		#B3q1		1148798911:		$B3q1		3.66		3.70		3.68		3.66		3.66		3.70		3.70		3.65

		S1148798941:		#B3q1		1148798941:		$B3q1		3.66		3.70		3.68		3.66		3.66		3.70		3.70		3.65

		S1148798971:		#B3q1		1148798971:		$B3q1		3.66		3.70		3.68		3.66		3.65		3.70		3.70		3.65

		S1148799001:		#B3q1		1148799001:		$B3q1		3.66		3.70		3.68		3.66		3.65		3.70		3.70		3.65

		S1148799031:		#B3q1		1148799031:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799061:		#B3q1		1148799061:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799091:		#B3q1		1148799091:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799121:		#B3q1		1148799121:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799151:		#B3q1		1148799151:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799181:		#B3q1		1148799181:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799211:		#B3q1		1148799211:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799241:		#B3q1		1148799241:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799271:		#B3q1		1148799271:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799301:		#B3q1		1148799301:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.70		3.70		3.65

		S1148799331:		#B3q1		1148799331:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.65

		S1148799361:		#B3q1		1148799361:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.65

		S1148799391:		#B3q1		1148799391:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.65

		S1148799421:		#B3q1		1148799421:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.65

		S1148799451:		#B3q1		1148799451:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.65

		S1148799481:		#B3q1		1148799481:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.64

		S1148799511:		#B3q1		1148799511:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.64

		S1148799541:		#B3q1		1148799541:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.64

		S1148799571:		#B3q1		1148799571:		$B3q1		3.66		3.70		3.68		3.65		3.65		3.69		3.70		3.64

		S1148799601:		#B3q1		1148799601:		$B3q1		3.66		3.70		3.68		3.65		3.64		3.69		3.70		3.64

		S1148799631:		#B3q1		1148799631:		$B3q1		3.66		3.70		3.68		3.65		3.64		3.69		3.70		3.64

		S1148799661:		#B3q1		1148799661:		$B3q1		3.66		3.70		3.68		3.65		3.64		3.69		3.70		3.64

		S1148799691:		#B3q1		1148799691:		$B3q1		3.66		3.70		3.68		3.64		3.64		3.69		3.70		3.64

		S1148799721:		#B3q1		1148799721:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799751:		#B3q1		1148799751:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799781:		#B3q1		1148799781:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799811:		#B3q1		1148799811:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799841:		#B3q1		1148799841:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799871:		#B3q1		1148799871:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799901:		#B3q1		1148799901:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799931:		#B3q1		1148799931:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799961:		#B3q1		1148799961:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148799991:		#B3q1		1148799991:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800021:		#B3q1		1148800021:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800051:		#B3q1		1148800051:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800081:		#B3q1		1148800081:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800111:		#B3q1		1148800111:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800141:		#B3q1		1148800141:		$B3q1		3.66		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800171:		#B3q1		1148800171:		$B3q1		3.65		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800201:		#B3q1		1148800201:		$B3q1		3.65		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800231:		#B3q1		1148800231:		$B3q1		3.65		3.70		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800261:		#B3q1		1148800261:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800291:		#B3q1		1148800291:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800321:		#B3q1		1148800321:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800351:		#B3q1		1148800351:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800381:		#B3q1		1148800381:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800411:		#B3q1		1148800411:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800441:		#B3q1		1148800441:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800471:		#B3q1		1148800471:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800501:		#B3q1		1148800501:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800531:		#B3q1		1148800531:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800561:		#B3q1		1148800561:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800591:		#B3q1		1148800591:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800621:		#B3q1		1148800621:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800651:		#B3q1		1148800651:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800681:		#B3q1		1148800681:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800711:		#B3q1		1148800711:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800741:		#B3q1		1148800741:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800771:		#B3q1		1148800771:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800801:		#B3q1		1148800801:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800831:		#B3q1		1148800831:		$B3q1		3.65		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800861:		#B3q1		1148800861:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800891:		#B3q1		1148800891:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800921:		#B3q1		1148800921:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800951:		#B3q1		1148800951:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148800981:		#B3q1		1148800981:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801011:		#B3q1		1148801011:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801041:		#B3q1		1148801041:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801071:		#B3q1		1148801071:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801101:		#B3q1		1148801101:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801131:		#B3q1		1148801131:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801161:		#B3q1		1148801161:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801191:		#B3q1		1148801191:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801221:		#B3q1		1148801221:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801251:		#B3q1		1148801251:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.69		3.69		3.64

		S1148801281:		#B3q1		1148801281:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.68		3.69		3.64

		S1148801311:		#B3q1		1148801311:		$B3q1		3.64		3.69		3.67		3.64		3.64		3.68		3.69		3.64

		S1148801341:		#B3q1		1148801341:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801371:		#B3q1		1148801371:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801401:		#B3q1		1148801401:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801431:		#B3q1		1148801431:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801461:		#B3q1		1148801461:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801491:		#B3q1		1148801491:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801521:		#B3q1		1148801521:		$B3q1		3.64		3.69		3.66		3.64		3.64		3.68		3.69		3.63

		S1148801551:		#B3q1		1148801551:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801581:		#B3q1		1148801581:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801611:		#B3q1		1148801611:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801641:		#B3q1		1148801641:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801671:		#B3q1		1148801671:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801701:		#B3q1		1148801701:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801731:		#B3q1		1148801731:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.69		3.63

		S1148801761:		#B3q1		1148801761:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801791:		#B3q1		1148801791:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801821:		#B3q1		1148801821:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801851:		#B3q1		1148801851:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801881:		#B3q1		1148801881:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801911:		#B3q1		1148801911:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801941:		#B3q1		1148801941:		$B3q1		3.64		3.69		3.66		3.64		3.63		3.68		3.68		3.63

		S1148801971:		#B3q1		1148801971:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802001:		#B3q1		1148802001:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802031:		#B3q1		1148802031:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802061:		#B3q1		1148802061:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802091:		#B3q1		1148802091:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802121:		#B3q1		1148802121:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802151:		#B3q1		1148802151:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802181:		#B3q1		1148802181:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802211:		#B3q1		1148802211:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802241:		#B3q1		1148802241:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802271:		#B3q1		1148802271:		$B3q1		3.64		3.69		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802301:		#B3q1		1148802301:		$B3q1		3.64		3.68		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802331:		#B3q1		1148802331:		$B3q1		3.64		3.68		3.66		3.63		3.63		3.68		3.68		3.63

		S1148802361:		#B3q1		1148802361:		$B3q1		3.64		3.68		3.66		3.63		3.63		3.68		3.68		3.62

		S1148802391:		#B3q1		1148802391:		$B3q1		3.64		3.68		3.66		3.63		3.63		3.68		3.68		3.62

		S1148802421:		#B3q1		1148802421:		$B3q1		3.64		3.68		3.66		3.63		3.63		3.67		3.68		3.62

		S1148802451:		#B3q1		1148802451:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802481:		#B3q1		1148802481:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802511:		#B3q1		1148802511:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802541:		#B3q1		1148802541:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802571:		#B3q1		1148802571:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802601:		#B3q1		1148802601:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802631:		#B3q1		1148802631:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802661:		#B3q1		1148802661:		$B3q1		3.64		3.68		3.66		3.63		3.62		3.67		3.68		3.62

		S1148802691:		#B3q1		1148802691:		$B3q1		3.64		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802721:		#B3q1		1148802721:		$B3q1		3.64		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802751:		#B3q1		1148802751:		$B3q1		3.64		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802781:		#B3q1		1148802781:		$B3q1		3.64		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802811:		#B3q1		1148802811:		$B3q1		3.64		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802841:		#B3q1		1148802841:		$B3q1		3.63		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802871:		#B3q1		1148802871:		$B3q1		3.63		3.68		3.65		3.63		3.62		3.67		3.67		3.62

		S1148802901:		#B3q1		1148802901:		$B3q1		3.63		3.68		3.65		3.63		3.62		3.67		3.68		3.62

		S1148802931:		#B3q1		1148802931:		$B3q1		3.63		3.68		3.65		3.62		3.62		3.67		3.67		3.62

		S1148802961:		#B3q1		1148802961:		$B3q1		3.63		3.68		3.65		3.62		3.62		3.67		3.67		3.61

		S1148802991:		#B3q1		1148802991:		$B3q1		3.63		3.68		3.65		3.62		3.62		3.67		3.67		3.61

		S1148803021:		#B3q1		1148803021:		$B3q1		3.63		3.68		3.65		3.62		3.62		3.67		3.67		3.61

		S1148803051:		#B3q1		1148803051:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.61

		S1148803081:		#B3q1		1148803081:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.61

		S1148803111:		#B3q1		1148803111:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.61

		S1148803141:		#B3q1		1148803141:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.61

		S1148803171:		#B3q1		1148803171:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.61

		S1148803201:		#B3q1		1148803201:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.60

		S1148803231:		#B3q1		1148803231:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.60

		S1148803261:		#B3q1		1148803261:		$B3q1		3.63		3.68		3.65		3.62		3.61		3.67		3.67		3.60

		S1148803291:		#B3q1		1148803291:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.60

		S1148803321:		#B3q1		1148803321:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.60

		S1148803351:		#B3q1		1148803351:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.60

		S1148803381:		#B3q1		1148803381:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.60

		S1148803411:		#B3q1		1148803411:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.60

		S1148803441:		#B3q1		1148803441:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.59

		S1148803471:		#B3q1		1148803471:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.59

		S1148803501:		#B3q1		1148803501:		$B3q1		3.63		3.68		3.65		3.62		3.60		3.67		3.67		3.59

		S1148803531:		#B3q1		1148803531:		$B3q1		3.63		3.68		3.65		3.62		3.59		3.67		3.67		3.59

		S1148803561:		#B3q1		1148803561:		$B3q1		3.63		3.67		3.65		3.62		3.59		3.67		3.67		3.59

		S1148803591:		#B3q1		1148803591:		$B3q1		3.63		3.67		3.65		3.62		3.59		3.67		3.67		3.58

		S1148803621:		#B3q1		1148803621:		$B3q1		3.63		3.67		3.65		3.61		3.59		3.67		3.67		3.58

		S1148803651:		#B3q1		1148803651:		$B3q1		3.63		3.67		3.64		3.61		3.59		3.67		3.67		3.58

		S1148803681:		#B3q1		1148803681:		$B3q1		3.63		3.67		3.64		3.61		3.58		3.67		3.67		3.58

		S1148803711:		#B3q1		1148803711:		$B3q1		3.63		3.67		3.64		3.61		3.58		3.67		3.67		3.58

		S1148803741:		#B3q1		1148803741:		$B3q1		3.63		3.67		3.64		3.61		3.58		3.67		3.67		3.58

		S1148803771:		#B3q1		1148803771:		$B3q1		3.62		3.67		3.64		3.61		3.58		3.67		3.67		3.58

		S1148803801:		#B3q1		1148803801:		$B3q1		3.62		3.67		3.64		3.61		3.58		3.67		3.67		3.57

		S1148803831:		#B3q1		1148803831:		$B3q1		3.62		3.67		3.64		3.61		3.58		3.67		3.67		3.57

		S1148803861:		#B3q1		1148803861:		$B3q1		3.62		3.67		3.64		3.61		3.58		3.67		3.67		3.57

		S1148803891:		#B3q1		1148803891:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.57

		S1148803921:		#B3q1		1148803921:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.57

		S1148803951:		#B3q1		1148803951:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.57

		S1148803981:		#B3q1		1148803981:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.56

		S1148804011:		#B3q1		1148804011:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.56

		S1148804041:		#B3q1		1148804041:		$B3q1		3.62		3.67		3.64		3.60		3.57		3.67		3.67		3.56

		S1148804071:		#B3q1		1148804071:		$B3q1		3.62		3.67		3.64		3.60		3.56		3.67		3.67		3.56

		S1148804101:		#B3q1		1148804101:		$B3q1		3.62		3.67		3.64		3.60		3.56		3.67		3.67		3.55

		S1148804131:		#B3q1		1148804131:		$B3q1		3.62		3.67		3.64		3.60		3.56		3.66		3.67		3.55

		S1148804161:		#B3q1		1148804161:		$B3q1		3.62		3.67		3.64		3.59		3.56		3.66		3.67		3.55

		S1148804191:		#B3q1		1148804191:		$B3q1		3.62		3.67		3.64		3.59		3.55		3.66		3.67		3.55

		S1148804221:		#B3q1		1148804221:		$B3q1		3.62		3.67		3.64		3.59		3.55		3.66		3.67		3.55

		S1148804251:		#B3q1		1148804251:		$B3q1		3.62		3.67		3.64		3.59		3.55		3.66		3.67		3.55

		S1148804281:		#B3q1		1148804281:		$B3q1		3.62		3.67		3.64		3.59		3.55		3.66		3.67		3.54

		S1148804311:		#B3q1		1148804311:		$B3q1		3.62		3.67		3.64		3.59		3.55		3.66		3.67		3.54

		S1148804341:		#B3q1		1148804341:		$B3q1		3.61		3.67		3.64		3.58		3.55		3.66		3.67		3.54

		S1148804371:		#B3q1		1148804371:		$B3q1		3.61		3.67		3.64		3.58		3.54		3.66		3.67		3.54

		S1148804401:		#B3q1		1148804401:		$B3q1		3.61		3.67		3.64		3.58		3.54		3.66		3.67		3.53

		S1148804431:		#B3q1		1148804431:		$B3q1		3.61		3.67		3.64		3.58		3.54		3.66		3.67		3.53

		S1148804461:		#B3q1		1148804461:		$B3q1		3.61		3.67		3.64		3.58		3.53		3.66		3.67		3.53

		S1148804491:		#B3q1		1148804491:		$B3q1		3.61		3.67		3.64		3.58		3.53		3.66		3.67		3.53

		S1148804521:		#B3q1		1148804521:		$B3q1		3.61		3.67		3.64		3.58		3.53		3.66		3.67		3.53

		S1148804551:		#B3q1		1148804551:		$B3q1		3.60		3.67		3.64		3.58		3.53		3.66		3.67		3.53

		S1148804581:		#B3q1		1148804581:		$B3q1		3.60		3.67		3.64		3.57		3.53		3.66		3.67		3.52

		S1148804611:		#B3q1		1148804611:		$B3q1		3.60		3.67		3.64		3.57		3.53		3.66		3.66		3.52

		S1148804641:		#B3q1		1148804641:		$B3q1		3.60		3.67		3.64		3.57		3.52		3.66		3.66		3.52

		S1148804671:		#B3q1		1148804671:		$B3q1		3.60		3.67		3.64		3.57		3.52		3.66		3.66		3.51

		S1148804701:		#B3q1		1148804701:		$B3q1		3.60		3.67		3.64		3.57		3.52		3.66		3.66		3.51

		S1148804731:		#B3q1		1148804731:		$B3q1		3.60		3.67		3.64		3.57		3.51		3.66		3.66		3.51

		S1148804761:		#B3q1		1148804761:		$B3q1		3.60		3.67		3.64		3.57		3.51		3.66		3.66		3.51

		S1148804791:		#B3q1		1148804791:		$B3q1		3.60		3.67		3.64		3.56		3.51		3.66		3.66		3.51

		S1148804821:		#B3q1		1148804821:		$B3q1		3.59		3.67		3.64		3.56		3.51		3.66		3.66		3.50

		S1148804851:		#B3q1		1148804851:		$B3q1		3.59		3.67		3.64		3.56		3.51		3.66		3.66		3.50

		S1148804881:		#B3q1		1148804881:		$B3q1		3.59		3.67		3.64		3.56		3.50		3.66		3.66		3.50

		S1148804911:		#B3q1		1148804911:		$B3q1		3.59		3.67		3.64		3.55		3.50		3.66		3.66		3.50

		S1148804941:		#B3q1		1148804941:		$B3q1		3.59		3.67		3.64		3.55		3.50		3.66		3.66		3.50

		S1148804971:		#B3q1		1148804971:		$B3q1		3.58		3.67		3.64		3.55		3.50		3.66		3.66		3.49

		S1148805001:		#B3q1		1148805001:		$B3q1		3.58		3.67		3.64		3.55		3.49		3.66		3.66		3.49

		S1148805031:		#B3q1		1148805031:		$B3q1		3.58		3.67		3.64		3.55		3.49		3.66		3.66		3.49

		S1148805061:		#B3q1		1148805061:		$B3q1		3.58		3.67		3.64		3.55		3.49		3.66		3.66		3.48

		S1148805091:		#B3q1		1148805091:		$B3q1		3.58		3.67		3.64		3.55		3.48		3.66		3.66		3.48

		S1148805121:		#B3q1		1148805121:		$B3q1		3.58		3.67		3.64		3.54		3.48		3.66		3.66		3.48

		S1148805151:		#B3q1		1148805151:		$B3q1		3.58		3.67		3.64		3.54		3.48		3.66		3.66		3.48

		S1148805181:		#B3q1		1148805181:		$B3q1		3.57		3.67		3.64		3.54		3.48		3.66		3.66		3.47

		S1148805211:		#B3q1		1148805211:		$B3q1		3.57		3.67		3.64		3.54		3.47		3.66		3.66		3.47

		S1148805241:		#B3q1		1148805241:		$B3q1		3.57		3.66		3.64		3.53		3.47		3.66		3.66		3.47

		S1148805271:		#B3q1		1148805271:		$B3q1		3.57		3.66		3.64		3.53		3.47		3.66		3.66		3.46

		S1148805301:		#B3q1		1148805301:		$B3q1		3.57		3.66		3.64		3.53		3.46		3.66		3.66		3.46

		S1148805331:		#B3q1		1148805331:		$B3q1		3.57		3.66		3.64		3.53		3.46		3.66		3.66		3.46

		S1148805361:		#B3q1		1148805361:		$B3q1		3.57		3.66		3.64		3.53		3.46		3.66		3.66		3.46

		S1148805391:		#B3q1		1148805391:		$B3q1		3.56		3.66		3.64		3.53		3.46		3.66		3.66		3.45

		S1148805421:		#B3q1		1148805421:		$B3q1		3.56		3.66		3.64		3.52		3.45		3.66		3.66		3.45

		S1148805451:		#B3q1		1148805451:		$B3q1		3.56		3.66		3.64		3.52		3.45		3.66		3.66		3.45

		S1148805481:		#B3q1		1148805481:		$B3q1		3.56		3.66		3.64		3.52		3.44		3.65		3.66		3.45

		S1148805511:		#B3q1		1148805511:		$B3q1		3.55		3.66		3.64		3.51		3.44		3.65		3.66		3.44

		S1148805541:		#B3q1		1148805541:		$B3q1		3.55		3.66		3.64		3.51		3.44		3.65		3.66		3.44

		S1148805571:		#B3q1		1148805571:		$B3q1		3.55		3.66		3.64		3.51		3.44		3.65		3.66		3.44

		S1148805601:		#B3q1		1148805601:		$B3q1		3.55		3.66		3.64		3.51		3.43		3.65		3.66		3.44

		S1148805631:		#B3q1		1148805631:		$B3q1		3.55		3.66		3.64		3.51		3.43		3.65		3.66		3.43

		S1148805661:		#B3q1		1148805661:		$B3q1		3.55		3.66		3.64		3.51		3.42		3.65		3.66		3.43

		S1148805691:		#B3q1		1148805691:		$B3q1		3.54		3.66		3.64		3.51		3.42		3.65		3.66		3.43

		S1148805721:		#B3q1		1148805721:		$B3q1		3.54		3.66		3.64		3.51		3.42		3.65		3.66		3.42

		S1148805751:		#B3q1		1148805751:		$B3q1		3.54		3.66		3.64		3.51		3.41		3.65		3.66		3.42

		S1148805781:		#B3q1		1148805781:		$B3q1		3.54		3.66		3.63		3.51		3.41		3.65		3.66		3.42

		S1148805811:		#B3q1		1148805811:		$B3q1		3.53		3.66		3.63		3.50		3.41		3.65		3.66		3.41

		S1148805841:		#B3q1		1148805841:		$B3q1		3.53		3.66		3.63		3.50		3.40		3.65		3.66		3.41

		S1148805871:		#B3q1		1148805871:		$B3q1		3.53		3.66		3.63		3.50		3.40		3.65		3.66		3.41

		S1148805901:		#B3q1		1148805901:		$B3q1		3.53		3.66		3.63		3.50		3.39		3.65		3.65		3.41

		S1148805931:		#B3q1		1148805931:		$B3q1		3.53		3.66		3.63		3.50		3.39		3.65		3.65		3.40

		S1148805961:		#B3q1		1148805961:		$B3q1		3.52		3.66		3.63		3.50		3.39		3.65		3.65		3.40

		S1148805991:		#B3q1		1148805991:		$B3q1		3.52		3.66		3.63		3.49		3.38		3.65		3.65		3.39

		S1148806021:		#B3q1		1148806021:		$B3q1		3.52		3.66		3.63		3.49		3.38		3.65		3.65		3.39

		S1148806051:		#B3q1		1148806051:		$B3q1		3.52		3.66		3.63		3.49		3.37		3.65		3.65		3.39

		S1148806081:		#B3q1		1148806081:		$B3q1		3.51		3.66		3.63		3.49		3.37		3.65		3.65		3.39

		S1148806111:		#B3q1		1148806111:		$B3q1		3.51		3.66		3.63		3.48		3.37		3.65		3.65		3.39

		S1148806141:		#B3q1		1148806141:		$B3q1		3.51		3.66		3.63		3.48		3.36		3.65		3.65		3.39

		S1148806171:		#B3q1		1148806171:		$B3q1		3.51		3.66		3.63		3.48		3.35		3.65		3.65		3.38

		S1148806201:		#B3q1		1148806201:		$B3q1		3.51		3.66		3.63		3.48		3.35		3.65		3.65		3.38

		S1148806231:		#B3q1		1148806231:		$B3q1		3.50		3.66		3.63		3.48		3.35		3.64		3.65		3.38

		S1148806261:		#B3q1		1148806261:		$B3q1		3.50		3.66		3.63		3.47		3.34		3.64		3.65		3.37

		S1148806291:		#B3q1		1148806291:		$B3q1		3.50		3.66		3.63		3.47		3.33		3.64		3.65		3.37

		S1148806321:		#B3q1		1148806321:		$B3q1		3.50		3.66		3.63		3.47		3.33		3.64		3.65		3.37

		S1148806351:		#B3q1		1148806351:		$B3q1		3.50		3.66		3.63		3.47		3.32		3.64		3.65		3.37

		S1148806381:		#B3q1		1148806381:		$B3q1		3.49		3.66		3.63		3.46		3.32		3.64		3.65		3.36

		S1148806411:		#B3q1		1148806411:		$B3q1		3.49		3.66		3.63		3.46		3.32		3.64		3.65		3.36

		S1148806441:		#B3q1		1148806441:		$B3q1		3.49		3.66		3.63		3.46		3.31		3.64		3.65		3.36

		S1148806471:		#B3q1		1148806471:		$B3q1		3.48		3.66		3.63		3.46		3.30		3.64		3.65		3.35

		S1148806501:		#B3q1		1148806501:		$B3q1		3.48		3.66		3.63		3.46		3.30		3.64		3.65		3.35

		S1148806531:		#B3q1		1148806531:		$B3q1		3.48		3.66		3.63		3.45		3.29		3.64		3.65		3.35

		S1148806561:		#B3q1		1148806561:		$B3q1		3.48		3.66		3.62		3.45		3.28		3.64		3.65		3.34

		S1148806591:		#B3q1		1148806591:		$B3q1		3.47		3.66		3.62		3.45		3.28		3.64		3.65		3.34

		S1148806621:		#B3q1		1148806621:		$B3q1		3.47		3.65		3.62		3.44		3.27		3.64		3.65		3.33

		S1148806651:		#B3q1		1148806651:		$B3q1		3.47		3.65		3.62		3.45		3.26		3.64		3.65		3.33

		S1148806681:		#B3q1		1148806681:		$B3q1		3.46		3.65		3.62		3.45		3.26		3.64		3.65		3.33

		S1148806711:		#B3q1		1148806711:		$B3q1		3.46		3.65		3.62		3.45		3.25		3.64		3.65		3.32

		S1148806741:		#B3q1		1148806741:		$B3q1		3.46		3.65		3.62		3.45		3.24		3.64		3.64		3.32

		S1148806771:		#B3q1		1148806771:		$B3q1		3.46		3.65		3.62		3.44		3.23		3.64		3.64		3.32

		S1148806801:		#B3q1		1148806801:		$B3q1		3.45		3.65		3.62		3.44		3.23		3.64		3.64		3.31

		S1148806831:		#B3q1		1148806831:		$B3q1		3.45		3.65		3.62		3.44		3.22		3.64		3.64		3.31

		S1148806861:		#B3q1		1148806861:		$B3q1		3.44		3.65		3.62		3.44		3.21		3.64		3.64		3.30

		S1148806891:		#B3q1		1148806891:		$B3q1		3.44		3.65		3.62		3.44		3.20		3.64		3.64		3.30

		S1148806921:		#B3q1		1148806921:		$B3q1		3.44		3.65		3.62		3.44		3.19		3.64		3.64		3.30

		S1148806951:		#B3q1		1148806951:		$B3q1		3.44		3.65		3.62		3.43		3.18		3.64		3.64		3.29

		S1148806981:		#B3q1		1148806981:		$B3q1		3.43		3.65		3.62		3.43		3.17		3.64		3.64		3.29

		S1148807011:		#B3q1		1148807011:		$B3q1		3.43		3.65		3.62		3.43		3.16		3.64		3.64		3.28

		S1148807041:		#B3q1		1148807041:		$B3q1		3.42		3.65		3.62		3.43		3.15		3.64		3.64		3.28

		S1148807071:		#B3q1		1148807071:		$B3q1		3.43		3.65		3.62		3.42		3.14		3.64		3.64		3.27

		S1148807101:		#B3q1		1148807101:		$B3q1		3.46		3.67		3.64		3.45		3.17		3.67		3.67		3.30

		S1148807131:		#B3q1		1148807131:		$B3q1		3.46		3.67		3.64		3.46		3.17		3.67		3.67		3.31

		S1148807161:		#B3q1		1148807161:		$B3q1		3.46		3.67		3.64		3.46		3.18		3.67		3.67		3.31

		S1148807191:		#B3q1		1148807191:		$B3q1		3.46		3.67		3.64		3.46		3.18		3.67		3.67		3.32

		S1148807221:		#B3q1		1148807221:		$B3q1		3.46		3.67		3.64		3.46		3.18		3.67		3.67		3.32

		S1148807251:		#B3q1		1148807251:		$B3q1		3.46		3.67		3.64		3.46		3.19		3.67		3.67		3.32

		S1148807281:		#B3q1		1148807281:		$B3q1		3.46		3.67		3.65		3.47		3.19		3.67		3.67		3.32

		S1148807311:		#B3q1		1148807311:		$B3q1		3.46		3.67		3.65		3.47		3.19		3.67		3.67		3.33

		S1148807341:		#B3q1		1148807341:		$B3q1		3.46		3.67		3.65		3.47		3.20		3.67		3.67		3.33

		S1148807371:		#B3q1		1148807371:		$B3q1		3.47		3.67		3.65		3.47		3.21		3.67		3.67		3.33

		S1148807401:		#B3q1		1148807401:		$B3q1		3.47		3.67		3.65		3.47		3.21		3.67		3.67		3.33

		S1148807431:		#B3q1		1148807431:		$B3q1		3.47		3.67		3.65		3.47		3.22		3.67		3.67		3.33

		S1148807461:		#B3q1		1148807461:		$B3q1		3.47		3.67		3.65		3.48		3.22		3.67		3.67		3.33

		S1148807491:		#B3q1		1148807491:		$B3q1		3.47		3.67		3.65		3.48		3.23		3.67		3.67		3.34

		S1148807521:		#B3q1		1148807521:		$B3q1		3.47		3.67		3.65		3.48		3.23		3.67		3.67		3.34

		S1148807551:		#B3q1		1148807551:		$B3q1		3.47		3.67		3.65		3.48		3.23		3.67		3.67		3.34

		S1148807581:		#B3q1		1148807581:		$B3q1		3.47		3.67		3.65		3.48		3.24		3.67		3.67		3.34

		S1148807611:		#B3q1		1148807611:		$B3q1		3.47		3.68		3.65		3.48		3.25		3.67		3.67		3.35

		S1148807641:		#B3q1		1148807641:		$B3q1		3.47		3.67		3.65		3.48		3.26		3.67		3.67		3.35

		S1148807671:		#B3q1		1148807671:		$B3q1		3.47		3.67		3.65		3.48		3.26		3.67		3.67		3.35

		S1148807701:		#B3q1		1148807701:		$B3q1		3.48		3.67		3.65		3.48		3.26		3.67		3.67		3.35

		S1148807731:		#B3q1		1148807731:		$B3q1		3.48		3.67		3.65		3.48		3.27		3.67		3.67		3.36

		S1148807761:		#B3q1		1148807761:		$B3q1		3.48		3.68		3.65		3.49		3.28		3.67		3.67		3.36

		S1148807791:		#B3q1		1148807791:		$B3q1		3.48		3.68		3.65		3.49		3.28		3.67		3.67		3.37

		S1148807821:		#B3q1		1148807821:		$B3q1		3.48		3.67		3.65		3.49		3.28		3.67		3.67		3.37

		S1148807851:		#B3q1		1148807851:		$B3q1		3.48		3.68		3.65		3.49		3.29		3.67		3.67		3.37

		S1148807881:		#B3q1		1148807881:		$B3q1		3.48		3.67		3.65		3.49		3.29		3.67		3.67		3.37

		S1148807911:		#B3q1		1148807911:		$B3q1		3.48		3.68		3.65		3.49		3.29		3.67		3.67		3.37

		S1148807941:		#B3q1		1148807941:		$B3q1		3.48		3.68		3.65		3.49		3.30		3.67		3.67		3.38

		S1148807971:		#B3q1		1148807971:		$B3q1		3.48		3.68		3.65		3.49		3.30		3.67		3.67		3.38

		S1148808001:		#B3q1		1148808001:		$B3q1		3.48		3.68		3.65		3.50		3.30		3.67		3.67		3.38

		S1148808031:		#B3q1		1148808031:		$B3q1		3.48		3.68		3.65		3.50		3.31		3.67		3.67		3.38

		S1148808061:		#B3q1		1148808061:		$B3q1		3.48		3.68		3.65		3.50		3.31		3.67		3.67		3.38

		S1148808091:		#B3q1		1148808091:		$B3q1		3.48		3.68		3.65		3.50		3.31		3.67		3.67		3.38

		S1148808121:		#B3q1		1148808121:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.38

		S1148808151:		#B3q1		1148808151:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.38

		S1148808181:		#B3q1		1148808181:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.39

		S1148808211:		#B3q1		1148808211:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.39

		S1148808241:		#B3q1		1148808241:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.39

		S1148808271:		#B3q1		1148808271:		$B3q1		3.48		3.68		3.65		3.50		3.32		3.67		3.67		3.39

		S1148808301:		#B3q1		1148808301:		$B3q1		3.48		3.68		3.65		3.50		3.33		3.67		3.67		3.39

		S1148808331:		#B3q1		1148808331:		$B3q1		3.48		3.68		3.65		3.50		3.33		3.67		3.67		3.39

		S1148808361:		#B3q1		1148808361:		$B3q1		3.48		3.68		3.65		3.50		3.33		3.67		3.67		3.39

		S1148808391:		#B3q1		1148808391:		$B3q1		3.49		3.68		3.65		3.50		3.33		3.67		3.67		3.39

		S1148808421:		#B3q1		1148808421:		$B3q1		3.49		3.68		3.65		3.50		3.33		3.67		3.67		3.39

		S1148808451:		#B3q1		1148808451:		$B3q1		3.49		3.68		3.65		3.50		3.33		3.67		3.67		3.40

		S1148808481:		#B3q1		1148808481:		$B3q1		3.49		3.68		3.65		3.51		3.34		3.67		3.67		3.40

		S1148808511:		#B3q1		1148808511:		$B3q1		3.49		3.68		3.65		3.51		3.34		3.67		3.67		3.40

		S1148808541:		#B3q1		1148808541:		$B3q1		3.49		3.68		3.65		3.51		3.34		3.67		3.67		3.40

		S1148808571:		#B3q1		1148808571:		$B3q1		3.49		3.68		3.65		3.51		3.34		3.67		3.67		3.40

		S1148808601:		#B3q1		1148808601:		$B3q1		3.49		3.68		3.65		3.51		3.34		3.67		3.67		3.40

		S1148808631:		#B3q1		1148808631:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.40

		S1148808661:		#B3q1		1148808661:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.40

		S1148808691:		#B3q1		1148808691:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808721:		#B3q1		1148808721:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808751:		#B3q1		1148808751:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808781:		#B3q1		1148808781:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808811:		#B3q1		1148808811:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808841:		#B3q1		1148808841:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808871:		#B3q1		1148808871:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.41

		S1148808901:		#B3q1		1148808901:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.42

		S1148808931:		#B3q1		1148808931:		$B3q1		3.49		3.68		3.65		3.51		3.35		3.67		3.67		3.42

		S1148808961:		#B3q1		1148808961:		$B3q1		3.49		3.68		3.65		3.51		3.36		3.67		3.67		3.42

		S1148808991:		#B3q1		1148808991:		$B3q1		3.50		3.68		3.65		3.51		3.36		3.67		3.67		3.42

		S1148809021:		#B3q1		1148809021:		$B3q1		3.50		3.68		3.65		3.51		3.36		3.67		3.67		3.42

		S1148809051:		#B3q1		1148809051:		$B3q1		3.50		3.68		3.65		3.51		3.36		3.67		3.67		3.43

		S1148809081:		#B3q1		1148809081:		$B3q1		3.50		3.68		3.65		3.51		3.36		3.67		3.67		3.43

		S1148809111:		#B3q1		1148809111:		$B3q1		3.50		3.68		3.65		3.51		3.36		3.67		3.67		3.43

		S1148809141:		#B3q1		1148809141:		$B3q1		3.50		3.68		3.65		3.52		3.36		3.67		3.67		3.43

		S1148809171:		#B3q1		1148809171:		$B3q1		3.50		3.68		3.65		3.52		3.36		3.67		3.67		3.43

		S1148809201:		#B3q1		1148809201:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.43

		S1148809231:		#B3q1		1148809231:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809261:		#B3q1		1148809261:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809291:		#B3q1		1148809291:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809321:		#B3q1		1148809321:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809351:		#B3q1		1148809351:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809381:		#B3q1		1148809381:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809411:		#B3q1		1148809411:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809441:		#B3q1		1148809441:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809471:		#B3q1		1148809471:		$B3q1		3.50		3.68		3.65		3.52		3.37		3.67		3.67		3.44

		S1148809501:		#B3q1		1148809501:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.44

		S1148809531:		#B3q1		1148809531:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.44

		S1148809561:		#B3q1		1148809561:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809591:		#B3q1		1148809591:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809621:		#B3q1		1148809621:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809651:		#B3q1		1148809651:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809681:		#B3q1		1148809681:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809711:		#B3q1		1148809711:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809741:		#B3q1		1148809741:		$B3q1		3.50		3.68		3.66		3.52		3.37		3.67		3.67		3.45

		S1148809771:		#B3q1		1148809771:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809801:		#B3q1		1148809801:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809831:		#B3q1		1148809831:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809861:		#B3q1		1148809861:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809891:		#B3q1		1148809891:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809921:		#B3q1		1148809921:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809951:		#B3q1		1148809951:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148809981:		#B3q1		1148809981:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148810011:		#B3q1		1148810011:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148810041:		#B3q1		1148810041:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148810071:		#B3q1		1148810071:		$B3q1		3.50		3.68		3.66		3.53		3.38		3.67		3.67		3.46

		S1148810101:		#B3q1		1148810101:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810131:		#B3q1		1148810131:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810161:		#B3q1		1148810161:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810191:		#B3q1		1148810191:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810221:		#B3q1		1148810221:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810251:		#B3q1		1148810251:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810281:		#B3q1		1148810281:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810311:		#B3q1		1148810311:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.47

		S1148810341:		#B3q1		1148810341:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810371:		#B3q1		1148810371:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810401:		#B3q1		1148810401:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810431:		#B3q1		1148810431:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810461:		#B3q1		1148810461:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810491:		#B3q1		1148810491:		$B3q1		3.51		3.68		3.66		3.53		3.38		3.67		3.67		3.48

		S1148810521:		#B3q1		1148810521:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810551:		#B3q1		1148810551:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810581:		#B3q1		1148810581:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810611:		#B3q1		1148810611:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810641:		#B3q1		1148810641:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810671:		#B3q1		1148810671:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810701:		#B3q1		1148810701:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810731:		#B3q1		1148810731:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810761:		#B3q1		1148810761:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.48

		S1148810791:		#B3q1		1148810791:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810821:		#B3q1		1148810821:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810851:		#B3q1		1148810851:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810881:		#B3q1		1148810881:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810911:		#B3q1		1148810911:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810941:		#B3q1		1148810941:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148810971:		#B3q1		1148810971:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811001:		#B3q1		1148811001:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811031:		#B3q1		1148811031:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811061:		#B3q1		1148811061:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811091:		#B3q1		1148811091:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811121:		#B3q1		1148811121:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811151:		#B3q1		1148811151:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811181:		#B3q1		1148811181:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811211:		#B3q1		1148811211:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811241:		#B3q1		1148811241:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811271:		#B3q1		1148811271:		$B3q1		3.51		3.68		3.66		3.53		3.39		3.67		3.67		3.49

		S1148811301:		#B3q1		1148811301:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.67		3.67		3.50

		S1148811331:		#B3q1		1148811331:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.67		3.67		3.50

		S1148811361:		#B3q1		1148811361:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.67		3.67		3.50

		S1148811391:		#B3q1		1148811391:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.67		3.67		3.50

		S1148811421:		#B3q1		1148811421:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.67		3.67		3.50

		S1148811451:		#B3q1		1148811451:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811481:		#B3q1		1148811481:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811511:		#B3q1		1148811511:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811541:		#B3q1		1148811541:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811571:		#B3q1		1148811571:		$B3q1		3.52		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811601:		#B3q1		1148811601:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811631:		#B3q1		1148811631:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811661:		#B3q1		1148811661:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811691:		#B3q1		1148811691:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811721:		#B3q1		1148811721:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811751:		#B3q1		1148811751:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811781:		#B3q1		1148811781:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811811:		#B3q1		1148811811:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811841:		#B3q1		1148811841:		$B3q1		3.53		3.68		3.66		3.53		3.39		3.68		3.67		3.50

		S1148811871:		#B3q1		1148811871:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148811901:		#B3q1		1148811901:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148811931:		#B3q1		1148811931:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148811961:		#B3q1		1148811961:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148811991:		#B3q1		1148811991:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148812021:		#B3q1		1148812021:		$B3q1		3.53		3.68		3.66		3.54		3.39		3.68		3.67		3.50

		S1148812051:		#B3q1		1148812051:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812081:		#B3q1		1148812081:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812111:		#B3q1		1148812111:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812141:		#B3q1		1148812141:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812171:		#B3q1		1148812171:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812201:		#B3q1		1148812201:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812231:		#B3q1		1148812231:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812261:		#B3q1		1148812261:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812291:		#B3q1		1148812291:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812321:		#B3q1		1148812321:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812351:		#B3q1		1148812351:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812381:		#B3q1		1148812381:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.50

		S1148812411:		#B3q1		1148812411:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.68		3.50

		S1148812441:		#B3q1		1148812441:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.67		3.51

		S1148812471:		#B3q1		1148812471:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812501:		#B3q1		1148812501:		$B3q1		3.53		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812531:		#B3q1		1148812531:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812561:		#B3q1		1148812561:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.67		3.51

		S1148812591:		#B3q1		1148812591:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812621:		#B3q1		1148812621:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.67		3.51

		S1148812651:		#B3q1		1148812651:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.67		3.51

		S1148812681:		#B3q1		1148812681:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812711:		#B3q1		1148812711:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812741:		#B3q1		1148812741:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812771:		#B3q1		1148812771:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812801:		#B3q1		1148812801:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812831:		#B3q1		1148812831:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812861:		#B3q1		1148812861:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812891:		#B3q1		1148812891:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812921:		#B3q1		1148812921:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812951:		#B3q1		1148812951:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148812981:		#B3q1		1148812981:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813011:		#B3q1		1148813011:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813041:		#B3q1		1148813041:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813071:		#B3q1		1148813071:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813101:		#B3q1		1148813101:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813131:		#B3q1		1148813131:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813161:		#B3q1		1148813161:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813191:		#B3q1		1148813191:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813221:		#B3q1		1148813221:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813251:		#B3q1		1148813251:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813281:		#B3q1		1148813281:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813311:		#B3q1		1148813311:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813341:		#B3q1		1148813341:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813371:		#B3q1		1148813371:		$B3q1		3.54		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813401:		#B3q1		1148813401:		$B3q1		3.55		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813431:		#B3q1		1148813431:		$B3q1		3.55		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813461:		#B3q1		1148813461:		$B3q1		3.55		3.68		3.66		3.54		3.41		3.68		3.68		3.51

		S1148813491:		#B3q1		1148813491:		$B3q1		3.55		3.68		3.66		3.54		3.40		3.68		3.68		3.51

		S1148813521:		#B3q1		1148813521:		$B3q1		3.55		3.68		3.66		3.54		3.41		3.68		3.68		3.51

		S1148813551:		#B3q1		1148813551:		$B3q1		3.55		3.68		3.66		3.54		3.41		3.68		3.68		3.51

		S1148813581:		#B3q1		1148813581:		$B3q1		3.55		3.68		3.66		3.54		3.41		3.68		3.68		3.51

		S1148813611:		#B3q1		1148813611:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813641:		#B3q1		1148813641:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813671:		#B3q1		1148813671:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813701:		#B3q1		1148813701:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813731:		#B3q1		1148813731:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813761:		#B3q1		1148813761:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813791:		#B3q1		1148813791:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813821:		#B3q1		1148813821:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813851:		#B3q1		1148813851:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813881:		#B3q1		1148813881:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813911:		#B3q1		1148813911:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813941:		#B3q1		1148813941:		$B3q1		3.55		3.68		3.66		3.54		3.42		3.68		3.68		3.51

		S1148813971:		#B3q1		1148813971:		$B3q1		3.55		3.68		3.66		3.54		3.43		3.68		3.68		3.51

		S1148814001:		#B3q1		1148814001:		$B3q1		3.55		3.68		3.66		3.54		3.43		3.68		3.68		3.51

		S1148814031:		#B3q1		1148814031:		$B3q1		3.55		3.68		3.66		3.54		3.43		3.68		3.68		3.51

		S1148814061:		#B3q1		1148814061:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814091:		#B3q1		1148814091:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814121:		#B3q1		1148814121:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814151:		#B3q1		1148814151:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814181:		#B3q1		1148814181:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814211:		#B3q1		1148814211:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814241:		#B3q1		1148814241:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814271:		#B3q1		1148814271:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814301:		#B3q1		1148814301:		$B3q1		3.55		3.68		3.66		3.55		3.43		3.68		3.68		3.51

		S1148814331:		#B3q1		1148814331:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814361:		#B3q1		1148814361:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814391:		#B3q1		1148814391:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814421:		#B3q1		1148814421:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814451:		#B3q1		1148814451:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814481:		#B3q1		1148814481:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814511:		#B3q1		1148814511:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814541:		#B3q1		1148814541:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814571:		#B3q1		1148814571:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814601:		#B3q1		1148814601:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814631:		#B3q1		1148814631:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814661:		#B3q1		1148814661:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814691:		#B3q1		1148814691:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814721:		#B3q1		1148814721:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814751:		#B3q1		1148814751:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814781:		#B3q1		1148814781:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814811:		#B3q1		1148814811:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814841:		#B3q1		1148814841:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814871:		#B3q1		1148814871:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814901:		#B3q1		1148814901:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814931:		#B3q1		1148814931:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814961:		#B3q1		1148814961:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148814991:		#B3q1		1148814991:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148815021:		#B3q1		1148815021:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148815051:		#B3q1		1148815051:		$B3q1		3.55		3.68		3.66		3.55		3.44		3.68		3.68		3.51

		S1148815081:		#B3q1		1148815081:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815111:		#B3q1		1148815111:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815141:		#B3q1		1148815141:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815171:		#B3q1		1148815171:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815201:		#B3q1		1148815201:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815231:		#B3q1		1148815231:		$B3q1		3.55		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815261:		#B3q1		1148815261:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.51

		S1148815291:		#B3q1		1148815291:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815321:		#B3q1		1148815321:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815351:		#B3q1		1148815351:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815381:		#B3q1		1148815381:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815411:		#B3q1		1148815411:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815441:		#B3q1		1148815441:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815471:		#B3q1		1148815471:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815501:		#B3q1		1148815501:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815531:		#B3q1		1148815531:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815561:		#B3q1		1148815561:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815591:		#B3q1		1148815591:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815621:		#B3q1		1148815621:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815651:		#B3q1		1148815651:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815681:		#B3q1		1148815681:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815711:		#B3q1		1148815711:		$B3q1		3.56		3.68		3.66		3.55		3.45		3.68		3.68		3.52

		S1148815741:		#B3q1		1148815741:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815771:		#B3q1		1148815771:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815801:		#B3q1		1148815801:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815831:		#B3q1		1148815831:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815861:		#B3q1		1148815861:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815891:		#B3q1		1148815891:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815921:		#B3q1		1148815921:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815951:		#B3q1		1148815951:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148815981:		#B3q1		1148815981:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816011:		#B3q1		1148816011:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816041:		#B3q1		1148816041:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816071:		#B3q1		1148816071:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816101:		#B3q1		1148816101:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816131:		#B3q1		1148816131:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816161:		#B3q1		1148816161:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816191:		#B3q1		1148816191:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816221:		#B3q1		1148816221:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816251:		#B3q1		1148816251:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816281:		#B3q1		1148816281:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816311:		#B3q1		1148816311:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816341:		#B3q1		1148816341:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816371:		#B3q1		1148816371:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816401:		#B3q1		1148816401:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816431:		#B3q1		1148816431:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816461:		#B3q1		1148816461:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816491:		#B3q1		1148816491:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816521:		#B3q1		1148816521:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816551:		#B3q1		1148816551:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816581:		#B3q1		1148816581:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816611:		#B3q1		1148816611:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816641:		#B3q1		1148816641:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816671:		#B3q1		1148816671:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816701:		#B3q1		1148816701:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816731:		#B3q1		1148816731:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816761:		#B3q1		1148816761:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816791:		#B3q1		1148816791:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816821:		#B3q1		1148816821:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816851:		#B3q1		1148816851:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816881:		#B3q1		1148816881:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816911:		#B3q1		1148816911:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816941:		#B3q1		1148816941:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148816971:		#B3q1		1148816971:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817001:		#B3q1		1148817001:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817031:		#B3q1		1148817031:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817061:		#B3q1		1148817061:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817091:		#B3q1		1148817091:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817121:		#B3q1		1148817121:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817151:		#B3q1		1148817151:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817181:		#B3q1		1148817181:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817211:		#B3q1		1148817211:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817241:		#B3q1		1148817241:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817271:		#B3q1		1148817271:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817301:		#B3q1		1148817301:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817331:		#B3q1		1148817331:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817361:		#B3q1		1148817361:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817391:		#B3q1		1148817391:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817421:		#B3q1		1148817421:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817451:		#B3q1		1148817451:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817481:		#B3q1		1148817481:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817511:		#B3q1		1148817511:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817541:		#B3q1		1148817541:		$B3q1		3.56		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817571:		#B3q1		1148817571:		$B3q1		3.56		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817601:		#B3q1		1148817601:		$B3q1		3.57		3.68		3.66		3.55		3.46		3.68		3.68		3.52

		S1148817631:		#B3q1		1148817631:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817661:		#B3q1		1148817661:		$B3q1		3.56		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817691:		#B3q1		1148817691:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817721:		#B3q1		1148817721:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817751:		#B3q1		1148817751:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817781:		#B3q1		1148817781:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817811:		#B3q1		1148817811:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817841:		#B3q1		1148817841:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817871:		#B3q1		1148817871:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817901:		#B3q1		1148817901:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817931:		#B3q1		1148817931:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817961:		#B3q1		1148817961:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148817991:		#B3q1		1148817991:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818021:		#B3q1		1148818021:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818051:		#B3q1		1148818051:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818081:		#B3q1		1148818081:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818111:		#B3q1		1148818111:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818141:		#B3q1		1148818141:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818171:		#B3q1		1148818171:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818201:		#B3q1		1148818201:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818231:		#B3q1		1148818231:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.52

		S1148818261:		#B3q1		1148818261:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818291:		#B3q1		1148818291:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818321:		#B3q1		1148818321:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818351:		#B3q1		1148818351:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818381:		#B3q1		1148818381:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818411:		#B3q1		1148818411:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818441:		#B3q1		1148818441:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818471:		#B3q1		1148818471:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818501:		#B3q1		1148818501:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818531:		#B3q1		1148818531:		$B3q1		3.57		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818561:		#B3q1		1148818561:		$B3q1		3.57		3.69		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818591:		#B3q1		1148818591:		$B3q1		3.58		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818621:		#B3q1		1148818621:		$B3q1		3.58		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818651:		#B3q1		1148818651:		$B3q1		3.58		3.68		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818681:		#B3q1		1148818681:		$B3q1		3.58		3.69		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818711:		#B3q1		1148818711:		$B3q1		3.58		3.69		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818741:		#B3q1		1148818741:		$B3q1		3.58		3.69		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818771:		#B3q1		1148818771:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818801:		#B3q1		1148818801:		$B3q1		3.58		3.69		3.66		3.55		3.47		3.68		3.68		3.53

		S1148818831:		#B3q1		1148818831:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818861:		#B3q1		1148818861:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818891:		#B3q1		1148818891:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818921:		#B3q1		1148818921:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818951:		#B3q1		1148818951:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148818981:		#B3q1		1148818981:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819011:		#B3q1		1148819011:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819041:		#B3q1		1148819041:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819071:		#B3q1		1148819071:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819101:		#B3q1		1148819101:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819131:		#B3q1		1148819131:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819161:		#B3q1		1148819161:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819191:		#B3q1		1148819191:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819221:		#B3q1		1148819221:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819251:		#B3q1		1148819251:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819281:		#B3q1		1148819281:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819311:		#B3q1		1148819311:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819341:		#B3q1		1148819341:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819371:		#B3q1		1148819371:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819401:		#B3q1		1148819401:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819431:		#B3q1		1148819431:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819461:		#B3q1		1148819461:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819491:		#B3q1		1148819491:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819521:		#B3q1		1148819521:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819551:		#B3q1		1148819551:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819581:		#B3q1		1148819581:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819611:		#B3q1		1148819611:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819641:		#B3q1		1148819641:		$B3q1		3.58		3.68		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819671:		#B3q1		1148819671:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819701:		#B3q1		1148819701:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819731:		#B3q1		1148819731:		$B3q1		3.58		3.69		3.66		3.56		3.47		3.68		3.68		3.53

		S1148819761:		#B3q1		1148819761:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819791:		#B3q1		1148819791:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819821:		#B3q1		1148819821:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819851:		#B3q1		1148819851:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819881:		#B3q1		1148819881:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819911:		#B3q1		1148819911:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819941:		#B3q1		1148819941:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148819971:		#B3q1		1148819971:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820001:		#B3q1		1148820001:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820031:		#B3q1		1148820031:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820061:		#B3q1		1148820061:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820091:		#B3q1		1148820091:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820121:		#B3q1		1148820121:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820151:		#B3q1		1148820151:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820181:		#B3q1		1148820181:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820211:		#B3q1		1148820211:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820241:		#B3q1		1148820241:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820271:		#B3q1		1148820271:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820301:		#B3q1		1148820301:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820331:		#B3q1		1148820331:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820361:		#B3q1		1148820361:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820391:		#B3q1		1148820391:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820421:		#B3q1		1148820421:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820451:		#B3q1		1148820451:		$B3q1		3.58		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820481:		#B3q1		1148820481:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820511:		#B3q1		1148820511:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820541:		#B3q1		1148820541:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820571:		#B3q1		1148820571:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820601:		#B3q1		1148820601:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820631:		#B3q1		1148820631:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820661:		#B3q1		1148820661:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820691:		#B3q1		1148820691:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820721:		#B3q1		1148820721:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820751:		#B3q1		1148820751:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820781:		#B3q1		1148820781:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820811:		#B3q1		1148820811:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820841:		#B3q1		1148820841:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820871:		#B3q1		1148820871:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820901:		#B3q1		1148820901:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820931:		#B3q1		1148820931:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820961:		#B3q1		1148820961:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148820991:		#B3q1		1148820991:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821021:		#B3q1		1148821021:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821051:		#B3q1		1148821051:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821081:		#B3q1		1148821081:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821111:		#B3q1		1148821111:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821141:		#B3q1		1148821141:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821171:		#B3q1		1148821171:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821201:		#B3q1		1148821201:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821231:		#B3q1		1148821231:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821261:		#B3q1		1148821261:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821291:		#B3q1		1148821291:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821321:		#B3q1		1148821321:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821351:		#B3q1		1148821351:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821381:		#B3q1		1148821381:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821411:		#B3q1		1148821411:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.53

		S1148821441:		#B3q1		1148821441:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821471:		#B3q1		1148821471:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821501:		#B3q1		1148821501:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821531:		#B3q1		1148821531:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821561:		#B3q1		1148821561:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821591:		#B3q1		1148821591:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821621:		#B3q1		1148821621:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821651:		#B3q1		1148821651:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821681:		#B3q1		1148821681:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821711:		#B3q1		1148821711:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821741:		#B3q1		1148821741:		$B3q1		3.59		3.69		3.67		3.56		3.47		3.68		3.68		3.54

		S1148821771:		#B3q1		1148821771:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821801:		#B3q1		1148821801:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821831:		#B3q1		1148821831:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821861:		#B3q1		1148821861:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821891:		#B3q1		1148821891:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821921:		#B3q1		1148821921:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821951:		#B3q1		1148821951:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148821981:		#B3q1		1148821981:		$B3q1		3.59		3.69		3.67		3.56		3.48		3.68		3.68		3.54

		S1148822011:		#B3q1		1148822011:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822041:		#B3q1		1148822041:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822071:		#B3q1		1148822071:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822101:		#B3q1		1148822101:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822131:		#B3q1		1148822131:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822161:		#B3q1		1148822161:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822191:		#B3q1		1148822191:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822221:		#B3q1		1148822221:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822251:		#B3q1		1148822251:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822281:		#B3q1		1148822281:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822311:		#B3q1		1148822311:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822341:		#B3q1		1148822341:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822371:		#B3q1		1148822371:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822401:		#B3q1		1148822401:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822431:		#B3q1		1148822431:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822461:		#B3q1		1148822461:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822491:		#B3q1		1148822491:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822521:		#B3q1		1148822521:		$B3q1		3.59		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822551:		#B3q1		1148822551:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822581:		#B3q1		1148822581:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822611:		#B3q1		1148822611:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822641:		#B3q1		1148822641:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822671:		#B3q1		1148822671:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822701:		#B3q1		1148822701:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822731:		#B3q1		1148822731:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822761:		#B3q1		1148822761:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822791:		#B3q1		1148822791:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822821:		#B3q1		1148822821:		$B3q1		3.60		3.69		3.67		3.57		3.48		3.68		3.68		3.54

		S1148822851:		#B3q1		1148822851:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148822881:		#B3q1		1148822881:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148822911:		#B3q1		1148822911:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148822941:		#B3q1		1148822941:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148822971:		#B3q1		1148822971:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823001:		#B3q1		1148823001:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823031:		#B3q1		1148823031:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823061:		#B3q1		1148823061:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823091:		#B3q1		1148823091:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823121:		#B3q1		1148823121:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823151:		#B3q1		1148823151:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823181:		#B3q1		1148823181:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823211:		#B3q1		1148823211:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823241:		#B3q1		1148823241:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823271:		#B3q1		1148823271:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823301:		#B3q1		1148823301:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823331:		#B3q1		1148823331:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823361:		#B3q1		1148823361:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823391:		#B3q1		1148823391:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823421:		#B3q1		1148823421:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823451:		#B3q1		1148823451:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823481:		#B3q1		1148823481:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823511:		#B3q1		1148823511:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823541:		#B3q1		1148823541:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823571:		#B3q1		1148823571:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823601:		#B3q1		1148823601:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823631:		#B3q1		1148823631:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823661:		#B3q1		1148823661:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823691:		#B3q1		1148823691:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823721:		#B3q1		1148823721:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823751:		#B3q1		1148823751:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823781:		#B3q1		1148823781:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823811:		#B3q1		1148823811:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823841:		#B3q1		1148823841:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823871:		#B3q1		1148823871:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823901:		#B3q1		1148823901:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823931:		#B3q1		1148823931:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823961:		#B3q1		1148823961:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148823991:		#B3q1		1148823991:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824021:		#B3q1		1148824021:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824051:		#B3q1		1148824051:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824081:		#B3q1		1148824081:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824111:		#B3q1		1148824111:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824141:		#B3q1		1148824141:		$B3q1		3.60		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824171:		#B3q1		1148824171:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824201:		#B3q1		1148824201:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824231:		#B3q1		1148824231:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824261:		#B3q1		1148824261:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824291:		#B3q1		1148824291:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824321:		#B3q1		1148824321:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824351:		#B3q1		1148824351:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824381:		#B3q1		1148824381:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824411:		#B3q1		1148824411:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824441:		#B3q1		1148824441:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824471:		#B3q1		1148824471:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824501:		#B3q1		1148824501:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824531:		#B3q1		1148824531:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824561:		#B3q1		1148824561:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824591:		#B3q1		1148824591:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824621:		#B3q1		1148824621:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824651:		#B3q1		1148824651:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824681:		#B3q1		1148824681:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824711:		#B3q1		1148824711:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824741:		#B3q1		1148824741:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824771:		#B3q1		1148824771:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824801:		#B3q1		1148824801:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824831:		#B3q1		1148824831:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824861:		#B3q1		1148824861:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824891:		#B3q1		1148824891:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.69		3.68		3.54

		S1148824921:		#B3q1		1148824921:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824951:		#B3q1		1148824951:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148824981:		#B3q1		1148824981:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825011:		#B3q1		1148825011:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825041:		#B3q1		1148825041:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825071:		#B3q1		1148825071:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825101:		#B3q1		1148825101:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825131:		#B3q1		1148825131:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825161:		#B3q1		1148825161:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825191:		#B3q1		1148825191:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825221:		#B3q1		1148825221:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825251:		#B3q1		1148825251:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825281:		#B3q1		1148825281:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825311:		#B3q1		1148825311:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825341:		#B3q1		1148825341:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825371:		#B3q1		1148825371:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825401:		#B3q1		1148825401:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825431:		#B3q1		1148825431:		$B3q1		3.61		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825461:		#B3q1		1148825461:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825491:		#B3q1		1148825491:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825521:		#B3q1		1148825521:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825551:		#B3q1		1148825551:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.69		3.68		3.54

		S1148825581:		#B3q1		1148825581:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825611:		#B3q1		1148825611:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825641:		#B3q1		1148825641:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825671:		#B3q1		1148825671:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825701:		#B3q1		1148825701:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825731:		#B3q1		1148825731:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825761:		#B3q1		1148825761:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825791:		#B3q1		1148825791:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825821:		#B3q1		1148825821:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825851:		#B3q1		1148825851:		$B3q1		3.62		3.69		3.67		3.58		3.48		3.68		3.68		3.54

		S1148825881:		#B3q1		1148825881:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148825911:		#B3q1		1148825911:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148825941:		#B3q1		1148825941:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148825971:		#B3q1		1148825971:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826001:		#B3q1		1148826001:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826031:		#B3q1		1148826031:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826061:		#B3q1		1148826061:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826091:		#B3q1		1148826091:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826121:		#B3q1		1148826121:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826151:		#B3q1		1148826151:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826181:		#B3q1		1148826181:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826211:		#B3q1		1148826211:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826241:		#B3q1		1148826241:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826271:		#B3q1		1148826271:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826301:		#B3q1		1148826301:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826331:		#B3q1		1148826331:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826361:		#B3q1		1148826361:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826391:		#B3q1		1148826391:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826421:		#B3q1		1148826421:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826451:		#B3q1		1148826451:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826481:		#B3q1		1148826481:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826511:		#B3q1		1148826511:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826541:		#B3q1		1148826541:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826571:		#B3q1		1148826571:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826601:		#B3q1		1148826601:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826631:		#B3q1		1148826631:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826661:		#B3q1		1148826661:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826691:		#B3q1		1148826691:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826721:		#B3q1		1148826721:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826751:		#B3q1		1148826751:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826781:		#B3q1		1148826781:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826811:		#B3q1		1148826811:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148826841:		#B3q1		1148826841:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826871:		#B3q1		1148826871:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826901:		#B3q1		1148826901:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826931:		#B3q1		1148826931:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826961:		#B3q1		1148826961:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148826991:		#B3q1		1148826991:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827021:		#B3q1		1148827021:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827051:		#B3q1		1148827051:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827081:		#B3q1		1148827081:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827111:		#B3q1		1148827111:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827141:		#B3q1		1148827141:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827171:		#B3q1		1148827171:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827201:		#B3q1		1148827201:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827231:		#B3q1		1148827231:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827261:		#B3q1		1148827261:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827291:		#B3q1		1148827291:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827321:		#B3q1		1148827321:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827351:		#B3q1		1148827351:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827381:		#B3q1		1148827381:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827411:		#B3q1		1148827411:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827441:		#B3q1		1148827441:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827471:		#B3q1		1148827471:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827501:		#B3q1		1148827501:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827531:		#B3q1		1148827531:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827561:		#B3q1		1148827561:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827591:		#B3q1		1148827591:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827621:		#B3q1		1148827621:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827651:		#B3q1		1148827651:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827681:		#B3q1		1148827681:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827711:		#B3q1		1148827711:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827741:		#B3q1		1148827741:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827771:		#B3q1		1148827771:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827801:		#B3q1		1148827801:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.69		3.68		3.54

		S1148827831:		#B3q1		1148827831:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827861:		#B3q1		1148827861:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827891:		#B3q1		1148827891:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148827921:		#B3q1		1148827921:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148827951:		#B3q1		1148827951:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148827981:		#B3q1		1148827981:		$B3q1		3.62		3.69		3.67		3.59		3.48		3.68		3.68		3.54

		S1148828011:		#B3q1		1148828011:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828041:		#B3q1		1148828041:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828071:		#B3q1		1148828071:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828101:		#B3q1		1148828101:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828131:		#B3q1		1148828131:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.54

		S1148828161:		#B3q1		1148828161:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.54

		S1148828191:		#B3q1		1148828191:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828221:		#B3q1		1148828221:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.54

		S1148828251:		#B3q1		1148828251:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828281:		#B3q1		1148828281:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828311:		#B3q1		1148828311:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828341:		#B3q1		1148828341:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828371:		#B3q1		1148828371:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828401:		#B3q1		1148828401:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.54

		S1148828431:		#B3q1		1148828431:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.54

		S1148828461:		#B3q1		1148828461:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828491:		#B3q1		1148828491:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828521:		#B3q1		1148828521:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828551:		#B3q1		1148828551:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828581:		#B3q1		1148828581:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828611:		#B3q1		1148828611:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828641:		#B3q1		1148828641:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828671:		#B3q1		1148828671:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828701:		#B3q1		1148828701:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828731:		#B3q1		1148828731:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828761:		#B3q1		1148828761:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828791:		#B3q1		1148828791:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148828821:		#B3q1		1148828821:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828851:		#B3q1		1148828851:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828881:		#B3q1		1148828881:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828911:		#B3q1		1148828911:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828941:		#B3q1		1148828941:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148828971:		#B3q1		1148828971:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829001:		#B3q1		1148829001:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829031:		#B3q1		1148829031:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829061:		#B3q1		1148829061:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829091:		#B3q1		1148829091:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829121:		#B3q1		1148829121:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829151:		#B3q1		1148829151:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829181:		#B3q1		1148829181:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829211:		#B3q1		1148829211:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829241:		#B3q1		1148829241:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829271:		#B3q1		1148829271:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829301:		#B3q1		1148829301:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829331:		#B3q1		1148829331:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829361:		#B3q1		1148829361:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829391:		#B3q1		1148829391:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829421:		#B3q1		1148829421:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148829451:		#B3q1		1148829451:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829481:		#B3q1		1148829481:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829511:		#B3q1		1148829511:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829541:		#B3q1		1148829541:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829571:		#B3q1		1148829571:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829601:		#B3q1		1148829601:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829631:		#B3q1		1148829631:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829661:		#B3q1		1148829661:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829691:		#B3q1		1148829691:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829721:		#B3q1		1148829721:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829751:		#B3q1		1148829751:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829781:		#B3q1		1148829781:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829811:		#B3q1		1148829811:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829841:		#B3q1		1148829841:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829871:		#B3q1		1148829871:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829901:		#B3q1		1148829901:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829931:		#B3q1		1148829931:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829961:		#B3q1		1148829961:		$B3q1		3.62		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148829991:		#B3q1		1148829991:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830021:		#B3q1		1148830021:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830051:		#B3q1		1148830051:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830081:		#B3q1		1148830081:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148830111:		#B3q1		1148830111:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830141:		#B3q1		1148830141:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830171:		#B3q1		1148830171:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830201:		#B3q1		1148830201:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830231:		#B3q1		1148830231:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830261:		#B3q1		1148830261:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830291:		#B3q1		1148830291:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830321:		#B3q1		1148830321:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830351:		#B3q1		1148830351:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830381:		#B3q1		1148830381:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830411:		#B3q1		1148830411:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148830441:		#B3q1		1148830441:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148830471:		#B3q1		1148830471:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830501:		#B3q1		1148830501:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830531:		#B3q1		1148830531:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830561:		#B3q1		1148830561:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148830591:		#B3q1		1148830591:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.69		3.68		3.55

		S1148830621:		#B3q1		1148830621:		$B3q1		3.63		3.69		3.67		3.59		3.49		3.68		3.68		3.55

		S1148830651:		#B3q1		1148830651:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830681:		#B3q1		1148830681:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830711:		#B3q1		1148830711:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830741:		#B3q1		1148830741:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830771:		#B3q1		1148830771:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830801:		#B3q1		1148830801:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830831:		#B3q1		1148830831:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830861:		#B3q1		1148830861:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.68		3.68		3.55

		S1148830891:		#B3q1		1148830891:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148830921:		#B3q1		1148830921:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.68		3.68		3.55

		S1148830951:		#B3q1		1148830951:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.68		3.68		3.55

		S1148830981:		#B3q1		1148830981:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831011:		#B3q1		1148831011:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831041:		#B3q1		1148831041:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831071:		#B3q1		1148831071:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831101:		#B3q1		1148831101:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831131:		#B3q1		1148831131:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831161:		#B3q1		1148831161:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831191:		#B3q1		1148831191:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831221:		#B3q1		1148831221:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831251:		#B3q1		1148831251:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831281:		#B3q1		1148831281:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831311:		#B3q1		1148831311:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831341:		#B3q1		1148831341:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831371:		#B3q1		1148831371:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831401:		#B3q1		1148831401:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831431:		#B3q1		1148831431:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831461:		#B3q1		1148831461:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831491:		#B3q1		1148831491:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831521:		#B3q1		1148831521:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831551:		#B3q1		1148831551:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831581:		#B3q1		1148831581:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831611:		#B3q1		1148831611:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831641:		#B3q1		1148831641:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831671:		#B3q1		1148831671:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831701:		#B3q1		1148831701:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831731:		#B3q1		1148831731:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831761:		#B3q1		1148831761:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831791:		#B3q1		1148831791:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831821:		#B3q1		1148831821:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831851:		#B3q1		1148831851:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831881:		#B3q1		1148831881:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831911:		#B3q1		1148831911:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831941:		#B3q1		1148831941:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148831971:		#B3q1		1148831971:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832001:		#B3q1		1148832001:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832031:		#B3q1		1148832031:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832061:		#B3q1		1148832061:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832091:		#B3q1		1148832091:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832121:		#B3q1		1148832121:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832151:		#B3q1		1148832151:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832181:		#B3q1		1148832181:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832211:		#B3q1		1148832211:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832241:		#B3q1		1148832241:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832271:		#B3q1		1148832271:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832301:		#B3q1		1148832301:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832331:		#B3q1		1148832331:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832361:		#B3q1		1148832361:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832391:		#B3q1		1148832391:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832421:		#B3q1		1148832421:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832451:		#B3q1		1148832451:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832481:		#B3q1		1148832481:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832511:		#B3q1		1148832511:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832541:		#B3q1		1148832541:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832571:		#B3q1		1148832571:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832601:		#B3q1		1148832601:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832631:		#B3q1		1148832631:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832661:		#B3q1		1148832661:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832691:		#B3q1		1148832691:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832721:		#B3q1		1148832721:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832751:		#B3q1		1148832751:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832781:		#B3q1		1148832781:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832811:		#B3q1		1148832811:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832841:		#B3q1		1148832841:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832871:		#B3q1		1148832871:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832901:		#B3q1		1148832901:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832931:		#B3q1		1148832931:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832961:		#B3q1		1148832961:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148832991:		#B3q1		1148832991:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833021:		#B3q1		1148833021:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833051:		#B3q1		1148833051:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833081:		#B3q1		1148833081:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833111:		#B3q1		1148833111:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833141:		#B3q1		1148833141:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833171:		#B3q1		1148833171:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833201:		#B3q1		1148833201:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833231:		#B3q1		1148833231:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833261:		#B3q1		1148833261:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833291:		#B3q1		1148833291:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833321:		#B3q1		1148833321:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833351:		#B3q1		1148833351:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833381:		#B3q1		1148833381:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833411:		#B3q1		1148833411:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833441:		#B3q1		1148833441:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833471:		#B3q1		1148833471:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833501:		#B3q1		1148833501:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833531:		#B3q1		1148833531:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833561:		#B3q1		1148833561:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833591:		#B3q1		1148833591:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833621:		#B3q1		1148833621:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833651:		#B3q1		1148833651:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833681:		#B3q1		1148833681:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833711:		#B3q1		1148833711:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833741:		#B3q1		1148833741:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833771:		#B3q1		1148833771:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833801:		#B3q1		1148833801:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833831:		#B3q1		1148833831:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55

		S1148833861:		#B3q1		1148833861:		$B3q1		3.63		3.69		3.67		3.60		3.49		3.69		3.68		3.55





Chart3

		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111

		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333

		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556

		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778

		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125

		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222

		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444

		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667

		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889

		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111

		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333

		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556

		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778

		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625

		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222

		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444

		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667

		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889

		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111

		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333

		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556

		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778

		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375

		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222

		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444

		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667

		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889

		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111

		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333

		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556

		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778

		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125

		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222

		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444

		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667

		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889

		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111

		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333

		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556

		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778

		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625

		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222

		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444

		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667

		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889

		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111

		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333

		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556

		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778

		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875

		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222

		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444

		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667

		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889

		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111

		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333

		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556

		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778

		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875

		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222

		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444

		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667

		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889

		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111

		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333

		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556

		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778

		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741		0.0250115741

		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222

		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444

		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667

		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889

		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111

		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333

		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556

		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519		0.0277893519

		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125

		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222

		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444

		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667		0.0291666667

		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889

		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111

		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074		0.0302199074

		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556

		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778

		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125

		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222

		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444

		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667

		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889

		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111

		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333

		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556

		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778

		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375

		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222

		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444

		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667

		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889

		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111

		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333

		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556

		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778

		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375

		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222

		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444

		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667

		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889

		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111

		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333

		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556

		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778

		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625

		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222

		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444

		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667

		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889

		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111

		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333

		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556

		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778

		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375

		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222

		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444

		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667

		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889

		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111

		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333

		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556

		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778

		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741		0.0468865741

		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222

		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444

		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667

		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889

		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111

		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333

		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556

		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778

		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741		0.0500115741

		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222

		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444

		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667

		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889

		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111

		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333

		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556

		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778

		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125

		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222

		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444

		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667

		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889

		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111

		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333

		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296		0.0555671296

		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519		0.0559143519

		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625

		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222

		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444

		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667

		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889

		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111

		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333

		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556

		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778

		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375

		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222

		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444

		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667

		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889

		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111

		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333

		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556

		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778

		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625

		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222

		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444

		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667

		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463		0.063900463

		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111

		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333

		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296		0.0649421296

		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778

		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625

		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222

		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444

		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667

		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889

		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111

		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333

		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556

		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778

		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875

		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222

		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444

		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667

		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889

		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111

		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333

		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556

		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519		0.0715393519

		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875

		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963		0.0722337963

		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444

		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667

		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889

		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111

		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333

		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556

		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778

		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075

		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222		0.0753472222

		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444

		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667

		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889

		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111

		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333

		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556

		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778

		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125

		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222

		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444

		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667

		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889

		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111

		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333

		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296		0.0805671296

		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778

		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125

		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963		0.0816087963

		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444

		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667

		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889

		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111

		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333

		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556

		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778

		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375

		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222

		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185		0.0850810185

		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667

		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889

		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111

		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333

		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556

		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778

		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875

		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222

		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185		0.0882060185

		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667

		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889

		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111

		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333

		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556

		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778

		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625

		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222

		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444

		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407		0.0916782407

		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889

		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111

		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333

		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556

		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778

		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375

		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963		0.0941087963

		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444

		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407		0.0948032407

		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889

		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111

		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333

		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556

		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778

		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875

		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222

		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444

		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667

		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463		0.098275463

		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852		0.0986226852

		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333

		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556

		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519		0.0996643519

		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1

		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222

		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444

		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667

		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889

		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111

		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333

		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556

		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778

		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125

		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222

		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444

		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667

		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889

		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111

		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333

		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556

		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778

		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741		0.1062615741

		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222

		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444

		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667

		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889

		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111

		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333

		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556

		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519		0.1090393519

		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375

		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963		0.1097337963

		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185		0.1100810185

		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407		0.1104282407

		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889

		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852		0.1111226852

		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333

		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556

		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778

		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741		0.1125115741

		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222

		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444

		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667

		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889

		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111

		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333

		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296		0.1149421296

		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519		0.1152893519

		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625

		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222

		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185		0.1163310185

		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407		0.1166782407

		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889

		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111

		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333

		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556

		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519		0.1184143519

		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875

		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222

		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444

		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667

		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889

		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111

		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333

		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296		0.1211921296

		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778

		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875

		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222

		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185		0.1225810185

		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667

		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889

		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111

		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333

		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556

		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778

		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125

		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222

		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444

		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667

		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463		0.126400463

		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852		0.1267476852

		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333

		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556

		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778

		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125

		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222

		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444

		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667

		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889

		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111

		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333

		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556

		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778

		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741		0.1312615741

		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222

		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444

		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667

		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889

		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111

		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074		0.1333449074

		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556

		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778

		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375

		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963		0.1347337963

		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444

		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667

		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889

		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111

		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333

		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556

		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778

		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375

		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222

		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185		0.1382060185

		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667

		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889

		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852		0.1392476852

		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333

		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296		0.1399421296

		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519		0.1402893519

		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741		0.1406365741

		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963		0.1409837963

		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444

		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667

		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111		0.1782986111

		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593		0.1786342593

		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556		0.1789930556

		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037		0.1793287037

		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875		0.1796875

		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222		0.1800347222

		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444		0.1803819444

		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667		0.1807291667

		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148		0.1810648148

		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111		0.1814236111

		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333		0.1817708333

		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556		0.1821180556

		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778		0.1824652778

		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125		0.1828125

		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481		0.1831481481

		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444		0.1835069444

		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926		0.1838425926

		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889		0.1842013889

		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037		0.184537037

		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593		0.1848842593

		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556		0.1852430556

		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778		0.1855902778

		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375		0.1859375

		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222		0.1862847222

		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704		0.1866203704

		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667		0.1869791667

		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889		0.1873263889

		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111		0.1876736111

		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593		0.1880092593

		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556		0.1883680556

		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778		0.1887152778

		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625		0.1890625

		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481		0.1893981481

		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444		0.1897569444

		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667		0.1901041667

		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889		0.1904513889

		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111		0.1907986111

		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593		0.1911342593

		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815		0.1914814815

		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778		0.1918402778

		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259		0.1921759259

		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481		0.1925231481

		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444		0.1928819444

		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926		0.1932175926

		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889		0.1935763889

		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111		0.1939236111

		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593		0.1942592593

		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815		0.1946064815

		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778		0.1949652778

		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125		0.1953125

		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222		0.1956597222

		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444		0.1960069444

		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667		0.1963541667

		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148		0.1966898148

		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111		0.1970486111

		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333		0.1973958333

		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556		0.1977430556

		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037		0.1980787037

		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375		0.1984375

		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222		0.1987847222

		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444		0.1991319444

		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667		0.1994791667

		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889		0.1998263889

		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037		0.200162037

		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333		0.2005208333

		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556		0.2008680556

		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778		0.2012152778

		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625		0.2015625

		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222		0.2019097222

		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444		0.2022569444

		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667		0.2026041667

		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889		0.2029513889

		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111		0.2032986111

		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333		0.2036458333

		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815		0.2039814815

		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037		0.2043287037

		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875		0.2046875

		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222		0.2050347222

		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444		0.2053819444

		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667		0.2057291667

		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889		0.2060763889

		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111		0.2064236111

		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333		0.2067708333

		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556		0.2071180556

		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778		0.2074652778

		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125		0.2078125

		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222		0.2081597222

		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444		0.2085069444

		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667		0.2088541667

		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889		0.2092013889

		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037		0.209537037

		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333		0.2098958333

		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556		0.2102430556

		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778		0.2105902778

		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375		0.2109375

		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481		0.2112731481

		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444		0.2116319444

		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667		0.2119791667

		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889		0.2123263889

		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111		0.2126736111

		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333		0.2130208333

		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556		0.2133680556

		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778		0.2137152778

		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625		0.2140625

		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481		0.2143981481

		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444		0.2147569444

		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667		0.2151041667

		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889		0.2154513889

		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111		0.2157986111

		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333		0.2161458333

		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556		0.2164930556

		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778		0.2168402778

		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875		0.2171875

		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222		0.2175347222

		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444		0.2178819444

		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667		0.2182291667

		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889		0.2185763889

		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111		0.2189236111

		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333		0.2192708333

		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556		0.2196180556

		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778		0.2199652778

		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125		0.2203125

		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222		0.2206597222

		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444		0.2210069444

		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667		0.2213541667

		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889		0.2217013889

		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037		0.222037037

		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333		0.2223958333

		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556		0.2227430556

		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778		0.2230902778

		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375		0.2234375

		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222		0.2237847222

		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444		0.2241319444

		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667		0.2244791667

		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889		0.2248263889

		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111		0.2251736111

		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333		0.2255208333

		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556		0.2258680556

		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778		0.2262152778

		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625		0.2265625

		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222		0.2269097222

		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444		0.2272569444

		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667		0.2276041667

		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889		0.2279513889

		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111		0.2282986111

		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333		0.2286458333

		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815		0.2289814815

		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778		0.2293402778

		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875		0.2296875

		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222		0.2300347222

		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444		0.2303819444

		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037		0.230787037

		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593		0.2311342593

		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815		0.2314814815

		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037		0.2318287037

		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259		0.2321759259

		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481		0.2325231481

		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704		0.2328703704

		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926		0.2332175926

		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148		0.2335648148

		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037		0.233912037

		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593		0.2342592593

		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815		0.2346064815

		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037		0.2349537037

		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259		0.2353009259

		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481		0.2356481481

		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704		0.2359953704

		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926		0.2363425926

		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148		0.2366898148

		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037		0.237037037

		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593		0.2373842593

		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815		0.2377314815

		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037		0.2380787037

		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259		0.2384259259

		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481		0.2387731481

		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704		0.2391203704

		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926		0.2394675926

		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148		0.2398148148

		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037		0.240162037

		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593		0.2405092593

		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815		0.2408564815

		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333		0.2411458333

		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556		0.2414930556

		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778		0.2418402778

		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875		0.2421875

		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481		0.2425231481

		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704		0.2428703704

		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667		0.2432291667

		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889		0.2435763889

		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111		0.2439236111

		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333		0.2442708333

		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556		0.2446180556

		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778		0.2449652778

		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125		0.2453125

		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222		0.2456597222

		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444		0.2460069444

		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667		0.2463541667

		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889		0.2467013889

		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111		0.2470486111

		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333		0.2473958333

		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556		0.2477430556

		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778		0.2480902778

		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375		0.2484375

		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222		0.2487847222

		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444		0.2491319444

		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667		0.2494791667

		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889		0.2498263889

		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111		0.2501736111

		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333		0.2505208333

		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556		0.2508680556

		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778		0.2512152778

		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625		0.2515625

		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222		0.2519097222

		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444		0.2522569444

		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667		0.2526041667

		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889		0.2529513889

		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111		0.2532986111

		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333		0.2536458333

		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556		0.2539930556

		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778		0.2543402778

		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875		0.2546875

		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222		0.2550347222

		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444		0.2553819444

		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667		0.2557291667

		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889		0.2560763889

		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111		0.2564236111

		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333		0.2567708333

		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556		0.2571180556

		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778		0.2574652778

		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125		0.2578125

		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222		0.2581597222

		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444		0.2585069444

		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667		0.2588541667

		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889		0.2592013889

		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111		0.2595486111

		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333		0.2598958333

		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556		0.2602430556

		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778		0.2605902778

		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375		0.2609375

		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222		0.2612847222

		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444		0.2616319444

		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667		0.2619791667

		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889		0.2623263889

		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111		0.2626736111

		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333		0.2630208333

		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556		0.2633680556

		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778		0.2637152778

		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625		0.2640625

		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222		0.2644097222

		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444		0.2647569444

		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667		0.2651041667

		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889		0.2654513889

		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111		0.2657986111

		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333		0.2661458333

		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556		0.2664930556

		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778		0.2668402778

		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875		0.2671875

		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222		0.2675347222

		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444		0.2678819444

		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667		0.2682291667

		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889		0.2685763889

		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111		0.2689236111

		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333		0.2692708333

		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556		0.2696180556

		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778		0.2699652778

		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125		0.2703125

		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222		0.2706597222

		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444		0.2710069444

		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667		0.2713541667

		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889		0.2717013889

		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111		0.2720486111

		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333		0.2723958333

		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556		0.2727430556

		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778		0.2730902778

		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375		0.2734375

		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222		0.2737847222

		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444		0.2741319444

		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667		0.2744791667

		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889		0.2748263889

		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111		0.2751736111

		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333		0.2755208333

		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556		0.2758680556

		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778		0.2762152778

		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625		0.2765625

		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222		0.2769097222

		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444		0.2772569444

		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667		0.2776041667

		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889		0.2779513889

		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111		0.2782986111

		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333		0.2786458333

		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556		0.2789930556

		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778		0.2793402778

		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875		0.2796875

		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222		0.2800347222

		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444		0.2803819444

		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667		0.2807291667

		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889		0.2810763889

		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111		0.2814236111

		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333		0.2817708333

		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556		0.2821180556

		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778		0.2824652778

		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125		0.2828125

		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222		0.2831597222

		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444		0.2835069444

		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667		0.2838541667

		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889		0.2842013889

		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111		0.2845486111

		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333		0.2848958333

		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556		0.2852430556

		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778		0.2855902778

		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375		0.2859375

		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222		0.2862847222

		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444		0.2866319444

		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667		0.2869791667

		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889		0.2873263889

		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111		0.2876736111

		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333		0.2880208333

		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556		0.2883680556

		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778		0.2887152778

		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625		0.2890625

		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222		0.2894097222

		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444		0.2897569444

		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667		0.2901041667

		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889		0.2904513889

		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111		0.2907986111

		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333		0.2911458333

		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556		0.2914930556

		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778		0.2918402778

		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875		0.2921875

		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222		0.2925347222

		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444		0.2928819444

		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667		0.2932291667

		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889		0.2935763889

		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111		0.2939236111

		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333		0.2942708333

		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556		0.2946180556

		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778		0.2949652778

		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125		0.2953125

		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222		0.2956597222

		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444		0.2960069444

		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667		0.2963541667

		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889		0.2967013889

		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111		0.2970486111

		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333		0.2973958333

		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556		0.2977430556

		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778		0.2980902778

		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375		0.2984375

		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222		0.2987847222

		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444		0.2991319444

		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667		0.2994791667

		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889		0.2998263889

		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111		0.3001736111

		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333		0.3005208333

		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556		0.3008680556

		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778		0.3012152778

		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625		0.3015625

		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222		0.3019097222

		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444		0.3022569444

		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667		0.3026041667

		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889		0.3029513889

		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111		0.3032986111

		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333		0.3036458333

		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556		0.3039930556

		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778		0.3043402778

		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875		0.3046875

		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222		0.3050347222

		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444		0.3053819444

		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667		0.3057291667

		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889		0.3060763889

		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111		0.3064236111

		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333		0.3067708333

		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556		0.3071180556

		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778		0.3074652778

		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125		0.3078125

		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222		0.3081597222

		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444		0.3085069444

		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667		0.3088541667

		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889		0.3092013889

		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111		0.3095486111

		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333		0.3098958333

		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556		0.3102430556

		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778		0.3105902778

		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375		0.3109375

		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222		0.3112847222

		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444		0.3116319444

		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667		0.3119791667

		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889		0.3123263889

		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111		0.3126736111

		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333		0.3130208333

		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556		0.3133680556

		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778		0.3137152778

		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625		0.3140625

		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222		0.3144097222

		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444		0.3147569444

		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667		0.3151041667

		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889		0.3154513889

		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111		0.3157986111

		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333		0.3161458333

		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556		0.3164930556

		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778		0.3168402778

		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875		0.3171875

		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222		0.3175347222

		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444		0.3178819444

		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667		0.3182291667

		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889		0.3185763889

		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111		0.3189236111

		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333		0.3192708333

		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556		0.3196180556

		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778		0.3199652778

		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125		0.3203125

		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222		0.3206597222

		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444		0.3210069444

		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667		0.3213541667

		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889		0.3217013889

		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111		0.3220486111

		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333		0.3223958333

		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556		0.3227430556

		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778		0.3230902778

		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375		0.3234375

		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222		0.3237847222

		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444		0.3241319444

		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667		0.3244791667

		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889		0.3248263889

		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111		0.3251736111

		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333		0.3255208333

		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556		0.3258680556

		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778		0.3262152778

		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625		0.3265625

		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222		0.3269097222

		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444		0.3272569444

		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667		0.3276041667

		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889		0.3279513889

		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111		0.3282986111

		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333		0.3286458333

		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556		0.3289930556

		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778		0.3293402778

		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875		0.3296875

		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222		0.3300347222

		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444		0.3303819444

		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667		0.3307291667

		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889		0.3310763889

		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111		0.3314236111

		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333		0.3317708333

		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556		0.3321180556

		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778		0.3324652778

		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125		0.3328125

		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222		0.3331597222

		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444		0.3335069444

		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667		0.3338541667

		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889		0.3342013889

		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111		0.3345486111

		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333		0.3348958333

		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556		0.3352430556

		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778		0.3355902778

		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375		0.3359375

		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222		0.3362847222

		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444		0.3366319444

		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667		0.3369791667

		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889		0.3373263889

		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111		0.3376736111

		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333		0.3380208333

		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556		0.3383680556

		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778		0.3387152778

		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625		0.3390625

		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222		0.3394097222

		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444		0.3397569444

		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667		0.3401041667

		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889		0.3404513889

		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111		0.3407986111

		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333		0.3411458333

		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556		0.3414930556

		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778		0.3418402778

		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875		0.3421875

		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222		0.3425347222

		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444		0.3428819444

		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667		0.3432291667

		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889		0.3435763889

		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111		0.3439236111

		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333		0.3442708333

		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556		0.3446180556

		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778		0.3449652778

		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125		0.3453125

		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222		0.3456597222

		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444		0.3460069444

		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667		0.3463541667

		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889		0.3467013889

		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111		0.3470486111

		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333		0.3473958333

		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556		0.3477430556

		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778		0.3480902778

		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375		0.3484375

		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222		0.3487847222

		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444		0.3491319444

		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667		0.3494791667

		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889		0.3498263889

		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111		0.3501736111

		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333		0.3505208333

		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556		0.3508680556

		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778		0.3512152778

		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625		0.3515625

		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222		0.3519097222

		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444		0.3522569444

		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667		0.3526041667

		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889		0.3529513889

		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111		0.3532986111

		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333		0.3536458333

		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556		0.3539930556

		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778		0.3543402778

		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875		0.3546875

		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222		0.3550347222

		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444		0.3553819444

		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667		0.3557291667

		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889		0.3560763889

		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111		0.3564236111

		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333		0.3567708333

		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556		0.3571180556

		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778		0.3574652778

		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125		0.3578125

		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222		0.3581597222

		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444		0.3585069444

		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667		0.3588541667

		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889		0.3592013889

		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111		0.3595486111

		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333		0.3598958333

		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556		0.3602430556

		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778		0.3605902778

		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375		0.3609375

		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222		0.3612847222

		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444		0.3616319444

		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667		0.3619791667

		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889		0.3623263889

		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111		0.3626736111

		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333		0.3630208333

		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556		0.3633680556

		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778		0.3637152778

		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625		0.3640625

		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222		0.3644097222

		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444		0.3647569444

		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667		0.3651041667

		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889		0.3654513889

		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111		0.3657986111

		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333		0.3661458333

		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556		0.3664930556

		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778		0.3668402778

		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875		0.3671875

		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222		0.3675347222

		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444		0.3678819444

		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667		0.3682291667

		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889		0.3685763889

		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111		0.3689236111

		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333		0.3692708333

		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556		0.3696180556

		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778		0.3699652778

		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125		0.3703125

		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222		0.3706597222

		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444		0.3710069444

		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667		0.3713541667

		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889		0.3717013889

		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111		0.3720486111

		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333		0.3723958333

		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556		0.3727430556

		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778		0.3730902778

		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375		0.3734375

		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222		0.3737847222

		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444		0.3741319444

		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667		0.3744791667

		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889		0.3748263889

		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111		0.3751736111

		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333		0.3755208333

		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556		0.3758680556

		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778		0.3762152778

		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625		0.3765625

		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222		0.3769097222

		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444		0.3772569444

		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667		0.3776041667

		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889		0.3779513889

		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111		0.3782986111

		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333		0.3786458333

		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556		0.3789930556

		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778		0.3793402778

		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875		0.3796875

		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222		0.3800347222

		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444		0.3803819444

		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667		0.3807291667

		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889		0.3810763889

		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111		0.3814236111

		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333		0.3817708333

		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556		0.3821180556

		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778		0.3824652778

		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125		0.3828125

		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222		0.3831597222

		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444		0.3835069444

		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667		0.3838541667

		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889		0.3842013889

		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111		0.3845486111

		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333		0.3848958333

		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556		0.3852430556

		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778		0.3855902778

		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375		0.3859375

		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222		0.3862847222

		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444		0.3866319444

		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667		0.3869791667

		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889		0.3873263889

		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111		0.3876736111

		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333		0.3880208333

		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556		0.3883680556

		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778		0.3887152778

		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625		0.3890625

		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222		0.3894097222

		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444		0.3897569444

		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667		0.3901041667

		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889		0.3904513889

		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111		0.3907986111

		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333		0.3911458333

		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556		0.3914930556

		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778		0.3918402778

		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875		0.3921875

		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222		0.3925347222

		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444		0.3928819444

		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667		0.3932291667

		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889		0.3935763889

		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111		0.3939236111

		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333		0.3942708333

		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556		0.3946180556

		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778		0.3949652778

		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125		0.3953125

		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222		0.3956597222

		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444		0.3960069444

		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667		0.3963541667

		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889		0.3967013889

		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111		0.3970486111

		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333		0.3973958333

		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556		0.3977430556

		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778		0.3980902778

		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375		0.3984375

		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222		0.3987847222

		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444		0.3991319444

		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667		0.3994791667

		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889		0.3998263889

		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111		0.4001736111

		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333		0.4005208333

		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556		0.4008680556

		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778		0.4012152778

		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625		0.4015625

		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222		0.4019097222

		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444		0.4022569444

		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667		0.4026041667

		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889		0.4029513889

		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111		0.4032986111

		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333		0.4036458333

		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556		0.4039930556

		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778		0.4043402778

		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875		0.4046875

		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222		0.4050347222

		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444		0.4053819444

		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667		0.4057291667

		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889		0.4060763889

		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111		0.4064236111

		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333		0.4067708333

		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556		0.4071180556

		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778		0.4074652778

		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125		0.4078125

		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222		0.4081597222

		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444		0.4085069444

		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667		0.4088541667

		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889		0.4092013889

		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111		0.4095486111

		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333		0.4098958333

		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556		0.4102430556

		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778		0.4105902778

		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375		0.4109375

		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222		0.4112847222

		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444		0.4116319444

		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667		0.4119791667

		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889		0.4123263889

		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111		0.4126736111

		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333		0.4130208333

		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556		0.4133680556

		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778		0.4137152778

		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625		0.4140625

		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222		0.4144097222

		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444		0.4147569444

		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667		0.4151041667

		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889		0.4154513889

		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111		0.4157986111

		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333		0.4161458333

		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556		0.4164930556

		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778		0.4168402778

		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875		0.4171875

		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222		0.4175347222

		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444		0.4178819444

		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667		0.4182291667

		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889		0.4185763889

		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111		0.4189236111

		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333		0.4192708333

		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556		0.4196180556

		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778		0.4199652778

		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125		0.4203125

		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222		0.4206597222

		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444		0.4210069444

		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667		0.4213541667

		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889		0.4217013889

		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111		0.4220486111

		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333		0.4223958333

		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556		0.4227430556

		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778		0.4230902778

		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375		0.4234375

		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222		0.4237847222

		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444		0.4241319444

		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667		0.4244791667

		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889		0.4248263889

		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111		0.4251736111

		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333		0.4255208333

		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556		0.4258680556

		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778		0.4262152778

		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625		0.4265625

		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222		0.4269097222

		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444		0.4272569444

		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667		0.4276041667

		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889		0.4279513889

		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111		0.4282986111

		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333		0.4286458333

		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556		0.4289930556

		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778		0.4293402778

		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875		0.4296875

		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222		0.4300347222

		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444		0.4303819444

		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667		0.4307291667

		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889		0.4310763889

		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111		0.4314236111

		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333		0.4317708333

		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556		0.4321180556

		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778		0.4324652778

		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125		0.4328125

		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222		0.4331597222

		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444		0.4335069444

		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667		0.4338541667

		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889		0.4342013889

		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111		0.4345486111

		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333		0.4348958333

		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556		0.4352430556

		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778		0.4355902778

		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375		0.4359375

		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222		0.4362847222

		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444		0.4366319444

		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667		0.4369791667

		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889		0.4373263889

		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111		0.4376736111

		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333		0.4380208333

		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556		0.4383680556

		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778		0.4387152778

		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625		0.4390625

		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222		0.4394097222

		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444		0.4397569444

		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667		0.4401041667

		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889		0.4404513889

		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111		0.4407986111

		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333		0.4411458333

		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556		0.4414930556

		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778		0.4418402778

		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875		0.4421875

		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222		0.4425347222

		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444		0.4428819444

		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667		0.4432291667

		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889		0.4435763889

		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111		0.4439236111

		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333		0.4442708333

		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556		0.4446180556

		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778		0.4449652778

		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125		0.4453125

		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222		0.4456597222

		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444		0.4460069444

		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667		0.4463541667

		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889		0.4467013889

		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111		0.4470486111

		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333		0.4473958333

		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556		0.4477430556

		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778		0.4480902778

		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375		0.4484375

		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222		0.4487847222

		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444		0.4491319444

		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667		0.4494791667

		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889		0.4498263889

		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111		0.4501736111

		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333		0.4505208333

		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556		0.4508680556

		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778		0.4512152778

		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625		0.4515625

		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222		0.4519097222

		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444		0.4522569444

		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667		0.4526041667

		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889		0.4529513889

		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111		0.4532986111

		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333		0.4536458333

		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556		0.4539930556

		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778		0.4543402778

		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875		0.4546875

		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222		0.4550347222

		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444		0.4553819444

		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667		0.4557291667

		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889		0.4560763889

		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111		0.4564236111

		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333		0.4567708333

		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556		0.4571180556

		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778		0.4574652778

		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125		0.4578125

		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222		0.4581597222

		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444		0.4585069444

		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667		0.4588541667

		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889		0.4592013889

		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111		0.4595486111

		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333		0.4598958333

		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556		0.4602430556

		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778		0.4605902778

		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375		0.4609375

		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222		0.4612847222

		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444		0.4616319444

		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667		0.4619791667

		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889		0.4623263889

		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111		0.4626736111

		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333		0.4630208333

		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556		0.4633680556

		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778		0.4637152778

		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625		0.4640625

		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222		0.4644097222

		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444		0.4647569444

		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667		0.4651041667

		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889		0.4654513889

		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111		0.4657986111

		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333		0.4661458333

		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556		0.4664930556

		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778		0.4668402778

		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875		0.4671875

		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222		0.4675347222

		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444		0.4678819444

		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667		0.4682291667

		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889		0.4685763889

		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111		0.4689236111

		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333		0.4692708333

		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556		0.4696180556

		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778		0.4699652778

		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125		0.4703125

		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222		0.4706597222

		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444		0.4710069444

		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667		0.4713541667

		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889		0.4717013889

		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111		0.4720486111

		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333		0.4723958333

		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556		0.4727430556

		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778		0.4730902778

		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375		0.4734375

		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222		0.4737847222

		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444		0.4741319444

		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667		0.4744791667

		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889		0.4748263889

		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111		0.4751736111

		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333		0.4755208333

		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556		0.4758680556

		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778		0.4762152778

		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625		0.4765625

		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222		0.4769097222

		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444		0.4772569444

		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667		0.4776041667

		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889		0.4779513889

		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111		0.4782986111

		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333		0.4786458333

		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556		0.4789930556

		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778		0.4793402778

		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875		0.4796875

		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222		0.4800347222

		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444		0.4803819444

		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667		0.4807291667

		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889		0.4810763889

		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111		0.4814236111

		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333		0.4817708333

		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556		0.4821180556

		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778		0.4824652778

		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125		0.4828125

		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222		0.4831597222

		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444		0.4835069444

		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667		0.4838541667

		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889		0.4842013889

		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111		0.4845486111

		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333		0.4848958333

		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556		0.4852430556

		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778		0.4855902778

		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375		0.4859375

		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222		0.4862847222

		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444		0.4866319444

		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667		0.4869791667

		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889		0.4873263889

		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111		0.4876736111

		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333		0.4880208333

		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556		0.4883680556

		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778		0.4887152778

		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625		0.4890625

		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222		0.4894097222

		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444		0.4897569444

		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667		0.4901041667

		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889		0.4904513889

		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111		0.4907986111

		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333		0.4911458333

		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556		0.4914930556

		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778		0.4918402778

		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875		0.4921875

		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222		0.4925347222

		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444		0.4928819444

		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667		0.4932291667

		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889		0.4935763889

		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111		0.4939236111

		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333		0.4942708333

		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556		0.4946180556

		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778		0.4949652778

		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125		0.4953125

		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222		0.4956597222

		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444		0.4960069444

		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667		0.4963541667

		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889		0.4967013889

		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111		0.4970486111

		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333		0.4973958333

		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556		0.4977430556

		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778		0.4980902778

		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375		0.4984375

		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222		0.4987847222

		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444		0.4991319444

		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667		0.4994791667

		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889		0.4998263889

		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111		0.5001736111

		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333		0.5005208333

		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556		0.5008680556

		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778		0.5012152778

		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625		0.5015625

		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222		0.5019097222

		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444		0.5022569444

		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667		0.5026041667

		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889		0.5029513889

		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111		0.5032986111

		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333		0.5036458333

		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556		0.5039930556

		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778		0.5043402778

		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875		0.5046875

		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222		0.5050347222

		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444		0.5053819444

		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667		0.5057291667

		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889		0.5060763889

		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111		0.5064236111

		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333		0.5067708333

		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556		0.5071180556

		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778		0.5074652778

		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125		0.5078125

		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222		0.5081597222

		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444		0.5085069444

		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667		0.5088541667

		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889		0.5092013889

		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111		0.5095486111

		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333		0.5098958333

		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556		0.5102430556

		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778		0.5105902778

		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375		0.5109375

		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222		0.5112847222

		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444		0.5116319444

		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667		0.5119791667

		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889		0.5123263889

		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111		0.5126736111

		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333		0.5130208333

		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556		0.5133680556

		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778		0.5137152778

		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625		0.5140625

		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222		0.5144097222

		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444		0.5147569444

		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667		0.5151041667

		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889		0.5154513889

		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111		0.5157986111

		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333		0.5161458333

		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556		0.5164930556

		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778		0.5168402778

		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875		0.5171875

		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222		0.5175347222

		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444		0.5178819444

		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667		0.5182291667

		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889		0.5185763889

		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111		0.5189236111

		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333		0.5192708333

		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556		0.5196180556

		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778		0.5199652778

		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125		0.5203125

		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222		0.5206597222

		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444		0.5210069444

		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667		0.5213541667

		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889		0.5217013889

		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111		0.5220486111

		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333		0.5223958333

		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556		0.5227430556

		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778		0.5230902778

		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375		0.5234375

		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222		0.5237847222

		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444		0.5241319444

		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667		0.5244791667

		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889		0.5248263889

		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111		0.5251736111

		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333		0.5255208333

		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556		0.5258680556

		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778		0.5262152778

		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625		0.5265625

		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222		0.5269097222

		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444		0.5272569444

		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667		0.5276041667

		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889		0.5279513889

		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111		0.5282986111

		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333		0.5286458333

		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556		0.5289930556

		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778		0.5293402778

		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875		0.5296875

		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222		0.5300347222

		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444		0.5303819444

		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667		0.5307291667

		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889		0.5310763889

		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111		0.5314236111

		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333		0.5317708333

		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556		0.5321180556

		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778		0.5324652778

		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125		0.5328125

		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222		0.5331597222

		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444		0.5335069444

		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667		0.5338541667

		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889		0.5342013889

		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111		0.5345486111

		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333		0.5348958333

		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556		0.5352430556

		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778		0.5355902778

		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375		0.5359375

		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222		0.5362847222

		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444		0.5366319444

		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667		0.5369791667

		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889		0.5373263889

		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111		0.5376736111

		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333		0.5380208333

		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556		0.5383680556

		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778		0.5387152778

		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625		0.5390625

		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222		0.5394097222

		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444		0.5397569444

		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667		0.5401041667

		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889		0.5404513889

		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111		0.5407986111

		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333		0.5411458333

		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556		0.5414930556

		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778		0.5418402778

		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875		0.5421875

		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222		0.5425347222

		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444		0.5428819444

		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667		0.5432291667

		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889		0.5435763889

		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111		0.5439236111

		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333		0.5442708333

		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556		0.5446180556

		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778		0.5449652778

		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125		0.5453125

		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222		0.5456597222

		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444		0.5460069444

		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667		0.5463541667

		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889		0.5467013889

		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111		0.5470486111

		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333		0.5473958333

		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556		0.5477430556

		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778		0.5480902778

		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375		0.5484375

		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222		0.5487847222

		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444		0.5491319444

		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667		0.5494791667

		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889		0.5498263889

		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111		0.5501736111

		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333		0.5505208333

		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556		0.5508680556

		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778		0.5512152778

		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625		0.5515625

		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222		0.5519097222

		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444		0.5522569444

		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667		0.5526041667

		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889		0.5529513889

		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111		0.5532986111

		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333		0.5536458333

		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556		0.5539930556

		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778		0.5543402778

		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875		0.5546875

		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222		0.5550347222

		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444		0.5553819444

		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667		0.5557291667

		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889		0.5560763889

		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111		0.5564236111

		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333		0.5567708333

		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556		0.5571180556

		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778		0.5574652778

		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125		0.5578125

		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222		0.5581597222

		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444		0.5585069444

		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667		0.5588541667

		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889		0.5592013889

		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111		0.5595486111

		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333		0.5598958333

		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556		0.5602430556

		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778		0.5605902778

		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375		0.5609375

		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222		0.5612847222

		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444		0.5616319444

		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667		0.5619791667

		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889		0.5623263889

		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111		0.5626736111

		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333		0.5630208333

		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556		0.5633680556

		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778		0.5637152778

		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625		0.5640625

		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222		0.5644097222

		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444		0.5647569444

		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667		0.5651041667

		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889		0.5654513889

		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111		0.5657986111

		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333		0.5661458333

		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556		0.5664930556

		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778		0.5668402778

		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875		0.5671875

		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222		0.5675347222

		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444		0.5678819444

		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667		0.5682291667

		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889		0.5685763889

		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111		0.5689236111

		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333		0.5692708333

		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556		0.5696180556

		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778		0.5699652778

		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125		0.5703125

		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222		0.5706597222

		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444		0.5710069444

		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667		0.5713541667

		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889		0.5717013889

		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111		0.5720486111

		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333		0.5723958333

		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556		0.5727430556

		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778		0.5730902778

		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375		0.5734375

		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222		0.5737847222

		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444		0.5741319444

		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667		0.5744791667

		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889		0.5748263889

		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111		0.5751736111

		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333		0.5755208333

		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556		0.5758680556

		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778		0.5762152778

		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625		0.5765625

		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222		0.5769097222

		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444		0.5772569444

		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667		0.5776041667

		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889		0.5779513889

		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111		0.5782986111

		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333		0.5786458333

		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556		0.5789930556

		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778		0.5793402778

		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875		0.5796875

		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222		0.5800347222

		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444		0.5803819444

		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667		0.5807291667

		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889		0.5810763889

		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111		0.5814236111

		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333		0.5817708333

		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556		0.5821180556

		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778		0.5824652778

		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125		0.5828125

		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222		0.5831597222

		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444		0.5835069444

		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667		0.5838541667

		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889		0.5842013889

		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111		0.5845486111

		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333		0.5848958333

		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556		0.5852430556

		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778		0.5855902778

		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375		0.5859375

		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222		0.5862847222

		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444		0.5866319444

		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667		0.5869791667

		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889		0.5873263889

		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111		0.5876736111

		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333		0.5880208333

		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556		0.5883680556

		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778		0.5887152778

		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625		0.5890625

		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222		0.5894097222

		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444		0.5897569444

		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667		0.5901041667

		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889		0.5904513889

		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111		0.5907986111

		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333		0.5911458333

		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556		0.5914930556

		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778		0.5918402778

		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875		0.5921875

		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222		0.5925347222

		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444		0.5928819444

		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667		0.5932291667

		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889		0.5935763889

		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111		0.5939236111

		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333		0.5942708333

		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556		0.5946180556

		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778		0.5949652778

		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125		0.5953125

		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222		0.5956597222

		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444		0.5960069444

		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667		0.5963541667

		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889		0.5967013889

		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111		0.5970486111

		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333		0.5973958333

		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556		0.5977430556

		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778		0.5980902778

		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375		0.5984375

		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222		0.5987847222

		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444		0.5991319444

		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667		0.5994791667

		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889		0.5998263889

		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111		0.6001736111

		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333		0.6005208333

		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556		0.6008680556

		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778		0.6012152778

		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625		0.6015625

		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222		0.6019097222

		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444		0.6022569444

		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667		0.6026041667

		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889		0.6029513889

		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111		0.6032986111

		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333		0.6036458333

		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556		0.6039930556

		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778		0.6043402778

		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875		0.6046875

		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222		0.6050347222

		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444		0.6053819444

		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667		0.6057291667

		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889		0.6060763889

		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111		0.6064236111

		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333		0.6067708333

		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556		0.6071180556

		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778		0.6074652778

		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125		0.6078125

		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222		0.6081597222

		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444		0.6085069444

		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667		0.6088541667

		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889		0.6092013889

		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111		0.6095486111

		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333		0.6098958333

		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556		0.6102430556

		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778		0.6105902778

		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375		0.6109375

		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222		0.6112847222

		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444		0.6116319444

		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667		0.6119791667

		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889		0.6123263889

		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111		0.6126736111

		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333		0.6130208333

		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556		0.6133680556

		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778		0.6137152778

		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625		0.6140625

		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222		0.6144097222

		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444		0.6147569444

		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667		0.6151041667

		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889		0.6154513889

		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111		0.6157986111

		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333		0.6161458333

		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556		0.6164930556

		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778		0.6168402778

		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875		0.6171875

		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222		0.6175347222

		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444		0.6178819444

		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667		0.6182291667

		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889		0.6185763889

		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111		0.6189236111

		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333		0.6192708333

		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556		0.6196180556

		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778		0.6199652778

		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125		0.6203125

		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222		0.6206597222

		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444		0.6210069444

		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667		0.6213541667

		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889		0.6217013889

		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111		0.6220486111

		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333		0.6223958333

		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556		0.6227430556

		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778		0.6230902778

		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375		0.6234375

		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222		0.6237847222

		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444		0.6241319444

		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667		0.6244791667

		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889		0.6248263889

		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111		0.6251736111

		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333		0.6255208333

		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556		0.6258680556

		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778		0.6262152778

		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625		0.6265625

		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222		0.6269097222

		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444		0.6272569444

		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667		0.6276041667

		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889		0.6279513889

		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111		0.6282986111

		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333		0.6286458333

		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556		0.6289930556

		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778		0.6293402778

		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875		0.6296875

		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222		0.6300347222

		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444		0.6303819444

		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667		0.6307291667

		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889		0.6310763889

		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111		0.6314236111

		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333		0.6317708333

		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556		0.6321180556

		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778		0.6324652778

		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125		0.6328125

		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222		0.6331597222

		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444		0.6335069444

		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667		0.6338541667

		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889		0.6342013889

		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111		0.6345486111

		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333		0.6348958333

		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556		0.6352430556

		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778		0.6355902778

		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375		0.6359375

		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222		0.6362847222

		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444		0.6366319444

		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667		0.6369791667

		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889		0.6373263889

		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111		0.6376736111

		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333		0.6380208333

		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556		0.6383680556

		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778		0.6387152778

		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625		0.6390625

		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222		0.6394097222

		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444		0.6397569444

		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667		0.6401041667

		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889		0.6404513889

		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111		0.6407986111

		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333		0.6411458333

		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556		0.6414930556

		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778		0.6418402778

		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875		0.6421875

		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222		0.6425347222

		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444		0.6428819444

		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667		0.6432291667

		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889		0.6435763889

		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111		0.6439236111

		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333		0.6442708333

		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556		0.6446180556

		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778		0.6449652778

		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125		0.6453125

		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222		0.6456597222

		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444		0.6460069444

		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667		0.6463541667

		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889		0.6467013889

		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111		0.6470486111

		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333		0.6473958333

		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556		0.6477430556

		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778		0.6480902778

		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375		0.6484375

		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222		0.6487847222

		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444		0.6491319444

		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667		0.6494791667

		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889		0.6498263889

		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111		0.6501736111

		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333		0.6505208333

		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556		0.6508680556

		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778		0.6512152778

		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625		0.6515625

		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222		0.6519097222

		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444		0.6522569444

		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667		0.6526041667

		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889		0.6529513889

		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111		0.6532986111

		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333		0.6536458333

		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556		0.6539930556

		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778		0.6543402778

		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875		0.6546875

		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222		0.6550347222

		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444		0.6553819444

		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667		0.6557291667

		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889		0.6560763889

		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111		0.6564236111

		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333		0.6567708333

		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556		0.6571180556

		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778		0.6574652778

		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125		0.6578125

		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222		0.6581597222

		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444		0.6585069444

		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667		0.6588541667

		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889		0.6592013889

		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111		0.6595486111

		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333		0.6598958333

		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556		0.6602430556

		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778		0.6605902778

		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375		0.6609375

		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222		0.6612847222

		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444		0.6616319444

		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667		0.6619791667

		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889		0.6623263889

		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111		0.6626736111

		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333		0.6630208333

		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556		0.6633680556

		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778		0.6637152778

		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625		0.6640625

		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222		0.6644097222

		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444		0.6647569444

		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667		0.6651041667

		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889		0.6654513889

		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111		0.6657986111

		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333		0.6661458333

		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556		0.6664930556

		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778		0.6668402778

		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875		0.6671875

		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222		0.6675347222

		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444		0.6678819444

		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667		0.6682291667

		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889		0.6685763889

		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111		0.6689236111

		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333		0.6692708333

		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556		0.6696180556

		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778		0.6699652778

		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125		0.6703125

		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222		0.6706597222

		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444		0.6710069444

		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667		0.6713541667

		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889		0.6717013889

		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111		0.6720486111

		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333		0.6723958333

		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556		0.6727430556

		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778		0.6730902778

		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375		0.6734375

		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222		0.6737847222

		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444		0.6741319444

		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667		0.6744791667

		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889		0.6748263889

		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111		0.6751736111

		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333		0.6755208333

		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556		0.6758680556

		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778		0.6762152778

		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625		0.6765625

		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222		0.6769097222

		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444		0.6772569444

		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667		0.6776041667

		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889		0.6779513889

		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111		0.6782986111

		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333		0.6786458333

		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556		0.6789930556

		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778		0.6793402778

		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875		0.6796875

		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222		0.6800347222

		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444		0.6803819444

		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667		0.6807291667

		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889		0.6810763889

		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111		0.6814236111

		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333		0.6817708333

		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556		0.6821180556

		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778		0.6824652778

		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125		0.6828125

		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222		0.6831597222

		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444		0.6835069444

		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667		0.6838541667

		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889		0.6842013889

		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111		0.6845486111

		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333		0.6848958333

		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556		0.6852430556

		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778		0.6855902778

		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375		0.6859375

		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222		0.6862847222

		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444		0.6866319444

		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667		0.6869791667

		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889		0.6873263889

		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111		0.6876736111

		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333		0.6880208333

		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556		0.6883680556

		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778		0.6887152778

		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625		0.6890625

		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222		0.6894097222

		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444		0.6897569444

		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667		0.6901041667

		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889		0.6904513889

		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111		0.6907986111

		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333		0.6911458333

		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556		0.6914930556

		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778		0.6918402778

		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875		0.6921875

		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222		0.6925347222

		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444		0.6928819444

		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667		0.6932291667

		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889		0.6935763889

		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111		0.6939236111

		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333		0.6942708333

		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556		0.6946180556

		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778		0.6949652778

		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125		0.6953125

		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222		0.6956597222

		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444		0.6960069444

		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667		0.6963541667

		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889		0.6967013889

		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111		0.6970486111

		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333		0.6973958333

		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556		0.6977430556

		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778		0.6980902778

		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375		0.6984375

		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222		0.6987847222

		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444		0.6991319444

		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667		0.6994791667

		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889		0.6998263889

		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111		0.7001736111

		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333		0.7005208333

		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556		0.7008680556

		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778		0.7012152778

		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625		0.7015625

		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222		0.7019097222

		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444		0.7022569444

		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667		0.7026041667

		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889		0.7029513889

		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111		0.7032986111

		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333		0.7036458333

		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556		0.7039930556

		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778		0.7043402778

		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875		0.7046875

		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222		0.7050347222

		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444		0.7053819444

		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667		0.7057291667

		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889		0.7060763889

		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111		0.7064236111

		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333		0.7067708333

		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556		0.7071180556

		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778		0.7074652778

		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125		0.7078125

		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222		0.7081597222

		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444		0.7085069444

		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667		0.7088541667

		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889		0.7092013889

		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111		0.7095486111

		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333		0.7098958333

		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556		0.7102430556

		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778		0.7105902778

		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375		0.7109375

		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222		0.7112847222

		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444		0.7116319444

		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667		0.7119791667

		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889		0.7123263889

		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111		0.7126736111

		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333		0.7130208333

		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556		0.7133680556

		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778		0.7137152778

		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625		0.7140625

		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222		0.7144097222

		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444		0.7147569444

		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667		0.7151041667

		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889		0.7154513889

		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111		0.7157986111

		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333		0.7161458333

		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556		0.7164930556

		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778		0.7168402778

		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875		0.7171875

		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222		0.7175347222

		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444		0.7178819444

		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667		0.7182291667

		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889		0.7185763889

		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111		0.7189236111

		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333		0.7192708333

		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556		0.7196180556

		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778		0.7199652778

		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125		0.7203125

		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222		0.7206597222

		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444		0.7210069444

		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667		0.7213541667

		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889		0.7217013889

		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111		0.7220486111

		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333		0.7223958333

		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556		0.7227430556

		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778		0.7230902778

		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375		0.7234375

		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222		0.7237847222

		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444		0.7241319444

		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667		0.7244791667

		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889		0.7248263889

		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111		0.7251736111

		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333		0.7255208333

		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556		0.7258680556

		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778		0.7262152778

		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625		0.7265625

		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222		0.7269097222

		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444		0.7272569444

		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667		0.7276041667

		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889		0.7279513889

		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111		0.7282986111

		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333		0.7286458333

		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556		0.7289930556

		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778		0.7293402778

		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875		0.7296875

		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222		0.7300347222

		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444		0.7303819444

		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667		0.7307291667

		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889		0.7310763889

		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111		0.7314236111

		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333		0.7317708333

		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556		0.7321180556

		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778		0.7324652778

		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125		0.7328125

		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222		0.7331597222

		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444		0.7335069444

		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667		0.7338541667

		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889		0.7342013889

		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111		0.7345486111

		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333		0.7348958333

		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556		0.7352430556

		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778		0.7355902778

		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375		0.7359375

		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222		0.7362847222

		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444		0.7366319444

		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667		0.7369791667

		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889		0.7373263889

		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111		0.7376736111

		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333		0.7380208333

		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556		0.7383680556

		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778		0.7387152778

		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625		0.7390625

		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222		0.7394097222

		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444		0.7397569444

		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667		0.7401041667

		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889		0.7404513889

		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111		0.7407986111

		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333		0.7411458333

		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556		0.7414930556

		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778		0.7418402778

		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875		0.7421875

		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222		0.7425347222

		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444		0.7428819444

		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667		0.7432291667

		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889		0.7435763889

		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111		0.7439236111

		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333		0.7442708333

		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556		0.7446180556

		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778		0.7449652778

		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125		0.7453125

		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222		0.7456597222

		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444		0.7460069444

		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667		0.7463541667

		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889		0.7467013889

		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111		0.7470486111

		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333		0.7473958333

		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556		0.7477430556

		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778		0.7480902778

		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375		0.7484375

		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222		0.7487847222

		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444		0.7491319444

		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667		0.7494791667

		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889		0.7498263889

		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111		0.7501736111

		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333		0.7505208333

		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556		0.7508680556

		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778		0.7512152778

		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625		0.7515625

		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222		0.7519097222

		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444		0.7522569444

		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667		0.7526041667

		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889		0.7529513889

		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111		0.7532986111

		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333		0.7536458333

		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556		0.7539930556

		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778		0.7543402778

		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875		0.7546875

		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222		0.7550347222

		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444		0.7553819444

		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667		0.7557291667

		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889		0.7560763889

		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111		0.7564236111

		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333		0.7567708333

		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556		0.7571180556

		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778		0.7574652778

		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125		0.7578125

		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222		0.7581597222

		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444		0.7585069444

		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667		0.7588541667

		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889		0.7592013889

		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111		0.7595486111

		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333		0.7598958333

		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556		0.7602430556

		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778		0.7605902778

		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375		0.7609375

		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222		0.7612847222

		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444		0.7616319444

		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667		0.7619791667

		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889		0.7623263889

		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111		0.7626736111

		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333		0.7630208333

		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556		0.7633680556

		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778		0.7637152778

		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625		0.7640625

		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222		0.7644097222

		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444		0.7647569444

		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667		0.7651041667

		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889		0.7654513889

		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111		0.7657986111

		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333		0.7661458333

		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556		0.7664930556

		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778		0.7668402778

		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875		0.7671875

		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222		0.7675347222

		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444		0.7678819444

		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667		0.7682291667

		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889		0.7685763889

		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111		0.7689236111

		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333		0.7692708333

		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556		0.7696180556

		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778		0.7699652778

		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125		0.7703125

		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222		0.7706597222

		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444		0.7710069444

		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667		0.7713541667

		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889		0.7717013889

		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111		0.7720486111

		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333		0.7723958333

		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556		0.7727430556

		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778		0.7730902778

		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375		0.7734375

		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222		0.7737847222

		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444		0.7741319444

		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667		0.7744791667

		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889		0.7748263889

		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111		0.7751736111

		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333		0.7755208333

		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556		0.7758680556

		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778		0.7762152778

		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625		0.7765625

		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222		0.7769097222

		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444		0.7772569444

		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667		0.7776041667

		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889		0.7779513889

		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111		0.7782986111

		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333		0.7786458333

		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556		0.7789930556

		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778		0.7793402778

		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875		0.7796875

		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222		0.7800347222

		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444		0.7803819444

		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667		0.7807291667

		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889		0.7810763889

		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111		0.7814236111

		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333		0.7817708333

		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556		0.7821180556

		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778		0.7824652778

		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125		0.7828125

		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222		0.7831597222

		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444		0.7835069444

		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667		0.7838541667

		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889		0.7842013889

		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111		0.7845486111

		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333		0.7848958333

		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556		0.7852430556

		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778		0.7855902778

		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375		0.7859375

		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222		0.7862847222

		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444		0.7866319444

		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667		0.7869791667

		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889		0.7873263889

		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111		0.7876736111

		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333		0.7880208333

		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556		0.7883680556

		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778		0.7887152778

		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625		0.7890625

		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222		0.7894097222

		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444		0.7897569444

		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667		0.7901041667

		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889		0.7904513889

		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111		0.7907986111

		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333		0.7911458333

		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556		0.7914930556

		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778		0.7918402778

		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875		0.7921875

		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222		0.7925347222

		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444		0.7928819444

		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667		0.7932291667

		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889		0.7935763889

		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111		0.7939236111

		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333		0.7942708333

		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556		0.7946180556

		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778		0.7949652778

		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125		0.7953125

		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222		0.7956597222

		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444		0.7960069444

		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667		0.7963541667

		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889		0.7967013889

		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111		0.7970486111

		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333		0.7973958333

		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556		0.7977430556

		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778		0.7980902778

		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375		0.7984375

		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222		0.7987847222

		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444		0.7991319444

		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667		0.7994791667

		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889		0.7998263889

		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111		0.8001736111

		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333		0.8005208333

		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556		0.8008680556

		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778		0.8012152778

		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625		0.8015625

		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222		0.8019097222

		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444		0.8022569444

		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667		0.8026041667

		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889		0.8029513889

		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111		0.8032986111

		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333		0.8036458333

		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556		0.8039930556

		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778		0.8043402778

		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875		0.8046875

		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222		0.8050347222

		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444		0.8053819444

		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667		0.8057291667

		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889		0.8060763889

		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111		0.8064236111

		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333		0.8067708333

		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556		0.8071180556

		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778		0.8074652778

		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125		0.8078125

		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222		0.8081597222

		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444		0.8085069444

		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667		0.8088541667

		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889		0.8092013889

		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111		0.8095486111

		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333		0.8098958333

		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556		0.8102430556

		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778		0.8105902778

		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375		0.8109375

		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222		0.8112847222

		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444		0.8116319444

		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667		0.8119791667

		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889		0.8123263889

		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111		0.8126736111

		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333		0.8130208333

		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556		0.8133680556

		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778		0.8137152778

		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625		0.8140625

		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222		0.8144097222

		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444		0.8147569444

		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667		0.8151041667

		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889		0.8154513889

		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111		0.8157986111

		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333		0.8161458333

		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556		0.8164930556

		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778		0.8168402778

		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875		0.8171875

		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222		0.8175347222

		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444		0.8178819444

		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667		0.8182291667

		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889		0.8185763889

		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111		0.8189236111

		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333		0.8192708333

		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556		0.8196180556

		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778		0.8199652778

		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125		0.8203125

		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222		0.8206597222

		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444		0.8210069444

		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667		0.8213541667

		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889		0.8217013889

		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111		0.8220486111

		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333		0.8223958333

		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556		0.8227430556

		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778		0.8230902778

		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375		0.8234375

		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222		0.8237847222

		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444		0.8241319444

		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667		0.8244791667

		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889		0.8248263889

		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111		0.8251736111

		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333		0.8255208333

		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556		0.8258680556

		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778		0.8262152778

		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625		0.8265625

		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222		0.8269097222

		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444		0.8272569444

		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667		0.8276041667

		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889		0.8279513889

		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111		0.8282986111

		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333		0.8286458333

		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556		0.8289930556

		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778		0.8293402778

		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875		0.8296875

		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222		0.8300347222

		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444		0.8303819444

		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667		0.8307291667

		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889		0.8310763889

		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111		0.8314236111

		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333		0.8317708333

		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556		0.8321180556

		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778		0.8324652778

		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125		0.8328125

		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222		0.8331597222

		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444		0.8335069444

		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667		0.8338541667

		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889		0.8342013889

		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111		0.8345486111

		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333		0.8348958333

		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556		0.8352430556

		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778		0.8355902778

		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375		0.8359375

		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222		0.8362847222

		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444		0.8366319444

		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667		0.8369791667

		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889		0.8373263889

		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111		0.8376736111

		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333		0.8380208333

		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556		0.8383680556

		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778		0.8387152778

		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625		0.8390625

		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222		0.8394097222

		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444		0.8397569444

		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667		0.8401041667

		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889		0.8404513889

		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111		0.8407986111

		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333		0.8411458333

		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556		0.8414930556

		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778		0.8418402778

		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875		0.8421875

		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222		0.8425347222

		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444		0.8428819444

		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667		0.8432291667

		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889		0.8435763889

		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111		0.8439236111

		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333		0.8442708333

		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556		0.8446180556

		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778		0.8449652778

		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125		0.8453125

		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222		0.8456597222

		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444		0.8460069444

		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667		0.8463541667

		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889		0.8467013889

		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111		0.8470486111

		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333		0.8473958333

		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556		0.8477430556

		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778		0.8480902778

		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375		0.8484375

		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222		0.8487847222

		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444		0.8491319444

		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667		0.8494791667

		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889		0.8498263889

		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111		0.8501736111

		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333		0.8505208333

		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556		0.8508680556

		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778		0.8512152778

		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625		0.8515625

		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222		0.8519097222

		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444		0.8522569444

		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667		0.8526041667

		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889		0.8529513889

		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111		0.8532986111

		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333		0.8536458333

		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556		0.8539930556

		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778		0.8543402778

		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875		0.8546875

		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222		0.8550347222

		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444		0.8553819444

		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667		0.8557291667

		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889		0.8560763889

		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111		0.8564236111

		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333		0.8567708333

		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556		0.8571180556

		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778		0.8574652778

		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125		0.8578125

		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222		0.8581597222

		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444		0.8585069444

		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667		0.8588541667

		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889		0.8592013889

		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111		0.8595486111

		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333		0.8598958333

		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556		0.8602430556

		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778		0.8605902778

		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375		0.8609375

		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222		0.8612847222

		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444		0.8616319444

		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667		0.8619791667

		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889		0.8623263889

		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111		0.8626736111

		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333		0.8630208333

		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556		0.8633680556

		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778		0.8637152778

		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625		0.8640625

		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222		0.8644097222

		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444		0.8647569444

		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667		0.8651041667

		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889		0.8654513889

		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111		0.8657986111

		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333		0.8661458333

		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556		0.8664930556

		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778		0.8668402778

		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875		0.8671875

		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222		0.8675347222

		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444		0.8678819444

		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667		0.8682291667

		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889		0.8685763889

		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111		0.8689236111

		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333		0.8692708333

		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556		0.8696180556

		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778		0.8699652778

		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125		0.8703125

		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222		0.8706597222

		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444		0.8710069444

		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667		0.8713541667

		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889		0.8717013889

		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111		0.8720486111

		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333		0.8723958333

		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556		0.8727430556

		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778		0.8730902778

		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375		0.8734375

		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222		0.8737847222

		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444		0.8741319444

		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667		0.8744791667

		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889		0.8748263889

		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111		0.8751736111

		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333		0.8755208333

		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556		0.8758680556

		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778		0.8762152778

		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625		0.8765625

		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222		0.8769097222

		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444		0.8772569444

		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667		0.8776041667

		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889		0.8779513889

		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111		0.8782986111

		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333		0.8786458333

		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556		0.8789930556

		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778		0.8793402778

		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875		0.8796875

		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222		0.8800347222

		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444		0.8803819444

		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667		0.8807291667

		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889		0.8810763889

		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111		0.8814236111

		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333		0.8817708333

		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556		0.8821180556

		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778		0.8824652778

		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125		0.8828125

		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222		0.8831597222

		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444		0.8835069444

		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667		0.8838541667

		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889		0.8842013889

		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111		0.8845486111

		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333		0.8848958333

		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556		0.8852430556

		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778		0.8855902778

		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375		0.8859375

		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222		0.8862847222

		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444		0.8866319444

		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667		0.8869791667

		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889		0.8873263889

		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111		0.8876736111

		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333		0.8880208333

		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556		0.8883680556

		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778		0.8887152778

		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625		0.8890625

		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222		0.8894097222

		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444		0.8897569444

		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667		0.8901041667

		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889		0.8904513889

		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111		0.8907986111

		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333		0.8911458333

		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556		0.8914930556

		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778		0.8918402778

		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875		0.8921875

		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222		0.8925347222

		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444		0.8928819444

		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667		0.8932291667

		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889		0.8935763889

		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111		0.8939236111

		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333		0.8942708333

		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556		0.8946180556

		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778		0.8949652778

		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125		0.8953125

		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222		0.8956597222

		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444		0.8960069444

		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667		0.8963541667

		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889		0.8967013889

		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111		0.8970486111

		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333		0.8973958333

		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556		0.8977430556

		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778		0.8980902778

		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375		0.8984375

		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222		0.8987847222

		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444		0.8991319444

		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667		0.8994791667

		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889		0.8998263889

		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111		0.9001736111

		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333		0.9005208333

		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556		0.9008680556

		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778		0.9012152778

		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625		0.9015625

		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222		0.9019097222

		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444		0.9022569444

		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667		0.9026041667

		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889		0.9029513889

		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111		0.9032986111

		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333		0.9036458333

		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556		0.9039930556

		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778		0.9043402778

		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875		0.9046875

		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222		0.9050347222

		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444		0.9053819444

		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667		0.9057291667

		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889		0.9060763889

		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111		0.9064236111

		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333		0.9067708333

		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556		0.9071180556

		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778		0.9074652778

		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125		0.9078125

		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222		0.9081597222

		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444		0.9085069444

		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667		0.9088541667

		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889		0.9092013889

		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111		0.9095486111

		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333		0.9098958333

		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556		0.9102430556

		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778		0.9105902778

		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375		0.9109375

		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222		0.9112847222

		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444		0.9116319444

		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667		0.9119791667

		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889		0.9123263889

		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111		0.9126736111

		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333		0.9130208333

		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556		0.9133680556

		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778		0.9137152778

		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625		0.9140625

		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222		0.9144097222

		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444		0.9147569444

		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667		0.9151041667

		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889		0.9154513889

		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111		0.9157986111

		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333		0.9161458333

		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556		0.9164930556

		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778		0.9168402778

		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875		0.9171875

		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222		0.9175347222

		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444		0.9178819444

		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667		0.9182291667

		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889		0.9185763889

		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111		0.9189236111

		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333		0.9192708333

		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556		0.9196180556

		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778		0.9199652778

		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125		0.9203125

		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222		0.9206597222

		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444		0.9210069444

		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667		0.9213541667

		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889		0.9217013889

		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111		0.9220486111

		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333		0.9223958333

		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556		0.9227430556

		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778		0.9230902778

		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375		0.9234375

		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222		0.9237847222

		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444		0.9241319444

		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667		0.9244791667

		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889		0.9248263889

		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111		0.9251736111

		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333		0.9255208333

		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556		0.9258680556

		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778		0.9262152778

		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625		0.9265625

		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222		0.9269097222

		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444		0.9272569444

		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667		0.9276041667

		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889		0.9279513889

		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111		0.9282986111

		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333		0.9286458333

		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556		0.9289930556

		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778		0.9293402778

		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875		0.9296875

		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222		0.9300347222

		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444		0.9303819444

		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667		0.9307291667

		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889		0.9310763889

		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111		0.9314236111

		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333		0.9317708333

		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556		0.9321180556

		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778		0.9324652778

		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125		0.9328125

		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222		0.9331597222

		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444		0.9335069444
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4

4

4.02

4.02

4

4

7.9702888889

4

4.03

4.01

4

4

4.02

4.02

4

4.1

8.0042888889

4

4.03

4.01

4

4

4.02

4.02

4

4

8.0379555556

4

4.03

4

4

4

4.02

4.02

4

4

8.0716222222

4

4.03

4

4

4

4.02

4.02

4

4

8.1049555556

4

4.03

4

4

4

4.02

4.02

4

4

8.1386222222

4

4.03

4

3.99

4

4.02

4.02

4

4

8.1719555556

4

4.03

4

3.99

4

4.02

4.02

4

4

8.2052888889

4

4.02

4

3.99

4

4.02

4.02

4

4

8.2400777778

4

4.02

4

3.99

4

4.02

4.02

4

4

8.2726222222

4

4.02

4

3.99

4

4.01

4.02

4

4

8.3059555556

4

4.02

4

3.99

4

4.01

4.02

4

4

8.3396222222

4

4.02

4

3.99

4

4.01

4.02

4

4

8.3732888889

4

4.02

4

3.99

4

4.01

4.02

4

4

8.4066222222

4

4.02

4

3.99

4

4.01

4.02

4

4.1

8.4406222222

4

4.02

4

3.99

4

4.01

4.02

4

4

8.4739555556

4

4.02

4

3.99

4

4.01

4.02

4

4

8.5072888889

4

4.02

4

3.99

4

4.01

4.02

4

4

8.5409555556

3.99

4.02

4

3.99

4

4.01

4.02

4

4

8.5754

3.99

4.02

4

3.99

4

4.01

4.02

4

4

8.6076222222

3.99

4.02

4

3.99

4

4.01

4.01

4

4

8.6412888889

3.99

4.02

4

3.99

4

4.01

4.01

4

4

8.6749555556

3.99

4.02

4

3.99

4

4.01

4.01

4

4

8.7086222222

3.99

4.02

4

3.99

4

4.01

4.01

4

4

8.7419555556

3.99

4.02

4

3.98

3.99

4.01

4.01

3.99

4

8.7756222222

3.99

4.02

4

3.98

3.99

4.01

4.01

3.99

4

8.8104111111

3.99

4.02

4

3.98

3.99

4.01

4.01

3.99

4

8.8426333333

3.99

4.01

4

3.98

3.99

4.01

4.01

3.99

4

8.8770777778

3.99

4.01

4

3.98

3.99

4.01

4.01

3.99

4.1

8.9099444444

3.99

4.01

4

3.98

3.99

4.01

4.01

3.99

4.1

8.9439444444

3.99

4.01

4

3.98

3.99

4.01

4.01

3.99

4

8.9772777778

3.99

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4.1

9.0112777778

3.99

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.0449444444

3.99

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.0782777778

3.99

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4.1

9.1122777778

3.99

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.1459444444

3.98

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.1792777778

3.98

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.2137222222

3.98

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4.1

9.2477222222

3.98

4.01

3.99

3.98

3.99

4.01

4.01

3.99

4

9.2796222222

3.98

4.01

3.99

3.98

3.99

4

4.01

3.99

4

9.3129555556

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.3477444444

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.3802888889

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.4139555556

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.4472888889

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.4809555556

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.5146222222

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.5482888889

3.98

4.01

3.99

3.98

3.98

4

4.01

3.98

4

9.5816222222

3.98

4.01

3.99

3.98

3.98

4

4

3.98

4.1

9.6156222222

3.98

4.01

3.98

3.98

3.98

4

4

3.98

4

9.6489555556

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4

9.6826222222

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4

9.7159555556

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4

9.7496222222

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4

9.7832888889

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4.1

9.8172888889

3.98

4.01

3.98

3.97

3.98

4

4

3.98

4

9.8506222222

3.98

4

3.98

3.97

3.98

4

4

3.98

4

9.8842888889

3.98

4

3.98

3.97

3.98

4

4

3.98

4

9.9179555556

3.98

4

3.98

3.97

3.98

4

4

3.98

4

9.9516222222

3.98

4

3.98

3.97

3.98

4

4

3.98

4

9.9860666667

3.98

4

3.98

3.97

3.98

4

4

3.98

4

10.0182888889

3.98

4

3.98

3.97

3.98

4

4

3.98

4

10.0516222222

3.98

4

3.98

3.97

3.98

4

4

3.98

4

10.0852888889

3.97

4

3.98

3.97

3.98

4

4

3.98

4

10.1186222222

3.97

4

3.98

3.97

3.98

4

4

3.98

4

10.1522888889

3.97

4

3.98

3.97

3.98

4

4

3.98

4

10.1859555556

3.97

4

3.98

3.97

3.98

4

4

3.98

4

10.2192888889

3.97

4

3.98

3.97

3.97

4

4

3.98

4

10.2537333333

3.97

4

3.98

3.97

3.97

4

4

3.97

4

10.2862777778

3.97

4

3.98

3.96

3.97

4

4

3.97

4

10.3210666667

3.97

4

3.98

3.96

3.97

4

4

3.97

4

10.3544

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.3877333333

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.4199555556

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.4547444444

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4.1

10.4876111111

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.5212777778

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.5549444444

3.97

4

3.98

3.96

3.97

3.99

4

3.97

4

10.5893888889

3.97

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.6216111111

3.97

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.6549444444

3.97

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.6886111111

3.97

4

3.97

3.96

3.97

3.99

3.99

3.97

4.1

10.7226111111

3.96

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.7562777778

3.96

4

3.97

3.96

3.97

3.99

3.99

3.97

4.1

10.7902777778

3.96

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.8247222222

3.96

4

3.97

3.96

3.97

3.99

3.99

3.97

4

10.8580555556

3.96

4

3.97

3.96

3.96

3.99

3.99

3.96

4

10.8906

3.96

3.99

3.97

3.96

3.96

3.99

3.99

3.96

4

10.9242666667

3.96

3.99

3.97

3.96

3.96

3.99

3.99

3.96

4

10.9590555556

3.96

3.99

3.97

3.96

3.96

3.99

3.99

3.96

4

10.9927222222

3.96

3.99

3.97

3.96

3.96

3.99

3.99

3.96

4

11.0249444444

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.0586111111

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.0922777778

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.1252777778

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.1597222222

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.1919444444

3.96

3.99

3.97

3.96

3.96

3.98

3.99

3.96

4

11.2252777778

3.96

3.99

3.97

3.95

3.96

3.98

3.98

3.96

4

11.2589444444

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.2922777778

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.3259444444

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.3592777778

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.3926111111

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.4274

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.4599444444

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.4932777778

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.5269444444

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.5613888889

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4.1

11.5942555556

3.96

3.99

3.96

3.95

3.96

3.98

3.98

3.96

4

11.6275888889

3.96

3.98

3.96

3.95

3.96

3.98

3.98

3.96

4

11.6612555556

3.96

3.98

3.96

3.95

3.96

3.98

3.98

3.96

4

11.6949222222

3.95

3.98

3.96

3.95

3.96

3.98

3.98

3.96

4

11.7285888889

3.95

3.98

3.96

3.95

3.96

3.98

3.98

3.96

4

11.7622555556

3.95

3.98

3.96

3.95

3.95

3.98

3.98

3.96

4.1

11.7962555556

3.95

3.98

3.96

3.95

3.95

3.98

3.98

3.96

4

11.8295888889

3.95

3.98

3.96

3.95

3.95

3.98

3.98

3.95

4

11.8629222222

3.95

3.98

3.96

3.95

3.95

3.98

3.98

3.95

4

11.8965888889

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4

11.9310333333

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4.1

11.9650333333

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4

11.9975777778

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4

12.0309111111

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4

12.0642444444

3.95

3.98

3.96

3.94

3.95

3.98

3.98

3.95

4

12.0975777778

3.95

3.98

3.96

3.94

3.95

3.97

3.98

3.95

4

12.1312444444

3.95

3.98

3.96

3.94

3.95

3.97

3.98

3.95

4

12.1645777778

3.95

3.98

3.96

3.94

3.95

3.97

3.98

3.95

4

12.1979111111

3.95

3.98

3.96

3.94

3.95

3.97

3.98

3.95

4

12.2315777778

3.95

3.98

3.96

3.94

3.95

3.97

3.98

3.95

4

12.2649111111

3.95

3.98

3.96

3.94

3.95

3.97

3.97

3.95

4

12.2985777778

3.95

3.98

3.95

3.94

3.95

3.97

3.97

3.95

4

12.3322444444

3.95

3.98

3.95

3.94

3.95

3.97

3.97

3.95

4

12.3655777778

3.95

3.98

3.95

3.94

3.95

3.97

3.97

3.95

4

12.4003666667

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.95

4

12.4329111111

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.95

4

12.4665777778

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4

12.4999111111

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4

12.5332444444

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4

12.5669111111

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4.1

12.6020444444

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4

12.6345888889

3.94

3.98

3.95

3.94

3.94

3.97

3.97

3.94

4

12.6682555556

3.94

3.97

3.95

3.94

3.94

3.97

3.97

3.94

4

12.7019222222

3.94

3.97

3.95

3.94

3.94

3.97

3.97

3.94

4

12.7363666667

3.94

3.97

3.95

3.94

3.94

3.97

3.97

3.94

4

12.7685888889

3.94

3.97

3.95

3.94

3.94

3.96

3.97

3.94

4

12.8019222222

3.94

3.97

3.95

3.94

3.94

3.96

3.97

3.94

4

12.8352555556

3.94

3.97

3.95

3.94

3.94

3.96

3.97

3.94

4

12.8689222222

3.94

3.97

3.95

3.94

3.94

3.96

3.97

3.94

4

12.9025888889

3.94

3.97

3.95

3.93

3.94

3.96

3.97

3.94

4.1

12.9365888889

3.94

3.97

3.95

3.93

3.94

3.96

3.97

3.94

4

12.9699222222

3.94

3.97

3.95

3.93

3.94

3.96

3.97

3.94

4

13.0035888889

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4.1

13.0375888889

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4.1

13.0727222222

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.1049444444

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.1386111111

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4.1

13.1737444444

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.2059666667

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.2407555556

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.2740888889

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4

13.3077555556

3.94

3.96

3.94

3.93

3.94

3.96

3.96

3.94

4

13.3414222222

3.94

3.97

3.94

3.93

3.94

3.96

3.96

3.94

4
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b3_discharge

		Send Time		Send String		Receive Time		Cmd		Batt State		Batt Voltage		Current		Round Current		Max Temp		Cell1		Cell2		Cell3		Cell4		Cell5		Cell6		Cell7		Cell8		Time		Total Ah		Total Wh

		S1148753357:		#B3q0		1148753357:		$B3q0		d-		33.22		0.0		0.0		21.19		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15		0:02:30		0.00		0.00

		S1148753387:		#B3q0		1148753387:		$B3q0		d-		33.18		0.0		0.0		21.28		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15		0:03:00		0.00		0.00

		S1148753417:		#B3q0		1148753417:		$B3q0		d-		33.22		0.0		0.0		21.28		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15		0:03:30		0.00		0.00

		S1148753447:		#B3q0		1148753447:		$B3q0		d-		33.22		0.0		0.0		21.38		4.14		4.16		4.14		4.14		4.15		4.15		4.16		4.15		0:04:00		0.00		0.00

		S1148753477:		#B3q0		1148753477:		$B3q0		d-		32.99		4.0		4.0		21.38		4.12		4.14		4.12		4.12		4.13		4.13		4.13		4.13		0:04:30		0.03		0.55

		S1148753507:		#B3q0		1148753507:		$B3q0		d-		32.99		4.0		4.0		21.48		4.12		4.14		4.12		4.12		4.13		4.13		4.13		4.12		0:05:00		0.07		1.65

		S1148753537:		#B3q0		1148753537:		$B3q0		d-		32.95		4.0		4.0		21.48		4.12		4.13		4.12		4.12		4.13		4.13		4.13		4.12		0:05:30		0.10		2.74

		S1148753567:		#B3q0		1148753567:		$B3q0		d-		32.95		4.0		4.0		21.48		4.12		4.13		4.11		4.11		4.12		4.12		4.13		4.12		0:06:00		0.13		3.84

		S1148753597:		#B3q0		1148753597:		$B3q0		d-		32.95		4.0		4.0		21.58		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12		0:06:30		0.17		4.93

		S1148753627:		#B3q0		1148753627:		$B3q0		d-		32.95		4.0		4.0		21.58		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12		0:07:00		0.20		6.02

		S1148753657:		#B3q0		1148753657:		$B3q0		d-		32.91		4.0		4.0		21.67		4.11		4.13		4.11		4.11		4.12		4.12		4.13		4.12		0:07:30		0.23		7.12

		S1148753687:		#B3q0		1148753687:		$B3q0		d-		32.91		4.0		4.0		21.67		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12		0:08:00		0.27		8.21

		S1148753717:		#B3q0		1148753717:		$B3q0		d-		32.91		4.0		4.0		21.67		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12		0:08:30		0.30		9.30

		S1148753747:		#B3q0		1148753747:		$B3q0		d-		32.91		4.0		4.0		21.87		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12		0:09:00		0.33		10.40

		S1148753777:		#B3q0		1148753777:		$B3q0		d-		32.91		4.0		4.0		21.87		4.11		4.13		4.11		4.11		4.12		4.12		4.12		4.12		0:09:30		0.37		11.49

		S1148753807:		#B3q0		1148753807:		$B3q0		d-		32.95		4.0		4.0		21.87		4.11		4.12		4.11		4.11		4.12		4.12		4.12		4.11		0:10:00		0.40		12.60

		S1148753837:		#B3q0		1148753837:		$B3q0		d-		32.95		4.0		4.0		21.97		4.11		4.12		4.11		4.10		4.12		4.12		4.12		4.11		0:10:30		0.43		13.69

		S1148753867:		#B3q0		1148753867:		$B3q0		d-		32.91		4.0		4.0		21.87		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11		0:11:00		0.47		14.79

		S1148753897:		#B3q0		1148753897:		$B3q0		d-		32.91		4.0		4.0		21.87		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11		0:11:30		0.50		15.87

		S1148753927:		#B3q0		1148753927:		$B3q0		d-		32.95		4.0		4.0		21.97		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11		0:12:00		0.53		16.96

		S1148753957:		#B3q0		1148753957:		$B3q0		d-		32.91		4.0		4.0		22.07		4.10		4.12		4.10		4.10		4.12		4.12		4.12		4.11		0:12:30		0.57		18.06

		S1148753987:		#B3q0		1148753987:		$B3q0		d-		32.91		4.0		4.0		22.07		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11		0:13:00		0.60		19.15

		S1148754017:		#B3q0		1148754017:		$B3q0		d-		32.91		4.0		4.0		22.16		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11		0:13:30		0.63		20.25

		S1148754047:		#B3q0		1148754047:		$B3q0		d-		32.88		4.0		4.0		22.16		4.10		4.12		4.10		4.10		4.11		4.12		4.12		4.11		0:14:00		0.67		21.35

		S1148754077:		#B3q0		1148754077:		$B3q0		d-		32.88		4.0		4.0		22.26		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11		0:14:30		0.70		22.45

		S1148754107:		#B3q0		1148754107:		$B3q0		d-		32.91		4.0		4.0		22.26		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11		0:15:00		0.73		23.54

		S1148754137:		#B3q0		1148754137:		$B3q0		d-		32.84		4.0		4.0		22.26		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.11		0:15:30		0.76		24.63

		S1148754167:		#B3q0		1148754167:		$B3q0		d-		32.84		4.0		4.0		22.26		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10		0:16:00		0.80		25.72

		S1148754197:		#B3q0		1148754197:		$B3q0		d-		32.88		4.0		4.0		22.26		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10		0:16:30		0.83		26.82

		S1148754227:		#B3q0		1148754227:		$B3q0		d-		32.84		4.0		4.0		22.36		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10		0:17:00		0.86		27.92

		S1148754257:		#B3q0		1148754257:		$B3q0		d-		32.84		4.0		4.0		22.36		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10		0:17:30		0.90		29.01

		S1148754287:		#B3q0		1148754287:		$B3q0		d-		32.88		4.0		4.0		22.36		4.10		4.12		4.10		4.10		4.11		4.11		4.12		4.10		0:18:00		0.93		30.11

		S1148754317:		#B3q0		1148754317:		$B3q0		d-		32.84		4.0		4.0		22.46		4.10		4.12		4.10		4.10		4.11		4.11		4.11		4.10		0:18:30		0.96		31.20

		S1148754347:		#B3q0		1148754347:		$B3q0		d-		32.84		4.0		4.0		22.46		4.10		4.12		4.10		4.10		4.11		4.11		4.11		4.10		0:19:00		1.00		32.30

		S1148754377:		#B3q0		1148754377:		$B3q0		d-		32.84		4.0		4.0		22.46		4.10		4.12		4.10		4.10		4.10		4.11		4.11		4.10		0:19:30		1.03		33.38

		S1148754407:		#B3q0		1148754407:		$B3q0		d-		32.84		4.0		4.0		22.46		4.10		4.12		4.10		4.09		4.10		4.11		4.11		4.10		0:20:00		1.06		34.47

		S1148754437:		#B3q0		1148754437:		$B3q0		d-		32.88		4.0		4.0		22.55		4.10		4.12		4.10		4.09		4.10		4.11		4.11		4.10		0:20:30		1.10		35.56

		S1148754467:		#B3q0		1148754467:		$B3q0		d-		32.84		4.0		4.0		22.55		4.09		4.12		4.10		4.09		4.10		4.11		4.11		4.10		0:21:00		1.13		36.66

		S1148754497:		#B3q0		1148754497:		$B3q0		d-		32.88		4.0		4.0		22.65		4.09		4.11		4.10		4.09		4.10		4.11		4.11		4.10		0:21:30		1.16		37.76

		S1148754527:		#B3q0		1148754527:		$B3q0		d-		32.84		4.0		4.0		22.65		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:22:00		1.20		38.86

		S1148754557:		#B3q0		1148754557:		$B3q0		d-		32.84		4.0		4.0		22.65		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:22:30		1.23		39.96

		S1148754587:		#B3q0		1148754587:		$B3q0		d-		32.84		4.0		4.0		22.65		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:23:00		1.27		41.06

		S1148754617:		#B3q0		1148754617:		$B3q0		d-		32.84		4.0		4.0		22.75		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:23:30		1.30		42.16

		S1148754647:		#B3q0		1148754647:		$B3q0		d-		32.76		4.0		4.0		22.75		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:24:00		1.33		43.25

		S1148754677:		#B3q0		1148754677:		$B3q0		d-		32.8		4.0		4.0		22.75		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:24:30		1.36		44.34

		S1148754707:		#B3q0		1148754707:		$B3q0		d-		32.84		4.0		4.0		22.85		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:25:00		1.40		45.43

		S1148754737:		#B3q0		1148754737:		$B3q0		d-		32.84		4.0		4.0		22.85		4.09		4.11		4.09		4.09		4.10		4.10		4.11		4.10		0:25:30		1.43		46.53

		S1148754767:		#B3q0		1148754767:		$B3q0		d-		32.8		4.0		4.0		22.85		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.10		0:26:00		1.47		47.63

		S1148754797:		#B3q0		1148754797:		$B3q0		d-		32.76		4.0		4.0		22.85		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.10		0:26:30		1.50		48.72

		S1148754827:		#B3q0		1148754827:		$B3q0		d-		32.76		4.0		4.0		22.85		4.09		4.11		4.09		4.09		4.10		4.10		4.10		4.09		0:27:00		1.53		49.82

		S1148754857:		#B3q0		1148754857:		$B3q0		d-		32.76		4.0		4.0		22.85		4.09		4.11		4.09		4.08		4.10		4.10		4.10		4.09		0:27:30		1.57		50.92

		S1148754887:		#B3q0		1148754887:		$B3q0		d-		32.8		4.0		4.0		23.04		4.09		4.11		4.09		4.08		4.10		4.10		4.10		4.09		0:28:00		1.60		52.01

		S1148754917:		#B3q0		1148754917:		$B3q0		d-		32.76		4.0		4.0		23.04		4.08		4.11		4.09		4.08		4.10		4.10		4.10		4.09		0:28:30		1.63		53.10

		S1148754947:		#B3q0		1148754947:		$B3q0		d-		32.76		4.0		4.0		23.04		4.08		4.11		4.09		4.08		4.10		4.10		4.10		4.09		0:29:00		1.67		54.19

		S1148754977:		#B3q0		1148754977:		$B3q0		d-		32.73		4.0		4.0		23.04		4.08		4.10		4.08		4.08		4.10		4.10		4.10		4.09		0:29:30		1.70		55.28

		S1148755007:		#B3q0		1148755007:		$B3q0		d-		32.76		4.0		4.0		23.04		4.08		4.10		4.08		4.08		4.10		4.10		4.10		4.09		0:30:00		1.73		56.37

		S1148755037:		#B3q0		1148755037:		$B3q0		d-		32.76		4.0		4.0		23.04		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:30:30		1.76		57.45

		S1148755067:		#B3q0		1148755067:		$B3q0		d-		32.73		4.0		4.0		23.04		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:31:00		1.80		58.54

		S1148755097:		#B3q0		1148755097:		$B3q0		d-		32.73		4.0		4.0		23.14		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:31:30		1.83		59.63

		S1148755127:		#B3q0		1148755127:		$B3q0		d-		32.73		4.0		4.0		23.04		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:32:00		1.86		60.72

		S1148755157:		#B3q0		1148755157:		$B3q0		d-		32.69		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:32:30		1.90		61.81

		S1148755187:		#B3q0		1148755187:		$B3q0		d-		32.76		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:33:00		1.93		62.90

		S1148755217:		#B3q0		1148755217:		$B3q0		d-		32.8		4.0		4.0		23.14		4.08		4.10		4.08		4.08		4.09		4.10		4.10		4.09		0:33:30		1.96		63.99

		S1148755247:		#B3q0		1148755247:		$B3q0		d-		32.76		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:34:00		2.00		65.09

		S1148755277:		#B3q0		1148755277:		$B3q0		d-		32.73		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:34:30		2.03		66.19

		S1148755307:		#B3q0		1148755307:		$B3q0		d-		32.73		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:35:00		2.07		67.29

		S1148755337:		#B3q0		1148755337:		$B3q0		d-		32.69		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:35:30		2.10		68.39

		S1148755367:		#B3q0		1148755368:		$B3q0		d-		32.73		4.0		4.0		23.24		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:36:01		2.13		69.52

		S1148755397:		#B3q0		1148755397:		$B3q0		d-		32.73		4.0		4.0		23.33		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:36:30		2.17		70.58

		S1148755427:		#B3q0		1148755427:		$B3q0		d-		32.69		4.0		4.0		23.33		4.08		4.10		4.08		4.08		4.09		4.09		4.10		4.08		0:37:00		2.20		71.68

		S1148755457:		#B3q0		1148755457:		$B3q0		d-		32.73		4.0		4.0		23.33		4.08		4.10		4.08		4.08		4.08		4.09		4.10		4.08		0:37:30		2.23		72.77

		S1148755487:		#B3q0		1148755487:		$B3q0		d-		32.69		4.0		4.0		23.33		4.08		4.10		4.08		4.08		4.08		4.09		4.10		4.08		0:38:00		2.27		73.87

		S1148755517:		#B3q0		1148755517:		$B3q0		d-		32.73		4.0		4.0		23.43		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:38:30		2.30		74.97

		S1148755547:		#B3q0		1148755547:		$B3q0		d-		32.73		4.0		4.0		23.33		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:39:00		2.33		76.06

		S1148755577:		#B3q0		1148755577:		$B3q0		d-		32.69		4.0		4.0		23.43		4.08		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:39:30		2.37		77.16

		S1148755607:		#B3q0		1148755608:		$B3q0		d-		32.69		4.0		4.0		23.53		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:40:01		2.40		78.29

		S1148755637:		#B3q0		1148755637:		$B3q0		d-		32.73		4.0		4.0		23.43		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:40:30		2.43		79.35

		S1148755667:		#B3q0		1148755667:		$B3q0		d-		32.69		4.0		4.0		23.43		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:41:00		2.47		80.45

		S1148755697:		#B3q0		1148755697:		$B3q0		d-		32.73		4.0		4.0		23.53		4.07		4.10		4.08		4.07		4.08		4.09		4.09		4.08		0:41:30		2.50		81.54

		S1148755727:		#B3q0		1148755727:		$B3q0		d-		32.73		4.0		4.0		23.53		4.07		4.10		4.07		4.07		4.08		4.09		4.09		4.08		0:42:00		2.53		82.64

		S1148755757:		#B3q0		1148755757:		$B3q0		d-		32.69		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.09		4.09		4.08		0:42:30		2.57		83.74

		S1148755787:		#B3q0		1148755787:		$B3q0		d-		32.69		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08		0:43:00		2.60		84.83

		S1148755817:		#B3q0		1148755818:		$B3q0		d-		32.69		4.0		4.0		23.53		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08		0:43:31		2.64		85.96

		S1148755847:		#B3q0		1148755847:		$B3q0		d-		32.69		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08		0:44:00		2.67		87.02

		S1148755877:		#B3q0		1148755877:		$B3q0		d-		32.61		4.0		4.0		23.53		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08		0:44:30		2.70		88.10

		S1148755907:		#B3q0		1148755907:		$B3q0		d-		32.69		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.08		0:45:00		2.73		89.19

		S1148755937:		#B3q0		1148755937:		$B3q0		d-		32.69		4.0		4.0		23.53		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07		0:45:30		2.77		90.29

		S1148755967:		#B3q0		1148755967:		$B3q0		d-		32.61		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07		0:46:00		2.80		91.38

		S1148755997:		#B3q0		1148755997:		$B3q0		d-		32.65		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07		0:46:30		2.84		92.47

		S1148756027:		#B3q0		1148756027:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.07		4.08		4.08		4.09		4.07		0:47:00		2.87		93.57

		S1148756057:		#B3q0		1148756057:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.07		4.08		4.08		4.08		4.07		0:47:30		2.90		94.66

		S1148756087:		#B3q0		1148756087:		$B3q0		d-		32.65		4.0		4.0		23.63		4.07		4.09		4.07		4.07		4.08		4.08		4.08		4.07		0:48:00		2.94		95.75

		S1148756117:		#B3q0		1148756117:		$B3q0		d-		32.61		4.0		4.0		23.82		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07		0:48:30		2.97		96.84

		S1148756147:		#B3q0		1148756147:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07		0:49:00		3.00		97.93

		S1148756177:		#B3q0		1148756177:		$B3q0		d-		32.61		4.0		4.0		23.82		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07		0:49:30		3.04		99.01

		S1148756207:		#B3q0		1148756207:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.07		4.07		4.08		4.08		4.07		0:50:00		3.07		100.10

		S1148756237:		#B3q0		1148756237:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.06		4.07		4.08		4.08		4.07		0:50:30		3.10		101.19

		S1148756267:		#B3q0		1148756267:		$B3q0		d-		32.61		4.0		4.0		23.73		4.07		4.09		4.07		4.06		4.07		4.08		4.08		4.07		0:51:00		3.14		102.28

		S1148756297:		#B3q0		1148756297:		$B3q0		d-		32.61		4.0		4.0		23.92		4.07		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:51:30		3.17		103.37

		S1148756327:		#B3q0		1148756327:		$B3q0		d-		32.61		4.0		4.0		23.82		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:52:00		3.20		104.46

		S1148756357:		#B3q0		1148756357:		$B3q0		d-		32.61		4.0		4.0		23.82		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:52:30		3.24		105.55

		S1148756387:		#B3q0		1148756387:		$B3q0		d-		32.65		4.0		4.0		23.92		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:53:00		3.27		106.65

		S1148756417:		#B3q0		1148756417:		$B3q0		d-		32.61		4.0		4.0		23.92		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:53:30		3.30		107.74

		S1148756447:		#B3q0		1148756447:		$B3q0		d-		32.61		4.0		4.0		23.82		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:54:00		3.34		108.83

		S1148756477:		#B3q0		1148756477:		$B3q0		d-		32.61		4.0		4.0		23.82		4.06		4.08		4.07		4.06		4.07		4.08		4.08		4.07		0:54:30		3.37		109.92

		S1148756507:		#B3q0		1148756507:		$B3q0		d-		32.61		4.0		4.0		23.82		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07		0:55:00		3.40		111.01

		S1148756537:		#B3q0		1148756537:		$B3q0		d-		32.57		4.1		4.1		23.92		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07		0:55:30		3.44		112.11

		S1148756567:		#B3q0		1148756567:		$B3q0		d-		32.57		4.1		4.1		24.02		4.06		4.08		4.06		4.06		4.07		4.08		4.08		4.07		0:56:00		3.47		113.22

		S1148756597:		#B3q0		1148756597:		$B3q0		d-		32.53		4.0		4.0		23.92		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.07		0:56:30		3.51		114.32

		S1148756627:		#B3q0		1148756627:		$B3q0		d-		32.61		4.0		4.0		24.02		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.07		0:57:00		3.54		115.41

		S1148756657:		#B3q0		1148756657:		$B3q0		d-		32.53		4.0		4.0		24.02		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.06		0:57:30		3.57		116.50

		S1148756687:		#B3q0		1148756687:		$B3q0		d-		32.57		4.1		4.1		24.02		4.06		4.08		4.06		4.06		4.07		4.07		4.08		4.06		0:58:00		3.61		117.59

		S1148756717:		#B3q0		1148756717:		$B3q0		d-		32.57		4.0		4.0		23.92		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06		0:58:30		3.64		118.70

		S1148756747:		#B3q0		1148756747:		$B3q0		d-		32.57		4.0		4.0		23.92		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06		0:59:00		3.67		119.79

		S1148756777:		#B3q0		1148756777:		$B3q0		d-		32.53		4.0		4.0		24.02		4.06		4.08		4.06		4.05		4.07		4.07		4.08		4.06		0:59:30		3.71		120.89

		S1148756807:		#B3q0		1148756807:		$B3q0		d-		32.53		4.0		4.0		24.02		4.05		4.08		4.06		4.05		4.06		4.07		4.08		4.06		1:00:00		3.74		121.98

		S1148756837:		#B3q0		1148756837:		$B3q0		d-		32.53		4.0		4.0		24.02		4.05		4.08		4.06		4.05		4.06		4.07		4.08		4.06		1:00:30		3.77		123.07

		S1148756867:		#B3q0		1148756867:		$B3q0		d-		32.53		4.0		4.0		24.02		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:01:00		3.81		124.16

		S1148756897:		#B3q0		1148756898:		$B3q0		d-		32.53		4.0		4.0		24.02		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:01:30		3.84		125.26

		S1148756927:		#B3q0		1148756927:		$B3q0		d-		32.53		4.1		4.1		24.02		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:02:00		3.88		126.36

		S1148756957:		#B3q0		1148756957:		$B3q0		d-		32.53		4.0		4.0		24.12		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:02:30		3.91		127.46

		S1148756987:		#B3q0		1148756987:		$B3q0		d-		32.53		4.0		4.0		24.12		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:03:00		3.94		128.56

		S1148757017:		#B3q0		1148757017:		$B3q0		d-		32.5		4.1		4.1		24.12		4.05		4.08		4.06		4.05		4.06		4.07		4.07		4.06		1:03:30		3.98		129.66

		S1148757047:		#B3q0		1148757047:		$B3q0		d-		32.53		4.1		4.1		24.21		4.05		4.08		4.05		4.05		4.06		4.07		4.07		4.06		1:04:00		4.01		130.76

		S1148757077:		#B3q0		1148757077:		$B3q0		d-		32.53		4.0		4.0		24.21		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.06		1:04:30		4.04		131.86

		S1148757107:		#B3q0		1148757107:		$B3q0		d-		32.53		4.0		4.0		24.12		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.06		1:05:00		4.08		132.96

		S1148757137:		#B3q0		1148757137:		$B3q0		d-		32.5		4.0		4.0		24.12		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:05:30		4.11		134.05

		S1148757167:		#B3q0		1148757167:		$B3q0		d-		32.53		4.0		4.0		24.12		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:06:00		4.15		135.14

		S1148757197:		#B3q0		1148757197:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:06:30		4.18		136.23

		S1148757227:		#B3q0		1148757227:		$B3q0		d-		32.53		4.0		4.0		24.21		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:07:00		4.21		137.32

		S1148757257:		#B3q0		1148757257:		$B3q0		d-		32.46		4.0		4.0		24.21		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:07:31		4.25		138.44

		S1148757287:		#B3q0		1148757287:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.06		4.07		4.07		4.05		1:08:00		4.28		139.49

		S1148757317:		#B3q0		1148757317:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.05		4.07		4.07		4.05		1:08:30		4.31		140.57

		S1148757347:		#B3q0		1148757347:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.05		4.07		4.07		4.05		1:09:00		4.35		141.66

		S1148757377:		#B3q0		1148757377:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.05		4.06		4.07		4.05		1:09:30		4.38		142.75

		S1148757407:		#B3q0		1148757407:		$B3q0		d-		32.46		4.0		4.0		24.31		4.05		4.07		4.05		4.05		4.05		4.06		4.07		4.05		1:10:00		4.41		143.84

		S1148757437:		#B3q0		1148757437:		$B3q0		d-		32.46		4.0		4.0		24.31		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:10:30		4.45		144.94

		S1148757467:		#B3q0		1148757467:		$B3q0		d-		32.5		4.0		4.0		24.31		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:11:00		4.48		146.03

		S1148757497:		#B3q0		1148757497:		$B3q0		d-		32.46		4.0		4.0		24.31		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:11:30		4.51		147.12

		S1148757527:		#B3q0		1148757528:		$B3q0		d-		32.46		4.1		4.1		24.41		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:12:01		4.55		148.26

		S1148757557:		#B3q0		1148757557:		$B3q0		d-		32.42		4.0		4.0		24.41		4.05		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:12:30		4.58		149.32

		S1148757587:		#B3q0		1148757587:		$B3q0		d-		32.42		4.0		4.0		24.31		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:13:00		4.62		150.41

		S1148757617:		#B3q0		1148757617:		$B3q0		d-		32.42		4.1		4.1		24.41		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:13:30		4.65		151.50

		S1148757647:		#B3q0		1148757647:		$B3q0		d-		32.5		4.1		4.1		24.41		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:14:00		4.68		152.60

		S1148757677:		#B3q0		1148757677:		$B3q0		d-		32.42		4.0		4.0		24.31		4.04		4.07		4.05		4.04		4.05		4.06		4.07		4.05		1:14:30		4.72		153.70

		S1148757707:		#B3q0		1148757707:		$B3q0		d-		32.42		4.0		4.0		24.41		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05		1:15:00		4.75		154.79

		S1148757737:		#B3q0		1148757737:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05		1:15:30		4.78		155.88

		S1148757767:		#B3q0		1148757767:		$B3q0		d-		32.42		4.0		4.0		24.41		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05		1:16:00		4.82		156.97

		S1148757797:		#B3q0		1148757797:		$B3q0		d-		32.42		4.0		4.0		24.41		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05		1:16:30		4.85		158.06

		S1148757827:		#B3q0		1148757827:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.07		4.05		4.04		4.05		4.06		4.06		4.05		1:17:00		4.88		159.15

		S1148757857:		#B3q0		1148757857:		$B3q0		d-		32.42		4.1		4.1		24.41		4.04		4.07		4.04		4.04		4.05		4.06		4.06		4.05		1:17:30		4.92		160.24

		S1148757887:		#B3q0		1148757887:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.06		4.04		4.04		4.05		4.06		4.06		4.04		1:18:00		4.95		161.33

		S1148757917:		#B3q0		1148757917:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.07		4.04		4.04		4.05		4.06		4.06		4.04		1:18:30		4.99		162.42

		S1148757947:		#B3q0		1148757947:		$B3q0		d-		32.38		4.0		4.0		24.51		4.04		4.06		4.04		4.03		4.05		4.05		4.06		4.04		1:19:00		5.02		163.50

		S1148757977:		#B3q0		1148757977:		$B3q0		d-		32.42		4.0		4.0		24.41		4.04		4.06		4.04		4.03		4.05		4.05		4.06		4.04		1:19:30		5.05		164.58

		S1148758007:		#B3q0		1148758007:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:20:01		5.09		165.71

		S1148758037:		#B3q0		1148758037:		$B3q0		d-		32.42		4.0		4.0		24.51		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:20:31		5.12		166.80

		S1148758067:		#B3q0		1148758067:		$B3q0		d-		32.38		4.0		4.0		24.51		4.04		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:21:00		5.15		167.85

		S1148758097:		#B3q0		1148758097:		$B3q0		d-		32.42		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:21:30		5.19		168.95

		S1148758127:		#B3q0		1148758127:		$B3q0		d-		32.42		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:22:00		5.22		170.04

		S1148758157:		#B3q0		1148758157:		$B3q0		d-		32.42		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:22:30		5.25		171.13

		S1148758187:		#B3q0		1148758187:		$B3q0		d-		32.38		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:23:00		5.29		172.22

		S1148758217:		#B3q0		1148758217:		$B3q0		d-		32.42		4.0		4.0		24.6		4.03		4.06		4.04		4.03		4.04		4.05		4.06		4.04		1:23:30		5.32		173.31

		S1148758247:		#B3q0		1148758247:		$B3q0		d-		32.38		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04		1:24:00		5.36		174.40

		S1148758277:		#B3q0		1148758277:		$B3q0		d-		32.38		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04		1:24:30		5.39		175.47

		S1148758307:		#B3q0		1148758307:		$B3q0		d-		32.38		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04		1:25:00		5.42		176.55

		S1148758337:		#B3q0		1148758337:		$B3q0		d-		32.38		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04		1:25:30		5.46		177.63

		S1148758367:		#B3q0		1148758367:		$B3q0		d-		32.35		4.0		4.0		24.51		4.03		4.06		4.04		4.03		4.04		4.05		4.05		4.04		1:26:00		5.49		178.71

		S1148758397:		#B3q0		1148758397:		$B3q0		d-		32.35		4.0		4.0		24.6		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03		1:26:30		5.52		179.79

		S1148758427:		#B3q0		1148758427:		$B3q0		d-		32.35		4.0		4.0		24.6		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03		1:27:00		5.56		180.87

		S1148758457:		#B3q0		1148758457:		$B3q0		d-		32.38		4.0		4.0		24.7		4.03		4.06		4.03		4.03		4.04		4.05		4.05		4.03		1:27:30		5.59		181.95

		S1148758487:		#B3q0		1148758487:		$B3q0		d-		32.35		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.04		4.05		4.05		4.03		1:28:00		5.62		183.04

		S1148758517:		#B3q0		1148758517:		$B3q0		d-		32.35		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:28:30		5.66		184.13

		S1148758547:		#B3q0		1148758547:		$B3q0		d-		32.31		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:29:00		5.69		185.21

		S1148758577:		#B3q0		1148758577:		$B3q0		d-		32.35		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:29:30		5.72		186.30

		S1148758607:		#B3q0		1148758607:		$B3q0		d-		32.31		4.0		4.0		24.6		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:30:00		5.76		187.38

		S1148758637:		#B3q0		1148758637:		$B3q0		d-		32.31		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:30:30		5.79		188.46

		S1148758667:		#B3q0		1148758667:		$B3q0		d-		32.35		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:31:00		5.82		189.54

		S1148758697:		#B3q0		1148758697:		$B3q0		d-		32.35		4.0		4.0		24.7		4.03		4.05		4.03		4.03		4.03		4.05		4.05		4.03		1:31:30		5.86		190.62

		S1148758727:		#B3q0		1148758727:		$B3q0		d-		32.31		4.0		4.0		24.7		4.03		4.05		4.03		4.02		4.03		4.05		4.05		4.03		1:32:01		5.89		191.74

		S1148758757:		#B3q0		1148758757:		$B3q0		d-		32.31		4.0		4.0		24.7		4.03		4.05		4.03		4.02		4.03		4.05		4.05		4.03		1:32:30		5.92		192.78

		S1148758787:		#B3q0		1148758787:		$B3q0		d-		32.35		4.0		4.0		24.8		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:33:00		5.96		193.86

		S1148758817:		#B3q0		1148758818:		$B3q0		d-		32.35		4.0		4.0		24.8		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:33:31		5.99		194.98

		S1148758847:		#B3q0		1148758847:		$B3q0		d-		32.31		4.0		4.0		24.8		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:34:00		6.02		196.03

		S1148758877:		#B3q0		1148758877:		$B3q0		d-		32.31		4.0		4.0		24.8		4.03		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:34:30		6.06		197.11

		S1148758907:		#B3q0		1148758907:		$B3q0		d-		32.31		4.0		4.0		24.8		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:35:00		6.09		198.19

		S1148758937:		#B3q0		1148758937:		$B3q0		d-		32.31		4.0		4.0		24.7		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:35:30		6.12		199.28

		S1148758967:		#B3q0		1148758967:		$B3q0		d-		32.27		4.0		4.0		24.7		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:36:00		6.16		200.35

		S1148758997:		#B3q0		1148758997:		$B3q0		d-		32.27		4.0		4.0		24.7		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:36:30		6.19		201.43

		S1148759027:		#B3q0		1148759027:		$B3q0		d-		32.27		4.1		4.1		24.7		4.02		4.05		4.03		4.02		4.03		4.04		4.05		4.03		1:37:00		6.23		202.53

		S1148759057:		#B3q0		1148759057:		$B3q0		d-		32.27		4.0		4.0		24.8		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03		1:37:30		6.26		203.62

		S1148759087:		#B3q0		1148759087:		$B3q0		d-		32.27		4.0		4.0		24.7		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03		1:38:00		6.29		204.70

		S1148759117:		#B3q0		1148759117:		$B3q0		d-		32.27		4.0		4.0		24.8		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.03		1:38:30		6.33		205.79

		S1148759147:		#B3q0		1148759147:		$B3q0		d-		32.31		4.1		4.1		24.8		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02		1:39:00		6.36		206.87

		S1148759177:		#B3q0		1148759177:		$B3q0		d-		32.27		4.0		4.0		24.9		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02		1:39:30		6.39		207.96

		S1148759207:		#B3q0		1148759207:		$B3q0		d-		32.27		4.0		4.0		24.8		4.02		4.05		4.03		4.02		4.03		4.04		4.04		4.02		1:40:00		6.43		209.05

		S1148759237:		#B3q0		1148759237:		$B3q0		d-		32.27		4.0		4.0		24.8		4.02		4.05		4.03		4.01		4.03		4.04		4.04		4.02		1:40:30		6.46		210.13

		S1148759267:		#B3q0		1148759267:		$B3q0		d-		32.23		4.1		4.1		24.9		4.02		4.05		4.02		4.01		4.02		4.04		4.04		4.02		1:41:00		6.49		211.22

		S1148759297:		#B3q0		1148759297:		$B3q0		d-		32.27		4.0		4.0		24.8		4.02		4.05		4.02		4.01		4.02		4.04		4.04		4.02		1:41:30		6.53		212.31

		S1148759327:		#B3q0		1148759327:		$B3q0		d-		32.23		4.0		4.0		24.9		4.02		4.04		4.02		4.01		4.02		4.04		4.04		4.02		1:42:00		6.56		213.39

		S1148759357:		#B3q0		1148759357:		$B3q0		d-		32.23		4.0		4.0		24.8		4.02		4.04		4.02		4.01		4.02		4.04		4.04		4.02		1:42:30		6.60		214.46

		S1148759387:		#B3q0		1148759388:		$B3q0		d-		32.23		4.0		4.0		24.9		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:43:01		6.63		215.57

		S1148759417:		#B3q0		1148759417:		$B3q0		d-		32.27		4.0		4.0		24.9		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:43:30		6.66		216.61

		S1148759447:		#B3q0		1148759447:		$B3q0		d-		32.27		4.0		4.0		24.9		4.02		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:44:01		6.70		217.72

		S1148759477:		#B3q0		1148759477:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:44:30		6.73		218.77

		S1148759507:		#B3q0		1148759507:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:45:00		6.76		219.85

		S1148759537:		#B3q0		1148759537:		$B3q0		d-		32.27		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:45:30		6.80		220.93

		S1148759567:		#B3q0		1148759567:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:46:00		6.83		222.01

		S1148759597:		#B3q0		1148759597:		$B3q0		d-		32.27		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:46:30		6.86		223.08

		S1148759627:		#B3q0		1148759627:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:47:00		6.90		224.16

		S1148759657:		#B3q0		1148759657:		$B3q0		d-		32.19		4.1		4.1		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.04		4.02		1:47:30		6.93		225.24

		S1148759687:		#B3q0		1148759687:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.02		1:48:00		6.96		226.33

		S1148759717:		#B3q0		1148759717:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.01		1:48:30		7.00		227.41

		S1148759747:		#B3q0		1148759747:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.02		4.03		4.03		4.01		1:49:00		7.03		228.49

		S1148759777:		#B3q0		1148759777:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.04		4.02		4.01		4.01		4.03		4.03		4.01		1:49:30		7.06		229.56

		S1148759807:		#B3q0		1148759807:		$B3q0		d-		32.23		4.0		4.0		24.9		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01		1:50:00		7.10		230.64

		S1148759837:		#B3q0		1148759837:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01		1:50:30		7.13		231.72

		S1148759867:		#B3q0		1148759867:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.04		4.01		4.01		4.01		4.03		4.03		4.01		1:51:00		7.16		232.81

		S1148759897:		#B3q0		1148759897:		$B3q0		d-		32.16		4.0		4.0		25		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01		1:51:30		7.20		233.88

		S1148759927:		#B3q0		1148759927:		$B3q0		d-		32.16		4.0		4.0		24.9		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01		1:52:00		7.23		234.96

		S1148759957:		#B3q0		1148759957:		$B3q0		d-		32.19		4.0		4.0		24.9		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01		1:52:30		7.26		236.03

		S1148759987:		#B3q0		1148759987:		$B3q0		d-		32.19		4.1		4.1		24.9		4.01		4.03		4.01		4.01		4.01		4.03		4.03		4.01		1:53:00		7.30		237.11

		S1148760017:		#B3q0		1148760017:		$B3q0		d-		32.19		4.1		4.1		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:53:30		7.33		238.21

		S1148760047:		#B3q0		1148760047:		$B3q0		d-		32.19		4.0		4.0		25.09		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:54:00		7.37		239.29

		S1148760077:		#B3q0		1148760077:		$B3q0		d-		32.12		4.0		4.0		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:54:30		7.40		240.36

		S1148760107:		#B3q0		1148760107:		$B3q0		d-		32.19		4.1		4.1		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:55:00		7.43		241.44

		S1148760137:		#B3q0		1148760137:		$B3q0		d-		32.16		4.0		4.0		25.09		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:55:30		7.47		242.53

		S1148760167:		#B3q0		1148760168:		$B3q0		d-		32.16		4.0		4.0		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:56:01		7.50		243.65

		S1148760197:		#B3q0		1148760197:		$B3q0		d-		32.16		4.1		4.1		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:56:30		7.53		244.69

		S1148760227:		#B3q0		1148760227:		$B3q0		d-		32.12		4.0		4.0		25		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:57:00		7.57		245.77

		S1148760257:		#B3q0		1148760257:		$B3q0		d-		32.16		4.0		4.0		25.09		4.01		4.03		4.01		4.00		4.01		4.03		4.03		4.01		1:57:31		7.60		246.89

		S1148760287:		#B3q0		1148760287:		$B3q0		d-		32.16		4.0		4.0		25		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		1:58:00		7.63		247.93

		S1148760317:		#B3q0		1148760317:		$B3q0		d-		32.16		4.0		4.0		25.09		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		1:58:30		7.67		249.01

		S1148760347:		#B3q0		1148760347:		$B3q0		d-		32.12		4.0		4.0		25		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		1:59:00		7.70		250.08

		S1148760377:		#B3q0		1148760377:		$B3q0		d-		32.12		4.0		4.0		25		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		1:59:30		7.74		251.16

		S1148760407:		#B3q0		1148760407:		$B3q0		d-		32.12		4.0		4.0		25.09		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		2:00:00		7.77		252.23

		S1148760437:		#B3q0		1148760437:		$B3q0		d-		32.16		4.1		4.1		25.09		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		2:00:30		7.80		253.32

		S1148760467:		#B3q0		1148760467:		$B3q0		d-		32.12		4.0		4.0		25.09		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.01		2:01:00		7.84		254.40

		S1148760497:		#B3q0		1148760497:		$B3q0		d-		32.16		4.0		4.0		25.09		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.00		2:01:30		7.87		255.48

		S1148760527:		#B3q0		1148760527:		$B3q0		d-		32.12		4.0		4.0		25		4.00		4.03		4.01		4.00		4.01		4.02		4.03		4.00		2:02:00		7.90		256.56

		S1148760557:		#B3q0		1148760558:		$B3q0		d-		32.12		4.0		4.0		25.09		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00		2:02:31		7.94		257.67

		S1148760587:		#B3q0		1148760587:		$B3q0		d-		32.12		4.0		4.0		25.19		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00		2:03:00		7.97		258.71

		S1148760617:		#B3q0		1148760617:		$B3q0		d-		32.12		4.1		4.1		25.09		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00		2:03:30		8.00		259.80

		S1148760647:		#B3q0		1148760647:		$B3q0		d-		32.12		4.0		4.0		25.19		4.00		4.03		4.01		4.00		4.00		4.02		4.02		4.00		2:04:00		8.04		260.88

		S1148760677:		#B3q0		1148760677:		$B3q0		d-		32.12		4.0		4.0		25.09		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00		2:04:30		8.07		261.96

		S1148760707:		#B3q0		1148760707:		$B3q0		d-		32.08		4.0		4.0		25.19		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00		2:05:00		8.10		263.04

		S1148760737:		#B3q0		1148760737:		$B3q0		d-		32.08		4.0		4.0		25.09		4.00		4.03		4.00		4.00		4.00		4.02		4.02		4.00		2:05:30		8.14		264.11

		S1148760767:		#B3q0		1148760767:		$B3q0		d-		32.08		4.0		4.0		25.09		4.00		4.03		4.00		3.99		4.00		4.02		4.02		4.00		2:06:00		8.17		265.19

		S1148760797:		#B3q0		1148760797:		$B3q0		d-		32.08		4.0		4.0		25.19		4.00		4.03		4.00		3.99		4.00		4.02		4.02		4.00		2:06:30		8.21		266.26

		S1148760827:		#B3q0		1148760827:		$B3q0		d-		32.08		4.0		4.0		25.09		4.00		4.02		4.00		3.99		4.00		4.02		4.02		4.00		2:07:01		8.24		267.37

		S1148760857:		#B3q0		1148760857:		$B3q0		d-		32.08		4.0		4.0		25.29		4.00		4.02		4.00		3.99		4.00		4.02		4.02		4.00		2:07:30		8.27		268.41

		S1148760887:		#B3q0		1148760887:		$B3q0		d-		32.04		4.0		4.0		25.09		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:08:00		8.31		269.49

		S1148760917:		#B3q0		1148760917:		$B3q0		d-		32.08		4.0		4.0		25.09		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:08:30		8.34		270.56

		S1148760947:		#B3q0		1148760947:		$B3q0		d-		32.04		4.0		4.0		25.19		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:09:00		8.37		271.64

		S1148760977:		#B3q0		1148760977:		$B3q0		d-		32.08		4.0		4.0		25.19		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:09:30		8.41		272.71

		S1148761007:		#B3q0		1148761007:		$B3q0		d-		32.04		4.1		4.1		25.19		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:10:00		8.44		273.79

		S1148761037:		#B3q0		1148761037:		$B3q0		d-		32.08		4.0		4.0		25.19		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:10:30		8.47		274.87

		S1148761067:		#B3q0		1148761067:		$B3q0		d-		32.08		4.0		4.0		25.29		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:11:00		8.51		275.94

		S1148761097:		#B3q0		1148761097:		$B3q0		d-		32.08		4.0		4.0		25.19		4.00		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:11:30		8.54		277.02

		S1148761127:		#B3q0		1148761127:		$B3q0		d-		32.04		4.0		4.0		25.29		3.99		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:12:01		8.58		278.13

		S1148761157:		#B3q0		1148761157:		$B3q0		d-		32.08		4.0		4.0		25.29		3.99		4.02		4.00		3.99		4.00		4.01		4.02		4.00		2:12:30		8.61		279.16

		S1148761187:		#B3q0		1148761187:		$B3q0		d-		32.04		4.0		4.0		25.29		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00		2:13:00		8.64		280.23

		S1148761217:		#B3q0		1148761217:		$B3q0		d-		32.04		4.0		4.0		25.19		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00		2:13:30		8.67		281.31

		S1148761247:		#B3q0		1148761247:		$B3q0		d-		32.04		4.0		4.0		25.19		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00		2:14:00		8.71		282.39

		S1148761277:		#B3q0		1148761277:		$B3q0		d-		32		4.0		4.0		25.19		3.99		4.02		4.00		3.99		4.00		4.01		4.01		4.00		2:14:30		8.74		283.46

		S1148761307:		#B3q0		1148761307:		$B3q0		d-		32.04		4.0		4.0		25.19		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99		2:15:00		8.78		284.54

		S1148761337:		#B3q0		1148761337:		$B3q0		d-		32.04		4.0		4.0		25.19		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99		2:15:31		8.81		285.65

		S1148761367:		#B3q0		1148761367:		$B3q0		d-		32.04		4.0		4.0		25.29		3.99		4.02		4.00		3.98		3.99		4.01		4.01		3.99		2:16:00		8.84		286.69

		S1148761397:		#B3q0		1148761397:		$B3q0		d-		32.04		4.0		4.0		25.29		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99		2:16:31		8.88		287.79

		S1148761427:		#B3q0		1148761427:		$B3q0		d-		32		4.1		4.1		25.39		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99		2:17:00		8.91		288.83

		S1148761457:		#B3q0		1148761457:		$B3q0		d-		32		4.1		4.1		25.29		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99		2:17:30		8.94		289.92

		S1148761487:		#B3q0		1148761487:		$B3q0		d-		32		4.0		4.0		25.29		3.99		4.01		4.00		3.98		3.99		4.01		4.01		3.99		2:18:00		8.98		291.00

		S1148761517:		#B3q0		1148761517:		$B3q0		d-		32		4.1		4.1		25.29		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:18:30		9.01		292.08

		S1148761547:		#B3q0		1148761547:		$B3q0		d-		32		4.0		4.0		25.29		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:19:00		9.04		293.16

		S1148761577:		#B3q0		1148761577:		$B3q0		d-		32		4.0		4.0		25.29		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:19:30		9.08		294.23

		S1148761607:		#B3q0		1148761607:		$B3q0		d-		32		4.1		4.1		25.29		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:20:00		9.11		295.31

		S1148761637:		#B3q0		1148761637:		$B3q0		d-		32		4.0		4.0		25.39		3.99		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:20:30		9.15		296.39

		S1148761667:		#B3q0		1148761667:		$B3q0		d-		31.97		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:21:00		9.18		297.46

		S1148761697:		#B3q0		1148761697:		$B3q0		d-		32		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:21:31		9.21		298.57

		S1148761727:		#B3q0		1148761727:		$B3q0		d-		31.97		4.1		4.1		25.29		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:22:01		9.25		299.64

		S1148761757:		#B3q0		1148761757:		$B3q0		d-		32		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.99		4.01		4.01		3.99		2:22:30		9.28		300.68

		S1148761787:		#B3q0		1148761787:		$B3q0		d-		31.97		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.99		4.00		4.01		3.99		2:23:00		9.31		301.74

		S1148761817:		#B3q0		1148761817:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:23:31		9.35		302.85

		S1148761847:		#B3q0		1148761847:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:24:00		9.38		303.89

		S1148761877:		#B3q0		1148761877:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:24:30		9.41		304.96

		S1148761907:		#B3q0		1148761907:		$B3q0		d-		32		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:25:00		9.45		306.03

		S1148761937:		#B3q0		1148761937:		$B3q0		d-		31.97		4.0		4.0		25.29		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:25:30		9.48		307.11

		S1148761967:		#B3q0		1148761967:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:26:00		9.51		308.18

		S1148761997:		#B3q0		1148761997:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:26:30		9.55		309.26

		S1148762027:		#B3q0		1148762027:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.01		3.98		2:27:00		9.58		310.33

		S1148762057:		#B3q0		1148762057:		$B3q0		d-		31.93		4.1		4.1		25.39		3.98		4.01		3.99		3.98		3.98		4.00		4.00		3.98		2:27:30		9.62		311.40

		S1148762087:		#B3q0		1148762087:		$B3q0		d-		31.97		4.0		4.0		25.48		3.98		4.01		3.98		3.98		3.98		4.00		4.00		3.98		2:28:00		9.65		312.48

		S1148762117:		#B3q0		1148762117:		$B3q0		d-		31.97		4.0		4.0		25.29		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:28:30		9.68		313.55

		S1148762147:		#B3q0		1148762147:		$B3q0		d-		31.97		4.0		4.0		25.39		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:29:00		9.72		314.62

		S1148762177:		#B3q0		1148762177:		$B3q0		d-		31.93		4.0		4.0		25.48		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:29:30		9.75		315.69

		S1148762207:		#B3q0		1148762207:		$B3q0		d-		31.93		4.0		4.0		25.39		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:30:00		9.78		316.77

		S1148762237:		#B3q0		1148762237:		$B3q0		d-		31.93		4.1		4.1		25.48		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:30:30		9.82		317.85

		S1148762267:		#B3q0		1148762267:		$B3q0		d-		31.93		4.0		4.0		25.48		3.98		4.01		3.98		3.97		3.98		4.00		4.00		3.98		2:31:00		9.85		318.92

		S1148762297:		#B3q0		1148762297:		$B3q0		d-		31.93		4.0		4.0		25.39		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:31:30		9.88		319.99

		S1148762327:		#B3q0		1148762327:		$B3q0		d-		31.93		4.0		4.0		25.48		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:32:00		9.92		321.07

		S1148762357:		#B3q0		1148762357:		$B3q0		d-		31.89		4.0		4.0		25.48		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:32:30		9.95		322.14

		S1148762387:		#B3q0		1148762387:		$B3q0		d-		31.93		4.0		4.0		25.39		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:33:01		9.99		323.25

		S1148762417:		#B3q0		1148762417:		$B3q0		d-		31.93		4.0		4.0		25.48		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:33:30		10.02		324.28

		S1148762447:		#B3q0		1148762447:		$B3q0		d-		31.93		4.0		4.0		25.48		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:34:00		10.05		325.34

		S1148762477:		#B3q0		1148762477:		$B3q0		d-		31.89		4.0		4.0		25.39		3.98		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:34:30		10.09		326.41

		S1148762507:		#B3q0		1148762507:		$B3q0		d-		31.93		4.0		4.0		25.48		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:35:00		10.12		327.48

		S1148762537:		#B3q0		1148762537:		$B3q0		d-		31.93		4.0		4.0		25.48		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:35:30		10.15		328.55

		S1148762567:		#B3q0		1148762567:		$B3q0		d-		31.89		4.0		4.0		25.39		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:36:00		10.19		329.62

		S1148762597:		#B3q0		1148762597:		$B3q0		d-		31.89		4.0		4.0		25.48		3.97		4.00		3.98		3.97		3.98		4.00		4.00		3.98		2:36:30		10.22		330.69

		S1148762627:		#B3q0		1148762627:		$B3q0		d-		31.89		4.0		4.0		25.39		3.97		4.00		3.98		3.97		3.97		4.00		4.00		3.98		2:37:01		10.25		331.79

		S1148762657:		#B3q0		1148762657:		$B3q0		d-		31.89		4.0		4.0		25.48		3.97		4.00		3.98		3.97		3.97		4.00		4.00		3.97		2:37:30		10.29		332.82

		S1148762687:		#B3q0		1148762687:		$B3q0		d-		31.89		4.0		4.0		25.48		3.97		4.00		3.98		3.96		3.97		4.00		4.00		3.97		2:38:01		10.32		333.93

		S1148762717:		#B3q0		1148762717:		$B3q0		d-		31.85		4.0		4.0		25.39		3.97		4.00		3.98		3.96		3.97		4.00		4.00		3.97		2:38:31		10.35		335.00

		S1148762747:		#B3q0		1148762747:		$B3q0		d-		31.85		4.0		4.0		25.48		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:39:01		10.39		336.06

		S1148762777:		#B3q0		1148762777:		$B3q0		d-		31.89		4.0		4.0		25.39		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:39:30		10.42		337.09

		S1148762807:		#B3q0		1148762807:		$B3q0		d-		31.85		4.0		4.0		25.48		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:40:01		10.45		338.19

		S1148762837:		#B3q0		1148762837:		$B3q0		d-		31.85		4.1		4.1		25.58		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:40:30		10.49		339.23

		S1148762867:		#B3q0		1148762867:		$B3q0		d-		31.82		4.0		4.0		25.48		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:41:00		10.52		340.31

		S1148762897:		#B3q0		1148762897:		$B3q0		d-		31.85		4.0		4.0		25.58		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:41:30		10.55		341.38

		S1148762927:		#B3q0		1148762927:		$B3q0		d-		31.82		4.0		4.0		25.58		3.97		4.00		3.98		3.96		3.97		3.99		4.00		3.97		2:42:01		10.59		342.48

		S1148762957:		#B3q0		1148762957:		$B3q0		d-		31.85		4.0		4.0		25.48		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:42:30		10.62		343.51

		S1148762987:		#B3q0		1148762987:		$B3q0		d-		31.85		4.0		4.0		25.48		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:43:00		10.65		344.57

		S1148763017:		#B3q0		1148763017:		$B3q0		d-		31.85		4.0		4.0		25.48		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:43:30		10.69		345.64

		S1148763047:		#B3q0		1148763047:		$B3q0		d-		31.85		4.1		4.1		25.48		3.97		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:44:00		10.72		346.71

		S1148763077:		#B3q0		1148763077:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:44:30		10.76		347.79

		S1148763107:		#B3q0		1148763107:		$B3q0		d-		31.82		4.1		4.1		25.58		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:45:00		10.79		348.87

		S1148763137:		#B3q0		1148763137:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:45:31		10.82		349.97

		S1148763167:		#B3q0		1148763167:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		4.00		3.97		3.96		3.97		3.99		3.99		3.97		2:46:01		10.86		351.04

		S1148763197:		#B3q0		1148763197:		$B3q0		d-		31.85		4.0		4.0		25.58		3.96		4.00		3.97		3.96		3.96		3.99		3.99		3.96		2:46:30		10.89		352.07

		S1148763227:		#B3q0		1148763227:		$B3q0		d-		31.85		4.0		4.0		25.58		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96		2:47:00		10.92		353.14

		S1148763257:		#B3q0		1148763257:		$B3q0		d-		31.82		4.0		4.0		25.48		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96		2:47:31		10.96		354.25

		S1148763287:		#B3q0		1148763287:		$B3q0		d-		31.82		4.0		4.0		25.48		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96		2:48:01		10.99		355.32

		S1148763317:		#B3q0		1148763317:		$B3q0		d-		31.82		4.0		4.0		25.68		3.96		3.99		3.97		3.96		3.96		3.99		3.99		3.96		2:48:30		11.02		356.35

		S1148763347:		#B3q0		1148763347:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:49:00		11.06		357.41

		S1148763377:		#B3q0		1148763377:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:49:30		11.09		358.49

		S1148763407:		#B3q0		1148763407:		$B3q0		d-		31.82		4.0		4.0		25.68		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:50:00		11.13		359.55

		S1148763437:		#B3q0		1148763437:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:50:31		11.16		360.64

		S1148763467:		#B3q0		1148763467:		$B3q0		d-		31.82		4.0		4.0		25.48		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:51:00		11.19		361.66

		S1148763497:		#B3q0		1148763497:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.97		3.96		3.96		3.98		3.99		3.96		2:51:30		11.23		362.72

		S1148763527:		#B3q0		1148763527:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.97		3.95		3.96		3.98		3.98		3.96		2:52:00		11.26		363.79

		S1148763557:		#B3q0		1148763557:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:52:30		11.29		364.85

		S1148763587:		#B3q0		1148763587:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:53:00		11.33		365.92

		S1148763617:		#B3q0		1148763617:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:53:30		11.36		366.98

		S1148763647:		#B3q0		1148763647:		$B3q0		d-		31.82		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:54:00		11.39		368.04

		S1148763677:		#B3q0		1148763677:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:54:31		11.43		369.14

		S1148763707:		#B3q0		1148763707:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:55:00		11.46		370.18

		S1148763737:		#B3q0		1148763737:		$B3q0		d-		31.78		4.0		4.0		25.68		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:55:30		11.49		371.24

		S1148763767:		#B3q0		1148763767:		$B3q0		d-		31.74		4.0		4.0		25.68		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:56:00		11.53		372.31

		S1148763797:		#B3q0		1148763797:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:56:31		11.56		373.41

		S1148763827:		#B3q0		1148763827:		$B3q0		d-		31.74		4.1		4.1		25.58		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:57:00		11.59		374.44

		S1148763857:		#B3q0		1148763857:		$B3q0		d-		31.78		4.0		4.0		25.68		3.96		3.99		3.96		3.95		3.96		3.98		3.98		3.96		2:57:30		11.63		375.51

		S1148763887:		#B3q0		1148763887:		$B3q0		d-		31.74		4.0		4.0		25.68		3.96		3.98		3.96		3.95		3.96		3.98		3.98		3.96		2:58:00		11.66		376.57

		S1148763917:		#B3q0		1148763917:		$B3q0		d-		31.78		4.0		4.0		25.58		3.96		3.98		3.96		3.95		3.96		3.98		3.98		3.96		2:58:30		11.69		377.64

		S1148763947:		#B3q0		1148763947:		$B3q0		d-		31.74		4.0		4.0		25.58		3.95		3.98		3.96		3.95		3.96		3.98		3.98		3.96		2:59:00		11.73		378.71

		S1148763977:		#B3q0		1148763977:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.95		3.96		3.98		3.98		3.96		2:59:30		11.76		379.78

		S1148764007:		#B3q0		1148764007:		$B3q0		d-		31.74		4.1		4.1		25.68		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.96		3:00:00		11.80		380.85

		S1148764037:		#B3q0		1148764037:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.96		3:00:30		11.83		381.92

		S1148764067:		#B3q0		1148764067:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.95		3:01:00		11.86		382.98

		S1148764097:		#B3q0		1148764097:		$B3q0		d-		31.74		4.0		4.0		25.58		3.95		3.98		3.96		3.95		3.95		3.98		3.98		3.95		3:01:30		11.90		384.04

		S1148764127:		#B3q0		1148764127:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:02:01		11.93		385.14

		S1148764157:		#B3q0		1148764157:		$B3q0		d-		31.7		4.1		4.1		25.58		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:02:31		11.97		386.21

		S1148764187:		#B3q0		1148764187:		$B3q0		d-		31.7		4.0		4.0		25.78		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:03:00		12.00		387.25

		S1148764217:		#B3q0		1148764217:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:03:30		12.03		388.31

		S1148764247:		#B3q0		1148764247:		$B3q0		d-		31.7		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:04:00		12.06		389.37

		S1148764277:		#B3q0		1148764277:		$B3q0		d-		31.7		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.98		3.98		3.95		3:04:30		12.10		390.42

		S1148764307:		#B3q0		1148764307:		$B3q0		d-		31.7		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95		3:05:00		12.13		391.49

		S1148764337:		#B3q0		1148764337:		$B3q0		d-		31.74		4.0		4.0		25.68		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95		3:05:30		12.16		392.55

		S1148764367:		#B3q0		1148764367:		$B3q0		d-		31.7		4.0		4.0		25.78		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95		3:06:00		12.20		393.61

		S1148764397:		#B3q0		1148764397:		$B3q0		d-		31.7		4.0		4.0		25.78		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95		3:06:30		12.23		394.67

		S1148764427:		#B3q0		1148764427:		$B3q0		d-		31.7		4.0		4.0		25.78		3.95		3.98		3.96		3.94		3.95		3.97		3.98		3.95		3:07:00		12.26		395.73

		S1148764457:		#B3q0		1148764457:		$B3q0		d-		31.7		4.0		4.0		25.78		3.95		3.98		3.96		3.94		3.95		3.97		3.97		3.95		3:07:30		12.30		396.79

		S1148764487:		#B3q0		1148764487:		$B3q0		d-		31.66		4.0		4.0		25.78		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95		3:08:00		12.33		397.86

		S1148764517:		#B3q0		1148764517:		$B3q0		d-		31.7		4.0		4.0		25.68		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95		3:08:30		12.37		398.92

		S1148764547:		#B3q0		1148764547:		$B3q0		d-		31.66		4.0		4.0		25.68		3.95		3.98		3.95		3.94		3.95		3.97		3.97		3.95		3:09:01		12.40		400.02

		S1148764577:		#B3q0		1148764577:		$B3q0		d-		31.7		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.95		3:09:30		12.43		401.05

		S1148764607:		#B3q0		1148764607:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.95		3:10:00		12.47		402.11

		S1148764637:		#B3q0		1148764637:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:10:30		12.50		403.17

		S1148764667:		#B3q0		1148764667:		$B3q0		d-		31.7		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:11:00		12.53		404.23

		S1148764697:		#B3q0		1148764697:		$B3q0		d-		31.66		4.0		4.0		25.68		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:11:30		12.57		405.29

		S1148764727:		#B3q0		1148764727:		$B3q0		d-		31.66		4.1		4.1		25.68		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:12:01		12.60		406.40

		S1148764757:		#B3q0		1148764757:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:12:30		12.63		407.43

		S1148764787:		#B3q0		1148764787:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.98		3.95		3.94		3.94		3.97		3.97		3.94		3:13:00		12.67		408.50

		S1148764817:		#B3q0		1148764817:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94		3:13:30		12.70		409.57

		S1148764847:		#B3q0		1148764847:		$B3q0		d-		31.66		4.0		4.0		25.78		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94		3:14:01		12.74		410.66

		S1148764877:		#B3q0		1148764877:		$B3q0		d-		31.66		4.0		4.0		25.87		3.94		3.97		3.95		3.94		3.94		3.97		3.97		3.94		3:14:30		12.77		411.68

		S1148764907:		#B3q0		1148764907:		$B3q0		d-		31.66		4.0		4.0		25.68		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94		3:15:00		12.80		412.74

		S1148764937:		#B3q0		1148764937:		$B3q0		d-		31.62		4.0		4.0		25.78		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94		3:15:30		12.84		413.79

		S1148764967:		#B3q0		1148764967:		$B3q0		d-		31.62		4.0		4.0		25.87		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94		3:16:00		12.87		414.85

		S1148764997:		#B3q0		1148764997:		$B3q0		d-		31.62		4.0		4.0		25.78		3.94		3.97		3.95		3.94		3.94		3.96		3.97		3.94		3:16:30		12.90		415.92

		S1148765027:		#B3q0		1148765027:		$B3q0		d-		31.62		4.1		4.1		25.78		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94		3:17:00		12.94		416.99

		S1148765057:		#B3q0		1148765057:		$B3q0		d-		31.62		4.0		4.0		25.78		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94		3:17:30		12.97		418.05

		S1148765087:		#B3q0		1148765087:		$B3q0		d-		31.62		4.0		4.0		25.78		3.94		3.97		3.95		3.93		3.94		3.96		3.97		3.94		3:18:00		13.00		419.11

		S1148765117:		#B3q0		1148765117:		$B3q0		d-		31.62		4.1		4.1		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:18:30		13.04		420.18

		S1148765147:		#B3q0		1148765147:		$B3q0		d-		31.62		4.1		4.1		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:19:01		13.07		421.29

		S1148765177:		#B3q0		1148765177:		$B3q0		d-		31.62		4.0		4.0		25.87		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:19:30		13.10		422.32

		S1148765207:		#B3q0		1148765207:		$B3q0		d-		31.62		4.0		4.0		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:20:00		13.14		423.38

		S1148765237:		#B3q0		1148765237:		$B3q0		d-		31.59		4.1		4.1		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:20:31		13.17		424.48

		S1148765267:		#B3q0		1148765267:		$B3q0		d-		31.59		4.0		4.0		25.87		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:21:00		13.21		425.51

		S1148765297:		#B3q0		1148765297:		$B3q0		d-		31.62		4.0		4.0		25.87		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:21:31		13.24		426.61

		S1148765327:		#B3q0		1148765327:		$B3q0		d-		31.59		4.0		4.0		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:22:01		13.27		427.66

		S1148765357:		#B3q0		1148765357:		$B3q0		d-		31.59		4.0		4.0		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:22:31		13.31		428.72

		S1148765387:		#B3q0		1148765387:		$B3q0		d-		31.59		4.0		4.0		25.78		3.94		3.96		3.94		3.93		3.94		3.96		3.96		3.94		3:23:01		13.34		429.79

		S1148765417:		#B3q0		1148765417:		$B3q0		d-		31.59		4.0		4.0		25.78		3.94		3.97		3.94		3.93		3.94		3.96		3.96		3.94		3:23:30		13.37		430.81

		S1148765447:		#B3q0		1148765447:		$B3q0		d-		31.59		4.1		4.1		25.87		3.94		3.96		3.94		3.93		3.93		3.96		3.96		3.94		3:24:00		13.41		431.87

		S1148768612:		#B3q0		1148768612:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89		4:16:45		16.96		544.08

		S1148768641:		#B3q0		1148768641:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89		4:17:14		16.99		545.09

		S1148768671:		#B3q0		1148768671:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89		4:17:45		17.03		546.18

		S1148768701:		#B3q0		1148768701:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.93		3.91		3.89		3.89		3.92		3.92		3.89		4:18:14		17.06		547.19

		S1148768731:		#B3q0		1148768731:		$B3q0		d-		31.28		4.0		4.0		26.26		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89		4:18:45		17.09		548.28

		S1148768761:		#B3q0		1148768761:		$B3q0		d-		31.28		4.0		4.0		26.26		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89		4:19:15		17.13		549.33

		S1148768791:		#B3q0		1148768791:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89		4:19:45		17.16		550.38

		S1148768821:		#B3q0		1148768821:		$B3q0		d-		31.28		4.1		4.1		26.17		3.89		3.93		3.90		3.89		3.89		3.92		3.92		3.89		4:20:15		17.19		551.43

		S1148768851:		#B3q0		1148768851:		$B3q0		d-		31.25		4.0		4.0		26.26		3.89		3.92		3.90		3.89		3.89		3.92		3.92		3.89		4:20:44		17.23		552.46

		S1148768881:		#B3q0		1148768881:		$B3q0		d-		31.25		4.0		4.0		26.07		3.89		3.92		3.90		3.89		3.89		3.92		3.92		3.89		4:21:15		17.26		553.54

		S1148768911:		#B3q0		1148768911:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:21:45		17.30		554.60

		S1148768941:		#B3q0		1148768942:		$B3q0		d-		31.25		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:22:15		17.33		555.65

		S1148768971:		#B3q0		1148768971:		$B3q0		d-		31.25		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:22:45		17.36		556.70

		S1148769001:		#B3q0		1148769001:		$B3q0		d-		31.28		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:23:15		17.40		557.75

		S1148769031:		#B3q0		1148769031:		$B3q0		d-		31.25		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:23:44		17.43		558.76

		S1148769061:		#B3q0		1148769061:		$B3q0		d-		31.25		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:24:15		17.46		559.85

		S1148769091:		#B3q0		1148769091:		$B3q0		d-		31.25		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:24:44		17.50		560.86

		S1148769121:		#B3q0		1148769121:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:25:15		17.53		561.94

		S1148769151:		#B3q0		1148769151:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:25:44		17.56		562.96

		S1148769181:		#B3q0		1148769181:		$B3q0		d-		31.21		4.0		4.0		26.17		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:26:14		17.60		564.00

		S1148769211:		#B3q0		1148769211:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:26:45		17.63		565.08

		S1148769241:		#B3q0		1148769241:		$B3q0		d-		31.25		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:27:15		17.67		566.13

		S1148769271:		#B3q0		1148769271:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:27:45		17.70		567.18

		S1148769301:		#B3q0		1148769301:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:28:15		17.73		568.24

		S1148769331:		#B3q0		1148769331:		$B3q0		d-		31.21		4.1		4.1		26.26		3.89		3.92		3.90		3.88		3.89		3.92		3.92		3.89		4:28:44		17.77		569.26

		S1148769361:		#B3q0		1148769361:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.89		3.88		3.89		3.91		3.92		3.89		4:29:15		17.80		570.34

		S1148769391:		#B3q0		1148769391:		$B3q0		d-		31.21		4.0		4.0		26.17		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.89		4:29:45		17.83		571.38

		S1148769421:		#B3q0		1148769421:		$B3q0		d-		31.21		4.1		4.1		26.26		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.89		4:30:15		17.87		572.43

		S1148769451:		#B3q0		1148769451:		$B3q0		d-		31.21		4.0		4.0		26.26		3.89		3.92		3.89		3.88		3.88		3.91		3.92		3.88		4:30:44		17.90		573.45

		S1148769481:		#B3q0		1148769481:		$B3q0		d-		31.21		4.0		4.0		26.26		3.88		3.92		3.89		3.88		3.88		3.91		3.92		3.88		4:31:15		17.93		574.52

		S1148769511:		#B3q0		1148769511:		$B3q0		d-		31.21		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.92		3.88		4:31:45		17.97		575.56

		S1148769541:		#B3q0		1148769541:		$B3q0		d-		31.21		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:32:15		18.00		576.61

		S1148769571:		#B3q0		1148769571:		$B3q0		d-		31.17		4.0		4.0		26.17		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:32:44		18.03		577.62

		S1148769601:		#B3q0		1148769601:		$B3q0		d-		31.17		4.1		4.1		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:33:15		18.07		578.71

		S1148769631:		#B3q0		1148769631:		$B3q0		d-		31.21		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:33:45		18.10		579.77

		S1148769661:		#B3q0		1148769661:		$B3q0		d-		31.21		4.0		4.0		26.17		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:34:15		18.14		580.82

		S1148769691:		#B3q0		1148769691:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:34:45		18.17		581.86

		S1148769721:		#B3q0		1148769721:		$B3q0		d-		31.21		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:35:14		18.20		582.86

		S1148769751:		#B3q0		1148769751:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:35:44		18.23		583.91

		S1148769781:		#B3q0		1148769781:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:36:15		18.27		584.99

		S1148769811:		#B3q0		1148769811:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:36:44		18.30		586.00

		S1148769841:		#B3q0		1148769841:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:37:14		18.34		587.05

		S1148769871:		#B3q0		1148769871:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:37:45		18.37		588.13

		S1148769901:		#B3q0		1148769901:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:38:14		18.40		589.14

		S1148769931:		#B3q0		1148769931:		$B3q0		d-		31.13		4.0		4.0		26.26		3.88		3.92		3.89		3.87		3.88		3.91		3.91		3.88		4:38:45		18.44		590.22

		S1148769961:		#B3q0		1148769961:		$B3q0		d-		31.13		4.0		4.0		26.17		3.88		3.92		3.89		3.87		3.87		3.91		3.91		3.88		4:39:15		18.47		591.27

		S1148769991:		#B3q0		1148769991:		$B3q0		d-		31.13		4.0		4.0		26.26		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.88		4:39:44		18.50		592.29

		S1148770021:		#B3q0		1148770021:		$B3q0		d-		31.13		4.0		4.0		26.26		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:40:14		18.54		593.33

		S1148770051:		#B3q0		1148770051:		$B3q0		d-		31.17		4.0		4.0		26.26		3.88		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:40:45		18.57		594.41

		S1148770081:		#B3q0		1148770081:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:41:15		18.61		595.46

		S1148770111:		#B3q0		1148770111:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:41:45		18.64		596.50

		S1148770141:		#B3q0		1148770141:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:42:15		18.67		597.55

		S1148770171:		#B3q0		1148770171:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:42:45		18.71		598.60

		S1148770201:		#B3q0		1148770201:		$B3q0		d-		31.13		4.1		4.1		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:43:14		18.74		599.62

		S1148770231:		#B3q0		1148770231:		$B3q0		d-		31.13		4.0		4.0		26.17		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:43:45		18.77		600.70

		S1148770261:		#B3q0		1148770261:		$B3q0		d-		31.09		4.0		4.0		26.36		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:44:15		18.81		601.74

		S1148770291:		#B3q0		1148770291:		$B3q0		d-		31.13		4.1		4.1		26.26		3.87		3.91		3.89		3.87		3.87		3.91		3.91		3.87		4:44:45		18.84		602.80

		S1148770321:		#B3q0		1148770321:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.88		3.87		3.87		3.91		3.91		3.87		4:45:14		18.87		603.81

		S1148770351:		#B3q0		1148770351:		$B3q0		d-		31.09		4.1		4.1		26.26		3.87		3.91		3.88		3.87		3.87		3.91		3.91		3.87		4:45:45		18.91		604.90

		S1148770381:		#B3q0		1148770381:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.87		3.87		3.90		3.91		3.87		4:46:15		18.94		605.95

		S1148770411:		#B3q0		1148770411:		$B3q0		d-		31.09		4.1		4.1		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:46:45		18.98		607.01

		S1148770441:		#B3q0		1148770441:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:47:15		19.01		608.06

		S1148770471:		#B3q0		1148770471:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:47:45		19.04		609.10

		S1148770501:		#B3q0		1148770501:		$B3q0		d-		31.13		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:48:14		19.08		610.11

		S1148770531:		#B3q0		1148770531:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:48:45		19.11		611.18

		S1148770561:		#B3q0		1148770561:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:49:15		19.14		612.21

		S1148770591:		#B3q0		1148770591:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.91		3.87		4:49:45		19.18		613.25

		S1148770621:		#B3q0		1148770621:		$B3q0		d-		31.09		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:50:15		19.21		614.29

		S1148770651:		#B3q0		1148770651:		$B3q0		d-		31.09		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:50:45		19.24		615.33

		S1148770681:		#B3q0		1148770681:		$B3q0		d-		31.06		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:51:15		19.28		616.38

		S1148770711:		#B3q0		1148770711:		$B3q0		d-		31.09		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:51:45		19.31		617.43

		S1148770741:		#B3q0		1148770741:		$B3q0		d-		31.06		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:52:15		19.35		618.47

		S1148770771:		#B3q0		1148770771:		$B3q0		d-		31.09		4.0		4.0		26.36		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:52:45		19.38		619.51

		S1148770801:		#B3q0		1148770801:		$B3q0		d-		31.09		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:53:15		19.41		620.55

		S1148770831:		#B3q0		1148770831:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.87		3.90		3.90		3.87		4:53:44		19.44		621.56

		S1148770861:		#B3q0		1148770861:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.87		4:54:14		19.48		622.60

		S1148770891:		#B3q0		1148770891:		$B3q0		d-		31.06		4.1		4.1		26.26		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.86		4:54:45		19.51		623.68

		S1148770921:		#B3q0		1148770921:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.91		3.88		3.86		3.86		3.90		3.90		3.86		4:55:15		19.55		624.73

		S1148770951:		#B3q0		1148770951:		$B3q0		d-		31.06		4.0		4.0		26.36		3.87		3.91		3.87		3.86		3.86		3.90		3.90		3.86		4:55:45		19.58		625.77

		S1148770981:		#B3q0		1148770981:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.91		3.87		3.86		3.86		3.90		3.90		3.86		4:56:15		19.61		626.81

		S1148771011:		#B3q0		1148771011:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.90		3.87		3.86		3.86		3.90		3.90		3.86		4:56:45		19.65		627.85

		S1148771041:		#B3q0		1148771041:		$B3q0		d-		31.06		4.0		4.0		26.26		3.87		3.90		3.87		3.86		3.86		3.89		3.90		3.86		4:57:15		19.68		628.90

		S1148771071:		#B3q0		1148771071:		$B3q0		d-		31.06		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		4:57:45		19.71		629.94

		S1148771101:		#B3q0		1148771101:		$B3q0		d-		31.06		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		4:58:15		19.75		630.98

		S1148771131:		#B3q0		1148771131:		$B3q0		d-		31.02		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		4:58:45		19.78		632.02

		S1148771161:		#B3q0		1148771161:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		4:59:15		19.81		633.05

		S1148771191:		#B3q0		1148771191:		$B3q0		d-		31.06		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		4:59:45		19.85		634.09

		S1148771221:		#B3q0		1148771221:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		5:00:15		19.88		635.14

		S1148771251:		#B3q0		1148771251:		$B3q0		d-		31.02		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.86		3.89		3.90		3.86		5:00:45		19.92		636.18

		S1148771281:		#B3q0		1148771281:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:01:15		19.95		637.23

		S1148771311:		#B3q0		1148771311:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:01:44		19.98		638.23

		S1148771341:		#B3q0		1148771341:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:02:15		20.02		639.30

		S1148771371:		#B3q0		1148771371:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:02:45		20.05		640.34

		S1148771401:		#B3q0		1148771401:		$B3q0		d-		30.98		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:03:15		20.08		641.38

		S1148771431:		#B3q0		1148771431:		$B3q0		d-		30.98		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:03:45		20.12		642.42

		S1148771461:		#B3q0		1148771461:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.86		3.89		3.89		3.86		5:04:14		20.15		643.42

		S1148771491:		#B3q0		1148771491:		$B3q0		d-		31.02		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.86		5:04:45		20.18		644.49

		S1148771521:		#B3q0		1148771521:		$B3q0		d-		31.02		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:05:15		20.22		645.52

		S1148771551:		#B3q0		1148771551:		$B3q0		d-		30.98		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:05:45		20.25		646.56

		S1148771581:		#B3q0		1148771581:		$B3q0		d-		30.98		4.0		4.0		26.26		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:06:15		20.28		647.60

		S1148771611:		#B3q0		1148771611:		$B3q0		d-		30.98		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:06:45		20.32		648.64

		S1148771641:		#B3q0		1148771641:		$B3q0		d-		31.02		4.1		4.1		26.36		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:07:15		20.35		649.69

		S1148771671:		#B3q0		1148771671:		$B3q0		d-		30.98		4.0		4.0		26.36		3.86		3.90		3.87		3.85		3.85		3.89		3.89		3.85		5:07:45		20.38		650.73

		S1148771701:		#B3q0		1148771701:		$B3q0		d-		30.98		4.0		4.0		26.26		3.86		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:08:15		20.42		651.77

		S1148771731:		#B3q0		1148771731:		$B3q0		d-		30.98		4.0		4.0		26.36		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:08:44		20.45		652.78

		S1148771761:		#B3q0		1148771761:		$B3q0		d-		30.98		4.1		4.1		26.26		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:09:15		20.49		653.86

		S1148771791:		#B3q0		1148771791:		$B3q0		d-		30.98		4.0		4.0		26.36		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:09:45		20.52		654.90

		S1148771821:		#B3q0		1148771821:		$B3q0		d-		30.98		4.0		4.0		26.36		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:10:15		20.55		655.94

		S1148771851:		#B3q0		1148771851:		$B3q0		d-		30.98		4.0		4.0		26.26		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:10:45		20.59		656.98

		S1148771881:		#B3q0		1148771881:		$B3q0		d-		30.98		4.1		4.1		26.36		3.85		3.89		3.87		3.85		3.85		3.89		3.89		3.85		5:11:15		20.62		658.03

		S1148771911:		#B3q0		1148771911:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85		5:11:45		20.65		659.08

		S1148771941:		#B3q0		1148771941:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85		5:12:15		20.69		660.11

		S1148771971:		#B3q0		1148771971:		$B3q0		d-		30.91		4.0		4.0		26.26		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85		5:12:45		20.72		661.15

		S1148772001:		#B3q0		1148772001:		$B3q0		d-		30.94		4.0		4.0		26.36		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85		5:13:15		20.75		662.18

		S1148772031:		#B3q0		1148772031:		$B3q0		d-		30.94		4.0		4.0		26.36		3.85		3.89		3.86		3.85		3.85		3.89		3.89		3.85		5:13:45		20.79		663.22

		S1148772061:		#B3q0		1148772061:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:14:15		20.82		664.26

		S1148772091:		#B3q0		1148772091:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:14:45		20.86		665.29

		S1148772121:		#B3q0		1148772121:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:15:15		20.89		666.32

		S1148772151:		#B3q0		1148772151:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:15:45		20.92		667.36

		S1148772181:		#B3q0		1148772181:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:16:15		20.96		668.40

		S1148772211:		#B3q0		1148772211:		$B3q0		d-		30.94		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:16:45		20.99		669.44

		S1148772241:		#B3q0		1148772241:		$B3q0		d-		30.94		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:17:15		21.02		670.48

		S1148772271:		#B3q0		1148772271:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.89		3.85		5:17:45		21.06		671.52

		S1148772301:		#B3q0		1148772301:		$B3q0		d-		30.94		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85		5:18:15		21.09		672.56

		S1148772331:		#B3q0		1148772331:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85		5:18:45		21.12		673.60

		S1148772361:		#B3q0		1148772361:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85		5:19:15		21.16		674.65

		S1148772391:		#B3q0		1148772391:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85		5:19:44		21.19		675.65

		S1148772421:		#B3q0		1148772421:		$B3q0		d-		30.94		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.85		3.88		3.88		3.85		5:20:15		21.23		676.73

		S1148772451:		#B3q0		1148772451:		$B3q0		d-		30.91		4.0		4.0		26.26		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.85		5:20:45		21.26		677.77

		S1148772481:		#B3q0		1148772481:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.85		5:21:15		21.29		678.81

		S1148772511:		#B3q0		1148772511:		$B3q0		d-		30.91		4.1		4.1		26.36		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84		5:21:45		21.33		679.85

		S1148772541:		#B3q0		1148772541:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84		5:22:15		21.36		680.89

		S1148772571:		#B3q0		1148772571:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.86		3.84		3.84		3.88		3.88		3.84		5:22:45		21.39		681.93

		S1148772601:		#B3q0		1148772601:		$B3q0		d-		30.91		4.0		4.0		26.26		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84		5:23:15		21.43		682.97

		S1148772631:		#B3q0		1148772631:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84		5:23:45		21.46		684.01

		S1148772661:		#B3q0		1148772661:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.89		3.85		3.84		3.84		3.88		3.88		3.84		5:24:15		21.49		685.04

		S1148772691:		#B3q0		1148772691:		$B3q0		d-		30.91		4.0		4.0		26.36		3.85		3.88		3.85		3.84		3.84		3.87		3.88		3.84		5:24:45		21.53		686.08

		S1148772721:		#B3q0		1148772721:		$B3q0		d-		30.87		4.0		4.0		26.36		3.85		3.88		3.85		3.84		3.84		3.87		3.88		3.84		5:25:15		21.56		687.12

		S1148772751:		#B3q0		1148772751:		$B3q0		d-		30.87		4.0		4.0		26.46		3.84		3.88		3.85		3.84		3.84		3.87		3.88		3.84		5:25:45		21.60		688.16

		S1148772781:		#B3q0		1148772781:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84		5:26:15		21.63		689.20

		S1148772811:		#B3q0		1148772811:		$B3q0		d-		30.87		4.1		4.1		26.46		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84		5:26:45		21.66		690.25

		S1148772841:		#B3q0		1148772841:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84		5:27:15		21.70		691.29

		S1148772871:		#B3q0		1148772871:		$B3q0		d-		30.91		4.1		4.1		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84		5:27:45		21.73		692.34

		S1148772901:		#B3q0		1148772901:		$B3q0		d-		30.87		4.0		4.0		26.46		3.84		3.88		3.85		3.83		3.84		3.87		3.88		3.84		5:28:15		21.76		693.38

		S1148772931:		#B3q0		1148772931:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:28:45		21.80		694.42

		S1148772961:		#B3q0		1148772961:		$B3q0		d-		30.87		4.0		4.0		26.46		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:29:15		21.83		695.46

		S1148772991:		#B3q0		1148772991:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:29:44		21.86		696.46

		S1148773021:		#B3q0		1148773021:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:30:15		21.90		697.52

		S1148773051:		#B3q0		1148773051:		$B3q0		d-		30.87		4.0		4.0		26.46		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:30:45		21.93		698.55

		S1148773081:		#B3q0		1148773081:		$B3q0		d-		30.87		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:31:15		21.96		699.58

		S1148773111:		#B3q0		1148773111:		$B3q0		d-		30.83		4.0		4.0		26.26		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:31:45		22.00		700.61

		S1148773141:		#B3q0		1148773141:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:32:20		22.04		701.82

		S1148773171:		#B3q0		1148773171:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.84		3.87		3.87		3.84		5:32:50		22.07		702.85

		S1148773201:		#B3q0		1148773201:		$B3q0		d-		30.83		4.1		4.1		26.36		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83		5:33:20		22.11		703.90

		S1148773231:		#B3q0		1148773231:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83		5:33:50		22.14		704.94

		S1148773261:		#B3q0		1148773261:		$B3q0		d-		30.87		4.0		4.0		26.46		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83		5:34:20		22.17		705.98

		S1148773291:		#B3q0		1148773291:		$B3q0		d-		30.83		4.0		4.0		26.26		3.84		3.88		3.85		3.83		3.83		3.87		3.87		3.83		5:34:50		22.21		707.02

		S1148773321:		#B3q0		1148773321:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:35:20		22.24		708.05

		S1148773351:		#B3q0		1148773351:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:35:50		22.27		709.09

		S1148773381:		#B3q0		1148773381:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:36:20		22.31		710.12

		S1148773411:		#B3q0		1148773411:		$B3q0		d-		30.83		4.0		4.0		26.46		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:36:50		22.34		711.16

		S1148773441:		#B3q0		1148773441:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:37:20		22.37		712.20

		S1148773471:		#B3q0		1148773471:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:37:50		22.41		713.23

		S1148773501:		#B3q0		1148773501:		$B3q0		d-		30.83		4.0		4.0		26.36		3.84		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:38:20		22.44		714.26

		S1148773531:		#B3q0		1148773531:		$B3q0		d-		30.83		4.0		4.0		26.46		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:38:50		22.47		715.29

		S1148773561:		#B3q0		1148773561:		$B3q0		d-		30.83		4.0		4.0		26.36		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:39:20		22.51		716.32

		S1148773591:		#B3q0		1148773591:		$B3q0		d-		30.83		4.0		4.0		26.46		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:39:50		22.54		717.35

		S1148773621:		#B3q0		1148773621:		$B3q0		d-		30.79		4.1		4.1		26.46		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:40:20		22.58		718.40

		S1148773651:		#B3q0		1148773651:		$B3q0		d-		30.79		4.0		4.0		26.46		3.83		3.87		3.85		3.83		3.83		3.87		3.87		3.83		5:40:50		22.61		719.43

		S1148773681:		#B3q0		1148773681:		$B3q0		d-		30.79		4.0		4.0		26.46		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:41:20		22.64		720.47

		S1148773711:		#B3q0		1148773711:		$B3q0		d-		30.79		4.0		4.0		26.46		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:41:50		22.68		721.50

		S1148773741:		#B3q0		1148773741:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:42:20		22.71		722.54

		S1148773771:		#B3q0		1148773771:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:42:50		22.74		723.58

		S1148773801:		#B3q0		1148773801:		$B3q0		d-		30.83		4.1		4.1		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:43:20		22.78		724.62

		S1148773831:		#B3q0		1148773831:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:43:50		22.81		725.66

		S1148773861:		#B3q0		1148773861:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:44:20		22.84		726.70

		S1148773891:		#B3q0		1148773891:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:44:50		22.88		727.73

		S1148773921:		#B3q0		1148773921:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.83		3.83		3.86		3.87		3.83		5:45:20		22.91		728.75

		S1148773951:		#B3q0		1148773951:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:45:50		22.95		729.78

		S1148773981:		#B3q0		1148773981:		$B3q0		d-		30.79		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:46:20		22.98		730.82

		S1148774011:		#B3q0		1148774011:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:46:50		23.01		731.86

		S1148774041:		#B3q0		1148774041:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:47:15		23.04		732.72

		S1148774071:		#B3q0		1148774071:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:47:45		23.07		733.74

		S1148774101:		#B3q0		1148774101:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:48:15		23.11		734.77

		S1148774131:		#B3q0		1148774131:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:48:45		23.14		735.80

		S1148774161:		#B3q0		1148774161:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:49:14		23.17		736.80

		S1148774191:		#B3q0		1148774191:		$B3q0		d-		30.79		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:49:44		23.21		737.84

		S1148774221:		#B3q0		1148774221:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:50:15		23.24		738.90

		S1148774251:		#B3q0		1148774251:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:50:45		23.27		739.93

		S1148774281:		#B3q0		1148774281:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.83		3.86		3.86		3.83		5:51:15		23.31		740.97

		S1148774311:		#B3q0		1148774311:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.87		3.84		3.82		3.82		3.86		3.86		3.83		5:51:45		23.34		742.00

		S1148774341:		#B3q0		1148774341:		$B3q0		d-		30.79		4.0		4.0		26.36		3.83		3.86		3.84		3.82		3.82		3.86		3.86		3.83		5:52:15		23.38		743.03

		S1148774371:		#B3q0		1148774371:		$B3q0		d-		30.75		4.1		4.1		26.46		3.83		3.86		3.84		3.82		3.82		3.86		3.86		3.83		5:52:45		23.41		744.07

		S1148774401:		#B3q0		1148774401:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.86		3.84		3.82		3.82		3.85		3.86		3.82		5:53:15		23.44		745.10

		S1148774431:		#B3q0		1148774431:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.86		3.84		3.82		3.82		3.85		3.86		3.82		5:53:45		23.48		746.13

		S1148774461:		#B3q0		1148774461:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:54:15		23.51		747.17

		S1148774491:		#B3q0		1148774491:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:54:45		23.54		748.20

		S1148774521:		#B3q0		1148774521:		$B3q0		d-		30.75		4.0		4.0		26.36		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:55:15		23.58		749.24

		S1148774551:		#B3q0		1148774551:		$B3q0		d-		30.71		4.0		4.0		26.36		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:55:45		23.61		750.27

		S1148774581:		#B3q0		1148774581:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:56:15		23.64		751.31

		S1148774611:		#B3q0		1148774611:		$B3q0		d-		30.71		4.1		4.1		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:56:45		23.68		752.35

		S1148774641:		#B3q0		1148774641:		$B3q0		d-		30.75		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:57:15		23.71		753.38

		S1148774671:		#B3q0		1148774671:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.86		3.82		5:57:45		23.75		754.40

		S1148774701:		#B3q0		1148774701:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82		5:58:15		23.78		755.43

		S1148774731:		#B3q0		1148774731:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82		5:58:45		23.81		756.46

		S1148774761:		#B3q0		1148774761:		$B3q0		d-		30.71		4.0		4.0		26.46		3.83		3.86		3.83		3.82		3.82		3.85		3.85		3.82		5:59:15		23.85		757.49

		S1148774791:		#B3q0		1148774791:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		5:59:45		23.88		758.51

		S1148774821:		#B3q0		1148774821:		$B3q0		d-		30.71		4.0		4.0		26.36		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:00:15		23.91		759.55

		S1148774851:		#B3q0		1148774851:		$B3q0		d-		30.71		4.0		4.0		26.36		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:00:45		23.95		760.58

		S1148774881:		#B3q0		1148774881:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:01:15		23.98		761.61

		S1148774911:		#B3q0		1148774911:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:01:45		24.01		762.64

		S1148774941:		#B3q0		1148774941:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:02:15		24.05		763.67

		S1148774971:		#B3q0		1148774971:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:02:45		24.08		764.70

		S1148775001:		#B3q0		1148775001:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:03:15		24.11		765.73

		S1148775031:		#B3q0		1148775031:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.86		3.83		3.82		3.82		3.85		3.85		3.82		6:03:45		24.15		766.75

		S1148775061:		#B3q0		1148775061:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:04:15		24.18		767.78

		S1148775091:		#B3q0		1148775091:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:04:45		24.21		768.81

		S1148775121:		#B3q0		1148775121:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:05:15		24.25		769.84

		S1148775151:		#B3q0		1148775151:		$B3q0		d-		30.71		4.0		4.0		26.46		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:05:45		24.28		770.86

		S1148775181:		#B3q0		1148775181:		$B3q0		d-		30.68		4.0		4.0		26.36		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:06:15		24.32		771.89

		S1148775211:		#B3q0		1148775211:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.82		3.82		3.85		3.85		3.82		6:06:45		24.35		772.92

		S1148775241:		#B3q0		1148775241:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:07:15		24.38		773.95

		S1148775271:		#B3q0		1148775271:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:07:45		24.42		774.98

		S1148775301:		#B3q0		1148775301:		$B3q0		d-		30.68		4.0		4.0		26.36		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:08:15		24.45		776.01

		S1148775331:		#B3q0		1148775331:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:08:45		24.48		777.04

		S1148775361:		#B3q0		1148775361:		$B3q0		d-		30.68		4.0		4.0		26.36		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:09:15		24.52		778.08

		S1148775391:		#B3q0		1148775391:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:09:45		24.55		779.10

		S1148775421:		#B3q0		1148775421:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:10:15		24.58		780.13

		S1148775451:		#B3q0		1148775451:		$B3q0		d-		30.64		4.1		4.1		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:10:45		24.62		781.16

		S1148775481:		#B3q0		1148775481:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:11:15		24.65		782.19

		S1148775511:		#B3q0		1148775511:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.85		3.85		3.82		6:11:45		24.68		783.22

		S1148775541:		#B3q0		1148775541:		$B3q0		d-		30.68		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.84		3.85		3.82		6:12:15		24.72		784.24

		S1148775571:		#B3q0		1148775571:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.82		3.84		3.85		3.82		6:12:45		24.75		785.26

		S1148775601:		#B3q0		1148775601:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.82		6:13:15		24.78		786.29

		S1148775631:		#B3q0		1148775631:		$B3q0		d-		30.68		4.0		4.0		26.36		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.82		6:13:45		24.82		787.32

		S1148775661:		#B3q0		1148775661:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81		6:14:15		24.85		788.34

		S1148775691:		#B3q0		1148775691:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81		6:14:45		24.89		789.38

		S1148775721:		#B3q0		1148775721:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81		6:15:15		24.92		790.40

		S1148775751:		#B3q0		1148775751:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81		6:15:45		24.95		791.43

		S1148775781:		#B3q0		1148775781:		$B3q0		d-		30.64		4.0		4.0		26.36		3.82		3.85		3.83		3.81		3.81		3.84		3.85		3.81		6:16:15		24.99		792.46

		S1148775811:		#B3q0		1148775811:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:16:45		25.02		793.49

		S1148775841:		#B3q0		1148775841:		$B3q0		d-		30.6		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:17:15		25.05		794.52

		S1148775871:		#B3q0		1148775871:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:17:45		25.09		795.55

		S1148775901:		#B3q0		1148775901:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:18:15		25.12		796.59

		S1148775931:		#B3q0		1148775931:		$B3q0		d-		30.64		4.1		4.1		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:18:45		25.15		797.62

		S1148775961:		#B3q0		1148775961:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:19:15		25.19		798.65

		S1148775991:		#B3q0		1148775991:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:19:45		25.22		799.68

		S1148776021:		#B3q0		1148776021:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:20:15		25.26		800.71

		S1148776051:		#B3q0		1148776051:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:20:45		25.29		801.74

		S1148776081:		#B3q0		1148776081:		$B3q0		d-		30.64		4.0		4.0		26.46		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:21:15		25.32		802.77

		S1148776111:		#B3q0		1148776111:		$B3q0		d-		30.64		4.0		4.0		26.36		3.82		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:21:45		25.36		803.80

		S1148776141:		#B3q0		1148776141:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.85		3.82		3.81		3.81		3.84		3.84		3.81		6:22:15		25.39		804.83

		S1148776171:		#B3q0		1148776171:		$B3q0		d-		30.6		4.0		4.0		26.36		3.81		3.85		3.82		3.80		3.81		3.84		3.84		3.81		6:22:45		25.42		805.86

		S1148776201:		#B3q0		1148776201:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.85		3.82		3.80		3.81		3.84		3.84		3.81		6:23:15		25.46		806.88

		S1148776231:		#B3q0		1148776231:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81		6:23:45		25.49		807.91

		S1148776261:		#B3q0		1148776261:		$B3q0		d-		30.64		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81		6:24:15		25.52		808.94

		S1148776291:		#B3q0		1148776291:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81		6:24:45		25.56		809.96

		S1148776321:		#B3q0		1148776321:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81		6:25:15		25.59		810.99

		S1148776351:		#B3q0		1148776351:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.84		3.84		3.81		6:25:45		25.62		812.01

		S1148776381:		#B3q0		1148776381:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81		6:26:15		25.66		813.04

		S1148776411:		#B3q0		1148776411:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81		6:26:45		25.69		814.07

		S1148776441:		#B3q0		1148776441:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81		6:27:15		25.73		815.09

		S1148776471:		#B3q0		1148776471:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81		6:27:45		25.76		816.12

		S1148776501:		#B3q0		1148776501:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.81		3.83		3.84		3.81		6:28:15		25.79		817.15

		S1148776531:		#B3q0		1148776531:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.81		6:28:45		25.83		818.17

		S1148776561:		#B3q0		1148776561:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.81		6:29:15		25.86		819.20

		S1148776591:		#B3q0		1148776591:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80		6:29:45		25.89		820.23

		S1148776621:		#B3q0		1148776621:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80		6:30:15		25.93		821.24

		S1148776651:		#B3q0		1148776651:		$B3q0		d-		30.56		4.1		4.1		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.84		3.80		6:30:45		25.96		822.27

		S1148776681:		#B3q0		1148776681:		$B3q0		d-		30.6		4.1		4.1		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:31:15		25.99		823.31

		S1148776711:		#B3q0		1148776711:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:31:45		26.03		824.35

		S1148776741:		#B3q0		1148776741:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:32:15		26.06		825.37

		S1148776771:		#B3q0		1148776771:		$B3q0		d-		30.56		4.0		4.0		26.36		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:32:45		26.09		826.40

		S1148776801:		#B3q0		1148776801:		$B3q0		d-		30.6		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:33:15		26.13		827.42

		S1148776831:		#B3q0		1148776831:		$B3q0		d-		30.56		4.1		4.1		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:33:45		26.16		828.46

		S1148776861:		#B3q0		1148776861:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:34:15		26.20		829.49

		S1148776891:		#B3q0		1148776891:		$B3q0		d-		30.56		4.1		4.1		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:34:45		26.23		830.53

		S1148776921:		#B3q0		1148776921:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:35:15		26.26		831.56

		S1148776951:		#B3q0		1148776951:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:35:45		26.30		832.59

		S1148776981:		#B3q0		1148776981:		$B3q0		d-		30.56		4.0		4.0		26.56		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:36:15		26.33		833.61

		S1148777011:		#B3q0		1148777011:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:36:45		26.36		834.64

		S1148777041:		#B3q0		1148777041:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.84		3.82		3.80		3.80		3.83		3.83		3.80		6:37:15		26.40		835.67

		S1148777071:		#B3q0		1148777071:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.83		3.82		3.80		3.80		3.83		3.83		3.80		6:37:45		26.43		836.69

		S1148777101:		#B3q0		1148777101:		$B3q0		d-		30.56		4.0		4.0		26.46		3.81		3.83		3.82		3.80		3.80		3.83		3.83		3.80		6:38:15		26.46		837.71

		S1148777131:		#B3q0		1148777131:		$B3q0		d-		30.56		4.0		4.0		26.46		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80		6:38:45		26.50		838.73

		S1148777161:		#B3q0		1148777161:		$B3q0		d-		30.56		4.0		4.0		26.56		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80		6:39:15		26.53		839.76

		S1148777191:		#B3q0		1148777191:		$B3q0		d-		30.56		4.0		4.0		26.46		3.80		3.83		3.82		3.80		3.80		3.83		3.83		3.80		6:39:45		26.57		840.79

		S1148777221:		#B3q0		1148777221:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:40:15		26.60		841.82

		S1148777251:		#B3q0		1148777251:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:40:45		26.63		842.84

		S1148777281:		#B3q0		1148777281:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:41:15		26.67		843.86

		S1148777311:		#B3q0		1148777311:		$B3q0		d-		30.56		4.0		4.0		26.56		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:41:45		26.70		844.89

		S1148777341:		#B3q0		1148777341:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:42:15		26.73		845.92

		S1148777371:		#B3q0		1148777371:		$B3q0		d-		30.53		4.1		4.1		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:42:45		26.77		846.95

		S1148777401:		#B3q0		1148777401:		$B3q0		d-		30.56		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:43:15		26.80		847.99

		S1148777431:		#B3q0		1148777431:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:43:45		26.84		849.02

		S1148777461:		#B3q0		1148777461:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:44:15		26.87		850.04

		S1148777491:		#B3q0		1148777491:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:44:45		26.90		851.06

		S1148777521:		#B3q0		1148777521:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:45:15		26.94		852.09

		S1148777551:		#B3q0		1148777551:		$B3q0		d-		30.53		4.1		4.1		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:45:45		26.97		853.12

		S1148777581:		#B3q0		1148777581:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:46:15		27.00		854.15

		S1148777611:		#B3q0		1148777611:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:46:45		27.04		855.17

		S1148777641:		#B3q0		1148777641:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.80		3.80		3.83		3.83		3.80		6:47:15		27.07		856.20

		S1148777671:		#B3q0		1148777671:		$B3q0		d-		30.53		4.0		4.0		26.56		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80		6:47:45		27.10		857.22

		S1148777701:		#B3q0		1148777701:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80		6:48:15		27.14		858.24

		S1148777731:		#B3q0		1148777731:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.83		3.83		3.80		6:48:45		27.17		859.26

		S1148777761:		#B3q0		1148777761:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:49:15		27.20		860.28

		S1148777791:		#B3q0		1148777791:		$B3q0		d-		30.49		4.1		4.1		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:49:45		27.24		861.30

		S1148777821:		#B3q0		1148777821:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:50:15		27.27		862.33

		S1148777851:		#B3q0		1148777851:		$B3q0		d-		30.49		4.0		4.0		26.56		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:50:45		27.31		863.36

		S1148777881:		#B3q0		1148777881:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:51:15		27.34		864.39

		S1148777911:		#B3q0		1148777911:		$B3q0		d-		30.53		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:51:45		27.37		865.42

		S1148777941:		#B3q0		1148777941:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:52:15		27.41		866.44

		S1148777971:		#B3q0		1148777971:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.83		3.80		6:52:45		27.44		867.47

		S1148778001:		#B3q0		1148778001:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.80		3.82		3.82		3.80		6:53:15		27.47		868.49

		S1148778031:		#B3q0		1148778031:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.80		6:53:45		27.51		869.51

		S1148778061:		#B3q0		1148778061:		$B3q0		d-		30.45		4.0		4.0		26.56		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.80		6:54:15		27.54		870.53

		S1148778091:		#B3q0		1148778091:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79		6:54:45		27.57		871.55

		S1148778121:		#B3q0		1148778121:		$B3q0		d-		30.49		4.0		4.0		26.56		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79		6:55:15		27.61		872.56

		S1148778151:		#B3q0		1148778151:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79		6:55:45		27.64		873.59

		S1148778181:		#B3q0		1148778181:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79		6:56:15		27.67		874.61

		S1148778211:		#B3q0		1148778211:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.81		3.79		3.79		3.82		3.82		3.79		6:56:45		27.71		875.63

		S1148778241:		#B3q0		1148778241:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:57:15		27.74		876.66

		S1148778271:		#B3q0		1148778271:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:57:45		27.77		877.68

		S1148778301:		#B3q0		1148778301:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:58:15		27.81		878.71

		S1148778331:		#B3q0		1148778331:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:58:45		27.84		879.73

		S1148778361:		#B3q0		1148778361:		$B3q0		d-		30.45		4.1		4.1		26.46		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:59:15		27.88		880.77

		S1148778391:		#B3q0		1148778391:		$B3q0		d-		30.49		4.0		4.0		26.56		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		6:59:45		27.91		881.80

		S1148778421:		#B3q0		1148778421:		$B3q0		d-		30.45		4.0		4.0		26.56		3.80		3.83		3.80		3.79		3.79		3.82		3.82		3.79		7:00:15		27.94		882.82

		S1148778451:		#B3q0		1148778451:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:00:45		27.98		883.84

		S1148778481:		#B3q0		1148778481:		$B3q0		d-		30.45		4.0		4.0		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:01:15		28.01		884.86

		S1148778511:		#B3q0		1148778511:		$B3q0		d-		30.45		4.1		4.1		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:01:45		28.04		885.88

		S1148778541:		#B3q0		1148778541:		$B3q0		d-		30.49		4.0		4.0		26.56		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:02:15		28.08		886.91

		S1148778571:		#B3q0		1148778571:		$B3q0		d-		30.45		4.0		4.0		26.56		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:02:45		28.11		887.94

		S1148778601:		#B3q0		1148778601:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:03:15		28.14		888.96

		S1148778631:		#B3q0		1148778631:		$B3q0		d-		30.45		4.0		4.0		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:03:45		28.18		889.98

		S1148778661:		#B3q0		1148778661:		$B3q0		d-		30.49		4.0		4.0		26.46		3.80		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:04:15		28.21		891.00

		S1148778691:		#B3q0		1148778691:		$B3q0		d-		30.45		4.0		4.0		26.56		3.79		3.82		3.80		3.79		3.79		3.82		3.82		3.79		7:04:45		28.25		892.02

		S1148778721:		#B3q0		1148778721:		$B3q0		d-		30.45		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:05:15		28.28		893.05

		S1148778751:		#B3q0		1148778751:		$B3q0		d-		30.45		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:05:45		28.31		894.07

		S1148778781:		#B3q0		1148778781:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:06:15		28.35		895.09

		S1148778811:		#B3q0		1148778811:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:06:45		28.38		896.11

		S1148778841:		#B3q0		1148778841:		$B3q0		d-		30.45		4.1		4.1		26.46		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:07:15		28.41		897.13

		S1148778871:		#B3q0		1148778871:		$B3q0		d-		30.45		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:07:45		28.45		898.16

		S1148778901:		#B3q0		1148778901:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:08:15		28.48		899.18

		S1148778931:		#B3q0		1148778931:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:08:45		28.51		900.20

		S1148778961:		#B3q0		1148778961:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:09:15		28.55		901.23

		S1148778991:		#B3q0		1148778991:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:09:45		28.58		902.25

		S1148779021:		#B3q0		1148779021:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:10:15		28.62		903.28

		S1148779051:		#B3q0		1148779051:		$B3q0		d-		30.41		4.1		4.1		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:10:45		28.65		904.31

		S1148779081:		#B3q0		1148779081:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.79		3.82		3.82		3.79		7:11:15		28.68		905.33

		S1148779111:		#B3q0		1148779111:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.79		7:11:45		28.72		906.35

		S1148779141:		#B3q0		1148779141:		$B3q0		d-		30.45		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:12:15		28.75		907.37

		S1148779171:		#B3q0		1148779171:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:12:45		28.78		908.39

		S1148779201:		#B3q0		1148779201:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:13:15		28.82		909.41

		S1148779231:		#B3q0		1148779231:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:13:45		28.85		910.44

		S1148779261:		#B3q0		1148779261:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:14:15		28.88		911.46

		S1148779291:		#B3q0		1148779291:		$B3q0		d-		30.45		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.82		3.82		3.78		7:14:45		28.92		912.48

		S1148779321:		#B3q0		1148779321:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:15:15		28.95		913.51

		S1148779351:		#B3q0		1148779351:		$B3q0		d-		30.41		4.1		4.1		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:15:45		28.99		914.54

		S1148779381:		#B3q0		1148779381:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:16:15		29.02		915.57

		S1148779411:		#B3q0		1148779411:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:16:45		29.05		916.59

		S1148779441:		#B3q0		1148779441:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:17:15		29.09		917.61

		S1148779471:		#B3q0		1148779471:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:17:45		29.12		918.64

		S1148779501:		#B3q0		1148779501:		$B3q0		d-		30.41		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.82		3.78		7:18:15		29.15		919.66

		S1148779531:		#B3q0		1148779531:		$B3q0		d-		30.41		4.1		4.1		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:18:45		29.19		920.69

		S1148779561:		#B3q0		1148779561:		$B3q0		d-		30.41		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:19:15		29.22		921.71

		S1148779591:		#B3q0		1148779591:		$B3q0		d-		30.37		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:19:45		29.25		922.73

		S1148779621:		#B3q0		1148779621:		$B3q0		d-		30.37		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:20:15		29.29		923.74

		S1148779651:		#B3q0		1148779651:		$B3q0		d-		30.37		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:20:45		29.32		924.77

		S1148779681:		#B3q0		1148779681:		$B3q0		d-		30.37		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:21:15		29.36		925.79

		S1148779711:		#B3q0		1148779711:		$B3q0		d-		30.37		4.0		4.0		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:21:45		29.39		926.81

		S1148779741:		#B3q0		1148779741:		$B3q0		d-		30.37		4.0		4.0		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:22:15		29.42		927.83

		S1148779771:		#B3q0		1148779771:		$B3q0		d-		30.41		4.1		4.1		26.46		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:22:45		29.46		928.86

		S1148779801:		#B3q0		1148779801:		$B3q0		d-		30.37		4.1		4.1		26.56		3.79		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:23:15		29.49		929.90

		S1148779831:		#B3q0		1148779831:		$B3q0		d-		30.41		4.0		4.0		26.56		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:23:45		29.52		930.92

		S1148779861:		#B3q0		1148779861:		$B3q0		d-		30.37		4.0		4.0		26.46		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:24:15		29.56		931.94

		S1148779891:		#B3q0		1148779891:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78		7:24:45		29.59		932.96

		S1148779921:		#B3q0		1148779921:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.82		3.80		3.78		3.78		3.81		3.81		3.78		7:25:15		29.63		933.98

		S1148779951:		#B3q0		1148779951:		$B3q0		d-		30.37		4.0		4.0		26.46		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78		7:25:45		29.66		935.00

		S1148779981:		#B3q0		1148779981:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.82		3.79		3.78		3.78		3.81		3.81		3.78		7:26:15		29.69		936.03

		S1148780011:		#B3q0		1148780011:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:26:45		29.73		937.04

		S1148780041:		#B3q0		1148780041:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:27:15		29.76		938.06

		S1148780071:		#B3q0		1148780071:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:27:45		29.79		939.08

		S1148780101:		#B3q0		1148780101:		$B3q0		d-		30.33		4.1		4.1		26.46		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:28:15		29.83		940.11

		S1148780131:		#B3q0		1148780131:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:28:45		29.86		941.14

		S1148780161:		#B3q0		1148780161:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:29:15		29.89		942.16

		S1148780191:		#B3q0		1148780191:		$B3q0		d-		30.37		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:29:45		29.93		943.18

		S1148780221:		#B3q0		1148780221:		$B3q0		d-		30.33		4.0		4.0		26.46		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:30:15		29.96		944.19

		S1148780251:		#B3q0		1148780251:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:30:45		30.00		945.22

		S1148780281:		#B3q0		1148780281:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:31:15		30.03		946.24

		S1148780311:		#B3q0		1148780311:		$B3q0		d-		30.33		4.0		4.0		26.46		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:31:45		30.06		947.25

		S1148780341:		#B3q0		1148780341:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.81		3.81		3.78		7:32:15		30.10		948.27

		S1148780371:		#B3q0		1148780371:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78		7:32:45		30.13		949.29

		S1148780401:		#B3q0		1148780401:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78		7:33:15		30.16		950.31

		S1148780431:		#B3q0		1148780431:		$B3q0		d-		30.3		4.1		4.1		26.46		3.78		3.81		3.79		3.78		3.78		3.80		3.81		3.78		7:33:45		30.20		951.34

		S1148780461:		#B3q0		1148780461:		$B3q0		d-		30.33		4.0		4.0		26.46		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:34:15		30.23		952.36

		S1148780491:		#B3q0		1148780491:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:34:45		30.26		953.37

		S1148780521:		#B3q0		1148780521:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:35:15		30.30		954.39

		S1148780551:		#B3q0		1148780551:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:35:45		30.33		955.40

		S1148780581:		#B3q0		1148780581:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:36:15		30.36		956.41

		S1148780611:		#B3q0		1148780611:		$B3q0		d-		30.33		4.1		4.1		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.81		3.78		7:36:45		30.40		957.43

		S1148780641:		#B3q0		1148780641:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78		7:37:15		30.43		958.46

		S1148780671:		#B3q0		1148780671:		$B3q0		d-		30.33		4.0		4.0		26.66		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78		7:37:45		30.47		959.48

		S1148780701:		#B3q0		1148780701:		$B3q0		d-		30.33		4.1		4.1		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78		7:38:15		30.50		960.51

		S1148780731:		#B3q0		1148780731:		$B3q0		d-		30.33		4.0		4.0		26.46		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78		7:38:45		30.53		961.53

		S1148780761:		#B3q0		1148780761:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.78		3.80		3.80		3.78		7:39:15		30.57		962.55

		S1148780791:		#B3q0		1148780791:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78		7:39:45		30.60		963.57

		S1148780821:		#B3q0		1148780821:		$B3q0		d-		30.3		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78		7:40:15		30.63		964.59

		S1148780851:		#B3q0		1148780851:		$B3q0		d-		30.3		4.0		4.0		26.46		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.78		7:40:45		30.67		965.61

		S1148780881:		#B3q0		1148780881:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:41:15		30.70		966.64

		S1148780911:		#B3q0		1148780911:		$B3q0		d-		30.33		4.0		4.0		26.46		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:41:45		30.73		967.65

		S1148780941:		#B3q0		1148780941:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:42:15		30.77		968.67

		S1148780971:		#B3q0		1148780971:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:42:45		30.80		969.69

		S1148781001:		#B3q0		1148781001:		$B3q0		d-		30.3		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:43:15		30.84		970.71

		S1148781031:		#B3q0		1148781031:		$B3q0		d-		30.33		4.0		4.0		26.56		3.78		3.81		3.79		3.77		3.77		3.80		3.80		3.77		7:43:45		30.87		971.72

		S1148781061:		#B3q0		1148781061:		$B3q0		d-		
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Chart1

		0		0		0		0		0		0		0		0		0		0

		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222		0.0003472222

		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444		0.0006944444

		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667		0.0010416667

		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889		0.0013888889

		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111		0.0017361111

		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333		0.0020833333

		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556		0.0024305556

		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778		0.0027777778

		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125		0.003125

		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222		0.0034722222

		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444		0.0038194444

		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667		0.0041666667

		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889		0.0045138889

		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111		0.0048611111

		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333		0.0052083333

		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556		0.0055555556

		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778		0.0059027778

		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625		0.00625

		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222		0.0065972222

		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444		0.0069444444

		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667		0.0072916667

		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889		0.0076388889

		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111		0.0079861111

		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333		0.0083333333

		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556		0.0086805556

		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778		0.0090277778

		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375		0.009375

		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222		0.0097222222

		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444		0.0100694444

		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667		0.0104166667

		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889		0.0107638889

		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111		0.0111111111

		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333		0.0114583333

		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556		0.0118055556

		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778		0.0121527778

		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125		0.0125

		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222		0.0128472222

		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444		0.0131944444

		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667		0.0135416667

		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889		0.0138888889

		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111		0.0142361111

		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333		0.0145833333

		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556		0.0149305556

		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778		0.0152777778

		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625		0.015625

		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222		0.0159722222

		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444		0.0163194444

		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667		0.0166666667

		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889		0.0170138889

		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111		0.0173611111

		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333		0.0177083333

		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556		0.0180555556

		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778		0.0184027778

		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875		0.01875

		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222		0.0190972222

		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444		0.0194444444

		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667		0.0197916667

		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889		0.0201388889

		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111		0.0204861111

		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333		0.0208333333

		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556		0.0211805556

		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778		0.0215277778

		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875		0.021875

		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222		0.0222222222

		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444		0.0225694444

		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667		0.0229166667

		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889		0.0232638889

		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111		0.0236111111

		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333		0.0239583333

		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556		0.0243055556

		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778		0.0246527778

		0.025		0.025		0.025		0.025		0.025		0.025		0.025		0.025		0.025		0.025

		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222		0.0253472222

		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444		0.0256944444

		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667		0.0260416667

		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889		0.0263888889

		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111		0.0267361111

		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333		0.0270833333

		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556		0.0274305556

		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778		0.0277777778

		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125		0.028125

		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222		0.0284722222

		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444		0.0288194444

		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407		0.0291782407

		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889		0.0295138889

		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111		0.0298611111

		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333		0.0302083333

		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556		0.0305555556

		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778		0.0309027778

		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125		0.03125

		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222		0.0315972222

		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444		0.0319444444

		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667		0.0322916667

		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889		0.0326388889

		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111		0.0329861111

		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333		0.0333333333

		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556		0.0336805556

		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778		0.0340277778

		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375		0.034375

		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222		0.0347222222

		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444		0.0350694444

		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667		0.0354166667

		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889		0.0357638889

		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111		0.0361111111

		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333		0.0364583333

		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556		0.0368055556

		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778		0.0371527778

		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375		0.0375

		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222		0.0378472222

		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444		0.0381944444

		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667		0.0385416667

		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889		0.0388888889

		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111		0.0392361111

		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333		0.0395833333

		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556		0.0399305556

		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778		0.0402777778

		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625		0.040625

		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222		0.0409722222

		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444		0.0413194444

		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667		0.0416666667

		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889		0.0420138889

		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111		0.0423611111

		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333		0.0427083333

		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556		0.0430555556

		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778		0.0434027778

		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375		0.04375

		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222		0.0440972222

		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444		0.0444444444

		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667		0.0447916667

		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889		0.0451388889

		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111		0.0454861111

		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333		0.0458333333

		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556		0.0461805556

		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778		0.0465277778

		0.046875		0.046875		0.046875		0.046875		0.046875		0.046875		0.046875		0.046875		0.046875		0.046875

		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222		0.0472222222

		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444		0.0475694444

		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667		0.0479166667

		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889		0.0482638889

		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111		0.0486111111

		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333		0.0489583333

		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556		0.0493055556

		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778		0.0496527778

		0.05		0.05		0.05		0.05		0.05		0.05		0.05		0.05		0.05		0.05

		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222		0.0503472222

		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444		0.0506944444

		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667		0.0510416667

		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889		0.0513888889

		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111		0.0517361111

		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333		0.0520833333

		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556		0.0524305556

		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778		0.0527777778

		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125		0.053125

		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222		0.0534722222

		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444		0.0538194444

		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667		0.0541666667

		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889		0.0545138889

		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111		0.0548611111

		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333		0.0552083333

		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556		0.0555555556

		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778		0.0559027778

		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625		0.05625

		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222		0.0565972222

		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444		0.0569444444

		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667		0.0572916667

		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889		0.0576388889

		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111		0.0579861111

		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333		0.0583333333

		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556		0.0586805556

		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778		0.0590277778

		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375		0.059375

		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222		0.0597222222

		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444		0.0600694444

		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667		0.0604166667

		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889		0.0607638889

		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111		0.0611111111

		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333		0.0614583333

		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556		0.0618055556

		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778		0.0621527778

		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625		0.0625

		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222		0.0628472222

		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444		0.0631944444

		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667		0.0635416667

		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889		0.0638888889

		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111		0.0642361111

		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333		0.0645833333

		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556		0.0649305556

		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778		0.0652777778

		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625		0.065625

		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222		0.0659722222

		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444		0.0663194444

		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667		0.0666666667

		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889		0.0670138889

		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111		0.0673611111

		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333		0.0677083333

		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556		0.0680555556

		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778		0.0684027778

		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875		0.06875

		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222		0.0690972222

		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444		0.0694444444

		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667		0.0697916667

		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889		0.0701388889

		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111		0.0704861111

		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333		0.0708333333

		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556		0.0711805556

		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778		0.0715277778

		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875		0.071875

		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222		0.0722222222

		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444		0.0725694444

		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667		0.0729166667

		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889		0.0732638889

		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111		0.0736111111

		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333		0.0739583333

		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556		0.0743055556

		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778		0.0746527778

		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075		0.075

		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963		0.0753587963

		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444		0.0756944444

		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667		0.0760416667

		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889		0.0763888889

		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111		0.0767361111

		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333		0.0770833333

		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556		0.0774305556

		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778		0.0777777778

		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125		0.078125

		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222		0.0784722222

		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444		0.0788194444

		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667		0.0791666667

		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889		0.0795138889

		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111		0.0798611111

		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333		0.0802083333

		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556		0.0805555556

		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778		0.0809027778

		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125		0.08125

		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222		0.0815972222

		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444		0.0819444444

		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667		0.0822916667

		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889		0.0826388889

		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111		0.0829861111

		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333		0.0833333333

		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556		0.0836805556

		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778		0.0840277778

		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375		0.084375

		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222		0.0847222222

		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444		0.0850694444

		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667		0.0854166667

		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889		0.0857638889

		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111		0.0861111111

		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333		0.0864583333

		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556		0.0868055556

		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778		0.0871527778

		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875		0.0875

		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222		0.0878472222

		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444		0.0881944444

		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667		0.0885416667

		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889		0.0888888889

		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111		0.0892361111

		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333		0.0895833333

		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556		0.0899305556

		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778		0.0902777778

		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625		0.090625

		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222		0.0909722222

		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444		0.0913194444

		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667		0.0916666667

		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889		0.0920138889

		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111		0.0923611111

		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333		0.0927083333

		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556		0.0930555556

		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778		0.0934027778

		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375		0.09375

		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222		0.0940972222

		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444		0.0944444444

		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667		0.0947916667

		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889		0.0951388889

		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111		0.0954861111

		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333		0.0958333333

		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556		0.0961805556

		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778		0.0965277778

		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875		0.096875

		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222		0.0972222222

		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444		0.0975694444

		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667		0.0979166667

		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889		0.0982638889

		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111		0.0986111111

		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333		0.0989583333

		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556		0.0993055556

		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778		0.0996527778

		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1		0.1

		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222		0.1003472222

		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444		0.1006944444

		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667		0.1010416667

		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889		0.1013888889

		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111		0.1017361111

		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333		0.1020833333

		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556		0.1024305556

		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778		0.1027777778

		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125		0.103125

		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222		0.1034722222

		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444		0.1038194444

		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667		0.1041666667

		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889		0.1045138889

		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111		0.1048611111

		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333		0.1052083333

		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556		0.1055555556

		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778		0.1059027778

		0.10625		0.10625		0.10625		0.10625		0.10625		0.10625		0.10625		0.10625		0.10625		0.10625

		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222		0.1065972222

		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444		0.1069444444

		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667		0.1072916667

		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889		0.1076388889

		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111		0.1079861111

		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333		0.1083333333

		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556		0.1086805556

		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778		0.1090277778

		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375		0.109375

		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222		0.1097222222

		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444		0.1100694444

		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667		0.1104166667

		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889		0.1107638889

		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111		0.1111111111

		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333		0.1114583333

		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556		0.1118055556

		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778		0.1121527778

		0.1125		0.1125		0.1125		0.1125		0.1125		0.1125		0.1125		0.1125		0.1125		0.1125

		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222		0.1128472222

		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444		0.1131944444

		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667		0.1135416667

		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889		0.1138888889

		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111		0.1142361111

		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333		0.1145833333

		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556		0.1149305556

		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778		0.1152777778

		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625		0.115625

		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222		0.1159722222

		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444		0.1163194444

		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667		0.1166666667

		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889		0.1170138889

		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111		0.1173611111

		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333		0.1177083333

		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556		0.1180555556

		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778		0.1184027778

		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875		0.11875

		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222		0.1190972222

		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444		0.1194444444

		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667		0.1197916667

		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889		0.1201388889

		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111		0.1204861111

		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333		0.1208333333

		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556		0.1211805556

		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778		0.1215277778

		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875		0.121875

		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222		0.1222222222

		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444		0.1225694444

		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667		0.1229166667

		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889		0.1232638889

		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111		0.1236111111

		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333		0.1239583333

		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556		0.1243055556

		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778		0.1246527778

		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125		0.125

		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222		0.1253472222

		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444		0.1256944444

		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667		0.1260416667

		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889		0.1263888889

		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111		0.1267361111

		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333		0.1270833333

		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556		0.1274305556

		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778		0.1277777778

		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125		0.128125

		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222		0.1284722222

		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444		0.1288194444

		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667		0.1291666667

		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889		0.1295138889

		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111		0.1298611111

		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333		0.1302083333

		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556		0.1305555556

		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778		0.1309027778

		0.13125		0.13125		0.13125		0.13125		0.13125		0.13125		0.13125		0.13125		0.13125		0.13125

		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222		0.1315972222

		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444		0.1319444444

		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667		0.1322916667

		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889		0.1326388889

		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111		0.1329861111

		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333		0.1333333333

		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556		0.1336805556

		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778		0.1340277778

		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375		0.134375

		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222		0.1347222222

		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444		0.1350694444

		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667		0.1354166667

		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889		0.1357638889

		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111		0.1361111111

		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333		0.1364583333

		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556		0.1368055556

		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778		0.1371527778

		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375		0.1375

		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222		0.1378472222

		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444		0.1381944444

		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667		0.1385416667

		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889		0.1388888889

		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111		0.1392361111

		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333		0.1395833333

		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556		0.1399305556

		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778		0.1402777778

		0.140625		0.140625		0.140625		0.140625		0.140625		0.140625		0.140625		0.140625		0.140625		0.140625

		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222		0.1409722222

		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444		0.1413194444

		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667		0.1416666667

		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889		0.1420138889

		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111		0.1423611111

		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333		0.1427083333

		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556		0.1430555556

		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778		0.1434027778

		0.14375		0.14375		0.14375		0.14375		0.14375		0.14375		0.14375		0.14375		0.14375		0.14375

		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222		0.1440972222

		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444		0.1444444444

		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667		0.1447916667

		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889		0.1451388889

		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111		0.1454861111

		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333		0.1458333333

		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556		0.1461805556

		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778		0.1465277778

		0.146875		0.146875		0.146875		0.146875		0.146875		0.146875		0.146875		0.146875		0.146875		0.146875

		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222		0.1472222222

		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444		0.1475694444

		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667		0.1479166667

		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889		0.1482638889

		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111		0.1486111111

		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333		0.1489583333

		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556		0.1493055556

		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778		0.1496527778

		0.15		0.15		0.15		0.15		0.15		0.15		0.15		0.15		0.15		0.15

		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222		0.1503472222

		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444		0.1506944444

		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667		0.1510416667

		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889		0.1513888889

		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111		0.1517361111

		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333		0.1520833333

		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556		0.1524305556

		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778		0.1527777778

		0.153125		0.153125		0.153125		0.153125		0.153125		0.153125		0.153125		0.153125		0.153125		0.153125

		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222		0.1534722222

		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444		0.1538194444

		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667		0.1541666667

		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889		0.1545138889

		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111		0.1548611111

		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333		0.1552083333

		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556		0.1555555556

		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778		0.1559027778

		0.15625		0.15625		0.15625		0.15625		0.15625		0.15625		0.15625		0.15625		0.15625		0.15625

		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222		0.1565972222

		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444		0.1569444444

		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667		0.1572916667

		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889		0.1576388889

		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111		0.1579861111

		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333		0.1583333333

		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556		0.1586805556

		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778		0.1590277778

		0.159375		0.159375		0.159375		0.159375		0.159375		0.159375		0.159375		0.159375		0.159375		0.159375

		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222		0.1597222222

		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444		0.1600694444

		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667		0.1604166667

		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889		0.1607638889

		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111		0.1611111111

		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333		0.1614583333

		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556		0.1618055556

		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778		0.1621527778

		0.1625		0.1625		0.1625		0.1625		0.1625		0.1625		0.1625		0.1625		0.1625		0.1625

		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222		0.1628472222

		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444		0.1631944444

		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667		0.1635416667

		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889		0.1638888889

		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111		0.1642361111

		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333		0.1645833333

		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556		0.1649305556

		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778		0.1652777778

		0.165625		0.165625		0.165625		0.165625		0.165625		0.165625		0.165625		0.165625		0.165625		0.165625

		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222		0.1659722222

		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444		0.1663194444

		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667		0.1666666667

		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889		0.1670138889

		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111		0.1673611111

		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333		0.1677083333

		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556		0.1680555556

		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778		0.1684027778

		0.16875		0.16875		0.16875		0.16875		0.16875		0.16875		0.16875		0.16875		0.16875		0.16875

		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222		0.1690972222

		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444		0.1694444444

		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667		0.1697916667

		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889		0.1701388889

		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111		0.1704861111

		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333		0.1708333333

		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556		0.1711805556

		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778		0.1715277778

		0.171875		0.171875		0.171875		0.171875		0.171875		0.171875		0.171875		0.171875		0.171875		0.171875

		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222		0.1722222222

		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444		0.1725694444

		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667		0.1729166667

		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889		0.1732638889

		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111		0.1736111111

		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333		0.1739583333

		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556		0.1743055556

		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778		0.1746527778

		0.175		0.175		0.175		0.175		0.175		0.175		0.175		0.175		0.175		0.175

		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222		0.1753472222

		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444		0.1756944444

		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667		0.1760416667

		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889		0.1763888889

		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111		0.1767361111

		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333		0.1770833333

		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556		0.1774305556

		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778		0.1777777778

		0.178125		0.178125		0.178125		0.178125		0.178125		0.178125		0.178125		0.178125		0.178125		0.178125

		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222		0.1784722222

		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444		0.1788194444

		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667		0.1791666667

		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889		0.1795138889

		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111		0.1798611111

		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333		0.1802083333

		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556		0.1805555556

		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778		0.1809027778

		0.18125		0.18125		0.18125		0.18125		0.18125		0.18125		0.18125		0.18125		0.18125		0.18125

		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222		0.1815972222

		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444		0.1819444444

		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667		0.1822916667

		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889		0.1826388889

		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111		0.1829861111

		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333		0.1833333333

		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556		0.1836805556

		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778		0.1840277778

		0.184375		0.184375		0.184375		0.184375		0.184375		0.184375		0.184375		0.184375		0.184375		0.184375

		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222		0.1847222222

		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444		0.1850694444

		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667		0.1854166667

		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889		0.1857638889

		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111		0.1861111111

		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333		0.1864583333

		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556		0.1868055556

		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778		0.1871527778

		0.1875		0.1875		0.1875		0.1875		0.1875		0.1875		0.1875		0.1875		0.1875		0.1875

		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222		0.1878472222

		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444		0.1881944444

		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667		0.1885416667

		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889		0.1888888889

		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111		0.1892361111

		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333		0.1895833333

		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556		0.1899305556

		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778		0.1902777778

		0.190625		0.190625		0.190625		0.190625		0.190625		0.190625		0.190625		0.190625		0.190625		0.190625

		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222		0.1909722222

		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444		0.1913194444

		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667		0.1916666667

		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889		0.1920138889

		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111		0.1923611111

		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333		0.1927083333

		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556		0.1930555556

		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778		0.1934027778

		0.19375		0.19375		0.19375		0.19375		0.19375		0.19375		0.19375		0.19375		0.19375		0.19375

		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222		0.1940972222

		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444		0.1944444444

		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667		0.1947916667

		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889		0.1951388889

		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111		0.1954861111

		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333		0.1958333333

		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556		0.1961805556

		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778		0.1965277778

		0.196875		0.196875		0.196875		0.196875		0.196875		0.196875		0.196875		0.196875		0.196875		0.196875

		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222		0.1972222222

		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444		0.1975694444

		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667		0.1979166667

		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889		0.1982638889

		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111		0.1986111111

		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333		0.1989583333

		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556		0.1993055556

		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778		0.1996527778

		0.2		0.2		0.2		0.2		0.2		0.2		0.2		0.2		0.2		0.2

		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222		0.2003472222

		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444		0.2006944444

		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667		0.2010416667

		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889		0.2013888889

		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111		0.2017361111

		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333		0.2020833333

		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556		0.2024305556

		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778		0.2027777778

		0.203125		0.203125		0.203125		0.203125		0.203125		0.203125		0.203125		0.203125		0.203125		0.203125

		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222		0.2034722222

		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444		0.2038194444

		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667		0.2041666667

		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889		0.2045138889

		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111		0.2048611111

		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333		0.2052083333

		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556		0.2055555556

		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778		0.2059027778

		0.20625		0.20625		0.20625		0.20625		0.20625		0.20625		0.20625		0.20625		0.20625		0.20625

		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222		0.2065972222

		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444		0.2069444444

		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667		0.2072916667

		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889		0.2076388889

		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111		0.2079861111

		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333		0.2083333333

		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556		0.2086805556

		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778		0.2090277778

		0.209375		0.209375		0.209375		0.209375		0.209375		0.209375		0.209375		0.209375		0.209375		0.209375

		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222		0.2097222222

		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444		0.2100694444

		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667		0.2104166667

		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889		0.2107638889

		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111		0.2111111111

		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333		0.2114583333

		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556		0.2118055556

		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778		0.2121527778

		0.2125		0.2125		0.2125		0.2125		0.2125		0.2125		0.2125		0.2125		0.2125		0.2125

		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222		0.2128472222

		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444		0.2131944444

		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667		0.2135416667

		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889		0.2138888889

		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111		0.2142361111

		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333		0.2145833333

		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556		0.2149305556

		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778		0.2152777778

		0.215625		0.215625		0.215625		0.215625		0.215625		0.215625		0.215625		0.215625		0.215625		0.215625

		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222		0.2159722222

		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444		0.2163194444

		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667		0.2166666667

		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889		0.2170138889

		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111		0.2173611111

		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333		0.2177083333

		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556		0.2180555556

		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778		0.2184027778

		0.21875		0.21875		0.21875		0.21875		0.21875		0.21875		0.21875		0.21875		0.21875		0.21875

		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222		0.2190972222

		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444		0.2194444444

		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667		0.2197916667

		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889		0.2201388889

		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111		0.2204861111

		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333		0.2208333333

		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556		0.2211805556

		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778		0.2215277778

		0.221875		0.221875		0.221875		0.221875		0.221875		0.221875		0.221875		0.221875		0.221875		0.221875

		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222		0.2222222222

		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444		0.2225694444

		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667		0.2229166667

		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889		0.2232638889

		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111		0.2236111111

		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333		0.2239583333

		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556		0.2243055556

		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778		0.2246527778

		0.225		0.225		0.225		0.225		0.225		0.225		0.225		0.225		0.225		0.225

		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222		0.2253472222

		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444		0.2256944444

		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667		0.2260416667

		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889		0.2263888889

		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111		0.2267361111

		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333		0.2270833333

		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556		0.2274305556

		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778		0.2277777778

		0.228125		0.228125		0.228125		0.228125		0.228125		0.228125		0.228125		0.228125		0.228125		0.228125

		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222		0.2284722222

		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444		0.2288194444

		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667		0.2291666667

		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889		0.2295138889

		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111		0.2298611111

		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333		0.2302083333

		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556		0.2305555556

		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778		0.2309027778

		0.23125		0.23125		0.23125		0.23125		0.23125		0.23125		0.23125		0.23125		0.23125		0.23125

		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222		0.2315972222

		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444		0.2319444444

		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667		0.2322916667

		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889		0.2326388889

		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111		0.2329861111

		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333		0.2333333333

		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556		0.2336805556

		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778		0.2340277778

		0.234375		0.234375		0.234375		0.234375		0.234375		0.234375		0.234375		0.234375		0.234375		0.234375

		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222		0.2347222222

		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444		0.2350694444

		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667		0.2354166667

		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889		0.2357638889

		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111		0.2361111111

		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333		0.2364583333

		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556		0.2368055556

		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778		0.2371527778

		0.2375		0.2375		0.2375		0.2375		0.2375		0.2375		0.2375		0.2375		0.2375		0.2375

		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222		0.2378472222

		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444		0.2381944444

		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667		0.2385416667

		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889		0.2388888889

		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111		0.2392361111

		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333		0.2395833333

		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556		0.2399305556

		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778		0.2402777778

		0.240625		0.240625		0.240625		0.240625		0.240625		0.240625		0.240625		0.240625		0.240625		0.240625

		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222		0.2409722222

		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444		0.2413194444

		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667		0.2416666667

		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889		0.2420138889

		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111		0.2423611111

		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333		0.2427083333

		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556		0.2430555556

		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778		0.2434027778

		0.24375		0.24375		0.24375		0.24375		0.24375		0.24375		0.24375		0.24375		0.24375		0.24375

		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222		0.2440972222

		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444		0.2444444444

		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667		0.2447916667

		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889		0.2451388889

		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111		0.2454861111

		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333		0.2458333333

		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556		0.2461805556

		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778		0.2465277778

		0.246875		0.246875		0.246875		0.246875		0.246875		0.246875		0.246875		0.246875		0.246875		0.246875

		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222		0.2472222222

		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444		0.2475694444

		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667		0.2479166667

		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889		0.2482638889

		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111		0.2486111111

		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333		0.2489583333

		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556		0.2493055556

		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778		0.2496527778

		0.25		0.25		0.25		0.25		0.25		0.25		0.25		0.25		0.25		0.25

		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222		0.2503472222

		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444		0.2506944444

		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667		0.2510416667

		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889		0.2513888889

		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111		0.2517361111

		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333		0.2520833333

		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556		0.2524305556

		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778		0.2527777778

		0.253125		0.253125		0.253125		0.253125		0.253125		0.253125		0.253125		0.253125		0.253125		0.253125

		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222		0.2534722222

		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444		0.2538194444

		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667		0.2541666667

		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889		0.2545138889

		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111		0.2548611111

		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333		0.2552083333

		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556		0.2555555556

		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778		0.2559027778

		0.25625		0.25625		0.25625		0.25625		0.25625		0.25625		0.25625		0.25625		0.25625		0.25625

		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222		0.2565972222

		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444		0.2569444444

		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667		0.2572916667

		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889		0.2576388889

		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111		0.2579861111

		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333		0.2583333333

		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556		0.2586805556

		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778		0.2590277778

		0.259375		0.259375		0.259375		0.259375		0.259375		0.259375		0.259375		0.259375		0.259375		0.259375

		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222		0.2597222222

		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444		0.2600694444

		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667		0.2604166667

		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889		0.2607638889

		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111		0.2611111111

		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333		0.2614583333

		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556		0.2618055556

		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778		0.2621527778

		0.2625		0.2625		0.2625		0.2625		0.2625		0.2625		0.2625		0.2625		0.2625		0.2625

		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222		0.2628472222

		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444		0.2631944444

		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667		0.2635416667

		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889		0.2638888889

		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111		0.2642361111

		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333		0.2645833333

		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556		0.2649305556

		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778		0.2652777778

		0.265625		0.265625		0.265625		0.265625		0.265625		0.265625		0.265625		0.265625		0.265625		0.265625

		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222		0.2659722222

		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444		0.2663194444

		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667		0.2666666667

		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889		0.2670138889

		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111		0.2673611111

		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333		0.2677083333

		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556		0.2680555556

		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778		0.2684027778

		0.26875		0.26875		0.26875		0.26875		0.26875		0.26875		0.26875		0.26875		0.26875		0.26875

		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222		0.2690972222

		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444		0.2694444444

		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667		0.2697916667

		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889		0.2701388889

		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111		0.2704861111

		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333		0.2708333333

		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556		0.2711805556

		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778		0.2715277778

		0.271875		0.271875		0.271875		0.271875		0.271875		0.271875		0.271875		0.271875		0.271875		0.271875

		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222		0.2722222222

		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444		0.2725694444

		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667		0.2729166667

		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889		0.2732638889

		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111		0.2736111111

		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333		0.2739583333

		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556		0.2743055556

		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778		0.2746527778

		0.275		0.275		0.275		0.275		0.275		0.275		0.275		0.275		0.275		0.275

		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222		0.2753472222

		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444		0.2756944444

		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667		0.2760416667

		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889		0.2763888889

		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111		0.2767361111

		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333		0.2770833333

		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556		0.2774305556

		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778		0.2777777778

		0.278125		0.278125		0.278125		0.278125		0.278125		0.278125		0.278125		0.278125		0.278125		0.278125

		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222		0.2784722222

		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444		0.2788194444

		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667		0.2791666667

		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889		0.2795138889

		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111		0.2798611111

		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333		0.2802083333

		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556		0.2805555556

		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778		0.2809027778

		0.28125		0.28125		0.28125		0.28125		0.28125		0.28125		0.28125		0.28125		0.28125		0.28125

		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222		0.2815972222

		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444		0.2819444444

		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667		0.2822916667

		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889		0.2826388889

		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111		0.2829861111

		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333		0.2833333333

		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556		0.2836805556

		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778		0.2840277778

		0.284375		0.284375		0.284375		0.284375		0.284375		0.284375		0.284375		0.284375		0.284375		0.284375

		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222		0.2847222222

		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444		0.2850694444

		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667		0.2854166667

		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889		0.2857638889

		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111		0.2861111111

		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333		0.2864583333

		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556		0.2868055556

		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778		0.2871527778

		0.2875		0.2875		0.2875		0.2875		0.2875		0.2875		0.2875		0.2875		0.2875		0.2875

		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222		0.2878472222

		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444		0.2881944444

		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667		0.2885416667

		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889		0.2888888889

		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111		0.2892361111

		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333		0.2895833333

		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556		0.2899305556

		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778		0.2902777778

		0.290625		0.290625		0.290625		0.290625		0.290625		0.290625		0.290625		0.290625		0.290625		0.290625

		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222		0.2909722222

		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444		0.2913194444

		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667		0.2916666667

		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889		0.2920138889

		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111		0.2923611111

		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333		0.2927083333

		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556		0.2930555556

		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778		0.2934027778

		0.29375		0.29375		0.29375		0.29375		0.29375		0.29375		0.29375		0.29375		0.29375		0.29375

		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222		0.2940972222

		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444		0.2944444444

		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667		0.2947916667

		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889		0.2951388889

		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111		0.2954861111

		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333		0.2958333333

		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556		0.2961805556

		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778		0.2965277778

		0.296875		0.296875		0.296875		0.296875		0.296875		0.296875		0.296875		0.296875		0.296875		0.296875

		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222		0.2972222222

		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444		0.2975694444

		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667		0.2979166667

		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889		0.2982638889

		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111		0.2986111111

		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333		0.2989583333

		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556		0.2993055556

		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778		0.2996527778

		0.3		0.3		0.3		0.3		0.3		0.3		0.3		0.3		0.3		0.3

		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222		0.3003472222

		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444		0.3006944444

		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667		0.3010416667

		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889		0.3013888889

		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111		0.3017361111

		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333		0.3020833333

		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556		0.3024305556

		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778		0.3027777778

		0.303125		0.303125		0.303125		0.303125		0.303125		0.303125		0.303125		0.303125		0.303125		0.303125

		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222		0.3034722222

		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444		0.3038194444

		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667		0.3041666667

		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889		0.3045138889

		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111		0.3048611111

		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333		0.3052083333

		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556		0.3055555556

		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778		0.3059027778

		0.30625		0.30625		0.30625		0.30625		0.30625		0.30625		0.30625		0.30625		0.30625		0.30625

		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222		0.3065972222

		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444		0.3069444444

		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667		0.3072916667

		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889		0.3076388889

		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111		0.3079861111

		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333		0.3083333333

		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556		0.3086805556

		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778		0.3090277778

		0.309375		0.309375		0.309375		0.309375		0.309375		0.309375		0.309375		0.309375		0.309375		0.309375

		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222		0.3097222222

		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444		0.3100694444

		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667		0.3104166667

		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889		0.3107638889

		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111		0.3111111111

		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333		0.3114583333

		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556		0.3118055556

		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778		0.3121527778

		0.3125		0.3125		0.3125		0.3125		0.3125		0.3125		0.3125		0.3125		0.3125		0.3125

		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222		0.3128472222

		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444		0.3131944444

		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667		0.3135416667

		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889		0.3138888889

		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111		0.3142361111

		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333		0.3145833333

		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556		0.3149305556

		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778		0.3152777778

		0.315625		0.315625		0.315625		0.315625		0.315625		0.315625		0.315625		0.315625		0.315625		0.315625

		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222		0.3159722222

		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444		0.3163194444

		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667		0.3166666667

		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889		0.3170138889

		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111		0.3173611111

		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333		0.3177083333

		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556		0.3180555556

		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778		0.3184027778

		0.31875		0.31875		0.31875		0.31875		0.31875		0.31875		0.31875		0.31875		0.31875		0.31875

		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222		0.3190972222

		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444		0.3194444444

		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667		0.3197916667

		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889		0.3201388889

		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111		0.3204861111

		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333		0.3208333333

		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556		0.3211805556

		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778		0.3215277778

		0.321875		0.321875		0.321875		0.321875		0.321875		0.321875		0.321875		0.321875		0.321875		0.321875

		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222		0.3222222222

		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444		0.3225694444

		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667		0.3229166667

		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889		0.3232638889

		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111		0.3236111111

		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333		0.3239583333

		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556		0.3243055556

		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778		0.3246527778

		0.325		0.325		0.325		0.325		0.325		0.325		0.325		0.325		0.325		0.325

		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222		0.3253472222

		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444		0.3256944444

		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667		0.3260416667

		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889		0.3263888889

		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111		0.3267361111

		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333		0.3270833333

		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556		0.3274305556

		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778		0.3277777778

		0.328125		0.328125		0.328125		0.328125		0.328125		0.328125		0.328125		0.328125		0.328125		0.328125

		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222		0.3284722222

		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444		0.3288194444

		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667		0.3291666667

		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889		0.3295138889

		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111		0.3298611111

		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333		0.3302083333

		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556		0.3305555556

		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778		0.3309027778

		0.33125		0.33125		0.33125		0.33125		0.33125		0.33125		0.33125		0.33125		0.33125		0.33125

		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222		0.3315972222

		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444		0.3319444444

		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667		0.3322916667

		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889		0.3326388889

		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111		0.3329861111

		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333		0.3333333333

		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556		0.3336805556

		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778		0.3340277778

		0.334375		0.334375		0.334375		0.334375		0.334375		0.334375		0.334375		0.334375		0.334375		0.334375

		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222		0.3347222222

		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444		0.3350694444

		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667		0.3354166667

		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889		0.3357638889

		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111		0.3361111111

		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333		0.3364583333

		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556		0.3368055556

		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778		0.3371527778

		0.3375		0.3375		0.3375		0.3375		0.3375		0.3375		0.3375		0.3375		0.3375		0.3375

		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222		0.3378472222

		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444		0.3381944444

		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667		0.3385416667

		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889		0.3388888889

		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111		0.3392361111

		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333		0.3395833333

		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556		0.3399305556

		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778		0.3402777778

		0.340625		0.340625		0.340625		0.340625		0.340625		0.340625		0.340625		0.340625		0.340625		0.340625

		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222		0.3409722222

		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444		0.3413194444

		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667		0.3416666667

		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889		0.3420138889

		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111		0.3423611111

		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333		0.3427083333

		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556		0.3430555556

		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778		0.3434027778

		0.34375		0.34375		0.34375		0.34375		0.34375		0.34375		0.34375		0.34375		0.34375		0.34375

		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222		0.3440972222

		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444		0.3444444444

		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667		0.3447916667

		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889		0.3451388889

		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111		0.3454861111

		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333		0.3458333333

		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556		0.3461805556

		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778		0.3465277778

		0.346875		0.346875		0.346875		0.346875		0.346875		0.346875		0.346875		0.346875		0.346875		0.346875

		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222		0.3472222222

		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444		0.3475694444

		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667		0.3479166667

		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889		0.3482638889

		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111		0.3486111111

		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333		0.3489583333

		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556		0.3493055556

		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778		0.3496527778

		0.35		0.35		0.35		0.35		0.35		0.35		0.35		0.35		0.35		0.35

		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222		0.3503472222

		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444		0.3506944444

		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667		0.3510416667

		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889		0.3513888889

		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111		0.3517361111

		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333		0.3520833333

		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296		0.3524421296

		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778		0.3527777778

		0.353125		0.353125		0.353125		0.353125		0.353125		0.353125		0.353125		0.353125		0.353125		0.353125

		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222		0.3534722222

		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444		0.3538194444

		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667		0.3541666667

		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889		0.3545138889

		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111		0.3548611111

		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333		0.3552083333

		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556		0.3555555556

		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778		0.3559027778

		0.35625		0.35625		0.35625		0.35625		0.35625		0.35625		0.35625		0.35625		0.35625		0.35625

		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222		0.3565972222

		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444		0.3569444444

		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667		0.3572916667

		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889		0.3576388889

		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111		0.3579861111

		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333		0.3583333333

		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556		0.3586805556

		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778		0.3590277778

		0.359375		0.359375		0.359375		0.359375		0.359375		0.359375		0.359375		0.359375		0.359375		0.359375

		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222		0.3597222222

		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444		0.3600694444

		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667		0.3604166667

		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889		0.3607638889

		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111		0.3611111111

		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333		0.3614583333

		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556		0.3618055556

		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778		0.3621527778

		0.3625		0.3625		0.3625		0.3625		0.3625		0.3625		0.3625		0.3625		0.3625		0.3625

		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222		0.3628472222

		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444		0.3631944444

		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667		0.3635416667

		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889		0.3638888889

		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111		0.3642361111

		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333		0.3645833333

		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556		0.3649305556

		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778		0.3652777778

		0.365625		0.365625		0.365625		0.365625		0.365625		0.365625		0.365625		0.365625		0.365625		0.365625

		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222		0.3659722222

		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444		0.3663194444

		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667		0.3666666667

		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889		0.3670138889

		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111		0.3673611111

		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333		0.3677083333

		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556		0.3680555556

		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778		0.3684027778

		0.36875		0.36875		0.36875		0.36875		0.36875		0.36875		0.36875		0.36875		0.36875		0.36875

		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222		0.3690972222

		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444		0.3694444444

		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667		0.3697916667

		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889		0.3701388889

		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111		0.3704861111

		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333		0.3708333333

		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556		0.3711805556

		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778		0.3715277778

		0.371875		0.371875		0.371875		0.371875		0.371875		0.371875		0.371875		0.371875		0.371875		0.371875

		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222		0.3722222222

		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444		0.3725694444

		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667		0.3729166667

		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889		0.3732638889

		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111		0.3736111111

		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333		0.3739583333

		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556		0.3743055556

		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778		0.3746527778

		0.375		0.375		0.375		0.375		0.375		0.375		0.375		0.375		0.375		0.375

		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222		0.3753472222

		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444		0.3756944444

		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667		0.3760416667

		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889		0.3763888889

		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111		0.3767361111

		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333		0.3770833333

		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556		0.3774305556

		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778		0.3777777778

		0.378125		0.378125		0.378125		0.378125		0.378125		0.378125		0.378125		0.378125		0.378125		0.378125

		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222		0.3784722222

		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444		0.3788194444

		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667		0.3791666667

		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889		0.3795138889

		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111		0.3798611111

		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333		0.3802083333

		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556		0.3805555556

		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778		0.3809027778

		0.38125		0.38125		0.38125		0.38125		0.38125		0.38125		0.38125		0.38125		0.38125		0.38125

		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222		0.3815972222

		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444		0.3819444444

		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667		0.3822916667

		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889		0.3826388889

		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111		0.3829861111

		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333		0.3833333333

		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556		0.3836805556

		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778		0.3840277778

		0.384375		0.384375		0.384375		0.384375		0.384375		0.384375		0.384375		0.384375		0.384375		0.384375

		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222		0.3847222222

		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444		0.3850694444

		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667		0.3854166667

		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889		0.3857638889

		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111		0.3861111111

		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333		0.3864583333

		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556		0.3868055556

		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778		0.3871527778

		0.3875		0.3875		0.3875		0.3875		0.3875		0.3875		0.3875		0.3875		0.3875		0.3875

		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222		0.3878472222

		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444		0.3881944444

		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667		0.3885416667

		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889		0.3888888889

		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111		0.3892361111

		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333		0.3895833333

		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556		0.3899305556

		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778		0.3902777778

		0.390625		0.390625		0.390625		0.390625		0.390625		0.390625		0.390625		0.390625		0.390625		0.390625

		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222		0.3909722222

		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444		0.3913194444

		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667		0.3916666667

		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889		0.3920138889

		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111		0.3923611111

		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333		0.3927083333

		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556		0.3930555556

		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778		0.3934027778

		0.39375		0.39375		0.39375		0.39375		0.39375		0.39375		0.39375		0.39375		0.39375		0.39375

		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222		0.3940972222

		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444		0.3944444444

		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667		0.3947916667

		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889		0.3951388889

		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111		0.3954861111

		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333		0.3958333333

		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556		0.3961805556

		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778		0.3965277778

		0.396875		0.396875		0.396875		0.396875		0.396875		0.396875		0.396875		0.396875		0.396875		0.396875

		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222		0.3972222222

		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444		0.3975694444

		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667		0.3979166667

		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889		0.3982638889

		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111		0.3986111111

		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333		0.3989583333

		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556		0.3993055556

		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778		0.3996527778

		0.4		0.4		0.4		0.4		0.4		0.4		0.4		0.4		0.4		0.4

		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222		0.4003472222

		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444		0.4006944444

		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667		0.4010416667

		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889		0.4013888889

		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111		0.4017361111

		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333		0.4020833333

		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556		0.4024305556

		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778		0.4027777778

		0.403125		0.403125		0.403125		0.403125		0.403125		0.403125		0.403125		0.403125		0.403125		0.403125

		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222		0.4034722222

		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444		0.4038194444

		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667		0.4041666667

		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889		0.4045138889

		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111		0.4048611111

		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333		0.4052083333

		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556		0.4055555556

		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778		0.4059027778

		0.40625		0.40625		0.40625		0.40625		0.40625		0.40625		0.40625		0.40625		0.40625		0.40625

		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222		0.4065972222

		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444		0.4069444444

		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667		0.4072916667

		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889		0.4076388889

		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111		0.4079861111

		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333		0.4083333333

		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556		0.4086805556

		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778		0.4090277778

		0.409375		0.409375		0.409375		0.409375		0.409375		0.409375		0.409375		0.409375		0.409375		0.409375

		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222		0.4097222222

		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444		0.4100694444

		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667		0.4104166667

		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889		0.4107638889

		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111		0.4111111111

		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333		0.4114583333

		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556		0.4118055556

		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778		0.4121527778

		0.4125		0.4125		0.4125		0.4125		0.4125		0.4125		0.4125		0.4125		0.4125		0.4125

		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222		0.4128472222

		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444		0.4131944444

		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667		0.4135416667

		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889		0.4138888889

		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111		0.4142361111

		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333		0.4145833333

		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556		0.4149305556

		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778		0.4152777778

		0.415625		0.415625		0.415625		0.415625		0.415625		0.415625		0.415625		0.415625		0.415625		0.415625

		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222		0.4159722222

		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444		0.4163194444

		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667		0.4166666667

		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889		0.4170138889

		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111		0.4173611111

		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333		0.4177083333

		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556		0.4180555556

		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778		0.4184027778

		0.41875		0.41875		0.41875		0.41875		0.41875		0.41875		0.41875		0.41875		0.41875		0.41875

		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222		0.4190972222

		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444		0.4194444444

		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667		0.4197916667

		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889		0.4201388889

		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111		0.4204861111

		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333		0.4208333333

		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556		0.4211805556

		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778		0.4215277778

		0.421875		0.421875		0.421875		0.421875		0.421875		0.421875		0.421875		0.421875		0.421875		0.421875

		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222		0.4222222222

		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444		0.4225694444

		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667		0.4229166667

		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889		0.4232638889

		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111		0.4236111111

		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333		0.4239583333

		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556		0.4243055556

		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778		0.4246527778

		0.425		0.425		0.425		0.425		0.425		0.425		0.425		0.425		0.425		0.425

		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222		0.4253472222

		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444		0.4256944444

		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667		0.4260416667

		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889		0.4263888889

		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111		0.4267361111

		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333		0.4270833333

		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556		0.4274305556

		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778		0.4277777778

		0.428125		0.428125		0.428125		0.428125		0.428125		0.428125		0.428125		0.428125		0.428125		0.428125

		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222		0.4284722222

		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444		0.4288194444

		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667		0.4291666667

		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889		0.4295138889

		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111		0.4298611111

		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333		0.4302083333

		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556		0.4305555556

		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778		0.4309027778

		0.43125		0.43125		0.43125		0.43125		0.43125		0.43125		0.43125		0.43125		0.43125		0.43125

		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222		0.4315972222

		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444		0.4319444444

		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667		0.4322916667

		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889		0.4326388889

		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111		0.4329861111

		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333		0.4333333333

		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556		0.4336805556

		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778		0.4340277778

		0.434375		0.434375		0.434375		0.434375		0.434375		0.434375		0.434375		0.434375		0.434375		0.434375

		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222		0.4347222222

		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444		0.4350694444

		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667		0.4354166667

		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889		0.4357638889

		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111		0.4361111111

		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333		0.4364583333

		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556		0.4368055556

		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778		0.4371527778

		0.4375		0.4375		0.4375		0.4375		0.4375		0.4375		0.4375		0.4375		0.4375		0.4375

		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222		0.4378472222

		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444		0.4381944444

		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667		0.4385416667

		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889		0.4388888889

		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111		0.4392361111

		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333		0.4395833333

		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556		0.4399305556

		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778		0.4402777778

		0.440625		0.440625		0.440625		0.440625		0.440625		0.440625		0.440625		0.440625		0.440625		0.440625

		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222		0.4409722222

		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444		0.4413194444

		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667		0.4416666667

		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889		0.4420138889

		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111		0.4423611111

		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333		0.4427083333

		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556		0.4430555556

		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778		0.4434027778

		0.44375		0.44375		0.44375		0.44375		0.44375		0.44375		0.44375		0.44375		0.44375		0.44375

		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222		0.4440972222

		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444		0.4444444444

		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667		0.4447916667

		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889		0.4451388889

		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111		0.4454861111

		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333		0.4458333333

		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556		0.4461805556

		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778		0.4465277778

		0.446875		0.446875		0.446875		0.446875		0.446875		0.446875		0.446875		0.446875		0.446875		0.446875

		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222		0.4472222222

		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444		0.4475694444

		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667		0.4479166667

		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889		0.4482638889

		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111		0.4486111111

		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333		0.4489583333

		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556		0.4493055556

		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778		0.4496527778

		0.45		0.45		0.45		0.45		0.45		0.45		0.45		0.45		0.45		0.45

		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222		0.4503472222

		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444		0.4506944444

		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667		0.4510416667

		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889		0.4513888889

		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111		0.4517361111

		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333		0.4520833333

		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556		0.4524305556

		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778		0.4527777778

		0.453125		0.453125		0.453125		0.453125		0.453125		0.453125		0.453125		0.453125		0.453125		0.453125

		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222		0.4534722222

		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444		0.4538194444

		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667		0.4541666667

		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889		0.4545138889

		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111		0.4548611111

		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333		0.4552083333

		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556		0.4555555556

		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778		0.4559027778

		0.45625		0.45625		0.45625		0.45625		0.45625		0.45625		0.45625		0.45625		0.45625		0.45625

		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222		0.4565972222

		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444		0.4569444444

		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667		0.4572916667

		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889		0.4576388889

		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111		0.4579861111

		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333		0.4583333333

		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556		0.4586805556

		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778		0.4590277778

		0.459375		0.459375		0.459375		0.459375		0.459375		0.459375		0.459375		0.459375		0.459375		0.459375

		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222		0.4597222222

		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444		0.4600694444

		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667		0.4604166667

		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889		0.4607638889

		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111		0.4611111111

		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333		0.4614583333

		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556		0.4618055556

		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778		0.4621527778

		0.4625		0.4625		0.4625		0.4625		0.4625		0.4625		0.4625		0.4625		0.4625		0.4625

		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222		0.4628472222

		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444		0.4631944444

		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667		0.4635416667

		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889		0.4638888889

		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111		0.4642361111

		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333		0.4645833333

		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556		0.4649305556

		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778		0.4652777778

		0.465625		0.465625		0.465625		0.465625		0.465625		0.465625		0.465625		0.465625		0.465625		0.465625

		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222		0.4659722222

		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444		0.4663194444

		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667		0.4666666667

		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889		0.4670138889

		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111		0.4673611111

		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333		0.4677083333

		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556		0.4680555556

		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778		0.4684027778

		0.46875		0.46875		0.46875		0.46875		0.46875		0.46875		0.46875		0.46875		0.46875		0.46875

		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222		0.4690972222

		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444		0.4694444444

		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667		0.4697916667

		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889		0.4701388889

		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111		0.4704861111

		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333		0.4708333333

		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556		0.4711805556

		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778		0.4715277778

		0.471875		0.471875		0.471875		0.471875		0.471875		0.471875		0.471875		0.471875		0.471875		0.471875

		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222		0.4722222222

		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444		0.4725694444

		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667		0.4729166667

		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889		0.4732638889

		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111		0.4736111111

		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333		0.4739583333

		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556		0.4743055556

		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778		0.4746527778

		0.475		0.475		0.475		0.475		0.475		0.475		0.475		0.475		0.475		0.475

		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222		0.4753472222

		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444		0.4756944444

		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667		0.4760416667

		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889		0.4763888889

		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111		0.4767361111

		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333		0.4770833333

		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556		0.4774305556

		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778		0.4777777778

		0.478125		0.478125		0.478125		0.478125		0.478125		0.478125		0.478125		0.478125		0.478125		0.478125

		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222		0.4784722222

		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444		0.4788194444

		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667		0.4791666667

		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889		0.4795138889

		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111		0.4798611111

		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333		0.4802083333

		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556		0.4805555556

		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778		0.4809027778

		0.48125		0.48125		0.48125		0.48125		0.48125		0.48125		0.48125		0.48125		0.48125		0.48125

		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222		0.4815972222

		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444		0.4819444444

		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667		0.4822916667

		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889		0.4826388889

		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111		0.4829861111

		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333		0.4833333333

		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556		0.4836805556

		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778		0.4840277778

		0.484375		0.484375		0.484375		0.484375		0.484375		0.484375		0.484375		0.484375		0.484375		0.484375

		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222		0.4847222222

		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444		0.4850694444

		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667		0.4854166667

		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889		0.4857638889

		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111		0.4861111111

		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333		0.4864583333

		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556		0.4868055556

		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778		0.4871527778

		0.4875		0.4875		0.4875		0.4875		0.4875		0.4875		0.4875		0.4875		0.4875		0.4875

		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222		0.4878472222

		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444		0.4881944444

		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667		0.4885416667

		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889		0.4888888889

		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111		0.4892361111

		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333		0.4895833333

		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556		0.4899305556

		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778		0.4902777778

		0.490625		0.490625		0.490625		0.490625		0.490625		0.490625		0.490625		0.490625		0.490625		0.490625

		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222		0.4909722222

		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444		0.4913194444

		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667		0.4916666667

		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889		0.4920138889

		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111		0.4923611111

		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333		0.4927083333

		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556		0.4930555556

		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778		0.4934027778

		0.49375		0.49375		0.49375		0.49375		0.49375		0.49375		0.49375		0.49375		0.49375		0.49375

		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222		0.4940972222

		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444		0.4944444444

		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667		0.4947916667

		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889		0.4951388889

		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111		0.4954861111

		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333		0.4958333333

		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556		0.4961805556

		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778		0.4965277778

		0.496875		0.496875		0.496875		0.496875		0.496875		0.496875		0.496875		0.496875		0.496875		0.496875

		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222		0.4972222222

		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444		0.4975694444

		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667		0.4979166667

		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889		0.4982638889

		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111		0.4986111111

		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333		0.4989583333

		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556		0.4993055556

		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778		0.4996527778

		0.5		0.5		0.5		0.5		0.5		0.5		0.5		0.5		0.5		0.5

		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222		0.5003472222

		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444		0.5006944444

		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667		0.5010416667

		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889		0.5013888889

		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111		0.5017361111

		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333		0.5020833333

		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556		0.5024305556

		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778		0.5027777778

		0.503125		0.503125		0.503125		0.503125		0.503125		0.503125		0.503125		0.503125		0.503125		0.503125

		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222		0.5034722222

		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444		0.5038194444

		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667		0.5041666667

		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889		0.5045138889

		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111		0.5048611111

		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333		0.5052083333

		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556		0.5055555556

		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778		0.5059027778

		0.50625		0.50625		0.50625		0.50625		0.50625		0.50625		0.50625		0.50625		0.50625		0.50625

		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222		0.5065972222

		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444		0.5069444444

		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667		0.5072916667

		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889		0.5076388889

		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111		0.5079861111

		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333		0.5083333333

		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556		0.5086805556

		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778		0.5090277778

		0.509375		0.509375		0.509375		0.509375		0.509375		0.509375		0.509375		0.509375		0.509375		0.509375

		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222		0.5097222222

		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444		0.5100694444

		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667		0.5104166667

		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889		0.5107638889

		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111		0.5111111111

		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333		0.5114583333

		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556		0.5118055556

		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778		0.5121527778

		0.5125		0.5125		0.5125		0.5125		0.5125		0.5125		0.5125		0.5125		0.5125		0.5125

		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222		0.5128472222

		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444		0.5131944444

		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667		0.5135416667

		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889		0.5138888889

		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111		0.5142361111

		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333		0.5145833333

		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556		0.5149305556

		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778		0.5152777778

		0.515625		0.515625		0.515625		0.515625		0.515625		0.515625		0.515625		0.515625		0.515625		0.515625

		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222		0.5159722222

		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444		0.5163194444

		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667		0.5166666667

		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889		0.5170138889

		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111		0.5173611111

		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333		0.5177083333

		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556		0.5180555556

		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778		0.5184027778

		0.51875		0.51875		0.51875		0.51875		0.51875		0.51875		0.51875		0.51875		0.51875		0.51875

		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222		0.5190972222

		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444		0.5194444444

		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667		0.5197916667

		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889		0.5201388889

		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111		0.5204861111

		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333		0.5208333333

		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556		0.5211805556

		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778		0.5215277778

		0.521875		0.521875		0.521875		0.521875		0.521875		0.521875		0.521875		0.521875		0.521875		0.521875

		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222		0.5222222222

		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444		0.5225694444

		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667		0.5229166667

		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889		0.5232638889

		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111		0.5236111111

		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333		0.5239583333

		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556		0.5243055556

		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778		0.5246527778

		0.525		0.525		0.525		0.525		0.525		0.525		0.525		0.525		0.525		0.525

		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222		0.5253472222

		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444		0.5256944444

		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667		0.5260416667

		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889		0.5263888889

		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111		0.5267361111

		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333		0.5270833333

		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556		0.5274305556

		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778		0.5277777778

		0.528125		0.528125		0.528125		0.528125		0.528125		0.528125		0.528125		0.528125		0.528125		0.528125

		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222		0.5284722222

		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444		0.5288194444

		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667		0.5291666667

		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889		0.5295138889

		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111		0.5298611111

		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333		0.5302083333

		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556		0.5305555556

		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778		0.5309027778

		0.53125		0.53125		0.53125		0.53125		0.53125		0.53125		0.53125		0.53125		0.53125		0.53125

		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222		0.5315972222

		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444		0.5319444444

		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667		0.5322916667

		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889		0.5326388889

		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111		0.5329861111

		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333		0.5333333333

		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556		0.5336805556

		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778		0.5340277778

		0.534375		0.534375		0.534375		0.534375		0.534375		0.534375		0.534375		0.534375		0.534375		0.534375

		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222		0.5347222222

		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444		0.5350694444

		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667		0.5354166667

		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889		0.5357638889

		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111		0.5361111111

		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333		0.5364583333

		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556		0.5368055556

		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778		0.5371527778

		0.5375		0.5375		0.5375		0.5375		0.5375		0.5375		0.5375		0.5375		0.5375		0.5375

		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222		0.5378472222

		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444		0.5381944444

		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667		0.5385416667

		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889		0.5388888889

		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111		0.5392361111

		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333		0.5395833333

		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556		0.5399305556

		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778		0.5402777778

		0.540625		0.540625		0.540625		0.540625		0.540625		0.540625		0.540625		0.540625		0.540625		0.540625

		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222		0.5409722222

		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444		0.5413194444

		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667		0.5416666667

		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889		0.5420138889

		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111		0.5423611111

		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333		0.5427083333

		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556		0.5430555556

		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778		0.5434027778

		0.54375		0.54375		0.54375		0.54375		0.54375		0.54375		0.54375		0.54375		0.54375		0.54375

		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222		0.5440972222

		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444		0.5444444444

		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667		0.5447916667

		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889		0.5451388889

		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111		0.5454861111

		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333		0.5458333333

		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556		0.5461805556

		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778		0.5465277778

		0.546875		0.546875		0.546875		0.546875		0.546875		0.546875		0.546875		0.546875		0.546875		0.546875

		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222		0.5472222222

		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444		0.5475694444

		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667		0.5479166667

		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889		0.5482638889

		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111		0.5486111111

		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333		0.5489583333

		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556		0.5493055556

		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778		0.5496527778

		0.55		0.55		0.55		0.55		0.55		0.55		0.55		0.55		0.55		0.55

		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222		0.5503472222

		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444		0.5506944444

		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667		0.5510416667

		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889		0.5513888889

		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111		0.5517361111

		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333		0.5520833333

		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556		0.5524305556

		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778		0.5527777778

		0.553125		0.553125		0.553125		0.553125		0.553125		0.553125		0.553125		0.553125		0.553125		0.553125

		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222		0.5534722222

		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444		0.5538194444

		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667		0.5541666667

		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889		0.5545138889

		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111		0.5548611111

		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333		0.5552083333

		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556		0.5555555556

		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778		0.5559027778

		0.55625		0.55625		0.55625		0.55625		0.55625		0.55625		0.55625		0.55625		0.55625		0.55625

		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222		0.5565972222

		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444		0.5569444444

		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667		0.5572916667

		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889		0.5576388889

		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111		0.5579861111

		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333		0.5583333333

		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556		0.5586805556

		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778		0.5590277778

		0.559375		0.559375		0.559375		0.559375		0.559375		0.559375		0.559375		0.559375		0.559375		0.559375

		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222		0.5597222222

		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444		0.5600694444

		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667		0.5604166667

		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889		0.5607638889

		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111		0.5611111111

		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333		0.5614583333

		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556		0.5618055556

		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778		0.5621527778

		0.5625		0.5625		0.5625		0.5625		0.5625		0.5625		0.5625		0.5625		0.5625		0.5625

		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222		0.5628472222

		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444		0.5631944444

		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667		0.5635416667

		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889		0.5638888889

		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111		0.5642361111

		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333		0.5645833333

		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556		0.5649305556

		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778		0.5652777778

		0.565625		0.565625		0.565625		0.565625		0.565625		0.565625		0.565625		0.565625		0.565625		0.565625

		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222		0.5659722222

		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444		0.5663194444

		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667		0.5666666667

		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889		0.5670138889

		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111		0.5673611111

		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333		0.5677083333

		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556		0.5680555556

		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778		0.5684027778

		0.56875		0.56875		0.56875		0.56875		0.56875		0.56875		0.56875		0.56875		0.56875		0.56875

		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222		0.5690972222

		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444		0.5694444444

		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667		0.5697916667

		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889		0.5701388889

		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111		0.5704861111

		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333		0.5708333333

		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556		0.5711805556

		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778		0.5715277778

		0.571875		0.571875		0.571875		0.571875		0.571875		0.571875		0.571875		0.571875		0.571875		0.571875

		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222		0.5722222222

		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444		0.5725694444

		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667		0.5729166667

		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889		0.5732638889

		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111		0.5736111111

		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333		0.5739583333

		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556		0.5743055556

		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778		0.5746527778

		0.575		0.575		0.575		0.575		0.575		0.575		0.575		0.575		0.575		0.575

		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222		0.5753472222

		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444		0.5756944444

		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667		0.5760416667

		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889		0.5763888889

		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111		0.5767361111

		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333		0.5770833333

		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556		0.5774305556

		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778		0.5777777778

		0.578125		0.578125		0.578125		0.578125		0.578125		0.578125		0.578125		0.578125		0.578125		0.578125

		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222		0.5784722222

		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444		0.5788194444

		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667		0.5791666667

		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889		0.5795138889

		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111		0.5798611111

		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333		0.5802083333

		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556		0.5805555556

		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778		0.5809027778

		0.58125		0.58125		0.58125		0.58125		0.58125		0.58125		0.58125		0.58125		0.58125		0.58125

		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222		0.5815972222

		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444		0.5819444444

		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667		0.5822916667

		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889		0.5826388889

		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111		0.5829861111

		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333		0.5833333333

		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556		0.5836805556

		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778		0.5840277778

		0.584375		0.584375		0.584375		0.584375		0.584375		0.584375		0.584375		0.584375		0.584375		0.584375

		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222		0.5847222222

		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444		0.5850694444

		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667		0.5854166667

		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889		0.5857638889

		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111		0.5861111111

		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333		0.5864583333

		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556		0.5868055556

		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778		0.5871527778

		0.5875		0.5875		0.5875		0.5875		0.5875		0.5875		0.5875		0.5875		0.5875		0.5875

		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222		0.5878472222

		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444		0.5881944444

		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667		0.5885416667

		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889		0.5888888889

		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111		0.5892361111

		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333		0.5895833333

		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556		0.5899305556

		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778		0.5902777778

		0.590625		0.590625		0.590625		0.590625		0.590625		0.590625		0.590625		0.590625		0.590625		0.590625

		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222		0.5909722222

		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444		0.5913194444

		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667		0.5916666667

		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889		0.5920138889

		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111		0.5923611111

		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333		0.5927083333

		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556		0.5930555556

		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778		0.5934027778

		0.59375		0.59375		0.59375		0.59375		0.59375		0.59375		0.59375		0.59375		0.59375		0.59375

		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222		0.5940972222

		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444		0.5944444444

		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667		0.5947916667

		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889		0.5951388889

		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111		0.5954861111

		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333		0.5958333333

		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556		0.5961805556

		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778		0.5965277778

		0.596875		0.596875		0.596875		0.596875		0.596875		0.596875		0.596875		0.596875		0.596875		0.596875

		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222		0.5972222222

		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444		0.5975694444

		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667		0.5979166667

		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889		0.5982638889

		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111		0.5986111111

		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333		0.5989583333

		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556		0.5993055556

		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778		0.5996527778

		0.6		0.6		0.6		0.6		0.6		0.6		0.6		0.6		0.6		0.6

		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222		0.6003472222

		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444		0.6006944444

		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667		0.6010416667

		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889		0.6013888889

		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111		0.6017361111

		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333		0.6020833333

		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556		0.6024305556

		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778		0.6027777778

		0.603125		0.603125		0.603125		0.603125		0.603125		0.603125		0.603125		0.603125		0.603125		0.603125

		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222		0.6034722222

		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444		0.6038194444

		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667		0.6041666667

		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889		0.6045138889

		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111		0.6048611111

		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333		0.6052083333

		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556		0.6055555556

		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778		0.6059027778

		0.60625		0.60625		0.60625		0.60625		0.60625		0.60625		0.60625		0.60625		0.60625		0.60625

		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222		0.6065972222

		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444		0.6069444444

		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667		0.6072916667

		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889		0.6076388889

		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111		0.6079861111

		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333		0.6083333333

		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556		0.6086805556

		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778		0.6090277778

		0.609375		0.609375		0.609375		0.609375		0.609375		0.609375		0.609375		0.609375		0.609375		0.609375

		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222		0.6097222222

		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444		0.6100694444

		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667		0.6104166667

		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889		0.6107638889

		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111		0.6111111111

		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333		0.6114583333

		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556		0.6118055556

		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778		0.6121527778

		0.6125		0.6125		0.6125		0.6125		0.6125		0.6125		0.6125		0.6125		0.6125		0.6125

		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222		0.6128472222

		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444		0.6131944444

		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667		0.6135416667

		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889		0.6138888889

		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111		0.6142361111

		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333		0.6145833333

		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556		0.6149305556

		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778		0.6152777778

		0.615625		0.615625		0.615625		0.615625		0.615625		0.615625		0.615625		0.615625		0.615625		0.615625

		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222		0.6159722222

		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444		0.6163194444

		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667		0.6166666667

		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889		0.6170138889

		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111		0.6173611111

		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333		0.6177083333

		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556		0.6180555556

		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778		0.6184027778

		0.61875		0.61875		0.61875		0.61875		0.61875		0.61875		0.61875		0.61875		0.61875		0.61875

		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222		0.6190972222

		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444		0.6194444444

		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667		0.6197916667

		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889		0.6201388889

		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111		0.6204861111

		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333		0.6208333333

		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556		0.6211805556

		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778		0.6215277778

		0.621875		0.621875		0.621875		0.621875		0.621875		0.621875		0.621875		0.621875		0.621875		0.621875

		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222		0.6222222222

		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444		0.6225694444

		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667		0.6229166667

		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889		0.6232638889

		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111		0.6236111111

		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333		0.6239583333

		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556		0.6243055556

		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778		0.6246527778

		0.625		0.625		0.625		0.625		0.625		0.625		0.625		0.625		0.625		0.625

		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222		0.6253472222

		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444		0.6256944444

		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667		0.6260416667

		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889		0.6263888889

		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111		0.6267361111

		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333		0.6270833333

		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556		0.6274305556

		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778		0.6277777778

		0.628125		0.628125		0.628125		0.628125		0.628125		0.628125		0.628125		0.628125		0.628125		0.628125

		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222		0.6284722222

		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444		0.6288194444

		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667		0.6291666667

		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889		0.6295138889

		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111		0.6298611111

		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333		0.6302083333

		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556		0.6305555556

		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778		0.6309027778

		0.63125		0.63125		0.63125		0.63125		0.63125		0.63125		0.63125		0.63125		0.63125		0.63125

		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222		0.6315972222

		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444		0.6319444444

		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667		0.6322916667

		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889		0.6326388889

		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111		0.6329861111

		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333		0.6333333333

		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556		0.6336805556

		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778		0.6340277778

		0.634375		0.634375		0.634375		0.634375		0.634375		0.634375		0.634375		0.634375		0.634375		0.634375

		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222		0.6347222222

		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444		0.6350694444

		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667		0.6354166667

		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889		0.6357638889

		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111		0.6361111111

		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333		0.6364583333

		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556		0.6368055556

		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778		0.6371527778

		0.6375		0.6375		0.6375		0.6375		0.6375		0.6375		0.6375		0.6375		0.6375		0.6375

		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222		0.6378472222

		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444		0.6381944444

		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667		0.6385416667

		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889		0.6388888889

		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111		0.6392361111

		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333		0.6395833333

		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556		0.6399305556

		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778		0.6402777778

		0.640625		0.640625		0.640625		0.640625		0.640625		0.640625		0.640625		0.640625		0.640625		0.640625

		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222		0.6409722222

		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444		0.6413194444

		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667		0.6416666667

		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889		0.6420138889

		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111		0.6423611111

		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333		0.6427083333

		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556		0.6430555556

		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778		0.6434027778

		0.64375		0.64375		0.64375		0.64375		0.64375		0.64375		0.64375		0.64375		0.64375		0.64375

		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222		0.6440972222

		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444		0.6444444444

		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667		0.6447916667

		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889		0.6451388889

		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111		0.6454861111

		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333		0.6458333333

		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556		0.6461805556

		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778		0.6465277778

		0.646875		0.646875		0.646875		0.646875		0.646875		0.646875		0.646875		0.646875		0.646875		0.646875

		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222		0.6472222222

		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444		0.6475694444

		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667		0.6479166667

		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889		0.6482638889

		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111		0.6486111111

		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333		0.6489583333

		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556		0.6493055556

		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778		0.6496527778

		0.65		0.65		0.65		0.65		0.65		0.65		0.65		0.65		0.65		0.65

		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222		0.6503472222

		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444		0.6506944444

		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667		0.6510416667

		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889		0.6513888889

		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111		0.6517361111

		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333		0.6520833333

		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556		0.6524305556

		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778		0.6527777778

		0.653125		0.653125		0.653125		0.653125		0.653125		0.653125		0.653125		0.653125		0.653125		0.653125

		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222		0.6534722222

		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444		0.6538194444

		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667		0.6541666667

		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889		0.6545138889

		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111		0.6548611111

		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333		0.6552083333

		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556		0.6555555556

		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778		0.6559027778

		0.65625		0.65625		0.65625		0.65625		0.65625		0.65625		0.65625		0.65625		0.65625		0.65625

		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222		0.6565972222

		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444		0.6569444444

		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667		0.6572916667

		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889		0.6576388889

		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111		0.6579861111

		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333		0.6583333333

		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556		0.6586805556

		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778		0.6590277778

		0.659375		0.659375		0.659375		0.659375		0.659375		0.659375		0.659375		0.659375		0.659375		0.659375

		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222		0.6597222222

		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444		0.6600694444

		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667		0.6604166667

		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889		0.6607638889

		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111		0.6611111111

		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333		0.6614583333

		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556		0.6618055556

		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778		0.6621527778

		0.6625		0.6625		0.6625		0.6625		0.6625		0.6625		0.6625		0.6625		0.6625		0.6625

		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222		0.6628472222

		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444		0.6631944444

		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667		0.6635416667

		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889		0.6638888889

		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111		0.6642361111

		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333		0.6645833333

		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556		0.6649305556

		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778		0.6652777778

		0.665625		0.665625		0.665625		0.665625		0.665625		0.665625		0.665625		0.665625		0.665625		0.665625

		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222		0.6659722222

		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444		0.6663194444

		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667		0.6666666667

		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889		0.6670138889

		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111		0.6673611111

		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333		0.6677083333

		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556		0.6680555556

		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778		0.6684027778

		0.66875		0.66875		0.66875		0.66875		0.66875		0.66875		0.66875		0.66875		0.66875		0.66875

		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222		0.6690972222

		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444		0.6694444444

		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667		0.6697916667

		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889		0.6701388889

		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111		0.6704861111

		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333		0.6708333333

		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556		0.6711805556

		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778		0.6715277778

		0.671875		0.671875		0.671875		0.671875		0.671875		0.671875		0.671875		0.671875		0.671875		0.671875

		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222		0.6722222222

		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444		0.6725694444

		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667		0.6729166667

		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889		0.6732638889

		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111		0.6736111111

		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333		0.6739583333

		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556		0.6743055556

		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778		0.6746527778

		0.675		0.675		0.675		0.675		0.675		0.675		0.675		0.675		0.675		0.675

		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222		0.6753472222

		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444		0.6756944444

		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667		0.6760416667

		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889		0.6763888889

		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111		0.6767361111

		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333		0.6770833333

		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556		0.6774305556

		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778		0.6777777778

		0.678125		0.678125		0.678125		0.678125		0.678125		0.678125		0.678125		0.678125		0.678125		0.678125

		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222		0.6784722222

		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444		0.6788194444

		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667		0.6791666667

		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889		0.6795138889

		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111		0.6798611111

		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333		0.6802083333

		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556		0.6805555556

		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778		0.6809027778

		0.68125		0.68125		0.68125		0.68125		0.68125		0.68125		0.68125		0.68125		0.68125		0.68125

		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222		0.6815972222

		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444		0.6819444444

		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667		0.6822916667

		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889		0.6826388889

		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111		0.6829861111

		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333		0.6833333333

		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556		0.6836805556

		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778		0.6840277778

		0.684375		0.684375		0.684375		0.684375		0.684375		0.684375		0.684375		0.684375		0.684375		0.684375

		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222		0.6847222222

		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444		0.6850694444

		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667		0.6854166667

		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889		0.6857638889

		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111		0.6861111111

		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333		0.6864583333

		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556		0.6868055556

		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778		0.6871527778

		0.6875		0.6875		0.6875		0.6875		0.6875		0.6875		0.6875		0.6875		0.6875		0.6875

		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222		0.6878472222

		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444		0.6881944444

		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667		0.6885416667

		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889		0.6888888889

		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111		0.6892361111

		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333		0.6895833333

		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556		0.6899305556

		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778		0.6902777778

		0.690625		0.690625		0.690625		0.690625		0.690625		0.690625		0.690625		0.690625		0.690625		0.690625

		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222		0.6909722222

		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444		0.6913194444

		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667		0.6916666667

		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889		0.6920138889

		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111		0.6923611111

		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333		0.6927083333

		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556		0.6930555556

		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778		0.6934027778

		0.69375		0.69375		0.69375		0.69375		0.69375		0.69375		0.69375		0.69375		0.69375		0.69375

		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222		0.6940972222

		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444		0.6944444444

		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667		0.6947916667

		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889		0.6951388889

		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111		0.6954861111

		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333		0.6958333333

		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556		0.6961805556

		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778		0.6965277778

		0.696875		0.696875		0.696875		0.696875		0.696875		0.696875		0.696875		0.696875		0.696875		0.696875

		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222		0.6972222222

		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444		0.6975694444

		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667		0.6979166667

		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889		0.6982638889

		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111		0.6986111111

		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333		0.6989583333

		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556		0.6993055556

		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778		0.6996527778

		0.7		0.7		0.7		0.7		0.7		0.7		0.7		0.7		0.7		0.7

		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222		0.7003472222

		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444		0.7006944444

		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667		0.7010416667

		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889		0.7013888889

		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111		0.7017361111

		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333		0.7020833333

		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556		0.7024305556

		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778		0.7027777778

		0.703125		0.703125		0.703125		0.703125		0.703125		0.703125		0.703125		0.703125		0.703125		0.703125

		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222		0.7034722222

		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444		0.7038194444

		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667		0.7041666667

		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889		0.7045138889

		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111		0.7048611111

		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333		0.7052083333

		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556		0.7055555556

		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778		0.7059027778

		0.70625		0.70625		0.70625		0.70625		0.70625		0.70625		0.70625		0.70625		0.70625		0.70625

		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222		0.7065972222

		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444		0.7069444444

		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667		0.7072916667

		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889		0.7076388889

		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111		0.7079861111

		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333		0.7083333333

		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556		0.7086805556

		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778		0.7090277778

		0.709375		0.709375		0.709375		0.709375		0.709375		0.709375		0.709375		0.709375		0.709375		0.709375

		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222		0.7097222222

		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444		0.7100694444

		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667		0.7104166667

		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889		0.7107638889

		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111		0.7111111111

		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333		0.7114583333

		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556		0.7118055556

		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778		0.7121527778

		0.7125		0.7125		0.7125		0.7125		0.7125		0.7125		0.7125		0.7125		0.7125		0.7125

		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222		0.7128472222

		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444		0.7131944444

		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667		0.7135416667

		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889		0.7138888889

		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111		0.7142361111

		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333		0.7145833333

		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556		0.7149305556

		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778		0.7152777778

		0.715625		0.715625		0.715625		0.715625		0.715625		0.715625		0.715625		0.715625		0.715625		0.715625

		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222		0.7159722222

		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444		0.7163194444

		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667		0.7166666667

		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889		0.7170138889

		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111		0.7173611111

		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333		0.7177083333

		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556		0.7180555556

		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778		0.7184027778

		0.71875		0.71875		0.71875		0.71875		0.71875		0.71875		0.71875		0.71875		0.71875		0.71875

		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222		0.7190972222

		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444		0.7194444444

		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667		0.7197916667

		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889		0.7201388889

		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111		0.7204861111

		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333		0.7208333333

		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556		0.7211805556

		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778		0.7215277778

		0.721875		0.721875		0.721875		0.721875		0.721875		0.721875		0.721875		0.721875		0.721875		0.721875

		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222		0.7222222222

		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444		0.7225694444

		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667		0.7229166667

		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889		0.7232638889

		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111		0.7236111111

		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333		0.7239583333

		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556		0.7243055556

		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778		0.7246527778

		0.725		0.725		0.725		0.725		0.725		0.725		0.725		0.725		0.725		0.725

		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222		0.7253472222

		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444		0.7256944444

		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667		0.7260416667

		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889		0.7263888889

		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111		0.7267361111

		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333		0.7270833333

		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556		0.7274305556

		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778		0.7277777778

		0.728125		0.728125		0.728125		0.728125		0.728125		0.728125		0.728125		0.728125		0.728125		0.728125

		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222		0.7284722222

		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444		0.7288194444

		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667		0.7291666667

		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889		0.7295138889

		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111		0.7298611111

		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333		0.7302083333

		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556		0.7305555556

		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778		0.7309027778

		0.73125		0.73125		0.73125		0.73125		0.73125		0.73125		0.73125		0.73125		0.73125		0.73125

		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222		0.7315972222

		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444		0.7319444444

		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667		0.7322916667

		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889		0.7326388889

		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111		0.7329861111

		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333		0.7333333333

		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556		0.7336805556

		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778		0.7340277778

		0.734375		0.734375		0.734375		0.734375		0.734375		0.734375		0.734375		0.734375		0.734375		0.734375

		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222		0.7347222222

		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444		0.7350694444

		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667		0.7354166667

		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889		0.7357638889

		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111		0.7361111111

		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333		0.7364583333

		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556		0.7368055556

		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778		0.7371527778

		0.7375		0.7375		0.7375		0.7375		0.7375		0.7375		0.7375		0.7375		0.7375		0.7375

		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222		0.7378472222

		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444		0.7381944444

		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667		0.7385416667

		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889		0.7388888889

		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111		0.7392361111

		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333		0.7395833333

		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556		0.7399305556

		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778		0.7402777778

		0.740625		0.740625		0.740625		0.740625		0.740625		0.740625		0.740625		0.740625		0.740625		0.740625

		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222		0.7409722222

		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444		0.7413194444

		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667		0.7416666667

		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889		0.7420138889

		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111		0.7423611111

		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333		0.7427083333

		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556		0.7430555556

		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778		0.7434027778

		0.74375		0.74375		0.74375		0.74375		0.74375		0.74375		0.74375		0.74375		0.74375		0.74375

		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222		0.7440972222

		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444		0.7444444444

		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667		0.7447916667

		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889		0.7451388889

		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111		0.7454861111

		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333		0.7458333333

		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556		0.7461805556

		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778		0.7465277778

		0.746875		0.746875		0.746875		0.746875		0.746875		0.746875		0.746875		0.746875		0.746875		0.746875

		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222		0.7472222222

		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444		0.7475694444

		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667		0.7479166667

		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889		0.7482638889

		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111		0.7486111111

		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333		0.7489583333

		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556		0.7493055556

		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778		0.7496527778

		0.75		0.75		0.75		0.75		0.75		0.75		0.75		0.75		0.75		0.75

		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222		0.7503472222

		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444		0.7506944444

		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667		0.7510416667

		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889		0.7513888889

		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111		0.7517361111

		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333		0.7520833333

		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556		0.7524305556

		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778		0.7527777778

		0.753125		0.753125		0.753125		0.753125		0.753125		0.753125		0.753125		0.753125		0.753125		0.753125

		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222		0.7534722222

		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444		0.7538194444

		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667		0.7541666667

		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889		0.7545138889

		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111		0.7548611111

		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333		0.7552083333

		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556		0.7555555556

		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778		0.7559027778

		0.75625		0.75625		0.75625		0.75625		0.75625		0.75625		0.75625		0.75625		0.75625		0.75625

		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222		0.7565972222

		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444		0.7569444444

		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667		0.7572916667

		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889		0.7576388889

		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111		0.7579861111

		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333		0.7583333333

		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556		0.7586805556

		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778		0.7590277778

		0.759375		0.759375		0.759375		0.759375		0.759375		0.759375		0.759375		0.759375		0.759375		0.759375

		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222		0.7597222222

		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444		0.7600694444

		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667		0.7604166667

		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889		0.7607638889

		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111		0.7611111111

		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333		0.7614583333

		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556		0.7618055556

		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778		0.7621527778

		0.7625		0.7625		0.7625		0.7625		0.7625		0.7625		0.7625		0.7625		0.7625		0.7625

		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222		0.7628472222

		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444		0.7631944444

		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667		0.7635416667

		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889		0.7638888889

		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111		0.7642361111

		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333		0.7645833333

		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556		0.7649305556

		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778		0.7652777778

		0.765625		0.765625		0.765625		0.765625		0.765625		0.765625		0.765625		0.765625		0.765625		0.765625

		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222		0.7659722222

		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444		0.7663194444

		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667		0.7666666667

		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889		0.7670138889

		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111		0.7673611111

		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333		0.7677083333

		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556		0.7680555556

		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778		0.7684027778

		0.76875		0.76875		0.76875		0.76875		0.76875		0.76875		0.76875		0.76875		0.76875		0.76875

		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222		0.7690972222

		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444		0.7694444444

		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667		0.7697916667

		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889		0.7701388889

		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111		0.7704861111

		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333		0.7708333333

		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556		0.7711805556

		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778		0.7715277778

		0.771875		0.771875		0.771875		0.771875		0.771875		0.771875		0.771875		0.771875		0.771875		0.771875

		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222		0.7722222222

		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444		0.7725694444

		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667		0.7729166667

		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889		0.7732638889

		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111		0.7736111111

		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333		0.7739583333

		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556		0.7743055556

		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778		0.7746527778

		0.775		0.775		0.775		0.775		0.775		0.775		0.775		0.775		0.775		0.775

		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222		0.7753472222

		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444		0.7756944444

		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667		0.7760416667

		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889		0.7763888889

		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111		0.7767361111

		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333		0.7770833333

		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556		0.7774305556

		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778		0.7777777778

		0.778125		0.778125		0.778125		0.778125		0.778125		0.778125		0.778125		0.778125		0.778125		0.778125

		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222		0.7784722222

		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444		0.7788194444

		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667		0.7791666667

		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889		0.7795138889

		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111		0.7798611111

		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333		0.7802083333

		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556		0.7805555556

		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778		0.7809027778

		0.78125		0.78125		0.78125		0.78125		0.78125		0.78125		0.78125		0.78125		0.78125		0.78125

		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222		0.7815972222

		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444		0.7819444444

		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667		0.7822916667

		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889		0.7826388889

		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111		0.7829861111

		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333		0.7833333333

		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556		0.7836805556

		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778		0.7840277778

		0.784375		0.784375		0.784375		0.784375		0.784375		0.784375		0.784375		0.784375		0.784375		0.784375

		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222		0.7847222222

		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444		0.7850694444

		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667		0.7854166667

		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889		0.7857638889

		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111		0.7861111111

		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333		0.7864583333

		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556		0.7868055556

		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778		0.7871527778

		0.7875		0.7875		0.7875		0.7875		0.7875		0.7875		0.7875		0.7875		0.7875		0.7875

		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222		0.7878472222

		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444		0.7881944444

		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667		0.7885416667

		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889		0.7888888889

		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111		0.7892361111

		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333		0.7895833333

		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556		0.7899305556

		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778		0.7902777778

		0.790625		0.790625		0.790625		0.790625		0.790625		0.790625		0.790625		0.790625		0.790625		0.790625

		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222		0.7909722222

		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444		0.7913194444

		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667		0.7916666667

		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889		0.7920138889

		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111		0.7923611111

		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333		0.7927083333

		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556		0.7930555556

		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778		0.7934027778

		0.79375		0.79375		0.79375		0.79375		0.79375		0.79375		0.79375		0.79375		0.79375		0.79375

		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222		0.7940972222

		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444		0.7944444444

		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667		0.7947916667

		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889		0.7951388889

		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111		0.7954861111

		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333		0.7958333333

		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556		0.7961805556

		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778		0.7965277778

		0.796875		0.796875		0.796875		0.796875		0.796875		0.796875		0.796875		0.796875		0.796875		0.796875

		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222		0.7972222222

		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444		0.7975694444

		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667		0.7979166667

		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889		0.7982638889

		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111		0.7986111111

		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333		0.7989583333

		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556		0.7993055556

		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778		0.7996527778

		0.8		0.8		0.8		0.8		0.8		0.8		0.8		0.8		0.8		0.8

		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222		0.8003472222

		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444		0.8006944444

		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667		0.8010416667

		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889		0.8013888889

		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111		0.8017361111

		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333		0.8020833333

		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556		0.8024305556

		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778		0.8027777778

		0.803125		0.803125		0.803125		0.803125		0.803125		0.803125		0.803125		0.803125		0.803125		0.803125

		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222		0.8034722222

		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444		0.8038194444

		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667		0.8041666667

		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889		0.8045138889

		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111		0.8048611111

		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333		0.8052083333

		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556		0.8055555556

		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778		0.8059027778

		0.80625		0.80625		0.80625		0.80625		0.80625		0.80625		0.80625		0.80625		0.80625		0.80625

		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222		0.8065972222

		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444		0.8069444444

		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667		0.8072916667

		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889		0.8076388889

		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111		0.8079861111

		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333		0.8083333333

		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556		0.8086805556

		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778		0.8090277778

		0.809375		0.809375		0.809375		0.809375		0.809375		0.809375		0.809375		0.809375		0.809375		0.809375

		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222		0.8097222222

		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444		0.8100694444

		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667		0.8104166667

		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889		0.8107638889

		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111		0.8111111111

		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333		0.8114583333

		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556		0.8118055556

		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778		0.8121527778

		0.8125		0.8125		0.8125		0.8125		0.8125		0.8125		0.8125		0.8125		0.8125		0.8125

		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222		0.8128472222

		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444		0.8131944444

		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667		0.8135416667

		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889		0.8138888889

		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111		0.8142361111

		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333		0.8145833333

		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556		0.8149305556

		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778		0.8152777778

		0.815625		0.815625		0.815625		0.815625		0.815625		0.815625		0.815625		0.815625		0.815625		0.815625

		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222		0.8159722222

		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444		0.8163194444

		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667		0.8166666667

		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889		0.8170138889

		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111		0.8173611111

		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333		0.8177083333

		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556		0.8180555556

		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778		0.8184027778

		0.81875		0.81875		0.81875		0.81875		0.81875		0.81875		0.81875		0.81875		0.81875		0.81875

		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222		0.8190972222

		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444		0.8194444444

		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667		0.8197916667

		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889		0.8201388889

		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111		0.8204861111

		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333		0.8208333333

		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556		0.8211805556

		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778		0.8215277778

		0.821875		0.821875		0.821875		0.821875		0.821875		0.821875		0.821875		0.821875		0.821875		0.821875

		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222		0.8222222222

		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444		0.8225694444

		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667		0.8229166667

		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889		0.8232638889

		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111		0.8236111111

		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333		0.8239583333

		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556		0.8243055556

		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778		0.8246527778

		0.825		0.825		0.825		0.825		0.825		0.825		0.825		0.825		0.825		0.825

		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222		0.8253472222

		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444		0.8256944444

		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667		0.8260416667

		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889		0.8263888889

		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111		0.8267361111

		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333		0.8270833333

		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556		0.8274305556

		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778		0.8277777778

		0.828125		0.828125		0.828125		0.828125		0.828125		0.828125		0.828125		0.828125		0.828125		0.828125

		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222		0.8284722222

		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444		0.8288194444

		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667		0.8291666667

		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889		0.8295138889

		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111		0.8298611111

		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333		0.8302083333

		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556		0.8305555556

		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778		0.8309027778

		0.83125		0.83125		0.83125		0.83125		0.83125		0.83125		0.83125		0.83125		0.83125		0.83125

		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222		0.8315972222

		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444		0.8319444444

		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667		0.8322916667

		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889		0.8326388889

		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111		0.8329861111

		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333		0.8333333333

		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556		0.8336805556

		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778		0.8340277778

		0.834375		0.834375		0.834375		0.834375		0.834375		0.834375		0.834375		0.834375		0.834375		0.834375

		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222		0.8347222222

		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444		0.8350694444

		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667		0.8354166667

		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889		0.8357638889

		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111		0.8361111111

		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333		0.8364583333

		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556		0.8368055556

		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778		0.8371527778

		0.8375		0.8375		0.8375		0.8375		0.8375		0.8375		0.8375		0.8375		0.8375		0.8375

		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222		0.8378472222

		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444		0.8381944444

		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667		0.8385416667

		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889		0.8388888889

		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111		0.8392361111

		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333		0.8395833333

		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556		0.8399305556

		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778		0.8402777778

		0.840625		0.840625		0.840625		0.840625		0.840625		0.840625		0.840625		0.840625		0.840625		0.840625

		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222		0.8409722222

		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444		0.8413194444

		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667		0.8416666667

		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463		0.842025463

		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852		0.8423726852

		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074		0.8427199074

		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296		0.8430671296

		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519		0.8434143519

		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741		0.8437615741

		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963		0.8441087963

		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185		0.8444560185

		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407		0.8448032407

		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463		0.845150463

		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852		0.8454976852

		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074		0.8458449074

		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296		0.8461921296

		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519		0.8465393519

		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741		0.8468865741

		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963		0.8472337963

		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185		0.8475810185

		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407		0.8479282407

		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463		0.848275463

		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852		0.8486226852

		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074		0.8489699074

		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296		0.8493171296

		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519		0.8496643519

		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741		0.8500115741

		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963		0.8503587963

		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185		0.8507060185

		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407		0.8510532407

		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463		0.851400463

		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852		0.8517476852

		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074		0.8520949074

		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556		0.8524305556

		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778		0.8527777778

		0.853125		0.853125		0.853125		0.853125		0.853125		0.853125		0.853125		0.853125		0.853125		0.853125

		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222		0.8534722222

		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444		0.8538194444

		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667		0.8541666667

		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889		0.8545138889

		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111		0.8548611111

		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333		0.8552083333

		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556		0.8555555556

		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778		0.8559027778

		0.85625		0.85625		0.85625		0.85625		0.85625		0.85625		0.85625		0.85625		0.85625		0.85625

		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222		0.8565972222

		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444		0.8569444444

		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667		0.8572916667

		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889		0.8576388889

		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111		0.8579861111

		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333		0.8583333333

		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556		0.8586805556

		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778		0.8590277778

		0.859375		0.859375		0.859375		0.859375		0.859375		0.859375		0.859375		0.859375		0.859375		0.859375

		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222		0.8597222222

		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444		0.8600694444

		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667		0.8604166667

		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889		0.8607638889

		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111		0.8611111111

		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333		0.8614583333

		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556		0.8618055556

		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778		0.8621527778

		0.8625		0.8625		0.8625		0.8625		0.8625		0.8625		0.8625		0.8625		0.8625		0.8625

		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222		0.8628472222

		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444		0.8631944444

		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667		0.8635416667

		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889		0.8638888889

		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111		0.8642361111

		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333		0.8645833333

		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556		0.8649305556

		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778		0.8652777778

		0.865625		0.865625		0.865625		0.865625		0.865625		0.865625		0.865625		0.865625		0.865625		0.865625

		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222		0.8659722222

		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444		0.8663194444

		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667		0.8666666667

		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889		0.8670138889

		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111		0.8673611111

		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333		0.8677083333

		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556		0.8680555556

		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778		0.8684027778

		0.86875		0.86875		0.86875		0.86875		0.86875		0.86875		0.86875		0.86875		0.86875		0.86875

		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222		0.8690972222

		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444		0.8694444444

		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667		0.8697916667

		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889		0.8701388889

		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111		0.8704861111

		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333		0.8708333333

		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556		0.8711805556

		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778		0.8715277778

		0.871875		0.871875		0.871875		0.871875		0.871875		0.871875		0.871875		0.871875		0.871875		0.871875

		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222		0.8722222222

		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444		0.8725694444

		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667		0.8729166667

		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889		0.8732638889

		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111		0.8736111111

		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333		0.8739583333

		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556		0.8743055556

		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778		0.8746527778

		0.875		0.875		0.875		0.875		0.875		0.875		0.875		0.875		0.875		0.875

		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222		0.8753472222

		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444		0.8756944444

		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667		0.8760416667

		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889		0.8763888889

		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111		0.8767361111

		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333		0.8770833333

		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556		0.8774305556

		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778		0.8777777778

		0.878125		0.878125		0.878125		0.878125		0.878125		0.878125		0.878125		0.878125		0.878125		0.878125

		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222		0.8784722222

		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444		0.8788194444

		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667		0.8791666667

		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889		0.8795138889

		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111		0.8798611111

		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333		0.8802083333

		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556		0.8805555556

		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778		0.8809027778

		0.88125		0.88125		0.88125		0.88125		0.88125		0.88125		0.88125		0.88125		0.88125		0.88125

		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222		0.8815972222

		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444		0.8819444444

		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667		0.8822916667

		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889		0.8826388889

		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111		0.8829861111

		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333		0.8833333333

		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556		0.8836805556

		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778		0.8840277778

		0.884375		0.884375		0.884375		0.884375		0.884375		0.884375		0.884375		0.884375		0.884375		0.884375

		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222		0.8847222222

		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444		0.8850694444

		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667		0.8854166667

		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889		0.8857638889

		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111		0.8861111111

		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333		0.8864583333

		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556		0.8868055556

		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778		0.8871527778

		0.8875		0.8875		0.8875		0.8875		0.8875		0.8875		0.8875		0.8875		0.8875		0.8875

		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222		0.8878472222

		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444		0.8881944444

		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667		0.8885416667

		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889		0.8888888889

		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111		0.8892361111

		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333		0.8895833333

		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556		0.8899305556

		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778		0.8902777778

		0.890625		0.890625		0.890625		0.890625		0.890625		0.890625		0.890625		0.890625		0.890625		0.890625

		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222		0.8909722222

		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444		0.8913194444

		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667		0.8916666667

		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889		0.8920138889

		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111		0.8923611111

		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333		0.8927083333

		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556		0.8930555556

		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778		0.8934027778

		0.89375		0.89375		0.89375		0.89375		0.89375		0.89375		0.89375		0.89375		0.89375		0.89375

		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222		0.8940972222

		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444		0.8944444444

		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667		0.8947916667

		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889		0.8951388889

		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111		0.8954861111

		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333		0.8958333333

		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556		0.8961805556

		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778		0.8965277778

		0.896875		0.896875		0.896875		0.896875		0.896875		0.896875		0.896875		0.896875		0.896875		0.896875

		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222		0.8972222222

		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444		0.8975694444

		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667		0.8979166667

		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889		0.8982638889

		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111		0.8986111111
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4.33

3.95

3.94

3.94

3.93

3.92

3.93

3.94

3.92

14.9840916667

4.33

3.95

3.94

3.94

3.93

3.92

3.93

3.94

3.92

15.019925

4.3

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.0563416667

4.37

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.092425

4.33

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.1285083333

4.33

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.1643416667

4.3

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.200175

4.3

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.2362583333

4.33

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.2720916667

4.3

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.308175

4.33

3.95

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.3440083333

4.3

3.94

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.3800916667

4.33

3.94

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.416175

4.33

3.94

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.4520083333

4.3

3.94

3.94

3.94

3.92

3.92

3.93

3.94

3.92

15.4880916667

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.92

15.524175

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.92

15.5602583333

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.92

15.5963416667

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.92

15.632175

4.3

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.92

15.6685916667

4.37

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.91

15.704425

4.3

3.94

3.94

3.94

3.92

3.92

3.92

3.94

3.91

15.7405083333

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.93

3.91

15.7765916667

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.93

3.91

15.812675

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.93

3.91

15.8487583333

4.33

3.94

3.94

3.94

3.92

3.92

3.92

3.93

3.91

15.8848416667

4.33

3.94

3.94

3.93

3.92

3.92

3.92

3.93

3.91

15.920925

4.33

3.94

3.94

3.93

3.92

3.92

3.92

3.93

3.91

15.9570083333

4.33

3.94

3.94

3.93

3.92

3.92

3.92

3.93

3.91

15.9928416667

4.3

3.94

3.94

3.93

3.92

3.92

3.92

3.93

3.91

16.028925

4.33

3.94

3.94

3.93

3.92

3.92

3.92

3.93

3.91

16.0650083333

4.33

3.94

3.94

3.93

3.92

3.91

3.92

3.93

3.91

16.1008416667

4.3

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.136925

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.1730083333

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.2090916667

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.244925

4.3

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.2813416667

4.37

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.317425

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.3538416667

4.37

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.389925

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.4260083333

4.33

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.4618416667

4.3

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.4982583333

4.37

3.94

3.93

3.93

3.91

3.91

3.92

3.93

3.91

16.5340916667

4.3

3.93

3.93

3.93

3.91

3.91

3.92

3.92

3.91

16.570175

4.33

3.93

3.93

3.93

3.91

3.91

3.92

3.92

3.91

16.6062583333

4.33

3.93

3.93

3.93

3.91

3.91

3.92

3.92

3.91

16.6423416667

4.33

3.93

3.93

3.93

3.91

3.91

3.91

3.92

3.91

16.678425

4.33

3.93

3.93

3.93

3.91

3.91

3.91

3.92

3.91

16.7145083333

4.33

3.93

3.93

3.93

3.91

3.91

3.91

3.92

3.91

16.7503416667

4.3

3.93

3.93

3.92

3.91

3.91

3.91

3.92

3.9

16.7867583333

4.37

3.93

3.93

3.92

3.91

3.91

3.91

3.92

3.9

16.8228416667

4.33

3.93

3.93

3.92

3.91

3.91

3.91

3.92

3.9

16.858925

4.33

3.93

3.93

3.92

3.91

3.91

3.91

3.92

3.9

16.8950083333

4.33

3.93

3.93

3.92

3.91

3.91

3.91

3.92

3.9

16.9310916667

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

16.967175

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

17.0032583333

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

17.0393416667

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

17.075425

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

17.1115083333

4.33

3.93

3.92

3.92

3.91

3.91

3.91

3.92

3.9

17.1475916667

4.33

3.93

3.92

3.92

3.91

3.9

3.91

3.92

3.9

17.183675

4.33

3.93

3.92

3.92

3.91

3.9

3.91

3.92

3.9

17.2197583333

4.33

3.93

3.92

3.92

3.91

3.9

3.91

3.92

3.9

17.2558416667

4.33

3.93

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.2922583333

4.37

3.93

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.3283416667

4.33

3.93

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.364175

4.3

3.93

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.4002583333

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.4363416667

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.9

17.472425

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.5085083333

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.5445916667

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.580675

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.6167583333

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.6528416667

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.688925

4.33

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.7253416667

4.37

3.92

3.92

3.92

3.9

3.9

3.91

3.92

3.89

17.7620916667

4.41

3.92

3.92

3.92

3.9

3.9

3.9

3.91

3.89

17.798175

4.33

3.92

3.92

3.92

3.9

3.9

3.9

3.91

3.89

17.8342583333

4.33

3.92

3.92

3.92

3.9

3.9

3.9

3.91

3.89

17.8703416667

4.33

3.92

3.92

3.92

3.9

3.9

3.9

3.91

3.89

17.906425

4.33

3.92

3.92

3.92

3.9

3.89

3.9

3.91

3.89

17.9425083333

4.33

3.92

3.92

3.92

3.9

3.89

3.9

3.91

3.89

17.9785916667

4.33

3.92

3.92

3.91

3.9

3.89

3.9

3.91

3.89

18.014675

4.33

3.92

3.92

3.91

3.89

3.89

3.9

3.91

3.89

18.0507583333

4.33

3.92

3.92

3.91

3.89

3.89

3.9

3.91

3.89

18.0868416667

4.33

3.92

3.92

3.91

3.89

3.89

3.9

3.91

3.89

18.122925

4.33

3.92

3.92

3.91

3.89

3.89

3.9

3.91

3.89

18.1590083333

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.1950916667

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.231175

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.2672583333

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.3033416667

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.339425

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.3755083333

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.4115916667

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.447425

4.3

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.4835083333

4.33

3.92

3.91

3.91

3.89

3.89

3.9

3.91

3.89

18.5195916667

4.33

3.92

3.91

3.91

3.89

3.89

3.89

3.91

3.89

18.555675

4.33

3.92

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.5917583333

4.33

3.92

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.6278416667

4.33

3.92

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.663925

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.7000083333

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.7360916667

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.772175

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.8082583333

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.8443416667

4.33

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.880175

4.3

3.91

3.91

3.91

3.89

3.89

3.89

3.91

3.88

18.9162583333

4.33

3.91

3.91

3.91

3.89

3.88

3.89

3.91

3.88

18.952675

4.37

3.91

3.91

3.91

3.89

3.88

3.89

3.9

3.88

18.9885083333

4.3

3.91

3.91

3.91

3.89

3.88

3.89

3.9

3.88

19.0243416667

4.3

3.91

3.91

3.91

3.89

3.88

3.89

3.9

3.88

19.060425

4.33

3.91

3.91

3.91

3.89

3.88

3.89

3.9

3.88

19.0965083333

4.33

3.91

3.91

3.91

3.89

3.88

3.89

3.9

3.88

19.1325916667

4.33

3.91

3.91

3.91

3.88

3.88

3.89

3.9

3.88

19.168675

4.33

3.91

3.91

3.91

3.88

3.88

3.89

3.9

3.88

19.2047583333

4.33

3.91

3.91

3.91

3.88

3.88

3.89

3.9

3.88

19.2408416667

4.33

3.91

3.91

3.91

3.88

3.88

3.89

3.9

3.88

19.276675

4.3

3.91

3.91

3.9

3.88

3.88

3.89

3.9

3.87

19.3127583333

4.33

3.91

3.91

3.9

3.88

3.88

3.89

3.9

3.87

19.3488416667

4.33

3.91

3.91

3.9

3.88

3.88

3.89

3.9

3.87

19.384925

4.33

3.91

3.91

3.9

3.88

3.88

3.89

3.9

3.87

19.4210083333

4.33

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.4570916667

4.33

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.493175

4.33

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.5290083333

4.3

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.5650916667

4.33

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.601175

4.33

3.91

3.9

3.9

3.88

3.88

3.89

3.9

3.87

19.6372583333

4.33

3.91

3.9

3.9

3.88

3.87

3.89

3.9

3.87

19.6733416667

4.33

3.91

3.9

3.9

3.88

3.87

3.88

3.9

3.87

19.7097583333

4.37

3.91

3.9

3.9

3.88

3.87

3.88

3.9

3.87

19.7458416667

4.33

3.91

3.9

3.9

3.88

3.87

3.88

3.89

3.87

19.781925

4.33

3.91

3.9

3.9

3.88

3.87

3.88

3.89

3.87

19.8180083333

4.33

3.91

3.9

3.9

3.88

3.87

3.88

3.89

3.87

19.8540916667

4.33

3.91

3.9

3.9

3.87

3.87

3.88

3.89

3.87

19.890175

4.33

3.91

3.9

3.9

3.87

3.87

3.88

3.89

3.87

19.9262583333

4.33

3.9

3.9

3.9

3.87

3.87

3.88

3.89

3.87

19.9623416667

4.33

3.9

3.9

3.9

3.87

3.87

3.88

3.89

3.87

19.998425

4.33

3.9

3.9

3.9

3.87

3.87

3.88

3.89

3.87

20.0345083333

4.33

3.9

3.9

3.9

3.87

3.87

3.88

3.89

3.87

20.0705916667

4.33

3.9

3.9

3.9

3.87

3.87

3.88

3.89

3.87

20.106425

4.3

3.9

3.9

3.89

3.87

3.87

3.88

3.89

3.87

20.1428416667

4.37

3.9

3.9

3.89

3.87

3.87

3.88

3.89

3.87

20.178925

4.33

3.9

3.9

3.89

3.87

3.87

3.88

3.89

3.87

20.2150083333

4.33

3.9

3.89

3.89

3.87

3.87

3.88

3.89

3.87

20.2510916667

4.33

3.9

3.89

3.89

3.87

3.87

3.88

3.89

3.87

20.287175

4.33

3.9

3.89

3.89

3.87

3.87

3.88

3.89

3.87

20.3230083333

4.3

3.9

3.89

3.89

3.87

3.87

3.88

3.89

3.87

20.3588416667

4.3

3.9

3.89

3.89

3.87

3.87

3.88

3.89

3.86

20.394925

4.33

3.9

3.89

3.89

3.87
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22.774675
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24.0005916667

4.33

3.86

3.86

3.86

3.83

3.83

3.84

3.85

3.83

24.036675

4.33

3.86

3.86

3.86

3.83

3.83

3.84

3.85

3.83

24.0725083333

4.3

3.86

3.86

3.86

3.83

3.83

3.84

3.85

3.83

24.1085916667

4.33

3.86

3.86

3.86

3.83

3.83

3.84

3.85

3.83

24.144675

4.33

3.86

3.86

3.85

3.83

3.83

3.84

3.85

3.83

24.1805083333

4.3

3.86

3.86

3.85

3.83

3.83

3.84

3.85

3.83

24.2165916667

4.33

3.86

3.86

3.85

3.83

3.83

3.84

3.85

3.83

24.252425

4.3

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.2882583333

4.3

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.3243416667

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.360425

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.3968416667

4.37

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.4323416667

4.26

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.468425

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.5042583333

4.3

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.5403416667

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.576425

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.6125083333

4.33

3.86

3.85

3.85

3.83

3.83

3.84

3.85

3.83

24.6485916667

4.33

3.86

3.85

3.85

3.83

3.83

3.83

3.85

3.83

24.684425

4.3

3.86

3.85

3.85

3.83

3.83

3.83

3.85

3.83

24.7205083333

4.33

3.86

3.85

3.85

3.83

3.83

3.83

3.85

3.83

24.7563416667

4.3

3.85

3.85

3.85

3.83

3.83

3.83

3.85

3.83

24.792425

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.85

3.82

24.8285083333

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.85

3.82

24.8645916667

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.85

3.82

24.900675

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.85

3.82

24.9367583333

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.84

3.82

24.9728416667

4.33

3.85

3.85

3.85

3.83

3.83

3.83

3.84

3.82

25.008675

4.3

3.85

3.85

3.85

3.83

3.83

3.83

3.84

3.82

25.0445083333

4.3

3.85

3.85

3.85

3.83

3.82

3.83

3.84

3.82

25.0805916667

4.33

3.85

3.85

3.85

3.83

3.82

3.83

3.84

3.82

25.116675

4.33

3.85

3.85

3.85

3.83

3.82

3.83

3.84

3.82

25.1527583333

4.33

3.85

3.85

3.85

3.83

3.82

3.83

3.84

3.82

25.189175

4.37

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.2252583333

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.261675

4.37

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.2977583333

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.3335916667

4.3

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.369675

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.4057583333

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.442175

4.37

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.4782583333

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.5143416667

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.550425

4.33

3.85

3.85

3.85

3.82

3.82

3.83

3.84

3.82

25.5865083333

4.33

3.85

3.85

3.84

3.82

3.82

3.83

3.84

3.82

25.6225916667

4.33

3.85

3.85

3.84

3.82

3.82

3.83

3.84

3.82

25.658675

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.6945083333

4.3

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.7305916667

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.766675

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.8027583333

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.8388416667

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

25.874925

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

25.9107583333

4.3

3.85

3.84

3.84

3.82

3.82

3.83

3.84

3.82

25.9468416667

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

25.982925

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

26.0187583333

4.3

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

26.0548416667

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

26.090925

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

26.1270083333

4.33

3.85

3.84

3.84

3.82

3.82

3.83

3.83

3.82

26.1630916667

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.198925

4.3

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.2350083333

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.2708416667

4.3

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.306925

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.3430083333

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.3788416667

4.3

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.414925

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.4510083333

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.82

26.4870916667

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.81

26.523175

4.33

3.84

3.84

3.84

3.82

3.82

3.82

3.83

3.81

26.5592583333

4.33

3.84

3.84

3.83

3.82

3.82

3.82

3.83

3.81

26.5953416667

4.33

3.84

3.84

3.83

3.82

3.82

3.82

3.83

3.81

26.631425

4.33

3.84

3.83

3.83

3.82

3.82

3.82

3.83

3.81

26.6675083333

4.33

3.84

3.83

3.83

3.82

3.81

3.82

3.83

3.81

26.7035916667

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.739675

4.33

3.84

3.83

3.83

3.82

3.81

3.82

3.83

3.81

26.7757583333

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.8118416667

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.847925

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.8840083333

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.9200916667

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.956175

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

26.9920083333

4.3

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.0278416667

4.3

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.063925

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.1000083333

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.1360916667

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.172175

4.33

3.84

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.2082583333

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.2443416667

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.280425

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.3165083333

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.3525916667

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.388675

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.4247583333

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.83

3.81

27.4605916667

4.3

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.81

27.496675

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.81

27.5327583333

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.81

27.5688416667

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.81

27.604925

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.81

27.6410083333

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.8

27.6770916667

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.8

27.713175

4.33

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.8

27.7490083333

4.3

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.8

27.785425

4.37

3.83

3.83

3.83

3.81

3.81

3.82

3.82

3.8

27.8215083333

4.33

3.83

3.83

3.83

3.81

3.8

3.82

3.82

3.8

27.8573416667

4.3

3.83

3.83

3.83

3.81

3.8

3.82

3.82

3.8

27.8937583333

4.37

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

27.9298416667

4.33

3.83

3.83

3.83

3.81

3.8

3.81

3.82

3.8

27.965925

4.33

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.0020083333

4.33

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.0378416667

4.3

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.073675

4.3

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.1095083333

4.3

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.1453416667

4.3

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.181425

4.33

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.2175083333

4.33

3.83

3.83

3.83

3.8

3.8

3.81

3.82

3.8

28.2535916667

4.33

3.83

3.83

3.82

3.8

3.8

3.81

3.82

3.8

28.289675

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.3257583333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.3618416667

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.397925

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.4340083333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.4698416667

4.3

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.505925

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.5420083333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.5780916667

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.613925

4.3

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.6500083333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.6858416667

4.3

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.721925

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.7580083333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.7940916667

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.830175

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.8662583333

4.33

3.83

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.9023416667

4.33

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.9387583333

4.37

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

28.9748416667

4.33

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

29.010925

4.33

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

29.0467583333

4.3

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

29.0828416667

4.33

3.82

3.82

3.82

3.8

3.8

3.81

3.82

3.8

29.118925

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.82

3.8

29.1547583333

4.3

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.1908416667

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.226925

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.2630083333

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.2990916667

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.335175

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.3715916667

4.37

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.407675

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.4435083333

4.3

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.4793416667

4.3

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.515425

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.5515083333

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.8

29.5875916667

4.33

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.79

29.6240083333

4.37

3.82

3.82

3.82

3.8

3.8

3.8

3.81

3.79

29.6600916667

4.33

3.82

3.82

3.82

3.8

3.79

3.8

3.81

3.79

29.696175

4.33

3.82

3.82

3.82

3.79

3.8

3.8

3.81

3.79

29.7322583333

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.7683416667

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.804175

4.3

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.8402583333

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.8763416667

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.9127583333

4.37

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.9488416667

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

29.984675

4.3

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

30.0207583333

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

30.0568416667

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

30.092925

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

30.1290083333

4.33

3.82

3.82

3.82

3.79

3.79

3.8

3.81

3.79

30.1648416667

4.3

3.82

3.82

3.81

3.79

3.79

3.8

3.81

3.79

30.200925

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.2370083333

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.2730916667

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.308925

4.3

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.3450083333

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.3810916667

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.416925

4.3

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.4533416667

4.37

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.489175

4.3

3.82

3.81

3.81

3.79

3.79

3.8

3.81

3.79

30.5252583333

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.5613416667

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.597425

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.6335083333

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.6693416667

4.3

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.705425

4.33

3.82

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.7415083333

4.33

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.7775916667

4.33

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.813675

4.33

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.8500916667

4.37

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.8865083333

4.37

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.79

30.9225916667

4.33

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.78

30.958425

4.3

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.78

30.9945083333

4.33

3.81

3.81

3.81

3.79

3.79

3.8

3.8

3.78

31.030925

4.37

3.81

3.81

3.81

3.78

3.79

3.8

3.8

3.78

31.0670083333

4.33

3.81

3.81

3.81

3.78

3.78

3.8

3.8

3.78

31.1028416667

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.138675

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.1747583333

4.33

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.2105916667

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.246675

4.33

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.2827583333

4.33

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.3188416667

4.33

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.354675

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.3905083333

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.4263416667

4.3

3.81

3.81

3.81

3.78

3.78

3.79

3.8

3.78

31.462425

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.4985083333

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.5345916667

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.570675

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.6067583333

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.6428416667

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.678925

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.7150083333

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.7508416667

4.3

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.786925

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.8227583333

4.3

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.8588416667

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.894675

4.3

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.9307583333

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

31.9668416667

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.002925

4.33

3.81

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.0390083333

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.0750916667

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.111175

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.1472583333

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.1833416667

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.219425

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.2555083333

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.2915916667

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.327675

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.3637583333

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.3998416667

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.435925

4.33

3.8

3.8

3.8

3.78

3.78

3.79

3.8

3.78

32.4717583333

4.3

3.8

3.8

3.8

3.78

3.78

3.79

3.79

3.78

32.5078416667

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.8

3.78

32.543925

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.5800083333

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.6160916667

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.652175

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.6882583333

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.724675

4.37

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.7607583333

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.7968416667

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.832925

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.8690083333

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.9050916667

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.941175

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

32.9770083333

4.3

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

33.0130916667

4.33

3.8

3.8

3.8

3.77

3.78

3.78

3.79

3.78

33.049175

4.33

3.8

3.8

3.8

3.78

3.78

3.78

3.79

3.78

33.0852583333

4.33

3.8

3.8

3.8

3.77

3.78

3.78

3.79

3.77

33.1213416667

4.33

3.8

3.8

3.8

3.77

3.78

3.78

3.79

3.77

33.157425

4.33

3.8

3.8

3.8

3.77

3.78

3.78

3.79

3.77

33.1935083333

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.2295916667

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.265675

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.3017583333

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.3378416667

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.373925

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.4103416667

4.37

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.446425

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.4825083333

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.5185916667

4.33

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.554425

4.3

3.8

3.8

3.8

3.77

3.77

3.78

3.79

3.77

33.5905083333

4.33

3.8

3.79

3.8

3.77

3.77

3.78

3.79

3.77

33.6265916667

4.33

3.8

3.79

3.8

3.77

3.77

3.78

3.79

3.77

33.662675

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.6985083333

4.3

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.7345916667

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.770675

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.8067583333

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.8428416667

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.878675

4.3

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.9147583333

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.79

3.77

33.9508416667

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

33.986925

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.0230083333

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.0590916667

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.094925

4.3

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.1310083333

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.1670916667

4.33

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.202925

4.3

3.8

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.2390083333

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.2750916667

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.311175

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.3470083333

4.3

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.3830916667

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.4195083333

4.37

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.4555916667

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.491675

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.5277583333

4.33

3.79

3.79

3.79

3.76

3.77

3.78

3.78

3.77

34.5638416667

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.77

34.599925

4.33

3.79

3.79

3.79

3.76

3.77

3.78

3.78

3.77

34.6360083333

4.33

3.79

3.79

3.79

3.77

3.77

3.78

3.78

3.76

34.6720916667

4.33

3.79

3.79

3.79

3.76

3.76

3.78

3.78

3.76

34.708175

4.33

3.79

3.79

3.79

3.76

3.76

3.78

3.78

3.76

34.7445916667

4.37

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.780675

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.8167583333

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.8525916667

4.3

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.888675

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.9245083333

4.3

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.9605916667

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

34.996675

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

35.0327583333

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

35.0685916667

4.3

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

35.104675

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

35.1407583333

4.33

3.79

3.78

3.79

3.76

3.76

3.77

3.78

3.76

35.1768416667

4.33

3.79

3.79

3.79

3.76

3.76

3.77

3.78

3.76

35.212925

4.33

3.79

3.78

3.79

3.76

3.76

3.77

3.78

3.76

35.2490083333

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.2848416667

4.3

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.320675

4.3

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.3567583333

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.3928416667

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.428925

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.4647583333

4.3

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.5008416667

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.536925

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.5730083333

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.6088416667

4.3

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.644925

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.6810083333

4.33

3.79

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.7170916667

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.753175

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.7892583333

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.8250916667

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.860925

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.8970083333

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.9328416667

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

35.968675

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.0045083333

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.0405916667

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.076425

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.1125083333

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.1483416667

4.3

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.1847583333

4.37

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.2208416667

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.256925

4.33

3.78

3.78

3.78

3.76

3.76

3.77

3.78

3.76

36.2930083333

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.329425

4.37

3.78

3.78

3.78

3.76

3.76

3.76

3.78

3.76

36.3655083333

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.4015916667

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.437675

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.4737583333

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.5104416667

4.26

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.5453222222

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.5814055556

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.6174888889

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.6535722222

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.6894055556

4.3

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.7254888889

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.7619055556

4.37

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.7983222222

4.37

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.8341555556

4.3

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.8702388889

4.33

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.9060722222

4.3

3.78

3.78

3.78

3.76

3.76

3.76

3.77

3.76

36.9421555556

4.33

3.78

3.78

3.78

3.75

3.76

3.76

3.77

3.76

36.9782388889

4.33

3.78

3.78

3.78

3.75

3.76

3.76

3.77

3.76

37.0149888889

4.41

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.76

37.0510722222

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.76

37.0869055556

4.3

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.1229888889

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.1590722222

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.1951555556

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.2312388889

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.2670722222

4.3

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.3031555556

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.3389888889

4.3

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.3750722222

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.4111555556

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.4472388889

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.4833222222

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.5191555556

4.3

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.5552388889

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.5913222222

4.33

3.78

3.78

3.78

3.75

3.75

3.76

3.77

3.75

37.6274055556

4.33

3.78

3.77

3.78

3.75

3.75

3.76

3.77

3.75

37.6634888889

4.33

3.78

3.77

3.78

3.75

3.75

3.76

3.77

3.75

37.6995722222

4.33

3.78

3.77

3.78

3.75

3.75

3.76

3.77

3.75

37.7356555556

4.33

3.78

3.77

3.78

3.75

3.75

3.76

3.77

3.75

37.7717388889

4.33

3.78

3.77

3.78

3.75

3.75

3.76

3.77

3.75

37.8078222222

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.77

3.75

37.8436555556

4.3

3.78

3.77

3.77

3.75

3.75

3.76

3.77

3.75

37.8797388889

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.77

3.75

37.9158222222

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

37.9519055556

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.77

3.75

37.9879888889

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.0240722222

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.77

3.75

38.0601555556

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.0962388889

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.1320722222

4.3

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.1679055556

4.3

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.2039888889

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.2400722222

4.33

3.78

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.2761555556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.3122388889

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.3483222222

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.3844055556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.4204888889

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.4563222222

4.3

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.4924055556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.5284888889

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.5643222222

4.3

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.6004055556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.6364888889

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.6725722222

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.7086555556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.7447388889

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.7808222222

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.8169055556

4.33

3.77

3.77

3.77

3.75

3.75

3.76

3.76

3.75

38.8529888889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

38.8894055556

4.37

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

38.9254888889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

38.9615722222

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

38.9970722222

4.26

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.0331555556

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.0692388889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.1050722222

4.3

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.1409055556

4.3

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.1769888889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.2134055556

4.37

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.2494888889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.2855722222

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.3216555556

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.3577388889

4.33

3.77

3.77

3.77

3.75

3.75

3.75

3.76

3.75

39.3935722222

4.3

3.77

3.76

3.77

3.75

3.75

3.75

3.76

3.75

39.4296555556

4.33

3.77

3.76

3.77

3.75

3.75

3.75

3.76

3.75

39.4654888889

4.3

3.77

3.76

3.77

3.75

3.75

3.75

3.76

3.75

39.5015722222

4.33

3.77

3.76

3.77

3.74

3.74

3.75

3.76

3.75

39.5376555556

4.33

3.77

3.76

3.77

3.74

3.74

3.75

3.76

3.75

39.5737388889

4.33

3.77

3.76

3.77

3.74

3.74

3.75

3.76

3.75

39.6098222222

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.75

39.6459055556

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.6819888889

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.7180722222

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.7541555556

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.7899888889

4.3

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.8260722222

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.8621555556

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.8979888889

4.3

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.9340722222

4.33

3.77

3.76

3.76

3.74

3.74

3.75

3.76

3.74

39.9701555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.0062388889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.0423222222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.0784055556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.1144888889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.1503222222

4.3

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.1864055556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.2224888889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.2585722222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.2946555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.3307388889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.3668222222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.4029055556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.4389888889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.4750722222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.5111555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.5472388889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.5830722222

4.3

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.6191555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.6552388889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.76

3.74

40.6913222222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.7274055556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.7634888889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.7995722222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.8356555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.8714888889

4.3

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.9075722222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.9436555556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

40.9797388889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

41.0158222222

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

41.0519055556

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

41.0879888889

4.33

3.76

3.76

3.76

3.74

3.74

3.75

3.75

3.74

41.1240722222

4.33

3.76

3.76

3.76

3.74

3.73

3.75

3.75

3.74

41.1601555556

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.74

41.1962388889

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.74

41.2323222222

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.74

41.2681555556

4.3

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.74

41.3042388889

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.3403222222

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.3764055556

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.4124888889

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.4483222222

4.3

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.4844055556

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.5204888889

4.33

3.76

3.76

3.76

3.73

3.73

3.75

3.75

3.73

41.5565722222

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.5924055556

4.3

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.6284888889

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.6643222222

4.3

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.7004055556

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.7364888889

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.7725722222

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.8086555556

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.8447388889

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.8808222222

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.9169055556

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.9529888889

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

41.9890722222

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

42.0254888889

4.37

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

42.0615722222

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

42.0974055556

4.3

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.1334888889

4.33

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.1695722222

4.33

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.2056555556

4.33

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.2417388889

4.33

3.76

3.76

3.76

3.73

3.73

3.74

3.75

3.73

42.2775722222

4.3

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.3136555556

4.33

3.76

3.75

3.76

3.73

3.73

3.74

3.75

3.73

42.3497388889

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.3858222222

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.4219055556

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.4579888889

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.4940722222

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.5301555556

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.5656555556

4.26

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.6017388889

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.6378222222

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.6739055556

4.33

3.76

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.7099888889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.7460722222

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.7821555556

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.8182388889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.8540722222

4.3

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.8901555556

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.9262388889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.9623222222

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

42.9984055556

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.0344888889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.0705722222

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.1066555556

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.1427388889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.1788222222

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.2149055556

4.33

3.75

3.75

3.75

3.73

3.73

3.73

3.75

3.73

43.2509888889

4.33

3.75

3.75

3.75

3.73

3.73

3.74

3.75

3.73

43.2868222222

4.3

3.75

3.75

3.75

3.73

3.73

3.73

3.75

3.73

43.3229055556

4.33

3.75

3.75

3.75

3.73

3.73

3.73

3.75

3.73

43.3589888889

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.75

3.73

43.3948222222

4.3

3.75

3.75

3.75

3.73

3.72

3.73

3.75

3.73

43.4309055556

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.75

3.72

43.4669888889

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.5030722222

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.75

3.72

43.5394888889

4.37

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.5755722222

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.6116555556

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.6477388889

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.6838222222

4.33

3.75

3.75

3.75

3.73

3.72

3.73

3.74

3.72

43.7199055556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.7559888889

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.7920722222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.8281555556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.8639888889

4.3

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.9000722222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.9361555556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

43.9722388889

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.0083222222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.0444055556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.0804888889

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.1163222222

4.3

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.1524055556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.1884888889

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.2245722222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.2606555556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.2967388889

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.3328222222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.3686555556

4.3

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.4044888889

4.3

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.4405722222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.4766555556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.5124888889

4.3

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.5485722222

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.5846555556

4.33

3.75

3.75

3.75

3.72

3.72

3.73

3.74

3.72

44.6207388889

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.72

44.6568222222

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.72

44.6929055556

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.7293222222

4.37

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.7654055556

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.8014888889

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.8375722222

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.8734055556

4.3

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.9094888889

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.9455722222

4.33

3.75

3.75

3.75

3.72

3.71

3.73

3.74

3.71

44.9819888889

4.37

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.0184055556

4.37

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.0544888889

4.33

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.0905722222

4.33

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.1266555556

4.33

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.1621555556

4.26

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.1979888889

4.3

3.75

3.74

3.75

3.72

3.71

3.73

3.74

3.71

45.2338222222

4.3

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.2696555556

4.3

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.3057388889

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.3418222222

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.3779055556

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.4139888889

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.4500722222

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.4861555556

4.33

3.75

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.5219888889

4.3

3.74

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.5580722222

4.33

3.74

3.74

3.74

3.71

3.71

3.73

3.73

3.71

45.5935722222

4.26

3.74

3.74

3.74

3.71

3.71

3.72

3.73

3.71

45.6296555556

4.33

3.74

3.74

3.74

3.71

3.71

3.72

3.73

3.71

45.6654888889

4.3

3.74

3.74

3.74

3.71

3.71

3.72

3.73

3.71

45.7015722222

4.33

3.74

3.74

3.74

3.71

3.71

3.72

3.73

3.71

45.7376555556

4.33

3.74

3.74

3.74

3.71

3.71

3.72

3.73
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45.7737388889

4.33

3.74

3.74

3.74

3.71

3.71

3.72

3.73
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45.8095722222

4.3

3.74
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3.74
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3.71
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45.8456555556

4.33
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45.8817388889
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3.74

3.74
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45.9178222222

4.33

3.74

3.74
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45.9539055556

4.33
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3.72
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45.9899888889

4.33

3.74
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46.0260722222

4.33
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46.0621555556

4.33
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3.74

3.71
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46.0979888889
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3.74

3.74
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46.1340722222

4.33
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46.1701555556

4.33
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46.2062388889

4.33
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46.2423222222
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4.33
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46.4222388889

4.3

3.74

3.74

3.74

3.71

3.7

3.72

3.73

3.71
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46.5669055556
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46.6029888889
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47.0722388889
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47.1441555556
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47.1802388889
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47.3243222222

4.33

3.74

3.73

3.73

3.7

3.7

3.71

3.73

3.7
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3.69

3.67

52.8767388889

4.33

3.71

3.7

3.71

3.67

3.67

3.68

3.69

3.67

52.9128222222

4.33

3.71

3.7

3.71

3.67

3.66

3.68

3.69

3.67

52.9489055556

4.33

3.71

3.7

3.71

3.67

3.66

3.68

3.69

3.67

52.9849888889

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.0214055556

4.37

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.0574888889

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.0933222222

4.3

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.1294055556

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.1654888889

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.2015722222

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.2376555556

4.33

3.71

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.2737388889

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.3098222222

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.3459055556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.3819888889

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.4184055556

4.37

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.4548222222

4.37

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.4909055556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.5269888889

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.67

53.5630722222

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.5991555556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.6349888889

4.3

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.6710722222

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.7071555556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.7432388889

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.7793222222

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.8154055556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.8514888889

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.8875722222

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.9236555556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.9594888889

4.3

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

53.9953222222

4.3

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

54.0314055556

4.33

3.7

3.7

3.7

3.67

3.66

3.68

3.69

3.66

54.0672388889

4.3

3.7

3.7

3.7

3.67

3.66

3.67

3.69

3.66

54.1033222222

4.33

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.1394055556

4.33

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.1758222222

4.37

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.2116555556

4.3

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.2477388889

4.33

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.2835722222

4.3

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.3196555556

4.33

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.3557388889

4.33

3.7

3.69

3.7

3.66

3.66

3.67

3.69

3.66

54.3915722222

4.3

3.7

3.7

3.7

3.66

3.66

3.67

3.69

3.66

54.4276555556

4.33

3.7

3.69

3.7

3.66

3.65

3.67

3.69

3.66

54.4637388889

4.33

3.7

3.69

3.7

3.66

3.65

3.67

3.69

3.66

54.4998222222

4.33

3.7

3.69

3.7

3.66

3.65

3.67

3.69

3.66

54.5359055556

4.33

3.7

3.69

3.7

3.66

3.65

3.67

3.69

3.66

54.5719888889

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.6080722222

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.6439055556

4.3

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.6799888889

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.7160722222

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.7519055556

4.3

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.7879888889

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.8240722222

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.8601555556

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.8962388889

4.33

3.7

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.9320722222

4.3

3.69

3.69

3.69

3.66

3.65

3.67

3.69

3.66

54.9681555556

4.33

3.69

3.69

3.69

3.66

3.65

3.67

3.69

3.65

55.0042388889

4.33

3.69

3.69

3.69

3.66

3.65

3.67

3.69

3.65

55.0403222222

4.33

3.69

3.69

3.69

3.66

3.65

3.67

3.69

3.65

55.0764055556

4.33

3.69

3.69

3.69

3.66

3.65

3.67

3.68

3.65

55.1124888889

4.33

3.69

3.69

3.69

3.66

3.65

3.67

3.68

3.65

55.1489055556

4.37

3.69

3.69

3.69

3.66

3.65

3.67

3.68

3.65

55.1847388889

4.3

3.69

3.69

3.69

3.66

3.65

3.67

3.68

3.65

55.2208222222

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.2569055556

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.2929888889

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.3290722222

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.3651555556

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.4012388889

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.4370722222

4.3

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.4729055556

4.3

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.5089888889

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.5450722222

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.5811555556

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.6172388889

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.6533222222

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.6894055556

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.7254888889

4.33

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.7619055556

4.37

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.7977388889

4.3

3.69

3.69

3.69

3.66

3.64

3.67

3.68

3.65

55.8338222222

4.33

3.69

3.69

3.69

3.65

3.64

3.67

3.68

3.65

55.8699055556

4.33

3.69

3.69

3.69

3.65

3.64

3.67

3.68

3.65

55.9059888889

4.33

3.69

3.69

3.69

3.65

3.64

3.67

3.68

3.65

55.9420722222

4.33

3.69

3.69

3.69

3.65

3.64

3.67

3.68

3.65

55.9781555556

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.65

56.0142388889

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.65

56.0500722222

4.3

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.0859055556

4.3

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.1219888889

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.1580722222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.1944888889

4.37

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.2305722222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.2666555556

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.3027388889

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.3388222222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.3746555556

4.3

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.4107388889

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.68

3.64

56.4468222222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.4832388889

4.37

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.5193222222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.5554055556

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.5914888889

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.6275722222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.6634055556

4.3

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.6992388889

4.3

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.7353222222

4.33

3.69

3.69

3.69

3.65

3.64

3.66

3.67

3.64

56.7714055556

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.8074888889

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.8435722222

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.8799888889

4.37

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.9160722222

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.9521555556

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

56.9882388889

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

57.0240722222

4.3

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

57.0601555556

4.33

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

57.0959888889

4.3

3.69

3.68

3.69

3.64

3.64

3.66

3.67

3.64

57.1318222222

4.3

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.1679055556

4.33

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.2037388889

4.3

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.2395722222

4.3

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.2756555556

4.33

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.3117388889

4.33

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.3478222222

4.33

3.69

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.3836555556

4.3

3.68

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.4194888889

4.3

3.68

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.4555722222

4.33

3.68

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.4916555556

4.33

3.68

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.5277388889

4.33

3.68

3.68

3.68

3.64

3.64

3.66

3.67

3.64

57.5635722222

4.3

3.68

3.68

3.68

3.64

3.63

3.66

3.67

3.64

57.5996555556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.6357388889

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.6718222222

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.7079055556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.7439888889

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.7800722222

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.8161555556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.8519888889

4.3

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.8880722222

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.9241555556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.9605722222

4.37

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

57.9966555556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.0327388889

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.0688222222

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.1049055556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.1409888889

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.1770722222

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.2131555556

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.2492388889

4.33

3.68

3.68

3.68

3.64

3.63

3.65

3.67

3.64

58.2853222222

4.33

3.68

3.67

3.68

3.64

3.63

3.65

3.67

3.64

58.3214055556

4.33

3.68

3.67

3.68

3.64

3.63

3.65

3.67

3.64

58.3572388889

4.3

3.68

3.67

3.68

3.64

3.63

3.65

3.66

3.64

58.3930722222

4.3

3.68

3.67

3.68

3.64

3.63

3.65

3.66

3.64

58.4291555556

4.33

3.68

3.67

3.68

3.64

3.63

3.65

3.66

3.64

58.4649888889

4.3

3.68

3.67

3.68

3.64

3.63

3.65

3.66

3.64

58.5010722222

4.33

3.68

3.67

3.68

3.64

3.63

3.64

3.66

3.64

58.5371555556

4.33

3.68

3.67

3.68

3.64

3.63

3.64

3.66

3.64

58.5735722222

4.37

3.68

3.67

3.67

3.64

3.63

3.64

3.66

3.64

58.6096555556

4.33

3.68

3.67

3.67

3.64

3.63

3.64

3.66

3.64

58.6457388889

4.33

3.68

3.67

3.67

3.64

3.63

3.64

3.66

3.64

58.6815722222

4.3

3.68

3.67

3.67

3.64

3.63

3.64

3.66

3.63

58.7176555556

4.33

3.68

3.67

3.67

3.64

3.63

3.64

3.66

3.63

58.7534888889

4.3

3.68

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.7895722222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.8256555556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.8617388889

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.8978222222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.9339055556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

58.9699888889

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.0060722222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.0421555556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.0782388889

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.1140722222

4.3

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.1501555556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.1862388889

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.2223222222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.2584055556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.2944888889

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.3305722222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.3666555556

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.4024888889

4.3

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.4385722222

4.33

3.67

3.67

3.67

3.63

3.62

3.64

3.66

3.63

59.4746555556

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.63

59.5107388889

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.63

59.5468222222

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.5829055556

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.6189888889

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.6550722222

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.6911555556

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.7272388889

4.33

3.67

3.67

3.67

3.63

3.61

3.64

3.66

3.62

59.7633222222

4.33

3.67

3.67

3.67

3.63

3.6

3.64

3.66

3.62

59.7991555556

4.3

3.67

3.67

3.67

3.63

3.6

3.64

3.66

3.62

59.8352388889

4.33

3.67

3.67

3.67

3.63

3.6

3.64

3.66

3.62

59.8713222222

4.33

3.67

3.67

3.67

3.63

3.6

3.64

3.66

3.62

59.9071555556

4.3

3.67

3.67

3.67

3.63

3.6

3.64

3.66

3.62

59.9432388889

4.33

3.67

3.67

3.67

3.63

3.6

3.64

3.65

3.62

59.9796555556

4.37

3.67

3.67

3.67

3.63

3.6

3.64

3.65

3.62

60.0157388889

4.33

3.67

3.67

3.67

3.63

3.6

3.64

3.65

3.62

60.0518222222

4.33

3.67

3.67

3.67

3.63

3.59

3.64

3.65

3.62

60.0876555556

4.3

3.67

3.67

3.67

3.63

3.59

3.64

3.65

3.62

60.1237388889

4.33

3.67

3.67

3.67

3.63

3.59

3.64

3.65

3.62

60.1598222222

4.33

3.67

3.67

3.67

3.63

3.59

3.64

3.65

3.61

60.1959055556

4.33

3.67

3.67

3.67

3.63

3.59

3.64

3.65

3.61

60.2314055556

4.26

3.67

3.67

3.67

3.63

3.58

3.64

3.65

3.61

60.2674888889

4.33

3.67

3.67

3.67

3.63

3.58

3.64

3.65

3.61

60.3035722222

4.33

3.67

3.67

3.67

3.62

3.58

3.64

3.65

3.61

60.3396555556

4.33

3.67

3.67

3.67

3.62

3.58

3.64

3.65

3.61

60.3757388889

4.33

3.67

3.66

3.67

3.62

3.58

3.64

3.65

3.61

60.4118222222

4.33

3.67

3.66

3.67

3.62

3.58

3.64

3.65

3.6

60.4479055556

4.33

3.67

3.66

3.67

3.62

3.58

3.64

3.65

3.6

60.4837388889

4.3

3.67

3.66

3.67

3.62

3.57

3.64

3.65

3.6

60.5198222222

4.33

3.67

3.66

3.67

3.62

3.57

3.64

3.65

3.6

60.5559055556

4.33

3.67

3.66

3.67

3.62

3.57

3.64

3.65

3.6

60.5917388889

4.3

3.67

3.66

3.67

3.62

3.57

3.64

3.65

3.6

60.6275722222

4.3

3.67

3.66

3.67

3.62

3.57

3.64

3.65

3.6

60.6636555556

4.33

3.67

3.66

3.66

3.62

3.57

3.64

3.65

3.6

60.6997388889

4.33

3.67

3.66

3.66

3.62

3.57

3.64

3.65

3.6

60.7358222222

4.33

3.67

3.66

3.66

3.62

3.56

3.64

3.65

3.59

60.7719055556

4.33

3.67

3.66

3.66

3.62

3.56

3.64

3.65

3.59

60.8079888889

4.33

3.66

3.66

3.66

3.62

3.56

3.64

3.65

3.59

60.8440722222

4.33

3.66

3.66

3.66

3.62

3.56

3.64

3.65

3.59

60.8801555556

4.33

3.66

3.66

3.66

3.62

3.55

3.64

3.64

3.59

60.9162388889

4.33

3.66

3.66

3.66

3.62

3.55

3.63

3.65

3.58

60.9520722222

4.3

3.66

3.66

3.66

3.62

3.55

3.63

3.64

3.58

60.9879055556

4.3

3.66

3.66

3.66

3.62

3.55

3.63

3.64

3.58

61.0237388889

4.3

3.66

3.66

3.66

3.62

3.55

3.63

3.64

3.58

61.0598222222

4.33

3.66

3.66

3.66

3.62

3.54

3.63

3.64

3.58

61.0959055556

4.33

3.66

3.66

3.66

3.62

3.54

3.63

3.64

3.58

61.1319888889

4.33

3.66

3.66

3.66

3.62

3.54

3.63

3.64

3.58

61.1684055556

4.37

3.66

3.66

3.66

3.62

3.54

3.63

3.64

3.57

61.2044888889

4.33

3.66

3.66

3.66

3.62

3.53

3.63

3.64

3.57

61.2405722222

4.33

3.66

3.66

3.66

3.62

3.53

3.63

3.64

3.57

61.2766555556

4.33

3.66

3.66

3.66

3.62

3.53

3.63

3.64

3.57

61.3127388889

4.33

3.66

3.66

3.66

3.61

3.53

3.63

3.64

3.57

61.3488222222

4.33

3.66

3.66

3.66

3.61

3.53

3.63

3.64

3.57

61.3849055556

4.33

3.66

3.66

3.66

3.61

3.53

3.63

3.64

3.57

61.4207388889

4.3

3.66

3.66

3.66

3.61

3.52

3.63

3.64

3.56

61.4571555556

4.37

3.66

3.66

3.66

3.61

3.52

3.63

3.64

3.56

61.4935722222

4.37

3.66

3.66

3.66

3.61

3.52

3.63

3.64

3.56

61.5296555556

4.33

3.66

3.66

3.66

3.61

3.51

3.63

3.64

3.56

61.5657388889

4.33

3.66

3.66

3.66

3.61

3.51

3.63

3.64

3.56

61.6018222222

4.33

3.66

3.66

3.66

3.61

3.51

3.63

3.64

3.55

61.6379055556

4.33

3.66

3.66

3.66

3.61

3.51

3.63

3.64

3.55

61.6737388889

4.3

3.66

3.66

3.66

3.6

3.51

3.63

3.64

3.55

61.7098222222

4.33

3.66

3.66

3.66

3.6

3.5

3.63

3.64

3.55

61.7459055556

4.33

3.66

3.66

3.66

3.6

3.5

3.63

3.64

3.55

61.7817388889

4.3

3.66

3.66

3.66

3.6

3.5

3.63

3.64

3.55

61.8172388889

4.26

3.66

3.66

3.66

3.6

3.5

3.63

3.64

3.54

61.8533222222

4.33

3.66

3.66

3.66

3.6

3.49

3.63

3.64

3.54

61.8888222222

4.26

3.66

3.66

3.66

3.6

3.49

3.63

3.64

3.54

61.9252388889

4.37

3.66

3.66

3.66

3.6

3.49

3.63

3.64

3.54

61.9613222222

4.33

3.66

3.66

3.66

3.6

3.48

3.63

3.64

3.53

61.9974055556

4.33

3.66

3.66

3.66

3.6

3.48

3.63

3.64

3.53

62.0334888889

4.33

3.66

3.66

3.66

3.59

3.48

3.63

3.64

3.53

62.0695722222

4.33

3.66

3.66

3.66

3.59

3.48

3.63

3.64

3.53

62.1056555556

4.33

3.66

3.66

3.66

3.59

3.48

3.63

3.64

3.53

62.1414888889

4.3

3.66

3.66

3.66

3.59

3.47

3.63

3.64

3.53

62.1773222222

4.3

3.66

3.65

3.66

3.59

3.47

3.63

3.64

3.52

62.2134055556

4.33

3.66

3.65

3.66

3.59

3.47

3.63

3.64

3.52

62.2494888889

4.33

3.66

3.65

3.66

3.58

3.46

3.63

3.64

3.52

62.2855722222

4.33

3.66

3.65

3.66

3.58

3.46

3.62

3.64

3.52

62.3216555556

4.33

3.66

3.65

3.66

3.58

3.46

3.62

3.64

3.51

62.3577388889

4.33

3.66

3.65

3.66

3.58

3.46

3.62

3.64

3.51

62.3938222222

4.33

3.66

3.65

3.66

3.58

3.45

3.62

3.64

3.51

62.4299055556

4.33

3.66

3.65

3.66

3.58

3.45

3.62

3.64

3.51

62.4659888889

4.33

3.66

3.65

3.66

3.58

3.45

3.62

3.64

3.51

62.5020722222

4.33

3.65

3.65

3.65

3.58

3.44

3.62

3.64

3.5

62.5379055556

4.3

3.65

3.65

3.65

3.57

3.44

3.62

3.64

3.5

62.5737388889

4.3

3.65

3.65

3.65

3.57

3.44

3.62

3.64

3.5

62.6098222222

4.33

3.65

3.65

3.65

3.57

3.44

3.62

3.64

3.5

62.6459055556

4.33

3.65

3.65

3.65

3.57

3.43

3.62

3.64

3.5

62.6819888889

4.33

3.65

3.65

3.65

3.57

3.43

3.62

3.64

3.49

62.7180722222

4.33

3.65

3.65

3.65

3.57

3.42

3.62

3.64

3.49

62.7541555556

4.33

3.65

3.65

3.65

3.57

3.42

3.62

3.64

3.49

62.7902388889

4.33

3.65

3.65

3.65

3.56

3.42

3.62

3.64

3.48

62.8263222222

4.33

3.65

3.65

3.65

3.56

3.42

3.62

3.64

3.48

62.8624055556

4.33

3.65

3.65

3.65

3.56

3.41

3.62

3.64

3.48

62.8984888889

4.33

3.65

3.65

3.65

3.56

3.41

3.62

3.64

3.48

62.9345722222

4.33

3.65

3.65

3.65

3.56

3.41

3.62

3.64

3.48

62.9706555556

4.33

3.65

3.65

3.65

3.55

3.4

3.62

3.64

3.47

63.0067388889

4.33

3.65

3.65

3.65

3.55

3.4

3.62

3.64

3.47

63.0425722222

4.3

3.65

3.65

3.65

3.55

3.39

3.62

3.64

3.47

63.0784055556

4.3

3.65

3.64

3.65

3.55

3.39

3.61

3.64

3.46

63.1144888889

4.33

3.65

3.64

3.65

3.55

3.39

3.61

3.64

3.46

63.1503222222

4.3

3.65

3.65

3.65

3.55

3.39

3.61

3.64

3.46

63.1864055556

4.33

3.65

3.64

3.65

3.55

3.38

3.61

3.64

3.46

63.2224888889

4.33

3.65

3.64

3.65

3.55

3.38

3.61

3.64

3.45

63.2585722222

4.33

3.65

3.64

3.65

3.55

3.37

3.61

3.64

3.45

63.2946555556

4.33

3.65

3.64

3.65

3.55

3.37

3.61

3.64

3.45

63.3304888889

4.3

3.65

3.64

3.65

3.54

3.36

3.61

3.64

3.44

63.3663222222

4.3

3.65

3.64

3.65

3.54

3.36

3.61

3.64

3.44

63.4024055556

4.33

3.65

3.64

3.65

3.54

3.35

3.6

3.64

3.44

63.4384888889

4.33

3.65

3.64

3.64

3.54

3.35

3.6

3.64

3.44

63.4745722222

4.33

3.65

3.64

3.64

3.54

3.35

3.6

3.64

3.43

63.5104055556

4.3

3.65

3.64

3.64

3.54

3.34

3.6

3.64

3.43

63.5464888889

4.33

3.64

3.64

3.64

3.53

3.34

3.6

3.63
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b4_complete

		Send Time		String		Recv Time		String		State		Stack Voltage		Current		Max Temp		Cell 1		Cell 2		Cell 3		Cell 4		Cell 5		Cell 6		Cell 7		Cell 8								Elapsed Time				Ah		Wh

		S1148839044:		#B4q0		1148839044:		$B4q0		d-		33.13		0.41		25.19		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13		0		-23248.27		1:03:13		0:00:00		m		0.00		0

		S1148839074:		#B4q0		1148839074:		$B4q0		d-		33.13		0.38		25.29		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13		0		-23248.37		1:03:43		0:00:30		m		0.00		0.11

		S1148839104:		#B4q0		1148839104:		$B4q0		d-		33.13		0.38		25.19		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13		0		-23248.49		1:04:13		0:01:00		m		0.01		0.21

		S1148839134:		#B4q0		1148839134:		$B4q0		d-		32.98		4.33		25.29		4.12		4.12		4.11		4.12		4.12		4.11		4.12		4.11		0		-23249.3		1:04:43		0:01:30		m		0.04		0.86

		S1148839164:		#B4q0		1148839164:		$B4q0		d-		32.98		4.30		25.29		4.12		4.11		4.11		4.11		4.12		4.11		4.12		4.10		0		-23250.57		1:05:13		0:02:00		m		0.08		2.05

		S1148839194:		#B4q0		1148839194:		$B4q0		d-		32.94		4.26		25.29		4.12		4.11		4.11		4.11		4.12		4.11		4.12		4.10		0		-23251.67		1:05:43		0:02:30		m		0.11		3.22

		S1148839224:		#B4q0		1148839224:		$B4q0		d-		32.94		4.33		25.29		4.12		4.11		4.10		4.11		4.12		4.10		4.12		4.10		0		-23252.94		1:06:13		0:03:00		m		0.15		4.40

		S1148839254:		#B4q0		1148839254:		$B4q0		d-		32.90		4.30		25.39		4.11		4.11		4.10		4.11		4.12		4.10		4.11		4.10		0		-23254.04		1:06:43		0:03:30		m		0.19		5.59

		S1148839284:		#B4q0		1148839284:		$B4q0		d-		32.94		4.30		25.39		4.11		4.11		4.10		4.11		4.11		4.10		4.11		4.10		0		-23255.31		1:07:13		0:04:00		m		0.22		6.77

		S1148839314:		#B4q0		1148839314:		$B4q0		d-		32.90		4.33		25.39		4.11		4.11		4.10		4.11		4.11		4.10		4.11		4.10		0		-23256.42		1:07:43		0:04:30		m		0.26		7.95

		S1148839344:		#B4q0		1148839344:		$B4q0		d-		32.90		4.30		25.39		4.11		4.11		4.10		4.11		4.11		4.10		4.11		4.10		0		-23257.68		1:08:13		0:05:00		m		0.29		9.13

		S1148839374:		#B4q0		1148839374:		$B4q0		d-		32.90		4.30		25.39		4.11		4.11		4.10		4.11		4.11		4.10		4.11		4.10		0		-23258.78		1:08:43		0:05:30		m		0.33		10.31

		S1148839404:		#B4q0		1148839404:		$B4q0		d-		32.90		4.30		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23260.05		1:09:13		0:06:00		m		0.37		11.49

		S1148839434:		#B4q0		1148839434:		$B4q0		d-		32.90		4.33		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23261.15		1:09:43		0:06:30		m		0.40		12.67

		S1148839464:		#B4q0		1148839464:		$B4q0		d-		32.86		4.33		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23262.41		1:10:13		0:07:00		m		0.44		13.86

		S1148839494:		#B4q0		1148839494:		$B4q0		d-		32.86		4.30		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23263.51		1:10:43		0:07:30		m		0.47		15.04

		S1148839524:		#B4q0		1148839524:		$B4q0		d-		32.86		4.30		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23264.77		1:11:13		0:08:00		m		0.51		16.22

		S1148839554:		#B4q0		1148839554:		$B4q0		d-		32.86		4.30		25.39		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23265.88		1:11:43		0:08:30		m		0.54		17.40

		S1148839584:		#B4q0		1148839584:		$B4q0		d-		32.86		4.30		25.48		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.10		0		-23267.14		1:12:13		0:09:00		m		0.58		18.57

		S1148839614:		#B4q0		1148839614:		$B4q0		d-		32.86		4.30		25.48		4.11		4.10		4.10		4.10		4.11		4.10		4.11		4.09		0		-23268.24		1:12:43		0:09:30		m		0.62		19.75

		S1148839644:		#B4q0		1148839644:		$B4q0		d-		32.86		4.30		25.48		4.11		4.10		4.10		4.10		4.10		4.10		4.11		4.09		0		-23269.5		1:13:13		0:10:00		m		0.65		20.93

		S1148839674:		#B4q0		1148839674:		$B4q0		d-		32.86		4.33		25.48		4.10		4.10		4.10		4.10		4.10		4.10		4.10		4.09		0		-23270.6		1:13:43		0:10:30		m		0.69		22.11

		S1148839704:		#B4q0		1148839704:		$B4q0		d-		32.86		4.30		25.58		4.10		4.10		4.10		4.10		4.10		4.10		4.10		4.09		0		-23271.86		1:14:13		0:11:00		m		0.72		23.29

		S1148839734:		#B4q0		1148839734:		$B4q0		d-		32.86		4.33		25.58		4.10		4.10		4.10		4.10		4.10		4.10		4.10		4.09		0		-23272.96		1:14:43		0:11:30		m		0.76		24.47

		S1148839764:		#B4q0		1148839764:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.10		4.10		4.10		4.10		4.10		4.09		0		-23274.22		1:15:13		0:12:00		m		0.80		25.66

		S1148839794:		#B4q0		1148839794:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.10		4.10		4.10		4.10		4.10		4.09		0		-23275.32		1:15:43		0:12:30		m		0.83		26.83

		S1148839824:		#B4q0		1148839824:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23276.58		1:16:13		0:13:00		m		0.87		28.01

		S1148839854:		#B4q0		1148839854:		$B4q0		d-		32.83		4.33		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23277.68		1:16:43		0:13:30		m		0.90		29.19

		S1148839884:		#B4q0		1148839884:		$B4q0		d-		32.83		4.37		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23278.94		1:17:13		0:14:00		m		0.94		30.38

		S1148839914:		#B4q0		1148839914:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23280.04		1:17:43		0:14:30		m		0.98		31.56

		S1148839944:		#B4q0		1148839944:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23281.3		1:18:13		0:15:00		m		1.01		32.74

		S1148839974:		#B4q0		1148839974:		$B4q0		d-		32.83		4.33		25.58		4.10		4.10		4.09		4.10		4.10		4.09		4.10		4.09		0		-23282.41		1:18:43		0:15:30		m		1.05		33.92

		S1148840004:		#B4q0		1148840004:		$B4q0		d-		32.83		4.30		25.58		4.10		4.10		4.09		4.09		4.10		4.09		4.10		4.09		0		-23283.67		1:19:13		0:16:00		m		1.08		35.10

		S1148840034:		#B4q0		1148840034:		$B4q0		d-		32.83		4.33		25.68		4.10		4.10		4.09		4.09		4.10		4.09		4.10		4.08		0		-23284.77		1:19:43		0:16:30		m		1.12		36.28

		S1148840064:		#B4q0		1148840064:		$B4q0		d-		32.83		4.30		25.68		4.10		4.10		4.09		4.09		4.10		4.09		4.10		4.08		0		-23286.03		1:20:13		0:17:00		m		1.16		37.46

		S1148840094:		#B4q0		1148840094:		$B4q0		d-		32.79		4.30		25.68		4.10		4.10		4.09		4.09		4.10		4.09		4.10		4.08		0		-23287.13		1:20:43		0:17:30		m		1.19		38.64

		S1148840124:		#B4q0		1148840124:		$B4q0		d-		32.83		4.33		25.68		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23288.4		1:21:13		0:18:00		m		1.23		39.82

		S1148840154:		#B4q0		1148840154:		$B4q0		d-		32.83		4.30		25.68		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23289.5		1:21:43		0:18:30		m		1.26		41.00

		S1148840184:		#B4q0		1148840184:		$B4q0		d-		32.79		4.30		25.78		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23290.75		1:22:13		0:19:00		m		1.30		42.17

		S1148840214:		#B4q0		1148840214:		$B4q0		d-		32.83		4.30		25.78		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23291.85		1:22:43		0:19:30		m		1.34		43.35

		S1148840244:		#B4q0		1148840244:		$B4q0		d-		32.79		4.33		25.78		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23293.11		1:23:13		0:20:00		m		1.37		44.53

		S1148840274:		#B4q0		1148840274:		$B4q0		d-		32.75		4.30		25.78		4.10		4.09		4.09		4.09		4.10		4.09		4.10		4.08		0		-23294.21		1:23:43		0:20:30		m		1.41		45.71

		S1148840304:		#B4q0		1148840304:		$B4q0		d-		32.75		4.30		25.78		4.10		4.09		4.09		4.09		4.09		4.08		4.10		4.08		0		-23295.47		1:24:13		0:21:00		m		1.44		46.88

		S1148840334:		#B4q0		1148840334:		$B4q0		d-		32.79		4.30		25.78		4.10		4.09		4.08		4.09		4.09		4.08		4.10		4.08		0		-23296.57		1:24:43		0:21:30		m		1.48		48.06

		S1148840364:		#B4q0		1148840364:		$B4q0		d-		32.75		4.30		25.78		4.10		4.09		4.08		4.09		4.09		4.08		4.09		4.08		0		-23297.83		1:25:13		0:22:00		m		1.51		49.23

		S1148840394:		#B4q0		1148840394:		$B4q0		d-		32.75		4.33		25.78		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08		0		-23298.93		1:25:43		0:22:30		m		1.55		50.41

		S1148840424:		#B4q0		1148840424:		$B4q0		d-		32.75		4.37		25.78		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08		0		-23300.19		1:26:13		0:23:00		m		1.59		51.60

		S1148840454:		#B4q0		1148840454:		$B4q0		d-		32.71		4.33		25.87		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08		0		-23301.29		1:26:43		0:23:30		m		1.62		52.78

		S1148840484:		#B4q0		1148840484:		$B4q0		d-		32.75		4.30		25.87		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08		0		-23302.55		1:27:13		0:24:00		m		1.66		53.96

		S1148840514:		#B4q0		1148840514:		$B4q0		d-		32.75		4.33		25.87		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08		0		-23303.64		1:27:43		0:24:30		m		1.70		55.14

		S1148840544:		#B4q0		1148840544:		$B4q0		d-		32.75		4.33		25.87		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08		0		-23304.9		1:28:13		0:25:00		m		1.73		56.32

		S1148840574:		#B4q0		1148840574:		$B4q0		d-		32.75		4.33		25.87		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08		0		-23306		1:28:43		0:25:30		m		1.77		57.50

		S1148840604:		#B4q0		1148840604:		$B4q0		d-		32.75		4.33		25.87		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08		0		-23307.26		1:29:13		0:26:00		m		1.80		58.68

		S1148840634:		#B4q0		1148840634:		$B4q0		d-		32.75		4.30		25.97		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08		0		-23308.36		1:29:43		0:26:30		m		1.84		59.86

		S1148840664:		#B4q0		1148840664:		$B4q0		d-		32.75		4.33		25.97		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08		0		-23309.61		1:30:13		0:27:00		m		1.88		61.04

		S1148840694:		#B4q0		1148840694:		$B4q0		d-		32.75		4.30		25.87		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08		0		-23310.71		1:30:43		0:27:30		m		1.91		62.21

		S1148840724:		#B4q0		1148840724:		$B4q0		d-		32.71		4.33		25.97		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.07		0		-23311.97		1:31:13		0:28:00		m		1.95		63.39

		S1148840754:		#B4q0		1148840754:		$B4q0		d-		32.71		4.30		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07		0		-23313.07		1:31:43		0:28:30		m		1.98		64.57

		S1148840784:		#B4q0		1148840784:		$B4q0		d-		32.71		4.33		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07		0		-23314.33		1:32:13		0:29:00		m		2.02		65.74

		S1148840814:		#B4q0		1148840814:		$B4q0		d-		32.71		4.30		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07		0		-23315.43		1:32:43		0:29:30		m		2.05		66.92

		S1148840844:		#B4q0		1148840844:		$B4q0		d-		32.75		4.30		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07		0		-23316.69		1:33:13		0:30:00		m		2.09		68.09

		S1148840874:		#B4q0		1148840874:		$B4q0		d-		32.71		4.33		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.08		4.07		0		-23317.79		1:33:43		0:30:30		m		2.13		69.27

		S1148840905:		#B4q0		1148840905:		$B4q0		d-		32.71		4.30		25.97		4.09		4.08		4.08		4.08		4.08		4.08		4.08		4.07		0		-23319.05		1:34:13		0:31:00		m		2.16		70.45

		S1148840934:		#B4q0		1148840934:		$B4q0		d-		32.71		4.30		25.97		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07		0		-23320.15		1:34:43		0:31:30		m		2.20		71.62

		S1148840964:		#B4q0		1148840964:		$B4q0		d-		32.71		4.30		26.07		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07		0		-23321.41		1:35:13		0:32:00		m		2.23		72.79

		S1148840994:		#B4q0		1148840994:		$B4q0		d-		32.67		4.33		26.07		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07		0		-23322.5		1:35:43		0:32:30		m		2.27		73.97

		S1148841024:		#B4q0		1148841024:		$B4q0		d-		32.71		4.30		26.07		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07		0		-23323.76		1:36:13		0:33:00		m		2.31		75.14

		S1148841054:		#B4q0		1148841054:		$B4q0		d-		32.71		4.33		26.07		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07		0		-23324.86		1:36:43		0:33:30		m		2.34		76.32

		S1148841084:		#B4q0		1148841085:		$B4q0		d-		32.67		4.33		26.07		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07		0		-23326.11		1:37:13		0:34:00		m		2.38		77.50

		S1148841114:		#B4q0		1148841114:		$B4q0		d-		32.67		4.30		26.07		4.08		4.08		4.07		4.08		4.08		4.07		4.08		4.07		0		-23327.21		1:37:43		0:34:30		m		2.41		78.67

		S1148841144:		#B4q0		1148841144:		$B4q0		d-		32.67		4.30		26.17		4.08		4.08		4.07		4.08		4.08		4.07		4.08		4.07		0		-23328.47		1:38:13		0:35:00		m		2.45		79.84

		S1148841174:		#B4q0		1148841174:		$B4q0		d-		32.67		4.33		26.07		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23329.56		1:38:43		0:35:30		m		2.49		81.02

		S1148841204:		#B4q0		1148841204:		$B4q0		d-		32.67		4.33		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23330.82		1:39:13		0:36:00		m		2.52		82.20

		S1148841234:		#B4q0		1148841234:		$B4q0		d-		32.67		4.30		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23331.92		1:39:43		0:36:30		m		2.56		83.37

		S1148841264:		#B4q0		1148841264:		$B4q0		d-		32.64		4.33		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23333.17		1:40:13		0:37:00		m		2.59		84.55

		S1148841294:		#B4q0		1148841294:		$B4q0		d-		32.67		4.30		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23334.27		1:40:43		0:37:30		m		2.63		85.72

		S1148841324:		#B4q0		1148841324:		$B4q0		d-		32.64		4.33		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23335.53		1:41:13		0:38:00		m		2.67		86.89

		S1148841354:		#B4q0		1148841354:		$B4q0		d-		32.64		4.33		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23336.62		1:41:43		0:38:30		m		2.70		88.07

		S1148841384:		#B4q0		1148841384:		$B4q0		d-		32.64		4.30		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23337.88		1:42:13		0:39:00		m		2.74		89.25

		S1148841414:		#B4q0		1148841414:		$B4q0		d-		32.64		4.30		26.17		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07		0		-23338.97		1:42:43		0:39:30		m		2.77		90.41

		S1148841444:		#B4q0		1148841444:		$B4q0		d-		32.64		4.30		26.17		4.08		4.07		4.07		4.07		4.08		4.07		4.08		4.06		0		-23340.23		1:43:13		0:40:00		m		2.81		91.58

		S1148841475:		#B4q0		1148841475:		$B4q0		d-		32.64		4.30		26.17		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23341.32		1:43:43		0:40:30		m		2.85		92.75

		S1148841504:		#B4q0		1148841504:		$B4q0		d-		32.64		4.33		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23342.57		1:44:13		0:41:00		m		2.88		93.93

		S1148841534:		#B4q0		1148841534:		$B4q0		d-		32.60		4.30		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23343.67		1:44:43		0:41:30		m		2.92		95.10

		S1148841565:		#B4q0		1148841565:		$B4q0		d-		32.60		4.33		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23344.92		1:45:14		0:42:01		m		2.95		96.31

		S1148841594:		#B4q0		1148841594:		$B4q0		d-		32.60		4.30		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23346.02		1:45:43		0:42:30		m		2.99		97.44

		S1148841624:		#B4q0		1148841624:		$B4q0		d-		32.60		4.30		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23347.27		1:46:13		0:43:00		m		3.03		98.61

		S1148841654:		#B4q0		1148841654:		$B4q0		d-		32.60		4.30		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06		0		-23348.37		1:46:43		0:43:30		m		3.06		99.78

		S1148841684:		#B4q0		1148841684:		$B4q0		d-		32.60		4.37		26.36		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06		0		-23349.62		1:47:13		0:44:00		m		3.10		100.96

		S1148841714:		#B4q0		1148841714:		$B4q0		d-		32.60		4.30		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06		0		-23350.72		1:47:43		0:44:30		m		3.13		102.14

		S1148841744:		#B4q0		1148841744:		$B4q0		d-		32.60		4.33		26.26		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06		0		-23351.97		1:48:13		0:45:00		m		3.17		103.31

		S1148841774:		#B4q0		1148841774:		$B4q0		d-		32.60		4.33		26.26		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06		0		-23353.07		1:48:43		0:45:30		m		3.21		104.49

		S1148841804:		#B4q0		1148841804:		$B4q0		d-		32.56		4.33		26.36		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06		0		-23354.32		1:49:13		0:46:00		m		3.24		105.66

		S1148841834:		#B4q0		1148841835:		$B4q0		d-		32.60		4.33		26.36		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06		0		-23355.41		1:49:43		0:46:30		m		3.28		106.84

		S1148841864:		#B4q0		1148841865:		$B4q0		d-		32.56		4.33		26.36		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06		0		-23356.66		1:50:13		0:47:00		m		3.31		108.01

		S1148841894:		#B4q0		1148841894:		$B4q0		d-		32.56		4.30		26.36		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06		0		-23357.76		1:50:43		0:47:30		m		3.35		109.18

		S1148841924:		#B4q0		1148841924:		$B4q0		d-		32.56		4.30		26.36		4.07		4.07		4.07		4.06		4.07		4.06		4.07		4.05		0		-23359.01		1:51:13		0:48:00		m		3.39		110.35

		S1148841954:		#B4q0		1148841954:		$B4q0		d-		32.56		4.33		26.36		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23360.11		1:51:43		0:48:30		m		3.42		111.52

		S1148841984:		#B4q0		1148841984:		$B4q0		d-		32.56		4.37		26.36		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23361.36		1:52:13		0:49:00		m		3.46		112.70

		S1148842014:		#B4q0		1148842014:		$B4q0		d-		32.56		4.33		26.36		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23362.45		1:52:43		0:49:30		m		3.49		113.88

		S1148842044:		#B4q0		1148842044:		$B4q0		d-		32.60		4.33		26.36		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23363.71		1:53:13		0:50:00		m		3.53		115.06

		S1148842074:		#B4q0		1148842074:		$B4q0		d-		32.56		4.30		26.36		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23364.8		1:53:43		0:50:30		m		3.57		116.23

		S1148842104:		#B4q0		1148842104:		$B4q0		d-		32.52		4.33		26.46		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23366.06		1:54:13		0:51:00		m		3.60		117.40

		S1148842134:		#B4q0		1148842134:		$B4q0		d-		32.56		4.33		26.46		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23367.15		1:54:43		0:51:30		m		3.64		118.57

		S1148842164:		#B4q0		1148842164:		$B4q0		d-		32.56		4.30		26.46		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05		0		-23368.4		1:55:13		0:52:00		m		3.67		119.74

		S1148842194:		#B4q0		1148842194:		$B4q0		d-		32.56		4.33		26.46		4.07		4.07		4.06		4.06		4.06		4.06		4.07		4.05		0		-23369.49		1:55:43		0:52:30		m		3.71		120.91

		S1148842224:		#B4q0		1148842224:		$B4q0		d-		32.52		4.33		26.46		4.07		4.07		4.06		4.06		4.06		4.06		4.07		4.05		0		-23370.74		1:56:13		0:53:00		m		3.75		122.09

		S1148842254:		#B4q0		1148842254:		$B4q0		d-		32.52		4.30		26.46		4.07		4.06		4.06		4.06		4.06		4.06		4.07		4.05		0		-23371.84		1:56:43		0:53:30		m		3.78		123.26

		S1148842284:		#B4q0		1148842284:		$B4q0		d-		32.52		4.33		26.46		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05		0		-23373.08		1:57:13		0:54:00		m		3.82		124.43

		S1148842314:		#B4q0		1148842314:		$B4q0		d-		32.52		4.33		26.46		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05		0		-23374.17		1:57:43		0:54:30		m		3.85		125.60

		S1148842344:		#B4q0		1148842344:		$B4q0		d-		32.52		4.33		26.56		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05		0		-23375.43		1:58:13		0:55:00		m		3.89		126.77

		S1148842374:		#B4q0		1148842374:		$B4q0		d-		32.52		4.33		26.46		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05		0		-23376.52		1:58:43		0:55:30		m		3.93		127.95

		S1148842404:		#B4q0		1148842404:		$B4q0		d-		32.52		4.33		26.56		4.07		4.06		4.06		4.05		4.06		4.05		4.07		4.05		0		-23377.77		1:59:13		0:56:00		m		3.96		129.12

		S1148842434:		#B4q0		1148842434:		$B4q0		d-		32.52		4.30		26.56		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05		0		-23378.86		1:59:43		0:56:30		m		4.00		130.29

		S1148842464:		#B4q0		1148842464:		$B4q0		d-		32.52		4.33		26.56		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05		0		-23380.1		2:00:13		0:57:00		m		4.03		131.46

		S1148842494:		#B4q0		1148842494:		$B4q0		d-		32.52		4.33		26.56		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05		0		-23381.2		2:00:43		0:57:30		m		4.07		132.63

		S1148842524:		#B4q0		1148842524:		$B4q0		d-		32.48		4.33		26.56		4.07		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23382.45		2:01:13		0:58:00		m		4.11		133.81

		S1148842554:		#B4q0		1148842554:		$B4q0		d-		32.52		4.33		26.56		4.07		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23383.55		2:01:43		0:58:30		m		4.14		134.98

		S1148842584:		#B4q0		1148842584:		$B4q0		d-		32.48		4.33		26.56		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23384.8		2:02:13		0:59:00		m		4.18		136.15

		S1148842614:		#B4q0		1148842614:		$B4q0		d-		32.48		4.30		26.56		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23385.89		2:02:43		0:59:30		m		4.21		137.32

		S1148842644:		#B4q0		1148842644:		$B4q0		d-		32.52		4.33		26.56		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23387.14		2:03:13		1:00:00		m		4.25		138.49

		S1148842674:		#B4q0		1148842674:		$B4q0		d-		32.48		4.30		26.56		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05		0		-23388.24		2:03:43		1:00:30		m		4.29		139.66

		S1148842704:		#B4q0		1148842704:		$B4q0		d-		32.48		4.33		26.56		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04		0		-23389.49		2:04:13		1:01:00		m		4.32		140.82

		S1148842734:		#B4q0		1148842734:		$B4q0		d-		32.48		4.33		26.56		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04		0		-23390.58		2:04:43		1:01:30		m		4.36		142.00

		S1148842764:		#B4q0		1148842764:		$B4q0		d-		32.48		4.30		26.56		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04		0		-23391.83		2:05:13		1:02:00		m		4.39		143.16

		S1148842794:		#B4q0		1148842794:		$B4q0		d-		32.45		4.33		26.56		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04		0		-23392.92		2:05:43		1:02:30		m		4.43		144.33

		S1148842824:		#B4q0		1148842824:		$B4q0		d-		32.48		4.33		26.56		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04		0		-23394.17		2:06:13		1:03:00		m		4.47		145.50

		S1148842854:		#B4q0		1148842854:		$B4q0		d-		32.48		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04		0		-23395.25		2:06:43		1:03:30		m		4.50		146.67

		S1148842884:		#B4q0		1148842884:		$B4q0		d-		32.48		4.30		26.56		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04		0		-23396.5		2:07:13		1:04:00		m		4.54		147.84

		S1148842914:		#B4q0		1148842914:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04		0		-23397.59		2:07:43		1:04:30		m		4.57		149.01

		S1148842944:		#B4q0		1148842944:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23398.84		2:08:13		1:05:00		m		4.61		150.18

		S1148842974:		#B4q0		1148842974:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23399.93		2:08:43		1:05:30		m		4.65		151.35

		S1148843004:		#B4q0		1148843004:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23401.18		2:09:13		1:06:00		m		4.68		152.52

		S1148843034:		#B4q0		1148843034:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23402.27		2:09:43		1:06:30		m		4.72		153.69

		S1148843064:		#B4q0		1148843064:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23403.52		2:10:13		1:07:00		m		4.75		154.86

		S1148843094:		#B4q0		1148843094:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04		0		-23404.61		2:10:43		1:07:30		m		4.79		156.04

		S1148843124:		#B4q0		1148843124:		$B4q0		d-		32.45		4.33		26.66		4.06		4.05		4.05		4.05		4.05		4.04		4.05		4.04		0		-23405.85		2:11:13		1:08:00		m		4.83		157.21

		S1148843154:		#B4q0		1148843154:		$B4q0		d-		32.45		4.37		26.66		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.04		0		-23406.94		2:11:43		1:08:30		m		4.86		158.38

		S1148843184:		#B4q0		1148843184:		$B4q0		d-		32.41		4.33		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.04		0		-23408.19		2:12:13		1:09:00		m		4.90		159.56

		S1148843214:		#B4q0		1148843214:		$B4q0		d-		32.45		4.30		26.66		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23409.28		2:12:43		1:09:30		m		4.94		160.72

		S1148843244:		#B4q0		1148843244:		$B4q0		d-		32.41		4.30		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23410.52		2:13:13		1:10:00		m		4.97		161.89

		S1148843274:		#B4q0		1148843275:		$B4q0		d-		32.45		4.30		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23411.61		2:13:43		1:10:30		m		5.01		163.05

		S1148843304:		#B4q0		1148843304:		$B4q0		d-		32.41		4.30		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23412.86		2:14:13		1:11:00		m		5.04		164.21

		S1148843334:		#B4q0		1148843334:		$B4q0		d-		32.41		4.33		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23413.95		2:14:43		1:11:30		m		5.08		165.38

		S1148843364:		#B4q0		1148843364:		$B4q0		d-		32.41		4.33		26.75		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03		0		-23415.2		2:15:13		1:12:00		m		5.12		166.55

		S1148843394:		#B4q0		1148843394:		$B4q0		d-		32.41		4.30		26.75		4.05		4.05		4.04		4.04		4.05		4.04		4.05		4.03		0		-23416.28		2:15:43		1:12:30		m		5.15		167.71

		S1148843424:		#B4q0		1148843424:		$B4q0		d-		32.41		4.26		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23417.53		2:16:13		1:13:00		m		5.19		168.87

		S1148843454:		#B4q0		1148843454:		$B4q0		d-		32.41		4.30		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23418.62		2:16:43		1:13:30		m		5.22		170.02

		S1148843484:		#B4q0		1148843484:		$B4q0		d-		32.37		4.33		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23419.86		2:17:13		1:14:00		m		5.26		171.19

		S1148843514:		#B4q0		1148843514:		$B4q0		d-		32.41		4.33		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23420.96		2:17:43		1:14:30		m		5.29		172.36

		S1148843544:		#B4q0		1148843544:		$B4q0		d-		32.37		4.33		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23422.2		2:18:13		1:15:00		m		5.33		173.52

		S1148843574:		#B4q0		1148843574:		$B4q0		d-		32.37		4.33		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23423.29		2:18:43		1:15:30		m		5.37		174.69

		S1148843604:		#B4q0		1148843604:		$B4q0		d-		32.37		4.30		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23424.54		2:19:13		1:16:00		m		5.40		175.86

		S1148843634:		#B4q0		1148843634:		$B4q0		d-		32.37		4.33		26.75		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03		0		-23425.62		2:19:43		1:16:30		m		5.44		177.02

		S1148843664:		#B4q0		1148843664:		$B4q0		d-		32.37		4.33		26.75		4.05		4.05		4.04		4.03		4.04		4.03		4.05		4.03		0		-23426.87		2:20:13		1:17:00		m		5.47		178.19

		S1148843694:		#B4q0		1148843694:		$B4q0		d-		32.37		4.26		26.75		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03		0		-23427.96		2:20:43		1:17:30		m		5.51		179.35

		S1148843724:		#B4q0		1148843724:		$B4q0		d-		32.37		4.33		26.75		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03		0		-23429.2		2:21:13		1:18:00		m		5.55		180.51

		S1148843754:		#B4q0		1148843754:		$B4q0		d-		32.37		4.33		26.85		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03		0		-23430.29		2:21:43		1:18:30		m		5.58		181.67

		S1148843784:		#B4q0		1148843784:		$B4q0		d-		32.37		4.33		26.75		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03		0		-23431.54		2:22:13		1:19:00		m		5.62		182.84

		S1148843814:		#B4q0		1148843814:		$B4q0		d-		32.37		4.33		26.85		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03		0		-23432.63		2:22:43		1:19:30		m		5.65		184.01

		S1148843844:		#B4q0		1148843844:		$B4q0		d-		32.37		4.33		26.85		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03		0		-23433.87		2:23:13		1:20:00		m		5.69		185.18

		S1148843874:		#B4q0		1148843874:		$B4q0		d-		32.33		4.30		26.85		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03		0		-23434.97		2:23:43		1:20:30		m		5.73		186.34

		S1148843904:		#B4q0		1148843904:		$B4q0		d-		32.37		4.30		26.85		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03		0		-23436.21		2:24:13		1:21:00		m		5.76		187.50

		S1148843934:		#B4q0		1148843934:		$B4q0		d-		32.37		4.33		26.85		4.05		4.04		4.04		4.03		4.03		4.03		4.04		4.03		0		-23437.3		2:24:43		1:21:30		m		5.80		188.66

		S1148843964:		#B4q0		1148843964:		$B4q0		d-		32.37		4.30		26.85		4.05		4.04		4.04		4.03		4.03		4.03		4.04		4.03		0		-23438.55		2:25:13		1:22:00		m		5.83		189.83

		S1148843994:		#B4q0		1148843994:		$B4q0		d-		32.37		4.37		26.85		4.05		4.04		4.03		4.03		4.03		4.03		4.04		4.03		0		-23439.64		2:25:43		1:22:30		m		5.87		191.00

		S1148844024:		#B4q0		1148844024:		$B4q0		d-		32.37		4.30		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23440.88		2:26:13		1:23:00		m		5.91		192.17

		S1148844054:		#B4q0		1148844054:		$B4q0		d-		32.33		4.33		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23441.96		2:26:43		1:23:30		m		5.94		193.33

		S1148844084:		#B4q0		1148844084:		$B4q0		d-		32.33		4.33		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23443.2		2:27:13		1:24:00		m		5.98		194.50

		S1148844114:		#B4q0		1148844114:		$B4q0		d-		32.33		4.33		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23444.29		2:27:43		1:24:30		m		6.01		195.66

		S1148844144:		#B4q0		1148844144:		$B4q0		d-		32.33		4.33		26.95		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23445.53		2:28:13		1:25:00		m		6.05		196.83

		S1148844174:		#B4q0		1148844174:		$B4q0		d-		32.30		4.33		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23446.62		2:28:43		1:25:30		m		6.09		198.00

		S1148844204:		#B4q0		1148844204:		$B4q0		d-		32.33		4.33		26.85		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23447.87		2:29:13		1:26:00		m		6.12		199.16

		S1148844234:		#B4q0		1148844234:		$B4q0		d-		32.30		4.30		26.95		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23448.95		2:29:43		1:26:30		m		6.16		200.32

		S1148844264:		#B4q0		1148844264:		$B4q0		d-		32.30		4.33		26.95		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02		0		-23450.19		2:30:13		1:27:00		m		6.19		201.49

		S1148844294:		#B4q0		1148844294:		$B4q0		d-		32.30		4.33		26.85		4.04		4.03		4.03		4.03		4.03		4.03		4.04		4.02		0		-23451.28		2:30:43		1:27:30		m		6.23		202.65

		S1148844324:		#B4q0		1148844324:		$B4q0		d-		32.30		4.26		26.85		4.04		4.03		4.03		4.03		4.03		4.03		4.04		4.02		0		-23452.52		2:31:13		1:28:00		m		6.27		203.81

		S1148844354:		#B4q0		1148844354:		$B4q0		d-		32.30		4.26		26.95		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02		0		-23453.61		2:31:43		1:28:30		m		6.30		204.95

		S1148844384:		#B4q0		1148844384:		$B4q0		d-		32.30		4.30		26.95		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02		0		-23454.86		2:32:13		1:29:00		m		6.34		206.11

		S1148844414:		#B4q0		1148844414:		$B4q0		d-		32.30		4.30		26.95		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02		0		-23455.94		2:32:43		1:29:30		m		6.37		207.26

		S1148844444:		#B4q0		1148844444:		$B4q0		d-		32.30		4.33		26.95		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02		0		-23457.19		2:33:13		1:30:00		m		6.41		208.42

		S1148844474:		#B4q0		1148844474:		$B4q0		d-		32.30		4.33		26.95		4.04		4.03		4.03		4.02		4.03		4.03		4.03		4.02		0		-23458.27		2:33:43		1:30:30		m		6.45		209.59

		S1148844504:		#B4q0		1148844504:		$B4q0		d-		32.30		4.33		26.95		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.02		0		-23459.51		2:34:13		1:31:00		m		6.48		210.76

		S1148844534:		#B4q0		1148844534:		$B4q0		d-		32.30		4.26		26.95		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.02		0		-23460.6		2:34:43		1:31:30		m		6.52		211.91

		S1148844564:		#B4q0		1148844564:		$B4q0		d-		32.30		4.30		26.95		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23461.84		2:35:13		1:32:00		m		6.55		213.06

		S1148844594:		#B4q0		1148844594:		$B4q0		d-		32.30		4.33		26.95		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23462.93		2:35:43		1:32:30		m		6.59		214.23

		S1148844624:		#B4q0		1148844624:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23464.17		2:36:13		1:33:00		m		6.63		215.39

		S1148844654:		#B4q0		1148844654:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23465.25		2:36:43		1:33:30		m		6.66		216.55

		S1148844684:		#B4q0		1148844684:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23466.49		2:37:13		1:34:00		m		6.70		217.72

		S1148844714:		#B4q0		1148844714:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01		0		-23467.58		2:37:43		1:34:30		m		6.73		218.88

		S1148844744:		#B4q0		1148844744:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01		0		-23468.82		2:38:13		1:35:00		m		6.77		220.05

		S1148844774:		#B4q0		1148844774:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01		0		-23469.91		2:38:43		1:35:30		m		6.81		221.21

		S1148844804:		#B4q0		1148844804:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01		0		-23471.15		2:39:13		1:36:00		m		6.84		222.37

		S1148844834:		#B4q0		1148844834:		$B4q0		d-		32.26		4.33		26.95		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01		0		-23472.24		2:39:43		1:36:30		m		6.88		223.54

		S1148844864:		#B4q0		1148844864:		$B4q0		d-		32.22		4.30		27.05		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01		0		-23473.48		2:40:13		1:37:00		m		6.91		224.70

		S1148844894:		#B4q0		1148844894:		$B4q0		d-		32.22		4.33		26.95		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01		0		-23474.56		2:40:43		1:37:30		m		6.95		225.86

		S1148844924:		#B4q0		1148844924:		$B4q0		d-		32.22		4.26		27.05		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01		0		-23475.8		2:41:13		1:38:00		m		6.99		227.01

		S1148844954:		#B4q0		1148844954:		$B4q0		d-		32.22		4.33		26.95		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01		0		-23476.88		2:41:43		1:38:30		m		7.02		228.16

		S1148844984:		#B4q0		1148844984:		$B4q0		d-		32.26		4.30		27.05		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01		0		-23478.12		2:42:13		1:39:00		m		7.06		229.32

		S1148845014:		#B4q0		1148845014:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.02		4.03		4.01		0		-23479.21		2:42:43		1:39:30		m		7.09		230.48

		S1148845044:		#B4q0		1148845044:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.02		4.03		4.01		0		-23480.44		2:43:13		1:40:00		m		7.13		231.64

		S1148845074:		#B4q0		1148845074:		$B4q0		d-		32.22		4.30		27.05		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01		0		-23481.53		2:43:43		1:40:30		m		7.17		232.80

		S1148845104:		#B4q0		1148845104:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01		0		-23482.77		2:44:13		1:41:00		m		7.20		233.96

		S1148845134:		#B4q0		1148845134:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01		0		-23483.85		2:44:43		1:41:30		m		7.24		235.12

		S1148845164:		#B4q0		1148845164:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01		0		-23485.09		2:45:13		1:42:00		m		7.27		236.29

		S1148845194:		#B4q0		1148845194:		$B4q0		d-		32.22		4.33		27.05		4.03		4.03		4.02		4.01		4.02		4.01		4.02		4.01		0		-23486.18		2:45:43		1:42:30		m		7.31		237.45

		S1148845224:		#B4q0		1148845224:		$B4q0		d-		32.22		4.33		27.05		4.03		4.02		4.02		4.01		4.02		4.01		4.02		4.01		0		-23487.42		2:46:13		1:43:00		m		7.35		238.61

		S1148845254:		#B4q0		1148845254:		$B4q0		d-		32.22		4.33		27.05		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01		0		-23488.5		2:46:43		1:43:30		m		7.38		239.77

		S1148845284:		#B4q0		1148845284:		$B4q0		d-		32.22		4.30		27.05		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01		0		-23489.74		2:47:13		1:44:00		m		7.42		240.93

		S1148845314:		#B4q0		1148845314:		$B4q0		d-		32.22		4.30		27.05		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01		0		-23490.82		2:47:43		1:44:30		m		7.45		242.09

		S1148845344:		#B4q0		1148845344:		$B4q0		d-		32.22		4.33		27.14		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01		0		-23492.06		2:48:13		1:45:00		m		7.49		243.25

		S1148845374:		#B4q0		1148845374:		$B4q0		d-		32.22		4.33		27.14		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.00		0		-23493.14		2:48:43		1:45:30		m		7.53		244.41

		S1148845404:		#B4q0		1148845404:		$B4q0		d-		32.22		4.33		27.14		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.00		0		-23494.38		2:49:13		1:46:00		m		7.56		245.57

		S1148845434:		#B4q0		1148845434:		$B4q0		d-		32.18		4.33		27.14		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.00		0		-23495.47		2:49:43		1:46:30		m		7.60		246.73

		S1148845464:		#B4q0		1148845464:		$B4q0		d-		32.18		4.30		27.14		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.00		0		-23496.7		2:50:13		1:47:00		m		7.63		247.89

		S1148845494:		#B4q0		1148845494:		$B4q0		d-		32.18		4.33		27.14		4.03		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23497.79		2:50:43		1:47:30		m		7.67		249.05

		S1148845524:		#B4q0		1148845524:		$B4q0		d-		32.18		4.33		27.14		4.03		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23499.02		2:51:13		1:48:00		m		7.71		250.21

		S1148845555:		#B4q0		1148845555:		$B4q0		d-		32.22		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23500.11		2:51:44		1:48:31		m		7.74		251.41

		S1148845584:		#B4q0		1148845584:		$B4q0		d-		32.14		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23501.35		2:52:13		1:49:00		m		7.78		252.53

		S1148845614:		#B4q0		1148845614:		$B4q0		d-		32.18		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23502.43		2:52:43		1:49:30		m		7.81		253.69

		S1148845644:		#B4q0		1148845644:		$B4q0		d-		32.18		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23503.67		2:53:13		1:50:00		m		7.85		254.85

		S1148845674:		#B4q0		1148845674:		$B4q0		d-		32.14		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23504.74		2:53:43		1:50:30		m		7.89		256.01

		S1148845704:		#B4q0		1148845704:		$B4q0		d-		32.14		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23505.98		2:54:13		1:51:00		m		7.92		257.17

		S1148845734:		#B4q0		1148845734:		$B4q0		d-		32.14		4.33		27.14		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4.00		0		-23507.07		2:54:43		1:51:30		m		7.96		258.33

		S1148845764:		#B4q0		1148845764:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.01		4.02		4.00		0		-23508.3		2:55:13		1:52:00		m		7.99		259.49

		S1148845794:		#B4q0		1148845794:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.01		4.01		4.01		4.01		4.00		0		-23509.38		2:55:43		1:52:30		m		8.03		260.65

		S1148845824:		#B4q0		1148845824:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.01		4.01		4.00		0		-23510.61		2:56:13		1:53:00		m		8.07		261.81

		S1148845854:		#B4q0		1148845854:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.01		4.01		4.00		0		-23511.69		2:56:43		1:53:30		m		8.10		262.97

		S1148845884:		#B4q0		1148845884:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.00		4.01		4.00		0		-23512.93		2:57:13		1:54:00		m		8.14		264.13

		S1148845914:		#B4q0		1148845914:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.00		4.01		4.00		0		-23514.01		2:57:43		1:54:30		m		8.17		265.29

		S1148845944:		#B4q0		1148845944:		$B4q0		d-		32.14		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.00		4.01		4.00		0		-23515.25		2:58:13		1:55:00		m		8.21		266.45

		S1148845974:		#B4q0		1148845974:		$B4q0		d-		32.10		4.33		27.14		4.02		4.01		4.01		4.00		4.01		4.00		4.01		4.00		0		-23516.33		2:58:43		1:55:30		m		8.25		267.61

		S1148846004:		#B4q0		1148846004:		$B4q0		d-		32.10		4.33		27.14		4.02		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23517.57		2:59:13		1:56:00		m		8.28		268.77

		S1148846034:		#B4q0		1148846034:		$B4q0		d-		32.10		4.33		27.14		4.02		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23518.65		2:59:43		1:56:30		m		8.32		269.93

		S1148846064:		#B4q0		1148846064:		$B4q0		d-		32.14		4.37		27.14		4.02		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23519.89		3:00:13		1:57:00		m		8.36		271.09

		S1148846094:		#B4q0		1148846094:		$B4q0		d-		32.14		4.30		27.14		4.02		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23520.97		3:00:43		1:57:30		m		8.39		272.25

		S1148846124:		#B4q0		1148846124:		$B4q0		d-		32.14		4.26		27.14		4.01		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23522.21		3:01:13		1:58:00		m		8.43		273.40

		S1148846154:		#B4q0		1148846154:		$B4q0		d-		32.10		4.33		27.14		4.01		4.01		4.01		4.00		4.00		4.00		4.01		4.00		0		-23523.29		3:01:43		1:58:30		m		8.46		274.55

		S1148846184:		#B4q0		1148846184:		$B4q0		d-		32.10		4.30		27.14		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23524.52		3:02:13		1:59:00		m		8.50		275.70

		S1148846214:		#B4q0		1148846214:		$B4q0		d-		32.10		4.33		27.14		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23525.6		3:02:43		1:59:30		m		8.53		276.86

		S1148846244:		#B4q0		1148846244:		$B4q0		d-		32.10		4.30		27.24		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23526.84		3:03:13		2:00:00		m		8.57		278.01

		S1148846274:		#B4q0		1148846274:		$B4q0		d-		32.10		4.33		27.24		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23527.92		3:03:43		2:00:30		m		8.61		279.16

		S1148846304:		#B4q0		1148846305:		$B4q0		d-		32.10		4.30		27.24		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23529.16		3:04:13		2:01:00		m		8.64		280.32

		S1148846334:		#B4q0		1148846334:		$B4q0		d-		32.10		4.33		27.24		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23530.23		3:04:43		2:01:30		m		8.68		281.47

		S1148846364:		#B4q0		1148846364:		$B4q0		d-		32.07		4.33		27.24		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23531.47		3:05:13		2:02:00		m		8.71		282.63

		S1148846394:		#B4q0		1148846394:		$B4q0		d-		32.10		4.33		27.14		4.01		4.01		4.01		4.00		4.00		4.00		4.01		3.99		0		-23532.55		3:05:43		2:02:30		m		8.75		283.79

		S1148846424:		#B4q0		1148846424:		$B4q0		d-		32.07		4.30		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23533.78		3:06:13		2:03:00		m		8.79		284.94

		S1148846454:		#B4q0		1148846454:		$B4q0		d-		32.10		4.33		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23534.86		3:06:43		2:03:30		m		8.82		286.10

		S1148846484:		#B4q0		1148846484:		$B4q0		d-		32.10		4.33		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23536.1		3:07:13		2:04:00		m		8.86		287.25

		S1148846514:		#B4q0		1148846514:		$B4q0		d-		32.07		4.30		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23537.18		3:07:43		2:04:30		m		8.89		288.41

		S1148846544:		#B4q0		1148846544:		$B4q0		d-		32.10		4.30		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23538.41		3:08:13		2:05:00		m		8.93		289.56

		S1148846574:		#B4q0		1148846574:		$B4q0		d-		32.07		4.33		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.01		3.99		0		-23539.49		3:08:43		2:05:30		m		8.97		290.71

		S1148846604:		#B4q0		1148846604:		$B4q0		d-		32.07		4.33		27.24		4.01		4.01		4.00		3.99		4.00		4.00		4.00		3.99		0		-23540.72		3:09:13		2:06:00		m		9.00		291.87

		S1148846634:		#B4q0		1148846634:		$B4q0		d-		32.03		4.33		27.24		4.01		4.01		4.00		4.00		4.00		4.00		4.00		3.99		0		-23541.81		3:09:43		2:06:30		m		9.04		293.03

		S1148846664:		#B4q0		1148846664:		$B4q0		d-		32.07		4.33		27.24		4.01		4.01		4.00		3.99		4.00		4.00		4.00		3.99		0		-23543.04		3:10:13		2:07:00		m		9.07		294.18

		S1148846694:		#B4q0		1148846694:		$B4q0		d-		32.07		4.33		27.24		4.01		4.00		4.00		3.99		4.00		4.00		4.00		3.99		0		-23544.11		3:10:43		2:07:30		m		9.11		295.34

		S1148846724:		#B4q0		1148846724:		$B4q0		d-		32.07		4.33		27.24		4.01		4.00		4.00		3.99		4.00		4.00		4.00		3.98		0		-23545.35		3:11:13		2:08:00		m		9.15		296.50

		S1148846754:		#B4q0		1148846754:		$B4q0		d-		32.07		4.33		27.24		4.01		4.00		4.00		3.99		3.99		4.00		4.00		3.98		0		-23546.43		3:11:43		2:08:30		m		9.18		297.65

		S1148846784:		#B4q0		1148846784:		$B4q0		d-		32.03		4.30		27.24		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23547.66		3:12:13		2:09:00		m		9.22		298.81

		S1148846814:		#B4q0		1148846814:		$B4q0		d-		32.03		4.30		27.24		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23548.74		3:12:43		2:09:30		m		9.25		299.95

		S1148846844:		#B4q0		1148846844:		$B4q0		d-		32.03		4.30		27.24		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23549.97		3:13:13		2:10:00		m		9.29		301.10

		S1148846874:		#B4q0		1148846874:		$B4q0		d-		32.03		4.30		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23551.05		3:13:43		2:10:30		m		9.33		302.25

		S1148846904:		#B4q0		1148846904:		$B4q0		d-		32.03		4.33		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23552.28		3:14:13		2:11:00		m		9.36		303.40

		S1148846934:		#B4q0		1148846934:		$B4q0		d-		32.03		4.33		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23553.36		3:14:43		2:11:30		m		9.40		304.56

		S1148846964:		#B4q0		1148846964:		$B4q0		d-		31.99		4.30		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23554.59		3:15:13		2:12:00		m		9.43		305.71

		S1148846994:		#B4q0		1148846994:		$B4q0		d-		32.03		4.33		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23555.67		3:15:43		2:12:30		m		9.47		306.86

		S1148847024:		#B4q0		1148847024:		$B4q0		d-		32.03		4.30		27.34		4.01		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23556.9		3:16:13		2:13:00		m		9.51		308.01

		S1148847054:		#B4q0		1148847054:		$B4q0		d-		32.03		4.30		27.34		4.00		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23557.98		3:16:43		2:13:30		m		9.54		309.16

		S1148847084:		#B4q0		1148847084:		$B4q0		d-		32.03		4.33		27.34		4.00		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23559.21		3:17:13		2:14:00		m		9.58		310.31

		S1148847114:		#B4q0		1148847114:		$B4q0		d-		31.99		4.30		27.34		4.00		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23560.29		3:17:43		2:14:30		m		9.61		311.46

		S1148847144:		#B4q0		1148847144:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		4.00		3.99		3.99		3.99		4.00		3.98		0		-23561.51		3:18:13		2:15:00		m		9.65		312.61

		S1148847174:		#B4q0		1148847174:		$B4q0		d-		31.99		4.30		27.34		4.00		4.00		4.00		3.98		3.99		3.99		4.00		3.98		0		-23562.59		3:18:43		2:15:30		m		9.69		313.76

		S1148847204:		#B4q0		1148847204:		$B4q0		d-		31.99		4.30		27.34		4.00		4.00		4.00		3.98		3.99		3.99		4.00		3.98		0		-23563.82		3:19:13		2:16:00		m		9.72		314.91

		S1148847234:		#B4q0		1148847234:		$B4q0		d-		31.99		4.30		27.34		4.00		4.00		4.00		3.98		3.99		3.99		4.00		3.98		0		-23564.9		3:19:43		2:16:30		m		9.76		316.05

		S1148847264:		#B4q0		1148847264:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		4.00		3.98		3.99		3.99		4.00		3.98		0		-23566.13		3:20:13		2:17:00		m		9.79		317.20

		S1148847294:		#B4q0		1148847294:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		4.00		3.98		3.98		3.99		4.00		3.98		0		-23567.21		3:20:43		2:17:30		m		9.83		318.36

		S1148847324:		#B4q0		1148847324:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		4.00		3.98		3.98		3.99		4.00		3.98		0		-23568.44		3:21:13		2:18:00		m		9.87		319.51

		S1148847354:		#B4q0		1148847354:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		4.00		3.98		0		-23569.52		3:21:43		2:18:30		m		9.90		320.67

		S1148847384:		#B4q0		1148847384:		$B4q0		d-		31.96		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		4.00		3.98		0		-23570.75		3:22:13		2:19:00		m		9.94		321.82

		S1148847414:		#B4q0		1148847414:		$B4q0		d-		31.99		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		4.00		3.98		0		-23571.82		3:22:43		2:19:30		m		9.97		322.98

		S1148847444:		#B4q0		1148847444:		$B4q0		d-		31.96		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		4.00		3.98		0		-23573.05		3:23:13		2:20:00		m		10.01		324.13

		S1148847474:		#B4q0		1148847474:		$B4q0		d-		31.96		4.30		27.34		4.00		4.00		3.99		3.98		3.98		3.98		4.00		3.98		0		-23574.13		3:23:43		2:20:30		m		10.05		325.28

		S1148847504:		#B4q0		1148847504:		$B4q0		d-		31.96		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		3.99		3.98		0		-23575.36		3:24:13		2:21:00		m		10.08		326.43

		S1148847534:		#B4q0		1148847534:		$B4q0		d-		31.99		4.33		27.44		4.00		4.00		3.99		3.98		3.98		3.98		3.99		3.98		0		-23576.43		3:24:43		2:21:30		m		10.12		327.58

		S1148847564:		#B4q0		1148847564:		$B4q0		d-		31.96		4.37		27.44		4.00		4.00		3.99		3.98		3.98		3.98		3.99		3.98		0		-23577.66		3:25:13		2:22:00		m		10.15		328.74

		S1148847594:		#B4q0		1148847594:		$B4q0		d-		31.96		4.33		27.34		4.00		4.00		3.99		3.98		3.98		3.98		3.99		3.98		0		-23578.74		3:25:43		2:22:30		m		10.19		329.90

		S1148847624:		#B4q0		1148847624:		$B4q0		d-		31.96		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23579.97		3:26:13		2:23:00		m		10.23		331.05

		S1148847654:		#B4q0		1148847654:		$B4q0		d-		31.96		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23581.04		3:26:43		2:23:30		m		10.26		332.21

		S1148847684:		#B4q0		1148847684:		$B4q0		d-		31.92		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23582.27		3:27:13		2:24:00		m		10.30		333.36

		S1148847714:		#B4q0		1148847714:		$B4q0		d-		31.96		4.37		27.44		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23583.35		3:27:43		2:24:30		m		10.34		334.52

		S1148847744:		#B4q0		1148847744:		$B4q0		d-		31.92		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23584.58		3:28:13		2:25:00		m		10.37		335.67

		S1148847774:		#B4q0		1148847774:		$B4q0		d-		31.96		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23585.66		3:28:43		2:25:30		m		10.41		336.83

		S1148847804:		#B4q0		1148847804:		$B4q0		d-		31.92		4.37		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23586.88		3:29:13		2:26:00		m		10.44		337.98

		S1148847834:		#B4q0		1148847834:		$B4q0		d-		31.96		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23587.96		3:29:43		2:26:30		m		10.48		339.14

		S1148847864:		#B4q0		1148847864:		$B4q0		d-		31.96		4.33		27.34		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23589.19		3:30:13		2:27:00		m		10.52		340.29

		S1148847894:		#B4q0		1148847894:		$B4q0		d-		31.92		4.30		27.44		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23590.26		3:30:43		2:27:30		m		10.55		341.44

		S1148847924:		#B4q0		1148847924:		$B4q0		d-		31.92		4.33		27.44		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23591.49		3:31:13		2:28:00		m		10.59		342.59

		S1148847954:		#B4q0		1148847954:		$B4q0		d-		31.92		4.30		27.44		4.00		3.99		3.99		3.98		3.98		3.98		3.99		3.97		0		-23592.57		3:31:43		2:28:30		m		10.62		343.74

		S1148847984:		#B4q0		1148847984:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.98		3.98		3.98		3.99		3.97		0		-23593.8		3:32:13		2:29:00		m		10.66		344.89

		S1148848014:		#B4q0		1148848014:		$B4q0		d-		31.92		4.33		27.34		3.99		3.99		3.98		3.98		3.98		3.98		3.99		3.97		0		-23594.87		3:32:43		2:29:30		m		10.70		346.04

		S1148848044:		#B4q0		1148848044:		$B4q0		d-		31.92		4.30		27.44		3.99		3.99		3.98		3.97		3.98		3.98		3.99		3.97		0		-23596.1		3:33:13		2:30:00		m		10.73		347.19

		S1148848074:		#B4q0		1148848074:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.98		3.99		3.97		0		-23597.17		3:33:43		2:30:30		m		10.77		348.33

		S1148848104:		#B4q0		1148848104:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.98		3.99		3.97		0		-23598.4		3:34:13		2:31:00		m		10.80		349.49

		S1148848134:		#B4q0		1148848134:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97		0		-23599.47		3:34:43		2:31:30		m		10.84		350.64

		S1148848164:		#B4q0		1148848164:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97		0		-23600.7		3:35:13		2:32:00		m		10.88		351.79

		S1148848194:		#B4q0		1148848194:		$B4q0		d-		31.88		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97		0		-23601.77		3:35:43		2:32:30		m		10.91		352.94

		S1148848224:		#B4q0		1148848224:		$B4q0		d-		31.92		4.33		27.44		3.99		3.99		3.98		3.97		3.97		3.97		3.98		3.96		0		-23603		3:36:13		2:33:00		m		10.95		354.09

		S1148848254:		#B4q0		1148848254:		$B4q0		d-		31.88		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23604.08		3:36:43		2:33:30		m		10.98		355.24

		S1148848284:		#B4q0		1148848284:		$B4q0		d-		31.92		4.30		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23605.3		3:37:13		2:34:00		m		11.02		356.39

		S1148848314:		#B4q0		1148848314:		$B4q0		d-		31.92		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23606.37		3:37:43		2:34:30		m		11.06		357.54

		S1148848344:		#B4q0		1148848344:		$B4q0		d-		31.88		4.33		27.53		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23607.6		3:38:13		2:35:00		m		11.09		358.69

		S1148848374:		#B4q0		1148848374:		$B4q0		d-		31.88		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23608.67		3:38:43		2:35:30		m		11.13		359.84

		S1148848404:		#B4q0		1148848404:		$B4q0		d-		31.88		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23609.9		3:39:13		2:36:00		m		11.16		360.99

		S1148848434:		#B4q0		1148848434:		$B4q0		d-		31.88		4.30		27.53		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23610.97		3:39:43		2:36:30		m		11.20		362.14

		S1148848464:		#B4q0		1148848464:		$B4q0		d-		31.88		4.26		27.53		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23612.2		3:40:13		2:37:00		m		11.24		363.27

		S1148848494:		#B4q0		1148848494:		$B4q0		d-		31.88		4.30		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23613.27		3:40:43		2:37:30		m		11.27		364.41

		S1148848524:		#B4q0		1148848524:		$B4q0		d-		31.88		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23614.5		3:41:13		2:38:00		m		11.31		365.56

		S1148848554:		#B4q0		1148848554:		$B4q0		d-		31.88		4.33		27.53		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23615.57		3:41:43		2:38:30		m		11.34		366.71

		S1148848584:		#B4q0		1148848584:		$B4q0		d-		31.88		4.33		27.44		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96		0		-23616.79		3:42:13		2:39:00		m		11.38		367.86

		S1148848614:		#B4q0		1148848614:		$B4q0		d-		31.84		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23617.86		3:42:43		2:39:30		m		11.42		369.01

		S1148848644:		#B4q0		1148848644:		$B4q0		d-		31.84		4.33		27.44		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23619.09		3:43:13		2:40:00		m		11.45		370.15

		S1148848674:		#B4q0		1148848674:		$B4q0		d-		31.84		4.30		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23620.16		3:43:43		2:40:30		m		11.49		371.30

		S1148848704:		#B4q0		1148848704:		$B4q0		d-		31.84		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23621.38		3:44:13		2:41:00		m		11.52		372.44

		S1148848734:		#B4q0		1148848734:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23622.45		3:44:43		2:41:30		m		11.56		373.59

		S1148848764:		#B4q0		1148848764:		$B4q0		d-		31.80		4.30		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23623.68		3:45:13		2:42:00		m		11.60		374.74

		S1148848794:		#B4q0		1148848794:		$B4q0		d-		31.84		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23624.75		3:45:43		2:42:30		m		11.63		375.88

		S1148848824:		#B4q0		1148848824:		$B4q0		d-		31.84		4.30		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23625.98		3:46:13		2:43:00		m		11.67		377.03

		S1148848854:		#B4q0		1148848854:		$B4q0		d-		31.84		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96		0		-23627.05		3:46:43		2:43:30		m		11.70		378.17

		S1148848884:		#B4q0		1148848884:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.98		3.96		3.96		3.96		3.98		3.96		0		-23628.27		3:47:13		2:44:00		m		11.74		379.32

		S1148848914:		#B4q0		1148848914:		$B4q0		d-		31.80		4.30		27.53		3.98		3.98		3.98		3.96		3.96		3.96		3.98		3.96		0		-23629.34		3:47:43		2:44:30		m		11.78		380.46

		S1148848944:		#B4q0		1148848944:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.98		3.96		0		-23630.57		3:48:13		2:45:00		m		11.81		381.61

		S1148848974:		#B4q0		1148848974:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.98		3.96		0		-23631.64		3:48:43		2:45:30		m		11.85		382.75

		S1148849004:		#B4q0		1148849004:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96		0		-23632.86		3:49:13		2:46:00		m		11.88		383.90

		S1148849034:		#B4q0		1148849034:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96		0		-23633.92		3:49:43		2:46:30		m		11.92		385.05

		S1148849064:		#B4q0		1148849064:		$B4q0		d-		31.80		4.30		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96		0		-23635.15		3:50:13		2:47:00		m		11.96		386.19

		S1148849094:		#B4q0		1148849094:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95		0		-23636.22		3:50:43		2:47:30		m		11.99		387.33

		S1148849124:		#B4q0		1148849124:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95		0		-23637.44		3:51:13		2:48:00		m		12.03		388.48

		S1148849154:		#B4q0		1148849154:		$B4q0		d-		31.80		4.33		27.53		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95		0		-23638.51		3:51:43		2:48:30		m		12.06		389.63

		S1148849184:		#B4q0		1148849184:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23639.73		3:52:13		2:49:00		m		12.10		390.78

		S1148849214:		#B4q0		1148849214:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23640.8		3:52:43		2:49:30		m		12.14		391.92

		S1148849244:		#B4q0		1148849244:		$B4q0		d-		31.80		4.30		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23642.03		3:53:13		2:50:00		m		12.17		393.07

		S1148849274:		#B4q0		1148849274:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23643.1		3:53:43		2:50:30		m		12.21		394.21

		S1148849304:		#B4q0		1148849304:		$B4q0		d-		31.80		4.30		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23644.32		3:54:13		2:51:00		m		12.24		395.35

		S1148849334:		#B4q0		1148849334:		$B4q0		d-		31.80		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23645.39		3:54:43		2:51:30		m		12.28		396.49

		S1148849364:		#B4q0		1148849364:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23646.61		3:55:13		2:52:00		m		12.32		397.64

		S1148849394:		#B4q0		1148849394:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23647.68		3:55:43		2:52:30		m		12.35		398.79

		S1148849424:		#B4q0		1148849424:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95		0		-23648.91		3:56:13		2:53:00		m		12.39		399.93

		S1148849454:		#B4q0		1148849454:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.96		3.95		3.96		3.97		3.95		0		-23649.98		3:56:43		2:53:30		m		12.42		401.08

		S1148849484:		#B4q0		1148849484:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.95		3.95		3.96		3.97		3.95		0		-23651.2		3:57:13		2:54:00		m		12.46		402.23

		S1148849514:		#B4q0		1148849514:		$B4q0		d-		31.76		4.33		27.53		3.98		3.97		3.97		3.95		3.95		3.96		3.97		3.95		0		-23652.27		3:57:43		2:54:30		m		12.50		403.37

		S1148849544:		#B4q0		1148849544:		$B4q0		d-		31.76		4.33		27.53		3.97		3.97		3.97		3.95		3.95		3.96		3.97		3.95		0		-23653.49		3:58:13		2:55:00		m		12.53		404.52

		S1148849574:		#B4q0		1148849574:		$B4q0		d-		31.76		4.33		27.53		3.97		3.97		3.97		3.95		3.95		3.96		3.97		3.95		0		-23654.56		3:58:43		2:55:30		m		12.57		405.66

		S1148849604:		#B4q0		1148849604:		$B4q0		d-		31.76		4.33		27.53		3.97		3.97		3.96		3.95		3.95		3.96		3.97		3.95		0		-23655.78		3:59:13		2:56:00		m		12.61		406.81

		S1148849634:		#B4q0		1148849634:		$B4q0		d-		31.76		4.33		27.53		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95		0		-23656.85		3:59:43		2:56:30		m		12.64		407.96

		S1148849664:		#B4q0		1148849664:		$B4q0		d-		31.76		4.33		27.63		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95		0		-23658.07		4:00:13		2:57:00		m		12.68		409.10

		S1148849694:		#B4q0		1148849694:		$B4q0		d-		31.76		4.30		27.53		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95		0		-23659.14		4:00:43		2:57:30		m		12.71		410.24

		S1148849724:		#B4q0		1148849724:		$B4q0		d-		31.76		4.33		27.63		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.94		0		-23660.36		4:01:13		2:58:00		m		12.75		411.39

		S1148849754:		#B4q0		1148849754:		$B4q0		d-		31.73		4.30		27.63		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.94		0		-23661.43		4:01:43		2:58:30		m		12.79		412.53

		S1148849784:		#B4q0		1148849784:		$B4q0		d-		31.73		4.30		27.53		3.97		3.97		3.96		3.95		3.95		3.95		3.96		3.94		0		-23662.65		4:02:13		2:59:00		m		12.82		413.66

		S1148849814:		#B4q0		1148849814:		$B4q0		d-		31.76		4.30		27.63		3.97		3.97		3.96		3.95		3.95		3.95		3.96		3.94		0		-23663.72		4:02:43		2:59:30		m		12.86		414.80

		S1148849844:		#B4q0		1148849844:		$B4q0		d-		31.73		4.30		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23664.94		4:03:13		3:00:00		m		12.89		415.94

		S1148849874:		#B4q0		1148849874:		$B4q0		d-		31.73		4.33		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23666		4:03:43		3:00:30		m		12.93		417.08

		S1148849904:		#B4q0		1148849904:		$B4q0		d-		31.73		4.30		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23667.22		4:04:13		3:01:00		m		12.96		418.22

		S1148849934:		#B4q0		1148849934:		$B4q0		d-		31.73		4.33		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23668.29		4:04:43		3:01:30		m		13.00		419.36

		S1148849964:		#B4q0		1148849964:		$B4q0		d-		31.73		4.30		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23669.51		4:05:13		3:02:00		m		13.04		420.50

		S1148849994:		#B4q0		1148849994:		$B4q0		d-		31.73		4.30		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23670.58		4:05:43		3:02:30		m		13.07		421.64

		S1148850024:		#B4q0		1148850024:		$B4q0		d-		31.69		4.37		27.63		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94		0		-23671.8		4:06:13		3:03:00		m		13.11		422.79

		S1148850054:		#B4q0		1148850054:		$B4q0		d-		31.73		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23672.86		4:06:43		3:03:30		m		13.14		423.93

		S1148850084:		#B4q0		1148850084:		$B4q0		d-		31.73		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23674.08		4:07:13		3:04:00		m		13.18		425.08

		S1148850114:		#B4q0		1148850114:		$B4q0		d-		31.69		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23675.15		4:07:43		3:04:30		m		13.22		426.22

		S1148850144:		#B4q0		1148850144:		$B4q0		d-		31.69		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23676.37		4:08:13		3:05:00		m		13.25		427.37

		S1148850174:		#B4q0		1148850174:		$B4q0		d-		31.69		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23677.44		4:08:43		3:05:30		m		13.29		428.51

		S1148850204:		#B4q0		1148850204:		$B4q0		d-		31.69		4.33		27.63		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23678.66		4:09:13		3:06:00		m		13.33		429.65

		S1148850234:		#B4q0		1148850234:		$B4q0		d-		31.69		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23679.72		4:09:43		3:06:30		m		13.36		430.80

		S1148850264:		#B4q0		1148850264:		$B4q0		d-		31.69		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23680.94		4:10:13		3:07:00		m		13.40		431.94

		S1148850294:		#B4q0		1148850294:		$B4q0		d-		31.69		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23682		4:10:43		3:07:30		m		13.43		433.08

		S1148850324:		#B4q0		1148850324:		$B4q0		d-		31.69		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23683.22		4:11:13		3:08:00		m		13.47		434.23

		S1148850354:		#B4q0		1148850354:		$B4q0		d-		31.69		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23684.29		4:11:43		3:08:30		m		13.51		435.37

		S1148850384:		#B4q0		1148850384:		$B4q0		d-		31.69		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94		0		-23685.51		4:12:13		3:09:00		m		13.54		436.51

		S1148850414:		#B4q0		1148850414:		$B4q0		d-		31.65		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23686.57		4:12:43		3:09:30		m		13.58		437.66

		S1148850444:		#B4q0		1148850444:		$B4q0		d-		31.65		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23687.79		4:13:13		3:10:00		m		13.61		438.80

		S1148850474:		#B4q0		1148850474:		$B4q0		d-		31.65		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23688.86		4:13:43		3:10:30		m		13.65		439.94

		S1148850504:		#B4q0		1148850504:		$B4q0		d-		31.65		4.33		27.73		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23690.08		4:14:13		3:11:00		m		13.69		441.08

		S1148850534:		#B4q0		1148850534:		$B4q0		d-		31.65		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23691.14		4:14:43		3:11:30		m		13.72		442.23

		S1148850564:		#B4q0		1148850564:		$B4q0		d-		31.65		4.30		27.63		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94		0		-23692.36		4:15:13		3:12:00		m		13.76		443.36

		S1148850594:		#B4q0		1148850594:		$B4q0		d-		31.65		4.33		27.63		3.96		3.96		3.96		3.94		3.94		3.94		3.95		3.94		0		-23693.43		4:15:43		3:12:30		m		13.79		444.50

		S1148850624:		#B4q0		1148850624:		$B4q0		d-		31.65		4.33		27.63		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.94		0		-23694.65		4:16:13		3:13:00		m		13.83		445.64

		S1148850654:		#B4q0		1148850654:		$B4q0		d-		31.65		4.33		27.73		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23695.71		4:16:43		3:13:30		m		13.87		446.79

		S1148850684:		#B4q0		1148850684:		$B4q0		d-		31.65		4.30		27.73		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23696.92		4:17:13		3:14:00		m		13.90		447.92

		S1148850714:		#B4q0		1148850714:		$B4q0		d-		31.65		4.33		27.63		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23697.99		4:17:43		3:14:30		m		13.94		449.06

		S1148850744:		#B4q0		1148850744:		$B4q0		d-		31.61		4.33		27.73		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23699.2		4:18:13		3:15:00		m		13.97		450.20

		S1148850774:		#B4q0		1148850774:		$B4q0		d-		31.61		4.33		27.73		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23700.27		4:18:43		3:15:30		m		14.01		451.34

		S1148850804:		#B4q0		1148850804:		$B4q0		d-		31.65		4.33		27.73		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93		0		-23701.49		4:19:13		3:16:00		m		14.05		452.49

		S1148850834:		#B4q0		1148850834:		$B4q0		d-		31.61		4.37		27.73		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93		0		-23702.55		4:19:43		3:16:30		m		14.08		453.63

		S1148850864:		#B4q0		1148850864:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93		0		-23703.77		4:20:13		3:17:00		m		14.12		454.78

		S1148850894:		#B4q0		1148850894:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93		0		-23704.84		4:20:43		3:17:30		m		14.15		455.92

		S1148850924:		#B4q0		1148850924:		$B4q0		d-		31.61		4.30		27.73		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93		0		-23706.06		4:21:13		3:18:00		m		14.19		457.06

		S1148850954:		#B4q0		1148850954:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.94		3.93		3.94		3.95		3.93		0		-23707.12		4:21:43		3:18:30		m		14.23		458.19

		S1148850984:		#B4q0		1148850984:		$B4q0		d-		31.61		4.30		27.73		3.96		3.95		3.95		3.94		3.93		3.94		3.95		3.93		0		-23708.34		4:22:13		3:19:00		m		14.26		459.33

		S1148851014:		#B4q0		1148851014:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23709.4		4:22:43		3:19:30		m		14.30		460.47

		S1148851044:		#B4q0		1148851044:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23710.62		4:23:13		3:20:00		m		14.33		461.61

		S1148851074:		#B4q0		1148851074:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23711.69		4:23:43		3:20:30		m		14.37		462.75

		S1148851104:		#B4q0		1148851104:		$B4q0		d-		31.61		4.37		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23712.91		4:24:13		3:21:00		m		14.41		463.89

		S1148851134:		#B4q0		1148851134:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23713.97		4:24:43		3:21:30		m		14.44		465.04

		S1148851164:		#B4q0		1148851164:		$B4q0		d-		31.61		4.33		27.73		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23715.18		4:25:13		3:22:00		m		14.48		466.18

		S1148851194:		#B4q0		1148851194:		$B4q0		d-		31.61		4.30		27.73		3.95		3.95		3.95		3.93		3.93		3.94		3.95		3.93		0		-23716.25		4:25:43		3:22:30		m		14.52		467.32

		S1148851224:		#B4q0		1148851224:		$B4q0		d-		31.61		4.30		27.73		3.95		3.95		3.95		3.93		3.93		3.94		3.94		3.93		0		-23717.46		4:26:13		3:23:00		m		14.55		468.45

		S1148851254:		#B4q0		1148851254:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.95		3.93		3.93		3.94		3.94		3.93		0		-23718.52		4:26:43		3:23:30		m		14.59		469.58

		S1148851284:		#B4q0		1148851284:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92		0		-23719.74		4:27:13		3:24:00		m		14.62		470.72

		S1148851314:		#B4q0		1148851314:		$B4q0		d-		31.61		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92		0		-23720.81		4:27:43		3:24:30		m		14.66		471.86

		S1148851344:		#B4q0		1148851344:		$B4q0		d-		31.61		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92		0		-23722.02		4:28:13		3:25:00		m		14.70		473.00

		S1148851374:		#B4q0		1148851374:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92		0		-23723.08		4:28:43		3:25:30		m		14.73		474.14

		S1148851404:		#B4q0		1148851404:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92		0		-23724.3		4:29:13		3:26:00		m		14.77		475.28

		S1148851434:		#B4q0		1148851434:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92		0		-23725.36		4:29:43		3:26:30		m		14.80		476.42

		S1148851464:		#B4q0		1148851464:		$B4q0		d-		31.58		4.33		27.73		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92		0		-23726.58		4:30:13		3:27:00		m		14.84		477.56

		S1148851494:		#B4q0		1148851494:		$B4q0		d-		31.58		4.33		27.73		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92		0		-23727.64		4:30:43		3:27:30		m		14.88		478.70

		S1148851524:		#B4q0		1148851524:		$B4q0		d-		31.58		4.33		27.73		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92		0		-23728.86		4:31:13		3:28:00		m		14.91		479.84

		S1148851554:		#B4q0		1148851554:		$B4q0		d-		31.58		4.33		27.73		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92		0		-23729.92		4:31:43		3:28:30		m		14.95		480.98

		S1148851584:		#B4q0		1148851584:		$B4q0		d-		31.58		4.33		27.73		3.95		3.94		3.94		3.93		3.92		3.93		3.94		3.92		0		-23731.13		4:32:13		3:29:00		m		14.98		482.12

		S1148851614:		#B4q0		1148851614:		$B4q0		d-		31.58		4.30		27.83		3.95		3.94		3.94		3.93		3.92		3.93		3.94		3.92		0		-23732.2		4:32:43		3:29:30		m		15.02		483.26

		S1148851644:		#B4q0		1148851644:		$B4q0		d-		31.54		4.37		27.73		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23733.41		4:33:13		3:30:00		m		15.06		484.40

		S1148851674:		#B4q0		1148851674:		$B4q0		d-		31.58		4.33		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23734.47		4:33:43		3:30:30		m		15.09		485.54

		S1148851704:		#B4q0		1148851704:		$B4q0		d-		31.54		4.33		27.73		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23735.69		4:34:13		3:31:00		m		15.13		486.68

		S1148851734:		#B4q0		1148851734:		$B4q0		d-		31.54		4.30		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23736.75		4:34:43		3:31:30		m		15.16		487.81

		S1148851764:		#B4q0		1148851764:		$B4q0		d-		31.50		4.30		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23737.96		4:35:13		3:32:00		m		15.20		488.94

		S1148851794:		#B4q0		1148851794:		$B4q0		d-		31.54		4.33		27.73		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23739.02		4:35:43		3:32:30		m		15.24		490.08

		S1148851824:		#B4q0		1148851824:		$B4q0		d-		31.54		4.30		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23740.23		4:36:13		3:33:00		m		15.27		491.21

		S1148851854:		#B4q0		1148851854:		$B4q0		d-		31.54		4.33		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23741.3		4:36:43		3:33:30		m		15.31		492.34

		S1148851884:		#B4q0		1148851884:		$B4q0		d-		31.54		4.30		27.83		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23742.51		4:37:13		3:34:00		m		15.34		493.48

		S1148851914:		#B4q0		1148851914:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23743.57		4:37:43		3:34:30		m		15.38		494.61

		S1148851944:		#B4q0		1148851944:		$B4q0		d-		31.54		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23744.78		4:38:13		3:35:00		m		15.42		495.75

		S1148851974:		#B4q0		1148851974:		$B4q0		d-		31.50		4.30		27.83		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23745.84		4:38:43		3:35:30		m		15.45		496.88

		S1148852004:		#B4q0		1148852004:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92		0		-23747.06		4:39:13		3:36:00		m		15.49		498.02

		S1148852034:		#B4q0		1148852034:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92		0		-23748.12		4:39:43		3:36:30		m		15.52		499.15

		S1148852064:		#B4q0		1148852064:		$B4q0		d-		31.50		4.33		27.73		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92		0		-23749.33		4:40:13		3:37:00		m		15.56		500.29

		S1148852094:		#B4q0		1148852094:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92		0		-23750.39		4:40:43		3:37:30		m		15.60		501.43

		S1148852124:		#B4q0		1148852124:		$B4q0		d-		31.50		4.30		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92		0		-23751.61		4:41:13		3:38:00		m		15.63		502.56

		S1148852154:		#B4q0		1148852154:		$B4q0		d-		31.50		4.37		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92		0		-23752.67		4:41:43		3:38:30		m		15.67		503.70

		S1148852184:		#B4q0		1148852184:		$B4q0		d-		31.50		4.30		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.91		0		-23753.88		4:42:13		3:39:00		m		15.70		504.83

		S1148852214:		#B4q0		1148852214:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.91		0		-23754.94		4:42:43		3:39:30		m		15.74		505.97

		S1148852244:		#B4q0		1148852244:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91		0		-23756.15		4:43:13		3:40:00		m		15.78		507.10

		S1148852274:		#B4q0		1148852274:		$B4q0		d-		31.46		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91		0		-23757.21		4:43:43		3:40:30		m		15.81		508.24

		S1148852304:		#B4q0		1148852304:		$B4q0		d-		31.46		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91		0		-23758.42		4:44:13		3:41:00		m		15.85		509.37

		S1148852334:		#B4q0		1148852334:		$B4q0		d-		31.50		4.33		27.83		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91		0		-23759.48		4:44:43		3:41:30		m		15.88		510.51

		S1148852364:		#B4q0		1148852364:		$B4q0		d-		31.46		4.33		27.83		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91		0		-23760.69		4:45:13		3:42:00		m		15.92		511.65

		S1148852394:		#B4q0		1148852394:		$B4q0		d-		31.46		4.33		27.83		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91		0		-23761.75		4:45:43		3:42:30		m		15.96		512.78

		S1148852424:		#B4q0		1148852424:		$B4q0		d-		31.46		4.30		27.83		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91		0		-23762.96		4:46:13		3:43:00		m		15.99		513.91

		S1148852454:		#B4q0		1148852454:		$B4q0		d-		31.46		4.33		27.83		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91		0		-23764.02		4:46:43		3:43:30		m		16.03		515.04

		S1148852484:		#B4q0		1148852484:		$B4q0		d-		31.46		4.33		27.92		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91		0		-23765.24		4:47:13		3:44:00		m		16.07		516.18

		S1148852514:		#B4q0		1148852514:		$B4q0		d-		31.46		4.30		27.83		3.94		3.94		3.93		3.92		3.91		3.92		3.93		3.91		0		-23766.3		4:47:43		3:44:30		m		16.10		517.31

		S1148852544:		#B4q0		1148852544:		$B4q0		d-		31.46		4.33		27.83		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23767.51		4:48:13		3:45:00		m		16.14		518.44

		S1148852574:		#B4q0		1148852574:		$B4q0		d-		31.46		4.33		27.83		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23768.57		4:48:43		3:45:30		m		16.17		519.58

		S1148852604:		#B4q0		1148852604:		$B4q0		d-		31.46		4.33		27.83		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23769.78		4:49:13		3:46:00		m		16.21		520.71

		S1148852634:		#B4q0		1148852634:		$B4q0		d-		31.46		4.30		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23770.84		4:49:43		3:46:30		m		16.24		521.84

		S1148852664:		#B4q0		1148852664:		$B4q0		d-		31.46		4.37		27.83		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23772.05		4:50:13		3:47:00		m		16.28		522.98

		S1148852694:		#B4q0		1148852694:		$B4q0		d-		31.46		4.33		27.83		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23773.11		4:50:43		3:47:30		m		16.32		524.12

		S1148852724:		#B4q0		1148852724:		$B4q0		d-		31.46		4.37		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23774.32		4:51:13		3:48:00		m		16.35		525.26

		S1148852754:		#B4q0		1148852754:		$B4q0		d-		31.46		4.33		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23775.38		4:51:43		3:48:30		m		16.39		526.40

		S1148852784:		#B4q0		1148852784:		$B4q0		d-		31.42		4.33		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23776.59		4:52:13		3:49:00		m		16.43		527.54

		S1148852814:		#B4q0		1148852814:		$B4q0		d-		31.46		4.30		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23777.65		4:52:43		3:49:30		m		16.46		528.67

		S1148852844:		#B4q0		1148852844:		$B4q0		d-		31.42		4.37		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23778.86		4:53:13		3:50:00		m		16.50		529.80

		S1148852874:		#B4q0		1148852874:		$B4q0		d-		31.42		4.30		27.92		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91		0		-23779.91		4:53:43		3:50:30		m		16.53		530.94

		S1148852904:		#B4q0		1148852904:		$B4q0		d-		31.46		4.33		27.92		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91		0		-23781.12		4:54:13		3:51:00		m		16.57		532.07

		S1148852934:		#B4q0		1148852934:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91		0		-23782.18		4:54:43		3:51:30		m		16.61		533.20

		S1148852964:		#B4q0		1148852964:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91		0		-23783.39		4:55:13		3:52:00		m		16.64		534.34

		S1148852994:		#B4q0		1148852994:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91		0		-23784.45		4:55:43		3:52:30		m		16.68		535.47

		S1148853024:		#B4q0		1148853024:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91		0		-23785.66		4:56:13		3:53:00		m		16.71		536.60

		S1148853054:		#B4q0		1148853054:		$B4q0		d-		31.42		4.30		27.92		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91		0		-23786.72		4:56:43		3:53:30		m		16.75		537.73

		S1148853084:		#B4q0		1148853084:		$B4q0		d-		31.42		4.37		27.92		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.90		0		-23787.93		4:57:13		3:54:00		m		16.79		538.87

		S1148853114:		#B4q0		1148853114:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.90		0		-23788.98		4:57:43		3:54:30		m		16.82		540.01

		S1148853144:		#B4q0		1148853144:		$B4q0		d-		31.39		4.33		27.92		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.90		0		-23790.19		4:58:13		3:55:00		m		16.86		541.14

		S1148853174:		#B4q0		1148853174:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.90		0		-23791.25		4:58:43		3:55:30		m		16.90		542.27

		S1148853204:		#B4q0		1148853204:		$B4q0		d-		31.42		4.33		27.92		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.90		0		-23792.46		4:59:13		3:56:00		m		16.93		543.41

		S1148853234:		#B4q0		1148853234:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23793.52		4:59:43		3:56:30		m		16.97		544.54

		S1148853264:		#B4q0		1148853264:		$B4q0		d-		31.42		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23794.72		5:00:13		3:57:00		m		17.00		545.67

		S1148853294:		#B4q0		1148853294:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23795.78		5:00:43		3:57:30		m		17.04		546.81

		S1148853324:		#B4q0		1148853324:		$B4q0		d-		31.42		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23796.99		5:01:13		3:58:00		m		17.08		547.94

		S1148853354:		#B4q0		1148853354:		$B4q0		d-		31.42		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23798.05		5:01:43		3:58:30		m		17.11		549.07

		S1148853384:		#B4q0		1148853384:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.90		0		-23799.26		5:02:13		3:59:00		m		17.15		550.21

		S1148853414:		#B4q0		1148853414:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.90		3.91		3.92		3.90		0		-23800.31		5:02:43		3:59:30		m		17.18		551.34

		S1148853444:		#B4q0		1148853444:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.90		3.91		3.92		3.90		0		-23801.51		5:03:13		4:00:00		m		17.22		552.47

		S1148853474:		#B4q0		1148853474:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.91		3.90		3.91		3.92		3.90		0		-23802.57		5:03:43		4:00:30		m		17.26		553.60

		S1148853504:		#B4q0		1148853504:		$B4q0		d-		31.39		4.37		27.92		3.93		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23803.78		5:04:13		4:01:00		m		17.29		554.74

		S1148853534:		#B4q0		1148853534:		$B4q0		d-		31.39		4.33		27.92		3.93		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23804.84		5:04:43		4:01:30		m		17.33		555.88

		S1148853564:		#B4q0		1148853564:		$B4q0		d-		31.39		4.30		27.92		3.93		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23806.04		5:05:13		4:02:00		m		17.36		557.01

		S1148853594:		#B4q0		1148853594:		$B4q0		d-		31.35		4.33		27.92		3.93		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23807.1		5:05:43		4:02:30		m		17.40		558.14

		S1148853624:		#B4q0		1148853624:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23808.31		5:06:13		4:03:00		m		17.44		559.27

		S1148853654:		#B4q0		1148853654:		$B4q0		d-		31.39		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.90		0		-23809.36		5:06:43		4:03:30		m		17.47		560.40

		S1148853684:		#B4q0		1148853684:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23810.57		5:07:13		4:04:00		m		17.51		561.53

		S1148853714:		#B4q0		1148853714:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23811.63		5:07:43		4:04:30		m		17.54		562.66

		S1148853744:		#B4q0		1148853744:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23812.84		5:08:13		4:05:00		m		17.58		563.79

		S1148853774:		#B4q0		1148853774:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23813.9		5:08:43		4:05:30		m		17.62		564.93

		S1148853804:		#B4q0		1148853804:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23815.1		5:09:13		4:06:00		m		17.65		566.06

		S1148853834:		#B4q0		1148853834:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23816.16		5:09:43		4:06:30		m		17.69		567.19

		S1148853864:		#B4q0		1148853864:		$B4q0		d-		31.35		4.37		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23817.36		5:10:13		4:07:00		m		17.73		568.32

		S1148853894:		#B4q0		1148853894:		$B4q0		d-		31.31		4.41		27.92		3.92		3.92		3.92		3.90		3.90		3.91		3.92		3.89		0		-23818.42		5:10:43		4:07:30		m		17.76		569.47

		S1148853924:		#B4q0		1148853924:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.90		3.91		3.89		0		-23819.63		5:11:13		4:08:00		m		17.80		570.61

		S1148853954:		#B4q0		1148853954:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.90		3.91		3.89		0		-23820.68		5:11:43		4:08:30		m		17.83		571.74

		S1148853984:		#B4q0		1148853984:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.90		3.91		3.89		0		-23821.89		5:12:13		4:09:00		m		17.87		572.87

		S1148854014:		#B4q0		1148854014:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.92		3.90		3.90		3.90		3.91		3.89		0		-23822.94		5:12:43		4:09:30		m		17.91		574.00

		S1148854044:		#B4q0		1148854044:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.92		3.90		3.89		3.90		3.91		3.89		0		-23824.15		5:13:13		4:10:00		m		17.94		575.13

		S1148854074:		#B4q0		1148854074:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.92		3.90		3.89		3.90		3.91		3.89		0		-23825.2		5:13:43		4:10:30		m		17.98		576.26

		S1148854104:		#B4q0		1148854104:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.91		3.90		3.89		3.90		3.91		3.89		0		-23826.41		5:14:13		4:11:00		m		18.01		577.39

		S1148854134:		#B4q0		1148854134:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.91		3.89		3.89		3.90		3.91		3.89		0		-23827.47		5:14:43		4:11:30		m		18.05		578.52

		S1148854164:		#B4q0		1148854164:		$B4q0		d-		31.31		4.33		27.92		3.92		3.92		3.91		3.89		3.89		3.90		3.91		3.89		0		-23828.67		5:15:13		4:12:00		m		18.09		579.65

		S1148854194:		#B4q0		1148854194:		$B4q0		d-		31.35		4.33		27.92		3.92		3.92		3.91		3.89		3.89		3.90		3.91		3.89		0		-23829.72		5:15:43		4:12:30		m		18.12		580.78

		S1148854224:		#B4q0		1148854224:		$B4q0		d-		31.31		4.33		28.02		3.92		3.92		3.91		3.89		3.89		3.90		3.91		3.89		0		-23830.93		5:16:13		4:13:00		m		18.16		581.91

		S1148854254:		#B4q0		1148854254:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23831.98		5:16:43		4:13:30		m		18.20		583.04

		S1148854284:		#B4q0		1148854284:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23833.18		5:17:13		4:14:00		m		18.23		584.17

		S1148854314:		#B4q0		1148854314:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23834.24		5:17:43		4:14:30		m		18.27		585.30

		S1148854344:		#B4q0		1148854344:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23835.45		5:18:13		4:15:00		m		18.30		586.43

		S1148854374:		#B4q0		1148854374:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23836.5		5:18:43		4:15:30		m		18.34		587.56

		S1148854404:		#B4q0		1148854404:		$B4q0		d-		31.31		4.33		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23837.7		5:19:13		4:16:00		m		18.38		588.69

		S1148854434:		#B4q0		1148854434:		$B4q0		d-		31.31		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23838.76		5:19:43		4:16:30		m		18.41		589.82

		S1148854464:		#B4q0		1148854464:		$B4q0		d-		31.31		4.30		27.92		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23839.97		5:20:13		4:17:00		m		18.45		590.95

		S1148854494:		#B4q0		1148854494:		$B4q0		d-		31.27		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23841.02		5:20:43		4:17:30		m		18.48		592.07

		S1148854524:		#B4q0		1148854524:		$B4q0		d-		31.27		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.90		3.91		3.89		0		-23842.23		5:21:13		4:18:00		m		18.52		593.20

		S1148854554:		#B4q0		1148854554:		$B4q0		d-		31.31		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.89		0		-23843.28		5:21:43		4:18:30		m		18.56		594.33

		S1148854584:		#B4q0		1148854584:		$B4q0		d-		31.27		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23844.48		5:22:13		4:19:00		m		18.59		595.46

		S1148854614:		#B4q0		1148854614:		$B4q0		d-		31.31		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23845.54		5:22:43		4:19:30		m		18.63		596.59

		S1148854644:		#B4q0		1148854644:		$B4q0		d-		31.27		4.33		28.02		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23846.74		5:23:13		4:20:00		m		18.66		597.72

		S1148854674:		#B4q0		1148854674:		$B4q0		d-		31.27		4.33		27.92		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23847.79		5:23:43		4:20:30		m		18.70		598.85

		S1148854704:		#B4q0		1148854704:		$B4q0		d-		31.27		4.33		28.02		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23849		5:24:13		4:21:00		m		18.74		599.98

		S1148854734:		#B4q0		1148854734:		$B4q0		d-		31.27		4.33		27.92		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23850.05		5:24:43		4:21:30		m		18.77		601.10

		S1148854764:		#B4q0		1148854764:		$B4q0		d-		31.23		4.33		27.92		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23851.25		5:25:13		4:22:00		m		18.81		602.23

		S1148854794:		#B4q0		1148854794:		$B4q0		d-		31.27		4.33		28.02		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23852.3		5:25:43		4:22:30		m		18.84		603.36

		S1148854824:		#B4q0		1148854824:		$B4q0		d-		31.23		4.30		28.02		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23853.5		5:26:13		4:23:00		m		18.88		604.48

		S1148854854:		#B4q0		1148854854:		$B4q0		d-		31.27		4.33		28.02		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88		0		-23854.56		5:26:43		4:23:30		m		18.92		605.61

		S1148854884:		#B4q0		1148854884:		$B4q0		d-		31.23		4.37		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.91		3.88		0		-23855.76		5:27:13		4:24:00		m		18.95		606.74

		S1148854914:		#B4q0		1148854914:		$B4q0		d-		31.27		4.30		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.90		3.88		0		-23856.81		5:27:43		4:24:30		m		18.99		607.87

		S1148854944:		#B4q0		1148854944:		$B4q0		d-		31.23		4.30		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.90		3.88		0		-23858.01		5:28:13		4:25:00		m		19.02		608.99

		S1148854974:		#B4q0		1148854974:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.90		3.88		0		-23859.06		5:28:43		4:25:30		m		19.06		610.11

		S1148855004:		#B4q0		1148855004:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.90		3.88		0		-23860.26		5:29:13		4:26:00		m		19.10		611.24

		S1148855034:		#B4q0		1148855034:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.91		3.89		3.88		3.89		3.90		3.88		0		-23861.32		5:29:43		4:26:30		m		19.13		612.36

		S1148855064:		#B4q0		1148855064:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.91		3.88		3.88		3.89		3.90		3.88		0		-23862.52		5:30:13		4:27:00		m		19.17		613.49

		S1148855094:		#B4q0		1148855094:		$B4q0		d-		31.20		4.33		28.02		3.91		3.91		3.91		3.88		3.88		3.89		3.90		3.88		0		-23863.57		5:30:43		4:27:30		m		19.20		614.62

		S1148855124:		#B4q0		1148855124:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.91		3.88		3.88		3.89		3.90		3.88		0		-23864.77		5:31:13		4:28:00		m		19.24		615.74

		S1148855154:		#B4q0		1148855154:		$B4q0		d-		31.20		4.30		28.02		3.91		3.91		3.91		3.88		3.88		3.89		3.90		3.88		0		-23865.82		5:31:43		4:28:30		m		19.28		616.87

		S1148855184:		#B4q0		1148855184:		$B4q0		d-		31.20		4.33		28.02		3.91		3.91		3.90		3.88		3.88		3.89		3.90		3.87		0		-23867.03		5:32:13		4:29:00		m		19.31		617.99

		S1148855214:		#B4q0		1148855214:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.90		3.88		3.88		3.89		3.90		3.87		0		-23868.08		5:32:43		4:29:30		m		19.35		619.11

		S1148855244:		#B4q0		1148855244:		$B4q0		d-		31.23		4.33		28.02		3.91		3.91		3.90		3.88		3.88		3.89		3.90		3.87		0		-23869.28		5:33:13		4:30:00		m		19.38		620.24

		S1148855274:		#B4q0		1148855274:		$B4q0		d-		31.20		4.33		28.02		3.91		3.91		3.90		3.88		3.88		3.89		3.90		3.87		0		-23870.33		5:33:43		4:30:30		m		19.42		621.37

		S1148855304:		#B4q0		1148855304:		$B4q0		d-		31.20		4.33		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23871.53		5:34:13		4:31:00		m		19.46		622.49

		S1148855334:		#B4q0		1148855334:		$B4q0		d-		31.20		4.33		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23872.59		5:34:43		4:31:30		m		19.49		623.62

		S1148855364:		#B4q0		1148855364:		$B4q0		d-		31.23		4.30		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23873.79		5:35:13		4:32:00		m		19.53		624.74

		S1148855394:		#B4q0		1148855394:		$B4q0		d-		31.16		4.33		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23874.83		5:35:43		4:32:30		m		19.57		625.86

		S1148855424:		#B4q0		1148855424:		$B4q0		d-		31.20		4.33		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23876.04		5:36:13		4:33:00		m		19.60		626.99

		S1148855454:		#B4q0		1148855454:		$B4q0		d-		31.20		4.33		28.02		3.91		3.90		3.90		3.88		3.88		3.89		3.90		3.87		0		-23877.09		5:36:43		4:33:30		m		19.64		628.11

		S1148855484:		#B4q0		1148855484:		$B4q0		d-		31.20		4.33		28.12		3.91		3.90		3.90		3.88		3.87		3.89		3.90		3.87		0		-23878.28		5:37:13		4:34:00		m		19.67		629.24

		S1148855514:		#B4q0		1148855514:		$B4q0		d-		31.20		4.37		28.02		3.91		3.90		3.90		3.88		3.87		3.88		3.90		3.87		0		-23879.33		5:37:43		4:34:30		m		19.71		630.37

		S1148855544:		#B4q0		1148855544:		$B4q0		d-		31.20		4.33		28.02		3.91		3.90		3.90		3.88		3.87		3.88		3.90		3.87		0		-23880.53		5:38:13		4:35:00		m		19.75		631.50

		S1148855574:		#B4q0		1148855574:		$B4q0		d-		31.16		4.33		28.02		3.91		3.90		3.90		3.88		3.87		3.88		3.89		3.87		0		-23881.58		5:38:43		4:35:30		m		19.78		632.63

		S1148855604:		#B4q0		1148855604:		$B4q0		d-		31.16		4.33		28.02		3.91		3.90		3.90		3.88		3.87		3.88		3.89		3.87		0		-23882.78		5:39:13		4:36:00		m		19.82		633.75

		S1148855634:		#B4q0		1148855634:		$B4q0		d-		31.16		4.33		28.02		3.91		3.90		3.90		3.88		3.87		3.88		3.89		3.87		0		-23883.83		5:39:43		4:36:30		m		19.85		634.88

		S1148855664:		#B4q0		1148855664:		$B4q0		d-		31.16		4.33		28.02		3.91		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23885.03		5:40:13		4:37:00		m		19.89		636.00

		S1148855694:		#B4q0		1148855694:		$B4q0		d-		31.16		4.33		28.12		3.91		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23886.08		5:40:43		4:37:30		m		19.93		637.12

		S1148855724:		#B4q0		1148855724:		$B4q0		d-		31.16		4.33		28.12		3.90		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23887.28		5:41:13		4:38:00		m		19.96		638.25

		S1148855754:		#B4q0		1148855754:		$B4q0		d-		31.16		4.33		28.02		3.90		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23888.33		5:41:43		4:38:30		m		20.00		639.37

		S1148855784:		#B4q0		1148855784:		$B4q0		d-		31.16		4.33		28.02		3.90		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23889.53		5:42:13		4:39:00		m		20.03		640.50

		S1148855814:		#B4q0		1148855814:		$B4q0		d-		31.16		4.33		28.12		3.90		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23890.58		5:42:43		4:39:30		m		20.07		641.62

		S1148855844:		#B4q0		1148855844:		$B4q0		d-		31.16		4.30		28.02		3.90		3.90		3.90		3.87		3.87		3.88		3.89		3.87		0		-23891.77		5:43:13		4:40:00		m		20.11		642.74

		S1148855874:		#B4q0		1148855874:		$B4q0		d-		31.16		4.37		28.02		3.90		3.90		3.89		3.87		3.87		3.88		3.89		3.87		0		-23892.83		5:43:43		4:40:30		m		20.14		643.87

		S1148855904:		#B4q0		1148855904:		$B4q0		d-		31.16		4.33		28.02		3.90		3.90		3.89		3.87		3.87		3.88		3.89		3.87		0		-23894.02		5:44:13		4:41:00		m		20.18		645.00

		S1148855934:		#B4q0		1148855934:		$B4q0		d-		31.16		4.33		28.12		3.90		3.90		3.89		3.87		3.87		3.88		3.89		3.87		0		-23895.07		5:44:43		4:41:30		m		20.22		646.12

		S1148855964:		#B4q0		1148855964:		$B4q0		d-		31.12		4.33		28.02		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.87		0		-23896.27		5:45:13		4:42:00		m		20.25		647.25

		S1148855994:		#B4q0		1148855994:		$B4q0		d-		31.12		4.33		28.02		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.87		0		-23897.31		5:45:43		4:42:30		m		20.29		648.37

		S1148856024:		#B4q0		1148856024:		$B4q0		d-		31.16		4.30		28.02		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.87		0		-23898.52		5:46:13		4:43:00		m		20.32		649.49

		S1148856054:		#B4q0		1148856054:		$B4q0		d-		31.12		4.30		28.02		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.87		0		-23899.56		5:46:43		4:43:30		m		20.36		650.60

		S1148856084:		#B4q0		1148856084:		$B4q0		d-		31.12		4.33		28.12		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.86		0		-23900.76		5:47:13		4:44:00		m		20.39		651.72

		S1148856114:		#B4q0		1148856114:		$B4q0		d-		31.12		4.33		28.02		3.90		3.89		3.89		3.87		3.87		3.88		3.89		3.86		0		-23901.81		5:47:43		4:44:30		m		20.43		652.85

		S1148856144:		#B4q0		1148856144:		$B4q0		d-		31.12		4.33		28.02		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23903.01		5:48:13		4:45:00		m		20.47		653.97

		S1148856174:		#B4q0		1148856174:		$B4q0		d-		31.12		4.33		28.12		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23904.05		5:48:43		4:45:30		m		20.50		655.09

		S1148856204:		#B4q0		1148856204:		$B4q0		d-		31.12		4.33		28.12		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23905.25		5:49:13		4:46:00		m		20.54		656.21

		S1148856234:		#B4q0		1148856234:		$B4q0		d-		31.12		4.33		28.12		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23906.3		5:49:43		4:46:30		m		20.58		657.34

		S1148856264:		#B4q0		1148856264:		$B4q0		d-		31.12		4.37		28.02		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23907.5		5:50:13		4:47:00		m		20.61		658.47

		S1148856294:		#B4q0		1148856294:		$B4q0		d-		31.08		4.33		28.12		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23908.54		5:50:43		4:47:30		m		20.65		659.59

		S1148856324:		#B4q0		1148856324:		$B4q0		d-		31.12		4.33		28.02		3.90		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23909.74		5:51:13		4:48:00		m		20.68		660.72

		S1148856354:		#B4q0		1148856354:		$B4q0		d-		31.12		4.33		28.12		3.89		3.89		3.89		3.87		3.87		3.87		3.89		3.86		0		-23910.79		5:51:43		4:48:30		m		20.72		661.84

		S1148856384:		#B4q0		1148856384:		$B4q0		d-		31.08		4.33		28.02		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86		0		-23911.99		5:52:13		4:49:00		m		20.76		662.96

		S1148856414:		#B4q0		1148856414:		$B4q0		d-		31.12		4.33		28.12		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86		0		-23913.03		5:52:43		4:49:30		m		20.79		664.08

		S1148856444:		#B4q0		1148856444:		$B4q0		d-		31.08		4.30		28.12		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86		0		-23914.23		5:53:13		4:50:00		m		20.83		665.20

		S1148856474:		#B4q0		1148856474:		$B4q0		d-		31.08		4.30		28.02		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86		0		-23915.28		5:53:43		4:50:30		m		20.86		666.31

		S1148856504:		#B4q0		1148856504:		$B4q0		d-		31.08		4.33		28.12		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86		0		-23916.47		5:54:13		4:51:00		m		20.90		667.43

		S1148856534:		#B4q0		1148856534:		$B4q0		d-		31.08		4.33		28.12		3.89		3.89		3.89		3.87		3.86		3.87		3.88		3.86		0		-23917.52		5:54:43		4:51:30		m		20.94		668.55

		S1148856564:		#B4q0		1148856564:		$B4q0		d-		31.08		4.33		28.12		3.89		3.89		3.89		3.87		3.86		3.87		3.88		3.86		0		-23918.72		5:55:13		4:52:00		m		20.97		669.68

		S1148856594:		#B4q0		1148856594:		$B4q0		d-		31.08		4.33		28.02		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86		0		-23919.77		5:55:43		4:52:30		m		21.01		670.80

		S1148856624:		#B4q0		1148856624:		$B4q0		d-		31.05		4.33		28.12		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86		0		-23920.96		5:56:13		4:53:00		m		21.04		671.92

		S1148856654:		#B4q0		1148856654:		$B4q0		d-		31.05		4.33		28.12		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86		0		-23922.01		5:56:43		4:53:30		m		21.08		673.04

		S1148856684:		#B4q0		1148856684:		$B4q0		d-		31.08		4.33		28.12		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86		0		-23923.2		5:57:13		4:54:00		m		21.12		674.16

		S1148856714:		#B4q0		1148856714:		$B4q0		d-		31.08		4.33		28.02		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85		0		-23924.25		5:57:43		4:54:30		m		21.15		675.28

		S1148856744:		#B4q0		1148856744:		$B4q0		d-		31.05		4.33		28.02		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85		0		-23925.44		5:58:13		4:55:00		m		21.19		676.40

		S1148856774:		#B4q0		1148856774:		$B4q0		d-		31.08		4.30		28.12		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85		0		-23926.49		5:58:43		4:55:30		m		21.22		677.52

		S1148856804:		#B4q0		1148856804:		$B4q0		d-		31.08		4.33		28.02		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85		0		-23927.68		5:59:13		4:56:00		m		21.26		678.64

		S1148856834:		#B4q0		1148856834:		$B4q0		d-		31.05		4.33		28.12		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85		0		-23928.73		5:59:43		4:56:30		m		21.30		679.76

		S1148856864:		#B4q0		1148856864:		$B4q0		d-		31.05		4.33		28.12		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85		0		-23929.92		6:00:13		4:57:00		m		21.33		680.88

		S1148856894:		#B4q0		1148856894:		$B4q0		d-		31.05		4.33		28.12		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85		0		-23930.97		6:00:43		4:57:30		m		21.37		682.00

		S1148856924:		#B4q0		1148856924:		$B4q0		d-		31.05		4.30		28.12		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85		0		-23932.16		6:01:13		4:58:00		m		21.40		683.11

		S1148856954:		#B4q0		1148856954:		$B4q0		d-		31.05		4.33		28.12		3.89		3.88		3.88		3.86		3.86		3.87		3.88		3.85		0		-23933.21		6:01:43		4:58:30		m		21.44		684.23

		S1148856984:		#B4q0		1148856984:		$B4q0		d-		31.05		4.33		28.02		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85		0		-23934.41		6:02:13		4:59:00		m		21.48		685.35

		S1148857014:		#B4q0		1148857014:		$B4q0		d-		31.05		4.37		28.12		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85		0		-23935.45		6:02:43		4:59:30		m		21.51		686.48

		S1148857044:		#B4q0		1148857044:		$B4q0		d-		31.05		4.33		28.02		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85		0		-23936.64		6:03:13		5:00:00		m		21.55		687.60

		S1148857074:		#B4q0		1148857074:		$B4q0		d-		31.01		4.33		28.12		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85		0		-23937.68		6:03:43		5:00:30		m		21.59		688.72

		S1148857104:		#B4q0		1148857104:		$B4q0		d-		31.05		4.33		28.12		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85		0		-23938.88		6:04:13		5:01:00		m		21.62		689.84

		S1148857134:		#B4q0		1148857134:		$B4q0		d-		31.01		4.33		28.02		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85		0		-23939.93		6:04:43		5:01:30		m		21.66		690.96

		S1148857164:		#B4q0		1148857164:		$B4q0		d-		31.01		4.33		28.02		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23941.12		6:05:13		5:02:00		m		21.69		692.08

		S1148857194:		#B4q0		1148857194:		$B4q0		d-		31.01		4.33		28.12		3.89		3.88		3.88		3.86		3.85		3.86		3.87		3.85		0		-23942.17		6:05:43		5:02:30		m		21.73		693.20

		S1148857224:		#B4q0		1148857224:		$B4q0		d-		31.01		4.37		28.12		3.89		3.88		3.88		3.86		3.85		3.86		3.87		3.85		0		-23943.37		6:06:13		5:03:00		m		21.77		694.32

		S1148857254:		#B4q0		1148857254:		$B4q0		d-		31.05		4.30		28.12		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23944.41		6:06:43		5:03:30		m		21.80		695.44

		S1148857284:		#B4q0		1148857284:		$B4q0		d-		31.01		4.26		28.12		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23945.6		6:07:13		5:04:00		m		21.84		696.55

		S1148857314:		#B4q0		1148857314:		$B4q0		d-		31.05		4.33		28.12		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23946.65		6:07:43		5:04:30		m		21.87		697.66

		S1148857344:		#B4q0		1148857344:		$B4q0		d-		31.01		4.33		28.02		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23947.84		6:08:13		5:05:00		m		21.91		698.78

		S1148857374:		#B4q0		1148857374:		$B4q0		d-		31.01		4.33		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23948.88		6:08:43		5:05:30		m		21.95		699.90

		S1148857404:		#B4q0		1148857404:		$B4q0		d-		31.01		4.33		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23950.08		6:09:13		5:06:00		m		21.98		701.02

		S1148857434:		#B4q0		1148857434:		$B4q0		d-		31.05		4.33		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23951.12		6:09:43		5:06:30		m		22.02		702.14

		S1148857464:		#B4q0		1148857464:		$B4q0		d-		31.01		4.33		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23952.32		6:10:13		5:07:00		m		22.05		703.26

		S1148857494:		#B4q0		1148857494:		$B4q0		d-		31.01		4.33		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23953.36		6:10:43		5:07:30		m		22.09		704.38

		S1148857524:		#B4q0		1148857524:		$B4q0		d-		31.01		4.30		28.12		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85		0		-23954.55		6:11:13		5:08:00		m		22.13		705.49

		S1148857554:		#B4q0		1148857554:		$B4q0		d-		30.97		4.33		28.12		3.88		3.88		3.87		3.85		3.85		3.86		3.87		3.85		0		-23955.6		6:11:43		5:08:30		m		22.16		706.61

		S1148857584:		#B4q0		1148857584:		$B4q0		d-		30.97		4.33		28.12		3.88		3.88		3.87		3.85		3.85		3.86		3.87		3.85		0		-23956.79		6:12:13		5:09:00		m		22.20		707.72

		S1148857614:		#B4q0		1148857614:		$B4q0		d-		31.01		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85		0		-23957.83		6:12:43		5:09:30		m		22.23		708.84

		S1148857644:		#B4q0		1148857644:		$B4q0		d-		31.01		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85		0		-23959.02		6:13:13		5:10:00		m		22.27		709.96

		S1148857674:		#B4q0		1148857674:		$B4q0		d-		30.97		4.30		28.12		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85		0		-23960.07		6:13:43		5:10:30		m		22.31		711.08

		S1148857704:		#B4q0		1148857704:		$B4q0		d-		30.93		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85		0		-23961.26		6:14:13		5:11:00		m		22.34		712.19

		S1148857734:		#B4q0		1148857734:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23962.3		6:14:43		5:11:30		m		22.38		713.31

		S1148857764:		#B4q0		1148857764:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23963.5		6:15:13		5:12:00		m		22.41		714.42

		S1148857794:		#B4q0		1148857794:		$B4q0		d-		30.97		4.30		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23964.54		6:15:43		5:12:30		m		22.45		715.54

		S1148857824:		#B4q0		1148857824:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23965.73		6:16:13		5:13:00		m		22.49		716.65

		S1148857854:		#B4q0		1148857854:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23966.78		6:16:43		5:13:30		m		22.52		717.77

		S1148857884:		#B4q0		1148857884:		$B4q0		d-		30.97		4.30		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23967.96		6:17:13		5:14:00		m		22.56		718.88

		S1148857914:		#B4q0		1148857914:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23969		6:17:43		5:14:30		m		22.59		720.00

		S1148857944:		#B4q0		1148857944:		$B4q0		d-		30.93		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23970.19		6:18:13		5:15:00		m		22.63		721.11

		S1148857974:		#B4q0		1148857974:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84		0		-23971.24		6:18:43		5:15:30		m		22.67		722.23

		S1148858004:		#B4q0		1148858004:		$B4q0		d-		30.97		4.33		28.12		3.88		3.87		3.87		3.85		3.84		3.85		3.87		3.84		0		-23972.43		6:19:13		5:16:00		m		22.70		723.35

		S1148858034:		#B4q0		1148858034:		$B4q0		d-		30.93		4.37		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84		0		-23973.47		6:19:43		5:16:30		m		22.74		724.47

		S1148858064:		#B4q0		1148858064:		$B4q0		d-		30.93		4.30		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84		0		-23974.66		6:20:13		5:17:00		m		22.77		725.59

		S1148858094:		#B4q0		1148858094:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84		0		-23975.7		6:20:43		5:17:30		m		22.81		726.70

		S1148858124:		#B4q0		1148858124:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84		0		-23976.89		6:21:13		5:18:00		m		22.85		727.81

		S1148858154:		#B4q0		1148858154:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84		0		-23977.93		6:21:43		5:18:30		m		22.88		728.93

		S1148858184:		#B4q0		1148858184:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84		0		-23979.12		6:22:13		5:19:00		m		22.92		730.05

		S1148858214:		#B4q0		1148858214:		$B4q0		d-		30.93		4.37		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23980.16		6:22:43		5:19:30		m		22.96		731.17

		S1148858244:		#B4q0		1148858244:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23981.35		6:23:13		5:20:00		m		22.99		732.29

		S1148858274:		#B4q0		1148858274:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23982.39		6:23:43		5:20:30		m		23.03		733.40

		S1148858304:		#B4q0		1148858304:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23983.58		6:24:13		5:21:00		m		23.06		734.52

		S1148858334:		#B4q0		1148858334:		$B4q0		d-		30.93		4.30		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23984.62		6:24:43		5:21:30		m		23.10		735.63

		S1148858364:		#B4q0		1148858364:		$B4q0		d-		30.89		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23985.81		6:25:13		5:22:00		m		23.14		736.74

		S1148858394:		#B4q0		1148858394:		$B4q0		d-		30.93		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23986.85		6:25:43		5:22:30		m		23.17		737.86

		S1148858424:		#B4q0		1148858424:		$B4q0		d-		30.89		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23988.04		6:26:13		5:23:00		m		23.21		738.97

		S1148858454:		#B4q0		1148858454:		$B4q0		d-		30.89		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23989.08		6:26:43		5:23:30		m		23.24		740.09

		S1148858484:		#B4q0		1148858484:		$B4q0		d-		30.89		4.33		28.12		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84		0		-23990.27		6:27:13		5:24:00		m		23.28		741.20

		S1148858514:		#B4q0		1148858514:		$B4q0		d-		30.89		4.33		28.12		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.84		0		-23991.31		6:27:43		5:24:30		m		23.32		742.32

		S1148858544:		#B4q0		1148858544:		$B4q0		d-		30.89		4.30		28.12		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.83		0		-23992.51		6:28:13		5:25:00		m		23.35		743.43

		S1148858574:		#B4q0		1148858574:		$B4q0		d-		30.89		4.30		28.12		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.83		0		-23993.55		6:28:43		5:25:30		m		23.39		744.54

		S1148858604:		#B4q0		1148858604:		$B4q0		d-		30.89		4.33		28.12		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83		0		-23994.74		6:29:13		5:26:00		m		23.42		745.65

		S1148858634:		#B4q0		1148858634:		$B4q0		d-		30.89		4.33		28.12		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83		0		-23995.78		6:29:43		5:26:30		m		23.46		746.76

		S1148858664:		#B4q0		1148858664:		$B4q0		d-		30.89		4.33		28.12		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83		0		-23996.97		6:30:13		5:27:00		m		23.50		747.88

		S1148858694:		#B4q0		1148858694:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83		0		-23998.01		6:30:43		5:27:30		m		23.53		748.99

		S1148858724:		#B4q0		1148858724:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83		0		-23999.2		6:31:13		5:28:00		m		23.57		750.10

		S1148858754:		#B4q0		1148858754:		$B4q0		d-		30.85		4.30		28.22		3.87		3.86		3.86		3.84		3.83		3.85		3.86		3.83		0		-24000.24		6:31:43		5:28:30		m		23.60		751.21

		S1148858784:		#B4q0		1148858784:		$B4q0		d-		30.89		4.33		28.12		3.87		3.86		3.86		3.84		3.83		3.85		3.85		3.83		0		-24001.43		6:32:13		5:29:00		m		23.64		752.32

		S1148858814:		#B4q0		1148858814:		$B4q0		d-		30.85		4.33		28.22		3.87		3.86		3.86		3.84		3.83		3.85		3.85		3.83		0		-24002.47		6:32:43		5:29:30		m		23.68		753.44

		S1148858844:		#B4q0		1148858844:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.84		3.83		3.84		3.85		3.83		0		-24003.65		6:33:13		5:30:00		m		23.71		754.55

		S1148858874:		#B4q0		1148858874:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24004.7		6:33:43		5:30:30		m		23.75		755.66

		S1148858904:		#B4q0		1148858904:		$B4q0		d-		30.85		4.30		28.22		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24005.88		6:34:13		5:31:00		m		23.78		756.77

		S1148858934:		#B4q0		1148858934:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24006.92		6:34:43		5:31:30		m		23.82		757.88

		S1148858964:		#B4q0		1148858964:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24008.11		6:35:13		5:32:00		m		23.86		758.99

		S1148858994:		#B4q0		1148858994:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24009.15		6:35:43		5:32:30		m		23.89		760.11

		S1148859024:		#B4q0		1148859024:		$B4q0		d-		30.85		4.33		28.12		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24010.34		6:36:13		5:33:00		m		23.93		761.22

		S1148859054:		#B4q0		1148859054:		$B4q0		d-		30.85		4.33		28.12		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24011.38		6:36:43		5:33:30		m		23.96		762.33

		S1148859084:		#B4q0		1148859084:		$B4q0		d-		30.82		4.33		28.12		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24012.56		6:37:13		5:34:00		m		24.00		763.45

		S1148859114:		#B4q0		1148859114:		$B4q0		d-		30.82		4.33		28.12		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24013.6		6:37:43		5:34:30		m		24.04		764.56

		S1148859144:		#B4q0		1148859144:		$B4q0		d-		30.82		4.30		28.12		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24014.79		6:38:13		5:35:00		m		24.07		765.67

		S1148859174:		#B4q0		1148859174:		$B4q0		d-		30.85		4.33		28.22		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24015.83		6:38:43		5:35:30		m		24.11		766.78

		S1148859204:		#B4q0		1148859204:		$B4q0		d-		30.85		4.33		28.22		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83		0		-24017.02		6:39:13		5:36:00		m		24.14		767.89

		S1148859234:		#B4q0		1148859234:		$B4q0		d-		30.85		4.30		28.12		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83		0		-24018.06		6:39:43		5:36:30		m		24.18		769.00

		S1148859264:		#B4q0		1148859264:		$B4q0		d-		30.82		4.33		28.12		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83		0		-24019.25		6:40:13		5:37:00		m		24.22		770.11

		S1148859294:		#B4q0		1148859294:		$B4q0		d-		30.85		4.30		28.22		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83		0		-24020.29		6:40:43		5:37:30		m		24.25		771.22

		S1148859324:		#B4q0		1148859324:		$B4q0		d-		30.82		4.30		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24021.47		6:41:13		5:38:00		m		24.29		772.32

		S1148859354:		#B4q0		1148859354:		$B4q0		d-		30.82		4.33		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24022.51		6:41:43		5:38:30		m		24.32		773.43

		S1148859384:		#B4q0		1148859384:		$B4q0		d-		30.82		4.33		28.22		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24023.7		6:42:13		5:39:00		m		24.36		774.54

		S1148859414:		#B4q0		1148859414:		$B4q0		d-		30.82		4.37		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24024.73		6:42:43		5:39:30		m		24.40		775.66

		S1148859444:		#B4q0		1148859444:		$B4q0		d-		30.82		4.26		28.22		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24025.92		6:43:13		5:40:00		m		24.43		776.77

		S1148859474:		#B4q0		1148859474:		$B4q0		d-		30.82		4.33		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24026.96		6:43:43		5:40:30		m		24.47		777.87

		S1148859504:		#B4q0		1148859504:		$B4q0		d-		30.82		4.30		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24028.15		6:44:13		5:41:00		m		24.50		778.98

		S1148859534:		#B4q0		1148859534:		$B4q0		d-		30.82		4.33		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24029.18		6:44:43		5:41:30		m		24.54		780.09

		S1148859564:		#B4q0		1148859564:		$B4q0		d-		30.82		4.33		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24030.37		6:45:13		5:42:00		m		24.58		781.20

		S1148859594:		#B4q0		1148859594:		$B4q0		d-		30.82		4.33		28.12		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24031.41		6:45:43		5:42:30		m		24.61		782.31

		S1148859624:		#B4q0		1148859624:		$B4q0		d-		30.82		4.33		28.22		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83		0		-24032.59		6:46:13		5:43:00		m		24.65		783.42

		S1148859654:		#B4q0		1148859654:		$B4q0		d-		30.82		4.30		28.12		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83		0		-24033.63		6:46:43		5:43:30		m		24.68		784.53

		S1148859684:		#B4q0		1148859684:		$B4q0		d-		30.82		4.33		28.22		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83		0		-24034.82		6:47:13		5:44:00		m		24.72		785.64

		S1148859714:		#B4q0		1148859714:		$B4q0		d-		30.82		4.30		28.22		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83		0		-24035.86		6:47:43		5:44:30		m		24.76		786.75

		S1148859744:		#B4q0		1148859744:		$B4q0		d-		30.82		4.33		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.83		0		-24037.04		6:48:13		5:45:00		m		24.79		787.86

		S1148859774:		#B4q0		1148859774:		$B4q0		d-		30.78		4.33		28.12		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82		0		-24038.08		6:48:43		5:45:30		m		24.83		788.97

		S1148859804:		#B4q0		1148859804:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82		0		-24039.27		6:49:13		5:46:00		m		24.86		790.08

		S1148859834:		#B4q0		1148859834:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82		0		-24040.3		6:49:43		5:46:30		m		24.90		791.19

		S1148859864:		#B4q0		1148859864:		$B4q0		d-		30.78		4.33		28.12		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82		0		-24041.49		6:50:13		5:47:00		m		24.94		792.30

		S1148859894:		#B4q0		1148859894:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82		0		-24042.53		6:50:43		5:47:30		m		24.97		793.41

		S1148859924:		#B4q0		1148859924:		$B4q0		d-		30.78		4.30		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82		0		-24043.72		6:51:13		5:48:00		m		25.01		794.52

		S1148859954:		#B4q0		1148859954:		$B4q0		d-		30.78		4.30		28.22		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82		0		-24044.75		6:51:43		5:48:30		m		25.04		795.62

		S1148859984:		#B4q0		1148859984:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82		0		-24045.94		6:52:13		5:49:00		m		25.08		796.73

		S1148860014:		#B4q0		1148860014:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82		0		-24046.98		6:52:43		5:49:30		m		25.12		797.84

		S1148860044:		#B4q0		1148860044:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82		0		-24048.16		6:53:13		5:50:00		m		25.15		798.95

		S1148860074:		#B4q0		1148860074:		$B4q0		d-		30.78		4.37		28.12		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82		0		-24049.2		6:53:43		5:50:30		m		25.19		800.06

		S1148860104:		#B4q0		1148860104:		$B4q0		d-		30.78		4.33		28.12		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24050.38		6:54:13		5:51:00		m		25.23		801.18

		S1148860134:		#B4q0		1148860134:		$B4q0		d-		30.74		4.37		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24051.42		6:54:43		5:51:30		m		25.26		802.29

		S1148860164:		#B4q0		1148860164:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24052.61		6:55:13		5:52:00		m		25.30		803.41

		S1148860194:		#B4q0		1148860194:		$B4q0		d-		30.74		4.30		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24053.64		6:55:43		5:52:30		m		25.33		804.51

		S1148860224:		#B4q0		1148860224:		$B4q0		d-		30.78		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24054.82		6:56:13		5:53:00		m		25.37		805.62

		S1148860254:		#B4q0		1148860254:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24055.86		6:56:43		5:53:30		m		25.41		806.73

		S1148860284:		#B4q0		1148860284:		$B4q0		d-		30.74		4.37		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24057.04		6:57:13		5:54:00		m		25.44		807.84

		S1148860314:		#B4q0		1148860314:		$B4q0		d-		30.74		4.33		28.12		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24058.08		6:57:43		5:54:30		m		25.48		808.96

		S1148860344:		#B4q0		1148860344:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24059.26		6:58:13		5:55:00		m		25.51		810.07

		S1148860374:		#B4q0		1148860374:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24060.3		6:58:43		5:55:30		m		25.55		811.18

		S1148860404:		#B4q0		1148860404:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82		0		-24061.48		6:59:13		5:56:00		m		25.59		812.29

		S1148860434:		#B4q0		1148860434:		$B4q0		d-		30.74		4.33		28.22		3.85		3.85		3.84		3.82		3.82		3.83		3.84		3.82		0		-24062.52		6:59:43		5:56:30		m		25.62		813.39

		S1148860464:		#B4q0		1148860464:		$B4q0		d-		30.74		4.33		28.12		3.85		3.85		3.84		3.82		3.82		3.83		3.84		3.82		0		-24063.7		7:00:13		5:57:00		m		25.66		814.50

		S1148860494:		#B4q0		1148860494:		$B4q0		d-		30.74		4.30		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24064.74		7:00:43		5:57:30		m		25.69		815.61

		S1148860524:		#B4q0		1148860524:		$B4q0		d-		30.74		4.33		28.12		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24065.92		7:01:13		5:58:00		m		25.73		816.71

		S1148860554:		#B4q0		1148860554:		$B4q0		d-		30.74		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24066.96		7:01:43		5:58:30		m		25.77		817.82

		S1148860584:		#B4q0		1148860584:		$B4q0		d-		30.74		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24068.14		7:02:13		5:59:00		m		25.80		818.93

		S1148860614:		#B4q0		1148860614:		$B4q0		d-		30.74		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24069.17		7:02:43		5:59:30		m		25.84		820.04

		S1148860644:		#B4q0		1148860644:		$B4q0		d-		30.74		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24070.35		7:03:13		6:00:00		m		25.87		821.15

		S1148860674:		#B4q0		1148860674:		$B4q0		d-		30.74		4.30		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24071.39		7:03:43		6:00:30		m		25.91		822.26

		S1148860704:		#B4q0		1148860704:		$B4q0		d-		30.71		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82		0		-24072.57		7:04:13		6:01:00		m		25.95		823.36

		S1148860734:		#B4q0		1148860734:		$B4q0		d-		30.71		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24073.6		7:04:43		6:01:30		m		25.98		824.47

		S1148860764:		#B4q0		1148860764:		$B4q0		d-		30.71		4.30		28.12		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24074.78		7:05:13		6:02:00		m		26.02		825.57

		S1148860794:		#B4q0		1148860794:		$B4q0		d-		30.74		4.33		28.12		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24075.82		7:05:43		6:02:30		m		26.05		826.68

		S1148860824:		#B4q0		1148860824:		$B4q0		d-		30.71		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24077		7:06:13		6:03:00		m		26.09		827.79

		S1148860854:		#B4q0		1148860854:		$B4q0		d-		30.74		4.33		28.22		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24078.04		7:06:43		6:03:30		m		26.13		828.90

		S1148860884:		#B4q0		1148860884:		$B4q0		d-		30.71		4.33		28.12		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82		0		-24079.22		7:07:13		6:04:00		m		26.16		830.01

		S1148860914:		#B4q0		1148860914:		$B4q0		d-		30.71		4.30		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24080.26		7:07:43		6:04:30		m		26.20		831.11

		S1148860944:		#B4q0		1148860944:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24081.44		7:08:13		6:05:00		m		26.24		832.21

		S1148860974:		#B4q0		1148860974:		$B4q0		d-		30.71		4.30		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24082.47		7:08:43		6:05:30		m		26.27		833.32

		S1148861004:		#B4q0		1148861004:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24083.66		7:09:13		6:06:00		m		26.31		834.42

		S1148861034:		#B4q0		1148861034:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24084.69		7:09:43		6:06:30		m		26.34		835.53

		S1148861064:		#B4q0		1148861064:		$B4q0		d-		30.71		4.30		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24085.88		7:10:13		6:07:00		m		26.38		836.63

		S1148861094:		#B4q0		1148861094:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24086.91		7:10:43		6:07:30		m		26.41		837.74

		S1148861124:		#B4q0		1148861124:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24088.09		7:11:13		6:08:00		m		26.45		838.85

		S1148861154:		#B4q0		1148861155:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82		0		-24089.13		7:11:43		6:08:30		m		26.49		839.96

		S1148861184:		#B4q0		1148861184:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.81		0		-24090.31		7:12:13		6:09:00		m		26.52		841.06

		S1148861214:		#B4q0		1148861214:		$B4q0		d-		30.71		4.33		28.12		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.81		0		-24091.34		7:12:43		6:09:30		m		26.56		842.17

		S1148861244:		#B4q0		1148861244:		$B4q0		d-		30.71		4.33		28.12		3.84		3.84		3.83		3.82		3.82		3.82		3.83		3.81		0		-24092.53		7:13:13		6:10:00		m		26.60		843.28

		S1148861274:		#B4q0		1148861274:		$B4q0		d-		30.71		4.33		28.22		3.84		3.84		3.83		3.82		3.82		3.82		3.83		3.81		0		-24093.56		7:13:43		6:10:30		m		26.63		844.39

		S1148861304:		#B4q0		1148861304:		$B4q0		d-		30.67		4.33		28.22		3.84		3.83		3.83		3.82		3.82		3.82		3.83		3.81		0		-24094.75		7:14:13		6:11:00		m		26.67		845.49

		S1148861334:		#B4q0		1148861334:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.82		3.81		3.82		3.83		3.81		0		-24095.78		7:14:43		6:11:30		m		26.70		846.60

		S1148861364:		#B4q0		1148861364:		$B4q0		d-		30.71		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24096.96		7:15:13		6:12:00		m		26.74		847.71

		S1148861394:		#B4q0		1148861394:		$B4q0		d-		30.71		4.33		28.22		3.84		3.83		3.83		3.82		3.81		3.82		3.83		3.81		0		-24098		7:15:43		6:12:30		m		26.78		848.82

		S1148861424:		#B4q0		1148861425:		$B4q0		d-		30.71		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24099.18		7:16:13		6:13:00		m		26.81		849.93

		S1148861454:		#B4q0		1148861454:		$B4q0		d-		30.67		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24100.21		7:16:43		6:13:30		m		26.85		851.03

		S1148861484:		#B4q0		1148861484:		$B4q0		d-		30.67		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24101.39		7:17:13		6:14:00		m		26.88		852.14

		S1148861514:		#B4q0		1148861514:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24102.42		7:17:43		6:14:30		m		26.92		853.25

		S1148861544:		#B4q0		1148861545:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24103.61		7:18:13		6:15:00		m		26.96		854.35

		S1148861574:		#B4q0		1148861574:		$B4q0		d-		30.67		4.30		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24104.64		7:18:43		6:15:30		m		26.99		855.46

		S1148861604:		#B4q0		1148861604:		$B4q0		d-		30.67		4.30		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24105.82		7:19:13		6:16:00		m		27.03		856.55

		S1148861634:		#B4q0		1148861634:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24106.85		7:19:43		6:16:30		m		27.06		857.66

		S1148861664:		#B4q0		1148861664:		$B4q0		d-		30.67		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24108.03		7:20:13		6:17:00		m		27.10		858.76

		S1148861694:		#B4q0		1148861694:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24109.07		7:20:43		6:17:30		m		27.14		859.87

		S1148861724:		#B4q0		1148861724:		$B4q0		d-		30.63		4.33		28.22		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24110.25		7:21:13		6:18:00		m		27.17		860.98

		S1148861754:		#B4q0		1148861754:		$B4q0		d-		30.67		4.33		28.12		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24111.28		7:21:43		6:18:30		m		27.21		862.08

		S1148861784:		#B4q0		1148861784:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24112.46		7:22:13		6:19:00		m		27.24		863.19

		S1148861814:		#B4q0		1148861814:		$B4q0		d-		30.67		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24113.49		7:22:43		6:19:30		m		27.28		864.29

		S1148861844:		#B4q0		1148861844:		$B4q0		d-		30.63		4.33		28.22		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24114.67		7:23:13		6:20:00		m		27.32		865.40

		S1148861874:		#B4q0		1148861874:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24115.7		7:23:43		6:20:30		m		27.35		866.51

		S1148861904:		#B4q0		1148861904:		$B4q0		d-		30.63		4.33		28.22		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24116.87		7:24:13		6:21:00		m		27.39		867.61

		S1148861934:		#B4q0		1148861934:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24117.91		7:24:43		6:21:30		m		27.42		868.72

		S1148861964:		#B4q0		1148861964:		$B4q0		d-		30.63		4.30		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81		0		-24119.09		7:25:13		6:22:00		m		27.46		869.82

		S1148861994:		#B4q0		1148861994:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81		0		-24120.12		7:25:43		6:22:30		m		27.50		870.92

		S1148862024:		#B4q0		1148862024:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81		0		-24121.3		7:26:13		6:23:00		m		27.53		872.02

		S1148862054:		#B4q0		1148862054:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81		0		-24122.32		7:26:43		6:23:30		m		27.57		873.13

		S1148862084:		#B4q0		1148862084:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81		0		-24123.5		7:27:13		6:24:00		m		27.60		874.23

		S1148862114:		#B4q0		1148862114:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81		0		-24124.54		7:27:43		6:24:30		m		27.64		875.34

		S1148862144:		#B4q0		1148862144:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.80		0		-24125.71		7:28:13		6:25:00		m		27.68		876.45

		S1148862174:		#B4q0		1148862174:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.80		0		-24126.75		7:28:43		6:25:30		m		27.71		877.55

		S1148862204:		#B4q0		1148862204:		$B4q0		d-		30.59		4.30		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.80		0		-24127.92		7:29:13		6:26:00		m		27.75		878.65

		S1148862234:		#B4q0		1148862234:		$B4q0		d-		30.59		4.37		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.80		0		-24128.95		7:29:43		6:26:30		m		27.79		879.76

		S1148862264:		#B4q0		1148862264:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.80		0		-24130.13		7:30:13		6:27:00		m		27.82		880.87

		S1148862294:		#B4q0		1148862294:		$B4q0		d-		30.59		4.30		28.12		3.83		3.83		3.83		3.81		3.80		3.82		3.82		3.80		0		-24131.16		7:30:43		6:27:30		m		27.86		881.97

		S1148862324:		#B4q0		1148862324:		$B4q0		d-		30.63		4.37		28.12		3.83		3.83		3.83		3.81		3.80		3.82		3.82		3.80		0		-24132.34		7:31:13		6:28:00		m		27.89		883.07

		S1148862354:		#B4q0		1148862354:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24133.37		7:31:43		6:28:30		m		27.93		884.18

		S1148862384:		#B4q0		1148862384:		$B4q0		d-		30.59		4.33		28.12		3.83		3.83		3.83		3.81		3.80		3.81		3.82		3.80		0		-24134.55		7:32:13		6:29:00		m		27.97		885.29

		S1148862414:		#B4q0		1148862414:		$B4q0		d-		30.59		4.33		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24135.58		7:32:43		6:29:30		m		28.00		886.39

		S1148862444:		#B4q0		1148862444:		$B4q0		d-		30.63		4.30		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24136.75		7:33:13		6:30:00		m		28.04		887.49

		S1148862474:		#B4q0		1148862474:		$B4q0		d-		30.59		4.30		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24137.78		7:33:43		6:30:30		m		28.07		888.59

		S1148862504:		#B4q0		1148862504:		$B4q0		d-		30.59		4.30		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24138.96		7:34:13		6:31:00		m		28.11		889.68

		S1148862534:		#B4q0		1148862534:		$B4q0		d-		30.59		4.30		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24139.99		7:34:43		6:31:30		m		28.15		890.78

		S1148862564:		#B4q0		1148862564:		$B4q0		d-		30.63		4.33		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24141.16		7:35:13		6:32:00		m		28.18		891.88

		S1148862594:		#B4q0		1148862594:		$B4q0		d-		30.59		4.33		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24142.2		7:35:43		6:32:30		m		28.22		892.99

		S1148862624:		#B4q0		1148862624:		$B4q0		d-		30.59		4.33		28.12		3.83		3.83		3.83		3.80		3.80		3.81		3.82		3.80		0		-24143.37		7:36:13		6:33:00		m		28.25		894.09

		S1148862654:		#B4q0		1148862654:		$B4q0		d-		30.59		4.33		28.12		3.83		3.83		3.82		3.80		3.80		3.81		3.82		3.80		0		-24144.4		7:36:43		6:33:30		m		28.29		895.19

		S1148862684:		#B4q0		1148862684:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24145.58		7:37:13		6:34:00		m		28.33		896.30

		S1148862714:		#B4q0		1148862714:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24146.61		7:37:43		6:34:30		m		28.36		897.40

		S1148862744:		#B4q0		1148862744:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24147.78		7:38:13		6:35:00		m		28.40		898.50

		S1148862774:		#B4q0		1148862774:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24148.81		7:38:43		6:35:30		m		28.43		899.61

		S1148862804:		#B4q0		1148862804:		$B4q0		d-		30.59		4.30		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24149.99		7:39:13		6:36:00		m		28.47		900.71

		S1148862834:		#B4q0		1148862834:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24151.02		7:39:43		6:36:30		m		28.51		901.81

		S1148862864:		#B4q0		1148862864:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24152.2		7:40:13		6:37:00		m		28.54		902.91

		S1148862894:		#B4q0		1148862894:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24153.23		7:40:43		6:37:30		m		28.58		904.01

		S1148862924:		#B4q0		1148862924:		$B4q0		d-		30.55		4.30		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24154.41		7:41:13		6:38:00		m		28.61		905.11

		S1148862954:		#B4q0		1148862954:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24155.44		7:41:43		6:38:30		m		28.65		906.21

		S1148862984:		#B4q0		1148862984:		$B4q0		d-		30.59		4.30		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24156.61		7:42:13		6:39:00		m		28.69		907.31

		S1148863014:		#B4q0		1148863014:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24157.64		7:42:43		6:39:30		m		28.72		908.41

		S1148863044:		#B4q0		1148863044:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24158.82		7:43:13		6:40:00		m		28.76		909.51

		S1148863074:		#B4q0		1148863074:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24159.85		7:43:43		6:40:30		m		28.79		910.62

		S1148863104:		#B4q0		1148863104:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24161.03		7:44:13		6:41:00		m		28.83		911.72

		S1148863134:		#B4q0		1148863134:		$B4q0		d-		30.59		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24162.06		7:44:43		6:41:30		m		28.87		912.82

		S1148863164:		#B4q0		1148863164:		$B4q0		d-		30.55		4.33		28.12		3.83		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24163.24		7:45:13		6:42:00		m		28.90		913.92

		S1148863194:		#B4q0		1148863194:		$B4q0		d-		30.55		4.37		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24164.27		7:45:43		6:42:30		m		28.94		915.03

		S1148863224:		#B4q0		1148863224:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24165.45		7:46:13		6:43:00		m		28.97		916.14

		S1148863254:		#B4q0		1148863254:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24166.48		7:46:43		6:43:30		m		29.01		917.24

		S1148863284:		#B4q0		1148863284:		$B4q0		d-		30.55		4.30		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24167.65		7:47:13		6:44:00		m		29.05		918.34

		S1148863314:		#B4q0		1148863314:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24168.68		7:47:43		6:44:30		m		29.08		919.44

		S1148863344:		#B4q0		1148863344:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.81		3.82		3.80		0		-24169.86		7:48:13		6:45:00		m		29.12		920.54

		S1148863374:		#B4q0		1148863374:		$B4q0		d-		30.55		4.30		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.82		3.80		0		-24170.89		7:48:43		6:45:30		m		29.15		921.64

		S1148863404:		#B4q0		1148863404:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24172.07		7:49:13		6:46:00		m		29.19		922.74

		S1148863434:		#B4q0		1148863434:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24173.1		7:49:43		6:46:30		m		29.23		923.84

		S1148863464:		#B4q0		1148863464:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24174.27		7:50:13		6:47:00		m		29.26		924.94

		S1148863494:		#B4q0		1148863494:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24175.3		7:50:43		6:47:30		m		29.30		926.04

		S1148863524:		#B4q0		1148863524:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24176.48		7:51:13		6:48:00		m		29.34		927.15

		S1148863554:		#B4q0		1148863554:		$B4q0		d-		30.55		4.37		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24177.51		7:51:43		6:48:30		m		29.37		928.25

		S1148863584:		#B4q0		1148863584:		$B4q0		d-		30.55		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24178.68		7:52:13		6:49:00		m		29.41		929.36

		S1148863614:		#B4q0		1148863614:		$B4q0		d-		30.55		4.30		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24179.71		7:52:43		6:49:30		m		29.44		930.46

		S1148863644:		#B4q0		1148863644:		$B4q0		d-		30.55		4.30		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24180.89		7:53:13		6:50:00		m		29.48		931.55

		S1148863674:		#B4q0		1148863674:		$B4q0		d-		30.55		4.33		28.02		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24181.92		7:53:43		6:50:30		m		29.52		932.65

		S1148863704:		#B4q0		1148863704:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24183.09		7:54:13		6:51:00		m		29.55		933.75

		S1148863734:		#B4q0		1148863734:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.80		0		-24184.12		7:54:43		6:51:30		m		29.59		934.85

		S1148863764:		#B4q0		1148863764:		$B4q0		d-		30.55		4.37		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.79		0		-24185.29		7:55:13		6:52:00		m		29.62		935.96

		S1148863794:		#B4q0		1148863794:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.80		3.80		3.80		3.81		3.79		0		-24186.32		7:55:43		6:52:30		m		29.66		937.07

		S1148863824:		#B4q0		1148863824:		$B4q0		d-		30.51		4.33		28.02		3.82		3.82		3.82		3.80		3.79		3.80		3.81		3.79		0		-24187.5		7:56:13		6:53:00		m		29.70		938.17

		S1148863854:		#B4q0		1148863854:		$B4q0		d-		30.51		4.33		28.02		3.82		3.82		3.82		3.79		3.80		3.80		3.81		3.79		0		-24188.52		7:56:43		6:53:30		m		29.73		939.27

		S1148863884:		#B4q0		1148863884:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24189.7		7:57:13		6:54:00		m		29.77		940.37

		S1148863914:		#B4q0		1148863914:		$B4q0		d-		30.51		4.30		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24190.73		7:57:43		6:54:30		m		29.80		941.47

		S1148863944:		#B4q0		1148863944:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24191.9		7:58:13		6:55:00		m		29.84		942.57

		S1148863974:		#B4q0		1148863974:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24192.93		7:58:43		6:55:30		m		29.88		943.67

		S1148864004:		#B4q0		1148864004:		$B4q0		d-		30.51		4.37		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24194.1		7:59:13		6:56:00		m		29.91		944.77

		S1148864034:		#B4q0		1148864034:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24195.13		7:59:43		6:56:30		m		29.95		945.88

		S1148864064:		#B4q0		1148864064:		$B4q0		d-		30.51		4.30		28.02		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24196.31		8:00:13		6:57:00		m		29.98		946.98

		S1148864094:		#B4q0		1148864094:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24197.34		8:00:43		6:57:30		m		30.02		948.07

		S1148864124:		#B4q0		1148864124:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24198.51		8:01:13		6:58:00		m		30.06		949.17

		S1148864154:		#B4q0		1148864154:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24199.54		8:01:43		6:58:30		m		30.09		950.27

		S1148864184:		#B4q0		1148864184:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24200.72		8:02:13		6:59:00		m		30.13		951.37

		S1148864214:		#B4q0		1148864214:		$B4q0		d-		30.51		4.30		28.12		3.82		3.82		3.82		3.79		3.79		3.80		3.81		3.79		0		-24201.74		8:02:43		6:59:30		m		30.16		952.47

		S1148864244:		#B4q0		1148864244:		$B4q0		d-		30.51		4.33		28.12		3.82		3.82		3.81		3.79		3.79		3.80		3.81		3.79		0		-24202.92		8:03:13		7:00:00		m		30.20		953.57

		S1148864274:		#B4q0		1148864274:		$B4q0		d-		30.48		4.33		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24203.94		8:03:43		7:00:30		m		30.24		954.67

		S1148864304:		#B4q0		1148864304:		$B4q0		d-		30.48		4.33		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24205.12		8:04:13		7:01:00		m		30.27		955.77

		S1148864334:		#B4q0		1148864334:		$B4q0		d-		30.48		4.30		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24206.14		8:04:43		7:01:30		m		30.31		956.87

		S1148864364:		#B4q0		1148864364:		$B4q0		d-		30.48		4.33		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24207.32		8:05:13		7:02:00		m		30.35		957.96

		S1148864394:		#B4q0		1148864394:		$B4q0		d-		30.48		4.33		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24208.34		8:05:43		7:02:30		m		30.38		959.06

		S1148864424:		#B4q0		1148864424:		$B4q0		d-		30.48		4.30		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24209.52		8:06:13		7:03:00		m		30.42		960.16

		S1148864454:		#B4q0		1148864454:		$B4q0		d-		30.48		4.37		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24210.54		8:06:43		7:03:30		m		30.45		961.26

		S1148864484:		#B4q0		1148864484:		$B4q0		d-		30.48		4.30		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24211.72		8:07:13		7:04:00		m		30.49		962.36

		S1148864514:		#B4q0		1148864514:		$B4q0		d-		30.48		4.33		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.81		3.79		0		-24212.74		8:07:43		7:04:30		m		30.53		963.46

		S1148864544:		#B4q0		1148864544:		$B4q0		d-		30.51		4.33		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24213.92		8:08:13		7:05:00		m		30.56		964.56

		S1148864574:		#B4q0		1148864574:		$B4q0		d-		30.48		4.33		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24214.95		8:08:43		7:05:30		m		30.60		965.66

		S1148864604:		#B4q0		1148864604:		$B4q0		d-		30.44		4.33		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24216.12		8:09:13		7:06:00		m		30.63		966.76

		S1148864634:		#B4q0		1148864634:		$B4q0		d-		30.48		4.30		28.12		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24217.14		8:09:43		7:06:30		m		30.67		967.85

		S1148864664:		#B4q0		1148864664:		$B4q0		d-		30.44		4.33		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24218.31		8:10:13		7:07:00		m		30.71		968.95

		S1148864694:		#B4q0		1148864694:		$B4q0		d-		30.44		4.33		28.02		3.82		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24219.34		8:10:43		7:07:30		m		30.74		970.04

		S1148864724:		#B4q0		1148864724:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24220.51		8:11:13		7:08:00		m		30.78		971.14

		S1148864754:		#B4q0		1148864754:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24221.54		8:11:43		7:08:30		m		30.81		972.24

		S1148864784:		#B4q0		1148864784:		$B4q0		d-		30.48		4.37		28.12		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24222.71		8:12:13		7:09:00		m		30.85		973.35

		S1148864814:		#B4q0		1148864814:		$B4q0		d-		30.44		4.37		28.02		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24223.74		8:12:43		7:09:30		m		30.89		974.45

		S1148864844:		#B4q0		1148864844:		$B4q0		d-		30.48		4.33		28.12		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.79		0		-24224.91		8:13:13		7:10:00		m		30.92		975.56

		S1148864874:		#B4q0		1148864874:		$B4q0		d-		30.44		4.30		28.12		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.78		0		-24225.93		8:13:43		7:10:30		m		30.96		976.65

		S1148864904:		#B4q0		1148864904:		$B4q0		d-		30.48		4.33		28.02		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.78		0		-24227.1		8:14:13		7:11:00		m		30.99		977.75

		S1148864934:		#B4q0		1148864934:		$B4q0		d-		30.44		4.37		28.02		3.81		3.81		3.81		3.79		3.79		3.80		3.80		3.78		0		-24228.13		8:14:43		7:11:30		m		31.03		978.85

		S1148864964:		#B4q0		1148864964:		$B4q0		d-		30.44		4.33		28.02		3.81		3.81		3.81		3.78		3.79		3.80		3.80		3.78		0		-24229.3		8:15:13		7:12:00		m		31.07		979.96

		S1148864994:		#B4q0		1148864994:		$B4q0		d-		30.44		4.30		28.02		3.81		3.81		3.81		3.78		3.78		3.80		3.80		3.78		0		-24230.33		8:15:43		7:12:30		m		31.10		981.05

		S1148865024:		#B4q0		1148865024:		$B4q0		d-		30.44		4.30		28.02		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24231.5		8:16:13		7:13:00		m		31.14		982.14

		S1148865054:		#B4q0		1148865054:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24232.53		8:16:43		7:13:30		m		31.17		983.24

		S1148865084:		#B4q0		1148865084:		$B4q0		d-		30.44		4.30		28.02		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24233.7		8:17:13		7:14:00		m		31.21		984.33

		S1148865114:		#B4q0		1148865114:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24234.73		8:17:43		7:14:30		m		31.25		985.43

		S1148865144:		#B4q0		1148865144:		$B4q0		d-		30.44		4.33		28.02		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24235.9		8:18:13		7:15:00		m		31.28		986.52

		S1148865174:		#B4q0		1148865174:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24236.92		8:18:43		7:15:30		m		31.32		987.62

		S1148865204:		#B4q0		1148865204:		$B4q0		d-		30.44		4.30		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24238.09		8:19:13		7:16:00		m		31.35		988.72

		S1148865234:		#B4q0		1148865234:		$B4q0		d-		30.44		4.30		28.02		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24239.12		8:19:43		7:16:30		m		31.39		989.81

		S1148865264:		#B4q0		1148865264:		$B4q0		d-		30.44		4.30		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24240.29		8:20:13		7:17:00		m		31.43		990.90

		S1148865294:		#B4q0		1148865294:		$B4q0		d-		30.44		4.33		28.12		3.81		3.81		3.81		3.78		3.78		3.79		3.80		3.78		0		-24241.31		8:20:43		7:17:30		m		31.46		991.99

		S1148865324:		#B4q0		1148865324:		$B4q0		d-		30.44		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24242.49		8:21:13		7:18:00		m		31.50		993.09

		S1148865354:		#B4q0		1148865354:		$B4q0		d-		30.44		4.33		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24243.51		8:21:43		7:18:30		m		31.53		994.19

		S1148865384:		#B4q0		1148865384:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24244.68		8:22:13		7:19:00		m		31.57		995.29

		S1148865414:		#B4q0		1148865414:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24245.71		8:22:43		7:19:30		m		31.61		996.38

		S1148865444:		#B4q0		1148865444:		$B4q0		d-		30.40		4.33		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24246.88		8:23:13		7:20:00		m		31.64		997.48

		S1148865474:		#B4q0		1148865474:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24247.9		8:23:43		7:20:30		m		31.68		998.58

		S1148865504:		#B4q0		1148865504:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24249.07		8:24:13		7:21:00		m		31.72		999.68

		S1148865534:		#B4q0		1148865534:		$B4q0		d-		30.40		4.30		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24250.09		8:24:43		7:21:30		m		31.75		1000.77

		S1148865564:		#B4q0		1148865564:		$B4q0		d-		30.40		4.33		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24251.27		8:25:13		7:22:00		m		31.79		1001.86

		S1148865594:		#B4q0		1148865594:		$B4q0		d-		30.40		4.30		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24252.29		8:25:43		7:22:30		m		31.82		1002.95

		S1148865624:		#B4q0		1148865624:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24253.46		8:26:13		7:23:00		m		31.86		1004.05

		S1148865654:		#B4q0		1148865654:		$B4q0		d-		30.40		4.30		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24254.49		8:26:43		7:23:30		m		31.89		1005.14

		S1148865684:		#B4q0		1148865684:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24255.66		8:27:13		7:24:00		m		31.93		1006.23

		S1148865714:		#B4q0		1148865714:		$B4q0		d-		30.44		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24256.68		8:27:43		7:24:30		m		31.97		1007.33

		S1148865744:		#B4q0		1148865744:		$B4q0		d-		30.40		4.33		28.02		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24257.85		8:28:13		7:25:00		m		32.00		1008.43

		S1148865774:		#B4q0		1148865774:		$B4q0		d-		30.40		4.33		28.12		3.81		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24258.88		8:28:43		7:25:30		m		32.04		1009.53

		S1148865804:		#B4q0		1148865804:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24260.05		8:29:13		7:26:00		m		32.08		1010.62

		S1148865834:		#B4q0		1148865834:		$B4q0		d-		30.40		4.33		28.12		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24261.07		8:29:43		7:26:30		m		32.11		1011.72

		S1148865864:		#B4q0		1148865864:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24262.24		8:30:13		7:27:00		m		32.15		1012.82

		S1148865894:		#B4q0		1148865894:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24263.26		8:30:43		7:27:30		m		32.18		1013.91

		S1148865924:		#B4q0		1148865924:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24264.43		8:31:13		7:28:00		m		32.22		1015.01

		S1148865954:		#B4q0		1148865954:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24265.46		8:31:43		7:28:30		m		32.26		1016.11

		S1148865984:		#B4q0		1148865984:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24266.63		8:32:13		7:29:00		m		32.29		1017.20

		S1148866014:		#B4q0		1148866014:		$B4q0		d-		30.40		4.33		28.12		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24267.65		8:32:43		7:29:30		m		32.33		1018.30

		S1148866044:		#B4q0		1148866044:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24268.82		8:33:13		7:30:00		m		32.36		1019.40

		S1148866074:		#B4q0		1148866074:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24269.85		8:33:43		7:30:30		m		32.40		1020.50

		S1148866104:		#B4q0		1148866104:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24271.02		8:34:13		7:31:00		m		32.44		1021.59

		S1148866134:		#B4q0		1148866134:		$B4q0		d-		30.40		4.30		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.80		3.78		0		-24272.05		8:34:43		7:31:30		m		32.47		1022.69

		S1148866164:		#B4q0		1148866164:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.79		3.79		3.78		0		-24273.22		8:35:13		7:32:00		m		32.51		1023.78

		S1148866194:		#B4q0		1148866194:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.80		3.78		0		-24274.24		8:35:43		7:32:30		m		32.54		1024.88

		S1148866224:		#B4q0		1148866224:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24275.41		8:36:13		7:33:00		m		32.58		1025.97

		S1148866254:		#B4q0		1148866254:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24276.43		8:36:43		7:33:30		m		32.62		1027.07

		S1148866284:		#B4q0		1148866284:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24277.6		8:37:13		7:34:00		m		32.65		1028.17

		S1148866314:		#B4q0		1148866314:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24278.62		8:37:43		7:34:30		m		32.69		1029.26

		S1148866344:		#B4q0		1148866344:		$B4q0		d-		30.40		4.37		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24279.79		8:38:13		7:35:00		m		32.72		1030.36

		S1148866374:		#B4q0		1148866374:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24280.82		8:38:43		7:35:30		m		32.76		1031.47

		S1148866404:		#B4q0		1148866404:		$B4q0		d-		30.40		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24281.99		8:39:13		7:36:00		m		32.80		1032.56

		S1148866434:		#B4q0		1148866434:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24283.01		8:39:43		7:36:30		m		32.83		1033.66

		S1148866464:		#B4q0		1148866464:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24284.18		8:40:13		7:37:00		m		32.87		1034.75

		S1148866494:		#B4q0		1148866494:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24285.21		8:40:43		7:37:30		m		32.91		1035.85

		S1148866524:		#B4q0		1148866524:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24286.38		8:41:13		7:38:00		m		32.94		1036.95

		S1148866554:		#B4q0		1148866554:		$B4q0		d-		30.36		4.30		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24287.4		8:41:43		7:38:30		m		32.98		1038.04

		S1148866584:		#B4q0		1148866584:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24288.57		8:42:13		7:39:00		m		33.01		1039.13

		S1148866614:		#B4q0		1148866614:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.78		3.78		3.79		3.78		0		-24289.59		8:42:43		7:39:30		m		33.05		1040.22

		S1148866644:		#B4q0		1148866644:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.78		3.78		3.78		3.79		3.78		0		-24290.75		8:43:13		7:40:00		m		33.09		1041.32

		S1148866674:		#B4q0		1148866674:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.78		3.78		3.79		3.77		0		-24291.77		8:43:43		7:40:30		m		33.12		1042.42

		S1148866704:		#B4q0		1148866704:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.78		3.78		3.79		3.77		0		-24292.94		8:44:13		7:41:00		m		33.16		1043.51

		S1148866734:		#B4q0		1148866734:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.78		3.78		3.79		3.77		0		-24293.97		8:44:43		7:41:30		m		33.19		1044.61

		S1148866764:		#B4q0		1148866764:		$B4q0		d-		30.33		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24295.14		8:45:13		7:42:00		m		33.23		1045.70

		S1148866794:		#B4q0		1148866794:		$B4q0		d-		30.33		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24296.16		8:45:43		7:42:30		m		33.27		1046.80

		S1148866824:		#B4q0		1148866824:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24297.33		8:46:13		7:43:00		m		33.30		1047.89

		S1148866854:		#B4q0		1148866854:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24298.35		8:46:43		7:43:30		m		33.34		1048.99

		S1148866884:		#B4q0		1148866884:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24299.52		8:47:13		7:44:00		m		33.37		1050.08

		S1148866914:		#B4q0		1148866914:		$B4q0		d-		30.36		4.37		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24300.54		8:47:43		7:44:30		m		33.41		1051.18

		S1148866944:		#B4q0		1148866944:		$B4q0		d-		30.33		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24301.71		8:48:13		7:45:00		m		33.45		1052.28

		S1148866974:		#B4q0		1148866974:		$B4q0		d-		30.36		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24302.73		8:48:43		7:45:30		m		33.48		1053.38

		S1148867004:		#B4q0		1148867004:		$B4q0		d-		30.36		4.33		27.92		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24303.9		8:49:13		7:46:00		m		33.52		1054.47

		S1148867034:		#B4q0		1148867034:		$B4q0		d-		30.33		4.30		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24304.92		8:49:43		7:46:30		m		33.55		1055.56

		S1148867064:		#B4q0		1148867064:		$B4q0		d-		30.33		4.33		28.02		3.80		3.80		3.80		3.77		3.77		3.78		3.79		3.77		0		-24306.09		8:50:13		7:47:00		m		33.59		1056.65

		S1148867094:		#B4q0		1148867094:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.80		3.77		3.77		3.78		3.79		3.77		0		-24307.11		8:50:43		7:47:30		m		33.63		1057.75

		S1148867124:		#B4q0		1148867124:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.80		3.77		3.77		3.78		3.79		3.77		0		-24308.28		8:51:13		7:48:00		m		33.66		1058.84

		S1148867154:		#B4q0		1148867154:		$B4q0		d-		30.36		4.30		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24309.3		8:51:43		7:48:30		m		33.70		1059.93

		S1148867184:		#B4q0		1148867184:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24310.47		8:52:13		7:49:00		m		33.73		1061.03

		S1148867214:		#B4q0		1148867214:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24311.5		8:52:43		7:49:30		m		33.77		1062.12

		S1148867244:		#B4q0		1148867244:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24312.66		8:53:13		7:50:00		m		33.81		1063.21

		S1148867274:		#B4q0		1148867274:		$B4q0		d-		30.33		4.33		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24313.68		8:53:43		7:50:30		m		33.84		1064.31

		S1148867304:		#B4q0		1148867304:		$B4q0		d-		30.33		4.30		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24314.85		8:54:13		7:51:00		m		33.88		1065.40

		S1148867334:		#B4q0		1148867334:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24315.87		8:54:43		7:51:30		m		33.91		1066.49

		S1148867364:		#B4q0		1148867364:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.79		3.77		0		-24317.04		8:55:13		7:52:00		m		33.95		1067.58

		S1148867394:		#B4q0		1148867394:		$B4q0		d-		30.33		4.33		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24318.06		8:55:43		7:52:30		m		33.99		1068.68

		S1148867424:		#B4q0		1148867424:		$B4q0		d-		30.29		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24319.23		8:56:13		7:53:00		m		34.02		1069.77

		S1148867454:		#B4q0		1148867454:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24320.25		8:56:43		7:53:30		m		34.06		1070.87

		S1148867484:		#B4q0		1148867484:		$B4q0		d-		30.29		4.30		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24321.42		8:57:13		7:54:00		m		34.09		1071.96

		S1148867514:		#B4q0		1148867514:		$B4q0		d-		30.33		4.33		28.02		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24322.44		8:57:43		7:54:30		m		34.13		1073.05

		S1148867544:		#B4q0		1148867544:		$B4q0		d-		30.33		4.33		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24323.6		8:58:13		7:55:00		m		34.17		1074.14

		S1148867574:		#B4q0		1148867574:		$B4q0		d-		30.29		4.30		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24324.62		8:58:43		7:55:30		m		34.20		1075.23

		S1148867604:		#B4q0		1148867604:		$B4q0		d-		30.29		4.33		27.92		3.80		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24325.79		8:59:13		7:56:00		m		34.24		1076.32

		S1148867634:		#B4q0		1148867634:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24326.81		8:59:43		7:56:30		m		34.28		1077.41

		S1148867664:		#B4q0		1148867664:		$B4q0		d-		30.33		4.33		28.02		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24327.98		9:00:13		7:57:00		m		34.31		1078.51

		S1148867694:		#B4q0		1148867694:		$B4q0		d-		30.29		4.30		28.02		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24329		9:00:43		7:57:30		m		34.35		1079.60

		S1148867724:		#B4q0		1148867724:		$B4q0		d-		30.29		4.33		28.02		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24330.16		9:01:13		7:58:00		m		34.38		1080.69

		S1148867754:		#B4q0		1148867754:		$B4q0		d-		30.29		4.37		27.92		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24331.18		9:01:43		7:58:30		m		34.42		1081.78

		S1148867784:		#B4q0		1148867784:		$B4q0		d-		30.33		4.33		28.02		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24332.35		9:02:13		7:59:00		m		34.46		1082.88

		S1148867814:		#B4q0		1148867814:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24333.37		9:02:43		7:59:30		m		34.49		1083.98

		S1148867844:		#B4q0		1148867844:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24334.53		9:03:13		8:00:00		m		34.53		1085.07

		S1148867874:		#B4q0		1148867874:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.77		3.78		3.78		3.77		0		-24335.55		9:03:43		8:00:30		m		34.56		1086.16

		S1148867904:		#B4q0		1148867904:		$B4q0		d-		30.29		4.33		28.02		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77		0		-24336.72		9:04:13		8:01:00		m		34.60		1087.25

		S1148867934:		#B4q0		1148867934:		$B4q0		d-		30.29		4.33		28.02		3.79		3.79		3.79		3.76		3.77		3.78		3.78		3.77		0		-24337.74		9:04:43		8:01:30		m		34.64		1088.35

		S1148867964:		#B4q0		1148867964:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.76		0		-24338.91		9:05:13		8:02:00		m		34.67		1089.44

		S1148867994:		#B4q0		1148867994:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.78		3.78		3.76		0		-24339.93		9:05:43		8:02:30		m		34.71		1090.53

		S1148868024:		#B4q0		1148868024:		$B4q0		d-		30.29		4.37		27.92		3.79		3.79		3.79		3.76		3.76		3.78		3.78		3.76		0		-24341.1		9:06:13		8:03:00		m		34.74		1091.63

		S1148868054:		#B4q0		1148868054:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24342.12		9:06:43		8:03:30		m		34.78		1092.73

		S1148868084:		#B4q0		1148868084:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24343.28		9:07:13		8:04:00		m		34.82		1093.82

		S1148868114:		#B4q0		1148868114:		$B4q0		d-		30.25		4.30		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24344.3		9:07:43		8:04:30		m		34.85		1094.91

		S1148868144:		#B4q0		1148868144:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24345.47		9:08:13		8:05:00		m		34.89		1096.00

		S1148868174:		#B4q0		1148868174:		$B4q0		d-		30.29		4.30		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24346.49		9:08:43		8:05:30		m		34.92		1097.09

		S1148868204:		#B4q0		1148868204:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24347.66		9:09:13		8:06:00		m		34.96		1098.18

		S1148868234:		#B4q0		1148868234:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24348.68		9:09:43		8:06:30		m		35.00		1099.27

		S1148868264:		#B4q0		1148868264:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24349.84		9:10:13		8:07:00		m		35.03		1100.36

		S1148868294:		#B4q0		1148868294:		$B4q0		d-		30.25		4.30		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24350.86		9:10:43		8:07:30		m		35.07		1101.45

		S1148868324:		#B4q0		1148868324:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24352.03		9:11:13		8:08:00		m		35.10		1102.54

		S1148868354:		#B4q0		1148868354:		$B4q0		d-		30.29		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24353.05		9:11:43		8:08:30		m		35.14		1103.63

		S1148868384:		#B4q0		1148868384:		$B4q0		d-		30.29		4.33		27.92		3.79		3.78		3.79		3.76		3.76		3.77		3.78		3.76		0		-24354.22		9:12:13		8:09:00		m		35.18		1104.73

		S1148868414:		#B4q0		1148868414:		$B4q0		d-		30.25		4.33		27.92		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76		0		-24355.24		9:12:43		8:09:30		m		35.21		1105.82

		S1148868444:		#B4q0		1148868444:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.79		3.76		3.76		3.77		3.78		3.76		0		-24356.4		9:13:13		8:10:00		m		35.25		1106.91

		S1148868474:		#B4q0		1148868474:		$B4q0		d-		30.29		4.30		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24357.42		9:13:43		8:10:30		m		35.28		1108.00

		S1148868504:		#B4q0		1148868504:		$B4q0		d-		30.25		4.30		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24358.59		9:14:13		8:11:00		m		35.32		1109.08

		S1148868534:		#B4q0		1148868534:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24359.6		9:14:43		8:11:30		m		35.36		1110.17

		S1148868564:		#B4q0		1148868564:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24360.77		9:15:13		8:12:00		m		35.39		1111.26

		S1148868594:		#B4q0		1148868594:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24361.78		9:15:43		8:12:30		m		35.43		1112.35

		S1148868624:		#B4q0		1148868624:		$B4q0		d-		30.25		4.30		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24362.95		9:16:13		8:13:00		m		35.46		1113.44

		S1148868654:		#B4q0		1148868654:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24363.96		9:16:43		8:13:30		m		35.50		1114.53

		S1148868684:		#B4q0		1148868684:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24365.13		9:17:13		8:14:00		m		35.54		1115.62

		S1148868714:		#B4q0		1148868714:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24366.15		9:17:43		8:14:30		m		35.57		1116.71

		S1148868744:		#B4q0		1148868744:		$B4q0		d-		30.21		4.30		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24367.31		9:18:13		8:15:00		m		35.61		1117.80

		S1148868774:		#B4q0		1148868774:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24368.33		9:18:43		8:15:30		m		35.64		1118.89

		S1148868804:		#B4q0		1148868804:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24369.49		9:19:13		8:16:00		m		35.68		1119.98

		S1148868834:		#B4q0		1148868834:		$B4q0		d-		30.25		4.33		27.92		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24370.51		9:19:43		8:16:30		m		35.72		1121.07

		S1148868864:		#B4q0		1148868864:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24371.67		9:20:13		8:17:00		m		35.75		1122.16

		S1148868894:		#B4q0		1148868894:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24372.69		9:20:43		8:17:30		m		35.79		1123.25

		S1148868924:		#B4q0		1148868924:		$B4q0		d-		30.25		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24373.86		9:21:13		8:18:00		m		35.83		1124.34

		S1148868954:		#B4q0		1148868954:		$B4q0		d-		30.25		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24374.87		9:21:43		8:18:30		m		35.86		1125.42

		S1148868984:		#B4q0		1148868984:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24376.04		9:22:13		8:19:00		m		35.90		1126.51

		S1148869014:		#B4q0		1148869014:		$B4q0		d-		30.25		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24377.06		9:22:43		8:19:30		m		35.93		1127.60

		S1148869044:		#B4q0		1148869044:		$B4q0		d-		30.25		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24378.22		9:23:13		8:20:00		m		35.97		1128.68

		S1148869074:		#B4q0		1148869074:		$B4q0		d-		30.21		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24379.24		9:23:43		8:20:30		m		36.00		1129.77

		S1148869104:		#B4q0		1148869104:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24380.4		9:24:13		8:21:00		m		36.04		1130.85

		S1148869134:		#B4q0		1148869134:		$B4q0		d-		30.25		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24381.42		9:24:43		8:21:30		m		36.08		1131.94

		S1148869164:		#B4q0		1148869164:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24382.59		9:25:13		8:22:00		m		36.11		1133.03

		S1148869194:		#B4q0		1148869194:		$B4q0		d-		30.21		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24383.6		9:25:43		8:22:30		m		36.15		1134.12

		S1148869224:		#B4q0		1148869224:		$B4q0		d-		30.21		4.37		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24384.77		9:26:13		8:23:00		m		36.18		1135.21

		S1148869254:		#B4q0		1148869254:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24385.79		9:26:43		8:23:30		m		36.22		1136.30

		S1148869284:		#B4q0		1148869284:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24386.95		9:27:13		8:24:00		m		36.26		1137.39

		S1148869314:		#B4q0		1148869314:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76		0		-24387.97		9:27:43		8:24:30		m		36.29		1138.48

		S1148869344:		#B4q0		1148869344:		$B4q0		d-		30.21		4.37		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24389.13		9:28:13		8:25:00		m		36.33		1139.58

		S1148869374:		#B4q0		1148869374:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.78		3.76		0		-24390.15		9:28:43		8:25:30		m		36.37		1140.67

		S1148869404:		#B4q0		1148869404:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24391.31		9:29:13		8:26:00		m		36.40		1141.77

		S1148869434:		#B4q0		1148869434:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24392.33		9:29:43		8:26:30		m		36.44		1142.86

		S1148869464:		#B4q0		1148869464:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24393.5		9:30:13		8:27:00		m		36.47		1143.95

		S1148869494:		#B4q0		1148869495:		$B4q0		d-		30.21		4.26		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24394.51		9:30:44		8:27:31		m		36.51		1145.06

		S1148869524:		#B4q0		1148869524:		$B4q0		d-		30.21		4.33		27.83		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24395.67		9:31:13		8:28:00		m		36.55		1146.11

		S1148869554:		#B4q0		1148869554:		$B4q0		d-		30.25		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24396.69		9:31:43		8:28:30		m		36.58		1147.20

		S1148869584:		#B4q0		1148869584:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24397.85		9:32:13		8:29:00		m		36.62		1148.29

		S1148869614:		#B4q0		1148869614:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24398.87		9:32:43		8:29:30		m		36.65		1149.38

		S1148869644:		#B4q0		1148869644:		$B4q0		d-		30.21		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24400.03		9:33:13		8:30:00		m		36.69		1150.47

		S1148869674:		#B4q0		1148869674:		$B4q0		d-		30.21		4.33		27.83		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24401.05		9:33:43		8:30:30		m		36.73		1151.55

		S1148869704:		#B4q0		1148869704:		$B4q0		d-		30.21		4.37		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24402.22		9:34:13		8:31:00		m		36.76		1152.65

		S1148869734:		#B4q0		1148869734:		$B4q0		d-		30.21		4.37		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24403.24		9:34:43		8:31:30		m		36.80		1153.75

		S1148869764:		#B4q0		1148869764:		$B4q0		d-		30.21		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24404.4		9:35:13		8:32:00		m		36.83		1154.84

		S1148869794:		#B4q0		1148869794:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24405.42		9:35:43		8:32:30		m		36.87		1155.93

		S1148869824:		#B4q0		1148869824:		$B4q0		d-		30.17		4.30		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24406.58		9:36:13		8:33:00		m		36.91		1157.01

		S1148869854:		#B4q0		1148869854:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76		0		-24407.59		9:36:43		8:33:30		m		36.94		1158.10

		S1148869884:		#B4q0		1148869884:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.75		3.76		3.76		3.77		3.76		0		-24408.75		9:37:13		8:34:00		m		36.98		1159.19

		S1148869914:		#B4q0		1148869914:		$B4q0		d-		30.17		4.41		27.92		3.78		3.78		3.78		3.75		3.76		3.76		3.77		3.76		0		-24409.77		9:37:43		8:34:30		m		37.01		1160.29

		S1148869944:		#B4q0		1148869944:		$B4q0		d-		30.21		4.33		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.76		0		-24410.93		9:38:13		8:35:00		m		37.05		1161.39

		S1148869974:		#B4q0		1148869974:		$B4q0		d-		30.21		4.30		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.76		0		-24411.95		9:38:43		8:35:30		m		37.09		1162.47

		S1148870004:		#B4q0		1148870004:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24413.11		9:39:13		8:36:00		m		37.12		1163.56

		S1148870034:		#B4q0		1148870034:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24414.13		9:39:43		8:36:30		m		37.16		1164.65

		S1148870064:		#B4q0		1148870064:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24415.29		9:40:13		8:37:00		m		37.20		1165.74

		S1148870094:		#B4q0		1148870094:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24416.31		9:40:43		8:37:30		m		37.23		1166.83

		S1148870124:		#B4q0		1148870124:		$B4q0		d-		30.17		4.30		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24417.47		9:41:13		8:38:00		m		37.27		1167.91

		S1148870154:		#B4q0		1148870154:		$B4q0		d-		30.21		4.33		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24418.49		9:41:43		8:38:30		m		37.30		1169.00

		S1148870184:		#B4q0		1148870184:		$B4q0		d-		30.17		4.30		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24419.66		9:42:13		8:39:00		m		37.34		1170.08

		S1148870214:		#B4q0		1148870214:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24420.67		9:42:43		8:39:30		m		37.38		1171.17

		S1148870244:		#B4q0		1148870244:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24421.84		9:43:13		8:40:00		m		37.41		1172.26

		S1148870274:		#B4q0		1148870274:		$B4q0		d-		30.21		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24422.86		9:43:43		8:40:30		m		37.45		1173.34

		S1148870304:		#B4q0		1148870304:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24424.01		9:44:13		8:41:00		m		37.48		1174.43

		S1148870334:		#B4q0		1148870334:		$B4q0		d-		30.14		4.30		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24425.03		9:44:43		8:41:30		m		37.52		1175.52

		S1148870364:		#B4q0		1148870364:		$B4q0		d-		30.17		4.33		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24426.2		9:45:13		8:42:00		m		37.56		1176.60

		S1148870394:		#B4q0		1148870394:		$B4q0		d-		30.17		4.33		27.83		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24427.21		9:45:43		8:42:30		m		37.59		1177.69

		S1148870424:		#B4q0		1148870424:		$B4q0		d-		30.17		4.33		27.92		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75		0		-24428.37		9:46:13		8:43:00		m		37.63		1178.78

		S1148870454:		#B4q0		1148870454:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75		0		-24429.39		9:46:43		8:43:30		m		37.66		1179.87

		S1148870484:		#B4q0		1148870484:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75		0		-24430.55		9:47:13		8:44:00		m		37.70		1180.96

		S1148870514:		#B4q0		1148870514:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75		0		-24431.57		9:47:43		8:44:30		m		37.74		1182.05

		S1148870544:		#B4q0		1148870544:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75		0		-24432.72		9:48:13		8:45:00		m		37.77		1183.13

		S1148870574:		#B4q0		1148870574:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75		0		-24433.74		9:48:43		8:45:30		m		37.81		1184.22

		S1148870604:		#B4q0		1148870604:		$B4q0		d-		30.17		4.30		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75		0		-24434.9		9:49:13		8:46:00		m		37.84		1185.31

		S1148870634:		#B4q0		1148870634:		$B4q0		d-		30.14		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75		0		-24435.92		9:49:43		8:46:30		m		37.88		1186.39

		S1148870664:		#B4q0		1148870664:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75		0		-24437.08		9:50:13		8:47:00		m		37.92		1187.48

		S1148870694:		#B4q0		1148870694:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24438.1		9:50:43		8:47:30		m		37.95		1188.57

		S1148870724:		#B4q0		1148870724:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75		0		-24439.26		9:51:13		8:48:00		m		37.99		1189.66

		S1148870754:		#B4q0		1148870754:		$B4q0		d-		30.14		4.33		27.83		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24440.27		9:51:43		8:48:30		m		38.02		1190.75

		S1148870784:		#B4q0		1148870784:		$B4q0		d-		30.14		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75		0		-24441.43		9:52:13		8:49:00		m		38.06		1191.83

		S1148870814:		#B4q0		1148870814:		$B4q0		d-		30.17		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24442.45		9:52:43		8:49:30		m		38.10		1192.92

		S1148870844:		#B4q0		1148870844:		$B4q0		d-		30.17		4.30		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24443.61		9:53:13		8:50:00		m		38.13		1194.01

		S1148870874:		#B4q0		1148870874:		$B4q0		d-		30.17		4.30		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24444.62		9:53:43		8:50:30		m		38.17		1195.09

		S1148870904:		#B4q0		1148870904:		$B4q0		d-		30.14		4.33		27.92		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24445.78		9:54:13		8:51:00		m		38.20		1196.17

		S1148870934:		#B4q0		1148870934:		$B4q0		d-		30.17		4.33		27.83		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24446.79		9:54:43		8:51:30		m		38.24		1197.26

		S1148870964:		#B4q0		1148870964:		$B4q0		d-		30.17		4.33		27.83		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24447.95		9:55:13		8:52:00		m		38.28		1198.35

		S1148870994:		#B4q0		1148870994:		$B4q0		d-		30.14		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24448.97		9:55:43		8:52:30		m		38.31		1199.44

		S1148871024:		#B4q0		1148871024:		$B4q0		d-		30.17		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24450.13		9:56:13		8:53:00		m		38.35		1200.52

		S1148871054:		#B4q0		1148871054:		$B4q0		d-		30.14		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24451.15		9:56:43		8:53:30		m		38.38		1201.61

		S1148871084:		#B4q0		1148871084:		$B4q0		d-		30.17		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24452.31		9:57:13		8:54:00		m		38.42		1202.70

		S1148871114:		#B4q0		1148871114:		$B4q0		d-		30.14		4.30		27.92		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24453.32		9:57:43		8:54:30		m		38.46		1203.79

		S1148871144:		#B4q0		1148871144:		$B4q0		d-		30.17		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24454.49		9:58:13		8:55:00		m		38.49		1204.87

		S1148871174:		#B4q0		1148871174:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24455.5		9:58:43		8:55:30		m		38.53		1205.96

		S1148871204:		#B4q0		1148871204:		$B4q0		d-		30.14		4.30		27.92		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24456.66		9:59:13		8:56:00		m		38.56		1207.04

		S1148871234:		#B4q0		1148871234:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24457.68		9:59:43		8:56:30		m		38.60		1208.13

		S1148871264:		#B4q0		1148871264:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24458.84		10:00:13		8:57:00		m		38.64		1209.21

		S1148871294:		#B4q0		1148871294:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24459.85		10:00:43		8:57:30		m		38.67		1210.30

		S1148871324:		#B4q0		1148871324:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24461.01		10:01:13		8:58:00		m		38.71		1211.39

		S1148871354:		#B4q0		1148871354:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24462.03		10:01:43		8:58:30		m		38.74		1212.48

		S1148871384:		#B4q0		1148871384:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24463.19		10:02:13		8:59:00		m		38.78		1213.56

		S1148871414:		#B4q0		1148871414:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24464.2		10:02:43		8:59:30		m		38.82		1214.65

		S1148871444:		#B4q0		1148871444:		$B4q0		d-		30.10		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75		0		-24465.36		10:03:13		9:00:00		m		38.85		1215.74

		S1148871474:		#B4q0		1148871474:		$B4q0		d-		30.14		4.37		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24466.38		10:03:43		9:00:30		m		38.89		1216.83

		S1148871504:		#B4q0		1148871504:		$B4q0		d-		30.14		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24467.54		10:04:13		9:01:00		m		38.93		1217.92

		S1148871534:		#B4q0		1148871534:		$B4q0		d-		30.14		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24468.55		10:04:43		9:01:30		m		38.96		1219.01

		S1148871564:		#B4q0		1148871564:		$B4q0		d-		30.14		4.26		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24469.71		10:05:13		9:02:00		m		39.00		1220.09

		S1148871594:		#B4q0		1148871594:		$B4q0		d-		30.10		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24470.73		10:05:43		9:02:30		m		39.03		1221.17

		S1148871624:		#B4q0		1148871624:		$B4q0		d-		30.14		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24471.89		10:06:13		9:03:00		m		39.07		1222.25

		S1148871654:		#B4q0		1148871654:		$B4q0		d-		30.14		4.30		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24472.9		10:06:43		9:03:30		m		39.11		1223.34

		S1148871684:		#B4q0		1148871684:		$B4q0		d-		30.14		4.30		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24474.06		10:07:13		9:04:00		m		39.14		1224.42

		S1148871714:		#B4q0		1148871714:		$B4q0		d-		30.10		4.33		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24475.08		10:07:43		9:04:30		m		39.18		1225.50

		S1148871744:		#B4q0		1148871744:		$B4q0		d-		30.10		4.37		27.83		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24476.24		10:08:13		9:05:00		m		39.21		1226.59

		S1148871774:		#B4q0		1148871774:		$B4q0		d-		30.10		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24477.25		10:08:43		9:05:30		m		39.25		1227.68

		S1148871804:		#B4q0		1148871804:		$B4q0		d-		30.10		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24478.41		10:09:13		9:06:00		m		39.29		1228.77

		S1148871834:		#B4q0		1148871834:		$B4q0		d-		30.10		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24479.42		10:09:43		9:06:30		m		39.32		1229.85

		S1148871864:		#B4q0		1148871864:		$B4q0		d-		30.10		4.33		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24480.59		10:10:13		9:07:00		m		39.36		1230.94

		S1148871894:		#B4q0		1148871894:		$B4q0		d-		30.10		4.30		27.92		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75		0		-24481.6		10:10:43		9:07:30		m		39.39		1232.02

		S1148871924:		#B4q0		1148871924:		$B4q0		d-		30.14		4.33		27.92		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75		0		-24482.76		10:11:13		9:08:00		m		39.43		1233.11

		S1148871954:		#B4q0		1148871954:		$B4q0		d-		30.10		4.30		27.92		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75		0		-24483.77		10:11:43		9:08:30		m		39.47		1234.19

		S1148871984:		#B4q0		1148871984:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75		0		-24484.93		10:12:13		9:09:00		m		39.50		1235.27

		S1148872014:		#B4q0		1148872014:		$B4q0		d-		30.14		4.33		27.83		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75		0		-24485.94		10:12:43		9:09:30		m		39.54		1236.36

		S1148872044:		#B4q0		1148872044:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75		0		-24487.1		10:13:13		9:10:00		m		39.57		1237.44

		S1148872074:		#B4q0		1148872074:		$B4q0		d-		30.10		4.33		27.83		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75		0		-24488.12		10:13:43		9:10:30		m		39.61		1238.53

		S1148872104:		#B4q0		1148872104:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.75		0		-24489.28		10:14:13		9:11:00		m		39.65		1239.62

		S1148872134:		#B4q0		1148872134:		$B4q0		d-		30.10		4.33		27.83		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24490.29		10:14:43		9:11:30		m		39.68		1240.70

		S1148872164:		#B4q0		1148872164:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24491.45		10:15:13		9:12:00		m		39.72		1241.79

		S1148872194:		#B4q0		1148872194:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24492.47		10:15:43		9:12:30		m		39.75		1242.88

		S1148872224:		#B4q0		1148872224:		$B4q0		d-		30.10		4.30		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24493.63		10:16:13		9:13:00		m		39.79		1243.96

		S1148872254:		#B4q0		1148872254:		$B4q0		d-		30.10		4.33		27.83		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24494.64		10:16:43		9:13:30		m		39.83		1245.04

		S1148872284:		#B4q0		1148872284:		$B4q0		d-		30.10		4.33		27.83		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24495.8		10:17:13		9:14:00		m		39.86		1246.13

		S1148872314:		#B4q0		1148872314:		$B4q0		d-		30.10		4.30		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24496.81		10:17:43		9:14:30		m		39.90		1247.21

		S1148872344:		#B4q0		1148872344:		$B4q0		d-		30.10		4.33		27.92		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24497.97		10:18:13		9:15:00		m		39.93		1248.29

		S1148872374:		#B4q0		1148872374:		$B4q0		d-		30.10		4.33		27.83		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24498.98		10:18:43		9:15:30		m		39.97		1249.38

		S1148872404:		#B4q0		1148872404:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24500.14		10:19:13		9:16:00		m		40.01		1250.46

		S1148872434:		#B4q0		1148872434:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24501.16		10:19:43		9:16:30		m		40.04		1251.55

		S1148872464:		#B4q0		1148872464:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24502.31		10:20:13		9:17:00		m		40.08		1252.64

		S1148872494:		#B4q0		1148872494:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24503.33		10:20:43		9:17:30		m		40.11		1253.72

		S1148872524:		#B4q0		1148872524:		$B4q0		d-		30.10		4.30		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24504.49		10:21:13		9:18:00		m		40.15		1254.80

		S1148872554:		#B4q0		1148872554:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24505.5		10:21:43		9:18:30		m		40.19		1255.89

		S1148872584:		#B4q0		1148872584:		$B4q0		d-		30.10		4.33		27.83		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24506.66		10:22:13		9:19:00		m		40.22		1256.97

		S1148872614:		#B4q0		1148872614:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24507.67		10:22:43		9:19:30		m		40.26		1258.06

		S1148872644:		#B4q0		1148872644:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24508.83		10:23:13		9:20:00		m		40.29		1259.14

		S1148872674:		#B4q0		1148872674:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24509.84		10:23:43		9:20:30		m		40.33		1260.23

		S1148872704:		#B4q0		1148872704:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24511		10:24:13		9:21:00		m		40.37		1261.32

		S1148872734:		#B4q0		1148872734:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24512.01		10:24:43		9:21:30		m		40.40		1262.40

		S1148872764:		#B4q0		1148872764:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24513.17		10:25:13		9:22:00		m		40.44		1263.49

		S1148872794:		#B4q0		1148872794:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24514.18		10:25:43		9:22:30		m		40.48		1264.57

		S1148872824:		#B4q0		1148872824:		$B4q0		d-		30.10		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24515.34		10:26:13		9:23:00		m		40.51		1265.66

		S1148872854:		#B4q0		1148872854:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24516.35		10:26:43		9:23:30		m		40.55		1266.75

		S1148872884:		#B4q0		1148872884:		$B4q0		d-		30.10		4.30		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24517.5		10:27:13		9:24:00		m		40.58		1267.83

		S1148872914:		#B4q0		1148872914:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24518.52		10:27:43		9:24:30		m		40.62		1268.91

		S1148872944:		#B4q0		1148872944:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24519.68		10:28:13		9:25:00		m		40.66		1269.99

		S1148872974:		#B4q0		1148872974:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74		0		-24520.69		10:28:43		9:25:30		m		40.69		1271.08

		S1148873004:		#B4q0		1148873004:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24521.85		10:29:13		9:26:00		m		40.73		1272.16

		S1148873034:		#B4q0		1148873034:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24522.86		10:29:43		9:26:30		m		40.76		1273.25

		S1148873064:		#B4q0		1148873064:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24524.02		10:30:13		9:27:00		m		40.80		1274.33

		S1148873094:		#B4q0		1148873094:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24525.03		10:30:43		9:27:30		m		40.84		1275.42

		S1148873124:		#B4q0		1148873124:		$B4q0		d-		30.06		4.30		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24526.18		10:31:13		9:28:00		m		40.87		1276.50

		S1148873154:		#B4q0		1148873154:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24527.2		10:31:43		9:28:30		m		40.91		1277.58

		S1148873184:		#B4q0		1148873184:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24528.35		10:32:13		9:29:00		m		40.94		1278.66

		S1148873214:		#B4q0		1148873214:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24529.36		10:32:43		9:29:30		m		40.98		1279.75

		S1148873244:		#B4q0		1148873244:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24530.52		10:33:13		9:30:00		m		41.02		1280.83

		S1148873274:		#B4q0		1148873274:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24531.53		10:33:43		9:30:30		m		41.05		1281.92

		S1148873304:		#B4q0		1148873304:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24532.68		10:34:13		9:31:00		m		41.09		1283.00

		S1148873334:		#B4q0		1148873334:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74		0		-24533.69		10:34:43		9:31:30		m		41.12		1284.08

		S1148873364:		#B4q0		1148873364:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.74		3.73		3.75		3.75		3.74		0		-24534.84		10:35:13		9:32:00		m		41.16		1285.17

		S1148873394:		#B4q0		1148873394:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74		0		-24535.85		10:35:43		9:32:30		m		41.20		1286.25

		S1148873424:		#B4q0		1148873424:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74		0		-24537.01		10:36:13		9:33:00		m		41.23		1287.33

		S1148873454:		#B4q0		1148873454:		$B4q0		d-		30.06		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74		0		-24538.02		10:36:43		9:33:30		m		41.27		1288.41

		S1148873484:		#B4q0		1148873484:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74		0		-24539.17		10:37:13		9:34:00		m		41.30		1289.49

		S1148873514:		#B4q0		1148873514:		$B4q0		d-		30.06		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24540.18		10:37:43		9:34:30		m		41.34		1290.58

		S1148873544:		#B4q0		1148873544:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24541.34		10:38:13		9:35:00		m		41.38		1291.66

		S1148873574:		#B4q0		1148873574:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24542.35		10:38:43		9:35:30		m		41.41		1292.75

		S1148873604:		#B4q0		1148873604:		$B4q0		d-		30.06		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24543.51		10:39:13		9:36:00		m		41.45		1293.83

		S1148873634:		#B4q0		1148873634:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24544.52		10:39:43		9:36:30		m		41.48		1294.91

		S1148873664:		#B4q0		1148873664:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24545.68		10:40:13		9:37:00		m		41.52		1295.99

		S1148873694:		#B4q0		1148873694:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73		0		-24546.69		10:40:43		9:37:30		m		41.56		1297.07

		S1148873724:		#B4q0		1148873724:		$B4q0		d-		30.02		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24547.84		10:41:13		9:38:00		m		41.59		1298.15

		S1148873754:		#B4q0		1148873754:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24548.85		10:41:43		9:38:30		m		41.63		1299.23

		S1148873784:		#B4q0		1148873784:		$B4q0		d-		30.02		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24550.01		10:42:13		9:39:00		m		41.66		1300.31

		S1148873814:		#B4q0		1148873814:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24551.02		10:42:43		9:39:30		m		41.70		1301.39

		S1148873844:		#B4q0		1148873844:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24552.18		10:43:13		9:40:00		m		41.74		1302.47

		S1148873874:		#B4q0		1148873874:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24553.19		10:43:43		9:40:30		m		41.77		1303.56

		S1148873904:		#B4q0		1148873904:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24554.35		10:44:13		9:41:00		m		41.81		1304.64

		S1148873934:		#B4q0		1148873934:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24555.36		10:44:43		9:41:30		m		41.84		1305.72

		S1148873964:		#B4q0		1148873964:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24556.52		10:45:13		9:42:00		m		41.88		1306.81

		S1148873994:		#B4q0		1148873994:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24557.53		10:45:43		9:42:30		m		41.92		1307.89

		S1148874024:		#B4q0		1148874024:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24558.68		10:46:13		9:43:00		m		41.95		1308.97

		S1148874054:		#B4q0		1148874054:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24559.69		10:46:43		9:43:30		m		41.99		1310.06

		S1148874084:		#B4q0		1148874084:		$B4q0		d-		30.02		4.37		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24560.85		10:47:13		9:44:00		m		42.03		1311.15

		S1148874114:		#B4q0		1148874114:		$B4q0		d-		30.02		4.33		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24561.86		10:47:43		9:44:30		m		42.06		1312.23

		S1148874144:		#B4q0		1148874144:		$B4q0		d-		30.02		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24563.01		10:48:13		9:45:00		m		42.10		1313.31

		S1148874174:		#B4q0		1148874174:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24564.02		10:48:43		9:45:30		m		42.13		1314.39

		S1148874204:		#B4q0		1148874204:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24565.17		10:49:13		9:46:00		m		42.17		1315.47

		S1148874234:		#B4q0		1148874234:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24566.18		10:49:43		9:46:30		m		42.21		1316.56

		S1148874264:		#B4q0		1148874264:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24567.34		10:50:13		9:47:00		m		42.24		1317.64

		S1148874294:		#B4q0		1148874294:		$B4q0		d-		30.02		4.30		27.92		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73		0		-24568.35		10:50:43		9:47:30		m		42.28		1318.72

		S1148874324:		#B4q0		1148874324:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24569.5		10:51:13		9:48:00		m		42.31		1319.80

		S1148874354:		#B4q0		1148874354:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73		0		-24570.51		10:51:43		9:48:30		m		42.35		1320.88

		S1148874384:		#B4q0		1148874384:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24571.67		10:52:13		9:49:00		m		42.39		1321.96

		S1148874414:		#B4q0		1148874414:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24572.68		10:52:43		9:49:30		m		42.42		1323.05

		S1148874444:		#B4q0		1148874444:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24573.84		10:53:13		9:50:00		m		42.46		1324.13

		S1148874474:		#B4q0		1148874474:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24574.84		10:53:43		9:50:30		m		42.49		1325.21

		S1148874504:		#B4q0		1148874504:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24576		10:54:13		9:51:00		m		42.53		1326.29

		S1148874534:		#B4q0		1148874534:		$B4q0		d-		30.02		4.26		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24577.01		10:54:43		9:51:30		m		42.57		1327.37

		S1148874564:		#B4q0		1148874564:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24578.17		10:55:13		9:52:00		m		42.60		1328.44

		S1148874594:		#B4q0		1148874594:		$B4q0		d-		30.02		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24579.18		10:55:43		9:52:30		m		42.64		1329.52

		S1148874624:		#B4q0		1148874624:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24580.33		10:56:13		9:53:00		m		42.67		1330.61

		S1148874654:		#B4q0		1148874654:		$B4q0		d-		29.98		4.33		27.92		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24581.34		10:56:43		9:53:30		m		42.71		1331.69

		S1148874684:		#B4q0		1148874684:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24582.5		10:57:13		9:54:00		m		42.75		1332.77

		S1148874714:		#B4q0		1148874714:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24583.51		10:57:43		9:54:30		m		42.78		1333.85

		S1148874744:		#B4q0		1148874744:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24584.66		10:58:13		9:55:00		m		42.82		1334.93

		S1148874774:		#B4q0		1148874774:		$B4q0		d-		29.98		4.30		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24585.67		10:58:43		9:55:30		m		42.85		1336.01

		S1148874804:		#B4q0		1148874804:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24586.82		10:59:13		9:56:00		m		42.89		1337.09

		S1148874834:		#B4q0		1148874834:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24587.83		10:59:43		9:56:30		m		42.93		1338.17

		S1148874864:		#B4q0		1148874864:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24588.99		11:00:13		9:57:00		m		42.96		1339.25

		S1148874894:		#B4q0		1148874894:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24589.99		11:00:43		9:57:30		m		43.00		1340.33

		S1148874924:		#B4q0		1148874924:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24591.15		11:01:13		9:58:00		m		43.03		1341.42

		S1148874954:		#B4q0		1148874954:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24592.16		11:01:43		9:58:30		m		43.07		1342.50

		S1148874984:		#B4q0		1148874984:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24593.31		11:02:13		9:59:00		m		43.11		1343.58

		S1148875014:		#B4q0		1148875014:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24594.32		11:02:43		9:59:30		m		43.14		1344.66

		S1148875044:		#B4q0		1148875044:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24595.47		11:03:13		10:00:00		m		43.18		1345.74

		S1148875074:		#B4q0		1148875074:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24596.48		11:03:43		10:00:30		m		43.21		1346.82

		S1148875104:		#B4q0		1148875104:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73		0		-24597.64		11:04:13		10:01:00		m		43.25		1347.91

		S1148875134:		#B4q0		1148875134:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73		0		-24598.64		11:04:43		10:01:30		m		43.29		1348.98

		S1148875164:		#B4q0		1148875164:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73		0		-24599.8		11:05:13		10:02:00		m		43.32		1350.06

		S1148875194:		#B4q0		1148875194:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73		0		-24600.81		11:05:43		10:02:30		m		43.36		1351.14

		S1148875224:		#B4q0		1148875224:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.73		0		-24601.96		11:06:13		10:03:00		m		43.39		1352.22

		S1148875254:		#B4q0		1148875254:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.73		0		-24602.97		11:06:43		10:03:30		m		43.43		1353.30

		S1148875284:		#B4q0		1148875284:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.72		0		-24604.12		11:07:13		10:04:00		m		43.47		1354.38

		S1148875314:		#B4q0		1148875314:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24605.13		11:07:43		10:04:30		m		43.50		1355.46

		S1148875344:		#B4q0		1148875344:		$B4q0		d-		29.95		4.37		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.72		0		-24606.28		11:08:13		10:05:00		m		43.54		1356.54

		S1148875374:		#B4q0		1148875374:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24607.29		11:08:43		10:05:30		m		43.58		1357.63

		S1148875404:		#B4q0		1148875404:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24608.45		11:09:13		10:06:00		m		43.61		1358.71

		S1148875434:		#B4q0		1148875434:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24609.45		11:09:43		10:06:30		m		43.65		1359.79

		S1148875464:		#B4q0		1148875464:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24610.6		11:10:13		10:07:00		m		43.68		1360.87

		S1148875494:		#B4q0		1148875494:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72		0		-24611.61		11:10:43		10:07:30		m		43.72		1361.95

		S1148875524:		#B4q0		1148875524:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24612.76		11:11:13		10:08:00		m		43.76		1363.03

		S1148875554:		#B4q0		1148875554:		$B4q0		d-		29.98		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24613.77		11:11:43		10:08:30		m		43.79		1364.11

		S1148875584:		#B4q0		1148875584:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24614.93		11:12:13		10:09:00		m		43.83		1365.20

		S1148875614:		#B4q0		1148875614:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24615.93		11:12:43		10:09:30		m		43.86		1366.27

		S1148875644:		#B4q0		1148875644:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24617.09		11:13:13		10:10:00		m		43.90		1367.35

		S1148875674:		#B4q0		1148875674:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24618.1		11:13:43		10:10:30		m		43.94		1368.43

		S1148875704:		#B4q0		1148875704:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24619.25		11:14:13		10:11:00		m		43.97		1369.51

		S1148875734:		#B4q0		1148875734:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24620.26		11:14:43		10:11:30		m		44.01		1370.59

		S1148875764:		#B4q0		1148875764:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24621.41		11:15:13		10:12:00		m		44.04		1371.67

		S1148875794:		#B4q0		1148875794:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24622.42		11:15:43		10:12:30		m		44.08		1372.75

		S1148875824:		#B4q0		1148875824:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24623.57		11:16:13		10:13:00		m		44.12		1373.83

		S1148875854:		#B4q0		1148875854:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24624.58		11:16:43		10:13:30		m		44.15		1374.91

		S1148875884:		#B4q0		1148875884:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24625.73		11:17:13		10:14:00		m		44.19		1375.99

		S1148875914:		#B4q0		1148875914:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24626.74		11:17:43		10:14:30		m		44.22		1377.07

		S1148875944:		#B4q0		1148875944:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24627.89		11:18:13		10:15:00		m		44.26		1378.15

		S1148875974:		#B4q0		1148875974:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24628.9		11:18:43		10:15:30		m		44.30		1379.23

		S1148876004:		#B4q0		1148876004:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24630.05		11:19:13		10:16:00		m		44.33		1380.31

		S1148876034:		#B4q0		1148876034:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24631.06		11:19:43		10:16:30		m		44.37		1381.39

		S1148876064:		#B4q0		1148876064:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24632.21		11:20:13		10:17:00		m		44.40		1382.46

		S1148876094:		#B4q0		1148876094:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24633.22		11:20:43		10:17:30		m		44.44		1383.54

		S1148876124:		#B4q0		1148876124:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24634.37		11:21:13		10:18:00		m		44.48		1384.62

		S1148876154:		#B4q0		1148876154:		$B4q0		d-		29.95		4.30		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24635.38		11:21:43		10:18:30		m		44.51		1385.69

		S1148876184:		#B4q0		1148876184:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24636.53		11:22:13		10:19:00		m		44.55		1386.77

		S1148876214:		#B4q0		1148876214:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24637.54		11:22:43		10:19:30		m		44.58		1387.85

		S1148876244:		#B4q0		1148876244:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72		0		-24638.69		11:23:13		10:20:00		m		44.62		1388.93

		S1148876274:		#B4q0		1148876274:		$B4q0		d-		29.91		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.72		0		-24639.69		11:23:43		10:20:30		m		44.66		1390.01

		S1148876304:		#B4q0		1148876304:		$B4q0		d-		29.91		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.72		0		-24640.84		11:24:13		10:21:00		m		44.69		1391.09

		S1148876334:		#B4q0		1148876334:		$B4q0		d-		29.95		4.37		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24641.85		11:24:43		10:21:30		m		44.73		1392.18

		S1148876364:		#B4q0		1148876364:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24643.01		11:25:13		10:22:00		m		44.77		1393.26

		S1148876394:		#B4q0		1148876394:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24644.01		11:25:43		10:22:30		m		44.80		1394.34

		S1148876424:		#B4q0		1148876424:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24645.16		11:26:13		10:23:00		m		44.84		1395.42

		S1148876454:		#B4q0		1148876454:		$B4q0		d-		29.91		4.30		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24646.17		11:26:43		10:23:30		m		44.87		1396.50

		S1148876484:		#B4q0		1148876484:		$B4q0		d-		29.91		4.33		28.02		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24647.32		11:27:13		10:24:00		m		44.91		1397.58

		S1148876514:		#B4q0		1148876514:		$B4q0		d-		29.95		4.33		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24648.33		11:27:43		10:24:30		m		44.95		1398.66

		S1148876544:		#B4q0		1148876544:		$B4q0		d-		29.91		4.37		27.92		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71		0		-24649.48		11:28:13		10:25:00		m		44.98		1399.74

		S1148876574:		#B4q0		1148876574:		$B4q0		d-		29.87		4.37		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24650.48		11:28:43		10:25:30		m		45.02		1400.83

		S1148876604:		#B4q0		1148876604:		$B4q0		d-		29.91		4.33		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24651.63		11:29:13		10:26:00		m		45.05		1401.91

		S1148876634:		#B4q0		1148876634:		$B4q0		d-		29.87		4.33		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24652.64		11:29:43		10:26:30		m		45.09		1402.99

		S1148876664:		#B4q0		1148876664:		$B4q0		d-		29.87		4.33		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24653.79		11:30:13		10:27:00		m		45.13		1404.07

		S1148876694:		#B4q0		1148876694:		$B4q0		d-		29.91		4.26		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24654.8		11:30:43		10:27:30		m		45.16		1405.14

		S1148876724:		#B4q0		1148876724:		$B4q0		d-		29.87		4.30		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24655.95		11:31:13		10:28:00		m		45.20		1406.21

		S1148876754:		#B4q0		1148876754:		$B4q0		d-		29.87		4.30		27.92		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71		0		-24656.96		11:31:43		10:28:30		m		45.23		1407.28

		S1148876784:		#B4q0		1148876784:		$B4q0		d-		29.91		4.30		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24658.11		11:32:13		10:29:00		m		45.27		1408.35

		S1148876814:		#B4q0		1148876814:		$B4q0		d-		29.91		4.33		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24659.12		11:32:43		10:29:30		m		45.31		1409.42

		S1148876844:		#B4q0		1148876844:		$B4q0		d-		29.87		4.33		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24660.27		11:33:13		10:30:00		m		45.34		1410.50

		S1148876874:		#B4q0		1148876874:		$B4q0		d-		29.91		4.33		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24661.27		11:33:43		10:30:30		m		45.38		1411.58

		S1148876904:		#B4q0		1148876904:		$B4q0		d-		29.91		4.33		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24662.43		11:34:13		10:31:00		m		45.41		1412.66

		S1148876934:		#B4q0		1148876934:		$B4q0		d-		29.87		4.33		28.02		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24663.43		11:34:43		10:31:30		m		45.45		1413.74

		S1148876964:		#B4q0		1148876964:		$B4q0		d-		29.87		4.33		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24664.59		11:35:13		10:32:00		m		45.49		1414.81

		S1148876994:		#B4q0		1148876994:		$B4q0		d-		29.87		4.30		27.92		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24665.59		11:35:43		10:32:30		m		45.52		1415.89

		S1148877024:		#B4q0		1148877024:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24666.74		11:36:13		10:33:00		m		45.56		1416.96

		S1148877054:		#B4q0		1148877054:		$B4q0		d-		29.91		4.26		27.92		3.74		3.74		3.74		3.71		3.71		3.73		3.73		3.71		0		-24667.74		11:36:43		10:33:30		m		45.59		1418.03

		S1148877084:		#B4q0		1148877084:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24668.89		11:37:13		10:34:00		m		45.63		1419.10

		S1148877114:		#B4q0		1148877114:		$B4q0		d-		29.87		4.30		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24669.9		11:37:43		10:34:30		m		45.67		1420.18

		S1148877144:		#B4q0		1148877144:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24671.05		11:38:13		10:35:00		m		45.70		1421.25

		S1148877174:		#B4q0		1148877174:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24672.06		11:38:43		10:35:30		m		45.74		1422.33

		S1148877204:		#B4q0		1148877204:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24673.21		11:39:13		10:36:00		m		45.77		1423.41

		S1148877234:		#B4q0		1148877234:		$B4q0		d-		29.87		4.30		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24674.21		11:39:43		10:36:30		m		45.81		1424.48

		S1148877264:		#B4q0		1148877264:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24675.37		11:40:13		10:37:00		m		45.85		1425.55

		S1148877294:		#B4q0		1148877294:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24676.37		11:40:43		10:37:30		m		45.88		1426.63

		S1148877324:		#B4q0		1148877324:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24677.52		11:41:13		10:38:00		m		45.92		1427.71

		S1148877354:		#B4q0		1148877354:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24678.53		11:41:43		10:38:30		m		45.95		1428.79

		S1148877384:		#B4q0		1148877384:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24679.67		11:42:13		10:39:00		m		45.99		1429.86

		S1148877414:		#B4q0		1148877414:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24680.68		11:42:43		10:39:30		m		46.03		1430.94

		S1148877444:		#B4q0		1148877444:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24681.83		11:43:13		10:40:00		m		46.06		1432.02

		S1148877474:		#B4q0		1148877474:		$B4q0		d-		29.87		4.30		28.02		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24682.83		11:43:43		10:40:30		m		46.10		1433.09

		S1148877504:		#B4q0		1148877504:		$B4q0		d-		29.87		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24683.98		11:44:13		10:41:00		m		46.13		1434.17

		S1148877534:		#B4q0		1148877534:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24684.99		11:44:43		10:41:30		m		46.17		1435.24

		S1148877564:		#B4q0		1148877564:		$B4q0		d-		29.87		4.33		28.02		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24686.14		11:45:13		10:42:00		m		46.21		1436.32

		S1148877594:		#B4q0		1148877594:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24687.15		11:45:43		10:42:30		m		46.24		1437.40

		S1148877624:		#B4q0		1148877624:		$B4q0		d-		29.87		4.30		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24688.3		11:46:13		10:43:00		m		46.28		1438.47

		S1148877654:		#B4q0		1148877654:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24689.3		11:46:43		10:43:30		m		46.31		1439.55

		S1148877684:		#B4q0		1148877684:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24690.45		11:47:13		10:44:00		m		46.35		1440.62

		S1148877714:		#B4q0		1148877714:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24691.46		11:47:43		10:44:30		m		46.39		1441.70

		S1148877744:		#B4q0		1148877744:		$B4q0		d-		29.83		4.30		27.92		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71		0		-24692.61		11:48:13		10:45:00		m		46.42		1442.77

		S1148877774:		#B4q0		1148877774:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.71		0		-24693.61		11:48:43		10:45:30		m		46.46		1443.84

		S1148877804:		#B4q0		1148877804:		$B4q0		d-		29.83		4.37		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.71		0		-24694.76		11:49:13		10:46:00		m		46.49		1444.93

		S1148877834:		#B4q0		1148877834:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.71		0		-24695.77		11:49:43		10:46:30		m		46.53		1446.01

		S1148877864:		#B4q0		1148877864:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24696.91		11:50:13		10:47:00		m		46.57		1447.08

		S1148877894:		#B4q0		1148877894:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24697.91		11:50:43		10:47:30		m		46.60		1448.16

		S1148877924:		#B4q0		1148877924:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24699.06		11:51:13		10:48:00		m		46.64		1449.24

		S1148877954:		#B4q0		1148877954:		$B4q0		d-		29.83		4.33		27.92		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24700.07		11:51:43		10:48:30		m		46.68		1450.31

		S1148877984:		#B4q0		1148877984:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24701.21		11:52:13		10:49:00		m		46.71		1451.39

		S1148878014:		#B4q0		1148878014:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24702.22		11:52:43		10:49:30		m		46.75		1452.46

		S1148878044:		#B4q0		1148878044:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24703.37		11:53:13		10:50:00		m		46.78		1453.54

		S1148878074:		#B4q0		1148878074:		$B4q0		d-		29.83		4.33		28.02		3.74		3.74		3.74		3.71		3.70		3.72		3.73		3.70		0		-24704.37		11:53:43		10:50:30		m		46.82		1454.62

		S1148878104:		#B4q0		1148878104:		$B4q0		d-		29.83		4.37		27.92		3.74		3.73		3.74		3.71		3.70		3.72		3.73		3.70		0		-24705.52		11:54:13		10:51:00		m		46.86		1455.70

		S1148878134:		#B4q0		1148878134:		$B4q0		d-		29.83		4.37		28.02		3.74		3.73		3.74		3.71		3.70		3.72		3.73		3.70		0		-24706.52		11:54:43		10:51:30		m		46.89		1456.79

		S1148878164:		#B4q0		1148878164:		$B4q0		d-		29.83		4.33		27.92		3.74		3.73		3.74		3.71		3.70		3.72		3.73		3.70		0		-24707.67		11:55:13		10:52:00		m		46.93		1457.87

		S1148878194:		#B4q0		1148878194:		$B4q0		d-		29.83		4.33		28.02		3.74		3.73		3.74		3.71		3.70		3.72		3.73		3.70		0		-24708.67		11:55:43		10:52:30		m		46.96		1458.94

		S1148878224:		#B4q0		1148878224:		$B4q0		d-		29.83		4.33		27.92		3.74		3.73		3.74		3.71		3.70		3.72		3.73		3.70		0		-24709.82		11:56:13		10:53:00		m		47.00		1460.02

		S1148878254:		#B4q0		1148878254:		$B4q0		d-		29.80		4.30		27.92		3.74		3.73		3.74		3.71		3.70		3.71		3.73		3.70		0		-24710.83		11:56:43		10:53:30		m		47.04		1461.09

		S1148878284:		#B4q0		1148878284:		$B4q0		d-		29.80		4.30		28.02		3.74		3.73		3.73		3.71		3.70		3.71		3.73		3.70		0		-24711.97		11:57:13		10:54:00		m		47.07		1462.16

		S1148878314:		#B4q0		1148878314:		$B4q0		d-		29.83		4.30		28.02		3.74		3.73		3.73		3.71		3.70		3.71		3.73		3.70		0		-24712.98		11:57:43		10:54:30		m		47.11		1463.23

		S1148878344:		#B4q0		1148878344:		$B4q0		d-		29.83		4.33		28.02		3.74		3.73		3.73		3.71		3.70		3.71		3.73		3.70		0		-24714.13		11:58:13		10:55:00		m		47.14		1464.30

		S1148878374:		#B4q0		1148878374:		$B4q0		d-		29.80		4.33		28.02		3.74		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24715.13		11:58:43		10:55:30		m		47.18		1465.38

		S1148878404:		#B4q0		1148878404:		$B4q0		d-		29.80		4.33		28.02		3.74		3.73		3.73		3.71		3.70		3.71		3.73		3.70		0		-24716.28		11:59:13		10:56:00		m		47.22		1466.45

		S1148878434:		#B4q0		1148878434:		$B4q0		d-		29.83		4.33		28.02		3.74		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24717.28		11:59:43		10:56:30		m		47.25		1467.53

		S1148878464:		#B4q0		1148878464:		$B4q0		d-		29.80		4.30		27.92		3.74		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24718.43		12:00:13		10:57:00		m		47.29		1468.60

		S1148878494:		#B4q0		1148878494:		$B4q0		d-		29.80		4.33		28.02		3.74		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24719.43		12:00:43		10:57:30		m		47.32		1469.67

		S1148878524:		#B4q0		1148878524:		$B4q0		d-		29.80		4.33		28.02		3.74		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24720.58		12:01:13		10:58:00		m		47.36		1470.75

		S1148878554:		#B4q0		1148878554:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24721.58		12:01:43		10:58:30		m		47.40		1471.82

		S1148878584:		#B4q0		1148878584:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24722.73		12:02:13		10:59:00		m		47.43		1472.90

		S1148878614:		#B4q0		1148878614:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24723.73		12:02:43		10:59:30		m		47.47		1473.97

		S1148878644:		#B4q0		1148878644:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24724.88		12:03:13		11:00:00		m		47.50		1475.05

		S1148878674:		#B4q0		1148878674:		$B4q0		d-		29.80		4.30		27.92		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24725.89		12:03:43		11:00:30		m		47.54		1476.12

		S1148878704:		#B4q0		1148878704:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24727.03		12:04:13		11:01:00		m		47.58		1477.19

		S1148878734:		#B4q0		1148878734:		$B4q0		d-		29.80		4.30		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24728.04		12:04:43		11:01:30		m		47.61		1478.26

		S1148878764:		#B4q0		1148878764:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24729.19		12:05:13		11:02:00		m		47.65		1479.33

		S1148878794:		#B4q0		1148878794:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.70		3.71		3.73		3.70		0		-24730.19		12:05:43		11:02:30		m		47.68		1480.41

		S1148878824:		#B4q0		1148878824:		$B4q0		d-		29.80		4.30		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.73		3.70		0		-24731.34		12:06:13		11:03:00		m		47.72		1481.48

		S1148878854:		#B4q0		1148878854:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.73		3.70		0		-24732.34		12:06:43		11:03:30		m		47.76		1482.55

		S1148878884:		#B4q0		1148878884:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.73		3.70		0		-24733.49		12:07:13		11:04:00		m		47.79		1483.63

		S1148878914:		#B4q0		1148878914:		$B4q0		d-		29.80		4.37		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.73		3.70		0		-24734.49		12:07:43		11:04:30		m		47.83		1484.71

		S1148878944:		#B4q0		1148878944:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.70		0		-24735.64		12:08:13		11:05:00		m		47.87		1485.79

		S1148878974:		#B4q0		1148878974:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.70		0		-24736.64		12:08:43		11:05:30		m		47.90		1486.86

		S1148879004:		#B4q0		1148879004:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.70		0		-24737.79		12:09:13		11:06:00		m		47.94		1487.94

		S1148879034:		#B4q0		1148879034:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.70		0		-24738.79		12:09:43		11:06:30		m		47.97		1489.01

		S1148879064:		#B4q0		1148879064:		$B4q0		d-		29.80		4.37		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.70		0		-24739.94		12:10:13		11:07:00		m		48.01		1490.09

		S1148879094:		#B4q0		1148879094:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24740.95		12:10:43		11:07:30		m		48.05		1491.17

		S1148879124:		#B4q0		1148879124:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24742.09		12:11:13		11:08:00		m		48.08		1492.25

		S1148879154:		#B4q0		1148879154:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24743.1		12:11:43		11:08:30		m		48.12		1493.32

		S1148879184:		#B4q0		1148879184:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24744.25		12:12:13		11:09:00		m		48.15		1494.40

		S1148879214:		#B4q0		1148879214:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24745.25		12:12:43		11:09:30		m		48.19		1495.47

		S1148879244:		#B4q0		1148879244:		$B4q0		d-		29.76		4.30		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24746.4		12:13:13		11:10:00		m		48.23		1496.54

		S1148879274:		#B4q0		1148879274:		$B4q0		d-		29.80		4.30		27.92		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24747.4		12:13:43		11:10:30		m		48.26		1497.61

		S1148879304:		#B4q0		1148879304:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24748.55		12:14:13		11:11:00		m		48.30		1498.68

		S1148879334:		#B4q0		1148879334:		$B4q0		d-		29.76		4.37		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24749.55		12:14:43		11:11:30		m		48.33		1499.76

		S1148879364:		#B4q0		1148879364:		$B4q0		d-		29.80		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24750.7		12:15:13		11:12:00		m		48.37		1500.84

		S1148879394:		#B4q0		1148879394:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24751.7		12:15:43		11:12:30		m		48.41		1501.92

		S1148879424:		#B4q0		1148879424:		$B4q0		d-		29.80		4.30		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24752.84		12:16:13		11:13:00		m		48.44		1502.99

		S1148879454:		#B4q0		1148879454:		$B4q0		d-		29.80		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24753.84		12:16:43		11:13:30		m		48.48		1504.06

		S1148879484:		#B4q0		1148879484:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24754.99		12:17:13		11:14:00		m		48.51		1505.13

		S1148879514:		#B4q0		1148879514:		$B4q0		d-		29.76		4.30		28.02		3.73		3.73		3.73		3.70		3.69		3.71		3.72		3.69		0		-24755.99		12:17:43		11:14:30		m		48.55		1506.20

		S1148879544:		#B4q0		1148879544:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24757.14		12:18:13		11:15:00		m		48.59		1507.27

		S1148879574:		#B4q0		1148879574:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24758.14		12:18:43		11:15:30		m		48.62		1508.35

		S1148879604:		#B4q0		1148879604:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24759.28		12:19:13		11:16:00		m		48.66		1509.42

		S1148879634:		#B4q0		1148879634:		$B4q0		d-		29.76		4.30		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24760.28		12:19:43		11:16:30		m		48.69		1510.49

		S1148879664:		#B4q0		1148879664:		$B4q0		d-		29.76		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24761.43		12:20:13		11:17:00		m		48.73		1511.56

		S1148879694:		#B4q0		1148879694:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24762.43		12:20:43		11:17:30		m		48.77		1512.63

		S1148879724:		#B4q0		1148879724:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24763.58		12:21:13		11:18:00		m		48.80		1513.71

		S1148879754:		#B4q0		1148879754:		$B4q0		d-		29.72		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24764.58		12:21:43		11:18:30		m		48.84		1514.78

		S1148879784:		#B4q0		1148879784:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24765.73		12:22:13		11:19:00		m		48.87		1515.85

		S1148879814:		#B4q0		1148879814:		$B4q0		d-		29.72		4.30		27.92		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69		0		-24766.73		12:22:43		11:19:30		m		48.91		1516.92

		S1148879844:		#B4q0		1148879844:		$B4q0		d-		29.76		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24767.87		12:23:13		11:20:00		m		48.95		1517.99

		S1148879874:		#B4q0		1148879874:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24768.87		12:23:43		11:20:30		m		48.98		1519.07

		S1148879904:		#B4q0		1148879904:		$B4q0		d-		29.76		4.30		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24770.01		12:24:13		11:21:00		m		49.02		1520.14

		S1148879934:		#B4q0		1148879934:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24771.01		12:24:43		11:21:30		m		49.05		1521.21

		S1148879964:		#B4q0		1148879964:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24772.16		12:25:13		11:22:00		m		49.09		1522.28

		S1148879994:		#B4q0		1148879994:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24773.16		12:25:43		11:22:30		m		49.13		1523.35

		S1148880024:		#B4q0		1148880024:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.72		3.69		0		-24774.31		12:26:13		11:23:00		m		49.16		1524.42

		S1148880054:		#B4q0		1148880054:		$B4q0		d-		29.72		4.37		27.92		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24775.31		12:26:43		11:23:30		m		49.20		1525.50

		S1148880084:		#B4q0		1148880084:		$B4q0		d-		29.72		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24776.45		12:27:13		11:24:00		m		49.24		1526.58

		S1148880114:		#B4q0		1148880114:		$B4q0		d-		29.76		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24777.45		12:27:43		11:24:30		m		49.27		1527.65

		S1148880144:		#B4q0		1148880144:		$B4q0		d-		29.72		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24778.59		12:28:13		11:25:00		m		49.31		1528.72

		S1148880174:		#B4q0		1148880174:		$B4q0		d-		29.72		4.33		27.92		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24779.59		12:28:43		11:25:30		m		49.34		1529.80

		S1148880204:		#B4q0		1148880204:		$B4q0		d-		29.68		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24780.74		12:29:13		11:26:00		m		49.38		1530.87

		S1148880234:		#B4q0		1148880234:		$B4q0		d-		29.72		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24781.74		12:29:43		11:26:30		m		49.42		1531.94

		S1148880264:		#B4q0		1148880264:		$B4q0		d-		29.68		4.33		28.02		3.73		3.73		3.73		3.69		3.69		3.70		3.71		3.69		0		-24782.88		12:30:13		11:27:00		m		49.45		1533.01

		S1148880294:		#B4q0		1148880294:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.73		3.69		3.69		3.70		3.71		3.69		0		-24783.88		12:30:43		11:27:30		m		49.49		1534.08

		S1148880324:		#B4q0		1148880324:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.73		3.69		3.69		3.70		3.71		3.69		0		-24785.03		12:31:13		11:28:00		m		49.52		1535.15

		S1148880354:		#B4q0		1148880354:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.73		3.69		3.69		3.70		3.71		3.69		0		-24786.03		12:31:43		11:28:30		m		49.56		1536.23

		S1148880384:		#B4q0		1148880384:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24787.17		12:32:13		11:29:00		m		49.60		1537.30

		S1148880414:		#B4q0		1148880414:		$B4q0		d-		29.68		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24788.17		12:32:43		11:29:30		m		49.63		1538.37

		S1148880444:		#B4q0		1148880444:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24789.31		12:33:13		11:30:00		m		49.67		1539.44

		S1148880474:		#B4q0		1148880474:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24790.31		12:33:43		11:30:30		m		49.70		1540.52

		S1148880504:		#B4q0		1148880504:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24791.45		12:34:13		11:31:00		m		49.74		1541.59

		S1148880534:		#B4q0		1148880534:		$B4q0		d-		29.72		4.33		28.02		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24792.45		12:34:43		11:31:30		m		49.78		1542.66

		S1148880564:		#B4q0		1148880564:		$B4q0		d-		29.72		4.33		27.92		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24793.6		12:35:13		11:32:00		m		49.81		1543.73

		S1148880594:		#B4q0		1148880594:		$B4q0		d-		29.72		4.33		27.92		3.73		3.72		3.72		3.69		3.69		3.70		3.71		3.69		0		-24794.6		12:35:43		11:32:30		m		49.85		1544.80

		S1148880624:		#B4q0		1148880624:		$B4q0		d-		29.72		4.30		28.02		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24795.74		12:36:13		11:33:00		m		49.88		1545.87

		S1148880654:		#B4q0		1148880654:		$B4q0		d-		29.72		4.30		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24796.74		12:36:43		11:33:30		m		49.92		1546.94

		S1148880684:		#B4q0		1148880684:		$B4q0		d-		29.72		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24797.88		12:37:13		11:34:00		m		49.96		1548.01

		S1148880714:		#B4q0		1148880714:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24798.89		12:37:43		11:34:30		m		49.99		1549.08

		S1148880744:		#B4q0		1148880744:		$B4q0		d-		29.72		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24800.03		12:38:13		11:35:00		m		50.03		1550.15

		S1148880774:		#B4q0		1148880774:		$B4q0		d-		29.72		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24801.03		12:38:43		11:35:30		m		50.06		1551.22

		S1148880804:		#B4q0		1148880804:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24802.18		12:39:13		11:36:00		m		50.10		1552.29

		S1148880834:		#B4q0		1148880834:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24803.18		12:39:43		11:36:30		m		50.14		1553.37

		S1148880864:		#B4q0		1148880864:		$B4q0		d-		29.72		4.30		28.02		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24804.32		12:40:13		11:37:00		m		50.17		1554.43

		S1148880894:		#B4q0		1148880894:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24805.32		12:40:43		11:37:30		m		50.21		1555.50

		S1148880924:		#B4q0		1148880924:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24806.46		12:41:13		11:38:00		m		50.25		1556.57

		S1148880954:		#B4q0		1148880954:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69		0		-24807.46		12:41:43		11:38:30		m		50.28		1557.64

		S1148880984:		#B4q0		1148880984:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.70		3.71		3.69		0		-24808.6		12:42:13		11:39:00		m		50.32		1558.71

		S1148881014:		#B4q0		1148881014:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69		0		-24809.6		12:42:43		11:39:30		m		50.35		1559.79

		S1148881044:		#B4q0		1148881044:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69		0		-24810.74		12:43:13		11:40:00		m		50.39		1560.86

		S1148881074:		#B4q0		1148881074:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24811.74		12:43:43		11:40:30		m		50.43		1561.93

		S1148881104:		#B4q0		1148881104:		$B4q0		d-		29.64		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24812.89		12:44:13		11:41:00		m		50.46		1563.00

		S1148881134:		#B4q0		1148881134:		$B4q0		d-		29.68		4.30		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24813.88		12:44:43		11:41:30		m		50.50		1564.06

		S1148881164:		#B4q0		1148881164:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24815.03		12:45:13		11:42:00		m		50.53		1565.13

		S1148881194:		#B4q0		1148881194:		$B4q0		d-		29.68		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24816.03		12:45:43		11:42:30		m		50.57		1566.20

		S1148881224:		#B4q0		1148881224:		$B4q0		d-		29.64		4.33		28.02		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24817.16		12:46:13		11:43:00		m		50.61		1567.27

		S1148881254:		#B4q0		1148881254:		$B4q0		d-		29.68		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24818.16		12:46:43		11:43:30		m		50.64		1568.34

		S1148881284:		#B4q0		1148881284:		$B4q0		d-		29.64		4.44		27.92		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24819.31		12:47:13		11:44:00		m		50.68		1569.43

		S1148881314:		#B4q0		1148881314:		$B4q0		d-		29.64		4.33		27.92		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68		0		-24820.31		12:47:43		11:44:30		m		50.71		1570.51

		S1148881344:		#B4q0		1148881344:		$B4q0		d-		29.64		4.33		28.02		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68		0		-24821.45		12:48:13		11:45:00		m		50.75		1571.58

		S1148881374:		#B4q0		1148881374:		$B4q0		d-		29.64		4.33		27.92		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68		0		-24822.45		12:48:43		11:45:30		m		50.79		1572.65

		S1148881404:		#B4q0		1148881404:		$B4q0		d-		29.64		4.33		28.02		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68		0		-24823.59		12:49:13		11:46:00		m		50.82		1573.72

		S1148881434:		#B4q0		1148881434:		$B4q0		d-		29.64		4.33		27.92		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68		0		-24824.59		12:49:43		11:46:30		m		50.86		1574.79

		S1148881464:		#B4q0		1148881464:		$B4q0		d-		29.64		4.33		28.02		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68		0		-24825.73		12:50:13		11:47:00		m		50.90		1575.86

		S1148881494:		#B4q0		1148881494:		$B4q0		d-		29.64		4.30		28.02		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68		0		-24826.73		12:50:43		11:47:30		m		50.93		1576.92

		S1148881524:		#B4q0		1148881524:		$B4q0		d-		29.64		4.33		28.02		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68		0		-24827.87		12:51:13		11:48:00		m		50.97		1577.99

		S1148881554:		#B4q0		1148881554:		$B4q0		d-		29.64		4.30		27.92		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68		0		-24828.87		12:51:43		11:48:30		m		51.00		1579.05

		S1148881584:		#B4q0		1148881584:		$B4q0		d-		29.64		4.33		27.92		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68		0		-24830.01		12:52:13		11:49:00		m		51.04		1580.12

		S1148881614:		#B4q0		1148881614:		$B4q0		d-		29.64		4.30		27.92		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68		0		-24831.01		12:52:43		11:49:30		m		51.07		1581.19

		S1148881644:		#B4q0		1148881644:		$B4q0		d-		29.64		4.33		27.92		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68		0		-24832.15		12:53:13		11:50:00		m		51.11		1582.25

		S1148881674:		#B4q0		1148881674:		$B4q0		d-		29.64		4.30		27.92		3.72		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24833.15		12:53:43		11:50:30		m		51.15		1583.32

		S1148881704:		#B4q0		1148881704:		$B4q0		d-		29.64		4.30		27.92		3.72		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24834.29		12:54:13		11:51:00		m		51.18		1584.38

		S1148881734:		#B4q0		1148881734:		$B4q0		d-		29.64		4.33		28.02		3.72		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24835.29		12:54:43		11:51:30		m		51.22		1585.45

		S1148881764:		#B4q0		1148881764:		$B4q0		d-		29.64		4.33		28.02		3.72		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24836.43		12:55:13		11:52:00		m		51.25		1586.52

		S1148881794:		#B4q0		1148881794:		$B4q0		d-		29.64		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24837.43		12:55:43		11:52:30		m		51.29		1587.58

		S1148881824:		#B4q0		1148881824:		$B4q0		d-		29.61		4.37		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24838.57		12:56:13		11:53:00		m		51.33		1588.66

		S1148881854:		#B4q0		1148881854:		$B4q0		d-		29.64		4.30		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24839.57		12:56:43		11:53:30		m		51.36		1589.73

		S1148881884:		#B4q0		1148881884:		$B4q0		d-		29.64		4.30		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24840.71		12:57:13		11:54:00		m		51.40		1590.79

		S1148881914:		#B4q0		1148881914:		$B4q0		d-		29.64		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24841.71		12:57:43		11:54:30		m		51.44		1591.86

		S1148881944:		#B4q0		1148881944:		$B4q0		d-		29.64		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24842.85		12:58:13		11:55:00		m		51.47		1592.93

		S1148881974:		#B4q0		1148881974:		$B4q0		d-		29.64		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24843.85		12:58:43		11:55:30		m		51.51		1594.00

		S1148882004:		#B4q0		1148882004:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24844.99		12:59:13		11:56:00		m		51.54		1595.06

		S1148882034:		#B4q0		1148882034:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24845.98		12:59:43		11:56:30		m		51.58		1596.13

		S1148882064:		#B4q0		1148882064:		$B4q0		d-		29.64		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24847.12		13:00:13		11:57:00		m		51.62		1597.20

		S1148882094:		#B4q0		1148882094:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.68		0		-24848.12		13:00:43		11:57:30		m		51.65		1598.27

		S1148882124:		#B4q0		1148882124:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24849.26		13:01:13		11:58:00		m		51.69		1599.34

		S1148882154:		#B4q0		1148882154:		$B4q0		d-		29.64		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24850.26		13:01:43		11:58:30		m		51.72		1600.41

		S1148882184:		#B4q0		1148882184:		$B4q0		d-		29.61		4.30		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24851.4		13:02:13		11:59:00		m		51.76		1601.47

		S1148882214:		#B4q0		1148882214:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24852.4		13:02:43		11:59:30		m		51.80		1602.54

		S1148882244:		#B4q0		1148882244:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24853.54		13:03:13		12:00:00		m		51.83		1603.61

		S1148882274:		#B4q0		1148882274:		$B4q0		d-		29.61		4.30		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24854.53		13:03:43		12:00:30		m		51.87		1604.67

		S1148882304:		#B4q0		1148882304:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24855.67		13:04:13		12:01:00		m		51.90		1605.74

		S1148882334:		#B4q0		1148882334:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24856.67		13:04:43		12:01:30		m		51.94		1606.80

		S1148882364:		#B4q0		1148882364:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24857.81		13:05:13		12:02:00		m		51.98		1607.87

		S1148882394:		#B4q0		1148882394:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24858.81		13:05:43		12:02:30		m		52.01		1608.94

		S1148882424:		#B4q0		1148882424:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24859.95		13:06:13		12:03:00		m		52.05		1610.01

		S1148882454:		#B4q0		1148882454:		$B4q0		d-		29.61		4.30		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24860.95		13:06:43		12:03:30		m		52.08		1611.07

		S1148882484:		#B4q0		1148882484:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24862.08		13:07:13		12:04:00		m		52.12		1612.14

		S1148882514:		#B4q0		1148882514:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24863.08		13:07:43		12:04:30		m		52.16		1613.21

		S1148882544:		#B4q0		1148882544:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.68		3.67		3.69		3.70		3.67		0		-24864.22		13:08:13		12:05:00		m		52.19		1614.28

		S1148882574:		#B4q0		1148882574:		$B4q0		d-		29.61		4.33		28.02		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24865.21		13:08:43		12:05:30		m		52.23		1615.34

		S1148882604:		#B4q0		1148882604:		$B4q0		d-		29.61		4.30		28.02		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24866.35		13:09:13		12:06:00		m		52.26		1616.41

		S1148882634:		#B4q0		1148882634:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24867.35		13:09:43		12:06:30		m		52.30		1617.47

		S1148882664:		#B4q0		1148882664:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24868.49		13:10:13		12:07:00		m		52.34		1618.54

		S1148882694:		#B4q0		1148882694:		$B4q0		d-		29.57		4.33		28.02		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24869.48		13:10:43		12:07:30		m		52.37		1619.61

		S1148882724:		#B4q0		1148882724:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24870.62		13:11:13		12:08:00		m		52.41		1620.67

		S1148882754:		#B4q0		1148882754:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24871.62		13:11:43		12:08:30		m		52.44		1621.74

		S1148882784:		#B4q0		1148882784:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24872.75		13:12:13		12:09:00		m		52.48		1622.81

		S1148882814:		#B4q0		1148882814:		$B4q0		d-		29.57		4.33		28.02		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24873.75		13:12:43		12:09:30		m		52.52		1623.88

		S1148882844:		#B4q0		1148882844:		$B4q0		d-		29.57		4.30		28.02		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24874.89		13:13:13		12:10:00		m		52.55		1624.94

		S1148882874:		#B4q0		1148882874:		$B4q0		d-		29.61		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.69		3.70		3.67		0		-24875.88		13:13:43		12:10:30		m		52.59		1626.00

		S1148882904:		#B4q0		1148882904:		$B4q0		d-		29.57		4.30		28.02		3.71		3.71		3.71		3.67		3.67		3.68		3.70		3.67		0		-24877.02		13:14:13		12:11:00		m		52.62		1627.07

		S1148882934:		#B4q0		1148882934:		$B4q0		d-		29.57		4.33		28.02		3.71		3.71		3.71		3.67		3.67		3.68		3.70		3.67		0		-24878.02		13:14:43		12:11:30		m		52.66		1628.13

		S1148882964:		#B4q0		1148882964:		$B4q0		d-		29.57		4.30		27.92		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67		0		-24879.16		13:15:13		12:12:00		m		52.70		1629.19

		S1148882994:		#B4q0		1148882994:		$B4q0		d-		29.57		4.33		27.92		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67		0		-24880.15		13:15:43		12:12:30		m		52.73		1630.26

		S1148883024:		#B4q0		1148883024:		$B4q0		d-		29.57		4.33		28.02		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67		0		-24881.29		13:16:13		12:13:00		m		52.77		1631.32

		S1148883054:		#B4q0		1148883054:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.71		3.67		3.67		3.68		3.69		3.67		0		-24882.29		13:16:43		12:13:30		m		52.80		1632.39

		S1148883084:		#B4q0		1148883084:		$B4q0		d-		29.57		4.33		27.92		3.71		3.70		3.71		3.67		3.67		3.68		3.69		3.67		0		-24883.42		13:17:13		12:14:00		m		52.84		1633.46

		S1148883114:		#B4q0		1148883114:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.71		3.67		3.67		3.68		3.69		3.67		0		-24884.42		13:17:43		12:14:30		m		52.88		1634.52

		S1148883144:		#B4q0		1148883144:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.71		3.67		3.67		3.68		3.69		3.67		0		-24885.56		13:18:13		12:15:00		m		52.91		1635.59

		S1148883174:		#B4q0		1148883174:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.71		3.67		3.66		3.68		3.69		3.67		0		-24886.55		13:18:43		12:15:30		m		52.95		1636.66

		S1148883204:		#B4q0		1148883204:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.71		3.67		3.66		3.68		3.69		3.67		0		-24887.69		13:19:13		12:16:00		m		52.98		1637.73

		S1148883234:		#B4q0		1148883234:		$B4q0		d-		29.53		4.37		27.92		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24888.68		13:19:43		12:16:30		m		53.02		1638.80

		S1148883264:		#B4q0		1148883264:		$B4q0		d-		29.53		4.33		28.02		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24889.82		13:20:13		12:17:00		m		53.06		1639.87

		S1148883294:		#B4q0		1148883294:		$B4q0		d-		29.53		4.30		28.02		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24890.82		13:20:43		12:17:30		m		53.09		1640.93

		S1148883324:		#B4q0		1148883324:		$B4q0		d-		29.53		4.33		28.02		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24891.96		13:21:13		12:18:00		m		53.13		1641.99

		S1148883354:		#B4q0		1148883354:		$B4q0		d-		29.53		4.33		27.92		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24892.95		13:21:43		12:18:30		m		53.17		1643.06

		S1148883384:		#B4q0		1148883384:		$B4q0		d-		29.57		4.33		28.02		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24894.09		13:22:13		12:19:00		m		53.20		1644.12

		S1148883414:		#B4q0		1148883414:		$B4q0		d-		29.53		4.33		27.92		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24895.08		13:22:43		12:19:30		m		53.24		1645.19

		S1148883444:		#B4q0		1148883444:		$B4q0		d-		29.57		4.33		27.92		3.71		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24896.22		13:23:13		12:20:00		m		53.27		1646.26

		S1148883474:		#B4q0		1148883474:		$B4q0		d-		29.57		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24897.21		13:23:43		12:20:30		m		53.31		1647.32

		S1148883504:		#B4q0		1148883504:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24898.35		13:24:13		12:21:00		m		53.35		1648.39

		S1148883534:		#B4q0		1148883534:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24899.34		13:24:43		12:21:30		m		53.38		1649.45

		S1148883564:		#B4q0		1148883564:		$B4q0		d-		29.53		4.37		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24900.48		13:25:13		12:22:00		m		53.42		1650.52

		S1148883594:		#B4q0		1148883594:		$B4q0		d-		29.53		4.37		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24901.48		13:25:43		12:22:30		m		53.45		1651.60

		S1148883624:		#B4q0		1148883624:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24902.61		13:26:13		12:23:00		m		53.49		1652.67

		S1148883654:		#B4q0		1148883654:		$B4q0		d-		29.53		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24903.6		13:26:43		12:23:30		m		53.53		1653.74

		S1148883684:		#B4q0		1148883684:		$B4q0		d-		29.53		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.67		0		-24904.74		13:27:13		12:24:00		m		53.56		1654.80

		S1148883714:		#B4q0		1148883714:		$B4q0		d-		29.49		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24905.74		13:27:43		12:24:30		m		53.60		1655.87

		S1148883744:		#B4q0		1148883744:		$B4q0		d-		29.53		4.30		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24906.87		13:28:13		12:25:00		m		53.63		1656.93

		S1148883774:		#B4q0		1148883774:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24907.87		13:28:43		12:25:30		m		53.67		1657.99

		S1148883804:		#B4q0		1148883804:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24909		13:29:13		12:26:00		m		53.71		1659.05

		S1148883834:		#B4q0		1148883834:		$B4q0		d-		29.53		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24909.99		13:29:43		12:26:30		m		53.74		1660.12

		S1148883864:		#B4q0		1148883864:		$B4q0		d-		29.53		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24911.13		13:30:13		12:27:00		m		53.78		1661.19

		S1148883894:		#B4q0		1148883894:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24912.13		13:30:43		12:27:30		m		53.82		1662.25

		S1148883924:		#B4q0		1148883924:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24913.26		13:31:13		12:28:00		m		53.85		1663.31

		S1148883954:		#B4q0		1148883954:		$B4q0		d-		29.49		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24914.26		13:31:43		12:28:30		m		53.89		1664.38

		S1148883984:		#B4q0		1148883984:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24915.39		13:32:13		12:29:00		m		53.92		1665.44

		S1148884014:		#B4q0		1148884014:		$B4q0		d-		29.53		4.30		27.92		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24916.39		13:32:43		12:29:30		m		53.96		1666.50

		S1148884044:		#B4q0		1148884044:		$B4q0		d-		29.49		4.30		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24917.52		13:33:13		12:30:00		m		54.00		1667.56

		S1148884074:		#B4q0		1148884074:		$B4q0		d-		29.53		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24918.52		13:33:43		12:30:30		m		54.03		1668.62

		S1148884104:		#B4q0		1148884104:		$B4q0		d-		29.49		4.30		28.02		3.70		3.70		3.70		3.67		3.66		3.68		3.69		3.66		0		-24919.65		13:34:13		12:31:00		m		54.07		1669.68

		S1148884134:		#B4q0		1148884134:		$B4q0		d-		29.53		4.33		28.02		3.70		3.70		3.70		3.67		3.66		3.67		3.69		3.66		0		-24920.65		13:34:43		12:31:30		m		54.10		1670.74

		S1148884164:		#B4q0		1148884164:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24921.78		13:35:13		12:32:00		m		54.14		1671.81

		S1148884194:		#B4q0		1148884194:		$B4q0		d-		29.49		4.37		27.92		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24922.78		13:35:43		12:32:30		m		54.18		1672.88

		S1148884224:		#B4q0		1148884224:		$B4q0		d-		29.49		4.30		28.02		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24923.92		13:36:13		12:33:00		m		54.21		1673.94

		S1148884254:		#B4q0		1148884254:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24924.91		13:36:43		12:33:30		m		54.25		1675.00

		S1148884284:		#B4q0		1148884284:		$B4q0		d-		29.49		4.30		28.02		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24926.04		13:37:13		12:34:00		m		54.28		1676.06

		S1148884314:		#B4q0		1148884314:		$B4q0		d-		29.49		4.33		27.92		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24927.04		13:37:43		12:34:30		m		54.32		1677.13

		S1148884344:		#B4q0		1148884344:		$B4q0		d-		29.49		4.33		28.02		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24928.18		13:38:13		12:35:00		m		54.36		1678.19

		S1148884374:		#B4q0		1148884374:		$B4q0		d-		29.49		4.30		27.92		3.70		3.69		3.70		3.66		3.66		3.67		3.69		3.66		0		-24929.17		13:38:43		12:35:30		m		54.39		1679.25

		S1148884404:		#B4q0		1148884404:		$B4q0		d-		29.49		4.33		28.02		3.70		3.70		3.70		3.66		3.66		3.67		3.69		3.66		0		-24930.31		13:39:13		12:36:00		m		54.43		1680.31

		S1148884434:		#B4q0		1148884434:		$B4q0		d-		29.49		4.33		28.02		3.70		3.69		3.70		3.66		3.65		3.67		3.69		3.66		0		-24931.3		13:39:43		12:36:30		m		54.46		1681.37

		S1148884464:		#B4q0		1148884464:		$B4q0		d-		29.49		4.33		27.92		3.70		3.69		3.70		3.66		3.65		3.67		3.69		3.66		0		-24932.44		13:40:13		12:37:00		m		54.50		1682.44

		S1148884494:		#B4q0		1148884494:		$B4q0		d-		29.49		4.33		27.92		3.70		3.69		3.70		3.66		3.65		3.67		3.69		3.66		0		-24933.43		13:40:43		12:37:30		m		54.54		1683.50

		S1148884524:		#B4q0		1148884524:		$B4q0		d-		29.49		4.33		28.02		3.70		3.69		3.70		3.66		3.65		3.67		3.69		3.66		0		-24934.56		13:41:13		12:38:00		m		54.57		1684.57

		S1148884554:		#B4q0		1148884554:		$B4q0		d-		29.49		4.33		28.02		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24935.56		13:41:43		12:38:30		m		54.61		1685.63

		S1148884584:		#B4q0		1148884584:		$B4q0		d-		29.49		4.30		28.02		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24936.69		13:42:13		12:39:00		m		54.64		1686.69

		S1148884614:		#B4q0		1148884614:		$B4q0		d-		29.49		4.33		27.92		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24937.68		13:42:43		12:39:30		m		54.68		1687.75

		S1148884644:		#B4q0		1148884644:		$B4q0		d-		29.49		4.33		28.02		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24938.82		13:43:13		12:40:00		m		54.72		1688.82

		S1148884674:		#B4q0		1148884674:		$B4q0		d-		29.49		4.30		28.02		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24939.81		13:43:43		12:40:30		m		54.75		1689.88

		S1148884704:		#B4q0		1148884704:		$B4q0		d-		29.46		4.33		27.92		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24940.94		13:44:13		12:41:00		m		54.79		1690.94

		S1148884734:		#B4q0		1148884734:		$B4q0		d-		29.49		4.33		27.92		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24941.94		13:44:43		12:41:30		m		54.82		1692.00

		S1148884764:		#B4q0		1148884764:		$B4q0		d-		29.49		4.33		27.92		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24943.07		13:45:13		12:42:00		m		54.86		1693.06

		S1148884794:		#B4q0		1148884794:		$B4q0		d-		29.49		4.33		28.02		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24944.07		13:45:43		12:42:30		m		54.90		1694.13

		S1148884824:		#B4q0		1148884824:		$B4q0		d-		29.49		4.30		27.92		3.70		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24945.2		13:46:13		12:43:00		m		54.93		1695.19

		S1148884854:		#B4q0		1148884854:		$B4q0		d-		29.49		4.33		27.92		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.66		0		-24946.2		13:46:43		12:43:30		m		54.97		1696.25

		S1148884884:		#B4q0		1148884884:		$B4q0		d-		29.46		4.33		28.02		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65		0		-24947.34		13:47:13		12:44:00		m		55.00		1697.31

		S1148884914:		#B4q0		1148884914:		$B4q0		d-		29.49		4.33		27.92		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65		0		-24948.33		13:47:43		12:44:30		m		55.04		1698.38

		S1148884944:		#B4q0		1148884944:		$B4q0		d-		29.49		4.33		27.92		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65		0		-24949.46		13:48:13		12:45:00		m		55.08		1699.44

		S1148884974:		#B4q0		1148884974:		$B4q0		d-		29.46		4.33		28.02		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65		0		-24950.46		13:48:43		12:45:30		m		55.11		1700.50

		S1148885004:		#B4q0		1148885004:		$B4q0		d-		29.46		4.37		28.02		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65		0		-24951.59		13:49:13		12:46:00		m		55.15		1701.57

		S1148885034:		#B4q0		1148885034:		$B4q0		d-		29.46		4.30		27.92		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65		0		-24952.58		13:49:43		12:46:30		m		55.18		1702.64

		S1148885064:		#B4q0		1148885064:		$B4q0		d-		29.46		4.33		27.92		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65		0		-24953.71		13:50:13		12:47:00		m		55.22		1703.69

		S1148885094:		#B4q0		1148885094:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24954.7		13:50:43		12:47:30		m		55.26		1704.76

		S1148885124:		#B4q0		1148885124:		$B4q0		d-		29.46		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24955.84		13:51:13		12:48:00		m		55.29		1705.82

		S1148885154:		#B4q0		1148885154:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24956.83		13:51:43		12:48:30		m		55.33		1706.88

		S1148885184:		#B4q0		1148885184:		$B4q0		d-		29.46		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24957.96		13:52:13		12:49:00		m		55.37		1707.94

		S1148885214:		#B4q0		1148885214:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24958.95		13:52:43		12:49:30		m		55.40		1709.01

		S1148885244:		#B4q0		1148885244:		$B4q0		d-		29.42		4.30		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24960.08		13:53:13		12:50:00		m		55.44		1710.06

		S1148885274:		#B4q0		1148885274:		$B4q0		d-		29.46		4.30		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24961.08		13:53:43		12:50:30		m		55.47		1711.12

		S1148885304:		#B4q0		1148885304:		$B4q0		d-		29.46		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24962.21		13:54:13		12:51:00		m		55.51		1712.18

		S1148885334:		#B4q0		1148885334:		$B4q0		d-		29.46		4.33		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24963.21		13:54:43		12:51:30		m		55.55		1713.24

		S1148885364:		#B4q0		1148885364:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24964.34		13:55:13		12:52:00		m		55.58		1714.30

		S1148885394:		#B4q0		1148885394:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24965.33		13:55:43		12:52:30		m		55.62		1715.37

		S1148885424:		#B4q0		1148885424:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24966.46		13:56:13		12:53:00		m		55.65		1716.43

		S1148885454:		#B4q0		1148885454:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24967.45		13:56:43		12:53:30		m		55.69		1717.49

		S1148885484:		#B4q0		1148885484:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24968.58		13:57:13		12:54:00		m		55.73		1718.55

		S1148885514:		#B4q0		1148885514:		$B4q0		d-		29.42		4.37		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24969.57		13:57:43		12:54:30		m		55.76		1719.62

		S1148885544:		#B4q0		1148885544:		$B4q0		d-		29.42		4.30		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24970.71		13:58:13		12:55:00		m		55.80		1720.68

		S1148885574:		#B4q0		1148885574:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65		0		-24971.7		13:58:43		12:55:30		m		55.83		1721.74

		S1148885604:		#B4q0		1148885604:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65		0		-24972.83		13:59:13		12:56:00		m		55.87		1722.80

		S1148885634:		#B4q0		1148885634:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65		0		-24973.82		13:59:43		12:56:30		m		55.91		1723.86

		S1148885664:		#B4q0		1148885664:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65		0		-24974.95		14:00:13		12:57:00		m		55.94		1724.92

		S1148885694:		#B4q0		1148885694:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65		0		-24975.94		14:00:43		12:57:30		m		55.98		1725.98

		S1148885724:		#B4q0		1148885724:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.65		0		-24977.07		14:01:13		12:58:00		m		56.01		1727.04

		S1148885754:		#B4q0		1148885754:		$B4q0		d-		29.42		4.30		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.65		0		-24978.06		14:01:43		12:58:30		m		56.05		1728.10

		S1148885784:		#B4q0		1148885784:		$B4q0		d-		29.42		4.30		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24979.19		14:02:13		12:59:00		m		56.09		1729.16

		S1148885814:		#B4q0		1148885814:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24980.19		14:02:43		12:59:30		m		56.12		1730.21

		S1148885844:		#B4q0		1148885844:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24981.32		14:03:13		13:00:00		m		56.16		1731.28

		S1148885874:		#B4q0		1148885874:		$B4q0		d-		29.42		4.37		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24982.3		14:03:43		13:00:30		m		56.19		1732.34

		S1148885904:		#B4q0		1148885904:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24983.43		14:04:13		13:01:00		m		56.23		1733.41

		S1148885934:		#B4q0		1148885934:		$B4q0		d-		29.38		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24984.43		14:04:43		13:01:30		m		56.27		1734.47

		S1148885964:		#B4q0		1148885964:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24985.56		14:05:13		13:02:00		m		56.30		1735.53

		S1148885994:		#B4q0		1148885994:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24986.54		14:05:43		13:02:30		m		56.34		1736.59

		S1148886024:		#B4q0		1148886024:		$B4q0		d-		29.38		4.30		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24987.67		14:06:13		13:03:00		m		56.37		1737.65

		S1148886054:		#B4q0		1148886054:		$B4q0		d-		29.42		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24988.66		14:06:43		13:03:30		m		56.41		1738.71

		S1148886084:		#B4q0		1148886084:		$B4q0		d-		29.38		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64		0		-24989.8		14:07:13		13:04:00		m		56.45		1739.77

		S1148886114:		#B4q0		1148886114:		$B4q0		d-		29.42		4.37		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24990.78		14:07:43		13:04:30		m		56.48		1740.83

		S1148886144:		#B4q0		1148886144:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24991.92		14:08:13		13:05:00		m		56.52		1741.90

		S1148886174:		#B4q0		1148886174:		$B4q0		d-		29.42		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24992.91		14:08:43		13:05:30		m		56.56		1742.96

		S1148886204:		#B4q0		1148886204:		$B4q0		d-		29.38		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24994.04		14:09:13		13:06:00		m		56.59		1744.02

		S1148886234:		#B4q0		1148886234:		$B4q0		d-		29.38		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24995.02		14:09:43		13:06:30		m		56.63		1745.08

		S1148886264:		#B4q0		1148886264:		$B4q0		d-		29.38		4.30		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24996.16		14:10:13		13:07:00		m		56.66		1746.14

		S1148886294:		#B4q0		1148886294:		$B4q0		d-		29.34		4.30		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24997.15		14:10:43		13:07:30		m		56.70		1747.19

		S1148886324:		#B4q0		1148886324:		$B4q0		d-		29.38		4.33		28.02		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24998.28		14:11:13		13:08:00		m		56.74		1748.25

		S1148886354:		#B4q0		1148886354:		$B4q0		d-		29.38		4.33		27.92		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64		0		-24999.27		14:11:43		13:08:30		m		56.77		1749.31

		S1148886384:		#B4q0		1148886384:		$B4q0		d-		29.38		4.33		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25000.4		14:12:13		13:09:00		m		56.81		1750.37

		S1148886414:		#B4q0		1148886414:		$B4q0		d-		29.38		4.33		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25001.39		14:12:43		13:09:30		m		56.84		1751.43

		S1148886444:		#B4q0		1148886444:		$B4q0		d-		29.38		4.37		28.02		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25002.52		14:13:13		13:10:00		m		56.88		1752.49

		S1148886474:		#B4q0		1148886474:		$B4q0		d-		29.38		4.33		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25003.51		14:13:43		13:10:30		m		56.92		1753.56

		S1148886504:		#B4q0		1148886504:		$B4q0		d-		29.38		4.33		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25004.64		14:14:13		13:11:00		m		56.95		1754.62

		S1148886534:		#B4q0		1148886534:		$B4q0		d-		29.38		4.33		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25005.63		14:14:43		13:11:30		m		56.99		1755.68

		S1148886564:		#B4q0		1148886564:		$B4q0		d-		29.38		4.30		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25006.76		14:15:13		13:12:00		m		57.02		1756.73

		S1148886594:		#B4q0		1148886594:		$B4q0		d-		29.38		4.33		28.02		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25007.75		14:15:43		13:12:30		m		57.06		1757.79

		S1148886624:		#B4q0		1148886624:		$B4q0		d-		29.34		4.30		27.92		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25008.88		14:16:13		13:13:00		m		57.10		1758.85

		S1148886654:		#B4q0		1148886654:		$B4q0		d-		29.34		4.30		28.02		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64		0		-25009.87		14:16:43		13:13:30		m		57.13		1759.90

		S1148886684:		#B4q0		1148886684:		$B4q0		d-		29.34		4.33		27.92		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25011		14:17:13		13:14:00		m		57.17		1760.95

		S1148886714:		#B4q0		1148886714:		$B4q0		d-		29.34		4.30		28.02		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25011.99		14:17:43		13:14:30		m		57.20		1762.01

		S1148886744:		#B4q0		1148886744:		$B4q0		d-		29.34		4.30		27.92		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25013.12		14:18:13		13:15:00		m		57.24		1763.06

		S1148886774:		#B4q0		1148886774:		$B4q0		d-		29.34		4.33		28.02		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25014.11		14:18:43		13:15:30		m		57.28		1764.11

		S1148886804:		#B4q0		1148886804:		$B4q0		d-		29.34		4.33		27.92		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25015.24		14:19:13		13:16:00		m		57.31		1765.17

		S1148886834:		#B4q0		1148886834:		$B4q0		d-		29.34		4.33		27.92		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25016.23		14:19:43		13:16:30		m		57.35		1766.23

		S1148886864:		#B4q0		1148886864:		$B4q0		d-		29.34		4.30		28.02		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25017.36		14:20:13		13:17:00		m		57.38		1767.29

		S1148886894:		#B4q0		1148886894:		$B4q0		d-		29.34		4.30		27.92		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25018.35		14:20:43		13:17:30		m		57.42		1768.34

		S1148886924:		#B4q0		1148886924:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25019.48		14:21:13		13:18:00		m		57.46		1769.39

		S1148886954:		#B4q0		1148886954:		$B4q0		d-		29.38		4.33		28.02		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25020.47		14:21:43		13:18:30		m		57.49		1770.45

		S1148886984:		#B4q0		1148886984:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25021.6		14:22:13		13:19:00		m		57.53		1771.51

		S1148887014:		#B4q0		1148887014:		$B4q0		d-		29.34		4.30		27.92		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64		0		-25022.59		14:22:43		13:19:30		m		57.56		1772.57

		S1148887044:		#B4q0		1148887044:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.66		3.67		3.64		0		-25023.72		14:23:13		13:20:00		m		57.60		1773.62

		S1148887074:		#B4q0		1148887074:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25024.71		14:23:43		13:20:30		m		57.64		1774.68

		S1148887104:		#B4q0		1148887104:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25025.84		14:24:13		13:21:00		m		57.67		1775.74

		S1148887134:		#B4q0		1148887134:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25026.83		14:24:43		13:21:30		m		57.71		1776.80

		S1148887164:		#B4q0		1148887164:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25027.96		14:25:13		13:22:00		m		57.74		1777.86

		S1148887194:		#B4q0		1148887194:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25028.95		14:25:43		13:22:30		m		57.78		1778.91

		S1148887224:		#B4q0		1148887224:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25030.08		14:26:13		13:23:00		m		57.82		1779.97

		S1148887254:		#B4q0		1148887254:		$B4q0		d-		29.30		4.30		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25031.07		14:26:43		13:23:30		m		57.85		1781.03

		S1148887284:		#B4q0		1148887284:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25032.2		14:27:13		13:24:00		m		57.89		1782.08

		S1148887314:		#B4q0		1148887314:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25033.18		14:27:43		13:24:30		m		57.92		1783.14

		S1148887344:		#B4q0		1148887344:		$B4q0		d-		29.34		4.37		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25034.31		14:28:13		13:25:00		m		57.96		1784.20

		S1148887374:		#B4q0		1148887374:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25035.3		14:28:43		13:25:30		m		58.00		1785.27

		S1148887404:		#B4q0		1148887404:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25036.42		14:29:13		13:26:00		m		58.03		1786.33

		S1148887434:		#B4q0		1148887434:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25037.41		14:29:43		13:26:30		m		58.07		1787.39

		S1148887464:		#B4q0		1148887464:		$B4q0		d-		29.34		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25038.54		14:30:13		13:27:00		m		58.10		1788.44

		S1148887494:		#B4q0		1148887494:		$B4q0		d-		29.30		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25039.53		14:30:43		13:27:30		m		58.14		1789.50

		S1148887524:		#B4q0		1148887524:		$B4q0		d-		29.30		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25040.65		14:31:13		13:28:00		m		58.18		1790.56

		S1148887554:		#B4q0		1148887554:		$B4q0		d-		29.30		4.33		28.02		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25041.64		14:31:43		13:28:30		m		58.21		1791.62

		S1148887584:		#B4q0		1148887584:		$B4q0		d-		29.30		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25042.77		14:32:13		13:29:00		m		58.25		1792.67

		S1148887614:		#B4q0		1148887614:		$B4q0		d-		29.34		4.33		27.92		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64		0		-25043.76		14:32:43		13:29:30		m		58.29		1793.73

		S1148887644:		#B4q0		1148887644:		$B4q0		d-		29.30		4.33		27.92		3.68		3.67		3.68		3.64		3.63		3.65		3.67		3.64		0		-25044.89		14:33:13		13:30:00		m		58.32		1794.79

		S1148887674:		#B4q0		1148887674:		$B4q0		d-		29.30		4.30		27.92		3.68		3.67		3.68		3.64		3.63		3.65		3.67		3.64		0		-25045.87		14:33:43		13:30:30		m		58.36		1795.84

		S1148887704:		#B4q0		1148887704:		$B4q0		d-		29.30		4.30		28.02		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64		0		-25047		14:34:13		13:31:00		m		58.39		1796.89

		S1148887734:		#B4q0		1148887734:		$B4q0		d-		29.30		4.33		27.92		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64		0		-25047.98		14:34:43		13:31:30		m		58.43		1797.95

		S1148887764:		#B4q0		1148887764:		$B4q0		d-		29.30		4.30		28.02		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64		0		-25049.12		14:35:13		13:32:00		m		58.46		1799.00

		S1148887794:		#B4q0		1148887794:		$B4q0		d-		29.30		4.33		27.92		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64		0		-25050.1		14:35:43		13:32:30		m		58.50		1800.05

		S1148887824:		#B4q0		1148887824:		$B4q0		d-		29.30		4.33		28.02		3.68		3.67		3.68		3.64		3.63		3.64		3.66		3.64		0		-25051.23		14:36:13		13:33:00		m		58.54		1801.11

		S1148887854:		#B4q0		1148887854:		$B4q0		d-		29.30		4.37		27.92		3.68		3.67		3.68		3.64		3.63		3.64		3.66		3.64		0		-25052.22		14:36:43		13:33:30		m		58.57		1802.17

		S1148887884:		#B4q0		1148887884:		$B4q0		d-		29.30		4.33		27.92		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64		0		-25053.34		14:37:13		13:34:00		m		58.61		1803.24

		S1148887914:		#B4q0		1148887914:		$B4q0		d-		29.26		4.33		28.02		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64		0		-25054.33		14:37:43		13:34:30		m		58.65		1804.29

		S1148887944:		#B4q0		1148887944:		$B4q0		d-		29.26		4.30		27.92		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64		0		-25055.46		14:38:13		13:35:00		m		58.68		1805.34

		S1148887974:		#B4q0		1148887974:		$B4q0		d-		29.30		4.33		28.02		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.63		0		-25056.44		14:38:43		13:35:30		m		58.72		1806.40

		S1148888004:		#B4q0		1148888004:		$B4q0		d-		29.30		4.30		28.02		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.63		0		-25057.57		14:39:13		13:36:00		m		58.75		1807.45

		S1148888034:		#B4q0		1148888034:		$B4q0		d-		29.26		4.33		28.02		3.68		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25058.55		14:39:43		13:36:30		m		58.79		1808.50

		S1148888064:		#B4q0		1148888064:		$B4q0		d-		29.30		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25059.67		14:40:13		13:37:00		m		58.83		1809.56

		S1148888094:		#B4q0		1148888094:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25060.66		14:40:43		13:37:30		m		58.86		1810.62

		S1148888124:		#B4q0		1148888124:		$B4q0		d-		29.30		4.33		28.02		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25061.79		14:41:13		13:38:00		m		58.90		1811.67

		S1148888154:		#B4q0		1148888154:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25062.77		14:41:43		13:38:30		m		58.93		1812.73

		S1148888184:		#B4q0		1148888184:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25063.9		14:42:13		13:39:00		m		58.97		1813.79

		S1148888214:		#B4q0		1148888214:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25064.88		14:42:43		13:39:30		m		59.01		1814.84

		S1148888244:		#B4q0		1148888244:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25066.01		14:43:13		13:40:00		m		59.04		1815.90

		S1148888274:		#B4q0		1148888274:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25067		14:43:43		13:40:30		m		59.08		1816.95

		S1148888304:		#B4q0		1148888304:		$B4q0		d-		29.26		4.30		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25068.12		14:44:13		13:41:00		m		59.11		1818.00

		S1148888334:		#B4q0		1148888334:		$B4q0		d-		29.26		4.33		28.02		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25069.11		14:44:43		13:41:30		m		59.15		1819.06

		S1148888364:		#B4q0		1148888364:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25070.24		14:45:13		13:42:00		m		59.19		1820.11

		S1148888394:		#B4q0		1148888394:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25071.22		14:45:43		13:42:30		m		59.22		1821.17

		S1148888424:		#B4q0		1148888424:		$B4q0		d-		29.23		4.33		28.02		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25072.35		14:46:13		13:43:00		m		59.26		1822.22

		S1148888454:		#B4q0		1148888454:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25073.33		14:46:43		13:43:30		m		59.29		1823.28

		S1148888484:		#B4q0		1148888484:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25074.46		14:47:13		13:44:00		m		59.33		1824.33

		S1148888514:		#B4q0		1148888514:		$B4q0		d-		29.26		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25075.45		14:47:43		13:44:30		m		59.37		1825.39

		S1148888544:		#B4q0		1148888544:		$B4q0		d-		29.26		4.30		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25076.58		14:48:13		13:45:00		m		59.40		1826.44

		S1148888574:		#B4q0		1148888574:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25077.56		14:48:43		13:45:30		m		59.44		1827.49

		S1148888604:		#B4q0		1148888604:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63		0		-25078.68		14:49:13		13:46:00		m		59.47		1828.55

		S1148888634:		#B4q0		1148888634:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.63		0		-25079.67		14:49:43		13:46:30		m		59.51		1829.60

		S1148888664:		#B4q0		1148888664:		$B4q0		d-		29.23		4.33		28.02		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.63		0		-25080.79		14:50:13		13:47:00		m		59.55		1830.66

		S1148888694:		#B4q0		1148888694:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25081.77		14:50:43		13:47:30		m		59.58		1831.71

		S1148888724:		#B4q0		1148888724:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25082.9		14:51:13		13:48:00		m		59.62		1832.77

		S1148888754:		#B4q0		1148888754:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25083.88		14:51:43		13:48:30		m		59.66		1833.82

		S1148888784:		#B4q0		1148888784:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25085		14:52:13		13:49:00		m		59.69		1834.88

		S1148888814:		#B4q0		1148888814:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25085.99		14:52:43		13:49:30		m		59.73		1835.93

		S1148888844:		#B4q0		1148888844:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62		0		-25087.11		14:53:13		13:50:00		m		59.76		1836.98

		S1148888874:		#B4q0		1148888874:		$B4q0		d-		29.23		4.30		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.66		3.62		0		-25088.1		14:53:43		13:50:30		m		59.80		1838.04

		S1148888904:		#B4q0		1148888904:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.66		3.62		0		-25089.22		14:54:13		13:51:00		m		59.84		1839.09

		S1148888934:		#B4q0		1148888934:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.66		3.62		0		-25090.2		14:54:43		13:51:30		m		59.87		1840.14

		S1148888964:		#B4q0		1148888964:		$B4q0		d-		29.23		4.30		28.02		3.67		3.67		3.67		3.63		3.60		3.64		3.66		3.62		0		-25091.33		14:55:13		13:52:00		m		59.91		1841.19

		S1148888994:		#B4q0		1148888994:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.66		3.62		0		-25092.31		14:55:43		13:52:30		m		59.94		1842.24

		S1148889024:		#B4q0		1148889024:		$B4q0		d-		29.19		4.37		28.02		3.67		3.67		3.67		3.63		3.60		3.64		3.65		3.62		0		-25093.44		14:56:13		13:53:00		m		59.98		1843.30

		S1148889054:		#B4q0		1148889054:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.65		3.62		0		-25094.42		14:56:43		13:53:30		m		60.02		1844.36

		S1148889084:		#B4q0		1148889084:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.60		3.64		3.65		3.62		0		-25095.54		14:57:13		13:54:00		m		60.05		1845.41

		S1148889114:		#B4q0		1148889114:		$B4q0		d-		29.19		4.30		27.92		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62		0		-25096.52		14:57:43		13:54:30		m		60.09		1846.46

		S1148889144:		#B4q0		1148889144:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62		0		-25097.65		14:58:13		13:55:00		m		60.12		1847.51

		S1148889174:		#B4q0		1148889174:		$B4q0		d-		29.23		4.33		27.92		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62		0		-25098.63		14:58:43		13:55:30		m		60.16		1848.57

		S1148889204:		#B4q0		1148889204:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.61		0		-25099.75		14:59:13		13:56:00		m		60.20		1849.62

		S1148889234:		#B4q0		1148889234:		$B4q0		d-		29.15		4.26		27.92		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.61		0		-25100.73		14:59:43		13:56:30		m		60.23		1850.66

		S1148889264:		#B4q0		1148889264:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.58		3.64		3.65		3.61		0		-25101.86		15:00:13		13:57:00		m		60.27		1851.71

		S1148889294:		#B4q0		1148889294:		$B4q0		d-		29.19		4.33		27.92		3.67		3.67		3.67		3.63		3.58		3.64		3.65		3.61		0		-25102.84		15:00:43		13:57:30		m		60.30		1852.76

		S1148889324:		#B4q0		1148889324:		$B4q0		d-		29.19		4.33		28.02		3.67		3.67		3.67		3.62		3.58		3.64		3.65		3.61		0		-25103.96		15:01:13		13:58:00		m		60.34		1853.81

		S1148889354:		#B4q0		1148889354:		$B4q0		d-		29.15		4.33		27.92		3.67		3.67		3.67		3.62		3.58		3.64		3.65		3.61		0		-25104.94		15:01:43		13:58:30		m		60.38		1854.87

		S1148889384:		#B4q0		1148889384:		$B4q0		d-		29.15		4.33		27.92		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.61		0		-25106.07		15:02:13		13:59:00		m		60.41		1855.92

		S1148889414:		#B4q0		1148889414:		$B4q0		d-		29.15		4.33		27.92		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.60		0		-25107.05		15:02:43		13:59:30		m		60.45		1856.97

		S1148889444:		#B4q0		1148889444:		$B4q0		d-		29.15		4.30		27.92		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.60		0		-25108.17		15:03:13		14:00:00		m		60.48		1858.02

		S1148889474:		#B4q0		1148889474:		$B4q0		d-		29.15		4.33		27.92		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.60		0		-25109.15		15:03:43		14:00:30		m		60.52		1859.07

		S1148889504:		#B4q0		1148889504:		$B4q0		d-		29.15		4.33		27.92		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.60		0		-25110.27		15:04:13		14:01:00		m		60.56		1860.12

		S1148889534:		#B4q0		1148889534:		$B4q0		d-		29.11		4.30		27.92		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.60		0		-25111.25		15:04:43		14:01:30		m		60.59		1861.17

		S1148889564:		#B4q0		1148889564:		$B4q0		d-		29.11		4.30		27.92		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.60		0		-25112.37		15:05:13		14:02:00		m		60.63		1862.21

		S1148889594:		#B4q0		1148889594:		$B4q0		d-		29.15		4.33		27.92		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.60		0		-25113.35		15:05:43		14:02:30		m		60.66		1863.26

		S1148889624:		#B4q0		1148889624:		$B4q0		d-		29.11		4.33		27.92		3.67		3.66		3.66		3.62		3.57		3.64		3.65		3.60		0		-25114.48		15:06:13		14:03:00		m		60.70		1864.31

		S1148889654:		#B4q0		1148889654:		$B4q0		d-		29.11		4.33		27.92		3.67		3.66		3.66		3.62		3.57		3.64		3.65		3.60		0		-25115.46		15:06:43		14:03:30		m		60.74		1865.36

		S1148889684:		#B4q0		1148889684:		$B4q0		d-		29.11		4.33		27.92		3.67		3.66		3.66		3.62		3.56		3.64		3.65		3.59		0		-25116.58		15:07:13		14:04:00		m		60.77		1866.41

		S1148889714:		#B4q0		1148889714:		$B4q0		d-		29.08		4.33		27.92		3.67		3.66		3.66		3.62		3.56		3.64		3.65		3.59		0		-25117.56		15:07:43		14:04:30		m		60.81		1867.46

		S1148889744:		#B4q0		1148889744:		$B4q0		d-		29.11		4.33		27.92		3.66		3.66		3.66		3.62		3.56		3.64		3.65		3.59		0		-25118.68		15:08:13		14:05:00		m		60.84		1868.51

		S1148889774:		#B4q0		1148889774:		$B4q0		d-		29.11		4.33		27.92		3.66		3.66		3.66		3.62		3.56		3.64		3.65		3.59		0		-25119.66		15:08:43		14:05:30		m		60.88		1869.56

		S1148889804:		#B4q0		1148889804:		$B4q0		d-		29.08		4.33		27.92		3.66		3.66		3.66		3.62		3.55		3.64		3.64		3.59		0		-25120.78		15:09:13		14:06:00		m		60.92		1870.61

		S1148889834:		#B4q0		1148889834:		$B4q0		d-		29.08		4.30		27.92		3.66		3.66		3.66		3.62		3.55		3.63		3.65		3.58		0		-25121.76		15:09:43		14:06:30		m		60.95		1871.65

		S1148889864:		#B4q0		1148889864:		$B4q0		d-		29.08		4.30		27.92		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58		0		-25122.88		15:10:13		14:07:00		m		60.99		1872.70

		S1148889894:		#B4q0		1148889894:		$B4q0		d-		29.04		4.30		27.92		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58		0		-25123.85		15:10:43		14:07:30		m		61.02		1873.74

		S1148889924:		#B4q0		1148889924:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58		0		-25124.97		15:11:13		14:08:00		m		61.06		1874.78

		S1148889954:		#B4q0		1148889954:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58		0		-25125.95		15:11:43		14:08:30		m		61.10		1875.83

		S1148889984:		#B4q0		1148889984:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58		0		-25127.07		15:12:13		14:09:00		m		61.13		1876.88

		S1148890014:		#B4q0		1148890014:		$B4q0		d-		29.04		4.37		27.92		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58		0		-25128.05		15:12:43		14:09:30		m		61.17		1877.93

		S1148890044:		#B4q0		1148890044:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.57		0		-25129.17		15:13:13		14:10:00		m		61.20		1878.98

		S1148890074:		#B4q0		1148890074:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57		0		-25130.15		15:13:43		14:10:30		m		61.24		1880.03

		S1148890104:		#B4q0		1148890104:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57		0		-25131.26		15:14:13		14:11:00		m		61.28		1881.08

		S1148890134:		#B4q0		1148890134:		$B4q0		d-		29.00		4.33		27.92		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57		0		-25132.24		15:14:43		14:11:30		m		61.31		1882.13

		S1148890164:		#B4q0		1148890164:		$B4q0		d-		29.00		4.33		27.92		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57		0		-25133.36		15:15:13		14:12:00		m		61.35		1883.17

		S1148890194:		#B4q0		1148890194:		$B4q0		d-		29.04		4.33		27.92		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57		0		-25134.34		15:15:43		14:12:30		m		61.38		1884.22

		S1148890224:		#B4q0		1148890224:		$B4q0		d-		29.00		4.30		27.92		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57		0		-25135.45		15:16:13		14:13:00		m		61.42		1885.26

		S1148890254:		#B4q0		1148890254:		$B4q0		d-		29.04		4.37		27.92		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56		0		-25136.42		15:16:43		14:13:30		m		61.46		1886.31

		S1148890284:		#B4q0		1148890284:		$B4q0		d-		29.00		4.37		27.92		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56		0		-25137.54		15:17:13		14:14:00		m		61.49		1887.37

		S1148890314:		#B4q0		1148890314:		$B4q0		d-		29.00		4.33		27.92		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56		0		-25138.52		15:17:43		14:14:30		m		61.53		1888.42

		S1148890344:		#B4q0		1148890344:		$B4q0		d-		29.00		4.33		27.92		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.56		0		-25139.64		15:18:13		14:15:00		m		61.57		1889.47

		S1148890374:		#B4q0		1148890374:		$B4q0		d-		29.00		4.33		27.92		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.56		0		-25140.61		15:18:43		14:15:30		m		61.60		1890.51

		S1148890404:		#B4q0		1148890404:		$B4q0		d-		28.96		4.33		27.92		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.55		0		-25141.73		15:19:13		14:16:00		m		61.64		1891.56

		S1148890434:		#B4q0		1148890434:		$B4q0		d-		28.96		4.30		27.92		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.55		0		-25142.71		15:19:43		14:16:30		m		61.67		1892.60

		S1148890464:		#B4q0		1148890464:		$B4q0		d-		28.96		4.33		27.92		3.66		3.66		3.66		3.60		3.51		3.63		3.64		3.55		0		-25143.82		15:20:13		14:17:00		m		61.71		1893.64

		S1148890494:		#B4q0		1148890494:		$B4q0		d-		28.96		4.33		27.92		3.66		3.66		3.66		3.60		3.50		3.63		3.64		3.55		0		-25144.79		15:20:43		14:17:30		m		61.75		1894.69

		S1148890524:		#B4q0		1148890524:		$B4q0		d-		28.96		4.30		27.92		3.66		3.66		3.66		3.60		3.50		3.63		3.64		3.55		0		-25145.91		15:21:13		14:18:00		m		61.78		1895.73

		S1148890554:		#B4q0		1148890554:		$B4q0		d-		28.96		4.26		27.92		3.66		3.66		3.66		3.60		3.50		3.63		3.64		3.55		0		-25146.88		15:21:43		14:18:30		m		61.82		1896.76

		S1148890584:		#B4q0		1148890584:		$B4q0		d-		28.92		4.33		27.92		3.66		3.66		3.66		3.60		3.50		3.63		3.64		3.54		0		-25148		15:22:13		14:19:00		m		61.85		1897.80

		S1148890614:		#B4q0		1148890614:		$B4q0		d-		28.96		4.26		27.92		3.66		3.66		3.66		3.60		3.49		3.63		3.64		3.54		0		-25148.97		15:22:43		14:19:30		m		61.89		1898.83

		S1148890644:		#B4q0		1148890644:		$B4q0		d-		28.89		4.37		27.92		3.66		3.66		3.66		3.60		3.49		3.63		3.64		3.54		0		-25150.08		15:23:13		14:20:00		m		61.93		1899.87

		S1148890674:		#B4q0		1148890674:		$B4q0		d-		28.92		4.33		27.92		3.66		3.66		3.66		3.60		3.49		3.63		3.64		3.54		0		-25151.06		15:23:43		14:20:30		m		61.96		1900.92

		S1148890704:		#B4q0		1148890704:		$B4q0		d-		28.92		4.33		27.92		3.66		3.66		3.66		3.60		3.48		3.63		3.64		3.53		0		-25152.17		15:24:13		14:21:00		m		62.00		1901.96

		S1148890734:		#B4q0		1148890734:		$B4q0		d-		28.89		4.33		27.92		3.66		3.66		3.66		3.60		3.48		3.63		3.64		3.53		0		-25153.15		15:24:43		14:21:30		m		62.03		1903.01

		S1148890764:		#B4q0		1148890764:		$B4q0		d-		28.92		4.33		27.92		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53		0		-25154.26		15:25:13		14:22:00		m		62.07		1904.05

		S1148890794:		#B4q0		1148890794:		$B4q0		d-		28.89		4.33		27.92		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53		0		-25155.23		15:25:43		14:22:30		m		62.11		1905.09

		S1148890824:		#B4q0		1148890824:		$B4q0		d-		28.89		4.30		27.92		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53		0		-25156.35		15:26:13		14:23:00		m		62.14		1906.13

		S1148890854:		#B4q0		1148890854:		$B4q0		d-		28.89		4.30		27.92		3.66		3.66		3.66		3.59		3.47		3.63		3.64		3.53		0		-25157.32		15:26:43		14:23:30		m		62.18		1907.17

		S1148890884:		#B4q0		1148890884:		$B4q0		d-		28.89		4.33		27.92		3.66		3.65		3.66		3.59		3.47		3.63		3.64		3.52		0		-25158.43		15:27:13		14:24:00		m		62.21		1908.20

		S1148890914:		#B4q0		1148890914:		$B4q0		d-		28.89		4.33		27.92		3.66		3.65		3.66		3.59		3.47		3.63		3.64		3.52		0		-25159.41		15:27:43		14:24:30		m		62.25		1909.25

		S1148890944:		#B4q0		1148890944:		$B4q0		d-		28.89		4.33		27.92		3.66		3.65		3.66		3.58		3.46		3.63		3.64		3.52		0		-25160.52		15:28:13		14:25:00		m		62.29		1910.29

		S1148890974:		#B4q0		1148890974:		$B4q0		d-		28.85		4.33		27.92		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.52		0		-25161.49		15:28:43		14:25:30		m		62.32		1911.33

		S1148891004:		#B4q0		1148891004:		$B4q0		d-		28.81		4.33		27.92		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.51		0		-25162.6		15:29:13		14:26:00		m		62.36		1912.37

		S1148891034:		#B4q0		1148891034:		$B4q0		d-		28.85		4.33		27.92		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.51		0		-25163.57		15:29:43		14:26:30		m		62.39		1913.41

		S1148891064:		#B4q0		1148891064:		$B4q0		d-		28.81		4.33		27.92		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51		0		-25164.68		15:30:13		14:27:00		m		62.43		1914.45

		S1148891094:		#B4q0		1148891094:		$B4q0		d-		28.81		4.33		27.92		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51		0		-25165.65		15:30:43		14:27:30		m		62.47		1915.49

		S1148891124:		#B4q0		1148891124:		$B4q0		d-		28.81		4.33		27.92		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51		0		-25166.76		15:31:13		14:28:00		m		62.50		1916.53

		S1148891154:		#B4q0		1148891154:		$B4q0		d-		28.81		4.30		27.92		3.65		3.65		3.65		3.58		3.44		3.62		3.64		3.50		0		-25167.73		15:31:43		14:28:30		m		62.54		1917.57

		S1148891184:		#B4q0		1148891184:		$B4q0		d-		28.81		4.30		27.92		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.50		0		-25168.84		15:32:13		14:29:00		m		62.57		1918.60

		S1148891214:		#B4q0		1148891214:		$B4q0		d-		28.77		4.33		27.92		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.50		0		-25169.81		15:32:43		14:29:30		m		62.61		1919.63

		S1148891244:		#B4q0		1148891244:		$B4q0		d-		28.77		4.33		27.92		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.50		0		-25170.91		15:33:13		14:30:00		m		62.65		1920.67

		S1148891274:		#B4q0		1148891274:		$B4q0		d-		28.77		4.33		27.92		3.65		3.65		3.65		3.57		3.43		3.62		3.64		3.50		0		-25171.88		15:33:43		14:30:30		m		62.68		1921.71

		S1148891304:		#B4q0		1148891304:		$B4q0		d-		28.74		4.33		27.92		3.65		3.65		3.65		3.57		3.43		3.62		3.64		3.49		0		-25172.99		15:34:13		14:31:00		m		62.72		1922.75

		S1148891334:		#B4q0		1148891334:		$B4q0		d-		28.74		4.33		27.92		3.65		3.65		3.65		3.57		3.42		3.62		3.64		3.49		0		-25173.96		15:34:43		14:31:30		m		62.75		1923.79

		S1148891364:		#B4q0		1148891364:		$B4q0		d-		28.74		4.33		27.92		3.65		3.65		3.65		3.57		3.42		3.62		3.64		3.49		0		-25175.06		15:35:13		14:32:00		m		62.79		1924.82

		S1148891394:		#B4q0		1148891394:		$B4q0		d-		28.74		4.33		27.92		3.65		3.65		3.65		3.56		3.42		3.62		3.64		3.48		0		-25176.03		15:35:43		14:32:30		m		62.83		1925.86

		S1148891424:		#B4q0		1148891424:		$B4q0		d-		28.70		4.33		27.92		3.65		3.65		3.65		3.56		3.42		3.62		3.64		3.48		0		-25177.13		15:36:13		14:33:00		m		62.86		1926.90

		S1148891454:		#B4q0		1148891454:		$B4q0		d-		28.70		4.33		27.92		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48		0		-25178.1		15:36:43		14:33:30		m		62.90		1927.93

		S1148891484:		#B4q0		1148891484:		$B4q0		d-		28.70		4.33		27.92		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48		0		-25179.21		15:37:13		14:34:00		m		62.93		1928.97

		S1148891514:		#B4q0		1148891514:		$B4q0		d-		28.70		4.33		27.92		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48		0		-25180.17		15:37:43		14:34:30		m		62.97		1930.00

		S1148891544:		#B4q0		1148891544:		$B4q0		d-		28.66		4.33		27.92		3.65		3.65		3.65		3.55		3.40		3.62		3.64		3.47		0		-25181.28		15:38:13		14:35:00		m		63.01		1931.04

		S1148891574:		#B4q0		1148891574:		$B4q0		d-		28.66		4.30		27.92		3.65		3.65		3.65		3.55		3.40		3.62		3.64		3.47		0		-25182.25		15:38:43		14:35:30		m		63.04		1932.07

		S1148891604:		#B4q0		1148891604:		$B4q0		d-		28.66		4.30		27.92		3.65		3.65		3.65		3.55		3.39		3.62		3.64		3.47		0		-25183.35		15:39:13		14:36:00		m		63.08		1933.09

		S1148891634:		#B4q0		1148891634:		$B4q0		d-		28.66		4.33		27.92		3.65		3.64		3.65		3.55		3.39		3.61		3.64		3.46		0		-25184.32		15:39:43		14:36:30		m		63.11		1934.13

		S1148891664:		#B4q0		1148891664:		$B4q0		d-		28.62		4.30		27.92		3.65		3.64		3.65		3.55		3.39		3.61		3.64		3.46		0		-25185.42		15:40:13		14:37:00		m		63.15		1935.16

		S1148891694:		#B4q0		1148891694:		$B4q0		d-		28.62		4.33		27.92		3.65		3.65		3.65		3.55		3.39		3.61		3.64		3.46		0		-25186.38		15:40:43		14:37:30		m		63.19		1936.18

		S1148891724:		#B4q0		1148891724:		$B4q0		d-		28.62		4.33		27.92		3.65		3.64		3.65		3.55		3.38		3.61		3.64		3.46		0		-25187.49		15:41:13		14:38:00		m		63.22		1937.22

		S1148891754:		#B4q0		1148891754:		$B4q0		d-		28.62		4.33		27.92		3.65		3.64		3.65		3.55		3.38		3.61		3.64		3.45		0		-25188.45		15:41:43		14:38:30		m		63.26		1938.25

		S1148891784:		#B4q0		1148891784:		$B4q0		d-		28.62		4.33		27.92		3.65		3.64		3.65		3.55		3.37		3.61		3.64		3.45		0		-25189.55		15:42:13		14:39:00		m		63.29		1939.28

		S1148891814:		#B4q0		1148891814:		$B4q0		d-		28.58		4.30		27.92		3.65		3.64		3.65		3.55		3.37		3.61		3.64		3.45		0		-25190.51		15:42:43		14:39:30		m		63.33		1940.31

		S1148891844:		#B4q0		1148891844:		$B4q0		d-		28.58		4.30		27.92		3.65		3.64		3.65		3.54		3.36		3.61		3.64		3.44		0		-25191.61		15:43:13		14:40:00		m		63.37		1941.34

		S1148891874:		#B4q0		1148891874:		$B4q0		d-		28.58		4.33		27.92		3.65		3.64		3.65		3.54		3.36		3.61		3.64		3.44		0		-25192.58		15:43:43		14:40:30		m		63.40		1942.36

		S1148891904:		#B4q0		1148891904:		$B4q0		d-		28.58		4.33		27.92		3.65		3.64		3.65		3.54		3.35		3.60		3.64		3.44		0		-25193.68		15:44:13		14:41:00		m		63.44		1943.39

		S1148891934:		#B4q0		1148891934:		$B4q0		d-		28.58		4.33		27.92		3.65		3.64		3.64		3.54		3.35		3.60		3.64		3.44		0		-25194.64		15:44:43		14:41:30		m		63.47		1944.43

		S1148891964:		#B4q0		1148891964:		$B4q0		d-		28.55		4.30		27.92		3.65		3.64		3.64		3.54		3.35		3.60		3.64		3.43		0		-25195.74		15:45:13		14:42:00		m		63.51		1945.45

		S1148891994:		#B4q0		1148891994:		$B4q0		d-		28.55		4.33		27.92		3.65		3.64		3.64		3.54		3.34		3.60		3.64		3.43		0		-25196.7		15:45:43		14:42:30		m		63.55		1946.48

		S1148892024:		#B4q0		1148892024:		$B4q0		d-		28.51		4.33		27.92		3.64		3.64		3.64		3.53		3.34		3.60		3.63		3.42		0		-25197.8		15:46:13		14:43:00		m		63.58		1947.51

		S1148892054:		#B4q0		1148892054:		$B4q0		d-		28.51		4.33		27.92		3.64		3.64		3.64		3.53		3.33		3.60		3.63		3.42		0		-25198.76		15:46:43		14:43:30		m		63.62		1948.54

		S1148892084:		#B4q0		1148892084:		$B4q0		d-		28.47		4.33		27.92		3.64		3.64		3.64		3.53		3.33		3.60		3.63		3.42		0		-25199.85		15:47:13		14:44:00		m		63.65		1949.57

		S1148892114:		#B4q0		1148892114:		$B4q0		d-		28.51		4.33		27.92		3.64		3.64		3.64		3.53		3.32		3.60		3.63		3.42		0		-25200.81		15:47:43		14:44:30		m		63.69		1950.59

		S1148892144:		#B4q0		1148892144:		$B4q0		d-		28.47		4.33		27.92		3.64		3.64		3.64		3.53		3.32		3.60		3.63		3.42		0		-25201.91		15:48:13		14:45:00		m		63.73		1951.62

		S1148892174:		#B4q0		1148892174:		$B4q0		d-		28.47		4.33		27.92		3.64		3.64		3.64		3.53		3.31		3.59		3.63		3.42		0		-25202.87		15:48:43		14:45:30		m		63.76		1952.65

		S1148892204:		#B4q0		1148892204:		$B4q0		d-		28.43		4.41		27.92		3.64		3.64		3.64		3.52		3.31		3.59		3.63		3.41		0		-25203.96		15:49:13		14:46:00		m		63.80		1953.68

		S1148892234:		#B4q0		1148892234:		$B4q0		d-		28.47		4.33		27.92		3.64		3.64		3.64		3.52		3.30		3.59		3.63		3.41		0		-25204.92		15:49:43		14:46:30		m		63.84		1954.72

		S1148892264:		#B4q0		1148892264:		$B4q0		d-		28.43		4.37		27.92		3.64		3.64		3.64		3.52		3.30		3.59		3.63		3.41		0		-25206.02		15:50:13		14:47:00		m		63.87		1955.75

		S1148892294:		#B4q0		1148892294:		$B4q0		d-		28.43		4.33		27.92		3.64		3.64		3.64		3.52		3.29		3.59		3.63		3.41		0		-25206.97		15:50:43		14:47:30		m		63.91		1956.78

		S1148892324:		#B4q0		1148892324:		$B4q0		d-		28.39		4.33		27.92		3.64		3.64		3.64		3.52		3.28		3.59		3.63		3.40		0		-25208.07		15:51:13		14:48:00		m		63.94		1957.81

		S1148892354:		#B4q0		1148892354:		$B4q0		d-		28.39		4.30		27.92		3.64		3.64		3.64		3.51		3.28		3.58		3.63		3.40		0		-25209.02		15:51:43		14:48:30		m		63.98		1958.83

		S1148892384:		#B4q0		1148892384:		$B4q0		d-		28.39		4.33		27.92		3.64		3.64		3.64		3.51		3.27		3.58		3.63		3.39		0		-25210.12		15:52:13		14:49:00		m		64.02		1959.85

		S1148892414:		#B4q0		1148892414:		$B4q0		d-		28.36		4.33		27.92		3.64		3.64		3.64		3.51		3.26		3.58		3.63		3.39		0		-25211.07		15:52:43		14:49:30		m		64.05		1960.87

		S1148892444:		#B4q0		1148892444:		$B4q0		d-		28.36		4.30		27.92		3.64		3.64		3.64		3.51		3.26		3.58		3.63		3.39		0		-25212.16		15:53:13		14:50:00		m		64.09		1961.89

		S1148892474:		#B4q0		1148892474:		$B4q0		d-		28.36		4.33		27.92		3.64		3.64		3.64		3.51		3.25		3.58		3.63		3.39		0		-25213.12		15:53:43		14:50:30		m		64.12		1962.91

		S1148892504:		#B4q0		1148892504:		$B4q0		d-		28.32		4.33		27.92		3.64		3.64		3.64		3.51		3.24		3.58		3.63		3.38		0		-25214.21		15:54:13		14:51:00		m		64.16		1963.94

		S1148892534:		#B4q0		1148892534:		$B4q0		d-		28.28		4.30		27.92		3.64		3.64		3.64		3.51		3.23		3.58		3.63		3.38		0		-25215.16		15:54:43		14:51:30		m		64.20		1964.95

		S1148892564:		#B4q0		1148892564:		$B4q0		d-		28.32		4.30		27.92		3.64		3.64		3.64		3.51		3.23		3.58		3.63		3.37		0		-25216.25		15:55:13		14:52:00		m		64.23		1965.97

		S1148892594:		#B4q0		1148892594:		$B4q0		d-		28.28		4.33		27.92		3.64		3.64		3.64		3.50		3.22		3.57		3.63		3.37		0		-25217.2		15:55:43		14:52:30		m		64.27		1966.98

		S1148892624:		#B4q0		1148892624:		$B4q0		d-		28.25		4.33		27.92		3.64		3.64		3.64		3.50		3.21		3.57		3.63		3.37		0		-25218.29		15:56:13		14:53:00		m		64.30		1968.00

		S1148892654:		#B4q0		1148892654:		$B4q0		d-		28.28		4.30		27.92		3.64		3.64		3.64		3.50		3.21		3.57		3.63		3.37		0		-25219.24		15:56:43		14:53:30		m		64.34		1969.02

		S1148892684:		#B4q0		1148892684:		$B4q0		d-		28.25		4.33		27.92		3.64		3.64		3.64		3.50		3.20		3.57		3.63		3.36		0		-25220.33		15:57:13		14:54:00		m		64.38		1970.04

		S1148892714:		#B4q0		1148892714:		$B4q0		d-		28.21		4.33		27.92		3.64		3.64		3.64		3.50		3.19		3.57		3.63		3.36		0		-25221.28		15:57:43		14:54:30		m		64.41		1971.06

		S1148892744:		#B4q0		1148892744:		$B4q0		d-		28.21		4.33		27.92		3.64		3.64		3.64		3.50		3.18		3.57		3.63		3.35		0		-25222.37		15:58:13		14:55:00		m		64.45		1972.07

		S1148892774:		#B4q0		1148892774:		$B4q0		d-		28.21		4.33		27.92		3.64		3.64		3.64		3.49		3.17		3.57		3.63		3.35		0		-25223.32		15:58:43		14:55:30		m		64.48		1973.09

		S1148892804:		#B4q0		1148892804:		$B4q0		d-		28.13		4.33		27.92		3.64		3.64		3.64		3.49		3.16		3.57		3.63		3.35		0		-25224.4		15:59:13		14:56:00		m		64.52		1974.11

		S1148892834:		#B4q0		1148892834:		$B4q0		d-		28.13		4.33		27.92		3.64		3.64		3.64		3.49		3.16		3.56		3.63		3.34		0		-25225.35		15:59:43		14:56:30		m		64.56		1975.12

		S1148892864:		#B4q0		1148892864:		$B4q0		d-		28.13		4.33		27.92		3.64		3.64		3.64		3.49		3.15		3.56		3.63		3.34		0		-25226.44		16:00:13		14:57:00		m		64.59		1976.14

		S1148892894:		#B4q0		1148892894:		$B4q0		d-		28.13		4.33		27.92		3.64		3.64		3.64		3.48		3.14		3.56		3.63		3.33		0		-25227.38		16:00:43		14:57:30		m		64.63		1977.15

		S1148892924:		#B4q0		1148892924:		$B4q0		fc		28.28		0.00		27.92		3.66		3.66		3.66		3.51		3.17		3.58		3.65		3.36		0		-25228.06		16:01:13		14:58:00		m		64.63		1977.66

		S1148892954:		#B4q0		1148892954:		$B4q0		fc		28.32		0.00		27.92		3.66		3.66		3.66		3.51		3.17		3.58		3.65		3.36		0		-25228.06		16:01:43		14:58:30		m		64.63		1977.66

		S1148892984:		#B4q0		1148892984:		$B4q0		fc		28.36		0.00		27.83		3.67		3.66		3.66		3.51		3.18		3.58		3.65		3.37		0		-25228.06		16:02:13		14:59:00		m		64.63		1977.66

		S1148893014:		#B4q0		1148893014:		$B4q0		fc		28.36		0.00		27.83		3.67		3.66		3.66		3.51		3.19		3.58		3.65		3.37		0		-25228.06		16:02:43		14:59:30		m		64.63		1977.66

		S1148893044:		#B4q0		1148893044:		$B4q0		fc		28.36		0.00		27.83		3.67		3.66		3.67		3.51		3.19		3.59		3.65		3.37		0		-25228.06		16:03:13		15:00:00		m		64.63		1977.66

		S1148893074:		#B4q0		1148893074:		$B4q0		fc		28.36		0.00		27.83		3.67		3.66		3.67		3.52		3.20		3.59		3.66		3.37		0		-25228.06		16:03:43		15:00:30		m		64.63		1977.66

		S1148893104:		#B4q0		1148893104:		$B4q0		fc		28.36		0.00		27.83		3.67		3.66		3.67		3.52		3.20		3.59		3.66		3.37		0		-25228.06		16:04:13		15:01:00		m		64.63		1977.66

		S1148893134:		#B4q0		1148893134:		$B4q0		fc		28.39		0.00		27.83		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.37		0		-25228.06		16:04:43		15:01:30		m		64.63		1977.66

		S1148893164:		#B4q0		1148893164:		$B4q0		fc		28.39		0.00		27.83		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.38		0		-25228.06		16:05:13		15:02:00		m		64.63		1977.66

		S1148893194:		#B4q0		1148893194:		$B4q0		fc		28.39		0.00		27.83		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.38		0		-25228.06		16:05:43		15:02:30		m		64.63		1977.66

		S1148893224:		#B4q0		1148893224:		$B4q0		fc		28.39		0.00		27.73		3.67		3.66		3.67		3.52		3.22		3.59		3.66		3.38		0		-25228.06		16:06:13		15:03:00		m		64.63		1977.66

		S1148893254:		#B4q0		1148893254:		$B4q0		fc		28.39		0.00		27.73		3.67		3.67		3.67		3.52		3.22		3.59		3.66		3.38		0		-25228.06		16:06:43		15:03:30		m		64.63		1977.66

		S1148893284:		#B4q0		1148893284:		$B4q0		fc		28.43		0.00		27.73		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.38		0		-25228.06		16:07:13		15:04:00		m		64.63		1977.66

		S1148893314:		#B4q0		1148893314:		$B4q0		fc		28.43		0.00		27.73		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.38		0		-25228.06		16:07:43		15:04:30		m		64.63		1977.66

		S1148893344:		#B4q0		1148893344:		$B4q0		fc		28.43		0.00		27.73		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.39		0		-25228.06		16:08:13		15:05:00		m		64.63		1977.66

		S1148893374:		#B4q0		1148893374:		$B4q0		fc		28.43		0.00		27.73		3.67		3.66		3.67		3.53		3.23		3.59		3.66		3.39		0		-25228.06		16:08:43		15:05:30		m		64.63		1977.66

		S1148893404:		#B4q0		1148893404:		$B4q0		fc		28.43		0.00		27.73		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39		0		-25228.06		16:09:13		15:06:00		m		64.63		1977.66

		S1148893434:		#B4q0		1148893434:		$B4q0		fc		28.43		0.00		27.73		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39		0		-25228.06		16:09:43		15:06:30		m		64.63		1977.66

		S1148893464:		#B4q0		1148893464:		$B4q0		fc		28.43		0.00		27.63		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39		0		-25228.06		16:10:13		15:07:00		m		64.63		1977.66

		S1148893494:		#B4q0		1148893494:		$B4q0		fc		28.47		0.00		27.63		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39		0		-25228.06		16:10:43		15:07:30		m		64.63		1977.66

		S1148893524:		#B4q0		1148893524:		$B4q0		fc		28.47		0.00		27.63		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39		0		-25228.06		16:11:13		15:08:00		m		64.63		1977.66

		S1148893554:		#B4q0		1148893554:		$B4q0		fc		28.47		0.00		27.53		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39		0		-25228.06		16:11:43		15:08:30		m		64.63		1977.66

		S1148893584:		#B4q0		1148893584:		$B4q0		fc		28.47		0.00		27.63		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39		0		-25228.06		16:12:13		15:09:00		m		64.63		1977.66

		S1148893614:		#B4q0		1148893614:		$B4q0		fc		28.47		0.00		27.53		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39		0		-25228.06		16:12:43		15:09:30		m		64.63		1977.66

		S1148893644:		#B4q0		1148893644:		$B4q0		fc		28.47		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:13:13		15:10:00		m		64.63		1977.66

		S1148893674:		#B4q0		1148893674:		$B4q0		fc		28.51		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:13:43		15:10:30		m		64.63		1977.66

		S1148893704:		#B4q0		1148893704:		$B4q0		fc		28.47		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:14:13		15:11:00		m		64.63		1977.66

		S1148893734:		#B4q0		1148893734:		$B4q0		fc		28.51		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:14:43		15:11:30		m		64.63		1977.66

		S1148893764:		#B4q0		1148893764:		$B4q0		fc		28.51		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:15:13		15:12:00		m		64.63		1977.66

		S1148893794:		#B4q0		1148893794:		$B4q0		fc		28.47		0.00		27.53		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.40		0		-25228.06		16:15:43		15:12:30		m		64.63		1977.66

		S1148893824:		#B4q0		1148893824:		$B4q0		fc		28.51		0.00		27.53		3.67		3.67		3.67		3.53		3.27		3.60		3.66		3.40		0		-25228.06		16:16:13		15:13:00		m		64.63		1977.66

		S1148893854:		#B4q0		1148893854:		$B4q0		fc		28.51		0.00		27.53		3.67		3.67		3.67		3.53		3.28		3.60		3.66		3.40		0		-25228.06		16:16:43		15:13:30		m		64.63		1977.66

		S1148893884:		#B4q0		1148893884:		$B4q0		fc		28.51		0.00		27.44		3.67		3.67		3.67		3.53		3.28		3.60		3.66		3.41		0		-25228.06		16:17:13		15:14:00		m		64.63		1977.66

		S1148893914:		#B4q0		1148893914:		$B4q0		fc		28.51		0.00		27.44		3.67		3.67		3.67		3.53		3.28		3.60		3.66		3.41		0		-25228.06		16:17:43		15:14:30		m		64.63		1977.66

		S1148893944:		#B4q0		1148893944:		$B4q0		fc		28.55		0.00		27.44		3.67		3.67		3.67		3.53		3.29		3.60		3.66		3.41		0		-25228.06		16:18:13		15:15:00		m		64.63		1977.66

		S1148893974:		#B4q0		1148893974:		$B4q0		fc		28.55		0.00		27.44		3.67		3.67		3.67		3.53		3.29		3.60		3.66		3.41		0		-25228.06		16:18:43		15:15:30		m		64.63		1977.66

		S1148894004:		#B4q0		1148894004:		$B4q0		fc		28.55		0.00		27.44		3.67		3.67		3.67		3.54		3.29		3.60		3.66		3.41		0		-25228.06		16:19:13		15:16:00		m		64.63		1977.66

		S1148894034:		#B4q0		1148894034:		$B4q0		fc		28.55		0.00		27.44		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:19:43		15:16:30		m		64.63		1977.66

		S1148894064:		#B4q0		1148894064:		$B4q0		fc		28.55		0.00		27.44		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:20:13		15:17:00		m		64.63		1977.66

		S1148894094:		#B4q0		1148894094:		$B4q0		fc		28.55		0.00		27.34		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:20:43		15:17:30		m		64.63		1977.66

		S1148894124:		#B4q0		1148894124:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:21:13		15:18:00		m		64.63		1977.66

		S1148894154:		#B4q0		1148894154:		$B4q0		fc		28.55		0.00		27.34		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:21:43		15:18:30		m		64.63		1977.66

		S1148894184:		#B4q0		1148894184:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.30		3.60		3.66		3.41		0		-25228.06		16:22:13		15:19:00		m		64.63		1977.66

		S1148894214:		#B4q0		1148894214:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.31		3.60		3.66		3.41		0		-25228.06		16:22:43		15:19:30		m		64.63		1977.66

		S1148894244:		#B4q0		1148894244:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.31		3.60		3.66		3.41		0		-25228.06		16:23:13		15:20:00		m		64.63		1977.66

		S1148894274:		#B4q0		1148894274:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.31		3.60		3.66		3.41		0		-25228.06		16:23:43		15:20:30		m		64.63		1977.66

		S1148894304:		#B4q0		1148894304:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.31		3.60		3.66		3.42		0		-25228.06		16:24:13		15:21:00		m		64.63		1977.66

		S1148894334:		#B4q0		1148894334:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.32		3.60		3.66		3.42		0		-25228.06		16:24:43		15:21:30		m		64.63		1977.66

		S1148894364:		#B4q0		1148894364:		$B4q0		fc		28.58		0.00		27.34		3.67		3.67		3.67		3.54		3.32		3.60		3.66		3.42		0		-25228.06		16:25:13		15:22:00		m		64.63		1977.66

		S1148894394:		#B4q0		1148894394:		$B4q0		fc		28.58		0.00		27.24		3.67		3.67		3.67		3.54		3.33		3.60		3.66		3.42		0		-25228.06		16:25:43		15:22:30		m		64.63		1977.66

		S1148894424:		#B4q0		1148894424:		$B4q0		fc		28.58		0.00		27.24		3.67		3.67		3.67		3.54		3.33		3.60		3.66		3.42		0		-25228.06		16:26:13		15:23:00		m		64.63		1977.66

		S1148894454:		#B4q0		1148894454:		$B4q0		fc		28.58		0.00		27.24		3.67		3.67		3.67		3.54		3.33		3.60		3.66		3.42		0		-25228.06		16:26:43		15:23:30		m		64.63		1977.66

		S1148894484:		#B4q0		1148894484:		$B4q0		fc		28.58		0.00		27.24		3.67		3.67		3.67		3.54		3.34		3.60		3.66		3.42		0		-25228.06		16:27:13		15:24:00		m		64.63		1977.66

		S1148894514:		#B4q0		1148894514:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.54		3.34		3.60		3.66		3.42		0		-25228.06		16:27:43		15:24:30		m		64.63		1977.66

		S1148894544:		#B4q0		1148894544:		$B4q0		fc		28.58		0.00		27.24		3.67		3.67		3.67		3.54		3.34		3.60		3.66		3.42		0		-25228.06		16:28:13		15:25:00		m		64.63		1977.66

		S1148894574:		#B4q0		1148894574:		$B4q0		fc		28.58		0.00		27.14		3.67		3.67		3.67		3.55		3.35		3.60		3.66		3.42		0		-25228.06		16:28:43		15:25:30		m		64.63		1977.66

		S1148894604:		#B4q0		1148894604:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.35		3.60		3.66		3.42		0		-25228.06		16:29:13		15:26:00		m		64.63		1977.66

		S1148894634:		#B4q0		1148894634:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.35		3.60		3.66		3.42		0		-25228.06		16:29:43		15:26:30		m		64.63		1977.66

		S1148894664:		#B4q0		1148894664:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.35		3.60		3.66		3.42		0		-25228.06		16:30:13		15:27:00		m		64.63		1977.66

		S1148894694:		#B4q0		1148894694:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.36		3.60		3.66		3.43		0		-25228.06		16:30:43		15:27:30		m		64.63		1977.66

		S1148894724:		#B4q0		1148894724:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.36		3.60		3.66		3.43		0		-25228.06		16:31:13		15:28:00		m		64.63		1977.66

		S1148894754:		#B4q0		1148894754:		$B4q0		fc		28.62		0.00		27.14		3.67		3.67		3.67		3.55		3.36		3.60		3.66		3.43		0		-25228.06		16:31:43		15:28:30		m		64.63		1977.66

		S1148894784:		#B4q0		1148894784:		$B4q0		fc		28.66		0.00		27.14		3.67		3.67		3.67		3.55		3.36		3.60		3.66		3.43		0		-25228.06		16:32:13		15:29:00		m		64.63		1977.66

		S1148894814:		#B4q0		1148894814:		$B4q0		fc		28.66		0.00		27.14		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:32:43		15:29:30		m		64.63		1977.66

		S1148894844:		#B4q0		1148894844:		$B4q0		fc		28.66		0.00		27.14		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:33:13		15:30:00		m		64.63		1977.66

		S1148894874:		#B4q0		1148894874:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:33:43		15:30:30		m		64.63		1977.66

		S1148894904:		#B4q0		1148894904:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:34:13		15:31:00		m		64.63		1977.66

		S1148894934:		#B4q0		1148894934:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:34:43		15:31:30		m		64.63		1977.66

		S1148894964:		#B4q0		1148894964:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:35:13		15:32:00		m		64.63		1977.66

		S1148894994:		#B4q0		1148894994:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.37		3.60		3.66		3.43		0		-25228.06		16:35:43		15:32:30		m		64.63		1977.66

		S1148895024:		#B4q0		1148895024:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.38		3.60		3.66		3.43		0		-25228.06		16:36:13		15:33:00		m		64.63		1977.66

		S1148895054:		#B4q0		1148895054:		$B4q0		fc		28.66		0.00		27.05		3.67		3.67		3.67		3.55		3.38		3.60		3.66		3.43		0		-25228.06		16:36:43		15:33:30		m		64.63		1977.66

		S1148895084:		#B4q0		1148895084:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.38		3.60		3.66		3.44		0		-25228.06		16:37:13		15:34:00		m		64.63		1977.66

		S1148895114:		#B4q0		1148895114:		$B4q0		fc		28.66		0.00		26.95		3.67		3.67		3.67		3.55		3.38		3.60		3.66		3.44		0		-25228.06		16:37:43		15:34:30		m		64.63		1977.66

		S1148895144:		#B4q0		1148895144:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.38		3.60		3.66		3.44		0		-25228.06		16:38:13		15:35:00		m		64.63		1977.66

		S1148895174:		#B4q0		1148895174:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:38:43		15:35:30		m		64.63		1977.66

		S1148895204:		#B4q0		1148895204:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:39:13		15:36:00		m		64.63		1977.66

		S1148895234:		#B4q0		1148895234:		$B4q0		fc		28.66		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:39:43		15:36:30		m		64.63		1977.66

		S1148895264:		#B4q0		1148895264:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:40:13		15:37:00		m		64.63		1977.66

		S1148895294:		#B4q0		1148895294:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:40:43		15:37:30		m		64.63		1977.66

		S1148895324:		#B4q0		1148895324:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:41:13		15:38:00		m		64.63		1977.66

		S1148895354:		#B4q0		1148895354:		$B4q0		fc		28.66		0.00		26.85		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:41:43		15:38:30		m		64.63		1977.66

		S1148895384:		#B4q0		1148895384:		$B4q0		fc		28.70		0.00		26.95		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:42:13		15:39:00		m		64.63		1977.66

		S1148895414:		#B4q0		1148895414:		$B4q0		fc		28.70		0.00		26.85		3.67		3.67		3.67		3.55		3.39		3.60		3.66		3.44		0		-25228.06		16:42:43		15:39:30		m		64.63		1977.66

		S1148895444:		#B4q0		1148895444:		$B4q0		fc		28.74		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:43:13		15:40:00		m		64.63		1977.66

		S1148895474:		#B4q0		1148895474:		$B4q0		fc		28.74		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:43:43		15:40:30		m		64.63		1977.66

		S1148895504:		#B4q0		1148895504:		$B4q0		fc		28.70		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:44:13		15:41:00		m		64.63		1977.66

		S1148895534:		#B4q0		1148895534:		$B4q0		fc		28.70		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:44:43		15:41:30		m		64.63		1977.66

		S1148895564:		#B4q0		1148895564:		$B4q0		fc		28.74		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:45:13		15:42:00		m		64.63		1977.66

		S1148895594:		#B4q0		1148895594:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:45:43		15:42:30		m		64.63		1977.66

		S1148895624:		#B4q0		1148895624:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:46:13		15:43:00		m		64.63		1977.66

		S1148895654:		#B4q0		1148895654:		$B4q0		fc		28.74		0.00		26.85		3.67		3.67		3.67		3.55		3.40		3.60		3.66		3.44		0		-25228.06		16:46:43		15:43:30		m		64.63		1977.66

		S1148895684:		#B4q0		1148895684:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.55		3.41		3.60		3.66		3.44		0		-25228.06		16:47:13		15:44:00		m		64.63		1977.66

		S1148895714:		#B4q0		1148895714:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.44		0		-25228.06		16:47:43		15:44:30		m		64.63		1977.66

		S1148895744:		#B4q0		1148895744:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.44		0		-25228.06		16:48:13		15:45:00		m		64.63		1977.66

		S1148895774:		#B4q0		1148895774:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.55		3.41		3.60		3.66		3.44		0		-25228.06		16:48:43		15:45:30		m		64.63		1977.66

		S1148895804:		#B4q0		1148895804:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.44		0		-25228.06		16:49:13		15:46:00		m		64.63		1977.66

		S1148895834:		#B4q0		1148895834:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:49:43		15:46:30		m		64.63		1977.66

		S1148895864:		#B4q0		1148895864:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:50:13		15:47:00		m		64.63		1977.66

		S1148895894:		#B4q0		1148895894:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:50:43		15:47:30		m		64.63		1977.66

		S1148895924:		#B4q0		1148895924:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:51:13		15:48:00		m		64.63		1977.66

		S1148895954:		#B4q0		1148895954:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:51:43		15:48:30		m		64.63		1977.66

		S1148895984:		#B4q0		1148895984:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:52:13		15:49:00		m		64.63		1977.66

		S1148896014:		#B4q0		1148896014:		$B4q0		fc		28.74		0.00		26.75		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:52:43		15:49:30		m		64.63		1977.66

		S1148896044:		#B4q0		1148896044:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:53:13		15:50:00		m		64.63		1977.66

		S1148896074:		#B4q0		1148896074:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.46		0		-25228.06		16:53:43		15:50:30		m		64.63		1977.66

		S1148896104:		#B4q0		1148896104:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.46		0		-25228.06		16:54:13		15:51:00		m		64.63		1977.66

		S1148896134:		#B4q0		1148896134:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.46		0		-25228.06		16:54:43		15:51:30		m		64.63		1977.66

		S1148896164:		#B4q0		1148896164:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.41		3.60		3.66		3.45		0		-25228.06		16:55:13		15:52:00		m		64.63		1977.66

		S1148896194:		#B4q0		1148896194:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.42		3.60		3.66		3.46		0		-25228.06		16:55:43		15:52:30		m		64.63		1977.66

		S1148896224:		#B4q0		1148896224:		$B4q0		fc		28.77		0.00		26.66		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:56:13		15:53:00		m		64.63		1977.66

		S1148896254:		#B4q0		1148896254:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:56:43		15:53:30		m		64.63		1977.66

		S1148896284:		#B4q0		1148896284:		$B4q0		fc		28.77		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:57:13		15:54:00		m		64.63		1977.66

		S1148896314:		#B4q0		1148896314:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:57:43		15:54:30		m		64.63		1977.66

		S1148896344:		#B4q0		1148896344:		$B4q0		fc		28.74		0.00		26.66		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:58:13		15:55:00		m		64.63		1977.66

		S1148896374:		#B4q0		1148896374:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:58:43		15:55:30		m		64.63		1977.66

		S1148896404:		#B4q0		1148896404:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:59:13		15:56:00		m		64.63		1977.66

		S1148896434:		#B4q0		1148896434:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		16:59:43		15:56:30		m		64.63		1977.66

		S1148896464:		#B4q0		1148896464:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:00:13		15:57:00		m		64.63		1977.66

		S1148896494:		#B4q0		1148896494:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:00:43		15:57:30		m		64.63		1977.66

		S1148896524:		#B4q0		1148896524:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:01:13		15:58:00		m		64.63		1977.66

		S1148896554:		#B4q0		1148896554:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:01:43		15:58:30		m		64.63		1977.66

		S1148896584:		#B4q0		1148896584:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:02:13		15:59:00		m		64.63		1977.66

		S1148896614:		#B4q0		1148896614:		$B4q0		fc		28.77		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:02:43		15:59:30		m		64.63		1977.66

		S1148896644:		#B4q0		1148896644:		$B4q0		fc		28.74		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:03:13		16:00:00		m		64.63		1977.66

		S1148896674:		#B4q0		1148896674:		$B4q0		fc		28.77		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:03:43		16:00:30		m		64.63		1977.66

		S1148896704:		#B4q0		1148896704:		$B4q0		fc		28.74		0.00		26.46		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:04:13		16:01:00		m		64.63		1977.66

		S1148896734:		#B4q0		1148896734:		$B4q0		fc		28.77		0.00		26.56		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:04:43		16:01:30		m		64.63		1977.66

		S1148896764:		#B4q0		1148896764:		$B4q0		fc		28.74		0.00		26.46		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:05:13		16:02:00		m		64.63		1977.66

		S1148896794:		#B4q0		1148896794:		$B4q0		fc		28.74		0.00		26.46		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:05:43		16:02:30		m		64.63		1977.66

		S1148896824:		#B4q0		1148896824:		$B4q0		fc		28.77		0.00		26.46		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46		0		-25228.06		17:06:13		16:03:00		m		64.63		1977.66

		S1148896854:		#B4q0		1148896854:		$B4q0		fc		28.77		0.00		26.46		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:06:43		16:03:30		m		64.63		1977.66

		S1148896884:		#B4q0		1148896884:		$B4q0		fc		28.77		0.00		26.46		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:07:13		16:04:00		m		64.63		1977.66

		S1148896914:		#B4q0		1148896914:		$B4q0		fc		28.77		0.00		26.46		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:07:43		16:04:30		m		64.63		1977.66

		S1148896944:		#B4q0		1148896944:		$B4q0		fc		28.74		0.00		26.46		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:08:13		16:05:00		m		64.63		1977.66

		S1148896974:		#B4q0		1148896974:		$B4q0		fc		28.77		0.00		26.46		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:08:43		16:05:30		m		64.63		1977.66

		S1148897004:		#B4q0		1148897004:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:09:13		16:06:00		m		64.63		1977.66

		S1148897034:		#B4q0		1148897034:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:09:43		16:06:30		m		64.63		1977.66

		S1148897064:		#B4q0		1148897064:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:10:13		16:07:00		m		64.63		1977.66

		S1148897094:		#B4q0		1148897094:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:10:43		16:07:30		m		64.63		1977.66

		S1148897124:		#B4q0		1148897124:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:11:13		16:08:00		m		64.63		1977.66

		S1148897154:		#B4q0		1148897154:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:11:43		16:08:30		m		64.63		1977.66

		S1148897184:		#B4q0		1148897184:		$B4q0		fc		28.81		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:12:13		16:09:00		m		64.63		1977.66

		S1148897214:		#B4q0		1148897214:		$B4q0		fc		28.81		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:12:43		16:09:30		m		64.63		1977.66

		S1148897244:		#B4q0		1148897244:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:13:13		16:10:00		m		64.63		1977.66

		S1148897274:		#B4q0		1148897274:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46		0		-25228.06		17:13:43		16:10:30		m		64.63		1977.66

		S1148897304:		#B4q0		1148897304:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:14:13		16:11:00		m		64.63		1977.66

		S1148897334:		#B4q0		1148897334:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:14:43		16:11:30		m		64.63		1977.66

		S1148897364:		#B4q0		1148897364:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:15:13		16:12:00		m		64.63		1977.66

		S1148897394:		#B4q0		1148897394:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:15:43		16:12:30		m		64.63		1977.66

		S1148897424:		#B4q0		1148897424:		$B4q0		fc		28.77		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:16:13		16:13:00		m		64.63		1977.66

		S1148897454:		#B4q0		1148897454:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:16:43		16:13:30		m		64.63		1977.66

		S1148897484:		#B4q0		1148897484:		$B4q0		fc		28.81		0.00		26.36		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46		0		-25228.06		17:17:13		16:14:00		m		64.63		1977.66

		S1148897514:		#B4q0		1148897514:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.46		0		-25228.06		17:17:43		16:14:30		m		64.63		1977.66

		S1148897544:		#B4q0		1148897544:		$B4q0		fc		28.81		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:18:13		16:15:00		m		64.63		1977.66

		S1148897574:		#B4q0		1148897574:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:18:43		16:15:30		m		64.63		1977.66

		S1148897604:		#B4q0		1148897604:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:19:13		16:16:00		m		64.63		1977.66

		S1148897634:		#B4q0		1148897634:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:19:43		16:16:30		m		64.63		1977.66

		S1148897664:		#B4q0		1148897664:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:20:13		16:17:00		m		64.63		1977.66

		S1148897694:		#B4q0		1148897694:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:20:43		16:17:30		m		64.63		1977.66

		S1148897724:		#B4q0		1148897724:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:21:13		16:18:00		m		64.63		1977.66

		S1148897754:		#B4q0		1148897754:		$B4q0		fc		28.81		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:21:43		16:18:30		m		64.63		1977.66

		S1148897784:		#B4q0		1148897784:		$B4q0		fc		28.77		0.00		26.26		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:22:13		16:19:00		m		64.63		1977.66

		S1148897814:		#B4q0		1148897814:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:22:43		16:19:30		m		64.63		1977.66

		S1148897844:		#B4q0		1148897844:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:23:13		16:20:00		m		64.63		1977.66

		S1148897874:		#B4q0		1148897874:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:23:43		16:20:30		m		64.63		1977.66

		S1148897904:		#B4q0		1148897904:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:24:13		16:21:00		m		64.63		1977.66

		S1148897934:		#B4q0		1148897934:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:24:43		16:21:30		m		64.63		1977.66

		S1148897964:		#B4q0		1148897964:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:25:13		16:22:00		m		64.63		1977.66

		S1148897994:		#B4q0		1148897994:		$B4q0		fc		28.81		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:25:43		16:22:30		m		64.63		1977.66

		S1148898024:		#B4q0		1148898024:		$B4q0		fc		28.81		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:26:13		16:23:00		m		64.63		1977.66

		S1148898054:		#B4q0		1148898054:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:26:43		16:23:30		m		64.63		1977.66

		S1148898084:		#B4q0		1148898084:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:27:13		16:24:00		m		64.63		1977.66

		S1148898114:		#B4q0		1148898114:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:27:43		16:24:30		m		64.63		1977.66

		S1148898144:		#B4q0		1148898144:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:28:13		16:25:00		m		64.63		1977.66

		S1148898174:		#B4q0		1148898174:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:28:43		16:25:30		m		64.63		1977.66

		S1148898204:		#B4q0		1148898204:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:29:13		16:26:00		m		64.63		1977.66

		S1148898234:		#B4q0		1148898234:		$B4q0		fc		28.81		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:29:43		16:26:30		m		64.63		1977.66

		S1148898264:		#B4q0		1148898264:		$B4q0		fc		28.77		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:30:13		16:27:00		m		64.63		1977.66

		S1148898294:		#B4q0		1148898294:		$B4q0		fc		28.77		0.00		26.17		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:30:43		16:27:30		m		64.63		1977.66

		S1148898324:		#B4q0		1148898324:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:31:13		16:28:00		m		64.63		1977.66

		S1148898354:		#B4q0		1148898354:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:31:43		16:28:30		m		64.63		1977.66

		S1148898384:		#B4q0		1148898384:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:32:13		16:29:00		m		64.63		1977.66

		S1148898414:		#B4q0		1148898414:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:32:43		16:29:30		m		64.63		1977.66

		S1148898444:		#B4q0		1148898444:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:33:13		16:30:00		m		64.63		1977.66

		S1148898474:		#B4q0		1148898474:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:33:43		16:30:30		m		64.63		1977.66

		S1148898504:		#B4q0		1148898504:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47		0		-25228.06		17:34:13		16:31:00		m		64.63		1977.66

		S1148898534:		#B4q0		1148898534:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47		0		-25228.06		17:34:43		16:31:30		m		64.63		1977.66

		S1148898564:		#B4q0		1148898564:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47		0		-25228.06		17:35:13		16:32:00		m		64.63		1977.66

		S1148898594:		#B4q0		1148898594:		$B4q0		fc		28.81		0.00		26.07		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47		0		-25228.06		17:35:43		16:32:30		m		64.63		1977.66

		S1148898624:		#B4q0		1148898624:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47		0		-25228.06		17:36:13		16:33:00		m		64.63		1977.66

		S1148898654:		#B4q0		1148898654:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:36:43		16:33:30		m		64.63		1977.66

		S1148898684:		#B4q0		1148898684:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:37:13		16:34:00		m		64.63		1977.66

		S1148898714:		#B4q0		1148898714:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:37:43		16:34:30		m		64.63		1977.66

		S1148898744:		#B4q0		1148898744:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:38:13		16:35:00		m		64.63		1977.66

		S1148898774:		#B4q0		1148898774:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:38:43		16:35:30		m		64.63		1977.66

		S1148898804:		#B4q0		1148898804:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:39:13		16:36:00		m		64.63		1977.66

		S1148898834:		#B4q0		1148898834:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:39:43		16:36:30		m		64.63		1977.66

		S1148898864:		#B4q0		1148898864:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:40:13		16:37:00		m		64.63		1977.66

		S1148898894:		#B4q0		1148898894:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:40:43		16:37:30		m		64.63		1977.66

		S1148898924:		#B4q0		1148898924:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:41:13		16:38:00		m		64.63		1977.66

		S1148898954:		#B4q0		1148898954:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:41:43		16:38:30		m		64.63		1977.66

		S1148898984:		#B4q0		1148898984:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:42:13		16:39:00		m		64.63		1977.66

		S1148899014:		#B4q0		1148899014:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:42:43		16:39:30		m		64.63		1977.66

		S1148899044:		#B4q0		1148899044:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:43:13		16:40:00		m		64.63		1977.66

		S1148899074:		#B4q0		1148899074:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:43:43		16:40:30		m		64.63		1977.66

		S1148899104:		#B4q0		1148899104:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:44:13		16:41:00		m		64.63		1977.66

		S1148899134:		#B4q0		1148899134:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48		0		-25228.06		17:44:43		16:41:30		m		64.63		1977.66

		S1148899164:		#B4q0		1148899164:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:45:13		16:42:00		m		64.63		1977.66

		S1148899194:		#B4q0		1148899194:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:45:43		16:42:30		m		64.63		1977.66

		S1148899224:		#B4q0		1148899224:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:46:13		16:43:00		m		64.63		1977.66

		S1148899254:		#B4q0		1148899254:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:46:43		16:43:30		m		64.63		1977.66

		S1148899284:		#B4q0		1148899284:		$B4q0		fc		28.81		0.00		25.97		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48		0		-25228.06		17:47:13		16:44:00		m		64.63		1977.66

		S1148899314:		#B4q0		1148899314:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:47:43		16:44:30		m		64.63		1977.66

		S1148899344:		#B4q0		1148899344:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:48:13		16:45:00		m		64.63		1977.66

		S1148899374:		#B4q0		1148899374:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:48:43		16:45:30		m		64.63		1977.66

		S1148899404:		#B4q0		1148899404:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:49:13		16:46:00		m		64.63		1977.66

		S1148899434:		#B4q0		1148899434:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:49:43		16:46:30		m		64.63		1977.66

		S1148899464:		#B4q0		1148899464:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:50:13		16:47:00		m		64.63		1977.66

		S1148899494:		#B4q0		1148899494:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:50:43		16:47:30		m		64.63		1977.66

		S1148899524:		#B4q0		1148899524:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:51:13		16:48:00		m		64.63		1977.66

		S1148899554:		#B4q0		1148899554:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:51:43		16:48:30		m		64.63		1977.66

		S1148899584:		#B4q0		1148899584:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:52:13		16:49:00		m		64.63		1977.66

		S1148899614:		#B4q0		1148899614:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:52:43		16:49:30		m		64.63		1977.66

		S1148899644:		#B4q0		1148899644:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:53:13		16:50:00		m		64.63		1977.66

		S1148899674:		#B4q0		1148899674:		$B4q0		fc		28.81		0.00		25.87		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:53:43		16:50:30		m		64.63		1977.66

		S1148899704:		#B4q0		1148899704:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:54:13		16:51:00		m		64.63		1977.66

		S1148899734:		#B4q0		1148899734:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:54:43		16:51:30		m		64.63		1977.66

		S1148899764:		#B4q0		1148899764:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:55:13		16:52:00		m		64.63		1977.66

		S1148899794:		#B4q0		1148899794:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:55:43		16:52:30		m		64.63		1977.66

		S1148899824:		#B4q0		1148899824:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:56:13		16:53:00		m		64.63		1977.66

		S1148899854:		#B4q0		1148899854:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:56:43		16:53:30		m		64.63		1977.66

		S1148899884:		#B4q0		1148899884:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48		0		-25228.06		17:57:13		16:54:00		m		64.63		1977.66

		S1148899914:		#B4q0		1148899914:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		17:57:43		16:54:30		m		64.63		1977.66

		S1148899944:		#B4q0		1148899944:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		17:58:13		16:55:00		m		64.63		1977.66

		S1148899974:		#B4q0		1148899974:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		17:58:43		16:55:30		m		64.63		1977.66

		S1148900004:		#B4q0		1148900004:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		17:59:13		16:56:00		m		64.63		1977.66

		S1148900034:		#B4q0		1148900034:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		17:59:43		16:56:30		m		64.63		1977.66

		S1148900064:		#B4q0		1148900064:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		18:00:13		16:57:00		m		64.63		1977.66

		S1148900094:		#B4q0		1148900094:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		18:00:43		16:57:30		m		64.63		1977.66

		S1148900124:		#B4q0		1148900124:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		18:01:13		16:58:00		m		64.63		1977.66

		S1148900154:		#B4q0		1148900154:		$B4q0		fc		28.81		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		18:01:43		16:58:30		m		64.63		1977.66

		S1148900184:		#B4q0		1148900184:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48		0		-25228.06		18:02:13		16:59:00		m		64.63		1977.66

		S1148900214:		#B4q0		1148900214:		$B4q0		fc		28.89		0.00		25.78		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:02:43		16:59:30		m		64.63		1977.66

		S1148900244:		#B4q0		1148900244:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:03:13		17:00:00		m		64.63		1977.66

		S1148900274:		#B4q0		1148900274:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:03:43		17:00:30		m		64.63		1977.66

		S1148900304:		#B4q0		1148900304:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:04:13		17:01:00		m		64.63		1977.66

		S1148900334:		#B4q0		1148900334:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:04:43		17:01:30		m		64.63		1977.66

		S1148900364:		#B4q0		1148900364:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:05:13		17:02:00		m		64.63		1977.66

		S1148900394:		#B4q0		1148900394:		$B4q0		fc		28.85		0.00		25.78		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:05:43		17:02:30		m		64.63		1977.66

		S1148900424:		#B4q0		1148900424:		$B4q0		fc		28.89		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:06:13		17:03:00		m		64.63		1977.66

		S1148900454:		#B4q0		1148900454:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:06:43		17:03:30		m		64.63		1977.66

		S1148900484:		#B4q0		1148900484:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:07:13		17:04:00		m		64.63		1977.66

		S1148900514:		#B4q0		1148900514:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:07:43		17:04:30		m		64.63		1977.66

		S1148900544:		#B4q0		1148900544:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48		0		-25228.06		18:08:13		17:05:00		m		64.63		1977.66

		S1148900574:		#B4q0		1148900574:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:08:43		17:05:30		m		64.63		1977.66

		S1148900604:		#B4q0		1148900604:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:09:13		17:06:00		m		64.63		1977.66

		S1148900634:		#B4q0		1148900634:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:09:43		17:06:30		m		64.63		1977.66

		S1148900664:		#B4q0		1148900664:		$B4q0		fc		28.85		0.00		25.68		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:10:13		17:07:00		m		64.63		1977.66

		S1148900694:		#B4q0		1148900694:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:10:43		17:07:30		m		64.63		1977.66

		S1148900724:		#B4q0		1148900724:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:11:13		17:08:00		m		64.63		1977.66

		S1148900754:		#B4q0		1148900754:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:11:43		17:08:30		m		64.63		1977.66

		S1148900784:		#B4q0		1148900784:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:12:13		17:09:00		m		64.63		1977.66

		S1148900814:		#B4q0		1148900814:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:12:43		17:09:30		m		64.63		1977.66

		S1148900844:		#B4q0		1148900844:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:13:13		17:10:00		m		64.63		1977.66

		S1148900874:		#B4q0		1148900874:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:13:43		17:10:30		m		64.63		1977.66

		S1148900904:		#B4q0		1148900904:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:14:13		17:11:00		m		64.63		1977.66

		S1148900934:		#B4q0		1148900934:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:14:43		17:11:30		m		64.63		1977.66

		S1148900964:		#B4q0		1148900964:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:15:13		17:12:00		m		64.63		1977.66

		S1148900994:		#B4q0		1148900994:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:15:43		17:12:30		m		64.63		1977.66

		S1148901024:		#B4q0		1148901024:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:16:13		17:13:00		m		64.63		1977.66

		S1148901054:		#B4q0		1148901054:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:16:43		17:13:30		m		64.63		1977.66

		S1148901084:		#B4q0		1148901084:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:17:13		17:14:00		m		64.63		1977.66

		S1148901114:		#B4q0		1148901114:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:17:43		17:14:30		m		64.63		1977.66

		S1148901144:		#B4q0		1148901144:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:18:13		17:15:00		m		64.63		1977.66

		S1148901174:		#B4q0		1148901174:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:18:43		17:15:30		m		64.63		1977.66

		S1148901204:		#B4q0		1148901204:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:19:13		17:16:00		m		64.63		1977.66

		S1148901234:		#B4q0		1148901234:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:19:43		17:16:30		m		64.63		1977.66

		S1148901264:		#B4q0		1148901264:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:20:13		17:17:00		m		64.63		1977.66

		S1148901294:		#B4q0		1148901294:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:20:43		17:17:30		m		64.63		1977.66

		S1148901324:		#B4q0		1148901324:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:21:13		17:18:00		m		64.63		1977.66

		S1148901354:		#B4q0		1148901354:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:21:43		17:18:30		m		64.63		1977.66

		S1148901384:		#B4q0		1148901384:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49		0		-25228.06		18:22:13		17:19:00		m		64.63		1977.66

		S1148901414:		#B4q0		1148901414:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:22:43		17:19:30		m		64.63		1977.66

		S1148901444:		#B4q0		1148901444:		$B4q0		fc		28.89		0.00		25.58		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:23:13		17:20:00		m		64.63		1977.66

		S1148901474:		#B4q0		1148901474:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:23:43		17:20:30		m		64.63		1977.66

		S1148901504:		#B4q0		1148901504:		$B4q0		fc		28.85		0.00		25.58		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:24:13		17:21:00		m		64.63		1977.66

		S1148901534:		#B4q0		1148901534:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:24:43		17:21:30		m		64.63		1977.66

		S1148901564:		#B4q0		1148901564:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:25:13		17:22:00		m		64.63		1977.66

		S1148901594:		#B4q0		1148901594:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:25:43		17:22:30		m		64.63		1977.66

		S1148901624:		#B4q0		1148901624:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:26:13		17:23:00		m		64.63		1977.66

		S1148901654:		#B4q0		1148901654:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:26:43		17:23:30		m		64.63		1977.66

		S1148901684:		#B4q0		1148901684:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:27:13		17:24:00		m		64.63		1977.66

		S1148901714:		#B4q0		1148901714:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:27:43		17:24:30		m		64.63		1977.66

		S1148901744:		#B4q0		1148901744:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:28:13		17:25:00		m		64.63		1977.66

		S1148901774:		#B4q0		1148901774:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:28:43		17:25:30		m		64.63		1977.66

		S1148901804:		#B4q0		1148901804:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:29:13		17:26:00		m		64.63		1977.66

		S1148901834:		#B4q0		1148901834:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:29:43		17:26:30		m		64.63		1977.66

		S1148901864:		#B4q0		1148901864:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:30:13		17:27:00		m		64.63		1977.66

		S1148901894:		#B4q0		1148901894:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:30:43		17:27:30		m		64.63		1977.66

		S1148901924:		#B4q0		1148901924:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:31:13		17:28:00		m		64.63		1977.66

		S1148901954:		#B4q0		1148901954:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:31:43		17:28:30		m		64.63		1977.66

		S1148901984:		#B4q0		1148901984:		$B4q0		fc		28.85		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:32:13		17:29:00		m		64.63		1977.66

		S1148902014:		#B4q0		1148902014:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:32:43		17:29:30		m		64.63		1977.66

		S1148902044:		#B4q0		1148902044:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:33:13		17:30:00		m		64.63		1977.66

		S1148902074:		#B4q0		1148902074:		$B4q0		fc		28.89		0.00		25.48		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:33:43		17:30:30		m		64.63		1977.66

		S1148902104:		#B4q0		1148902104:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:34:13		17:31:00		m		64.63		1977.66

		S1148902134:		#B4q0		1148902134:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.49		0		-25228.06		18:34:43		17:31:30		m		64.63		1977.66

		S1148902164:		#B4q0		1148902164:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:35:13		17:32:00		m		64.63		1977.66

		S1148902194:		#B4q0		1148902194:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:35:43		17:32:30		m		64.63		1977.66

		S1148902224:		#B4q0		1148902224:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:36:13		17:33:00		m		64.63		1977.66

		S1148902254:		#B4q0		1148902254:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:36:43		17:33:30		m		64.63		1977.66

		S1148902284:		#B4q0		1148902284:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:37:13		17:34:00		m		64.63		1977.66

		S1148902314:		#B4q0		1148902314:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:37:43		17:34:30		m		64.63		1977.66

		S1148902344:		#B4q0		1148902344:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:38:13		17:35:00		m		64.63		1977.66

		S1148902374:		#B4q0		1148902374:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:38:43		17:35:30		m		64.63		1977.66

		S1148902404:		#B4q0		1148902404:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:39:13		17:36:00		m		64.63		1977.66

		S1148902434:		#B4q0		1148902434:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:39:43		17:36:30		m		64.63		1977.66

		S1148902464:		#B4q0		1148902464:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:40:13		17:37:00		m		64.63		1977.66

		S1148902494:		#B4q0		1148902494:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:40:43		17:37:30		m		64.63		1977.66

		S1148902524:		#B4q0		1148902524:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:41:13		17:38:00		m		64.63		1977.66

		S1148902554:		#B4q0		1148902554:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:41:43		17:38:30		m		64.63		1977.66

		S1148902584:		#B4q0		1148902584:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:42:13		17:39:00		m		64.63		1977.66

		S1148902614:		#B4q0		1148902614:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:42:43		17:39:30		m		64.63		1977.66

		S1148902644:		#B4q0		1148902644:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:43:13		17:40:00		m		64.63		1977.66

		S1148902674:		#B4q0		1148902674:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:43:43		17:40:30		m		64.63		1977.66

		S1148902704:		#B4q0		1148902704:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:44:13		17:41:00		m		64.63		1977.66

		S1148902734:		#B4q0		1148902734:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:44:43		17:41:30		m		64.63		1977.66

		S1148902764:		#B4q0		1148902764:		$B4q0		fc		28.85		0.00		25.39		3.67		3.67		3.67		3.60		3.45		3.62		3.67		3.50		0		-25228.06		18:45:13		17:42:00		m		64.63		1977.66

		S1148902794:		#B4q0		1148902794:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:45:43		17:42:30		m		64.63		1977.66

		S1148902824:		#B4q0		1148902824:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:46:13		17:43:00		m		64.63		1977.66

		S1148902854:		#B4q0		1148902854:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:46:43		17:43:30		m		64.63		1977.66

		S1148902884:		#B4q0		1148902884:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:47:13		17:44:00		m		64.63		1977.66

		S1148902914:		#B4q0		1148902914:		$B4q0		fc		28.89		0.00		25.39		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:47:43		17:44:30		m		64.63		1977.66

		S1148902944:		#B4q0		1148902944:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:48:13		17:45:00		m		64.63		1977.66

		S1148902974:		#B4q0		1148902974:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:48:43		17:45:30		m		64.63		1977.66

		S1148903004:		#B4q0		1148903004:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:49:13		17:46:00		m		64.63		1977.66

		S1148903034:		#B4q0		1148903034:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:49:43		17:46:30		m		64.63		1977.66

		S1148903064:		#B4q0		1148903064:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:50:13		17:47:00		m		64.63		1977.66

		S1148903094:		#B4q0		1148903094:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:50:43		17:47:30		m		64.63		1977.66

		S1148903124:		#B4q0		1148903124:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:51:13		17:48:00		m		64.63		1977.66

		S1148903154:		#B4q0		1148903154:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:51:43		17:48:30		m		64.63		1977.66

		S1148903184:		#B4q0		1148903184:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:52:13		17:49:00		m		64.63		1977.66

		S1148903214:		#B4q0		1148903214:		$B4q0		fc		28.85		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:52:43		17:49:30		m		64.63		1977.66

		S1148903244:		#B4q0		1148903244:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:53:13		17:50:00		m		64.63		1977.66

		S1148903274:		#B4q0		1148903274:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:53:43		17:50:30		m		64.63		1977.66

		S1148903304:		#B4q0		1148903304:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:54:13		17:51:00		m		64.63		1977.66

		S1148903334:		#B4q0		1148903334:		$B4q0		fc		28.85		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:54:43		17:51:30		m		64.63		1977.66

		S1148903364:		#B4q0		1148903364:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:55:13		17:52:00		m		64.63		1977.66

		S1148903394:		#B4q0		1148903394:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:55:43		17:52:30		m		64.63		1977.66

		S1148903424:		#B4q0		1148903424:		$B4q0		fc		28.89		0.00		25.29		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:56:13		17:53:00		m		64.63		1977.66

		S1148903454:		#B4q0		1148903454:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:56:43		17:53:30		m		64.63		1977.66

		S1148903484:		#B4q0		1148903484:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:57:13		17:54:00		m		64.63		1977.66

		S1148903514:		#B4q0		1148903514:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:57:43		17:54:30		m		64.63		1977.66

		S1148903544:		#B4q0		1148903544:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:58:13		17:55:00		m		64.63		1977.66

		S1148903574:		#B4q0		1148903574:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:58:43		17:55:30		m		64.63		1977.66

		S1148903604:		#B4q0		1148903604:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:59:13		17:56:00		m		64.63		1977.66

		S1148903634:		#B4q0		1148903634:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		18:59:43		17:56:30		m		64.63		1977.66

		S1148903664:		#B4q0		1148903664:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:00:13		17:57:00		m		64.63		1977.66

		S1148903694:		#B4q0		1148903694:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:00:43		17:57:30		m		64.63		1977.66

		S1148903724:		#B4q0		1148903724:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:01:13		17:58:00		m		64.63		1977.66

		S1148903754:		#B4q0		1148903754:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:01:43		17:58:30		m		64.63		1977.66

		S1148903784:		#B4q0		1148903784:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:02:13		17:59:00		m		64.63		1977.66

		S1148903814:		#B4q0		1148903814:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:02:43		17:59:30		m		64.63		1977.66

		S1148903844:		#B4q0		1148903844:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:03:13		18:00:00		m		64.63		1977.66

		S1148903874:		#B4q0		1148903874:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:03:43		18:00:30		m		64.63		1977.66

		S1148903904:		#B4q0		1148903904:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:04:13		18:01:00		m		64.63		1977.66

		S1148903934:		#B4q0		1148903934:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:04:43		18:01:30		m		64.63		1977.66

		S1148903964:		#B4q0		1148903964:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:05:13		18:02:00		m		64.63		1977.66

		S1148903994:		#B4q0		1148903994:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:05:43		18:02:30		m		64.63		1977.66

		S1148904024:		#B4q0		1148904024:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:06:13		18:03:00		m		64.63		1977.66

		S1148904054:		#B4q0		1148904054:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:06:43		18:03:30		m		64.63		1977.66

		S1148904084:		#B4q0		1148904084:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:07:13		18:04:00		m		64.63		1977.66

		S1148904114:		#B4q0		1148904114:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:07:43		18:04:30		m		64.63		1977.66

		S1148904144:		#B4q0		1148904144:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:08:13		18:05:00		m		64.63		1977.66

		S1148904174:		#B4q0		1148904174:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:08:43		18:05:30		m		64.63		1977.66

		S1148904204:		#B4q0		1148904204:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:09:13		18:06:00		m		64.63		1977.66

		S1148904234:		#B4q0		1148904234:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:09:43		18:06:30		m		64.63		1977.66

		S1148904264:		#B4q0		1148904264:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:10:13		18:07:00		m		64.63		1977.66

		S1148904294:		#B4q0		1148904294:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:10:43		18:07:30		m		64.63		1977.66

		S1148904324:		#B4q0		1148904324:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:11:13		18:08:00		m		64.63		1977.66

		S1148904354:		#B4q0		1148904354:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:11:43		18:08:30		m		64.63		1977.66

		S1148904384:		#B4q0		1148904384:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:12:13		18:09:00		m		64.63		1977.66

		S1148904414:		#B4q0		1148904414:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:12:43		18:09:30		m		64.63		1977.66

		S1148904444:		#B4q0		1148904444:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:13:13		18:10:00		m		64.63		1977.66

		S1148904474:		#B4q0		1148904474:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:13:43		18:10:30		m		64.63		1977.66

		S1148904504:		#B4q0		1148904504:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:14:13		18:11:00		m		64.63		1977.66

		S1148904534:		#B4q0		1148904534:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:14:43		18:11:30		m		64.63		1977.66

		S1148904564:		#B4q0		1148904564:		$B4q0		fc		28.89		0.00		25.19		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:15:13		18:12:00		m		64.63		1977.66

		S1148904594:		#B4q0		1148904594:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:15:43		18:12:30		m		64.63		1977.66

		S1148904624:		#B4q0		1148904624:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:16:13		18:13:00		m		64.63		1977.66

		S1148904654:		#B4q0		1148904654:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:16:43		18:13:30		m		64.63		1977.66

		S1148904684:		#B4q0		1148904684:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:17:13		18:14:00		m		64.63		1977.66

		S1148904714:		#B4q0		1148904714:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:17:43		18:14:30		m		64.63		1977.66

		S1148904744:		#B4q0		1148904744:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:18:13		18:15:00		m		64.63		1977.66

		S1148904774:		#B4q0		1148904774:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:18:43		18:15:30		m		64.63		1977.66

		S1148904804:		#B4q0		1148904804:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:19:13		18:16:00		m		64.63		1977.66

		S1148904834:		#B4q0		1148904834:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:19:43		18:16:30		m		64.63		1977.66

		S1148904864:		#B4q0		1148904864:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:20:13		18:17:00		m		64.63		1977.66

		S1148904894:		#B4q0		1148904894:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:20:43		18:17:30		m		64.63		1977.66

		S1148904924:		#B4q0		1148904924:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.50		0		-25228.06		19:21:13		18:18:00		m		64.63		1977.66

		S1148904954:		#B4q0		1148904954:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:21:43		18:18:30		m		64.63		1977.66

		S1148904984:		#B4q0		1148904984:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:22:13		18:19:00		m		64.63		1977.66

		S1148905014:		#B4q0		1148905014:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:22:43		18:19:30		m		64.63		1977.66

		S1148905044:		#B4q0		1148905044:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:23:13		18:20:00		m		64.63		1977.66

		S1148905074:		#B4q0		1148905074:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:23:43		18:20:30		m		64.63		1977.66

		S1148905104:		#B4q0		1148905104:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:24:13		18:21:00		m		64.63		1977.66

		S1148905134:		#B4q0		1148905134:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:24:43		18:21:30		m		64.63		1977.66

		S1148905164:		#B4q0		1148905164:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:25:13		18:22:00		m		64.63		1977.66

		S1148905194:		#B4q0		1148905194:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:25:43		18:22:30		m		64.63		1977.66

		S1148905224:		#B4q0		1148905224:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:26:13		18:23:00		m		64.63		1977.66

		S1148905254:		#B4q0		1148905254:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:26:43		18:23:30		m		64.63		1977.66

		S1148905284:		#B4q0		1148905284:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:27:13		18:24:00		m		64.63		1977.66

		S1148905314:		#B4q0		1148905314:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:27:43		18:24:30		m		64.63		1977.66

		S1148905344:		#B4q0		1148905344:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:28:13		18:25:00		m		64.63		1977.66

		S1148905374:		#B4q0		1148905374:		$B4q0		fc		28.89		0.00		25.09		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:28:43		18:25:30		m		64.63		1977.66

		S1148905404:		#B4q0		1148905404:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:29:13		18:26:00		m		64.63		1977.66

		S1148905434:		#B4q0		1148905434:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:29:43		18:26:30		m		64.63		1977.66

		S1148905464:		#B4q0		1148905464:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:30:13		18:27:00		m		64.63		1977.66

		S1148905494:		#B4q0		1148905494:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:30:43		18:27:30		m		64.63		1977.66

		S1148905524:		#B4q0		1148905524:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:31:13		18:28:00		m		64.63		1977.66

		S1148905554:		#B4q0		1148905554:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:31:43		18:28:30		m		64.63		1977.66

		S1148905584:		#B4q0		1148905584:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:32:13		18:29:00		m		64.63		1977.66

		S1148905614:		#B4q0		1148905614:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:32:43		18:29:30		m		64.63		1977.66

		S1148905644:		#B4q0		1148905644:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:33:13		18:30:00		m		64.63		1977.66

		S1148905674:		#B4q0		1148905674:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:33:43		18:30:30		m		64.63		1977.66

		S1148905704:		#B4q0		1148905704:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:34:13		18:31:00		m		64.63		1977.66

		S1148905734:		#B4q0		1148905734:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:34:43		18:31:30		m		64.63		1977.66

		S1148905764:		#B4q0		1148905764:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:35:13		18:32:00		m		64.63		1977.66

		S1148905794:		#B4q0		1148905794:		$B4q0		fc		28.89		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:35:43		18:32:30		m		64.63		1977.66

		S1148905824:		#B4q0		1148905824:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:36:13		18:33:00		m		64.63		1977.66

		S1148905854:		#B4q0		1148905854:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:36:43		18:33:30		m		64.63		1977.66

		S1148905884:		#B4q0		1148905884:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:37:13		18:34:00		m		64.63		1977.66

		S1148905914:		#B4q0		1148905914:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:37:43		18:34:30		m		64.63		1977.66

		S1148905944:		#B4q0		1148905944:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:38:13		18:35:00		m		64.63		1977.66

		S1148905974:		#B4q0		1148905974:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:38:43		18:35:30		m		64.63		1977.66

		S1148906004:		#B4q0		1148906004:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:39:13		18:36:00		m		64.63		1977.66

		S1148906034:		#B4q0		1148906034:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:39:43		18:36:30		m		64.63		1977.66

		S1148906064:		#B4q0		1148906064:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:40:13		18:37:00		m		64.63		1977.66

		S1148906094:		#B4q0		1148906094:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:40:43		18:37:30		m		64.63		1977.66

		S1148906124:		#B4q0		1148906124:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:41:13		18:38:00		m		64.63		1977.66

		S1148906154:		#B4q0		1148906154:		$B4q0		fc		28.89		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:41:43		18:38:30		m		64.63		1977.66

		S1148906184:		#B4q0		1148906184:		$B4q0		fc		28.89		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:42:13		18:39:00		m		64.63		1977.66

		S1148906214:		#B4q0		1148906214:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:42:43		18:39:30		m		64.63		1977.66

		S1148906244:		#B4q0		1148906244:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:43:13		18:40:00		m		64.63		1977.66

		S1148906274:		#B4q0		1148906274:		$B4q0		fc		28.89		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:43:43		18:40:30		m		64.63		1977.66

		S1148906304:		#B4q0		1148906304:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:44:13		18:41:00		m		64.63		1977.66

		S1148906334:		#B4q0		1148906334:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.67		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:44:43		18:41:30		m		64.63		1977.66

		S1148906364:		#B4q0		1148906364:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:45:13		18:42:00		m		64.63		1977.66

		S1148906394:		#B4q0		1148906394:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:45:43		18:42:30		m		64.63		1977.66

		S1148906424:		#B4q0		1148906424:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:46:13		18:43:00		m		64.63		1977.66

		S1148906454:		#B4q0		1148906454:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:46:43		18:43:30		m		64.63		1977.66

		S1148906484:		#B4q0		1148906484:		$B4q0		fc		28.92		0.00		24.9		3.67		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:47:13		18:44:00		m		64.63		1977.66

		S1148906514:		#B4q0		1148906514:		$B4q0		fc		28.89		0.00		24.9		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:47:43		18:44:30		m		64.63		1977.66

		S1148906544:		#B4q0		1148906544:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:48:13		18:45:00		m		64.63		1977.66

		S1148906574:		#B4q0		1148906574:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.60		3.46		3.62		3.67		3.51		0		-25228.06		19:48:43		18:45:30		m		64.63		1977.66

		S1148906604:		#B4q0		1148906604:		$B4q0		fc		28.92		0.00		25		3.67		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:49:13		18:46:00		m		64.63		1977.66

		S1148906634:		#B4q0		1148906634:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:49:43		18:46:30		m		64.63		1977.66

		S1148906664:		#B4q0		1148906664:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:50:13		18:47:00		m		64.63		1977.66

		S1148906694:		#B4q0		1148906694:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:50:43		18:47:30		m		64.63		1977.66

		S1148906724:		#B4q0		1148906724:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.51		0		-25228.06		19:51:13		18:48:00		m		64.63		1977.66

		S1148906754:		#B4q0		1148906754:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:51:43		18:48:30		m		64.63		1977.66

		S1148906784:		#B4q0		1148906784:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:52:13		18:49:00		m		64.63		1977.66

		S1148906814:		#B4q0		1148906814:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:52:43		18:49:30		m		64.63		1977.66

		S1148906844:		#B4q0		1148906844:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:53:13		18:50:00		m		64.63		1977.66

		S1148906874:		#B4q0		1148906874:		$B4q0		fc		28.92		0.00		25		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:53:43		18:50:30		m		64.63		1977.66

		S1148906904:		#B4q0		1148906904:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:54:13		18:51:00		m		64.63		1977.66

		S1148906934:		#B4q0		1148906934:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:54:43		18:51:30		m		64.63		1977.66

		S1148906964:		#B4q0		1148906964:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:55:13		18:52:00		m		64.63		1977.66

		S1148906994:		#B4q0		1148906994:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:55:43		18:52:30		m		64.63		1977.66

		S1148907024:		#B4q0		1148907024:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:56:13		18:53:00		m		64.63		1977.66

		S1148907054:		#B4q0		1148907054:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:56:43		18:53:30		m		64.63		1977.66

		S1148907084:		#B4q0		1148907084:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:57:13		18:54:00		m		64.63		1977.66

		S1148907114:		#B4q0		1148907114:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:57:43		18:54:30		m		64.63		1977.66

		S1148907144:		#B4q0		1148907144:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:58:13		18:55:00		m		64.63		1977.66

		S1148907174:		#B4q0		1148907174:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:58:43		18:55:30		m		64.63		1977.66

		S1148907204:		#B4q0		1148907204:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:59:13		18:56:00		m		64.63		1977.66

		S1148907234:		#B4q0		1148907234:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		19:59:43		18:56:30		m		64.63		1977.66

		S1148907264:		#B4q0		1148907264:		$B4q0		fc		28.96		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:00:13		18:57:00		m		64.63		1977.66

		S1148907294:		#B4q0		1148907294:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:00:43		18:57:30		m		64.63		1977.66

		S1148907324:		#B4q0		1148907324:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:01:13		18:58:00		m		64.63		1977.66

		S1148907354:		#B4q0		1148907354:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:01:43		18:58:30		m		64.63		1977.66

		S1148907384:		#B4q0		1148907384:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:02:13		18:59:00		m		64.63		1977.66

		S1148907414:		#B4q0		1148907414:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:02:43		18:59:30		m		64.63		1977.66

		S1148907444:		#B4q0		1148907444:		$B4q0		fc		28.96		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:03:13		19:00:00		m		64.63		1977.66

		S1148907474:		#B4q0		1148907474:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:03:43		19:00:30		m		64.63		1977.66

		S1148907504:		#B4q0		1148907504:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:04:13		19:01:00		m		64.63		1977.66

		S1148907534:		#B4q0		1148907534:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:04:43		19:01:30		m		64.63		1977.66

		S1148907564:		#B4q0		1148907564:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:05:13		19:02:00		m		64.63		1977.66

		S1148907594:		#B4q0		1148907594:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:05:43		19:02:30		m		64.63		1977.66

		S1148907624:		#B4q0		1148907624:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:06:13		19:03:00		m		64.63		1977.66

		S1148907654:		#B4q0		1148907654:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:06:43		19:03:30		m		64.63		1977.66

		S1148907684:		#B4q0		1148907684:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:07:13		19:04:00		m		64.63		1977.66

		S1148907714:		#B4q0		1148907714:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:07:43		19:04:30		m		64.63		1977.66

		S1148907744:		#B4q0		1148907744:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:08:13		19:05:00		m		64.63		1977.66

		S1148907774:		#B4q0		1148907774:		$B4q0		fc		28.92		0.00		24.9		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:08:43		19:05:30		m		64.63		1977.66

		S1148907804:		#B4q0		1148907804:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:09:13		19:06:00		m		64.63		1977.66

		S1148907834:		#B4q0		1148907834:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:09:43		19:06:30		m		64.63		1977.66

		S1148907864:		#B4q0		1148907864:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:10:13		19:07:00		m		64.63		1977.66

		S1148907894:		#B4q0		1148907894:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:10:43		19:07:30		m		64.63		1977.66

		S1148907924:		#B4q0		1148907924:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:11:13		19:08:00		m		64.63		1977.66

		S1148907954:		#B4q0		1148907954:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:11:43		19:08:30		m		64.63		1977.66

		S1148907984:		#B4q0		1148907984:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:12:13		19:09:00		m		64.63		1977.66

		S1148908014:		#B4q0		1148908014:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:12:43		19:09:30		m		64.63		1977.66

		S1148908044:		#B4q0		1148908044:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:13:13		19:10:00		m		64.63		1977.66

		S1148908074:		#B4q0		1148908074:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:13:43		19:10:30		m		64.63		1977.66

		S1148908104:		#B4q0		1148908104:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:14:13		19:11:00		m		64.63		1977.66

		S1148908134:		#B4q0		1148908134:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:14:43		19:11:30		m		64.63		1977.66

		S1148908164:		#B4q0		1148908164:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:15:13		19:12:00		m		64.63		1977.66

		S1148908194:		#B4q0		1148908194:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:15:43		19:12:30		m		64.63		1977.66

		S1148908224:		#B4q0		1148908224:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:16:13		19:13:00		m		64.63		1977.66

		S1148908254:		#B4q0		1148908254:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:16:43		19:13:30		m		64.63		1977.66

		S1148908284:		#B4q0		1148908284:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:17:13		19:14:00		m		64.63		1977.66

		S1148908314:		#B4q0		1148908314:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:17:43		19:14:30		m		64.63		1977.66

		S1148908344:		#B4q0		1148908344:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:18:13		19:15:00		m		64.63		1977.66

		S1148908374:		#B4q0		1148908374:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:18:43		19:15:30		m		64.63		1977.66

		S1148908404:		#B4q0		1148908404:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:19:13		19:16:00		m		64.63		1977.66

		S1148908434:		#B4q0		1148908434:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:19:43		19:16:30		m		64.63		1977.66

		S1148908464:		#B4q0		1148908464:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:20:13		19:17:00		m		64.63		1977.66

		S1148908494:		#B4q0		1148908494:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:20:43		19:17:30		m		64.63		1977.66

		S1148908524:		#B4q0		1148908524:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:21:13		19:18:00		m		64.63		1977.66

		S1148908554:		#B4q0		1148908554:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:21:43		19:18:30		m		64.63		1977.66

		S1148908584:		#B4q0		1148908584:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:22:13		19:19:00		m		64.63		1977.66

		S1148908614:		#B4q0		1148908614:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:22:43		19:19:30		m		64.63		1977.66

		S1148908644:		#B4q0		1148908644:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.52		0		-25228.06		20:23:13		19:20:00		m		64.63		1977.66

		S1148908674:		#B4q0		1148908674:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.62		3.67		3.52		0		-25228.06		20:23:43		19:20:30		m		64.63		1977.66

		S1148908704:		#B4q0		1148908704:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:24:13		19:21:00		m		64.63		1977.66

		S1148908734:		#B4q0		1148908734:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:24:43		19:21:30		m		64.63		1977.66

		S1148908764:		#B4q0		1148908764:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:25:13		19:22:00		m		64.63		1977.66

		S1148908794:		#B4q0		1148908794:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:25:43		19:22:30		m		64.63		1977.66

		S1148908824:		#B4q0		1148908824:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:26:13		19:23:00		m		64.63		1977.66

		S1148908854:		#B4q0		1148908854:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:26:43		19:23:30		m		64.63		1977.66

		S1148908884:		#B4q0		1148908884:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:27:13		19:24:00		m		64.63		1977.66

		S1148908914:		#B4q0		1148908914:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.46		3.63		3.67		3.53		0		-25228.06		20:27:43		19:24:30		m		64.63		1977.66

		S1148908944:		#B4q0		1148908944:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:28:13		19:25:00		m		64.63		1977.66

		S1148908974:		#B4q0		1148908974:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:28:43		19:25:30		m		64.63		1977.66

		S1148909004:		#B4q0		1148909004:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:29:13		19:26:00		m		64.63		1977.66

		S1148909034:		#B4q0		1148909034:		$B4q0		fc		28.96		0.00		24.8		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:29:43		19:26:30		m		64.63		1977.66

		S1148909064:		#B4q0		1148909064:		$B4q0		fc		28.92		0.00		24.8		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:30:13		19:27:00		m		64.63		1977.66

		S1148909094:		#B4q0		1148909094:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:30:43		19:27:30		m		64.63		1977.66

		S1148909124:		#B4q0		1148909124:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:31:13		19:28:00		m		64.63		1977.66

		S1148909154:		#B4q0		1148909154:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:31:43		19:28:30		m		64.63		1977.66

		S1148909184:		#B4q0		1148909184:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:32:13		19:29:00		m		64.63		1977.66

		S1148909214:		#B4q0		1148909214:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:32:43		19:29:30		m		64.63		1977.66

		S1148909244:		#B4q0		1148909244:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:33:13		19:30:00		m		64.63		1977.66

		S1148909274:		#B4q0		1148909274:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:33:43		19:30:30		m		64.63		1977.66

		S1148909304:		#B4q0		1148909304:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:34:13		19:31:00		m		64.63		1977.66

		S1148909334:		#B4q0		1148909334:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:34:43		19:31:30		m		64.63		1977.66

		S1148909364:		#B4q0		1148909364:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:35:13		19:32:00		m		64.63		1977.66

		S1148909394:		#B4q0		1148909394:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:35:43		19:32:30		m		64.63		1977.66

		S1148909424:		#B4q0		1148909424:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:36:13		19:33:00		m		64.63		1977.66

		S1148909454:		#B4q0		1148909454:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:36:43		19:33:30		m		64.63		1977.66

		S1148909484:		#B4q0		1148909484:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:37:13		19:34:00		m		64.63		1977.66

		S1148909514:		#B4q0		1148909514:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:37:43		19:34:30		m		64.63		1977.66

		S1148909544:		#B4q0		1148909544:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:38:13		19:35:00		m		64.63		1977.66

		S1148909574:		#B4q0		1148909574:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:38:43		19:35:30		m		64.63		1977.66

		S1148909604:		#B4q0		1148909604:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:39:13		19:36:00		m		64.63		1977.66

		S1148909634:		#B4q0		1148909634:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:39:43		19:36:30		m		64.63		1977.66

		S1148909664:		#B4q0		1148909664:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:40:13		19:37:00		m		64.63		1977.66

		S1148909694:		#B4q0		1148909694:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:40:43		19:37:30		m		64.63		1977.66

		S1148909724:		#B4q0		1148909724:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:41:13		19:38:00		m		64.63		1977.66

		S1148909754:		#B4q0		1148909754:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:41:43		19:38:30		m		64.63		1977.66

		S1148909784:		#B4q0		1148909784:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:42:13		19:39:00		m		64.63		1977.66

		S1148909814:		#B4q0		1148909814:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:42:43		19:39:30		m		64.63		1977.66

		S1148909844:		#B4q0		1148909844:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:43:13		19:40:00		m		64.63		1977.66

		S1148909874:		#B4q0		1148909874:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:43:43		19:40:30		m		64.63		1977.66

		S1148909904:		#B4q0		1148909904:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:44:13		19:41:00		m		64.63		1977.66

		S1148909934:		#B4q0		1148909934:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:44:43		19:41:30		m		64.63		1977.66

		S1148909964:		#B4q0		1148909964:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:45:13		19:42:00		m		64.63		1977.66

		S1148909994:		#B4q0		1148909994:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:45:43		19:42:30		m		64.63		1977.66

		S1148910024:		#B4q0		1148910024:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:46:13		19:43:00		m		64.63		1977.66

		S1148910054:		#B4q0		1148910054:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:46:43		19:43:30		m		64.63		1977.66

		S1148910084:		#B4q0		1148910084:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:47:13		19:44:00		m		64.63		1977.66

		S1148910114:		#B4q0		1148910114:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:47:43		19:44:30		m		64.63		1977.66

		S1148910144:		#B4q0		1148910144:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:48:13		19:45:00		m		64.63		1977.66

		S1148910174:		#B4q0		1148910174:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:48:43		19:45:30		m		64.63		1977.66

		S1148910204:		#B4q0		1148910204:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:49:13		19:46:00		m		64.63		1977.66

		S1148910234:		#B4q0		1148910234:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:49:43		19:46:30		m		64.63		1977.66

		S1148910264:		#B4q0		1148910264:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:50:13		19:47:00		m		64.63		1977.66

		S1148910294:		#B4q0		1148910294:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:50:43		19:47:30		m		64.63		1977.66

		S1148910324:		#B4q0		1148910324:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:51:13		19:48:00		m		64.63		1977.66

		S1148910354:		#B4q0		1148910354:		$B4q0		fc		28.92		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:51:43		19:48:30		m		64.63		1977.66

		S1148910384:		#B4q0		1148910384:		$B4q0		fc		28.96		0.00		24.7		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:52:13		19:49:00		m		64.63		1977.66

		S1148910414:		#B4q0		1148910414:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:52:43		19:49:30		m		64.63		1977.66

		S1148910444:		#B4q0		1148910444:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:53:13		19:50:00		m		64.63		1977.66

		S1148910474:		#B4q0		1148910474:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:53:43		19:50:30		m		64.63		1977.66

		S1148910504:		#B4q0		1148910504:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		20:54:13		19:51:00		m		64.63		1977.66

		S1148910534:		#B4q0		1148910534:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:54:43		19:51:30		m		64.63		1977.66

		S1148910564:		#B4q0		1148910564:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:55:13		19:52:00		m		64.63		1977.66

		S1148910594:		#B4q0		1148910594:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:55:43		19:52:30		m		64.63		1977.66

		S1148910624:		#B4q0		1148910624:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:56:13		19:53:00		m		64.63		1977.66

		S1148910654:		#B4q0		1148910654:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:56:43		19:53:30		m		64.63		1977.66

		S1148910684:		#B4q0		1148910684:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:57:13		19:54:00		m		64.63		1977.66

		S1148910714:		#B4q0		1148910714:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:57:43		19:54:30		m		64.63		1977.66

		S1148910744:		#B4q0		1148910744:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:58:13		19:55:00		m		64.63		1977.66

		S1148910774:		#B4q0		1148910774:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:58:43		19:55:30		m		64.63		1977.66

		S1148910804:		#B4q0		1148910804:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:59:13		19:56:00		m		64.63		1977.66

		S1148910834:		#B4q0		1148910834:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		20:59:43		19:56:30		m		64.63		1977.66

		S1148910864:		#B4q0		1148910864:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		21:00:13		19:57:00		m		64.63		1977.66

		S1148910894:		#B4q0		1148910894:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.53		0		-25228.06		21:00:43		19:57:30		m		64.63		1977.66

		S1148910924:		#B4q0		1148910924:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:01:13		19:58:00		m		64.63		1977.66

		S1148910954:		#B4q0		1148910954:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:01:43		19:58:30		m		64.63		1977.66

		S1148910984:		#B4q0		1148910984:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:02:13		19:59:00		m		64.63		1977.66

		S1148911014:		#B4q0		1148911014:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:02:43		19:59:30		m		64.63		1977.66

		S1148911044:		#B4q0		1148911044:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:03:13		20:00:00		m		64.63		1977.66

		S1148911074:		#B4q0		1148911074:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:03:43		20:00:30		m		64.63		1977.66

		S1148911104:		#B4q0		1148911104:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:04:13		20:01:00		m		64.63		1977.66

		S1148911134:		#B4q0		1148911134:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:04:43		20:01:30		m		64.63		1977.66

		S1148911164:		#B4q0		1148911164:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:05:13		20:02:00		m		64.63		1977.66

		S1148911194:		#B4q0		1148911194:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:05:43		20:02:30		m		64.63		1977.66

		S1148911224:		#B4q0		1148911224:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:06:13		20:03:00		m		64.63		1977.66

		S1148911254:		#B4q0		1148911254:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:06:43		20:03:30		m		64.63		1977.66

		S1148911284:		#B4q0		1148911284:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:07:13		20:04:00		m		64.63		1977.66

		S1148911314:		#B4q0		1148911314:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:07:43		20:04:30		m		64.63		1977.66

		S1148911344:		#B4q0		1148911344:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:08:13		20:05:00		m		64.63		1977.66

		S1148911374:		#B4q0		1148911374:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:08:43		20:05:30		m		64.63		1977.66

		S1148911404:		#B4q0		1148911404:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:09:13		20:06:00		m		64.63		1977.66

		S1148911434:		#B4q0		1148911434:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:09:43		20:06:30		m		64.63		1977.66

		S1148911464:		#B4q0		1148911464:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:10:13		20:07:00		m		64.63		1977.66

		S1148911494:		#B4q0		1148911494:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:10:43		20:07:30		m		64.63		1977.66

		S1148911524:		#B4q0		1148911524:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:11:13		20:08:00		m		64.63		1977.66

		S1148911554:		#B4q0		1148911554:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:11:43		20:08:30		m		64.63		1977.66

		S1148911584:		#B4q0		1148911584:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:12:13		20:09:00		m		64.63		1977.66

		S1148911614:		#B4q0		1148911614:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.61		3.47		3.63		3.67		3.54		0		-25228.06		21:12:43		20:09:30		m		64.63		1977.66

		S1148911644:		#B4q0		1148911644:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:13:13		20:10:00		m		64.63		1977.66

		S1148911674:		#B4q0		1148911674:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:13:43		20:10:30		m		64.63		1977.66

		S1148911704:		#B4q0		1148911704:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:14:13		20:11:00		m		64.63		1977.66

		S1148911734:		#B4q0		1148911734:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:14:43		20:11:30		m		64.63		1977.66

		S1148911764:		#B4q0		1148911764:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:15:13		20:12:00		m		64.63		1977.66

		S1148911794:		#B4q0		1148911794:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:15:44		20:12:31		m		64.63		1977.66

		S1148911824:		#B4q0		1148911824:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:16:14		20:13:01		m		64.63		1977.66

		S1148911854:		#B4q0		1148911854:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:16:44		20:13:31		m		64.63		1977.66

		S1148911884:		#B4q0		1148911884:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:17:14		20:14:01		m		64.63		1977.66

		S1148911914:		#B4q0		1148911914:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:17:44		20:14:31		m		64.63		1977.66

		S1148911944:		#B4q0		1148911944:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:18:14		20:15:01		m		64.63		1977.66

		S1148911974:		#B4q0		1148911974:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:18:44		20:15:31		m		64.63		1977.66

		S1148912004:		#B4q0		1148912004:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:19:14		20:16:01		m		64.63		1977.66

		S1148912034:		#B4q0		1148912034:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:19:44		20:16:31		m		64.63		1977.66

		S1148912064:		#B4q0		1148912064:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:20:14		20:17:01		m		64.63		1977.66

		S1148912094:		#B4q0		1148912094:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:20:44		20:17:31		m		64.63		1977.66

		S1148912124:		#B4q0		1148912124:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:21:14		20:18:01		m		64.63		1977.66

		S1148912154:		#B4q0		1148912154:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:21:44		20:18:31		m		64.63		1977.66

		S1148912184:		#B4q0		1148912184:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:22:14		20:19:01		m		64.63		1977.66

		S1148912214:		#B4q0		1148912214:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:22:44		20:19:31		m		64.63		1977.66

		S1148912244:		#B4q0		1148912244:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:23:14		20:20:01		m		64.63		1977.66

		S1148912274:		#B4q0		1148912274:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:23:44		20:20:31		m		64.63		1977.66

		S1148912304:		#B4q0		1148912304:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:24:14		20:21:01		m		64.63		1977.66

		S1148912334:		#B4q0		1148912334:		$B4q0		fc		28.92		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:24:44		20:21:31		m		64.63		1977.66

		S1148912364:		#B4q0		1148912364:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:25:14		20:22:01		m		64.63		1977.66

		S1148912394:		#B4q0		1148912394:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:25:44		20:22:31		m		64.63		1977.66

		S1148912424:		#B4q0		1148912424:		$B4q0		fc		28.96		0.00		24.6		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:26:14		20:23:01		m		64.63		1977.66

		S1148912454:		#B4q0		1148912454:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:26:44		20:23:31		m		64.63		1977.66

		S1148912484:		#B4q0		1148912484:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:27:14		20:24:01		m		64.63		1977.66

		S1148912514:		#B4q0		1148912514:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:27:44		20:24:31		m		64.63		1977.66

		S1148912544:		#B4q0		1148912544:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:28:14		20:25:01		m		64.63		1977.66

		S1148912574:		#B4q0		1148912574:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:28:44		20:25:31		m		64.63		1977.66

		S1148912604:		#B4q0		1148912604:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:29:14		20:26:01		m		64.63		1977.66

		S1148912634:		#B4q0		1148912634:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:29:44		20:26:31		m		64.63		1977.66

		S1148912664:		#B4q0		1148912664:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:30:14		20:27:01		m		64.63		1977.66

		S1148912694:		#B4q0		1148912694:		$B4q0		fc		28.96		0.00		24.51		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:30:43		20:27:30		m		64.63		1977.66

		S1148912724:		#B4q0		1148912724:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:31:13		20:28:00		m		64.63		1977.66

		S1148912754:		#B4q0		1148912754:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:31:43		20:28:30		m		64.63		1977.66

		S1148912784:		#B4q0		1148912784:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:32:13		20:29:00		m		64.63		1977.66

		S1148912814:		#B4q0		1148912814:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:32:43		20:29:30		m		64.63		1977.66

		S1148912844:		#B4q0		1148912844:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:33:13		20:30:00		m		64.63		1977.66

		S1148912874:		#B4q0		1148912874:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:33:43		20:30:30		m		64.63		1977.66

		S1148912904:		#B4q0		1148912904:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:34:13		20:31:00		m		64.63		1977.66

		S1148912934:		#B4q0		1148912934:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:34:43		20:31:30		m		64.63		1977.66

		S1148912964:		#B4q0		1148912964:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:35:13		20:32:00		m		64.63		1977.66

		S1148912994:		#B4q0		1148912994:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:35:43		20:32:30		m		64.63		1977.66

		S1148913024:		#B4q0		1148913024:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:36:13		20:33:00		m		64.63		1977.66

		S1148913054:		#B4q0		1148913054:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:36:43		20:33:30		m		64.63		1977.66

		S1148913084:		#B4q0		1148913084:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:37:13		20:34:00		m		64.63		1977.66

		S1148913114:		#B4q0		1148913114:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:37:43		20:34:30		m		64.63		1977.66

		S1148913144:		#B4q0		1148913144:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:38:13		20:35:00		m		64.63		1977.66

		S1148913174:		#B4q0		1148913174:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:38:43		20:35:30		m		64.63		1977.66

		S1148913204:		#B4q0		1148913204:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:39:13		20:36:00		m		64.63		1977.66

		S1148913234:		#B4q0		1148913234:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:39:43		20:36:30		m		64.63		1977.66

		S1148913264:		#B4q0		1148913264:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:40:13		20:37:00		m		64.63		1977.66

		S1148913294:		#B4q0		1148913294:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:40:43		20:37:30		m		64.63		1977.66

		S1148913324:		#B4q0		1148913324:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:41:13		20:38:00		m		64.63		1977.66

		S1148913354:		#B4q0		1148913354:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:41:43		20:38:30		m		64.63		1977.66

		S1148913384:		#B4q0		1148913384:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:42:13		20:39:00		m		64.63		1977.66

		S1148913414:		#B4q0		1148913414:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:42:43		20:39:30		m		64.63		1977.66

		S1148913444:		#B4q0		1148913444:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:43:13		20:40:00		m		64.63		1977.66

		S1148913474:		#B4q0		1148913474:		$B4q0		fc		28.96		0.00		24.51		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:43:43		20:40:30		m		64.63		1977.66

		S1148913504:		#B4q0		1148913504:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:44:13		20:41:00		m		64.63		1977.66

		S1148913534:		#B4q0		1148913534:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:44:43		20:41:30		m		64.63		1977.66

		S1148913564:		#B4q0		1148913564:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:45:13		20:42:00		m		64.63		1977.66

		S1148913594:		#B4q0		1148913594:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:45:43		20:42:30		m		64.63		1977.66

		S1148913624:		#B4q0		1148913624:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:46:13		20:43:00		m		64.63		1977.66

		S1148913654:		#B4q0		1148913654:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:46:43		20:43:30		m		64.63		1977.66

		S1148913684:		#B4q0		1148913684:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:47:13		20:44:00		m		64.63		1977.66

		S1148913714:		#B4q0		1148913714:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:47:43		20:44:30		m		64.63		1977.66

		S1148913744:		#B4q0		1148913744:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:48:13		20:45:00		m		64.63		1977.66

		S1148913774:		#B4q0		1148913774:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:48:43		20:45:30		m		64.63		1977.66

		S1148913804:		#B4q0		1148913804:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:49:13		20:46:00		m		64.63		1977.66

		S1148913834:		#B4q0		1148913834:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:49:43		20:46:30		m		64.63		1977.66

		S1148913864:		#B4q0		1148913864:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:50:13		20:47:00		m		64.63		1977.66

		S1148913894:		#B4q0		1148913894:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:50:43		20:47:30		m		64.63		1977.66

		S1148913924:		#B4q0		1148913924:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:51:13		20:48:00		m		64.63		1977.66

		S1148913954:		#B4q0		1148913954:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:51:43		20:48:30		m		64.63		1977.66

		S1148913984:		#B4q0		1148913984:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:52:13		20:49:00		m		64.63		1977.66

		S1148914014:		#B4q0		1148914014:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:52:43		20:49:30		m		64.63		1977.66

		S1148914044:		#B4q0		1148914044:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:53:13		20:50:00		m		64.63		1977.66

		S1148914074:		#B4q0		1148914074:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:53:43		20:50:30		m		64.63		1977.66

		S1148914104:		#B4q0		1148914104:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:54:13		20:51:00		m		64.63		1977.66

		S1148914134:		#B4q0		1148914134:		$B4q0		fc		28.92		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:54:43		20:51:30		m		64.63		1977.66

		S1148914164:		#B4q0		1148914164:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:55:13		20:52:00		m		64.63		1977.66

		S1148914194:		#B4q0		1148914194:		$B4q0		fc		28.96		0.00		24.51		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:55:43		20:52:30		m		64.63		1977.66

		S1148914224:		#B4q0		1148914224:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:56:13		20:53:00		m		64.63		1977.66

		S1148914254:		#B4q0		1148914254:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:56:43		20:53:30		m		64.63		1977.66

		S1148914284:		#B4q0		1148914284:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:57:13		20:54:00		m		64.63		1977.66

		S1148914314:		#B4q0		1148914314:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:57:43		20:54:30		m		64.63		1977.66

		S1148914344:		#B4q0		1148914344:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:58:13		20:55:00		m		64.63		1977.66

		S1148914374:		#B4q0		1148914374:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:58:43		20:55:30		m		64.63		1977.66

		S1148914404:		#B4q0		1148914404:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:59:13		20:56:00		m		64.63		1977.66

		S1148914434:		#B4q0		1148914434:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		21:59:43		20:56:30		m		64.63		1977.66

		S1148914464:		#B4q0		1148914464:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:00:13		20:57:00		m		64.63		1977.66

		S1148914494:		#B4q0		1148914494:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:00:43		20:57:30		m		64.63		1977.66

		S1148914524:		#B4q0		1148914524:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:01:13		20:58:00		m		64.63		1977.66

		S1148914554:		#B4q0		1148914554:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:01:43		20:58:30		m		64.63		1977.66

		S1148914584:		#B4q0		1148914584:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:02:13		20:59:00		m		64.63		1977.66

		S1148914614:		#B4q0		1148914614:		$B4q0		fc		29.00		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:02:43		20:59:30		m		64.63		1977.66

		S1148914644:		#B4q0		1148914644:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:03:13		21:00:00		m		64.63		1977.66

		S1148914674:		#B4q0		1148914674:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:03:43		21:00:30		m		64.63		1977.66

		S1148914704:		#B4q0		1148914704:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:04:13		21:01:00		m		64.63		1977.66

		S1148914734:		#B4q0		1148914734:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:04:43		21:01:30		m		64.63		1977.66

		S1148914764:		#B4q0		1148914764:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:05:13		21:02:00		m		64.63		1977.66

		S1148914794:		#B4q0		1148914794:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:05:43		21:02:30		m		64.63		1977.66

		S1148914824:		#B4q0		1148914824:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.54		0		-25228.06		22:06:13		21:03:00		m		64.63		1977.66

		S1148914854:		#B4q0		1148914854:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:06:43		21:03:30		m		64.63		1977.66

		S1148914884:		#B4q0		1148914884:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:07:13		21:04:00		m		64.63		1977.66

		S1148914914:		#B4q0		1148914914:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:07:43		21:04:30		m		64.63		1977.66

		S1148914944:		#B4q0		1148914944:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:08:13		21:05:00		m		64.63		1977.66

		S1148914974:		#B4q0		1148914974:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:08:43		21:05:30		m		64.63		1977.66

		S1148915004:		#B4q0		1148915004:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:09:13		21:06:00		m		64.63		1977.66

		S1148915034:		#B4q0		1148915034:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:09:43		21:06:30		m		64.63		1977.66

		S1148915064:		#B4q0		1148915064:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:10:13		21:07:00		m		64.63		1977.66

		S1148915094:		#B4q0		1148915094:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:10:43		21:07:30		m		64.63		1977.66

		S1148915124:		#B4q0		1148915124:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:11:13		21:08:00		m		64.63		1977.66

		S1148915154:		#B4q0		1148915154:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:11:43		21:08:30		m		64.63		1977.66

		S1148915184:		#B4q0		1148915184:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:12:13		21:09:00		m		64.63		1977.66

		S1148915214:		#B4q0		1148915214:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:12:43		21:09:30		m		64.63		1977.66

		S1148915244:		#B4q0		1148915244:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:13:13		21:10:00		m		64.63		1977.66

		S1148915274:		#B4q0		1148915274:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:13:43		21:10:30		m		64.63		1977.66

		S1148915304:		#B4q0		1148915304:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:14:13		21:11:00		m		64.63		1977.66

		S1148915334:		#B4q0		1148915334:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:14:43		21:11:30		m		64.63		1977.66

		S1148915364:		#B4q0		1148915364:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:15:13		21:12:00		m		64.63		1977.66

		S1148915394:		#B4q0		1148915394:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:15:43		21:12:30		m		64.63		1977.66

		S1148915424:		#B4q0		1148915424:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:16:13		21:13:00		m		64.63		1977.66

		S1148915454:		#B4q0		1148915454:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:16:43		21:13:30		m		64.63		1977.66

		S1148915484:		#B4q0		1148915484:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:17:13		21:14:00		m		64.63		1977.66

		S1148915514:		#B4q0		1148915514:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:17:43		21:14:30		m		64.63		1977.66

		S1148915544:		#B4q0		1148915544:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:18:13		21:15:00		m		64.63		1977.66

		S1148915574:		#B4q0		1148915574:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:18:43		21:15:30		m		64.63		1977.66

		S1148915604:		#B4q0		1148915604:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:19:13		21:16:00		m		64.63		1977.66

		S1148915634:		#B4q0		1148915634:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:19:43		21:16:30		m		64.63		1977.66

		S1148915664:		#B4q0		1148915664:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:20:13		21:17:00		m		64.63		1977.66

		S1148915694:		#B4q0		1148915694:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:20:43		21:17:30		m		64.63		1977.66

		S1148915724:		#B4q0		1148915724:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:21:13		21:18:00		m		64.63		1977.66

		S1148915754:		#B4q0		1148915754:		$B4q0		fc		28.96		0.00		24.41		3.68		3.67		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:21:43		21:18:30		m		64.63		1977.66

		S1148915784:		#B4q0		1148915784:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:22:13		21:19:00		m		64.63		1977.66

		S1148915814:		#B4q0		1148915814:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:22:43		21:19:30		m		64.63		1977.66

		S1148915844:		#B4q0		1148915844:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:23:13		21:20:00		m		64.63		1977.66

		S1148915874:		#B4q0		1148915874:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:23:43		21:20:30		m		64.63		1977.66

		S1148915904:		#B4q0		1148915904:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.47		3.63		3.67		3.55		0		-25228.06		22:24:13		21:21:00		m		64.63		1977.66

		S1148915934:		#B4q0		1148915934:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:24:43		21:21:30		m		64.63		1977.66

		S1148915964:		#B4q0		1148915964:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:25:13		21:22:00		m		64.63		1977.66

		S1148915994:		#B4q0		1148915994:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:25:43		21:22:30		m		64.63		1977.66

		S1148916024:		#B4q0		1148916024:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:26:13		21:23:00		m		64.63		1977.66

		S1148916054:		#B4q0		1148916054:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:26:43		21:23:30		m		64.63		1977.66

		S1148916084:		#B4q0		1148916084:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:27:13		21:24:00		m		64.63		1977.66

		S1148916114:		#B4q0		1148916114:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:27:43		21:24:30		m		64.63		1977.66

		S1148916144:		#B4q0		1148916144:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:28:13		21:25:00		m		64.63		1977.66

		S1148916174:		#B4q0		1148916174:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:28:43		21:25:30		m		64.63		1977.66

		S1148916204:		#B4q0		1148916204:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:29:13		21:26:00		m		64.63		1977.66

		S1148916234:		#B4q0		1148916234:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:29:43		21:26:30		m		64.63		1977.66

		S1148916264:		#B4q0		1148916264:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:30:13		21:27:00		m		64.63		1977.66

		S1148916294:		#B4q0		1148916294:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:30:43		21:27:30		m		64.63		1977.66

		S1148916324:		#B4q0		1148916324:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:31:13		21:28:00		m		64.63		1977.66

		S1148916354:		#B4q0		1148916354:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:31:43		21:28:30		m		64.63		1977.66

		S1148916384:		#B4q0		1148916384:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:32:13		21:29:00		m		64.63		1977.66

		S1148916414:		#B4q0		1148916414:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:32:43		21:29:30		m		64.63		1977.66

		S1148916444:		#B4q0		1148916444:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:33:13		21:30:00		m		64.63		1977.66

		S1148916474:		#B4q0		1148916474:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:33:43		21:30:30		m		64.63		1977.66

		S1148916504:		#B4q0		1148916504:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:34:13		21:31:00		m		64.63		1977.66

		S1148916534:		#B4q0		1148916534:		$B4q0		fc		29.00		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:34:43		21:31:30		m		64.63		1977.66

		S1148916564:		#B4q0		1148916564:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:35:13		21:32:00		m		64.63		1977.66

		S1148916594:		#B4q0		1148916594:		$B4q0		fc		28.96		0.00		24.31		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:35:43		21:32:30		m		64.63		1977.66

		S1148916624:		#B4q0		1148916624:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:36:13		21:33:00		m		64.63		1977.66

		S1148916654:		#B4q0		1148916654:		$B4q0		fc		29.00		0.00		24.31		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:36:43		21:33:30		m		64.63		1977.66

		S1148916684:		#B4q0		1148916684:		$B4q0		fc		28.96		0.00		24.41		3.68		3.68		3.68		3.62		3.48		3.63		3.67		3.55		0		-25228.06		22:37:13		21:34:00		m		64.63		1977.66





b4_q1

		S1148839044:		#B4q1		1148839044:		$B4q1		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13

		S1148839074:		#B4q1		1148839074:		$B4q1		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13

		S1148839104:		#B4q1		1148839104:		$B4q1		4.14		4.13		4.13		4.14		4.14		4.13		4.14		4.13

		S1148839134:		#B4q1		1148839134:		$B4q1		4.12		4.12		4.11		4.12		4.12		4.11		4.12		4.11

		S1148839164:		#B4q1		1148839164:		$B4q1		4.12		4.11		4.11		4.11		4.12		4.11		4.12		4.1

		S1148839194:		#B4q1		1148839194:		$B4q1		4.12		4.11		4.11		4.11		4.12		4.11		4.12		4.1

		S1148839224:		#B4q1		1148839224:		$B4q1		4.12		4.11		4.1		4.11		4.12		4.1		4.12		4.1

		S1148839254:		#B4q1		1148839254:		$B4q1		4.11		4.11		4.1		4.11		4.12		4.1		4.11		4.1

		S1148839284:		#B4q1		1148839284:		$B4q1		4.11		4.11		4.1		4.11		4.11		4.1		4.11		4.1

		S1148839314:		#B4q1		1148839314:		$B4q1		4.11		4.11		4.1		4.11		4.11		4.1		4.11		4.1

		S1148839344:		#B4q1		1148839344:		$B4q1		4.11		4.11		4.1		4.11		4.11		4.1		4.11		4.1

		S1148839374:		#B4q1		1148839374:		$B4q1		4.11		4.11		4.1		4.11		4.11		4.1		4.11		4.1

		S1148839404:		#B4q1		1148839404:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839434:		#B4q1		1148839434:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839464:		#B4q1		1148839464:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839494:		#B4q1		1148839494:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839524:		#B4q1		1148839524:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839554:		#B4q1		1148839554:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839584:		#B4q1		1148839584:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.1

		S1148839614:		#B4q1		1148839614:		$B4q1		4.11		4.1		4.1		4.1		4.11		4.1		4.11		4.09

		S1148839644:		#B4q1		1148839644:		$B4q1		4.11		4.1		4.1		4.1		4.1		4.1		4.11		4.09

		S1148839674:		#B4q1		1148839674:		$B4q1		4.1		4.1		4.1		4.1		4.1		4.1		4.1		4.09

		S1148839704:		#B4q1		1148839704:		$B4q1		4.1		4.1		4.1		4.1		4.1		4.1		4.1		4.09

		S1148839734:		#B4q1		1148839734:		$B4q1		4.1		4.1		4.1		4.1		4.1		4.1		4.1		4.09

		S1148839764:		#B4q1		1148839764:		$B4q1		4.1		4.1		4.1		4.1		4.1		4.1		4.1		4.09

		S1148839794:		#B4q1		1148839794:		$B4q1		4.1		4.1		4.1		4.1		4.1		4.1		4.1		4.09

		S1148839824:		#B4q1		1148839824:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148839854:		#B4q1		1148839854:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148839884:		#B4q1		1148839884:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148839914:		#B4q1		1148839914:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148839944:		#B4q1		1148839944:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148839974:		#B4q1		1148839974:		$B4q1		4.1		4.1		4.09		4.1		4.1		4.09		4.1		4.09

		S1148840004:		#B4q1		1148840004:		$B4q1		4.1		4.1		4.09		4.09		4.1		4.09		4.1		4.09

		S1148840034:		#B4q1		1148840034:		$B4q1		4.1		4.1		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840064:		#B4q1		1148840064:		$B4q1		4.1		4.1		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840094:		#B4q1		1148840094:		$B4q1		4.1		4.1		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840124:		#B4q1		1148840124:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840154:		#B4q1		1148840154:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840184:		#B4q1		1148840184:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840214:		#B4q1		1148840214:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840244:		#B4q1		1148840244:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840274:		#B4q1		1148840274:		$B4q1		4.1		4.09		4.09		4.09		4.1		4.09		4.1		4.08

		S1148840304:		#B4q1		1148840304:		$B4q1		4.1		4.09		4.09		4.09		4.09		4.08		4.1		4.08

		S1148840334:		#B4q1		1148840334:		$B4q1		4.1		4.09		4.08		4.09		4.09		4.08		4.1		4.08

		S1148840364:		#B4q1		1148840364:		$B4q1		4.1		4.09		4.08		4.09		4.09		4.08		4.09		4.08

		S1148840394:		#B4q1		1148840394:		$B4q1		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08

		S1148840424:		#B4q1		1148840424:		$B4q1		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08

		S1148840454:		#B4q1		1148840454:		$B4q1		4.09		4.09		4.08		4.09		4.09		4.08		4.09		4.08

		S1148840484:		#B4q1		1148840484:		$B4q1		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840514:		#B4q1		1148840514:		$B4q1		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840544:		#B4q1		1148840544:		$B4q1		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840574:		#B4q1		1148840574:		$B4q1		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840604:		#B4q1		1148840604:		$B4q1		4.09		4.09		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840634:		#B4q1		1148840634:		$B4q1		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840664:		#B4q1		1148840664:		$B4q1		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840694:		#B4q1		1148840694:		$B4q1		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.08

		S1148840724:		#B4q1		1148840724:		$B4q1		4.09		4.08		4.08		4.08		4.09		4.08		4.09		4.07

		S1148840754:		#B4q1		1148840754:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07

		S1148840784:		#B4q1		1148840784:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07

		S1148840814:		#B4q1		1148840814:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07

		S1148840844:		#B4q1		1148840844:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.09		4.07

		S1148840874:		#B4q1		1148840874:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.08		4.07

		S1148840904:		#B4q1		1148840905:		$B4q1		4.09		4.08		4.08		4.08		4.08		4.08		4.08		4.07

		S1148840934:		#B4q1		1148840934:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07

		S1148840964:		#B4q1		1148840964:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07

		S1148840994:		#B4q1		1148840994:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.08		4.08		4.07

		S1148841024:		#B4q1		1148841024:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07

		S1148841054:		#B4q1		1148841054:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07

		S1148841084:		#B4q1		1148841084:		$B4q1		4.08		4.08		4.08		4.08		4.08		4.07		4.08		4.07

		S1148841114:		#B4q1		1148841114:		$B4q1		4.08		4.08		4.07		4.08		4.08		4.07		4.08		4.07

		S1148841144:		#B4q1		1148841144:		$B4q1		4.08		4.08		4.07		4.08		4.08		4.07		4.08		4.07

		S1148841174:		#B4q1		1148841174:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841204:		#B4q1		1148841204:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841234:		#B4q1		1148841234:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841264:		#B4q1		1148841264:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841294:		#B4q1		1148841294:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841324:		#B4q1		1148841324:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841354:		#B4q1		1148841354:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841384:		#B4q1		1148841384:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841414:		#B4q1		1148841414:		$B4q1		4.08		4.08		4.07		4.07		4.08		4.07		4.08		4.07

		S1148841444:		#B4q1		1148841444:		$B4q1		4.08		4.07		4.07		4.07		4.08		4.07		4.08		4.06

		S1148841474:		#B4q1		1148841475:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841504:		#B4q1		1148841504:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841534:		#B4q1		1148841534:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841564:		#B4q1		1148841565:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841594:		#B4q1		1148841594:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841624:		#B4q1		1148841624:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841654:		#B4q1		1148841654:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.08		4.06

		S1148841684:		#B4q1		1148841684:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06

		S1148841714:		#B4q1		1148841714:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06

		S1148841744:		#B4q1		1148841744:		$B4q1		4.08		4.07		4.07		4.07		4.07		4.07		4.07		4.06

		S1148841774:		#B4q1		1148841774:		$B4q1		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06

		S1148841804:		#B4q1		1148841804:		$B4q1		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06

		S1148841834:		#B4q1		1148841834:		$B4q1		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06

		S1148841864:		#B4q1		1148841864:		$B4q1		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06

		S1148841894:		#B4q1		1148841894:		$B4q1		4.07		4.07		4.07		4.07		4.07		4.06		4.07		4.06

		S1148841924:		#B4q1		1148841924:		$B4q1		4.07		4.07		4.07		4.06		4.07		4.06		4.07		4.05

		S1148841954:		#B4q1		1148841954:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148841984:		#B4q1		1148841984:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842014:		#B4q1		1148842014:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842044:		#B4q1		1148842044:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842074:		#B4q1		1148842074:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842104:		#B4q1		1148842104:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842134:		#B4q1		1148842134:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842164:		#B4q1		1148842164:		$B4q1		4.07		4.07		4.06		4.06		4.07		4.06		4.07		4.05

		S1148842194:		#B4q1		1148842194:		$B4q1		4.07		4.07		4.06		4.06		4.06		4.06		4.07		4.05

		S1148842224:		#B4q1		1148842224:		$B4q1		4.07		4.07		4.06		4.06		4.06		4.06		4.07		4.05

		S1148842254:		#B4q1		1148842254:		$B4q1		4.07		4.06		4.06		4.06		4.06		4.06		4.07		4.05

		S1148842284:		#B4q1		1148842284:		$B4q1		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05

		S1148842314:		#B4q1		1148842314:		$B4q1		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05

		S1148842344:		#B4q1		1148842344:		$B4q1		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05

		S1148842374:		#B4q1		1148842374:		$B4q1		4.07		4.06		4.06		4.06		4.06		4.05		4.07		4.05

		S1148842404:		#B4q1		1148842404:		$B4q1		4.07		4.06		4.06		4.05		4.06		4.05		4.07		4.05

		S1148842434:		#B4q1		1148842434:		$B4q1		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05

		S1148842464:		#B4q1		1148842464:		$B4q1		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05

		S1148842494:		#B4q1		1148842494:		$B4q1		4.07		4.06		4.06		4.05		4.06		4.05		4.06		4.05

		S1148842524:		#B4q1		1148842524:		$B4q1		4.07		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842554:		#B4q1		1148842554:		$B4q1		4.07		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842584:		#B4q1		1148842584:		$B4q1		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842614:		#B4q1		1148842614:		$B4q1		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842644:		#B4q1		1148842644:		$B4q1		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842674:		#B4q1		1148842674:		$B4q1		4.06		4.06		4.05		4.05		4.06		4.05		4.06		4.05

		S1148842704:		#B4q1		1148842704:		$B4q1		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842734:		#B4q1		1148842734:		$B4q1		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842764:		#B4q1		1148842764:		$B4q1		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842794:		#B4q1		1148842794:		$B4q1		4.06		4.06		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842824:		#B4q1		1148842824:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842854:		#B4q1		1148842854:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842884:		#B4q1		1148842884:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842914:		#B4q1		1148842914:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.06		4.04

		S1148842944:		#B4q1		1148842944:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148842974:		#B4q1		1148842974:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148843004:		#B4q1		1148843004:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148843034:		#B4q1		1148843034:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148843064:		#B4q1		1148843064:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148843094:		#B4q1		1148843094:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.05		4.05		4.04

		S1148843124:		#B4q1		1148843124:		$B4q1		4.06		4.05		4.05		4.05		4.05		4.04		4.05		4.04

		S1148843154:		#B4q1		1148843154:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.04

		S1148843184:		#B4q1		1148843184:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.04

		S1148843214:		#B4q1		1148843214:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843244:		#B4q1		1148843244:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843274:		#B4q1		1148843274:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843304:		#B4q1		1148843304:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843334:		#B4q1		1148843334:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843364:		#B4q1		1148843364:		$B4q1		4.05		4.05		4.05		4.04		4.05		4.04		4.05		4.03

		S1148843394:		#B4q1		1148843394:		$B4q1		4.05		4.05		4.04		4.04		4.05		4.04		4.05		4.03

		S1148843424:		#B4q1		1148843424:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843454:		#B4q1		1148843454:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843484:		#B4q1		1148843484:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843514:		#B4q1		1148843514:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843544:		#B4q1		1148843544:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843574:		#B4q1		1148843574:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843604:		#B4q1		1148843604:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843634:		#B4q1		1148843634:		$B4q1		4.05		4.05		4.04		4.04		4.04		4.04		4.05		4.03

		S1148843664:		#B4q1		1148843664:		$B4q1		4.05		4.05		4.04		4.03		4.04		4.03		4.05		4.03

		S1148843694:		#B4q1		1148843694:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03

		S1148843724:		#B4q1		1148843724:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03

		S1148843754:		#B4q1		1148843754:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.05		4.03

		S1148843784:		#B4q1		1148843784:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03

		S1148843814:		#B4q1		1148843814:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03

		S1148843844:		#B4q1		1148843844:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03

		S1148843874:		#B4q1		1148843874:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03

		S1148843904:		#B4q1		1148843904:		$B4q1		4.05		4.04		4.04		4.03		4.04		4.03		4.04		4.03

		S1148843934:		#B4q1		1148843934:		$B4q1		4.05		4.04		4.04		4.03		4.03		4.03		4.04		4.03

		S1148843964:		#B4q1		1148843964:		$B4q1		4.05		4.04		4.04		4.03		4.03		4.03		4.04		4.03

		S1148843994:		#B4q1		1148843994:		$B4q1		4.05		4.04		4.03		4.03		4.03		4.03		4.04		4.03

		S1148844024:		#B4q1		1148844024:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844054:		#B4q1		1148844054:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844084:		#B4q1		1148844084:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844114:		#B4q1		1148844114:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844144:		#B4q1		1148844144:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844174:		#B4q1		1148844174:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844204:		#B4q1		1148844204:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844234:		#B4q1		1148844234:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844264:		#B4q1		1148844264:		$B4q1		4.04		4.04		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844294:		#B4q1		1148844294:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844324:		#B4q1		1148844324:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.04		4.02

		S1148844354:		#B4q1		1148844354:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02

		S1148844384:		#B4q1		1148844384:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02

		S1148844414:		#B4q1		1148844414:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02

		S1148844444:		#B4q1		1148844444:		$B4q1		4.04		4.03		4.03		4.03		4.03		4.03		4.03		4.02

		S1148844474:		#B4q1		1148844474:		$B4q1		4.04		4.03		4.03		4.02		4.03		4.03		4.03		4.02

		S1148844504:		#B4q1		1148844504:		$B4q1		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.02

		S1148844534:		#B4q1		1148844534:		$B4q1		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.02

		S1148844564:		#B4q1		1148844564:		$B4q1		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844594:		#B4q1		1148844594:		$B4q1		4.04		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844624:		#B4q1		1148844624:		$B4q1		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844654:		#B4q1		1148844654:		$B4q1		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844684:		#B4q1		1148844684:		$B4q1		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844714:		#B4q1		1148844714:		$B4q1		4.03		4.03		4.03		4.02		4.03		4.02		4.03		4.01

		S1148844744:		#B4q1		1148844744:		$B4q1		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01

		S1148844774:		#B4q1		1148844774:		$B4q1		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01

		S1148844804:		#B4q1		1148844804:		$B4q1		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01

		S1148844834:		#B4q1		1148844834:		$B4q1		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01

		S1148844864:		#B4q1		1148844864:		$B4q1		4.03		4.03		4.03		4.02		4.02		4.02		4.03		4.01

		S1148844894:		#B4q1		1148844894:		$B4q1		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01

		S1148844924:		#B4q1		1148844924:		$B4q1		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01

		S1148844954:		#B4q1		1148844954:		$B4q1		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01

		S1148844984:		#B4q1		1148844984:		$B4q1		4.03		4.03		4.02		4.02		4.02		4.02		4.03		4.01

		S1148845014:		#B4q1		1148845014:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.02		4.03		4.01

		S1148845044:		#B4q1		1148845044:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.02		4.03		4.01

		S1148845074:		#B4q1		1148845074:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01

		S1148845104:		#B4q1		1148845104:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01

		S1148845134:		#B4q1		1148845134:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01

		S1148845164:		#B4q1		1148845164:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.01		4.03		4.01

		S1148845194:		#B4q1		1148845194:		$B4q1		4.03		4.03		4.02		4.01		4.02		4.01		4.02		4.01

		S1148845224:		#B4q1		1148845224:		$B4q1		4.03		4.02		4.02		4.01		4.02		4.01		4.02		4.01

		S1148845254:		#B4q1		1148845254:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01

		S1148845284:		#B4q1		1148845284:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01

		S1148845314:		#B4q1		1148845314:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01

		S1148845344:		#B4q1		1148845344:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4.01

		S1148845374:		#B4q1		1148845374:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4

		S1148845404:		#B4q1		1148845404:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4

		S1148845434:		#B4q1		1148845434:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4

		S1148845464:		#B4q1		1148845464:		$B4q1		4.03		4.02		4.02		4.01		4.01		4.01		4.02		4

		S1148845494:		#B4q1		1148845494:		$B4q1		4.03		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845524:		#B4q1		1148845524:		$B4q1		4.03		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845554:		#B4q1		1148845555:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845584:		#B4q1		1148845584:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845614:		#B4q1		1148845614:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845644:		#B4q1		1148845644:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845674:		#B4q1		1148845674:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845704:		#B4q1		1148845704:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845734:		#B4q1		1148845734:		$B4q1		4.02		4.02		4.01		4.01		4.01		4.01		4.02		4

		S1148845764:		#B4q1		1148845764:		$B4q1		4.02		4.01		4.01		4		4.01		4.01		4.02		4

		S1148845794:		#B4q1		1148845794:		$B4q1		4.02		4.01		4.01		4.01		4.01		4.01		4.01		4

		S1148845824:		#B4q1		1148845824:		$B4q1		4.02		4.01		4.01		4		4.01		4.01		4.01		4

		S1148845854:		#B4q1		1148845854:		$B4q1		4.02		4.01		4.01		4		4.01		4.01		4.01		4

		S1148845884:		#B4q1		1148845884:		$B4q1		4.02		4.01		4.01		4		4.01		4		4.01		4

		S1148845914:		#B4q1		1148845914:		$B4q1		4.02		4.01		4.01		4		4.01		4		4.01		4

		S1148845944:		#B4q1		1148845944:		$B4q1		4.02		4.01		4.01		4		4.01		4		4.01		4

		S1148845974:		#B4q1		1148845974:		$B4q1		4.02		4.01		4.01		4		4.01		4		4.01		4

		S1148846004:		#B4q1		1148846004:		$B4q1		4.02		4.01		4.01		4		4		4		4.01		4

		S1148846034:		#B4q1		1148846034:		$B4q1		4.02		4.01		4.01		4		4		4		4.01		4

		S1148846064:		#B4q1		1148846064:		$B4q1		4.02		4.01		4.01		4		4		4		4.01		4

		S1148846094:		#B4q1		1148846094:		$B4q1		4.02		4.01		4.01		4		4		4		4.01		4

		S1148846124:		#B4q1		1148846124:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		4

		S1148846154:		#B4q1		1148846154:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		4

		S1148846184:		#B4q1		1148846184:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846214:		#B4q1		1148846214:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846244:		#B4q1		1148846244:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846274:		#B4q1		1148846274:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846304:		#B4q1		1148846304:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846334:		#B4q1		1148846334:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846364:		#B4q1		1148846364:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846394:		#B4q1		1148846394:		$B4q1		4.01		4.01		4.01		4		4		4		4.01		3.99

		S1148846424:		#B4q1		1148846424:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846454:		#B4q1		1148846454:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846484:		#B4q1		1148846484:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846514:		#B4q1		1148846514:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846544:		#B4q1		1148846544:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846574:		#B4q1		1148846574:		$B4q1		4.01		4.01		4		4		4		4		4.01		3.99

		S1148846604:		#B4q1		1148846604:		$B4q1		4.01		4.01		4		3.99		4		4		4		3.99

		S1148846634:		#B4q1		1148846634:		$B4q1		4.01		4.01		4		4		4		4		4		3.99

		S1148846664:		#B4q1		1148846664:		$B4q1		4.01		4.01		4		3.99		4		4		4		3.99

		S1148846694:		#B4q1		1148846694:		$B4q1		4.01		4		4		3.99		4		4		4		3.99

		S1148846724:		#B4q1		1148846724:		$B4q1		4.01		4		4		3.99		4		4		4		3.98

		S1148846754:		#B4q1		1148846754:		$B4q1		4.01		4		4		3.99		3.99		4		4		3.98

		S1148846784:		#B4q1		1148846784:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846814:		#B4q1		1148846814:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846844:		#B4q1		1148846844:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846874:		#B4q1		1148846874:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846904:		#B4q1		1148846904:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846934:		#B4q1		1148846934:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846964:		#B4q1		1148846964:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148846994:		#B4q1		1148846994:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148847024:		#B4q1		1148847024:		$B4q1		4.01		4		4		3.99		3.99		3.99		4		3.98

		S1148847054:		#B4q1		1148847054:		$B4q1		4		4		4		3.99		3.99		3.99		4		3.98

		S1148847084:		#B4q1		1148847084:		$B4q1		4		4		4		3.99		3.99		3.99		4		3.98

		S1148847114:		#B4q1		1148847114:		$B4q1		4		4		4		3.99		3.99		3.99		4		3.98

		S1148847144:		#B4q1		1148847144:		$B4q1		4		4		4		3.99		3.99		3.99		4		3.98

		S1148847174:		#B4q1		1148847174:		$B4q1		4		4		4		3.98		3.99		3.99		4		3.98

		S1148847204:		#B4q1		1148847204:		$B4q1		4		4		4		3.98		3.99		3.99		4		3.98

		S1148847234:		#B4q1		1148847234:		$B4q1		4		4		4		3.98		3.99		3.99		4		3.98

		S1148847264:		#B4q1		1148847264:		$B4q1		4		4		4		3.98		3.99		3.99		4		3.98

		S1148847294:		#B4q1		1148847294:		$B4q1		4		4		4		3.98		3.98		3.99		4		3.98

		S1148847324:		#B4q1		1148847324:		$B4q1		4		4		4		3.98		3.98		3.99		4		3.98

		S1148847354:		#B4q1		1148847354:		$B4q1		4		4		3.99		3.98		3.98		3.98		4		3.98

		S1148847384:		#B4q1		1148847384:		$B4q1		4		4		3.99		3.98		3.98		3.98		4		3.98

		S1148847414:		#B4q1		1148847414:		$B4q1		4		4		3.99		3.98		3.98		3.98		4		3.98

		S1148847444:		#B4q1		1148847444:		$B4q1		4		4		3.99		3.98		3.98		3.98		4		3.98

		S1148847474:		#B4q1		1148847474:		$B4q1		4		4		3.99		3.98		3.98		3.98		4		3.98

		S1148847504:		#B4q1		1148847504:		$B4q1		4		4		3.99		3.98		3.98		3.98		3.99		3.98

		S1148847534:		#B4q1		1148847534:		$B4q1		4		4		3.99		3.98		3.98		3.98		3.99		3.98

		S1148847564:		#B4q1		1148847564:		$B4q1		4		4		3.99		3.98		3.98		3.98		3.99		3.98

		S1148847594:		#B4q1		1148847594:		$B4q1		4		4		3.99		3.98		3.98		3.98		3.99		3.98

		S1148847624:		#B4q1		1148847624:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847654:		#B4q1		1148847654:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847684:		#B4q1		1148847684:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847714:		#B4q1		1148847714:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847744:		#B4q1		1148847744:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847774:		#B4q1		1148847774:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847804:		#B4q1		1148847804:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847834:		#B4q1		1148847834:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847864:		#B4q1		1148847864:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847894:		#B4q1		1148847894:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847924:		#B4q1		1148847924:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847954:		#B4q1		1148847954:		$B4q1		4		3.99		3.99		3.98		3.98		3.98		3.99		3.97

		S1148847984:		#B4q1		1148847984:		$B4q1		3.99		3.99		3.98		3.98		3.98		3.98		3.99		3.97

		S1148848014:		#B4q1		1148848014:		$B4q1		3.99		3.99		3.98		3.98		3.98		3.98		3.99		3.97

		S1148848044:		#B4q1		1148848044:		$B4q1		3.99		3.99		3.98		3.97		3.98		3.98		3.99		3.97

		S1148848074:		#B4q1		1148848074:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.98		3.99		3.97

		S1148848104:		#B4q1		1148848104:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.98		3.99		3.97

		S1148848134:		#B4q1		1148848134:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97

		S1148848164:		#B4q1		1148848164:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97

		S1148848194:		#B4q1		1148848194:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.98		3.98		3.97

		S1148848224:		#B4q1		1148848224:		$B4q1		3.99		3.99		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848254:		#B4q1		1148848254:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848284:		#B4q1		1148848284:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848314:		#B4q1		1148848314:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848344:		#B4q1		1148848344:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848374:		#B4q1		1148848374:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848404:		#B4q1		1148848404:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848434:		#B4q1		1148848434:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848464:		#B4q1		1148848464:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848494:		#B4q1		1148848494:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848524:		#B4q1		1148848524:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848554:		#B4q1		1148848554:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848584:		#B4q1		1148848584:		$B4q1		3.99		3.98		3.98		3.97		3.97		3.97		3.98		3.96

		S1148848614:		#B4q1		1148848614:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848644:		#B4q1		1148848644:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848674:		#B4q1		1148848674:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848704:		#B4q1		1148848704:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848734:		#B4q1		1148848734:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848764:		#B4q1		1148848764:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848794:		#B4q1		1148848794:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848824:		#B4q1		1148848824:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848854:		#B4q1		1148848854:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.97		3.98		3.96

		S1148848884:		#B4q1		1148848884:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.96		3.98		3.96

		S1148848914:		#B4q1		1148848914:		$B4q1		3.98		3.98		3.98		3.96		3.96		3.96		3.98		3.96

		S1148848944:		#B4q1		1148848944:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.98		3.96

		S1148848974:		#B4q1		1148848974:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.98		3.96

		S1148849004:		#B4q1		1148849004:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96

		S1148849034:		#B4q1		1148849034:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96

		S1148849064:		#B4q1		1148849064:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.96

		S1148849094:		#B4q1		1148849094:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849124:		#B4q1		1148849124:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849154:		#B4q1		1148849154:		$B4q1		3.98		3.98		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849184:		#B4q1		1148849184:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849214:		#B4q1		1148849214:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849244:		#B4q1		1148849244:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849274:		#B4q1		1148849274:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849304:		#B4q1		1148849304:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849334:		#B4q1		1148849334:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849364:		#B4q1		1148849364:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849394:		#B4q1		1148849394:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849424:		#B4q1		1148849424:		$B4q1		3.98		3.97		3.97		3.96		3.96		3.96		3.97		3.95

		S1148849454:		#B4q1		1148849454:		$B4q1		3.98		3.97		3.97		3.96		3.95		3.96		3.97		3.95

		S1148849484:		#B4q1		1148849484:		$B4q1		3.98		3.97		3.97		3.95		3.95		3.96		3.97		3.95

		S1148849514:		#B4q1		1148849514:		$B4q1		3.98		3.97		3.97		3.95		3.95		3.96		3.97		3.95

		S1148849544:		#B4q1		1148849544:		$B4q1		3.97		3.97		3.97		3.95		3.95		3.96		3.97		3.95

		S1148849574:		#B4q1		1148849574:		$B4q1		3.97		3.97		3.97		3.95		3.95		3.96		3.97		3.95

		S1148849604:		#B4q1		1148849604:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.97		3.95

		S1148849634:		#B4q1		1148849634:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95

		S1148849664:		#B4q1		1148849664:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95

		S1148849694:		#B4q1		1148849694:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.95

		S1148849724:		#B4q1		1148849724:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.94

		S1148849754:		#B4q1		1148849754:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.96		3.96		3.94

		S1148849784:		#B4q1		1148849784:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849814:		#B4q1		1148849814:		$B4q1		3.97		3.97		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849844:		#B4q1		1148849844:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849874:		#B4q1		1148849874:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849904:		#B4q1		1148849904:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849934:		#B4q1		1148849934:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849964:		#B4q1		1148849964:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148849994:		#B4q1		1148849994:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148850024:		#B4q1		1148850024:		$B4q1		3.97		3.96		3.96		3.95		3.95		3.95		3.96		3.94

		S1148850054:		#B4q1		1148850054:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850084:		#B4q1		1148850084:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850114:		#B4q1		1148850114:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850144:		#B4q1		1148850144:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850174:		#B4q1		1148850174:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850204:		#B4q1		1148850204:		$B4q1		3.97		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850234:		#B4q1		1148850234:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850264:		#B4q1		1148850264:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850294:		#B4q1		1148850294:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850324:		#B4q1		1148850324:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850354:		#B4q1		1148850354:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850384:		#B4q1		1148850384:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.95		3.96		3.94

		S1148850414:		#B4q1		1148850414:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850444:		#B4q1		1148850444:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850474:		#B4q1		1148850474:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850504:		#B4q1		1148850504:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850534:		#B4q1		1148850534:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850564:		#B4q1		1148850564:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.96		3.94

		S1148850594:		#B4q1		1148850594:		$B4q1		3.96		3.96		3.96		3.94		3.94		3.94		3.95		3.94

		S1148850624:		#B4q1		1148850624:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.94

		S1148850654:		#B4q1		1148850654:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850684:		#B4q1		1148850684:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850714:		#B4q1		1148850714:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850744:		#B4q1		1148850744:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850774:		#B4q1		1148850774:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850804:		#B4q1		1148850804:		$B4q1		3.96		3.96		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850834:		#B4q1		1148850834:		$B4q1		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850864:		#B4q1		1148850864:		$B4q1		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850894:		#B4q1		1148850894:		$B4q1		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850924:		#B4q1		1148850924:		$B4q1		3.96		3.95		3.95		3.94		3.94		3.94		3.95		3.93

		S1148850954:		#B4q1		1148850954:		$B4q1		3.96		3.95		3.95		3.94		3.93		3.94		3.95		3.93

		S1148850984:		#B4q1		1148850984:		$B4q1		3.96		3.95		3.95		3.94		3.93		3.94		3.95		3.93

		S1148851014:		#B4q1		1148851014:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851044:		#B4q1		1148851044:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851074:		#B4q1		1148851074:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851104:		#B4q1		1148851104:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851134:		#B4q1		1148851134:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851164:		#B4q1		1148851164:		$B4q1		3.96		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851194:		#B4q1		1148851194:		$B4q1		3.95		3.95		3.95		3.93		3.93		3.94		3.95		3.93

		S1148851224:		#B4q1		1148851224:		$B4q1		3.95		3.95		3.95		3.93		3.93		3.94		3.94		3.93

		S1148851254:		#B4q1		1148851254:		$B4q1		3.95		3.95		3.95		3.93		3.93		3.94		3.94		3.93

		S1148851284:		#B4q1		1148851284:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92

		S1148851314:		#B4q1		1148851314:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92

		S1148851344:		#B4q1		1148851344:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.94		3.94		3.92

		S1148851374:		#B4q1		1148851374:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851404:		#B4q1		1148851404:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851434:		#B4q1		1148851434:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851464:		#B4q1		1148851464:		$B4q1		3.95		3.95		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851494:		#B4q1		1148851494:		$B4q1		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851524:		#B4q1		1148851524:		$B4q1		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851554:		#B4q1		1148851554:		$B4q1		3.95		3.94		3.94		3.93		3.93		3.93		3.94		3.92

		S1148851584:		#B4q1		1148851584:		$B4q1		3.95		3.94		3.94		3.93		3.92		3.93		3.94		3.92

		S1148851614:		#B4q1		1148851614:		$B4q1		3.95		3.94		3.94		3.93		3.92		3.93		3.94		3.92

		S1148851644:		#B4q1		1148851644:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851674:		#B4q1		1148851674:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851704:		#B4q1		1148851704:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851734:		#B4q1		1148851734:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851764:		#B4q1		1148851764:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851794:		#B4q1		1148851794:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851824:		#B4q1		1148851824:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851854:		#B4q1		1148851854:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851884:		#B4q1		1148851884:		$B4q1		3.95		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851914:		#B4q1		1148851914:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851944:		#B4q1		1148851944:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148851974:		#B4q1		1148851974:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148852004:		#B4q1		1148852004:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.93		3.94		3.92

		S1148852034:		#B4q1		1148852034:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92

		S1148852064:		#B4q1		1148852064:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92

		S1148852094:		#B4q1		1148852094:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92

		S1148852124:		#B4q1		1148852124:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92

		S1148852154:		#B4q1		1148852154:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.92

		S1148852184:		#B4q1		1148852184:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.91

		S1148852214:		#B4q1		1148852214:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.94		3.91

		S1148852244:		#B4q1		1148852244:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91

		S1148852274:		#B4q1		1148852274:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91

		S1148852304:		#B4q1		1148852304:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91

		S1148852334:		#B4q1		1148852334:		$B4q1		3.94		3.94		3.94		3.92		3.92		3.92		3.93		3.91

		S1148852364:		#B4q1		1148852364:		$B4q1		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91

		S1148852394:		#B4q1		1148852394:		$B4q1		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91

		S1148852424:		#B4q1		1148852424:		$B4q1		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91

		S1148852454:		#B4q1		1148852454:		$B4q1		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91

		S1148852484:		#B4q1		1148852484:		$B4q1		3.94		3.94		3.93		3.92		3.92		3.92		3.93		3.91

		S1148852514:		#B4q1		1148852514:		$B4q1		3.94		3.94		3.93		3.92		3.91		3.92		3.93		3.91

		S1148852544:		#B4q1		1148852544:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852574:		#B4q1		1148852574:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852604:		#B4q1		1148852604:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852634:		#B4q1		1148852634:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852664:		#B4q1		1148852664:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852694:		#B4q1		1148852694:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852724:		#B4q1		1148852724:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852754:		#B4q1		1148852754:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852784:		#B4q1		1148852784:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852814:		#B4q1		1148852814:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852844:		#B4q1		1148852844:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852874:		#B4q1		1148852874:		$B4q1		3.94		3.93		3.93		3.91		3.91		3.92		3.93		3.91

		S1148852904:		#B4q1		1148852904:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91

		S1148852934:		#B4q1		1148852934:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91

		S1148852964:		#B4q1		1148852964:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.92		3.92		3.91

		S1148852994:		#B4q1		1148852994:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91

		S1148853024:		#B4q1		1148853024:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91

		S1148853054:		#B4q1		1148853054:		$B4q1		3.93		3.93		3.93		3.91		3.91		3.91		3.92		3.91

		S1148853084:		#B4q1		1148853084:		$B4q1		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853114:		#B4q1		1148853114:		$B4q1		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853144:		#B4q1		1148853144:		$B4q1		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853174:		#B4q1		1148853174:		$B4q1		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853204:		#B4q1		1148853204:		$B4q1		3.93		3.93		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853234:		#B4q1		1148853234:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853264:		#B4q1		1148853264:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853294:		#B4q1		1148853294:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853324:		#B4q1		1148853324:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853354:		#B4q1		1148853354:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853384:		#B4q1		1148853384:		$B4q1		3.93		3.92		3.92		3.91		3.91		3.91		3.92		3.9

		S1148853414:		#B4q1		1148853414:		$B4q1		3.93		3.92		3.92		3.91		3.9		3.91		3.92		3.9

		S1148853444:		#B4q1		1148853444:		$B4q1		3.93		3.92		3.92		3.91		3.9		3.91		3.92		3.9

		S1148853474:		#B4q1		1148853474:		$B4q1		3.93		3.92		3.92		3.91		3.9		3.91		3.92		3.9

		S1148853504:		#B4q1		1148853504:		$B4q1		3.93		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853534:		#B4q1		1148853534:		$B4q1		3.93		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853564:		#B4q1		1148853564:		$B4q1		3.93		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853594:		#B4q1		1148853594:		$B4q1		3.93		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853624:		#B4q1		1148853624:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853654:		#B4q1		1148853654:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.9

		S1148853684:		#B4q1		1148853684:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853714:		#B4q1		1148853714:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853744:		#B4q1		1148853744:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853774:		#B4q1		1148853774:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853804:		#B4q1		1148853804:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853834:		#B4q1		1148853834:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853864:		#B4q1		1148853864:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853894:		#B4q1		1148853894:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.91		3.92		3.89

		S1148853924:		#B4q1		1148853924:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.9		3.91		3.89

		S1148853954:		#B4q1		1148853954:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.9		3.91		3.89

		S1148853984:		#B4q1		1148853984:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.9		3.91		3.89

		S1148854014:		#B4q1		1148854014:		$B4q1		3.92		3.92		3.92		3.9		3.9		3.9		3.91		3.89

		S1148854044:		#B4q1		1148854044:		$B4q1		3.92		3.92		3.92		3.9		3.89		3.9		3.91		3.89

		S1148854074:		#B4q1		1148854074:		$B4q1		3.92		3.92		3.92		3.9		3.89		3.9		3.91		3.89

		S1148854104:		#B4q1		1148854104:		$B4q1		3.92		3.92		3.91		3.9		3.89		3.9		3.91		3.89

		S1148854134:		#B4q1		1148854134:		$B4q1		3.92		3.92		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854164:		#B4q1		1148854164:		$B4q1		3.92		3.92		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854194:		#B4q1		1148854194:		$B4q1		3.92		3.92		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854224:		#B4q1		1148854224:		$B4q1		3.92		3.92		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854254:		#B4q1		1148854254:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854284:		#B4q1		1148854284:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854314:		#B4q1		1148854314:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854344:		#B4q1		1148854344:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854374:		#B4q1		1148854374:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854404:		#B4q1		1148854404:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854434:		#B4q1		1148854434:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854464:		#B4q1		1148854464:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854494:		#B4q1		1148854494:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854524:		#B4q1		1148854524:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.9		3.91		3.89

		S1148854554:		#B4q1		1148854554:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.89

		S1148854584:		#B4q1		1148854584:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854614:		#B4q1		1148854614:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854644:		#B4q1		1148854644:		$B4q1		3.92		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854674:		#B4q1		1148854674:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854704:		#B4q1		1148854704:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854734:		#B4q1		1148854734:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854764:		#B4q1		1148854764:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854794:		#B4q1		1148854794:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854824:		#B4q1		1148854824:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854854:		#B4q1		1148854854:		$B4q1		3.91		3.91		3.91		3.89		3.89		3.89		3.91		3.88

		S1148854884:		#B4q1		1148854884:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.91		3.88

		S1148854914:		#B4q1		1148854914:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.9		3.88

		S1148854944:		#B4q1		1148854944:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.9		3.88

		S1148854974:		#B4q1		1148854974:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.9		3.88

		S1148855004:		#B4q1		1148855004:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.9		3.88

		S1148855034:		#B4q1		1148855034:		$B4q1		3.91		3.91		3.91		3.89		3.88		3.89		3.9		3.88

		S1148855064:		#B4q1		1148855064:		$B4q1		3.91		3.91		3.91		3.88		3.88		3.89		3.9		3.88

		S1148855094:		#B4q1		1148855094:		$B4q1		3.91		3.91		3.91		3.88		3.88		3.89		3.9		3.88

		S1148855124:		#B4q1		1148855124:		$B4q1		3.91		3.91		3.91		3.88		3.88		3.89		3.9		3.88

		S1148855154:		#B4q1		1148855154:		$B4q1		3.91		3.91		3.91		3.88		3.88		3.89		3.9		3.88

		S1148855184:		#B4q1		1148855184:		$B4q1		3.91		3.91		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855214:		#B4q1		1148855214:		$B4q1		3.91		3.91		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855244:		#B4q1		1148855244:		$B4q1		3.91		3.91		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855274:		#B4q1		1148855274:		$B4q1		3.91		3.91		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855304:		#B4q1		1148855304:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855334:		#B4q1		1148855334:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855364:		#B4q1		1148855364:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855394:		#B4q1		1148855394:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855424:		#B4q1		1148855424:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855454:		#B4q1		1148855454:		$B4q1		3.91		3.9		3.9		3.88		3.88		3.89		3.9		3.87

		S1148855484:		#B4q1		1148855484:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.89		3.9		3.87

		S1148855514:		#B4q1		1148855514:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.88		3.9		3.87

		S1148855544:		#B4q1		1148855544:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.88		3.9		3.87

		S1148855574:		#B4q1		1148855574:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.88		3.89		3.87

		S1148855604:		#B4q1		1148855604:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.88		3.89		3.87

		S1148855634:		#B4q1		1148855634:		$B4q1		3.91		3.9		3.9		3.88		3.87		3.88		3.89		3.87

		S1148855664:		#B4q1		1148855664:		$B4q1		3.91		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855694:		#B4q1		1148855694:		$B4q1		3.91		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855724:		#B4q1		1148855724:		$B4q1		3.9		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855754:		#B4q1		1148855754:		$B4q1		3.9		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855784:		#B4q1		1148855784:		$B4q1		3.9		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855814:		#B4q1		1148855814:		$B4q1		3.9		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855844:		#B4q1		1148855844:		$B4q1		3.9		3.9		3.9		3.87		3.87		3.88		3.89		3.87

		S1148855874:		#B4q1		1148855874:		$B4q1		3.9		3.9		3.89		3.87		3.87		3.88		3.89		3.87

		S1148855904:		#B4q1		1148855904:		$B4q1		3.9		3.9		3.89		3.87		3.87		3.88		3.89		3.87

		S1148855934:		#B4q1		1148855934:		$B4q1		3.9		3.9		3.89		3.87		3.87		3.88		3.89		3.87

		S1148855964:		#B4q1		1148855964:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.87

		S1148855994:		#B4q1		1148855994:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.87

		S1148856024:		#B4q1		1148856024:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.87

		S1148856054:		#B4q1		1148856054:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.87

		S1148856084:		#B4q1		1148856084:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.86

		S1148856114:		#B4q1		1148856114:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.88		3.89		3.86

		S1148856144:		#B4q1		1148856144:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856174:		#B4q1		1148856174:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856204:		#B4q1		1148856204:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856234:		#B4q1		1148856234:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856264:		#B4q1		1148856264:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856294:		#B4q1		1148856294:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856324:		#B4q1		1148856324:		$B4q1		3.9		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856354:		#B4q1		1148856354:		$B4q1		3.89		3.89		3.89		3.87		3.87		3.87		3.89		3.86

		S1148856384:		#B4q1		1148856384:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86

		S1148856414:		#B4q1		1148856414:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86

		S1148856444:		#B4q1		1148856444:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86

		S1148856474:		#B4q1		1148856474:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86

		S1148856504:		#B4q1		1148856504:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.89		3.86

		S1148856534:		#B4q1		1148856534:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.88		3.86

		S1148856564:		#B4q1		1148856564:		$B4q1		3.89		3.89		3.89		3.87		3.86		3.87		3.88		3.86

		S1148856594:		#B4q1		1148856594:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86

		S1148856624:		#B4q1		1148856624:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86

		S1148856654:		#B4q1		1148856654:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86

		S1148856684:		#B4q1		1148856684:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.86

		S1148856714:		#B4q1		1148856714:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85

		S1148856744:		#B4q1		1148856744:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85

		S1148856774:		#B4q1		1148856774:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85

		S1148856804:		#B4q1		1148856804:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85

		S1148856834:		#B4q1		1148856834:		$B4q1		3.89		3.89		3.89		3.86		3.86		3.87		3.88		3.85

		S1148856864:		#B4q1		1148856864:		$B4q1		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85

		S1148856894:		#B4q1		1148856894:		$B4q1		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85

		S1148856924:		#B4q1		1148856924:		$B4q1		3.89		3.89		3.88		3.86		3.86		3.87		3.88		3.85

		S1148856954:		#B4q1		1148856954:		$B4q1		3.89		3.88		3.88		3.86		3.86		3.87		3.88		3.85

		S1148856984:		#B4q1		1148856984:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85

		S1148857014:		#B4q1		1148857014:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85

		S1148857044:		#B4q1		1148857044:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.87		3.88		3.85

		S1148857074:		#B4q1		1148857074:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85

		S1148857104:		#B4q1		1148857104:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85

		S1148857134:		#B4q1		1148857134:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.86		3.88		3.85

		S1148857164:		#B4q1		1148857164:		$B4q1		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857194:		#B4q1		1148857194:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.86		3.87		3.85

		S1148857224:		#B4q1		1148857224:		$B4q1		3.89		3.88		3.88		3.86		3.85		3.86		3.87		3.85

		S1148857254:		#B4q1		1148857254:		$B4q1		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857284:		#B4q1		1148857284:		$B4q1		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857314:		#B4q1		1148857314:		$B4q1		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857344:		#B4q1		1148857344:		$B4q1		3.89		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857374:		#B4q1		1148857374:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857404:		#B4q1		1148857404:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857434:		#B4q1		1148857434:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857464:		#B4q1		1148857464:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857494:		#B4q1		1148857494:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857524:		#B4q1		1148857524:		$B4q1		3.88		3.88		3.88		3.85		3.85		3.86		3.87		3.85

		S1148857554:		#B4q1		1148857554:		$B4q1		3.88		3.88		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857584:		#B4q1		1148857584:		$B4q1		3.88		3.88		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857614:		#B4q1		1148857614:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857644:		#B4q1		1148857644:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857674:		#B4q1		1148857674:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857704:		#B4q1		1148857704:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.86		3.87		3.85

		S1148857734:		#B4q1		1148857734:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857764:		#B4q1		1148857764:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857794:		#B4q1		1148857794:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857824:		#B4q1		1148857824:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857854:		#B4q1		1148857854:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857884:		#B4q1		1148857884:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857914:		#B4q1		1148857914:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857944:		#B4q1		1148857944:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148857974:		#B4q1		1148857974:		$B4q1		3.88		3.87		3.87		3.85		3.85		3.85		3.87		3.84

		S1148858004:		#B4q1		1148858004:		$B4q1		3.88		3.87		3.87		3.85		3.84		3.85		3.87		3.84

		S1148858034:		#B4q1		1148858034:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84

		S1148858064:		#B4q1		1148858064:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84

		S1148858094:		#B4q1		1148858094:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.87		3.84

		S1148858124:		#B4q1		1148858124:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84

		S1148858154:		#B4q1		1148858154:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84

		S1148858184:		#B4q1		1148858184:		$B4q1		3.87		3.87		3.87		3.85		3.84		3.85		3.86		3.84

		S1148858214:		#B4q1		1148858214:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858244:		#B4q1		1148858244:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858274:		#B4q1		1148858274:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858304:		#B4q1		1148858304:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858334:		#B4q1		1148858334:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858364:		#B4q1		1148858364:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858394:		#B4q1		1148858394:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858424:		#B4q1		1148858424:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858454:		#B4q1		1148858454:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858484:		#B4q1		1148858484:		$B4q1		3.87		3.87		3.87		3.84		3.84		3.85		3.86		3.84

		S1148858514:		#B4q1		1148858514:		$B4q1		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.84

		S1148858544:		#B4q1		1148858544:		$B4q1		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858574:		#B4q1		1148858574:		$B4q1		3.87		3.87		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858604:		#B4q1		1148858604:		$B4q1		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858634:		#B4q1		1148858634:		$B4q1		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858664:		#B4q1		1148858664:		$B4q1		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858694:		#B4q1		1148858694:		$B4q1		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858724:		#B4q1		1148858724:		$B4q1		3.87		3.86		3.86		3.84		3.84		3.85		3.86		3.83

		S1148858754:		#B4q1		1148858754:		$B4q1		3.87		3.86		3.86		3.84		3.83		3.85		3.86		3.83

		S1148858784:		#B4q1		1148858784:		$B4q1		3.87		3.86		3.86		3.84		3.83		3.85		3.85		3.83

		S1148858814:		#B4q1		1148858814:		$B4q1		3.87		3.86		3.86		3.84		3.83		3.85		3.85		3.83

		S1148858844:		#B4q1		1148858844:		$B4q1		3.87		3.86		3.86		3.84		3.83		3.84		3.85		3.83

		S1148858874:		#B4q1		1148858874:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148858904:		#B4q1		1148858904:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148858934:		#B4q1		1148858934:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148858964:		#B4q1		1148858964:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148858994:		#B4q1		1148858994:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859024:		#B4q1		1148859024:		$B4q1		3.87		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859054:		#B4q1		1148859054:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859084:		#B4q1		1148859084:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859114:		#B4q1		1148859114:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859144:		#B4q1		1148859144:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859174:		#B4q1		1148859174:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859204:		#B4q1		1148859204:		$B4q1		3.86		3.86		3.86		3.83		3.83		3.84		3.85		3.83

		S1148859234:		#B4q1		1148859234:		$B4q1		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859264:		#B4q1		1148859264:		$B4q1		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859294:		#B4q1		1148859294:		$B4q1		3.86		3.86		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859324:		#B4q1		1148859324:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859354:		#B4q1		1148859354:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859384:		#B4q1		1148859384:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859414:		#B4q1		1148859414:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859444:		#B4q1		1148859444:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859474:		#B4q1		1148859474:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859504:		#B4q1		1148859504:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859534:		#B4q1		1148859534:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859564:		#B4q1		1148859564:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859594:		#B4q1		1148859594:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859624:		#B4q1		1148859624:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.84		3.85		3.83

		S1148859654:		#B4q1		1148859654:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83

		S1148859684:		#B4q1		1148859684:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83

		S1148859714:		#B4q1		1148859714:		$B4q1		3.86		3.85		3.85		3.83		3.83		3.83		3.85		3.83

		S1148859744:		#B4q1		1148859744:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.83

		S1148859774:		#B4q1		1148859774:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82

		S1148859804:		#B4q1		1148859804:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82

		S1148859834:		#B4q1		1148859834:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82

		S1148859864:		#B4q1		1148859864:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.85		3.82

		S1148859894:		#B4q1		1148859894:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82

		S1148859924:		#B4q1		1148859924:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82

		S1148859954:		#B4q1		1148859954:		$B4q1		3.85		3.85		3.85		3.83		3.83		3.83		3.84		3.82

		S1148859984:		#B4q1		1148859984:		$B4q1		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82

		S1148860014:		#B4q1		1148860014:		$B4q1		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82

		S1148860044:		#B4q1		1148860044:		$B4q1		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82

		S1148860074:		#B4q1		1148860074:		$B4q1		3.85		3.85		3.85		3.83		3.82		3.83		3.84		3.82

		S1148860104:		#B4q1		1148860104:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860134:		#B4q1		1148860134:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860164:		#B4q1		1148860164:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860194:		#B4q1		1148860194:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860224:		#B4q1		1148860224:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860254:		#B4q1		1148860254:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860284:		#B4q1		1148860284:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860314:		#B4q1		1148860314:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860344:		#B4q1		1148860344:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860374:		#B4q1		1148860374:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860404:		#B4q1		1148860404:		$B4q1		3.85		3.85		3.85		3.82		3.82		3.83		3.84		3.82

		S1148860434:		#B4q1		1148860434:		$B4q1		3.85		3.85		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860464:		#B4q1		1148860464:		$B4q1		3.85		3.85		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860494:		#B4q1		1148860494:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860524:		#B4q1		1148860524:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860554:		#B4q1		1148860554:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860584:		#B4q1		1148860584:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860614:		#B4q1		1148860614:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860644:		#B4q1		1148860644:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860674:		#B4q1		1148860674:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860704:		#B4q1		1148860704:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.84		3.82

		S1148860734:		#B4q1		1148860734:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860764:		#B4q1		1148860764:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860794:		#B4q1		1148860794:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860824:		#B4q1		1148860824:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860854:		#B4q1		1148860854:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860884:		#B4q1		1148860884:		$B4q1		3.85		3.84		3.84		3.82		3.82		3.83		3.83		3.82

		S1148860914:		#B4q1		1148860914:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148860944:		#B4q1		1148860944:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148860974:		#B4q1		1148860974:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861004:		#B4q1		1148861004:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861034:		#B4q1		1148861034:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861064:		#B4q1		1148861064:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861094:		#B4q1		1148861094:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861124:		#B4q1		1148861124:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861154:		#B4q1		1148861154:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.82

		S1148861184:		#B4q1		1148861184:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.81

		S1148861214:		#B4q1		1148861214:		$B4q1		3.84		3.84		3.84		3.82		3.82		3.82		3.83		3.81

		S1148861244:		#B4q1		1148861244:		$B4q1		3.84		3.84		3.83		3.82		3.82		3.82		3.83		3.81

		S1148861274:		#B4q1		1148861274:		$B4q1		3.84		3.84		3.83		3.82		3.82		3.82		3.83		3.81

		S1148861304:		#B4q1		1148861304:		$B4q1		3.84		3.83		3.83		3.82		3.82		3.82		3.83		3.81

		S1148861334:		#B4q1		1148861334:		$B4q1		3.84		3.83		3.83		3.82		3.81		3.82		3.83		3.81

		S1148861364:		#B4q1		1148861364:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861394:		#B4q1		1148861394:		$B4q1		3.84		3.83		3.83		3.82		3.81		3.82		3.83		3.81

		S1148861424:		#B4q1		1148861424:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861454:		#B4q1		1148861454:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861484:		#B4q1		1148861484:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861514:		#B4q1		1148861514:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861544:		#B4q1		1148861544:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861574:		#B4q1		1148861574:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861604:		#B4q1		1148861604:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861634:		#B4q1		1148861634:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861664:		#B4q1		1148861664:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861694:		#B4q1		1148861694:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861724:		#B4q1		1148861724:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861754:		#B4q1		1148861754:		$B4q1		3.84		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861784:		#B4q1		1148861784:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861814:		#B4q1		1148861814:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861844:		#B4q1		1148861844:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861874:		#B4q1		1148861874:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861904:		#B4q1		1148861904:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861934:		#B4q1		1148861934:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861964:		#B4q1		1148861964:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.83		3.81

		S1148861994:		#B4q1		1148861994:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81

		S1148862024:		#B4q1		1148862024:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81

		S1148862054:		#B4q1		1148862054:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81

		S1148862084:		#B4q1		1148862084:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81

		S1148862114:		#B4q1		1148862114:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.81

		S1148862144:		#B4q1		1148862144:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.8

		S1148862174:		#B4q1		1148862174:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.8

		S1148862204:		#B4q1		1148862204:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.8

		S1148862234:		#B4q1		1148862234:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.8

		S1148862264:		#B4q1		1148862264:		$B4q1		3.83		3.83		3.83		3.81		3.81		3.82		3.82		3.8

		S1148862294:		#B4q1		1148862294:		$B4q1		3.83		3.83		3.83		3.81		3.8		3.82		3.82		3.8

		S1148862324:		#B4q1		1148862324:		$B4q1		3.83		3.83		3.83		3.81		3.8		3.82		3.82		3.8

		S1148862354:		#B4q1		1148862354:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862384:		#B4q1		1148862384:		$B4q1		3.83		3.83		3.83		3.81		3.8		3.81		3.82		3.8

		S1148862414:		#B4q1		1148862414:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862444:		#B4q1		1148862444:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862474:		#B4q1		1148862474:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862504:		#B4q1		1148862504:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862534:		#B4q1		1148862534:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862564:		#B4q1		1148862564:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862594:		#B4q1		1148862594:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862624:		#B4q1		1148862624:		$B4q1		3.83		3.83		3.83		3.8		3.8		3.81		3.82		3.8

		S1148862654:		#B4q1		1148862654:		$B4q1		3.83		3.83		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862684:		#B4q1		1148862684:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862714:		#B4q1		1148862714:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862744:		#B4q1		1148862744:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862774:		#B4q1		1148862774:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862804:		#B4q1		1148862804:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862834:		#B4q1		1148862834:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862864:		#B4q1		1148862864:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862894:		#B4q1		1148862894:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862924:		#B4q1		1148862924:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862954:		#B4q1		1148862954:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148862984:		#B4q1		1148862984:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863014:		#B4q1		1148863014:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863044:		#B4q1		1148863044:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863074:		#B4q1		1148863074:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863104:		#B4q1		1148863104:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863134:		#B4q1		1148863134:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863164:		#B4q1		1148863164:		$B4q1		3.83		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863194:		#B4q1		1148863194:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863224:		#B4q1		1148863224:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863254:		#B4q1		1148863254:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863284:		#B4q1		1148863284:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863314:		#B4q1		1148863314:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863344:		#B4q1		1148863344:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.81		3.82		3.8

		S1148863374:		#B4q1		1148863374:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.82		3.8

		S1148863404:		#B4q1		1148863404:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863434:		#B4q1		1148863434:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863464:		#B4q1		1148863464:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863494:		#B4q1		1148863494:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863524:		#B4q1		1148863524:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863554:		#B4q1		1148863554:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863584:		#B4q1		1148863584:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863614:		#B4q1		1148863614:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863644:		#B4q1		1148863644:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863674:		#B4q1		1148863674:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863704:		#B4q1		1148863704:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863734:		#B4q1		1148863734:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.8

		S1148863764:		#B4q1		1148863764:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.79

		S1148863794:		#B4q1		1148863794:		$B4q1		3.82		3.82		3.82		3.8		3.8		3.8		3.81		3.79

		S1148863824:		#B4q1		1148863824:		$B4q1		3.82		3.82		3.82		3.8		3.79		3.8		3.81		3.79

		S1148863854:		#B4q1		1148863854:		$B4q1		3.82		3.82		3.82		3.79		3.8		3.8		3.81		3.79

		S1148863884:		#B4q1		1148863884:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148863914:		#B4q1		1148863914:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148863944:		#B4q1		1148863944:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148863974:		#B4q1		1148863974:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864004:		#B4q1		1148864004:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864034:		#B4q1		1148864034:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864064:		#B4q1		1148864064:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864094:		#B4q1		1148864094:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864124:		#B4q1		1148864124:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864154:		#B4q1		1148864154:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864184:		#B4q1		1148864184:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864214:		#B4q1		1148864214:		$B4q1		3.82		3.82		3.82		3.79		3.79		3.8		3.81		3.79

		S1148864244:		#B4q1		1148864244:		$B4q1		3.82		3.82		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864274:		#B4q1		1148864274:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864304:		#B4q1		1148864304:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864334:		#B4q1		1148864334:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864364:		#B4q1		1148864364:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864394:		#B4q1		1148864394:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864424:		#B4q1		1148864424:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864454:		#B4q1		1148864454:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864484:		#B4q1		1148864484:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864514:		#B4q1		1148864514:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.81		3.79

		S1148864544:		#B4q1		1148864544:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864574:		#B4q1		1148864574:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864604:		#B4q1		1148864604:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864634:		#B4q1		1148864634:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864664:		#B4q1		1148864664:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864694:		#B4q1		1148864694:		$B4q1		3.82		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864724:		#B4q1		1148864724:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864754:		#B4q1		1148864754:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864784:		#B4q1		1148864784:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864814:		#B4q1		1148864814:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864844:		#B4q1		1148864844:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.79

		S1148864874:		#B4q1		1148864874:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.78

		S1148864904:		#B4q1		1148864904:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.78

		S1148864934:		#B4q1		1148864934:		$B4q1		3.81		3.81		3.81		3.79		3.79		3.8		3.8		3.78

		S1148864964:		#B4q1		1148864964:		$B4q1		3.81		3.81		3.81		3.78		3.79		3.8		3.8		3.78

		S1148864994:		#B4q1		1148864994:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.8		3.8		3.78

		S1148865024:		#B4q1		1148865024:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865054:		#B4q1		1148865054:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865084:		#B4q1		1148865084:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865114:		#B4q1		1148865114:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865144:		#B4q1		1148865144:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865174:		#B4q1		1148865174:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865204:		#B4q1		1148865204:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865234:		#B4q1		1148865234:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865264:		#B4q1		1148865264:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865294:		#B4q1		1148865294:		$B4q1		3.81		3.81		3.81		3.78		3.78		3.79		3.8		3.78

		S1148865324:		#B4q1		1148865324:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865354:		#B4q1		1148865354:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865384:		#B4q1		1148865384:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865414:		#B4q1		1148865414:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865444:		#B4q1		1148865444:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865474:		#B4q1		1148865474:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865504:		#B4q1		1148865504:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865534:		#B4q1		1148865534:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865564:		#B4q1		1148865564:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865594:		#B4q1		1148865594:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865624:		#B4q1		1148865624:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865654:		#B4q1		1148865654:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865684:		#B4q1		1148865684:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865714:		#B4q1		1148865714:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865744:		#B4q1		1148865744:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865774:		#B4q1		1148865774:		$B4q1		3.81		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865804:		#B4q1		1148865804:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865834:		#B4q1		1148865834:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865864:		#B4q1		1148865864:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865894:		#B4q1		1148865894:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865924:		#B4q1		1148865924:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865954:		#B4q1		1148865954:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148865984:		#B4q1		1148865984:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866014:		#B4q1		1148866014:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866044:		#B4q1		1148866044:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866074:		#B4q1		1148866074:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866104:		#B4q1		1148866104:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866134:		#B4q1		1148866134:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.8		3.78

		S1148866164:		#B4q1		1148866164:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.79		3.79		3.78

		S1148866194:		#B4q1		1148866194:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.8		3.78

		S1148866224:		#B4q1		1148866224:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866254:		#B4q1		1148866254:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866284:		#B4q1		1148866284:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866314:		#B4q1		1148866314:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866344:		#B4q1		1148866344:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866374:		#B4q1		1148866374:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866404:		#B4q1		1148866404:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866434:		#B4q1		1148866434:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866464:		#B4q1		1148866464:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866494:		#B4q1		1148866494:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866524:		#B4q1		1148866524:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866554:		#B4q1		1148866554:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866584:		#B4q1		1148866584:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866614:		#B4q1		1148866614:		$B4q1		3.8		3.8		3.8		3.77		3.78		3.78		3.79		3.78

		S1148866644:		#B4q1		1148866644:		$B4q1		3.8		3.8		3.8		3.78		3.78		3.78		3.79		3.78

		S1148866674:		#B4q1		1148866674:		$B4q1		3.8		3.8		3.8		3.77		3.78		3.78		3.79		3.77

		S1148866704:		#B4q1		1148866704:		$B4q1		3.8		3.8		3.8		3.77		3.78		3.78		3.79		3.77

		S1148866734:		#B4q1		1148866734:		$B4q1		3.8		3.8		3.8		3.77		3.78		3.78		3.79		3.77

		S1148866764:		#B4q1		1148866764:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866794:		#B4q1		1148866794:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866824:		#B4q1		1148866824:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866854:		#B4q1		1148866854:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866884:		#B4q1		1148866884:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866914:		#B4q1		1148866914:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866944:		#B4q1		1148866944:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148866974:		#B4q1		1148866974:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867004:		#B4q1		1148867004:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867034:		#B4q1		1148867034:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867064:		#B4q1		1148867064:		$B4q1		3.8		3.8		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867094:		#B4q1		1148867094:		$B4q1		3.8		3.79		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867124:		#B4q1		1148867124:		$B4q1		3.8		3.79		3.8		3.77		3.77		3.78		3.79		3.77

		S1148867154:		#B4q1		1148867154:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867184:		#B4q1		1148867184:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867214:		#B4q1		1148867214:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867244:		#B4q1		1148867244:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867274:		#B4q1		1148867274:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867304:		#B4q1		1148867304:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867334:		#B4q1		1148867334:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867364:		#B4q1		1148867364:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.79		3.77

		S1148867394:		#B4q1		1148867394:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867424:		#B4q1		1148867424:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867454:		#B4q1		1148867454:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867484:		#B4q1		1148867484:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867514:		#B4q1		1148867514:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867544:		#B4q1		1148867544:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867574:		#B4q1		1148867574:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867604:		#B4q1		1148867604:		$B4q1		3.8		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867634:		#B4q1		1148867634:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867664:		#B4q1		1148867664:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867694:		#B4q1		1148867694:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867724:		#B4q1		1148867724:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867754:		#B4q1		1148867754:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867784:		#B4q1		1148867784:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867814:		#B4q1		1148867814:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867844:		#B4q1		1148867844:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867874:		#B4q1		1148867874:		$B4q1		3.79		3.79		3.79		3.76		3.77		3.78		3.78		3.77

		S1148867904:		#B4q1		1148867904:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.77

		S1148867934:		#B4q1		1148867934:		$B4q1		3.79		3.79		3.79		3.76		3.77		3.78		3.78		3.77

		S1148867964:		#B4q1		1148867964:		$B4q1		3.79		3.79		3.79		3.77		3.77		3.78		3.78		3.76

		S1148867994:		#B4q1		1148867994:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.78		3.78		3.76

		S1148868024:		#B4q1		1148868024:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.78		3.78		3.76

		S1148868054:		#B4q1		1148868054:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868084:		#B4q1		1148868084:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868114:		#B4q1		1148868114:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868144:		#B4q1		1148868144:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868174:		#B4q1		1148868174:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868204:		#B4q1		1148868204:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868234:		#B4q1		1148868234:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868264:		#B4q1		1148868264:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868294:		#B4q1		1148868294:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868324:		#B4q1		1148868324:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868354:		#B4q1		1148868354:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868384:		#B4q1		1148868384:		$B4q1		3.79		3.78		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868414:		#B4q1		1148868414:		$B4q1		3.79		3.79		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868444:		#B4q1		1148868444:		$B4q1		3.79		3.78		3.79		3.76		3.76		3.77		3.78		3.76

		S1148868474:		#B4q1		1148868474:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868504:		#B4q1		1148868504:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868534:		#B4q1		1148868534:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868564:		#B4q1		1148868564:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868594:		#B4q1		1148868594:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868624:		#B4q1		1148868624:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868654:		#B4q1		1148868654:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868684:		#B4q1		1148868684:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868714:		#B4q1		1148868714:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868744:		#B4q1		1148868744:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868774:		#B4q1		1148868774:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868804:		#B4q1		1148868804:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868834:		#B4q1		1148868834:		$B4q1		3.79		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868864:		#B4q1		1148868864:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868894:		#B4q1		1148868894:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868924:		#B4q1		1148868924:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868954:		#B4q1		1148868954:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148868984:		#B4q1		1148868984:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869014:		#B4q1		1148869014:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869044:		#B4q1		1148869044:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869074:		#B4q1		1148869074:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869104:		#B4q1		1148869104:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869134:		#B4q1		1148869134:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869164:		#B4q1		1148869164:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869194:		#B4q1		1148869194:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869224:		#B4q1		1148869224:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869254:		#B4q1		1148869254:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869284:		#B4q1		1148869284:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869314:		#B4q1		1148869314:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.77		3.78		3.76

		S1148869344:		#B4q1		1148869344:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869374:		#B4q1		1148869374:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.78		3.76

		S1148869404:		#B4q1		1148869404:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869434:		#B4q1		1148869434:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869464:		#B4q1		1148869464:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869494:		#B4q1		1148869494:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869524:		#B4q1		1148869524:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869554:		#B4q1		1148869554:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869584:		#B4q1		1148869584:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869614:		#B4q1		1148869614:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869644:		#B4q1		1148869644:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869674:		#B4q1		1148869674:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869704:		#B4q1		1148869704:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869734:		#B4q1		1148869734:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869764:		#B4q1		1148869764:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869794:		#B4q1		1148869794:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869824:		#B4q1		1148869824:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869854:		#B4q1		1148869854:		$B4q1		3.78		3.78		3.78		3.76		3.76		3.76		3.77		3.76

		S1148869884:		#B4q1		1148869884:		$B4q1		3.78		3.78		3.78		3.75		3.76		3.76		3.77		3.76

		S1148869914:		#B4q1		1148869914:		$B4q1		3.78		3.78		3.78		3.75		3.76		3.76		3.77		3.76

		S1148869944:		#B4q1		1148869944:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.76

		S1148869974:		#B4q1		1148869974:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.76

		S1148870004:		#B4q1		1148870004:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870034:		#B4q1		1148870034:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870064:		#B4q1		1148870064:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870094:		#B4q1		1148870094:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870124:		#B4q1		1148870124:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870154:		#B4q1		1148870154:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870184:		#B4q1		1148870184:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870214:		#B4q1		1148870214:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870244:		#B4q1		1148870244:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870274:		#B4q1		1148870274:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870304:		#B4q1		1148870304:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870334:		#B4q1		1148870334:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870364:		#B4q1		1148870364:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870394:		#B4q1		1148870394:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870424:		#B4q1		1148870424:		$B4q1		3.78		3.78		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870454:		#B4q1		1148870454:		$B4q1		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870484:		#B4q1		1148870484:		$B4q1		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870514:		#B4q1		1148870514:		$B4q1		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870544:		#B4q1		1148870544:		$B4q1		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870574:		#B4q1		1148870574:		$B4q1		3.78		3.77		3.78		3.75		3.75		3.76		3.77		3.75

		S1148870604:		#B4q1		1148870604:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75

		S1148870634:		#B4q1		1148870634:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75

		S1148870664:		#B4q1		1148870664:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75

		S1148870694:		#B4q1		1148870694:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870724:		#B4q1		1148870724:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75

		S1148870754:		#B4q1		1148870754:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870784:		#B4q1		1148870784:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.77		3.75

		S1148870814:		#B4q1		1148870814:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870844:		#B4q1		1148870844:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870874:		#B4q1		1148870874:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870904:		#B4q1		1148870904:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870934:		#B4q1		1148870934:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870964:		#B4q1		1148870964:		$B4q1		3.78		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148870994:		#B4q1		1148870994:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871024:		#B4q1		1148871024:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871054:		#B4q1		1148871054:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871084:		#B4q1		1148871084:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871114:		#B4q1		1148871114:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871144:		#B4q1		1148871144:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871174:		#B4q1		1148871174:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871204:		#B4q1		1148871204:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871234:		#B4q1		1148871234:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871264:		#B4q1		1148871264:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871294:		#B4q1		1148871294:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871324:		#B4q1		1148871324:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871354:		#B4q1		1148871354:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871384:		#B4q1		1148871384:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871414:		#B4q1		1148871414:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871444:		#B4q1		1148871444:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.76		3.76		3.75

		S1148871474:		#B4q1		1148871474:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871504:		#B4q1		1148871504:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871534:		#B4q1		1148871534:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871564:		#B4q1		1148871564:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871594:		#B4q1		1148871594:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871624:		#B4q1		1148871624:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871654:		#B4q1		1148871654:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871684:		#B4q1		1148871684:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871714:		#B4q1		1148871714:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871744:		#B4q1		1148871744:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871774:		#B4q1		1148871774:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871804:		#B4q1		1148871804:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871834:		#B4q1		1148871834:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871864:		#B4q1		1148871864:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871894:		#B4q1		1148871894:		$B4q1		3.77		3.77		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871924:		#B4q1		1148871924:		$B4q1		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871954:		#B4q1		1148871954:		$B4q1		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75

		S1148871984:		#B4q1		1148871984:		$B4q1		3.77		3.76		3.77		3.75		3.75		3.75		3.76		3.75

		S1148872014:		#B4q1		1148872014:		$B4q1		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75

		S1148872044:		#B4q1		1148872044:		$B4q1		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75

		S1148872074:		#B4q1		1148872074:		$B4q1		3.77		3.76		3.77		3.74		3.74		3.75		3.76		3.75

		S1148872104:		#B4q1		1148872104:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.75

		S1148872134:		#B4q1		1148872134:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872164:		#B4q1		1148872164:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872194:		#B4q1		1148872194:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872224:		#B4q1		1148872224:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872254:		#B4q1		1148872254:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872284:		#B4q1		1148872284:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872314:		#B4q1		1148872314:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872344:		#B4q1		1148872344:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872374:		#B4q1		1148872374:		$B4q1		3.77		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872404:		#B4q1		1148872404:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872434:		#B4q1		1148872434:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872464:		#B4q1		1148872464:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872494:		#B4q1		1148872494:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872524:		#B4q1		1148872524:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872554:		#B4q1		1148872554:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872584:		#B4q1		1148872584:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872614:		#B4q1		1148872614:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872644:		#B4q1		1148872644:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872674:		#B4q1		1148872674:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872704:		#B4q1		1148872704:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872734:		#B4q1		1148872734:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872764:		#B4q1		1148872764:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872794:		#B4q1		1148872794:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872824:		#B4q1		1148872824:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872854:		#B4q1		1148872854:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872884:		#B4q1		1148872884:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872914:		#B4q1		1148872914:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148872944:		#B4q1		1148872944:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148872974:		#B4q1		1148872974:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.76		3.74

		S1148873004:		#B4q1		1148873004:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873034:		#B4q1		1148873034:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873064:		#B4q1		1148873064:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873094:		#B4q1		1148873094:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873124:		#B4q1		1148873124:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873154:		#B4q1		1148873154:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873184:		#B4q1		1148873184:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873214:		#B4q1		1148873214:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873244:		#B4q1		1148873244:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873274:		#B4q1		1148873274:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873304:		#B4q1		1148873304:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873334:		#B4q1		1148873334:		$B4q1		3.76		3.76		3.76		3.74		3.74		3.75		3.75		3.74

		S1148873364:		#B4q1		1148873364:		$B4q1		3.76		3.76		3.76		3.74		3.73		3.75		3.75		3.74

		S1148873394:		#B4q1		1148873394:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74

		S1148873424:		#B4q1		1148873424:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74

		S1148873454:		#B4q1		1148873454:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74

		S1148873484:		#B4q1		1148873484:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.74

		S1148873514:		#B4q1		1148873514:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873544:		#B4q1		1148873544:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873574:		#B4q1		1148873574:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873604:		#B4q1		1148873604:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873634:		#B4q1		1148873634:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873664:		#B4q1		1148873664:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873694:		#B4q1		1148873694:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.75		3.75		3.73

		S1148873724:		#B4q1		1148873724:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873754:		#B4q1		1148873754:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873784:		#B4q1		1148873784:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873814:		#B4q1		1148873814:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873844:		#B4q1		1148873844:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873874:		#B4q1		1148873874:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873904:		#B4q1		1148873904:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873934:		#B4q1		1148873934:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873964:		#B4q1		1148873964:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148873994:		#B4q1		1148873994:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874024:		#B4q1		1148874024:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874054:		#B4q1		1148874054:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874084:		#B4q1		1148874084:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874114:		#B4q1		1148874114:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874144:		#B4q1		1148874144:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874174:		#B4q1		1148874174:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874204:		#B4q1		1148874204:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874234:		#B4q1		1148874234:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874264:		#B4q1		1148874264:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874294:		#B4q1		1148874294:		$B4q1		3.76		3.76		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874324:		#B4q1		1148874324:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874354:		#B4q1		1148874354:		$B4q1		3.76		3.75		3.76		3.73		3.73		3.74		3.75		3.73

		S1148874384:		#B4q1		1148874384:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874414:		#B4q1		1148874414:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874444:		#B4q1		1148874444:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874474:		#B4q1		1148874474:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874504:		#B4q1		1148874504:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874534:		#B4q1		1148874534:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874564:		#B4q1		1148874564:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874594:		#B4q1		1148874594:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874624:		#B4q1		1148874624:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874654:		#B4q1		1148874654:		$B4q1		3.76		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874684:		#B4q1		1148874684:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874714:		#B4q1		1148874714:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874744:		#B4q1		1148874744:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874774:		#B4q1		1148874774:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874804:		#B4q1		1148874804:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874834:		#B4q1		1148874834:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874864:		#B4q1		1148874864:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874894:		#B4q1		1148874894:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874924:		#B4q1		1148874924:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874954:		#B4q1		1148874954:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148874984:		#B4q1		1148874984:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148875014:		#B4q1		1148875014:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148875044:		#B4q1		1148875044:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148875074:		#B4q1		1148875074:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148875104:		#B4q1		1148875104:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73

		S1148875134:		#B4q1		1148875134:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.74		3.75		3.73

		S1148875164:		#B4q1		1148875164:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73

		S1148875194:		#B4q1		1148875194:		$B4q1		3.75		3.75		3.75		3.73		3.73		3.73		3.75		3.73

		S1148875224:		#B4q1		1148875224:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.73

		S1148875254:		#B4q1		1148875254:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.73

		S1148875284:		#B4q1		1148875284:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.72

		S1148875314:		#B4q1		1148875314:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875344:		#B4q1		1148875344:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.75		3.72

		S1148875374:		#B4q1		1148875374:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875404:		#B4q1		1148875404:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875434:		#B4q1		1148875434:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875464:		#B4q1		1148875464:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875494:		#B4q1		1148875494:		$B4q1		3.75		3.75		3.75		3.73		3.72		3.73		3.74		3.72

		S1148875524:		#B4q1		1148875524:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875554:		#B4q1		1148875554:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875584:		#B4q1		1148875584:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875614:		#B4q1		1148875614:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875644:		#B4q1		1148875644:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875674:		#B4q1		1148875674:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875704:		#B4q1		1148875704:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875734:		#B4q1		1148875734:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875764:		#B4q1		1148875764:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875794:		#B4q1		1148875794:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875824:		#B4q1		1148875824:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875854:		#B4q1		1148875854:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875884:		#B4q1		1148875884:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875914:		#B4q1		1148875914:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875944:		#B4q1		1148875944:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148875974:		#B4q1		1148875974:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876004:		#B4q1		1148876004:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876034:		#B4q1		1148876034:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876064:		#B4q1		1148876064:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876094:		#B4q1		1148876094:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876124:		#B4q1		1148876124:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876154:		#B4q1		1148876154:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876184:		#B4q1		1148876184:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876214:		#B4q1		1148876214:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876244:		#B4q1		1148876244:		$B4q1		3.75		3.75		3.75		3.72		3.72		3.73		3.74		3.72

		S1148876274:		#B4q1		1148876274:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.72

		S1148876304:		#B4q1		1148876304:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.72

		S1148876334:		#B4q1		1148876334:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876364:		#B4q1		1148876364:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876394:		#B4q1		1148876394:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876424:		#B4q1		1148876424:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876454:		#B4q1		1148876454:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876484:		#B4q1		1148876484:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876514:		#B4q1		1148876514:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876544:		#B4q1		1148876544:		$B4q1		3.75		3.75		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876574:		#B4q1		1148876574:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876604:		#B4q1		1148876604:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876634:		#B4q1		1148876634:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876664:		#B4q1		1148876664:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876694:		#B4q1		1148876694:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876724:		#B4q1		1148876724:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876754:		#B4q1		1148876754:		$B4q1		3.75		3.74		3.75		3.72		3.71		3.73		3.74		3.71

		S1148876784:		#B4q1		1148876784:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876814:		#B4q1		1148876814:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876844:		#B4q1		1148876844:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876874:		#B4q1		1148876874:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876904:		#B4q1		1148876904:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876934:		#B4q1		1148876934:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876964:		#B4q1		1148876964:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148876994:		#B4q1		1148876994:		$B4q1		3.75		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148877024:		#B4q1		1148877024:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148877054:		#B4q1		1148877054:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.73		3.73		3.71

		S1148877084:		#B4q1		1148877084:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877114:		#B4q1		1148877114:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877144:		#B4q1		1148877144:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877174:		#B4q1		1148877174:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877204:		#B4q1		1148877204:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877234:		#B4q1		1148877234:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877264:		#B4q1		1148877264:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877294:		#B4q1		1148877294:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877324:		#B4q1		1148877324:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877354:		#B4q1		1148877354:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877384:		#B4q1		1148877384:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877414:		#B4q1		1148877414:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877444:		#B4q1		1148877444:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877474:		#B4q1		1148877474:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877504:		#B4q1		1148877504:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877534:		#B4q1		1148877534:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877564:		#B4q1		1148877564:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877594:		#B4q1		1148877594:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877624:		#B4q1		1148877624:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877654:		#B4q1		1148877654:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877684:		#B4q1		1148877684:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877714:		#B4q1		1148877714:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877744:		#B4q1		1148877744:		$B4q1		3.74		3.74		3.74		3.71		3.71		3.72		3.73		3.71

		S1148877774:		#B4q1		1148877774:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.71

		S1148877804:		#B4q1		1148877804:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.71

		S1148877834:		#B4q1		1148877834:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.71

		S1148877864:		#B4q1		1148877864:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148877894:		#B4q1		1148877894:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148877924:		#B4q1		1148877924:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148877954:		#B4q1		1148877954:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148877984:		#B4q1		1148877984:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878014:		#B4q1		1148878014:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878044:		#B4q1		1148878044:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878074:		#B4q1		1148878074:		$B4q1		3.74		3.74		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878104:		#B4q1		1148878104:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878134:		#B4q1		1148878134:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878164:		#B4q1		1148878164:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878194:		#B4q1		1148878194:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878224:		#B4q1		1148878224:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.72		3.73		3.7

		S1148878254:		#B4q1		1148878254:		$B4q1		3.74		3.73		3.74		3.71		3.7		3.71		3.73		3.7

		S1148878284:		#B4q1		1148878284:		$B4q1		3.74		3.73		3.73		3.71		3.7		3.71		3.73		3.7

		S1148878314:		#B4q1		1148878314:		$B4q1		3.74		3.73		3.73		3.71		3.7		3.71		3.73		3.7

		S1148878344:		#B4q1		1148878344:		$B4q1		3.74		3.73		3.73		3.71		3.7		3.71		3.73		3.7

		S1148878374:		#B4q1		1148878374:		$B4q1		3.74		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878404:		#B4q1		1148878404:		$B4q1		3.74		3.73		3.73		3.71		3.7		3.71		3.73		3.7

		S1148878434:		#B4q1		1148878434:		$B4q1		3.74		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878464:		#B4q1		1148878464:		$B4q1		3.74		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878494:		#B4q1		1148878494:		$B4q1		3.74		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878524:		#B4q1		1148878524:		$B4q1		3.74		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878554:		#B4q1		1148878554:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878584:		#B4q1		1148878584:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878614:		#B4q1		1148878614:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878644:		#B4q1		1148878644:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878674:		#B4q1		1148878674:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878704:		#B4q1		1148878704:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878734:		#B4q1		1148878734:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878764:		#B4q1		1148878764:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878794:		#B4q1		1148878794:		$B4q1		3.73		3.73		3.73		3.7		3.7		3.71		3.73		3.7

		S1148878824:		#B4q1		1148878824:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.73		3.7

		S1148878854:		#B4q1		1148878854:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.73		3.7

		S1148878884:		#B4q1		1148878884:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.73		3.7

		S1148878914:		#B4q1		1148878914:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.73		3.7

		S1148878944:		#B4q1		1148878944:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.7

		S1148878974:		#B4q1		1148878974:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.7

		S1148879004:		#B4q1		1148879004:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.7

		S1148879034:		#B4q1		1148879034:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.7

		S1148879064:		#B4q1		1148879064:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.7

		S1148879094:		#B4q1		1148879094:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879124:		#B4q1		1148879124:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879154:		#B4q1		1148879154:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879184:		#B4q1		1148879184:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879214:		#B4q1		1148879214:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879244:		#B4q1		1148879244:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879274:		#B4q1		1148879274:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879304:		#B4q1		1148879304:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879334:		#B4q1		1148879334:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879364:		#B4q1		1148879364:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879394:		#B4q1		1148879394:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879424:		#B4q1		1148879424:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879454:		#B4q1		1148879454:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879484:		#B4q1		1148879484:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879514:		#B4q1		1148879514:		$B4q1		3.73		3.73		3.73		3.7		3.69		3.71		3.72		3.69

		S1148879544:		#B4q1		1148879544:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879574:		#B4q1		1148879574:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879604:		#B4q1		1148879604:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879634:		#B4q1		1148879634:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879664:		#B4q1		1148879664:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879694:		#B4q1		1148879694:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879724:		#B4q1		1148879724:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879754:		#B4q1		1148879754:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879784:		#B4q1		1148879784:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879814:		#B4q1		1148879814:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.71		3.72		3.69

		S1148879844:		#B4q1		1148879844:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148879874:		#B4q1		1148879874:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148879904:		#B4q1		1148879904:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148879934:		#B4q1		1148879934:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148879964:		#B4q1		1148879964:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148879994:		#B4q1		1148879994:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148880024:		#B4q1		1148880024:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.72		3.69

		S1148880054:		#B4q1		1148880054:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880084:		#B4q1		1148880084:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880114:		#B4q1		1148880114:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880144:		#B4q1		1148880144:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880174:		#B4q1		1148880174:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880204:		#B4q1		1148880204:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880234:		#B4q1		1148880234:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880264:		#B4q1		1148880264:		$B4q1		3.73		3.73		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880294:		#B4q1		1148880294:		$B4q1		3.73		3.72		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880324:		#B4q1		1148880324:		$B4q1		3.73		3.72		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880354:		#B4q1		1148880354:		$B4q1		3.73		3.72		3.73		3.69		3.69		3.7		3.71		3.69

		S1148880384:		#B4q1		1148880384:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880414:		#B4q1		1148880414:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880444:		#B4q1		1148880444:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880474:		#B4q1		1148880474:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880504:		#B4q1		1148880504:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880534:		#B4q1		1148880534:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880564:		#B4q1		1148880564:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880594:		#B4q1		1148880594:		$B4q1		3.73		3.72		3.72		3.69		3.69		3.7		3.71		3.69

		S1148880624:		#B4q1		1148880624:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880654:		#B4q1		1148880654:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880684:		#B4q1		1148880684:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880714:		#B4q1		1148880714:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880744:		#B4q1		1148880744:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880774:		#B4q1		1148880774:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880804:		#B4q1		1148880804:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880834:		#B4q1		1148880834:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880864:		#B4q1		1148880864:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880894:		#B4q1		1148880894:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880924:		#B4q1		1148880924:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148880954:		#B4q1		1148880954:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69

		S1148880984:		#B4q1		1148880984:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.7		3.71		3.69

		S1148881014:		#B4q1		1148881014:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69

		S1148881044:		#B4q1		1148881044:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.69

		S1148881074:		#B4q1		1148881074:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881104:		#B4q1		1148881104:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881134:		#B4q1		1148881134:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881164:		#B4q1		1148881164:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881194:		#B4q1		1148881194:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881224:		#B4q1		1148881224:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881254:		#B4q1		1148881254:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881284:		#B4q1		1148881284:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881314:		#B4q1		1148881314:		$B4q1		3.72		3.72		3.72		3.69		3.68		3.69		3.71		3.68

		S1148881344:		#B4q1		1148881344:		$B4q1		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881374:		#B4q1		1148881374:		$B4q1		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881404:		#B4q1		1148881404:		$B4q1		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881434:		#B4q1		1148881434:		$B4q1		3.72		3.72		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881464:		#B4q1		1148881464:		$B4q1		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881494:		#B4q1		1148881494:		$B4q1		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881524:		#B4q1		1148881524:		$B4q1		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881554:		#B4q1		1148881554:		$B4q1		3.72		3.71		3.72		3.68		3.68		3.69		3.71		3.68

		S1148881584:		#B4q1		1148881584:		$B4q1		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68

		S1148881614:		#B4q1		1148881614:		$B4q1		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68

		S1148881644:		#B4q1		1148881644:		$B4q1		3.72		3.71		3.71		3.68		3.68		3.69		3.71		3.68

		S1148881674:		#B4q1		1148881674:		$B4q1		3.72		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881704:		#B4q1		1148881704:		$B4q1		3.72		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881734:		#B4q1		1148881734:		$B4q1		3.72		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881764:		#B4q1		1148881764:		$B4q1		3.72		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881794:		#B4q1		1148881794:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881824:		#B4q1		1148881824:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881854:		#B4q1		1148881854:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881884:		#B4q1		1148881884:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881914:		#B4q1		1148881914:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881944:		#B4q1		1148881944:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148881974:		#B4q1		1148881974:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148882004:		#B4q1		1148882004:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148882034:		#B4q1		1148882034:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148882064:		#B4q1		1148882064:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148882094:		#B4q1		1148882094:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.68

		S1148882124:		#B4q1		1148882124:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882154:		#B4q1		1148882154:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882184:		#B4q1		1148882184:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882214:		#B4q1		1148882214:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882244:		#B4q1		1148882244:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882274:		#B4q1		1148882274:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882304:		#B4q1		1148882304:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882334:		#B4q1		1148882334:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882364:		#B4q1		1148882364:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882394:		#B4q1		1148882394:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882424:		#B4q1		1148882424:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882454:		#B4q1		1148882454:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882484:		#B4q1		1148882484:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882514:		#B4q1		1148882514:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882544:		#B4q1		1148882544:		$B4q1		3.71		3.71		3.71		3.68		3.67		3.69		3.7		3.67

		S1148882574:		#B4q1		1148882574:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882604:		#B4q1		1148882604:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882634:		#B4q1		1148882634:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882664:		#B4q1		1148882664:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882694:		#B4q1		1148882694:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882724:		#B4q1		1148882724:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882754:		#B4q1		1148882754:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882784:		#B4q1		1148882784:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882814:		#B4q1		1148882814:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882844:		#B4q1		1148882844:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882874:		#B4q1		1148882874:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.69		3.7		3.67

		S1148882904:		#B4q1		1148882904:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.68		3.7		3.67

		S1148882934:		#B4q1		1148882934:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.68		3.7		3.67

		S1148882964:		#B4q1		1148882964:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67

		S1148882994:		#B4q1		1148882994:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883024:		#B4q1		1148883024:		$B4q1		3.71		3.71		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883054:		#B4q1		1148883054:		$B4q1		3.71		3.7		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883084:		#B4q1		1148883084:		$B4q1		3.71		3.7		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883114:		#B4q1		1148883114:		$B4q1		3.71		3.7		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883144:		#B4q1		1148883144:		$B4q1		3.71		3.7		3.71		3.67		3.67		3.68		3.69		3.67

		S1148883174:		#B4q1		1148883174:		$B4q1		3.71		3.7		3.71		3.67		3.66		3.68		3.69		3.67

		S1148883204:		#B4q1		1148883204:		$B4q1		3.71		3.7		3.71		3.67		3.66		3.68		3.69		3.67

		S1148883234:		#B4q1		1148883234:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883264:		#B4q1		1148883264:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883294:		#B4q1		1148883294:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883324:		#B4q1		1148883324:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883354:		#B4q1		1148883354:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883384:		#B4q1		1148883384:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883414:		#B4q1		1148883414:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883444:		#B4q1		1148883444:		$B4q1		3.71		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883474:		#B4q1		1148883474:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883504:		#B4q1		1148883504:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883534:		#B4q1		1148883534:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883564:		#B4q1		1148883564:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883594:		#B4q1		1148883594:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883624:		#B4q1		1148883624:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883654:		#B4q1		1148883654:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883684:		#B4q1		1148883684:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.67

		S1148883714:		#B4q1		1148883714:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883744:		#B4q1		1148883744:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883774:		#B4q1		1148883774:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883804:		#B4q1		1148883804:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883834:		#B4q1		1148883834:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883864:		#B4q1		1148883864:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883894:		#B4q1		1148883894:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883924:		#B4q1		1148883924:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883954:		#B4q1		1148883954:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148883984:		#B4q1		1148883984:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148884014:		#B4q1		1148884014:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148884044:		#B4q1		1148884044:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148884074:		#B4q1		1148884074:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148884104:		#B4q1		1148884104:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.68		3.69		3.66

		S1148884134:		#B4q1		1148884134:		$B4q1		3.7		3.7		3.7		3.67		3.66		3.67		3.69		3.66

		S1148884164:		#B4q1		1148884164:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884194:		#B4q1		1148884194:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884224:		#B4q1		1148884224:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884254:		#B4q1		1148884254:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884284:		#B4q1		1148884284:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884314:		#B4q1		1148884314:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884344:		#B4q1		1148884344:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884374:		#B4q1		1148884374:		$B4q1		3.7		3.69		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884404:		#B4q1		1148884404:		$B4q1		3.7		3.7		3.7		3.66		3.66		3.67		3.69		3.66

		S1148884434:		#B4q1		1148884434:		$B4q1		3.7		3.69		3.7		3.66		3.65		3.67		3.69		3.66

		S1148884464:		#B4q1		1148884464:		$B4q1		3.7		3.69		3.7		3.66		3.65		3.67		3.69		3.66

		S1148884494:		#B4q1		1148884494:		$B4q1		3.7		3.69		3.7		3.66		3.65		3.67		3.69		3.66

		S1148884524:		#B4q1		1148884524:		$B4q1		3.7		3.69		3.7		3.66		3.65		3.67		3.69		3.66

		S1148884554:		#B4q1		1148884554:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884584:		#B4q1		1148884584:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884614:		#B4q1		1148884614:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884644:		#B4q1		1148884644:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884674:		#B4q1		1148884674:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884704:		#B4q1		1148884704:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884734:		#B4q1		1148884734:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884764:		#B4q1		1148884764:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884794:		#B4q1		1148884794:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884824:		#B4q1		1148884824:		$B4q1		3.7		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884854:		#B4q1		1148884854:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.66

		S1148884884:		#B4q1		1148884884:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65

		S1148884914:		#B4q1		1148884914:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65

		S1148884944:		#B4q1		1148884944:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.69		3.65

		S1148884974:		#B4q1		1148884974:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65

		S1148885004:		#B4q1		1148885004:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65

		S1148885034:		#B4q1		1148885034:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65

		S1148885064:		#B4q1		1148885064:		$B4q1		3.69		3.69		3.69		3.66		3.65		3.67		3.68		3.65

		S1148885094:		#B4q1		1148885094:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885124:		#B4q1		1148885124:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885154:		#B4q1		1148885154:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885184:		#B4q1		1148885184:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885214:		#B4q1		1148885214:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885244:		#B4q1		1148885244:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885274:		#B4q1		1148885274:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885304:		#B4q1		1148885304:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885334:		#B4q1		1148885334:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885364:		#B4q1		1148885364:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885394:		#B4q1		1148885394:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885424:		#B4q1		1148885424:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885454:		#B4q1		1148885454:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885484:		#B4q1		1148885484:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885514:		#B4q1		1148885514:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885544:		#B4q1		1148885544:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885574:		#B4q1		1148885574:		$B4q1		3.69		3.69		3.69		3.66		3.64		3.67		3.68		3.65

		S1148885604:		#B4q1		1148885604:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65

		S1148885634:		#B4q1		1148885634:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65

		S1148885664:		#B4q1		1148885664:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65

		S1148885694:		#B4q1		1148885694:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.67		3.68		3.65

		S1148885724:		#B4q1		1148885724:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.65

		S1148885754:		#B4q1		1148885754:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.65

		S1148885784:		#B4q1		1148885784:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885814:		#B4q1		1148885814:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885844:		#B4q1		1148885844:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885874:		#B4q1		1148885874:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885904:		#B4q1		1148885904:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885934:		#B4q1		1148885934:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885964:		#B4q1		1148885964:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148885994:		#B4q1		1148885994:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148886024:		#B4q1		1148886024:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148886054:		#B4q1		1148886054:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886084:		#B4q1		1148886084:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.68		3.64

		S1148886114:		#B4q1		1148886114:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886144:		#B4q1		1148886144:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886174:		#B4q1		1148886174:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886204:		#B4q1		1148886204:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886234:		#B4q1		1148886234:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886264:		#B4q1		1148886264:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886294:		#B4q1		1148886294:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886324:		#B4q1		1148886324:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886354:		#B4q1		1148886354:		$B4q1		3.69		3.69		3.69		3.65		3.64		3.66		3.67		3.64

		S1148886384:		#B4q1		1148886384:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886414:		#B4q1		1148886414:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886444:		#B4q1		1148886444:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886474:		#B4q1		1148886474:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886504:		#B4q1		1148886504:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886534:		#B4q1		1148886534:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886564:		#B4q1		1148886564:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886594:		#B4q1		1148886594:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886624:		#B4q1		1148886624:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886654:		#B4q1		1148886654:		$B4q1		3.69		3.68		3.69		3.64		3.64		3.66		3.67		3.64

		S1148886684:		#B4q1		1148886684:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886714:		#B4q1		1148886714:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886744:		#B4q1		1148886744:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886774:		#B4q1		1148886774:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886804:		#B4q1		1148886804:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886834:		#B4q1		1148886834:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886864:		#B4q1		1148886864:		$B4q1		3.69		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886894:		#B4q1		1148886894:		$B4q1		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886924:		#B4q1		1148886924:		$B4q1		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886954:		#B4q1		1148886954:		$B4q1		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148886984:		#B4q1		1148886984:		$B4q1		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148887014:		#B4q1		1148887014:		$B4q1		3.68		3.68		3.68		3.64		3.64		3.66		3.67		3.64

		S1148887044:		#B4q1		1148887044:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.66		3.67		3.64

		S1148887074:		#B4q1		1148887074:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887104:		#B4q1		1148887104:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887134:		#B4q1		1148887134:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887164:		#B4q1		1148887164:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887194:		#B4q1		1148887194:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887224:		#B4q1		1148887224:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887254:		#B4q1		1148887254:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887284:		#B4q1		1148887284:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887314:		#B4q1		1148887314:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887344:		#B4q1		1148887344:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887374:		#B4q1		1148887374:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887404:		#B4q1		1148887404:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887434:		#B4q1		1148887434:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887464:		#B4q1		1148887464:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887494:		#B4q1		1148887494:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887524:		#B4q1		1148887524:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887554:		#B4q1		1148887554:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887584:		#B4q1		1148887584:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887614:		#B4q1		1148887614:		$B4q1		3.68		3.68		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887644:		#B4q1		1148887644:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887674:		#B4q1		1148887674:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.67		3.64

		S1148887704:		#B4q1		1148887704:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64

		S1148887734:		#B4q1		1148887734:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64

		S1148887764:		#B4q1		1148887764:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64

		S1148887794:		#B4q1		1148887794:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.65		3.66		3.64

		S1148887824:		#B4q1		1148887824:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.64		3.66		3.64

		S1148887854:		#B4q1		1148887854:		$B4q1		3.68		3.67		3.68		3.64		3.63		3.64		3.66		3.64

		S1148887884:		#B4q1		1148887884:		$B4q1		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64

		S1148887914:		#B4q1		1148887914:		$B4q1		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64

		S1148887944:		#B4q1		1148887944:		$B4q1		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.64

		S1148887974:		#B4q1		1148887974:		$B4q1		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.63

		S1148888004:		#B4q1		1148888004:		$B4q1		3.68		3.67		3.67		3.64		3.63		3.64		3.66		3.63

		S1148888034:		#B4q1		1148888034:		$B4q1		3.68		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888064:		#B4q1		1148888064:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888094:		#B4q1		1148888094:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888124:		#B4q1		1148888124:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888154:		#B4q1		1148888154:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888184:		#B4q1		1148888184:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888214:		#B4q1		1148888214:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888244:		#B4q1		1148888244:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888274:		#B4q1		1148888274:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888304:		#B4q1		1148888304:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888334:		#B4q1		1148888334:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888364:		#B4q1		1148888364:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888394:		#B4q1		1148888394:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888424:		#B4q1		1148888424:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888454:		#B4q1		1148888454:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888484:		#B4q1		1148888484:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888514:		#B4q1		1148888514:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888544:		#B4q1		1148888544:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888574:		#B4q1		1148888574:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888604:		#B4q1		1148888604:		$B4q1		3.67		3.67		3.67		3.63		3.62		3.64		3.66		3.63

		S1148888634:		#B4q1		1148888634:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.63

		S1148888664:		#B4q1		1148888664:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.63

		S1148888694:		#B4q1		1148888694:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888724:		#B4q1		1148888724:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888754:		#B4q1		1148888754:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888784:		#B4q1		1148888784:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888814:		#B4q1		1148888814:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888844:		#B4q1		1148888844:		$B4q1		3.67		3.67		3.67		3.63		3.61		3.64		3.66		3.62

		S1148888874:		#B4q1		1148888874:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.66		3.62

		S1148888904:		#B4q1		1148888904:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.66		3.62

		S1148888934:		#B4q1		1148888934:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.66		3.62

		S1148888964:		#B4q1		1148888964:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.66		3.62

		S1148888994:		#B4q1		1148888994:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.66		3.62

		S1148889024:		#B4q1		1148889024:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.65		3.62

		S1148889054:		#B4q1		1148889054:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.65		3.62

		S1148889084:		#B4q1		1148889084:		$B4q1		3.67		3.67		3.67		3.63		3.6		3.64		3.65		3.62

		S1148889114:		#B4q1		1148889114:		$B4q1		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62

		S1148889144:		#B4q1		1148889144:		$B4q1		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62

		S1148889174:		#B4q1		1148889174:		$B4q1		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.62

		S1148889204:		#B4q1		1148889204:		$B4q1		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.61

		S1148889234:		#B4q1		1148889234:		$B4q1		3.67		3.67		3.67		3.63		3.59		3.64		3.65		3.61

		S1148889264:		#B4q1		1148889264:		$B4q1		3.67		3.67		3.67		3.63		3.58		3.64		3.65		3.61

		S1148889294:		#B4q1		1148889294:		$B4q1		3.67		3.67		3.67		3.63		3.58		3.64		3.65		3.61

		S1148889324:		#B4q1		1148889324:		$B4q1		3.67		3.67		3.67		3.62		3.58		3.64		3.65		3.61

		S1148889354:		#B4q1		1148889354:		$B4q1		3.67		3.67		3.67		3.62		3.58		3.64		3.65		3.61

		S1148889384:		#B4q1		1148889384:		$B4q1		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.61

		S1148889414:		#B4q1		1148889414:		$B4q1		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.6

		S1148889444:		#B4q1		1148889444:		$B4q1		3.67		3.66		3.67		3.62		3.58		3.64		3.65		3.6

		S1148889474:		#B4q1		1148889474:		$B4q1		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.6

		S1148889504:		#B4q1		1148889504:		$B4q1		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.6

		S1148889534:		#B4q1		1148889534:		$B4q1		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.6

		S1148889564:		#B4q1		1148889564:		$B4q1		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.6

		S1148889594:		#B4q1		1148889594:		$B4q1		3.67		3.66		3.67		3.62		3.57		3.64		3.65		3.6

		S1148889624:		#B4q1		1148889624:		$B4q1		3.67		3.66		3.66		3.62		3.57		3.64		3.65		3.6

		S1148889654:		#B4q1		1148889654:		$B4q1		3.67		3.66		3.66		3.62		3.57		3.64		3.65		3.6

		S1148889684:		#B4q1		1148889684:		$B4q1		3.67		3.66		3.66		3.62		3.56		3.64		3.65		3.59

		S1148889714:		#B4q1		1148889714:		$B4q1		3.67		3.66		3.66		3.62		3.56		3.64		3.65		3.59

		S1148889744:		#B4q1		1148889744:		$B4q1		3.66		3.66		3.66		3.62		3.56		3.64		3.65		3.59

		S1148889774:		#B4q1		1148889774:		$B4q1		3.66		3.66		3.66		3.62		3.56		3.64		3.65		3.59

		S1148889804:		#B4q1		1148889804:		$B4q1		3.66		3.66		3.66		3.62		3.55		3.64		3.64		3.59

		S1148889834:		#B4q1		1148889834:		$B4q1		3.66		3.66		3.66		3.62		3.55		3.63		3.65		3.58

		S1148889864:		#B4q1		1148889864:		$B4q1		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58

		S1148889894:		#B4q1		1148889894:		$B4q1		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58

		S1148889924:		#B4q1		1148889924:		$B4q1		3.66		3.66		3.66		3.62		3.55		3.63		3.64		3.58

		S1148889954:		#B4q1		1148889954:		$B4q1		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58

		S1148889984:		#B4q1		1148889984:		$B4q1		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58

		S1148890014:		#B4q1		1148890014:		$B4q1		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.58

		S1148890044:		#B4q1		1148890044:		$B4q1		3.66		3.66		3.66		3.62		3.54		3.63		3.64		3.57

		S1148890074:		#B4q1		1148890074:		$B4q1		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57

		S1148890104:		#B4q1		1148890104:		$B4q1		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57

		S1148890134:		#B4q1		1148890134:		$B4q1		3.66		3.66		3.66		3.62		3.53		3.63		3.64		3.57

		S1148890164:		#B4q1		1148890164:		$B4q1		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57

		S1148890194:		#B4q1		1148890194:		$B4q1		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57

		S1148890224:		#B4q1		1148890224:		$B4q1		3.66		3.66		3.66		3.61		3.53		3.63		3.64		3.57

		S1148890254:		#B4q1		1148890254:		$B4q1		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56

		S1148890284:		#B4q1		1148890284:		$B4q1		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56

		S1148890314:		#B4q1		1148890314:		$B4q1		3.66		3.66		3.66		3.61		3.52		3.63		3.64		3.56

		S1148890344:		#B4q1		1148890344:		$B4q1		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.56

		S1148890374:		#B4q1		1148890374:		$B4q1		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.56

		S1148890404:		#B4q1		1148890404:		$B4q1		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.55

		S1148890434:		#B4q1		1148890434:		$B4q1		3.66		3.66		3.66		3.61		3.51		3.63		3.64		3.55

		S1148890464:		#B4q1		1148890464:		$B4q1		3.66		3.66		3.66		3.6		3.51		3.63		3.64		3.55

		S1148890494:		#B4q1		1148890494:		$B4q1		3.66		3.66		3.66		3.6		3.5		3.63		3.64		3.55

		S1148890524:		#B4q1		1148890524:		$B4q1		3.66		3.66		3.66		3.6		3.5		3.63		3.64		3.55

		S1148890554:		#B4q1		1148890554:		$B4q1		3.66		3.66		3.66		3.6		3.5		3.63		3.64		3.55

		S1148890584:		#B4q1		1148890584:		$B4q1		3.66		3.66		3.66		3.6		3.5		3.63		3.64		3.54

		S1148890614:		#B4q1		1148890614:		$B4q1		3.66		3.66		3.66		3.6		3.49		3.63		3.64		3.54

		S1148890644:		#B4q1		1148890644:		$B4q1		3.66		3.66		3.66		3.6		3.49		3.63		3.64		3.54

		S1148890674:		#B4q1		1148890674:		$B4q1		3.66		3.66		3.66		3.6		3.49		3.63		3.64		3.54

		S1148890704:		#B4q1		1148890704:		$B4q1		3.66		3.66		3.66		3.6		3.48		3.63		3.64		3.53

		S1148890734:		#B4q1		1148890734:		$B4q1		3.66		3.66		3.66		3.6		3.48		3.63		3.64		3.53

		S1148890764:		#B4q1		1148890764:		$B4q1		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53

		S1148890794:		#B4q1		1148890794:		$B4q1		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53

		S1148890824:		#B4q1		1148890824:		$B4q1		3.66		3.66		3.66		3.59		3.48		3.63		3.64		3.53

		S1148890854:		#B4q1		1148890854:		$B4q1		3.66		3.66		3.66		3.59		3.47		3.63		3.64		3.53

		S1148890884:		#B4q1		1148890884:		$B4q1		3.66		3.65		3.66		3.59		3.47		3.63		3.64		3.52

		S1148890914:		#B4q1		1148890914:		$B4q1		3.66		3.65		3.66		3.59		3.47		3.63		3.64		3.52

		S1148890944:		#B4q1		1148890944:		$B4q1		3.66		3.65		3.66		3.58		3.46		3.63		3.64		3.52

		S1148890974:		#B4q1		1148890974:		$B4q1		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.52

		S1148891004:		#B4q1		1148891004:		$B4q1		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.51

		S1148891034:		#B4q1		1148891034:		$B4q1		3.66		3.65		3.66		3.58		3.46		3.62		3.64		3.51

		S1148891064:		#B4q1		1148891064:		$B4q1		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51

		S1148891094:		#B4q1		1148891094:		$B4q1		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51

		S1148891124:		#B4q1		1148891124:		$B4q1		3.66		3.65		3.66		3.58		3.45		3.62		3.64		3.51

		S1148891154:		#B4q1		1148891154:		$B4q1		3.65		3.65		3.65		3.58		3.44		3.62		3.64		3.5

		S1148891184:		#B4q1		1148891184:		$B4q1		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.5

		S1148891214:		#B4q1		1148891214:		$B4q1		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.5

		S1148891244:		#B4q1		1148891244:		$B4q1		3.65		3.65		3.65		3.57		3.44		3.62		3.64		3.5

		S1148891274:		#B4q1		1148891274:		$B4q1		3.65		3.65		3.65		3.57		3.43		3.62		3.64		3.5

		S1148891304:		#B4q1		1148891304:		$B4q1		3.65		3.65		3.65		3.57		3.43		3.62		3.64		3.49

		S1148891334:		#B4q1		1148891334:		$B4q1		3.65		3.65		3.65		3.57		3.42		3.62		3.64		3.49

		S1148891364:		#B4q1		1148891364:		$B4q1		3.65		3.65		3.65		3.57		3.42		3.62		3.64		3.49

		S1148891394:		#B4q1		1148891394:		$B4q1		3.65		3.65		3.65		3.56		3.42		3.62		3.64		3.48

		S1148891424:		#B4q1		1148891424:		$B4q1		3.65		3.65		3.65		3.56		3.42		3.62		3.64		3.48

		S1148891454:		#B4q1		1148891454:		$B4q1		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48

		S1148891484:		#B4q1		1148891484:		$B4q1		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48

		S1148891514:		#B4q1		1148891514:		$B4q1		3.65		3.65		3.65		3.56		3.41		3.62		3.64		3.48

		S1148891544:		#B4q1		1148891544:		$B4q1		3.65		3.65		3.65		3.55		3.4		3.62		3.64		3.47

		S1148891574:		#B4q1		1148891574:		$B4q1		3.65		3.65		3.65		3.55		3.4		3.62		3.64		3.47

		S1148891604:		#B4q1		1148891604:		$B4q1		3.65		3.65		3.65		3.55		3.39		3.62		3.64		3.47

		S1148891634:		#B4q1		1148891634:		$B4q1		3.65		3.64		3.65		3.55		3.39		3.61		3.64		3.46

		S1148891664:		#B4q1		1148891664:		$B4q1		3.65		3.64		3.65		3.55		3.39		3.61		3.64		3.46

		S1148891694:		#B4q1		1148891694:		$B4q1		3.65		3.65		3.65		3.55		3.39		3.61		3.64		3.46

		S1148891724:		#B4q1		1148891724:		$B4q1		3.65		3.64		3.65		3.55		3.38		3.61		3.64		3.46

		S1148891754:		#B4q1		1148891754:		$B4q1		3.65		3.64		3.65		3.55		3.38		3.61		3.64		3.45

		S1148891784:		#B4q1		1148891784:		$B4q1		3.65		3.64		3.65		3.55		3.37		3.61		3.64		3.45

		S1148891814:		#B4q1		1148891814:		$B4q1		3.65		3.64		3.65		3.55		3.37		3.61		3.64		3.45

		S1148891844:		#B4q1		1148891844:		$B4q1		3.65		3.64		3.65		3.54		3.36		3.61		3.64		3.44

		S1148891874:		#B4q1		1148891874:		$B4q1		3.65		3.64		3.65		3.54		3.36		3.61		3.64		3.44

		S1148891904:		#B4q1		1148891904:		$B4q1		3.65		3.64		3.65		3.54		3.35		3.6		3.64		3.44

		S1148891934:		#B4q1		1148891934:		$B4q1		3.65		3.64		3.64		3.54		3.35		3.6		3.64		3.44

		S1148891964:		#B4q1		1148891964:		$B4q1		3.65		3.64		3.64		3.54		3.35		3.6		3.64		3.43

		S1148891994:		#B4q1		1148891994:		$B4q1		3.65		3.64		3.64		3.54		3.34		3.6		3.64		3.43

		S1148892024:		#B4q1		1148892024:		$B4q1		3.64		3.64		3.64		3.53		3.34		3.6		3.63		3.42

		S1148892054:		#B4q1		1148892054:		$B4q1		3.64		3.64		3.64		3.53		3.33		3.6		3.63		3.42

		S1148892084:		#B4q1		1148892084:		$B4q1		3.64		3.64		3.64		3.53		3.33		3.6		3.63		3.42

		S1148892114:		#B4q1		1148892114:		$B4q1		3.64		3.64		3.64		3.53		3.32		3.6		3.63		3.42

		S1148892144:		#B4q1		1148892144:		$B4q1		3.64		3.64		3.64		3.53		3.32		3.6		3.63		3.42

		S1148892174:		#B4q1		1148892174:		$B4q1		3.64		3.64		3.64		3.53		3.31		3.59		3.63		3.42

		S1148892204:		#B4q1		1148892204:		$B4q1		3.64		3.64		3.64		3.52		3.31		3.59		3.63		3.41

		S1148892234:		#B4q1		1148892234:		$B4q1		3.64		3.64		3.64		3.52		3.3		3.59		3.63		3.41

		S1148892264:		#B4q1		1148892264:		$B4q1		3.64		3.64		3.64		3.52		3.3		3.59		3.63		3.41

		S1148892294:		#B4q1		1148892294:		$B4q1		3.64		3.64		3.64		3.52		3.29		3.59		3.63		3.41

		S1148892324:		#B4q1		1148892324:		$B4q1		3.64		3.64		3.64		3.52		3.28		3.59		3.63		3.4

		S1148892354:		#B4q1		1148892354:		$B4q1		3.64		3.64		3.64		3.51		3.28		3.58		3.63		3.4

		S1148892384:		#B4q1		1148892384:		$B4q1		3.64		3.64		3.64		3.51		3.27		3.58		3.63		3.39

		S1148892414:		#B4q1		1148892414:		$B4q1		3.64		3.64		3.64		3.51		3.26		3.58		3.63		3.39

		S1148892444:		#B4q1		1148892444:		$B4q1		3.64		3.64		3.64		3.51		3.26		3.58		3.63		3.39

		S1148892474:		#B4q1		1148892474:		$B4q1		3.64		3.64		3.64		3.51		3.25		3.58		3.63		3.39

		S1148892504:		#B4q1		1148892504:		$B4q1		3.64		3.64		3.64		3.51		3.24		3.58		3.63		3.38

		S1148892534:		#B4q1		1148892534:		$B4q1		3.64		3.64		3.64		3.51		3.23		3.58		3.63		3.38

		S1148892564:		#B4q1		1148892564:		$B4q1		3.64		3.64		3.64		3.51		3.23		3.58		3.63		3.37

		S1148892594:		#B4q1		1148892594:		$B4q1		3.64		3.64		3.64		3.5		3.22		3.57		3.63		3.37

		S1148892624:		#B4q1		1148892624:		$B4q1		3.64		3.64		3.64		3.5		3.21		3.57		3.63		3.37

		S1148892654:		#B4q1		1148892654:		$B4q1		3.64		3.64		3.64		3.5		3.21		3.57		3.63		3.37

		S1148892684:		#B4q1		1148892684:		$B4q1		3.64		3.64		3.64		3.5		3.2		3.57		3.63		3.36

		S1148892714:		#B4q1		1148892714:		$B4q1		3.64		3.64		3.64		3.5		3.19		3.57		3.63		3.36

		S1148892744:		#B4q1		1148892744:		$B4q1		3.64		3.64		3.64		3.5		3.18		3.57		3.63		3.35

		S1148892774:		#B4q1		1148892774:		$B4q1		3.64		3.64		3.64		3.49		3.17		3.57		3.63		3.35

		S1148892804:		#B4q1		1148892804:		$B4q1		3.64		3.64		3.64		3.49		3.16		3.57		3.63		3.35

		S1148892834:		#B4q1		1148892834:		$B4q1		3.64		3.64		3.64		3.49		3.16		3.56		3.63		3.34

		S1148892864:		#B4q1		1148892864:		$B4q1		3.64		3.64		3.64		3.49		3.15		3.56		3.63		3.34

		S1148892894:		#B4q1		1148892894:		$B4q1		3.64		3.64		3.64		3.48		3.14		3.56		3.63		3.33

		S1148892924:		#B4q1		1148892924:		$B4q1		3.66		3.66		3.66		3.51		3.17		3.58		3.65		3.36

		S1148892954:		#B4q1		1148892954:		$B4q1		3.66		3.66		3.66		3.51		3.17		3.58		3.65		3.36

		S1148892984:		#B4q1		1148892984:		$B4q1		3.67		3.66		3.66		3.51		3.18		3.58		3.65		3.37

		S1148893014:		#B4q1		1148893014:		$B4q1		3.67		3.66		3.66		3.51		3.19		3.58		3.65		3.37

		S1148893044:		#B4q1		1148893044:		$B4q1		3.67		3.66		3.67		3.51		3.19		3.59		3.65		3.37

		S1148893074:		#B4q1		1148893074:		$B4q1		3.67		3.66		3.67		3.52		3.2		3.59		3.66		3.37

		S1148893104:		#B4q1		1148893104:		$B4q1		3.67		3.66		3.67		3.52		3.2		3.59		3.66		3.37

		S1148893134:		#B4q1		1148893134:		$B4q1		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.37

		S1148893164:		#B4q1		1148893164:		$B4q1		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.38

		S1148893194:		#B4q1		1148893194:		$B4q1		3.67		3.66		3.67		3.52		3.21		3.59		3.66		3.38

		S1148893224:		#B4q1		1148893224:		$B4q1		3.67		3.66		3.67		3.52		3.22		3.59		3.66		3.38

		S1148893254:		#B4q1		1148893254:		$B4q1		3.67		3.67		3.67		3.52		3.22		3.59		3.66		3.38

		S1148893284:		#B4q1		1148893284:		$B4q1		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.38

		S1148893314:		#B4q1		1148893314:		$B4q1		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.38

		S1148893344:		#B4q1		1148893344:		$B4q1		3.67		3.66		3.67		3.52		3.23		3.59		3.66		3.39

		S1148893374:		#B4q1		1148893374:		$B4q1		3.67		3.66		3.67		3.53		3.23		3.59		3.66		3.39

		S1148893404:		#B4q1		1148893404:		$B4q1		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39

		S1148893434:		#B4q1		1148893434:		$B4q1		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39

		S1148893464:		#B4q1		1148893464:		$B4q1		3.67		3.67		3.67		3.53		3.24		3.59		3.66		3.39

		S1148893494:		#B4q1		1148893494:		$B4q1		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39

		S1148893524:		#B4q1		1148893524:		$B4q1		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39

		S1148893554:		#B4q1		1148893554:		$B4q1		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39

		S1148893584:		#B4q1		1148893584:		$B4q1		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39

		S1148893614:		#B4q1		1148893614:		$B4q1		3.67		3.67		3.67		3.53		3.25		3.59		3.66		3.39

		S1148893644:		#B4q1		1148893644:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893674:		#B4q1		1148893674:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893704:		#B4q1		1148893704:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893734:		#B4q1		1148893734:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893764:		#B4q1		1148893764:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893794:		#B4q1		1148893794:		$B4q1		3.67		3.67		3.67		3.53		3.26		3.59		3.66		3.4

		S1148893824:		#B4q1		1148893824:		$B4q1		3.67		3.67		3.67		3.53		3.27		3.6		3.66		3.4

		S1148893854:		#B4q1		1148893854:		$B4q1		3.67		3.67		3.67		3.53		3.28		3.6		3.66		3.4

		S1148893884:		#B4q1		1148893884:		$B4q1		3.67		3.67		3.67		3.53		3.28		3.6		3.66		3.41

		S1148893914:		#B4q1		1148893914:		$B4q1		3.67		3.67		3.67		3.53		3.28		3.6		3.66		3.41

		S1148893944:		#B4q1		1148893944:		$B4q1		3.67		3.67		3.67		3.53		3.29		3.6		3.66		3.41

		S1148893974:		#B4q1		1148893974:		$B4q1		3.67		3.67		3.67		3.53		3.29		3.6		3.66		3.41

		S1148894004:		#B4q1		1148894004:		$B4q1		3.67		3.67		3.67		3.54		3.29		3.6		3.66		3.41

		S1148894034:		#B4q1		1148894034:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894064:		#B4q1		1148894064:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894094:		#B4q1		1148894094:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894124:		#B4q1		1148894124:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894154:		#B4q1		1148894154:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894184:		#B4q1		1148894184:		$B4q1		3.67		3.67		3.67		3.54		3.3		3.6		3.66		3.41

		S1148894214:		#B4q1		1148894214:		$B4q1		3.67		3.67		3.67		3.54		3.31		3.6		3.66		3.41

		S1148894244:		#B4q1		1148894244:		$B4q1		3.67		3.67		3.67		3.54		3.31		3.6		3.66		3.41

		S1148894274:		#B4q1		1148894274:		$B4q1		3.67		3.67		3.67		3.54		3.31		3.6		3.66		3.41

		S1148894304:		#B4q1		1148894304:		$B4q1		3.67		3.67		3.67		3.54		3.31		3.6		3.66		3.42

		S1148894334:		#B4q1		1148894334:		$B4q1		3.67		3.67		3.67		3.54		3.32		3.6		3.66		3.42

		S1148894364:		#B4q1		1148894364:		$B4q1		3.67		3.67		3.67		3.54		3.32		3.6		3.66		3.42

		S1148894394:		#B4q1		1148894394:		$B4q1		3.67		3.67		3.67		3.54		3.33		3.6		3.66		3.42

		S1148894424:		#B4q1		1148894424:		$B4q1		3.67		3.67		3.67		3.54		3.33		3.6		3.66		3.42

		S1148894454:		#B4q1		1148894454:		$B4q1		3.67		3.67		3.67		3.54		3.33		3.6		3.66		3.42

		S1148894484:		#B4q1		1148894484:		$B4q1		3.67		3.67		3.67		3.54		3.34		3.6		3.66		3.42

		S1148894514:		#B4q1		1148894514:		$B4q1		3.67		3.67		3.67		3.54		3.34		3.6		3.66		3.42

		S1148894544:		#B4q1		1148894544:		$B4q1		3.67		3.67		3.67		3.54		3.34		3.6		3.66		3.42

		S1148894574:		#B4q1		1148894574:		$B4q1		3.67		3.67		3.67		3.55		3.35		3.6		3.66		3.42

		S1148894604:		#B4q1		1148894604:		$B4q1		3.67		3.67		3.67		3.55		3.35		3.6		3.66		3.42

		S1148894634:		#B4q1		1148894634:		$B4q1		3.67		3.67		3.67		3.55		3.35		3.6		3.66		3.42

		S1148894664:		#B4q1		1148894664:		$B4q1		3.67		3.67		3.67		3.55		3.35		3.6		3.66		3.42

		S1148894694:		#B4q1		1148894694:		$B4q1		3.67		3.67		3.67		3.55		3.36		3.6		3.66		3.43

		S1148894724:		#B4q1		1148894724:		$B4q1		3.67		3.67		3.67		3.55		3.36		3.6		3.66		3.43

		S1148894754:		#B4q1		1148894754:		$B4q1		3.67		3.67		3.67		3.55		3.36		3.6		3.66		3.43

		S1148894784:		#B4q1		1148894784:		$B4q1		3.67		3.67		3.67		3.55		3.36		3.6		3.66		3.43

		S1148894814:		#B4q1		1148894814:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894844:		#B4q1		1148894844:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894874:		#B4q1		1148894874:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894904:		#B4q1		1148894904:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894934:		#B4q1		1148894934:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894964:		#B4q1		1148894964:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148894994:		#B4q1		1148894994:		$B4q1		3.67		3.67		3.67		3.55		3.37		3.6		3.66		3.43

		S1148895024:		#B4q1		1148895024:		$B4q1		3.67		3.67		3.67		3.55		3.38		3.6		3.66		3.43

		S1148895054:		#B4q1		1148895054:		$B4q1		3.67		3.67		3.67		3.55		3.38		3.6		3.66		3.43

		S1148895084:		#B4q1		1148895084:		$B4q1		3.67		3.67		3.67		3.55		3.38		3.6		3.66		3.44

		S1148895114:		#B4q1		1148895114:		$B4q1		3.67		3.67		3.67		3.55		3.38		3.6		3.66		3.44

		S1148895144:		#B4q1		1148895144:		$B4q1		3.67		3.67		3.67		3.55		3.38		3.6		3.66		3.44

		S1148895174:		#B4q1		1148895174:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895204:		#B4q1		1148895204:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895234:		#B4q1		1148895234:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895264:		#B4q1		1148895264:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895294:		#B4q1		1148895294:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895324:		#B4q1		1148895324:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895354:		#B4q1		1148895354:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895384:		#B4q1		1148895384:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895414:		#B4q1		1148895414:		$B4q1		3.67		3.67		3.67		3.55		3.39		3.6		3.66		3.44

		S1148895444:		#B4q1		1148895444:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895474:		#B4q1		1148895474:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895504:		#B4q1		1148895504:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895534:		#B4q1		1148895534:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895564:		#B4q1		1148895564:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895594:		#B4q1		1148895594:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895624:		#B4q1		1148895624:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895654:		#B4q1		1148895654:		$B4q1		3.67		3.67		3.67		3.55		3.4		3.6		3.66		3.44

		S1148895684:		#B4q1		1148895684:		$B4q1		3.67		3.67		3.67		3.55		3.41		3.6		3.66		3.44

		S1148895714:		#B4q1		1148895714:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.44

		S1148895744:		#B4q1		1148895744:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.44

		S1148895774:		#B4q1		1148895774:		$B4q1		3.67		3.67		3.67		3.55		3.41		3.6		3.66		3.44

		S1148895804:		#B4q1		1148895804:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.44

		S1148895834:		#B4q1		1148895834:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148895864:		#B4q1		1148895864:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148895894:		#B4q1		1148895894:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148895924:		#B4q1		1148895924:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148895954:		#B4q1		1148895954:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148895984:		#B4q1		1148895984:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148896014:		#B4q1		1148896014:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148896044:		#B4q1		1148896044:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148896074:		#B4q1		1148896074:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.46

		S1148896104:		#B4q1		1148896104:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.46

		S1148896134:		#B4q1		1148896134:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.46

		S1148896164:		#B4q1		1148896164:		$B4q1		3.67		3.67		3.67		3.56		3.41		3.6		3.66		3.45

		S1148896194:		#B4q1		1148896194:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.6		3.66		3.46

		S1148896224:		#B4q1		1148896224:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896254:		#B4q1		1148896254:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896284:		#B4q1		1148896284:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896314:		#B4q1		1148896314:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896344:		#B4q1		1148896344:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896374:		#B4q1		1148896374:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896404:		#B4q1		1148896404:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896434:		#B4q1		1148896434:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896464:		#B4q1		1148896464:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896494:		#B4q1		1148896494:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896524:		#B4q1		1148896524:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896554:		#B4q1		1148896554:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896584:		#B4q1		1148896584:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896614:		#B4q1		1148896614:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896644:		#B4q1		1148896644:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896674:		#B4q1		1148896674:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896704:		#B4q1		1148896704:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896734:		#B4q1		1148896734:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896764:		#B4q1		1148896764:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896794:		#B4q1		1148896794:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896824:		#B4q1		1148896824:		$B4q1		3.67		3.67		3.67		3.56		3.42		3.61		3.66		3.46

		S1148896854:		#B4q1		1148896854:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148896884:		#B4q1		1148896884:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148896914:		#B4q1		1148896914:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148896944:		#B4q1		1148896944:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148896974:		#B4q1		1148896974:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897004:		#B4q1		1148897004:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897034:		#B4q1		1148897034:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897064:		#B4q1		1148897064:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897094:		#B4q1		1148897094:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897124:		#B4q1		1148897124:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897154:		#B4q1		1148897154:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897184:		#B4q1		1148897184:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897214:		#B4q1		1148897214:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897244:		#B4q1		1148897244:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897274:		#B4q1		1148897274:		$B4q1		3.67		3.67		3.67		3.56		3.43		3.61		3.66		3.46

		S1148897304:		#B4q1		1148897304:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897334:		#B4q1		1148897334:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897364:		#B4q1		1148897364:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897394:		#B4q1		1148897394:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897424:		#B4q1		1148897424:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897454:		#B4q1		1148897454:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897484:		#B4q1		1148897484:		$B4q1		3.67		3.67		3.67		3.57		3.43		3.61		3.66		3.46

		S1148897514:		#B4q1		1148897514:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.46

		S1148897544:		#B4q1		1148897544:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897574:		#B4q1		1148897574:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897604:		#B4q1		1148897604:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897634:		#B4q1		1148897634:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897664:		#B4q1		1148897664:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897694:		#B4q1		1148897694:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897724:		#B4q1		1148897724:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897754:		#B4q1		1148897754:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897784:		#B4q1		1148897784:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897814:		#B4q1		1148897814:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897844:		#B4q1		1148897844:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897874:		#B4q1		1148897874:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897904:		#B4q1		1148897904:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897934:		#B4q1		1148897934:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897964:		#B4q1		1148897964:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148897994:		#B4q1		1148897994:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898024:		#B4q1		1148898024:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898054:		#B4q1		1148898054:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898084:		#B4q1		1148898084:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898114:		#B4q1		1148898114:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898144:		#B4q1		1148898144:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898174:		#B4q1		1148898174:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898204:		#B4q1		1148898204:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898234:		#B4q1		1148898234:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898264:		#B4q1		1148898264:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898294:		#B4q1		1148898294:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898324:		#B4q1		1148898324:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898354:		#B4q1		1148898354:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898384:		#B4q1		1148898384:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898414:		#B4q1		1148898414:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898444:		#B4q1		1148898444:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898474:		#B4q1		1148898474:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898504:		#B4q1		1148898504:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47

		S1148898534:		#B4q1		1148898534:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47

		S1148898564:		#B4q1		1148898564:		$B4q1		3.67		3.67		3.67		3.57		3.44		3.61		3.66		3.47

		S1148898594:		#B4q1		1148898594:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47

		S1148898624:		#B4q1		1148898624:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.47

		S1148898654:		#B4q1		1148898654:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898684:		#B4q1		1148898684:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898714:		#B4q1		1148898714:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148898744:		#B4q1		1148898744:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898774:		#B4q1		1148898774:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898804:		#B4q1		1148898804:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898834:		#B4q1		1148898834:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898864:		#B4q1		1148898864:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898894:		#B4q1		1148898894:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148898924:		#B4q1		1148898924:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148898954:		#B4q1		1148898954:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148898984:		#B4q1		1148898984:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148899014:		#B4q1		1148899014:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148899044:		#B4q1		1148899044:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148899074:		#B4q1		1148899074:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148899104:		#B4q1		1148899104:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148899134:		#B4q1		1148899134:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.66		3.48

		S1148899164:		#B4q1		1148899164:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148899194:		#B4q1		1148899194:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148899224:		#B4q1		1148899224:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899254:		#B4q1		1148899254:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899284:		#B4q1		1148899284:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.61		3.67		3.48

		S1148899314:		#B4q1		1148899314:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899344:		#B4q1		1148899344:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899374:		#B4q1		1148899374:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899404:		#B4q1		1148899404:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899434:		#B4q1		1148899434:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899464:		#B4q1		1148899464:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899494:		#B4q1		1148899494:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899524:		#B4q1		1148899524:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899554:		#B4q1		1148899554:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899584:		#B4q1		1148899584:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899614:		#B4q1		1148899614:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899644:		#B4q1		1148899644:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899674:		#B4q1		1148899674:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899704:		#B4q1		1148899704:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899734:		#B4q1		1148899734:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899764:		#B4q1		1148899764:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899794:		#B4q1		1148899794:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899824:		#B4q1		1148899824:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899854:		#B4q1		1148899854:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899884:		#B4q1		1148899884:		$B4q1		3.67		3.67		3.67		3.58		3.44		3.62		3.67		3.48

		S1148899914:		#B4q1		1148899914:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148899944:		#B4q1		1148899944:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148899974:		#B4q1		1148899974:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900004:		#B4q1		1148900004:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900034:		#B4q1		1148900034:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900064:		#B4q1		1148900064:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900094:		#B4q1		1148900094:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900124:		#B4q1		1148900124:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900154:		#B4q1		1148900154:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900184:		#B4q1		1148900184:		$B4q1		3.67		3.67		3.67		3.59		3.44		3.62		3.67		3.48

		S1148900214:		#B4q1		1148900214:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900244:		#B4q1		1148900244:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900274:		#B4q1		1148900274:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900304:		#B4q1		1148900304:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900334:		#B4q1		1148900334:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900364:		#B4q1		1148900364:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900394:		#B4q1		1148900394:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900424:		#B4q1		1148900424:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900454:		#B4q1		1148900454:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900484:		#B4q1		1148900484:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900514:		#B4q1		1148900514:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900544:		#B4q1		1148900544:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.48

		S1148900574:		#B4q1		1148900574:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49
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		S1148900814:		#B4q1		1148900814:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49
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		S1148900904:		#B4q1		1148900904:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148900934:		#B4q1		1148900934:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148900964:		#B4q1		1148900964:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148900994:		#B4q1		1148900994:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901024:		#B4q1		1148901024:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901054:		#B4q1		1148901054:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901084:		#B4q1		1148901084:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901114:		#B4q1		1148901114:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901144:		#B4q1		1148901144:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901174:		#B4q1		1148901174:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901204:		#B4q1		1148901204:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901234:		#B4q1		1148901234:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901264:		#B4q1		1148901264:		$B4q1		3.67		3.67		3.67		3.59		3.45		3.62		3.67		3.49

		S1148901294:		#B4q1		1148901294:		$B4q1		3.67		3.67		3.67		3.6
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		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148		0.0323148148

		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037		0.032662037

		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593		0.0330092593

		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815		0.0333564815

		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037		0.0337037037

		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259		0.0340509259

		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481		0.0343981481

		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704		0.0347453704

		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926		0.0350925926

		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148		0.0354398148

		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037		0.035787037

		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593		0.0361342593

		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815		0.0364814815

		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037		0.0368287037

		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259		0.0371759259

		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481		0.0375231481

		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704		0.0378703704

		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926		0.0382175926

		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148		0.0385648148

		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037		0.038912037

		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593		0.0392592593

		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815		0.0396064815

		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037		0.0399537037

		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259		0.0403009259

		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481		0.0406481481

		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704		0.0409953704

		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926		0.0413425926

		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148		0.0416898148

		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037		0.042037037

		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593		0.0423842593

		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815		0.0427314815

		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037		0.0430787037

		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259		0.0434259259

		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481		0.0437731481

		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704		0.0441203704

		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926		0.0444675926

		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148		0.0448148148

		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037		0.045162037

		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593		0.0455092593

		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815		0.0458564815

		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037		0.0462037037

		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259		0.0465509259

		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222		0.0469097222

		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704		0.0472453704

		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926		0.0475925926

		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148		0.0479398148

		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037		0.048287037

		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593		0.0486342593

		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815		0.0489814815

		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037		0.0493287037

		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259		0.0496759259

		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481		0.0500231481

		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704		0.0503703704

		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926		0.0507175926

		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148		0.0510648148

		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037		0.051412037

		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593		0.0517592593

		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556		0.0521180556

		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037		0.0524537037

		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259		0.0528009259

		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481		0.0531481481

		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704		0.0534953704

		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667		0.0538541667

		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148		0.0541898148

		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037		0.054537037

		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593		0.0548842593

		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815		0.0552314815

		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037		0.0555787037

		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259		0.0559259259

		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481		0.0562731481

		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704		0.0566203704

		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926		0.0569675926

		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148		0.0573148148

		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037		0.057662037

		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593		0.0580092593

		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815		0.0583564815

		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037		0.0587037037

		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259		0.0590509259

		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481		0.0593981481

		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704		0.0597453704

		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926		0.0600925926

		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148		0.0604398148

		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111		0.0607986111

		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333		0.0611458333

		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815		0.0614814815

		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037		0.0618287037

		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875		0.0621875

		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481		0.0625231481

		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444		0.0628819444

		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926		0.0632175926

		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148		0.0635648148

		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037		0.063912037

		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593		0.0642592593

		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815		0.0646064815

		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037		0.0649537037

		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259		0.0653009259

		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481		0.0656481481

		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704		0.0659953704

		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926		0.0663425926

		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148		0.0666898148

		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037		0.067037037

		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593		0.0673842593

		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556		0.0677430556

		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037		0.0680787037

		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259		0.0684259259

		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481		0.0687731481

		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704		0.0691203704

		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926		0.0694675926

		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148		0.0698148148

		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037		0.070162037

		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593		0.0705092593

		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815		0.0708564815

		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037		0.0712037037

		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259		0.0715509259

		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481		0.0718981481

		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704		0.0722453704

		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926		0.0725925926

		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148		0.0729398148

		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037		0.073287037

		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593		0.0736342593

		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815		0.0739814815

		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037		0.0743287037

		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259		0.0746759259

		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481		0.0750231481

		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704		0.0753703704

		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926		0.0757175926

		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148		0.0760648148

		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037		0.076412037

		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593		0.0767592593

		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815		0.0771064815

		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037		0.0774537037

		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259		0.0778009259

		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481		0.0781481481

		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704		0.0784953704

		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926		0.0788425926

		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148		0.0791898148

		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037		0.079537037

		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593		0.0798842593

		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815		0.0802314815

		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037		0.0805787037

		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259		0.0809259259

		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481		0.0812731481

		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704		0.0816203704

		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926		0.0819675926

		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148		0.0823148148

		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037		0.082662037

		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593		0.0830092593

		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815		0.0833564815

		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037		0.0837037037

		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259		0.0840509259

		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481		0.0843981481

		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704		0.0847453704

		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926		0.0850925926

		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148		0.0854398148

		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037		0.085787037

		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593		0.0861342593

		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815		0.0864814815

		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037		0.0868287037

		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259		0.0871759259

		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481		0.0875231481

		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704		0.0878703704

		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926		0.0882175926

		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889		0.0885763889

		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037		0.088912037

		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593		0.0892592593

		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815		0.0896064815

		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037		0.0899537037

		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259		0.0903009259

		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481		0.0906481481

		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704		0.0909953704

		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926		0.0913425926

		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148		0.0916898148

		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037		0.092037037

		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593		0.0923842593

		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815		0.0927314815

		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037		0.0930787037

		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259		0.0934259259

		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222		0.0937847222

		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704		0.0941203704

		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926		0.0944675926

		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148		0.0948148148

		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037		0.095162037

		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333		0.0955208333

		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815		0.0958564815

		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037		0.0962037037

		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259		0.0965509259

		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481		0.0968981481

		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704		0.0972453704

		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926		0.0975925926

		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148		0.0979398148

		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037		0.098287037

		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593		0.0986342593

		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815		0.0989814815

		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037		0.0993287037

		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259		0.0996759259

		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481		0.1000231481

		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704		0.1003703704

		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926		0.1007175926

		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148		0.1010648148

		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037		0.101412037

		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593		0.1017592593

		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815		0.1021064815

		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037		0.1024537037

		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259		0.1028009259

		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481		0.1031481481

		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704		0.1034953704

		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926		0.1038425926

		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148		0.1041898148

		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111		0.1045486111

		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593		0.1048842593

		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815		0.1052314815

		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037		0.1055787037

		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259		0.1059259259

		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481		0.1062731481

		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704		0.1066203704

		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926		0.1069675926

		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148		0.1073148148

		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037		0.107662037

		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593		0.1080092593

		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815		0.1083564815

		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037		0.1087037037

		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259		0.1090509259

		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222		0.1094097222

		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704		0.1097453704

		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926		0.1100925926

		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889		0.1104513889

		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111		0.1107986111

		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593		0.1111342593

		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556		0.1114930556

		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037		0.1118287037

		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875		0.1121875

		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481		0.1125231481

		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444		0.1128819444

		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667		0.1132291667

		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889		0.1135763889

		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037		0.113912037

		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333		0.1142708333

		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556		0.1146180556

		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037		0.1149537037

		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259		0.1153009259

		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481		0.1156481481

		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704		0.1159953704

		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926		0.1163425926

		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889		0.1167013889

		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037		0.117037037

		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593		0.1173842593

		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815		0.1177314815

		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778		0.1180902778

		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259		0.1184259259

		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481		0.1187731481

		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704		0.1191203704

		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926		0.1194675926

		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148		0.1198148148

		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037		0.120162037

		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593		0.1205092593

		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815		0.1208564815

		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037		0.1212037037

		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259		0.1215509259

		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222		0.1219097222

		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444		0.1222569444

		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926		0.1225925926

		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148		0.1229398148

		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037		0.123287037

		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593		0.1236342593

		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556		0.1239930556

		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778		0.1243402778

		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259		0.1246759259

		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222		0.1250347222

		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704		0.1253703704

		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926		0.1257175926

		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148		0.1260648148

		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037		0.126412037

		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593		0.1267592593

		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815		0.1271064815

		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037		0.1274537037

		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259		0.1278009259

		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481		0.1422106481

		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704		0.1425578704

		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926		0.1429050926

		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148		0.1432523148

		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537		0.143599537

		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593		0.1439467593

		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815		0.1442939815

		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037		0.1446412037

		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259		0.1449884259

		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481		0.1453356481

		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704		0.1456828704

		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926		0.1460300926

		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148		0.1463773148

		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537		0.146724537

		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593		0.1470717593

		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815		0.1474189815

		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037		0.1477662037

		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259		0.1481134259

		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481		0.1484606481

		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704		0.1488078704

		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926		0.1491550926

		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148		0.1495023148

		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537		0.149849537

		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593		0.1501967593

		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815		0.1505439815

		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037		0.1508912037

		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259		0.1512384259

		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481		0.1515856481

		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704		0.1519328704

		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926		0.1522800926

		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148		0.1526273148

		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537		0.152974537

		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593		0.1533217593

		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815		0.1536689815

		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037		0.1540162037

		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259		0.1543634259

		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481		0.1547106481

		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704		0.1550578704

		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926		0.1554050926

		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148		0.1557523148

		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537		0.156099537

		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852		0.1564351852

		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815		0.1567939815

		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037		0.1571412037

		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259		0.1574884259

		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741		0.1578240741

		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704		0.1581828704

		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926		0.1585300926

		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148		0.1588773148

		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537		0.159224537

		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593		0.1595717593

		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815		0.1599189815

		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037		0.1602662037

		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259		0.1606134259

		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481		0.1609606481

		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704		0.1613078704

		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926		0.1616550926

		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148		0.1620023148

		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537		0.162349537

		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593		0.1626967593

		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815		0.1630439815

		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037		0.1633912037

		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259		0.1637384259

		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481		0.1640856481

		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704		0.1644328704

		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926		0.1647800926

		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148		0.1651273148

		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537		0.165474537

		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593		0.1658217593

		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815		0.1661689815

		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037		0.1665162037

		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259		0.1668634259

		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481		0.1672106481

		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704		0.1675578704

		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926		0.1679050926

		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148		0.1682523148

		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537		0.168599537

		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593		0.1689467593

		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815		0.1692939815

		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037		0.1696412037

		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259		0.1699884259

		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481		0.1703356481

		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704		0.1706828704

		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926		0.1710300926

		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148		0.1713773148

		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537		0.171724537

		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593		0.1720717593

		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815		0.1724189815

		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037		0.1727662037

		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259		0.1731134259

		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481		0.1734606481

		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704		0.1738078704

		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926		0.1741550926

		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148		0.1745023148

		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537		0.174849537

		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593		0.1751967593

		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815		0.1755439815

		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037		0.1758912037

		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259		0.1762384259

		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481		0.1765856481

		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704		0.1769328704

		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926		0.1772800926

		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148		0.1776273148

		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537		0.177974537

		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593		0.1783217593

		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815		0.1786689815

		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037		0.1790162037

		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259		0.1793634259

		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481		0.1797106481

		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704		0.1800578704

		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926		0.1804050926

		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148		0.1807523148

		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537		0.181099537

		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593		0.1814467593

		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815		0.1817939815

		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037		0.1821412037

		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259		0.1824884259

		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481		0.1828356481

		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704		0.1831828704

		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926		0.1835300926

		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148		0.1838773148

		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537		0.184224537

		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593		0.1845717593

		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815		0.1849189815

		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037		0.1852662037

		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259		0.1856134259

		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481		0.1859606481

		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704		0.1863078704

		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926		0.1866550926

		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148		0.1870023148

		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537		0.187349537

		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593		0.1876967593

		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815		0.1880439815

		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037		0.1883912037

		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259		0.1887384259

		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481		0.1890856481

		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704		0.1894328704

		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926		0.1897800926

		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148		0.1901273148

		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537		0.190474537

		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593		0.1908217593

		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815		0.1911689815

		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037		0.1915162037

		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259		0.1918634259

		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481		0.1922106481

		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704		0.1925578704

		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926		0.1929050926

		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148		0.1932523148

		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537		0.193599537

		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593		0.1939467593

		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815		0.1942939815

		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037		0.1946412037

		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259		0.1949884259

		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481		0.1953356481

		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704		0.1956828704

		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926		0.1960300926

		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148		0.1963773148

		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537		0.196724537

		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593		0.1970717593

		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815		0.1974189815

		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037		0.1977662037

		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259		0.1981134259

		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481		0.1984606481

		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704		0.1988078704

		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926		0.1991550926

		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148		0.1995023148

		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537		0.199849537

		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593		0.2001967593

		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815		0.2005439815

		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037		0.2008912037

		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259		0.2012384259

		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481		0.2015856481

		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704		0.2019328704

		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185		0.2022685185

		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148		0.2026273148

		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537		0.202974537

		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593		0.2033217593

		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815		0.2036689815

		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037		0.2040162037

		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259		0.2043634259

		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481		0.2047106481

		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704		0.2050578704

		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926		0.2054050926

		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148		0.2057523148

		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537		0.206099537

		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593		0.2064467593

		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815		0.2067939815

		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037		0.2071412037

		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259		0.2074884259

		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481		0.2078356481

		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704		0.2081828704

		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926		0.2085300926

		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148		0.2088773148

		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537		0.209224537

		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593		0.2095717593

		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815		0.2099189815

		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037		0.2102662037

		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259		0.2106134259

		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481		0.2109606481

		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704		0.2113078704

		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926		0.2116550926

		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148		0.2120023148

		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537		0.212349537

		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593		0.2126967593

		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815		0.2130439815

		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037		0.2133912037

		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259		0.2137384259

		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481		0.2140856481

		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704		0.2144328704

		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926		0.2147800926

		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148		0.2151273148

		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537		0.215474537

		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593		0.2158217593

		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815		0.2161689815

		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037		0.2165162037

		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259		0.2168634259

		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481		0.2172106481

		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704		0.2175578704

		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926		0.2179050926

		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148		0.2182523148

		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537		0.218599537

		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593		0.2189467593

		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815		0.2192939815

		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037		0.2196412037

		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259		0.2199884259

		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481		0.2203356481

		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704		0.2206828704

		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926		0.2210300926

		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148		0.2213773148

		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537		0.221724537

		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593		0.2220717593

		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815		0.2224189815

		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037		0.2227662037

		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259		0.2231134259

		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481		0.2234606481

		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704		0.2238078704

		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926		0.2241550926

		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148		0.2245023148

		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537		0.224849537

		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593		0.2251967593

		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815		0.2255439815

		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037		0.2258912037

		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259		0.2262384259

		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481		0.2265856481

		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704		0.2269328704

		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926		0.2272800926

		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148		0.2276273148

		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537		0.227974537

		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593		0.2283217593

		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815		0.2286689815

		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037		0.2290162037

		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259		0.2293634259

		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481		0.2297106481

		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704		0.2300578704

		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926		0.2304050926

		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148		0.2307523148

		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537		0.231099537

		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593		0.2314467593

		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815		0.2317939815

		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037		0.2321412037

		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259		0.2324884259

		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481		0.2328356481

		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704		0.2331828704

		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926		0.2335300926

		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148		0.2338773148

		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537		0.234224537

		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593		0.2345717593

		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815		0.2349189815

		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037		0.2352662037

		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259		0.2356134259

		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481		0.2359606481

		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704		0.2363078704

		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926		0.2366550926

		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148		0.2370023148

		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537		0.237349537

		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593		0.2376967593

		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815		0.2380439815

		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037		0.2383912037

		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259		0.2387384259

		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481		0.2390856481

		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704		0.2394328704

		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926		0.2397800926

		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148		0.2401273148

		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537		0.240474537

		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593		0.2408217593

		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815		0.2411689815

		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037		0.2415162037

		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259		0.2418634259

		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481		0.2422106481

		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704		0.2425578704

		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926		0.2429050926

		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148		0.2432523148

		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537		0.243599537

		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593		0.2439467593

		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815		0.2442939815

		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037		0.2446412037

		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259		0.2449884259

		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481		0.2453356481

		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704		0.2456828704

		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926		0.2460300926

		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148		0.2463773148

		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537		0.246724537

		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593		0.2470717593

		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815		0.2474189815

		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037		0.2477662037

		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259		0.2481134259

		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481		0.2484606481

		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704		0.2488078704

		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926		0.2491550926

		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148		0.2495023148

		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537		0.249849537

		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593		0.2501967593

		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815		0.2505439815

		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037		0.2508912037

		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259		0.2512384259

		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481		0.2515856481

		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704		0.2519328704

		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926		0.2522800926

		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148		0.2526273148

		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537		0.252974537

		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593		0.2533217593

		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815		0.2536689815

		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037		0.2540162037

		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259		0.2543634259

		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481		0.2547106481

		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704		0.2550578704

		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926		0.2554050926

		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148		0.2557523148

		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537		0.256099537

		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593		0.2564467593

		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815		0.2567939815

		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037		0.2571412037

		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259		0.2574884259

		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481		0.2578356481

		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704		0.2581828704

		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926		0.2585300926

		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148		0.2588773148

		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537		0.259224537

		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593		0.2595717593

		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815		0.2599189815

		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037		0.2602662037

		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259		0.2606134259

		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481		0.2609606481

		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704		0.2613078704

		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926		0.2616550926

		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148		0.2620023148

		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537		0.262349537

		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593		0.2626967593

		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815		0.2630439815

		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037		0.2633912037

		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259		0.2637384259

		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481		0.2640856481

		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704		0.2644328704

		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926		0.2647800926

		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148		0.2651273148

		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537		0.265474537

		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593		0.2658217593

		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815		0.2661689815

		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037		0.2665162037

		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259		0.2668634259

		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481		0.2672106481

		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704		0.2675578704

		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926		0.2679050926

		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148		0.2682523148

		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537		0.268599537

		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593		0.2689467593

		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815		0.2692939815

		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037		0.2696412037

		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259		0.2699884259

		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481		0.2703356481

		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704		0.2706828704

		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926		0.2710300926

		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148		0.2713773148

		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537		0.271724537

		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593		0.2720717593

		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815		0.2724189815

		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037		0.2727662037

		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259		0.2731134259

		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481		0.2734606481

		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704		0.2738078704

		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926		0.2741550926

		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148		0.2745023148

		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537		0.274849537

		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593		0.2751967593

		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815		0.2755439815

		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037		0.2758912037

		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259		0.2762384259

		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481		0.2765856481

		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704		0.2769328704

		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926		0.2772800926

		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148		0.2776273148

		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537		0.277974537

		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593		0.2783217593

		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815		0.2786689815

		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037		0.2790162037

		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259		0.2793634259

		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481		0.2797106481

		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704		0.2800578704

		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926		0.2804050926

		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148		0.2807523148

		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537		0.281099537

		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593		0.2814467593

		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815		0.2817939815

		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037		0.2821412037

		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259		0.2824884259

		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481		0.2828356481

		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704		0.2831828704

		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926		0.2835300926

		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148		0.2838773148

		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537		0.284224537

		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593		0.2845717593

		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815		0.2849189815

		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037		0.2852662037

		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259		0.2856134259

		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481		0.2859606481

		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704		0.2863078704

		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926		0.2866550926

		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148		0.2870023148

		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537		0.287349537

		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593		0.2876967593

		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815		0.2880439815

		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037		0.2883912037

		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259		0.2887384259

		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481		0.2890856481

		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704		0.2894328704

		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926		0.2897800926

		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148		0.2901273148

		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537		0.290474537

		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593		0.2908217593

		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815		0.2911689815

		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037		0.2915162037

		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259		0.2918634259

		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481		0.2922106481

		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704		0.2925578704

		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926		0.2929050926

		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148		0.2932523148

		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537		0.293599537

		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593		0.2939467593

		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815		0.2942939815

		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037		0.2946412037

		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259		0.2949884259

		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481		0.2953356481

		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704		0.2956828704

		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926		0.2960300926

		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148		0.2963773148

		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537		0.296724537

		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593		0.2970717593

		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815		0.2974189815

		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037		0.2977662037

		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259		0.2981134259

		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481		0.2984606481

		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704		0.2988078704

		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926		0.2991550926

		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148		0.2995023148

		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537		0.299849537

		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593		0.3001967593

		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815		0.3005439815

		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037		0.3008912037

		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259		0.3012384259

		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481		0.3015856481

		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704		0.3019328704

		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926		0.3022800926

		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148		0.3026273148

		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537		0.302974537

		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593		0.3033217593

		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815		0.3036689815

		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037		0.3040162037

		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259		0.3043634259

		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481		0.3047106481

		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704		0.3050578704

		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926		0.3054050926

		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148		0.3057523148

		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537		0.306099537

		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593		0.3064467593

		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815		0.3067939815

		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037		0.3071412037

		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259		0.3074884259

		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481		0.3078356481

		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704		0.3081828704

		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926		0.3085300926

		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148		0.3088773148

		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537		0.309224537

		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593		0.3095717593

		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815		0.3099189815

		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037		0.3102662037

		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259		0.3106134259

		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481		0.3109606481

		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704		0.3113078704

		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926		0.3116550926

		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148		0.3120023148

		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537		0.312349537

		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593		0.3126967593

		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815		0.3130439815

		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037		0.3133912037

		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259		0.3137384259

		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481		0.3140856481

		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704		0.3144328704

		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926		0.3147800926

		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148		0.3151273148

		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537		0.315474537

		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593		0.3158217593

		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815		0.3161689815

		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037		0.3165162037

		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259		0.3168634259

		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481		0.3172106481

		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704		0.3175578704

		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926		0.3179050926

		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148		0.3182523148

		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537		0.318599537

		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593		0.3189467593

		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815		0.3192939815

		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037		0.3196412037

		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259		0.3199884259

		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481		0.3203356481

		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704		0.3206828704

		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926		0.3210300926

		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148		0.3213773148

		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537		0.321724537

		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593		0.3220717593

		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815		0.3224189815

		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037		0.3227662037

		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259		0.3231134259

		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481		0.3234606481

		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704		0.3238078704

		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926		0.3241550926

		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148		0.3245023148

		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537		0.324849537

		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593		0.3251967593

		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815		0.3255439815

		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037		0.3258912037

		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259		0.3262384259

		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481		0.3265856481

		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704		0.3269328704

		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926		0.3272800926

		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148		0.3276273148

		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537		0.327974537

		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593		0.3283217593

		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815		0.3286689815

		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037		0.3290162037

		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259		0.3293634259

		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481		0.3297106481

		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704		0.3300578704

		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926		0.3304050926

		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148		0.3307523148

		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537		0.331099537

		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593		0.3314467593

		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815		0.3317939815

		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037		0.3321412037

		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259		0.3324884259

		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481		0.3328356481

		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704		0.3331828704

		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926		0.3335300926

		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148		0.3338773148

		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537		0.334224537

		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593		0.3345717593

		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815		0.3349189815

		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037		0.3352662037

		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259		0.3356134259

		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481		0.3359606481

		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704		0.3363078704

		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926		0.3366550926

		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148		0.3370023148

		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537		0.337349537

		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593		0.3376967593

		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815		0.3380439815

		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037		0.3383912037

		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259		0.3387384259

		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481		0.3390856481

		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704		0.3394328704

		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926		0.3397800926

		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148		0.3401273148

		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537		0.340474537

		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593		0.3408217593

		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815		0.3411689815

		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037		0.3415162037

		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259		0.3418634259

		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481		0.3422106481

		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704		0.3425578704

		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926		0.3429050926

		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148		0.3432523148

		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537		0.343599537

		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593		0.3439467593

		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815		0.3442939815

		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037		0.3446412037

		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259		0.3449884259

		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481		0.3453356481

		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704		0.3456828704

		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926		0.3460300926

		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148		0.3463773148

		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537		0.346724537

		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593		0.3470717593

		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815		0.3474189815

		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037		0.3477662037

		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259		0.3481134259

		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481		0.3484606481

		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704		0.3488078704

		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926		0.3491550926

		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148		0.3495023148

		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537		0.349849537

		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593		0.3501967593

		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815		0.3505439815

		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037		0.3508912037

		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259		0.3512384259

		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481		0.3515856481

		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704		0.3519328704

		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926		0.3522800926

		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148		0.3526273148

		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537		0.352974537

		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593		0.3533217593

		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815		0.3536689815

		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037		0.3540162037

		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259		0.3543634259

		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481		0.3547106481

		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704		0.3550578704

		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926		0.3554050926

		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148		0.3557523148

		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537		0.356099537

		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593		0.3564467593

		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815		0.3567939815

		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037		0.3571412037

		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259		0.3574884259

		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481		0.3578356481

		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704		0.3581828704

		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926		0.3585300926

		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148		0.3588773148

		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537		0.359224537

		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593		0.3595717593

		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815		0.3599189815

		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037		0.3602662037

		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259		0.3606134259

		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481		0.3609606481

		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704		0.3613078704

		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926		0.3616550926

		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148		0.3620023148

		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537		0.362349537

		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593		0.3626967593

		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815		0.3630439815

		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037		0.3633912037

		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259		0.3637384259

		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481		0.3640856481

		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704		0.3644328704

		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926		0.3647800926

		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148		0.3651273148

		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537		0.365474537

		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593		0.3658217593

		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815		0.3661689815

		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037		0.3665162037

		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259		0.3668634259

		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481		0.3672106481

		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704		0.3675578704

		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926		0.3679050926

		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148		0.3682523148

		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537		0.368599537

		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593		0.3689467593

		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815		0.3692939815

		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037		0.3696412037

		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259		0.3699884259

		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481		0.3703356481

		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704		0.3706828704

		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926		0.3710300926

		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148		0.3713773148

		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537		0.371724537

		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593		0.3720717593

		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815		0.3724189815

		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037		0.3727662037

		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259		0.3731134259

		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481		0.3734606481

		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704		0.3738078704

		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926		0.3741550926

		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148		0.3745023148

		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537		0.374849537

		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593		0.3751967593

		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815		0.3755439815

		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037		0.3758912037

		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259		0.3762384259

		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481		0.3765856481

		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704		0.3769328704

		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926		0.3772800926

		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148		0.3776273148

		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537		0.377974537

		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593		0.3783217593

		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815		0.3786689815

		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037		0.3790162037

		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259		0.3793634259

		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481		0.3797106481

		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704		0.3800578704

		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926		0.3804050926

		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148		0.3807523148

		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537		0.381099537

		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593		0.3814467593

		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815		0.3817939815

		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037		0.3821412037

		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259		0.3824884259

		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481		0.3828356481

		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704		0.3831828704

		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926		0.3835300926

		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148		0.3838773148

		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537		0.384224537

		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593		0.3845717593

		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815		0.3849189815

		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037		0.3852662037

		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259		0.3856134259

		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481		0.3859606481

		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704		0.3863078704

		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926		0.3866550926

		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148		0.3870023148

		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537		0.387349537

		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593		0.3876967593

		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815		0.3880439815

		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037		0.3883912037

		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259		0.3887384259

		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481		0.3890856481

		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704		0.3894328704

		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926		0.3897800926

		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148		0.3901273148

		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537		0.390474537

		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593		0.3908217593

		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815		0.3911689815

		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037		0.3915162037

		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259		0.3918634259

		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481		0.3922106481

		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704		0.3925578704

		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926		0.3929050926

		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148		0.3932523148

		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537		0.393599537

		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593		0.3939467593

		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815		0.3942939815

		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037		0.3946412037

		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259		0.3949884259

		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481		0.3953356481

		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704		0.3956828704

		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926		0.3960300926

		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148		0.3963773148

		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537		0.396724537

		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593		0.3970717593

		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815		0.3974189815

		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037		0.3977662037

		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259		0.3981134259

		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481		0.3984606481

		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704		0.3988078704

		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926		0.3991550926

		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148		0.3995023148

		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537		0.399849537

		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593		0.4001967593

		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815		0.4005439815

		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037		0.4008912037

		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259		0.4012384259

		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481		0.4015856481

		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704		0.4019328704

		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926		0.4022800926

		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148		0.4026273148

		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537		0.402974537

		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593		0.4033217593

		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815		0.4036689815

		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037		0.4040162037

		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259		0.4043634259

		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481		0.4047106481

		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704		0.4050578704

		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926		0.4054050926

		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148		0.4057523148

		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537		0.406099537

		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593		0.4064467593

		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815		0.4067939815

		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037		0.4071412037

		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259		0.4074884259

		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481		0.4078356481

		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704		0.4081828704

		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926		0.4085300926

		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148		0.4088773148

		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537		0.409224537

		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593		0.4095717593

		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815		0.4099189815

		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037		0.4102662037

		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259		0.4106134259

		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481		0.4109606481

		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704		0.4113078704

		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926		0.4116550926

		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148		0.4120023148

		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537		0.412349537

		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593		0.4126967593

		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815		0.4130439815

		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037		0.4133912037

		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259		0.4137384259

		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481		0.4140856481

		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704		0.4144328704

		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926		0.4147800926

		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148		0.4151273148

		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537		0.415474537

		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593		0.4158217593

		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815		0.4161689815

		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037		0.4165162037

		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259		0.4168634259

		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481		0.4172106481

		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704		0.4175578704

		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926		0.4179050926

		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148		0.4182523148

		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537		0.418599537

		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593		0.4189467593

		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815		0.4192939815

		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037		0.4196412037

		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259		0.4199884259

		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481		0.4203356481

		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704		0.4206828704

		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926		0.4210300926

		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148		0.4213773148

		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537		0.421724537

		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593		0.4220717593

		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815		0.4224189815

		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037		0.4227662037

		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259		0.4231134259

		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481		0.4234606481

		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704		0.4238078704

		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926		0.4241550926

		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148		0.4245023148

		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537		0.424849537

		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593		0.4251967593

		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815		0.4255439815

		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037		0.4258912037

		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259		0.4262384259

		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481		0.4265856481

		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704		0.4269328704

		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926		0.4272800926

		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148		0.4276273148

		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537		0.427974537

		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593		0.4283217593

		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815		0.4286689815

		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037		0.4290162037

		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259		0.4293634259

		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481		0.4297106481

		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704		0.4300578704

		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926		0.4304050926

		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148		0.4307523148

		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537		0.431099537

		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593		0.4314467593

		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815		0.4317939815

		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037		0.4321412037

		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259		0.4324884259

		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481		0.4328356481

		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704		0.4331828704

		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926		0.4335300926

		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148		0.4338773148

		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537		0.434224537

		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593		0.4345717593

		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815		0.4349189815

		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037		0.4352662037

		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259		0.4356134259

		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481		0.4359606481

		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704		0.4363078704

		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926		0.4366550926

		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148		0.4370023148

		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537		0.437349537

		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593		0.4376967593

		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815		0.4380439815

		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037		0.4383912037

		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259		0.4387384259

		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481		0.4390856481

		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704		0.4394328704

		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926		0.4397800926

		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148		0.4401273148

		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537		0.440474537

		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593		0.4408217593

		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815		0.4411689815

		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037		0.4415162037

		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259		0.4418634259

		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481		0.4422106481

		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704		0.4425578704

		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926		0.4429050926

		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148		0.4432523148

		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537		0.443599537

		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593		0.4439467593

		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815		0.4442939815

		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037		0.4446412037

		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259		0.4449884259

		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481		0.4453356481

		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704		0.4456828704

		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926		0.4460300926

		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148		0.4463773148

		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537		0.446724537

		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593		0.4470717593

		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815		0.4474189815

		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037		0.4477662037

		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259		0.4481134259

		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481		0.4484606481

		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704		0.4488078704

		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926		0.4491550926

		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148		0.4495023148

		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537		0.449849537

		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593		0.4501967593

		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815		0.4505439815

		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037		0.4508912037

		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259		0.4512384259

		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481		0.4515856481

		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704		0.4519328704

		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926		0.4522800926

		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148		0.4526273148

		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537		0.452974537

		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593		0.4533217593

		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815		0.4536689815

		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037		0.4540162037

		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259		0.4543634259

		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481		0.4547106481

		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704		0.4550578704

		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926		0.4554050926

		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148		0.4557523148

		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537		0.456099537

		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593		0.4564467593

		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815		0.4567939815

		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037		0.4571412037

		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259		0.4574884259

		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481		0.4578356481

		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704		0.4581828704

		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926		0.4585300926

		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148		0.4588773148

		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537		0.459224537

		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593		0.4595717593

		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815		0.4599189815

		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037		0.4602662037

		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259		0.4606134259

		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481		0.4609606481

		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704		0.4613078704

		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926		0.4616550926

		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148		0.4620023148

		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537		0.462349537

		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593		0.4626967593

		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815		0.4630439815

		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037		0.4633912037

		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259		0.4637384259

		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481		0.4640856481

		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704		0.4644328704

		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926		0.4647800926

		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148		0.4651273148

		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537		0.465474537

		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593		0.4658217593

		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815		0.4661689815

		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037		0.4665162037

		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259		0.4668634259

		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481		0.4672106481

		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704		0.4675578704

		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926		0.4679050926

		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148		0.4682523148

		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537		0.468599537

		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593		0.4689467593

		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815		0.4692939815

		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037		0.4696412037

		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259		0.4699884259

		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481		0.4703356481

		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704		0.4706828704

		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926		0.4710300926

		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148		0.4713773148

		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537		0.471724537

		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593		0.4720717593

		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815		0.4724189815

		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037		0.4727662037

		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259		0.4731134259

		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481		0.4734606481

		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704		0.4738078704

		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926		0.4741550926

		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148		0.4745023148

		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537		0.474849537

		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593		0.4751967593

		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815		0.4755439815

		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037		0.4758912037

		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259		0.4762384259

		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481		0.4765856481

		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704		0.4769328704

		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926		0.4772800926

		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148		0.4776273148

		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537		0.477974537

		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593		0.4783217593

		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815		0.4786689815

		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037		0.4790162037

		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259		0.4793634259

		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481		0.4797106481

		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704		0.4800578704

		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926		0.4804050926

		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148		0.4807523148

		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537		0.481099537

		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593		0.4814467593

		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815		0.4817939815

		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037		0.4821412037

		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259		0.4824884259

		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481		0.4828356481

		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704		0.4831828704

		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926		0.4835300926

		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148		0.4838773148

		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537		0.484224537

		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593		0.4845717593

		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815		0.4849189815

		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037		0.4852662037

		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259		0.4856134259

		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481		0.4859606481

		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704		0.4863078704

		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926		0.4866550926

		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148		0.4870023148

		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537		0.487349537

		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593		0.4876967593

		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815		0.4880439815

		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037		0.4883912037

		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259		0.4887384259

		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481		0.4890856481

		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704		0.4894328704

		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926		0.4897800926

		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148		0.4901273148

		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537		0.490474537

		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593		0.4908217593

		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815		0.4911689815

		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037		0.4915162037

		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259		0.4918634259

		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481		0.4922106481

		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704		0.4925578704

		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926		0.4929050926

		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148		0.4932523148

		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537		0.493599537

		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593		0.4939467593

		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815		0.4942939815

		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037		0.4946412037

		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259		0.4949884259

		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481		0.4953356481

		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704		0.4956828704

		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926		0.4960300926

		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148		0.4963773148

		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593		0.4970717593

		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815		0.4974189815

		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037		0.4977662037

		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259		0.4981134259

		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481		0.4984606481

		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704		0.4988078704

		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926		0.4991550926

		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148		0.4995023148

		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537		0.499849537

		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593		0.5001967593

		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815		0.5005439815

		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037		0.5008912037

		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259		0.5012384259

		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481		0.5015856481

		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704		0.5019328704

		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926		0.5022800926

		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148		0.5026273148

		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537		0.502974537

		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593		0.5033217593

		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815		0.5036689815

		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037		0.5040162037

		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259		0.5043634259

		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481		0.5047106481

		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704		0.5050578704

		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926		0.5054050926

		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148		0.5057523148

		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537		0.506099537

		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593		0.5064467593

		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815		0.5067939815

		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037		0.5071412037

		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259		0.5074884259

		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481		0.5078356481

		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704		0.5081828704

		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926		0.5085300926

		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148		0.5088773148

		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111		0.5092361111

		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593		0.5095717593

		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815		0.5099189815

		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037		0.5102662037

		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259		0.5106134259

		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481		0.5109606481

		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704		0.5113078704

		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926		0.5116550926

		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148		0.5120023148

		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537		0.512349537

		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593		0.5126967593

		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815		0.5130439815

		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037		0.5133912037

		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259		0.5137384259

		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481		0.5140856481

		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704		0.5144328704

		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926		0.5147800926

		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148		0.5151273148

		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537		0.515474537

		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593		0.5158217593

		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815		0.5161689815

		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037		0.5165162037

		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259		0.5168634259

		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481		0.5172106481

		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704		0.5175578704

		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926		0.5179050926

		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148		0.5182523148

		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537		0.518599537

		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593		0.5189467593

		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815		0.5192939815

		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037		0.5196412037

		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259		0.5199884259

		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481		0.5203356481

		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704		0.5206828704

		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926		0.5210300926

		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148		0.5213773148

		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537		0.521724537

		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593		0.5220717593

		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815		0.5224189815

		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037		0.5227662037

		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259		0.5231134259

		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481		0.5234606481

		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704		0.5238078704

		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926		0.5241550926

		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148		0.5245023148

		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537		0.524849537

		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593		0.5251967593

		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815		0.5255439815

		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037		0.5258912037

		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259		0.5262384259

		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481		0.5265856481

		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704		0.5269328704

		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926		0.5272800926

		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148		0.5276273148

		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537		0.527974537

		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593		0.5283217593

		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815		0.5286689815

		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037		0.5290162037

		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259		0.5293634259

		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481		0.5297106481

		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704		0.5300578704

		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926		0.5304050926

		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148		0.5307523148

		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537		0.531099537

		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593		0.5314467593

		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815		0.5317939815

		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037		0.5321412037

		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259		0.5324884259

		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481		0.5328356481

		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704		0.5331828704

		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667		0.5335416667

		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148		0.5338773148

		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537		0.534224537

		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593		0.5345717593

		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556		0.5349305556

		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037		0.5352662037

		0.535625		0.535625		0.535625		0.535625		0.535625		0.535625		0.535625		0.535625		0.535625		0.535625

		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222		0.5359722222

		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444		0.5363194444

		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926		0.5366550926

		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148		0.5370023148

		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537		0.537349537

		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593		0.5376967593

		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815		0.5380439815

		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778		0.5384027778

		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259		0.5387384259

		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481		0.5390856481

		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704		0.5394328704

		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926		0.5397800926

		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148		0.5401273148

		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537		0.540474537

		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593		0.5408217593

		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815		0.5411689815

		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037		0.5415162037

		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259		0.5418634259

		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222		0.5422222222

		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444		0.5425694444

		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926		0.5429050926

		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148		0.5432523148

		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111		0.5436111111

		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333		0.5439583333

		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815		0.5442939815

		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037		0.5446412037

		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259		0.5449884259

		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481		0.5453356481

		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444		0.5456944444

		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926		0.5460300926

		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889		0.5463888889

		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111		0.5467361111

		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593		0.5470717593

		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815		0.5474189815

		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037		0.5477662037

		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259		0.5481134259

		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481		0.5484606481

		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444		0.5488194444

		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926		0.5491550926

		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148		0.5495023148

		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111		0.5498611111

		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333		0.5502083333

		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815		0.5505439815

		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037		0.5508912037

		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259		0.5512384259

		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481		0.5515856481

		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444		0.5519444444

		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926		0.5522800926

		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889		0.5526388889

		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537		0.552974537

		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593		0.5533217593

		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815		0.5536689815

		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778		0.5540277778

		0.554375		0.554375		0.554375		0.554375		0.554375		0.554375		0.554375		0.554375		0.554375		0.554375

		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481		0.5547106481

		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444		0.5550694444

		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926		0.5554050926

		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889		0.5557638889

		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111		0.5561111111

		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593		0.5564467593

		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556		0.5568055556

		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037		0.5571412037

		0.5575		0.5575		0.5575		0.5575		0.5575		0.5575		0.5575		0.5575		0.5575		0.5575

		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222		0.5578472222

		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444		0.5581944444

		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667		0.5585416667

		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148		0.5588773148

		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111		0.5592361111

		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333		0.5595833333

		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815		0.5599189815

		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778		0.5602777778

		0.560625		0.560625		0.560625		0.560625		0.560625		0.560625		0.560625		0.560625		0.560625		0.560625

		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222		0.5609722222

		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444		0.5613194444

		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667		0.5616666667

		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889		0.5620138889

		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111		0.5623611111

		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593		0.5626967593

		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556		0.5630555556

		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037		0.5633912037

		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259		0.5637384259

		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222		0.5640972222

		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704		0.5644328704

		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926		0.5647800926

		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148		0.5651273148

		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537		0.565474537

		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593		0.5658217593

		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556		0.5661805556

		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778		0.5665277778

		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259		0.5668634259

		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481		0.5672106481

		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444		0.5675694444

		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926		0.5679050926

		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889		0.5682638889

		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111		0.5686111111

		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333		0.5689583333

		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556		0.5693055556

		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778		0.5696527778

		0.57		0.57		0.57		0.57		0.57		0.57		0.57		0.57		0.57		0.57

		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222		0.5703472222

		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444		0.5706944444

		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667		0.5710416667

		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889		0.5713888889

		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537		0.571724537

		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593		0.5720717593

		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815		0.5724189815

		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778		0.5727777778

		0.573125		0.573125		0.573125		0.573125		0.573125		0.573125		0.573125		0.573125		0.573125		0.573125

		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222		0.5734722222

		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444		0.5738194444

		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667		0.5741666667

		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889		0.5745138889

		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111		0.5748611111

		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333		0.5752083333

		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556		0.5755555556

		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778		0.5759027778

		0.57625		0.57625		0.57625		0.57625		0.57625		0.57625		0.57625		0.57625		0.57625		0.57625

		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222		0.5765972222

		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444		0.5769444444

		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667		0.5772916667

		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148		0.5776273148

		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111		0.5779861111

		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333		0.5783333333

		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556		0.5786805556

		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778		0.5790277778

		0.579375		0.579375		0.579375		0.579375		0.579375		0.579375		0.579375		0.579375		0.579375		0.579375

		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222		0.5797222222

		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444		0.5800694444

		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667		0.5804166667

		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889		0.5807638889

		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111		0.5811111111

		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333		0.5814583333

		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556		0.5818055556

		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778		0.5821527778

		0.5825		0.5825		0.5825		0.5825		0.5825		0.5825		0.5825		0.5825		0.5825		0.5825

		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222		0.5828472222

		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444		0.5831944444

		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667		0.5835416667

		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889		0.5838888889

		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111		0.5842361111

		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333		0.5845833333

		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556		0.5849305556

		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778		0.5852777778

		0.585625		0.585625		0.585625		0.585625		0.585625		0.585625		0.585625		0.585625		0.585625		0.585625

		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222		0.5859722222

		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444		0.5863194444

		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667		0.5866666667

		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889		0.5870138889

		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111		0.5873611111

		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333		0.5877083333

		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556		0.5880555556

		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778		0.5884027778

		0.58875		0.58875		0.58875		0.58875		0.58875		0.58875		0.58875		0.58875		0.58875		0.58875

		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222		0.5890972222

		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444		0.5894444444

		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667		0.5897916667

		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889		0.5901388889

		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111		0.5904861111

		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333		0.5908333333

		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556		0.5911805556

		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778		0.5915277778

		0.591875		0.591875		0.591875		0.591875		0.591875		0.591875		0.591875		0.591875		0.591875		0.591875

		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222		0.5922222222

		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444		0.5925694444

		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667		0.5929166667

		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889		0.5932638889

		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111		0.5936111111

		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333		0.5939583333

		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556		0.5943055556

		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778		0.5946527778

		0.595		0.595		0.595		0.595		0.595		0.595		0.595		0.595		0.595		0.595

		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222		0.5953472222

		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444		0.5956944444

		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667		0.5960416667

		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889		0.5963888889

		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111		0.5967361111

		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333		0.5970833333

		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556		0.5974305556

		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778		0.5977777778

		0.598125		0.598125		0.598125		0.598125		0.598125		0.598125		0.598125		0.598125		0.598125		0.598125

		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222		0.5984722222

		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444		0.5988194444

		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667		0.5991666667

		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889		0.5995138889

		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111		0.5998611111

		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333		0.6002083333

		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556		0.6005555556

		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778		0.6009027778

		0.60125		0.60125		0.60125		0.60125		0.60125		0.60125		0.60125		0.60125		0.60125		0.60125

		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222		0.6015972222

		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444		0.6019444444

		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667		0.6022916667

		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889		0.6026388889

		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111		0.6029861111

		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333		0.6033333333

		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556		0.6036805556

		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778		0.6040277778

		0.604375		0.604375		0.604375		0.604375		0.604375		0.604375		0.604375		0.604375		0.604375		0.604375

		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222		0.6047222222

		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444		0.6050694444

		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667		0.6054166667

		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889		0.6057638889

		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111		0.6061111111

		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333		0.6064583333

		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556		0.6068055556

		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778		0.6071527778

		0.6075		0.6075		0.6075		0.6075		0.6075		0.6075		0.6075		0.6075		0.6075		0.6075

		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222		0.6078472222

		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444		0.6081944444

		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667		0.6085416667

		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889		0.6088888889

		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111		0.6092361111

		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333		0.6095833333

		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556		0.6099305556

		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778		0.6102777778

		0.610625		0.610625		0.610625		0.610625		0.610625		0.610625		0.610625		0.610625		0.610625		0.610625

		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222		0.6109722222

		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444		0.6113194444

		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667		0.6116666667

		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889		0.6120138889

		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111		0.6123611111

		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333		0.6127083333

		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556		0.6130555556

		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778		0.6134027778

		0.61375		0.61375		0.61375		0.61375		0.61375		0.61375		0.61375		0.61375		0.61375		0.61375

		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222		0.6140972222

		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444		0.6144444444

		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667		0.6147916667

		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889		0.6151388889

		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111		0.6154861111

		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333		0.6158333333

		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556		0.6161805556

		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778		0.6165277778

		0.616875		0.616875		0.616875		0.616875		0.616875		0.616875		0.616875		0.616875		0.616875		0.616875

		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222		0.6172222222

		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444		0.6175694444

		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667		0.6179166667

		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889		0.6182638889

		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111		0.6186111111

		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333		0.6189583333

		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556		0.6193055556

		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778		0.6196527778

		0.62		0.62		0.62		0.62		0.62		0.62		0.62		0.62		0.62		0.62

		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222		0.6203472222

		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444		0.6206944444

		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667		0.6210416667

		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889		0.6213888889

		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111		0.6217361111

		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333		0.6220833333

		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556		0.6224305556

		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778		0.6227777778

		0.623125		0.623125		0.623125		0.623125		0.623125		0.623125		0.623125		0.623125		0.623125		0.623125

		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222		0.6234722222

		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444		0.6238194444

		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667		0.6241666667

		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889		0.6245138889

		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111		0.6248611111

		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333		0.6252083333

		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556		0.6255555556

		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778		0.6259027778

		0.62625		0.62625		0.62625		0.62625		0.62625		0.62625		0.62625		0.62625		0.62625		0.62625

		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222		0.6265972222

		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444		0.6269444444

		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667		0.6272916667

		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889		0.6276388889

		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111		0.6279861111

		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333		0.6283333333

		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556		0.6286805556

		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778		0.6290277778

		0.629375		0.629375		0.629375		0.629375		0.629375		0.629375		0.629375		0.629375		0.629375		0.629375

		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222		0.6297222222

		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444		0.6300694444

		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667		0.6304166667

		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889		0.6307638889

		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111		0.6311111111

		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333		0.6314583333

		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556		0.6318055556

		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778		0.6321527778

		0.6325		0.6325		0.6325		0.6325		0.6325		0.6325		0.6325		0.6325		0.6325		0.6325

		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222		0.6328472222

		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444		0.6331944444

		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667		0.6335416667

		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889		0.6338888889

		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111		0.6342361111

		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333		0.6345833333

		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556		0.6349305556

		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778		0.6352777778

		0.635625		0.635625		0.635625		0.635625		0.635625		0.635625		0.635625		0.635625		0.635625		0.635625

		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222		0.6359722222

		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444		0.6363194444

		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667		0.6366666667

		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889		0.6370138889

		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111		0.6373611111

		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333		0.6377083333

		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556		0.6380555556

		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778		0.6384027778

		0.63875		0.63875		0.63875		0.63875		0.63875		0.63875		0.63875		0.63875		0.63875		0.63875

		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222		0.6390972222

		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444		0.6394444444

		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667		0.6397916667

		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889		0.6401388889

		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111		0.6404861111

		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333		0.6408333333

		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556		0.6411805556

		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778		0.6415277778

		0.641875		0.641875		0.641875		0.641875		0.641875		0.641875		0.641875		0.641875		0.641875		0.641875

		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222		0.6422222222

		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444		0.6425694444

		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667		0.6429166667

		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889		0.6432638889

		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111		0.6436111111

		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333		0.6439583333

		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556		0.6443055556

		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778		0.6446527778

		0.645		0.645		0.645		0.645		0.645		0.645		0.645		0.645		0.645		0.645

		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222		0.6453472222

		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444		0.6456944444

		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667		0.6460416667

		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889		0.6463888889

		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111		0.6467361111

		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333		0.6470833333

		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556		0.6474305556

		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778		0.6477777778

		0.648125		0.648125		0.648125		0.648125		0.648125		0.648125		0.648125		0.648125		0.648125		0.648125

		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222		0.6484722222

		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444		0.6488194444

		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667		0.6491666667

		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889		0.6495138889

		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111		0.6498611111

		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333		0.6502083333

		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556		0.6505555556

		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778		0.6509027778

		0.65125		0.65125		0.65125		0.65125		0.65125		0.65125		0.65125		0.65125		0.65125		0.65125

		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222		0.6515972222

		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444		0.6519444444

		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667		0.6522916667

		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889		0.6526388889

		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111		0.6529861111

		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333		0.6533333333

		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556		0.6536805556

		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778		0.6540277778

		0.654375		0.654375		0.654375		0.654375		0.654375		0.654375		0.654375		0.654375		0.654375		0.654375

		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222		0.6547222222

		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444		0.6550694444

		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667		0.6554166667

		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889		0.6557638889

		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111		0.6561111111

		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333		0.6564583333

		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556		0.6568055556

		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778		0.6571527778

		0.6575		0.6575		0.6575		0.6575		0.6575		0.6575		0.6575		0.6575		0.6575		0.6575

		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222		0.6578472222

		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444		0.6581944444

		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667		0.6585416667

		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889		0.6588888889

		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111		0.6592361111

		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333		0.6595833333

		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556		0.6599305556

		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778		0.6602777778

		0.660625		0.660625		0.660625		0.660625		0.660625		0.660625		0.660625		0.660625		0.660625		0.660625

		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222		0.6609722222

		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444		0.6613194444

		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667		0.6616666667

		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889		0.6620138889

		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111		0.6623611111

		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333		0.6627083333

		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556		0.6630555556

		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778		0.6634027778

		0.66375		0.66375		0.66375		0.66375		0.66375		0.66375		0.66375		0.66375		0.66375		0.66375

		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222		0.6640972222

		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444		0.6644444444

		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667		0.6647916667

		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889		0.6651388889

		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111		0.6654861111

		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333		0.6658333333

		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556		0.6661805556

		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778		0.6665277778

		0.666875		0.666875		0.666875		0.666875		0.666875		0.666875		0.666875		0.666875		0.666875		0.666875

		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222		0.6672222222

		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444		0.6675694444

		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667		0.6679166667

		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889		0.6682638889

		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111		0.6686111111

		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333		0.6689583333

		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556		0.6693055556

		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778		0.6696527778

		0.67		0.67		0.67		0.67		0.67		0.67		0.67		0.67		0.67		0.67

		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222		0.6703472222

		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444		0.6706944444

		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667		0.6710416667

		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889		0.6713888889

		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111		0.6717361111

		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333		0.6720833333

		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556		0.6724305556

		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778		0.6727777778

		0.673125		0.673125		0.673125		0.673125		0.673125		0.673125		0.673125		0.673125		0.673125		0.673125

		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222		0.6734722222

		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444		0.6738194444

		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667		0.6741666667

		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889		0.6745138889

		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111		0.6748611111

		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333		0.6752083333

		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556		0.6755555556

		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778		0.6759027778

		0.67625		0.67625		0.67625		0.67625		0.67625		0.67625		0.67625		0.67625		0.67625		0.67625

		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222		0.6765972222

		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444		0.6769444444

		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667		0.6772916667

		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889		0.6776388889

		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111		0.6779861111

		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333		0.6783333333

		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556		0.6786805556

		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778		0.6790277778

		0.679375		0.679375		0.679375		0.679375		0.679375		0.679375		0.679375		0.679375		0.679375		0.679375

		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222		0.6797222222

		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444		0.6800694444

		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667		0.6804166667

		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889		0.6807638889

		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111		0.6811111111

		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333		0.6814583333

		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556		0.6818055556

		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778		0.6821527778

		0.6825		0.6825		0.6825		0.6825		0.6825		0.6825		0.6825		0.6825		0.6825		0.6825

		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222		0.6828472222

		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444		0.6831944444

		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667		0.6835416667

		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889		0.6838888889

		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111		0.6842361111

		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333		0.6845833333

		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556		0.6849305556

		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778		0.6852777778

		0.685625		0.685625		0.685625		0.685625		0.685625		0.685625		0.685625		0.685625		0.685625		0.685625

		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222		0.6859722222

		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444		0.6863194444

		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667		0.6866666667

		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889		0.6870138889

		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111		0.6873611111

		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333		0.6877083333

		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556		0.6880555556

		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778		0.6884027778

		0.68875		0.68875		0.68875		0.68875		0.68875		0.68875		0.68875		0.68875		0.68875		0.68875

		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222		0.6890972222

		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444		0.6894444444

		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667		0.6897916667

		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889		0.6901388889

		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111		0.6904861111

		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333		0.6908333333

		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556		0.6911805556

		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778		0.6915277778

		0.691875		0.691875		0.691875		0.691875		0.691875		0.691875		0.691875		0.691875		0.691875		0.691875

		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222		0.6922222222

		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444		0.6925694444

		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667		0.6929166667

		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889		0.6932638889

		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111		0.6936111111

		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333		0.6939583333

		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556		0.6943055556

		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778		0.6946527778

		0.695		0.695		0.695		0.695		0.695		0.695		0.695		0.695		0.695		0.695

		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222		0.6953472222

		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444		0.6956944444

		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667		0.6960416667

		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889		0.6963888889

		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111		0.6967361111

		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333		0.6970833333

		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556		0.6974305556

		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778		0.6977777778

		0.698125		0.698125		0.698125		0.698125		0.698125		0.698125		0.698125		0.698125		0.698125		0.698125

		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222		0.6984722222

		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444		0.6988194444

		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667		0.6991666667

		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889		0.6995138889

		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111		0.6998611111

		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333		0.7002083333

		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556		0.7005555556

		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778		0.7009027778

		0.70125		0.70125		0.70125		0.70125		0.70125		0.70125		0.70125		0.70125		0.70125		0.70125

		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222		0.7015972222

		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444		0.7019444444

		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667		0.7022916667

		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889		0.7026388889

		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111		0.7029861111

		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333		0.7033333333

		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556		0.7036805556

		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778		0.7040277778

		0.704375		0.704375		0.704375		0.704375		0.704375		0.704375		0.704375		0.704375		0.704375		0.704375

		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222		0.7047222222

		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444		0.7050694444

		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667		0.7054166667

		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889		0.7057638889

		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111		0.7061111111

		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333		0.7064583333

		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556		0.7068055556

		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778		0.7071527778

		0.7075		0.7075		0.7075		0.7075		0.7075		0.7075		0.7075		0.7075		0.7075		0.7075

		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222		0.7078472222

		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444		0.7081944444

		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667		0.7085416667

		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889		0.7088888889

		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111		0.7092361111

		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333		0.7095833333

		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556		0.7099305556

		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778		0.7102777778

		0.710625		0.710625		0.710625		0.710625		0.710625		0.710625		0.710625		0.710625		0.710625		0.710625

		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222		0.7109722222

		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444		0.7113194444

		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667		0.7116666667

		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889		0.7120138889

		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111		0.7123611111

		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333		0.7127083333

		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556		0.7130555556

		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778		0.7134027778

		0.71375		0.71375		0.71375		0.71375		0.71375		0.71375		0.71375		0.71375		0.71375		0.71375

		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222		0.7140972222

		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444		0.7144444444

		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667		0.7147916667

		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889		0.7151388889

		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111		0.7154861111

		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333		0.7158333333

		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556		0.7161805556

		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778		0.7165277778

		0.716875		0.716875		0.716875		0.716875		0.716875		0.716875		0.716875		0.716875		0.716875		0.716875

		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222		0.7172222222

		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444		0.7175694444

		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667		0.7179166667

		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889		0.7182638889

		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111		0.7186111111

		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333		0.7189583333

		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556		0.7193055556

		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778		0.7196527778

		0.72		0.72		0.72		0.72		0.72		0.72		0.72		0.72		0.72		0.72

		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222		0.7203472222

		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444		0.7206944444

		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667		0.7210416667

		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889		0.7213888889

		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111		0.7217361111

		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333		0.7220833333

		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556		0.7224305556

		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778		0.7227777778

		0.723125		0.723125		0.723125		0.723125		0.723125		0.723125		0.723125		0.723125		0.723125		0.723125

		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222		0.7234722222

		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444		0.7238194444

		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667		0.7241666667

		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889		0.7245138889

		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111		0.7248611111

		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333		0.7252083333

		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556		0.7255555556

		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778		0.7259027778

		0.72625		0.72625		0.72625		0.72625		0.72625		0.72625		0.72625		0.72625		0.72625		0.72625

		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222		0.7265972222

		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444		0.7269444444

		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667		0.7272916667

		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889		0.7276388889

		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111		0.7279861111

		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333		0.7283333333

		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556		0.7286805556

		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778		0.7290277778

		0.729375		0.729375		0.729375		0.729375		0.729375		0.729375		0.729375		0.729375		0.729375		0.729375

		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222		0.7297222222

		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444		0.7300694444

		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667		0.7304166667

		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889		0.7307638889

		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111		0.7311111111

		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333		0.7314583333

		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556		0.7318055556

		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778		0.7321527778

		0.7325		0.7325		0.7325		0.7325		0.7325		0.7325		0.7325		0.7325		0.7325		0.7325

		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222		0.7328472222

		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444		0.7331944444

		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667		0.7335416667

		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889		0.7338888889

		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111		0.7342361111

		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333		0.7345833333

		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556		0.7349305556

		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778		0.7352777778

		0.735625		0.735625		0.735625		0.735625		0.735625		0.735625		0.735625		0.735625		0.735625		0.735625

		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222		0.7359722222

		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444		0.7363194444

		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667		0.7366666667

		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889		0.7370138889

		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111		0.7373611111

		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333		0.7377083333

		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556		0.7380555556

		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778		0.7384027778

		0.73875		0.73875		0.73875		0.73875		0.73875		0.73875		0.73875		0.73875		0.73875		0.73875

		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222		0.7390972222

		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444		0.7394444444

		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667		0.7397916667

		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889		0.7401388889

		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111		0.7404861111

		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333		0.7408333333

		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556		0.7411805556

		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778		0.7415277778

		0.741875		0.741875		0.741875		0.741875		0.741875		0.741875		0.741875		0.741875		0.741875		0.741875

		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222		0.7422222222

		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444		0.7425694444

		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667		0.7429166667

		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889		0.7432638889

		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111		0.7436111111

		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333		0.7439583333

		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556		0.7443055556

		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778		0.7446527778

		0.745		0.745		0.745		0.745		0.745		0.745		0.745		0.745		0.745		0.745

		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222		0.7453472222

		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444		0.7456944444

		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667		0.7460416667

		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889		0.7463888889

		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111		0.7467361111

		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333		0.7470833333

		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556		0.7474305556

		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778		0.7477777778

		0.748125		0.748125		0.748125		0.748125		0.748125		0.748125		0.748125		0.748125		0.748125		0.748125

		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222		0.7484722222

		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444		0.7488194444

		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667		0.7491666667

		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889		0.7495138889

		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111		0.7498611111

		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333		0.7502083333

		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556		0.7505555556

		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778		0.7509027778

		0.75125		0.75125		0.75125		0.75125		0.75125		0.75125		0.75125		0.75125		0.75125		0.75125

		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222		0.7515972222

		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444		0.7519444444

		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667		0.7522916667

		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889		0.7526388889

		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111		0.7529861111

		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333		0.7533333333

		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556		0.7536805556

		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778		0.7540277778

		0.754375		0.754375		0.754375		0.754375		0.754375		0.754375		0.754375		0.754375		0.754375		0.754375

		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222		0.7547222222

		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444		0.7550694444

		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667		0.7554166667

		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889		0.7557638889

		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111		0.7561111111

		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333		0.7564583333

		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556		0.7568055556

		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778		0.7571527778

		0.7575		0.7575		0.7575		0.7575		0.7575		0.7575		0.7575		0.7575		0.7575		0.7575

		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222		0.7578472222

		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444		0.7581944444

		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667		0.7585416667

		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889		0.7588888889

		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111		0.7592361111

		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333		0.7595833333

		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556		0.7599305556

		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778		0.7602777778

		0.760625		0.760625		0.760625		0.760625		0.760625		0.760625		0.760625		0.760625		0.760625		0.760625

		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222		0.7609722222

		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444		0.7613194444

		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667		0.7616666667

		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889		0.7620138889

		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111		0.7623611111

		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333		0.7627083333

		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556		0.7630555556

		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778		0.7634027778

		0.76375		0.76375		0.76375		0.76375		0.76375		0.76375		0.76375		0.76375		0.76375		0.76375

		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222		0.7640972222

		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444		0.7644444444

		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667		0.7647916667

		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889		0.7651388889

		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111		0.7654861111

		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333		0.7658333333

		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556		0.7661805556

		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778		0.7665277778

		0.766875		0.766875		0.766875		0.766875		0.766875		0.766875		0.766875		0.766875		0.766875		0.766875

		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222		0.7672222222

		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444		0.7675694444

		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667		0.7679166667

		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889		0.7682638889

		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111		0.7686111111

		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333		0.7689583333

		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556		0.7693055556

		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778		0.7696527778

		0.77		0.77		0.77		0.77		0.77		0.77		0.77		0.77		0.77		0.77

		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222		0.7703472222

		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444		0.7706944444

		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667		0.7710416667

		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889		0.7713888889

		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111		0.7717361111

		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333		0.7720833333

		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556		0.7724305556

		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778		0.7727777778

		0.773125		0.773125		0.773125		0.773125		0.773125		0.773125		0.773125		0.773125		0.773125		0.773125

		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222		0.7734722222

		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444		0.7738194444

		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667		0.7741666667

		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889		0.7745138889

		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111		0.7748611111

		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333		0.7752083333

		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556		0.7755555556

		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778		0.7759027778

		0.77625		0.77625		0.77625		0.77625		0.77625		0.77625		0.77625		0.77625		0.77625		0.77625

		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222		0.7765972222

		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444		0.7769444444

		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667		0.7772916667

		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889		0.7776388889

		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111		0.7779861111

		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333		0.7783333333

		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556		0.7786805556

		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778		0.7790277778

		0.779375		0.779375		0.779375		0.779375		0.779375		0.779375		0.779375		0.779375		0.779375		0.779375

		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222		0.7797222222

		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444		0.7800694444

		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667		0.7804166667

		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889		0.7807638889

		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111		0.7811111111

		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333		0.7814583333

		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556		0.7818055556

		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778		0.7821527778

		0.7825		0.7825		0.7825		0.7825		0.7825		0.7825		0.7825		0.7825		0.7825		0.7825

		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222		0.7828472222

		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444		0.7831944444

		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667		0.7835416667

		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889		0.7838888889

		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111		0.7842361111

		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333		0.7845833333

		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556		0.7849305556

		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778		0.7852777778

		0.785625		0.785625		0.785625		0.785625		0.785625		0.785625		0.785625		0.785625		0.785625		0.785625

		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222		0.7859722222

		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444		0.7863194444

		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667		0.7866666667

		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889		0.7870138889

		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111		0.7873611111

		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333		0.7877083333

		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556		0.7880555556

		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778		0.7884027778

		0.78875		0.78875		0.78875		0.78875		0.78875		0.78875		0.78875		0.78875		0.78875		0.78875

		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222		0.7890972222

		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444		0.7894444444

		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667		0.7897916667

		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889		0.7901388889

		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111		0.7904861111

		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333		0.7908333333

		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556		0.7911805556

		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778		0.7915277778

		0.791875		0.791875		0.791875		0.791875		0.791875		0.791875		0.791875		0.791875		0.791875		0.791875

		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222		0.7922222222

		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444		0.7925694444

		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667		0.7929166667

		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889		0.7932638889

		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111		0.7936111111

		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333		0.7939583333

		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556		0.7943055556

		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778		0.7946527778

		0.795		0.795		0.795		0.795		0.795		0.795		0.795		0.795		0.795		0.795

		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222		0.7953472222

		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444		0.7956944444

		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667		0.7960416667

		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889		0.7963888889

		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111		0.7967361111

		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333		0.7970833333

		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556		0.7974305556

		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778		0.7977777778

		0.798125		0.798125		0.798125		0.798125		0.798125		0.798125		0.798125		0.798125		0.798125		0.798125

		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222		0.7984722222

		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444		0.7988194444

		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667		0.7991666667

		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889		0.7995138889

		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111		0.7998611111

		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333		0.8002083333

		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556		0.8005555556

		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778		0.8009027778

		0.80125		0.80125		0.80125		0.80125		0.80125		0.80125		0.80125		0.80125		0.80125		0.80125

		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222		0.8015972222

		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444		0.8019444444

		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667		0.8022916667

		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889		0.8026388889

		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111		0.8029861111

		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333		0.8033333333

		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556		0.8036805556

		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778		0.8040277778

		0.804375		0.804375		0.804375		0.804375		0.804375		0.804375		0.804375		0.804375		0.804375		0.804375

		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222		0.8047222222

		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444		0.8050694444

		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667		0.8054166667

		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889		0.8057638889

		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111		0.8061111111

		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333		0.8064583333

		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556		0.8068055556

		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778		0.8071527778

		0.8075		0.8075		0.8075		0.8075		0.8075		0.8075		0.8075		0.8075		0.8075		0.8075

		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222		0.8078472222

		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444		0.8081944444

		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667		0.8085416667

		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889		0.8088888889

		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111		0.8092361111

		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333		0.8095833333

		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556		0.8099305556

		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778		0.8102777778

		0.810625		0.810625		0.810625		0.810625		0.810625		0.810625		0.810625		0.810625		0.810625		0.810625

		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222		0.8109722222

		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444		0.8113194444

		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667		0.8116666667

		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889		0.8120138889

		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111		0.8123611111

		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333		0.8127083333

		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556		0.8130555556

		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778		0.8134027778

		0.81375		0.81375		0.81375		0.81375		0.81375		0.81375		0.81375		0.81375		0.81375		0.81375

		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222		0.8140972222

		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444		0.8144444444

		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667		0.8147916667

		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889		0.8151388889

		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111		0.8154861111

		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333		0.8158333333

		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556		0.8161805556

		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778		0.8165277778

		0.816875		0.816875		0.816875		0.816875		0.816875		0.816875		0.816875		0.816875		0.816875		0.816875

		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222		0.8172222222

		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444		0.8175694444

		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667		0.8179166667

		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889		0.8182638889

		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111		0.8186111111

		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333		0.8189583333

		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556		0.8193055556

		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778		0.8196527778

		0.82		0.82		0.82		0.82		0.82		0.82		0.82		0.82		0.82		0.82

		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222		0.8203472222

		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444		0.8206944444

		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667		0.8210416667

		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889		0.8213888889

		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111		0.8217361111

		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333		0.8220833333

		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556		0.8224305556

		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778		0.8227777778

		0.823125		0.823125		0.823125		0.823125		0.823125		0.823125		0.823125		0.823125		0.823125		0.823125

		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222		0.8234722222

		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444		0.8238194444

		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667		0.8241666667

		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889		0.8245138889

		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111		0.8248611111

		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333		0.8252083333

		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556		0.8255555556

		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778		0.8259027778

		0.82625		0.82625		0.82625		0.82625		0.82625		0.82625		0.82625		0.82625		0.82625		0.82625

		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222		0.8265972222

		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444		0.8269444444

		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667		0.8272916667

		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889		0.8276388889

		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111		0.8279861111

		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333		0.8283333333

		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556		0.8286805556

		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778		0.8290277778

		0.829375		0.829375		0.829375		0.829375		0.829375		0.829375		0.829375		0.829375		0.829375		0.829375

		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222		0.8297222222

		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444		0.8300694444

		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667		0.8304166667

		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889		0.8307638889

		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111		0.8311111111

		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333		0.8314583333

		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556		0.8318055556

		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778		0.8321527778

		0.8325		0.8325		0.8325		0.8325		0.8325		0.8325		0.8325		0.8325		0.8325		0.8325

		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222		0.8328472222

		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444		0.8331944444

		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667		0.8335416667

		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889		0.8338888889

		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111		0.8342361111

		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333		0.8345833333

		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556		0.8349305556

		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778		0.8352777778

		0.835625		0.835625		0.835625		0.835625		0.835625		0.835625		0.835625		0.835625		0.835625		0.835625

		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222		0.8359722222

		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444		0.8363194444

		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667		0.8366666667

		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889		0.8370138889

		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111		0.8373611111

		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333		0.8377083333

		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556		0.8380555556

		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778		0.8384027778

		0.83875		0.83875		0.83875		0.83875		0.83875		0.83875		0.83875		0.83875		0.83875		0.83875

		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222		0.8390972222

		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444		0.8394444444

		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667		0.8397916667

		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889		0.8401388889

		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111		0.8404861111

		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333		0.8408333333

		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556		0.8411805556

		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778		0.8415277778

		0.841875		0.841875		0.841875		0.841875		0.841875		0.841875		0.841875		0.841875		0.841875		0.841875

		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222		0.8422222222

		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444		0.8425694444

		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667		0.8429166667

		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889		0.8432638889

		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111		0.8436111111

		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333		0.8439583333

		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556		0.8443055556

		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778		0.8446527778

		0.845		0.845		0.845		0.845		0.845		0.845		0.845		0.845		0.845		0.845

		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222		0.8453472222

		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444		0.8456944444

		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667		0.8460416667

		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889		0.8463888889

		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111		0.8467361111

		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333		0.8470833333

		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556		0.8474305556

		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778		0.8477777778

		0.848125		0.848125		0.848125		0.848125		0.848125		0.848125		0.848125		0.848125		0.848125		0.848125

		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222		0.8484722222

		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444		0.8488194444

		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667		0.8491666667

		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889		0.8495138889

		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111		0.8498611111

		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333		0.8502083333

		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556		0.8505555556

		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778		0.8509027778

		0.85125		0.85125		0.85125		0.85125		0.85125		0.85125		0.85125		0.85125		0.85125		0.85125

		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222		0.8515972222

		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444		0.8519444444

		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667		0.8522916667

		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889		0.8526388889

		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111		0.8529861111

		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333		0.8533333333

		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556		0.8536805556

		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778		0.8540277778

		0.854375		0.854375		0.854375		0.854375		0.854375		0.854375		0.854375		0.854375		0.854375		0.854375

		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222		0.8547222222

		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444		0.8550694444

		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667		0.8554166667

		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889		0.8557638889

		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111		0.8561111111

		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333		0.8564583333

		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556		0.8568055556

		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778		0.8571527778

		0.8575		0.8575		0.8575		0.8575		0.8575		0.8575		0.8575		0.8575		0.8575		0.8575

		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222		0.8578472222

		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444		0.8581944444

		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667		0.8585416667

		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889		0.8588888889

		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111		0.8592361111

		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333		0.8595833333

		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556		0.8599305556

		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778		0.8602777778

		0.860625		0.860625		0.860625		0.860625		0.860625		0.860625		0.860625		0.860625		0.860625		0.860625

		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222		0.8609722222

		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444		0.8613194444

		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667		0.8616666667

		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889		0.8620138889

		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111		0.8623611111

		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333		0.8627083333

		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556		0.8630555556

		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778		0.8634027778

		0.86375		0.86375		0.86375		0.86375		0.86375		0.86375		0.86375		0.86375		0.86375		0.86375

		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222		0.8640972222

		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444		0.8644444444

		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667		0.8647916667

		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889		0.8651388889

		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111		0.8654861111

		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333		0.8658333333

		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556		0.8661805556

		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778		0.8665277778

		0.866875		0.866875		0.866875		0.866875		0.866875		0.866875		0.866875		0.866875		0.866875		0.866875

		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222		0.8672222222

		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444		0.8675694444

		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667		0.8679166667

		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889		0.8682638889

		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111		0.8686111111

		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333		0.8689583333

		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556		0.8693055556

		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778		0.8696527778

		0.87		0.87		0.87		0.87		0.87		0.87		0.87		0.87		0.87		0.87

		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222		0.8703472222

		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444		0.8706944444

		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667		0.8710416667

		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889		0.8713888889

		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111		0.8717361111

		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333		0.8720833333

		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556		0.8724305556

		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778		0.8727777778

		0.873125		0.873125		0.873125		0.873125		0.873125		0.873125		0.873125		0.873125		0.873125		0.873125

		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222		0.8734722222

		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444		0.8738194444

		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667		0.8741666667

		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889		0.8745138889

		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111		0.8748611111

		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333		0.8752083333

		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556		0.8755555556

		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778		0.8759027778

		0.87625		0.87625		0.87625		0.87625		0.87625		0.87625		0.87625		0.87625		0.87625		0.87625

		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222		0.8765972222

		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444		0.8769444444

		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667		0.8772916667

		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889		0.8776388889

		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111		0.8779861111

		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333		0.8783333333

		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556		0.8786805556

		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778		0.8790277778

		0.879375		0.879375		0.879375		0.879375		0.879375		0.879375		0.879375		0.879375		0.879375		0.879375

		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222		0.8797222222

		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444		0.8800694444

		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667		0.8804166667

		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889		0.8807638889

		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111		0.8811111111

		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333		0.8814583333

		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556		0.8818055556

		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778		0.8821527778

		0.8825		0.8825		0.8825		0.8825		0.8825		0.8825		0.8825		0.8825		0.8825		0.8825

		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222		0.8828472222

		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444		0.8831944444

		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667		0.8835416667

		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889		0.8838888889

		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111		0.8842361111

		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333		0.8845833333

		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556		0.8849305556

		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778		0.8852777778

		0.885625		0.885625		0.885625		0.885625		0.885625		0.885625		0.885625		0.885625		0.885625		0.885625

		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222		0.8859722222

		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444		0.8863194444

		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667		0.8866666667

		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889		0.8870138889

		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111		0.8873611111

		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333		0.8877083333

		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556		0.8880555556

		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778		0.8884027778

		0.88875		0.88875		0.88875		0.88875		0.88875		0.88875		0.88875		0.88875		0.88875		0.88875

		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222		0.8890972222

		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444		0.8894444444

		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667		0.8897916667

		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889		0.8901388889

		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111		0.8904861111

		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333		0.8908333333

		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556		0.8911805556

		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778		0.8915277778

		0.891875		0.891875		0.891875		0.891875		0.891875		0.891875		0.891875		0.891875		0.891875		0.891875

		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222		0.8922222222

		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444		0.8925694444

		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667		0.8929166667

		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889		0.8932638889

		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111		0.8936111111

		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333		0.8939583333

		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556		0.8943055556

		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778		0.8946527778

		0.895		0.895		0.895		0.895		0.895		0.895		0.895		0.895		0.895		0.895

		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222		0.8953472222

		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444		0.8956944444

		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667		0.8960416667

		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889		0.8963888889

		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111		0.8967361111

		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333		0.8970833333

		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556		0.8974305556

		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778		0.8977777778

		0.898125		0.898125		0.898125		0.898125		0.898125		0.898125		0.898125		0.898125		0.898125		0.898125

		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222		0.8984722222

		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444		0.8988194444

		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667		0.8991666667

		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889		0.8995138889

		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111		0.8998611111

		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333		0.9002083333

		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556		0.9005555556

		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778		0.9009027778

		0.90125		0.90125		0.90125		0.90125		0.90125		0.90125		0.90125		0.90125		0.90125		0.90125

		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222		0.9015972222

		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444		0.9019444444

		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667		0.9022916667

		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889		0.9026388889

		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111		0.9029861111

		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333		0.9033333333

		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556		0.9036805556

		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778		0.9040277778

		0.904375		0.904375		0.904375		0.904375		0.904375		0.904375		0.904375		0.904375		0.904375		0.904375

		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222		0.9047222222

		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444		0.9050694444

		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667		0.9054166667

		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889		0.9057638889

		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111		0.9061111111

		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333		0.9064583333

		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556		0.9068055556

		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778		0.9071527778

		0.9075		0.9075		0.9075		0.9075		0.9075		0.9075		0.9075		0.9075		0.9075		0.9075

		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222		0.9078472222

		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444		0.9081944444

		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667		0.9085416667

		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889		0.9088888889

		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111		0.9092361111

		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333		0.9095833333

		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556		0.9099305556

		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778		0.9102777778

		0.910625		0.910625		0.910625		0.910625		0.910625		0.910625		0.910625		0.910625		0.910625		0.910625

		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222		0.9109722222

		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444		0.9113194444

		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667		0.9116666667

		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889		0.9120138889

		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111		0.9123611111

		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333		0.9127083333

		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556		0.9130555556

		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778		0.9134027778

		0.91375		0.91375		0.91375		0.91375		0.91375		0.91375		0.91375		0.91375		0.91375		0.91375

		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222		0.9140972222

		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444		0.9144444444

		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667		0.9147916667

		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889		0.9151388889

		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111		0.9154861111

		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333		0.9158333333

		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556		0.9161805556

		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778		0.9165277778

		0.916875		0.916875		0.916875		0.916875		0.916875		0.916875		0.916875		0.916875		0.916875		0.916875

		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222		0.9172222222

		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444		0.9175694444

		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667		0.9179166667

		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889		0.9182638889

		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111		0.9186111111

		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333		0.9189583333

		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556		0.9193055556

		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778		0.9196527778

		0.92		0.92		0.92		0.92		0.92		0.92		0.92		0.92		0.92		0.92

		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222		0.9203472222

		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444		0.9206944444

		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667		0.9210416667

		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889		0.9213888889

		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111		0.9217361111

		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333		0.9220833333

		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556		0.9224305556

		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778		0.9227777778

		0.923125		0.923125		0.923125		0.923125		0.923125		0.923125		0.923125		0.923125		0.923125		0.923125

		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222		0.9234722222

		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444		0.9238194444

		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667		0.9241666667

		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889		0.9245138889

		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111		0.9248611111

		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333		0.9252083333

		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556		0.9255555556

		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778		0.9259027778

		0.92625		0.92625		0.92625		0.92625		0.92625		0.92625		0.92625		0.92625		0.92625		0.92625

		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222		0.9265972222

		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444		0.9269444444

		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667		0.9272916667

		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889		0.9276388889

		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111		0.9279861111

		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333		0.9283333333

		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556		0.9286805556

		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778		0.9290277778

		0.929375		0.929375		0.929375		0.929375		0.929375		0.929375		0.929375		0.929375		0.929375		0.929375

		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222		0.9297222222

		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444		0.9300694444

		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667		0.9304166667

		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889		0.9307638889

		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111		0.9311111111

		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333		0.9314583333

		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556		0.9318055556

		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778		0.9321527778

		0.9325		0.9325		0.9325		0.9325		0.9325		0.9325		0.9325		0.9325		0.9325		0.9325

		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222		0.9328472222

		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444		0.9331944444

		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667		0.9335416667

		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889		0.9338888889

		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111		0.9342361111

		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333		0.9345833333

		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556		0.9349305556

		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778		0.9352777778

		0.935625		0.935625		0.935625		0.935625		0.935625		0.935625		0.935625		0.935625		0.935625		0.935625

		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222		0.9359722222

		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444		0.9363194444

		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667		0.9366666667

		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889		0.9370138889

		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111		0.9373611111

		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333		0.9377083333

		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556		0.9380555556

		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778		0.9384027778

		0.93875		0.93875		0.93875		0.93875		0.93875		0.93875		0.93875		0.93875		0.93875		0.93875

		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222		0.9390972222

		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444		0.9394444444

		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667		0.9397916667

		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889		0.9401388889

		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111		0.9404861111

		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333		0.9408333333

		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556		0.9411805556

		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778		0.9415277778

		0.941875		0.941875		0.941875		0.941875		0.941875		0.941875		0.941875		0.941875		0.941875		0.941875

		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222		0.9422222222

		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444		0.9425694444

		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667		0.9429166667

		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889		0.9432638889

		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111		0.9436111111

		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333		0.9439583333

		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556		0.9443055556

		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778		0.9446527778

		0.945		0.945		0.945		0.945		0.945		0.945		0.945		0.945		0.945		0.945

		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222		0.9453472222

		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444		0.9456944444

		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667		0.9460416667

		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889		0.9463888889

		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111		0.9467361111

		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333		0.9470833333

		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556		0.9474305556

		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778		0.9477777778

		0.948125		0.948125		0.948125		0.948125		0.948125		0.948125		0.948125		0.948125		0.948125		0.948125

		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222		0.9484722222

		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444		0.9488194444

		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667		0.9491666667

		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889		0.9495138889

		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111		0.9498611111

		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333		0.9502083333
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