Test7- TestResultSummary.doc

Description:

· Cyclic bending test of Linksyn floats on non fish-bite protected cable.

· +/- 60 degrees, 200-5300lbs

· 235,000 bend cycles, cable rotated 90 degrees after 115,000 cycles.

Results:

· Sample broke 4.75" from nose of flanged socket at 13,500 lbs.

· Sample cut 114" from center of the pin in the crosby socket, reterminated, and re-broke.  This break occurred 96" from pin in crosby socket at 33,400lbs.
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Peak Load at Break = 13,500 lbf
Following 10 Cycles to 1,000 lbf
Specimen Broke 4-3/4" from the Nose of the Flanged Socket

Time, seconds

Tension, lbf

Specimen 2949D - 7
Tension versus Time
Cycle 1
27 July 2005
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		158.14008
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		158.73984

		158.83992

		158.94

		159.04008
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Peak Load at Break = 33,400 lbf
Following 10 Cycles to 2,500 lbf
Following Previous RBS Test and MBARI Flex Test
Specimen Broke 15.5" from the Nose of the Socket 
( 38.5" from the original Socket)

Time, seconds

Tension, lbf

Specimen 2949E - 7 
Tension versus Time
Cycle 11
11 August 2005
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