Test8- TestResultSummary.doc

Description:

· Cyclic bending test of Linksyn floats on fish-bite protected cable.

· +/- 60 degrees, 200-5300lbs

· 235,000 bend cycles, cable rotated 90 degrees after 115,000 cycles.

Results:

· Sample cut 114” from center of the pin in the Crosby socket before breaking.

· Long sample broke at 36,800lbs, 94” from center of the Crosby socket pin.

· Short sample broke at 15,300lbs, 7.5” from the nose of the flanged socket.
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		7.146252



&L




&C&14TMT Laboratories&10
&9Tension Member Technology
5721 Research Drive
Huntington Beach, CA  92649-1616
714-898-5641    Fax: 714-893-1925
www.tmtlabs.com

Peak Load at Break = 36,800 lbf
Following 10 Cycles to 1,000 lbf
Specimen broke 14" from the Nose of the Socket

Time, minutes

Tension, lbf

Specimen 2949F - #8 
Tension versus Time
Cycle 11
1 Sept 2005
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6048

6053

6061

6069

6086

6092

6108

6120

6120

6143

6156

6165

6173

6177

6187

6192

6210

6228

6234

6243

6255

6267

6270

6289

6300

6301

6324

6322

6334

6348

6369

6376

6385

6402

6413

6419

6434

6437

6451

6464

6467

6481

6487

6509

6518

6528

6538

6553

6562

6569

6585

6597

6614

6614

6620

6634

6655

6656

6672

6684

6689

6698

6706

6726

6736

6747

6757

6761

6778

6785

6798

6804

6825

6840

6842

6862

6872

6872

6880

6891

6907

6925

6928

6935

6954

6972

6975

6975

6997

7004

7007

7030

7043

7051

7054

7060

7085

7096

7099

7110

7126

7130

7142

7159

7177

7174

7183

7199

7213

7220

7225

7237

7249

7263

7275

7293

7303

7305

7320

7320

7334

7350

7362

7377

7378

7382

7409

7416

7423

7439

7445

7456

7478

7488

7494

7494

7511

7535

7538

7548

7555

7568

7581

7584

7598

7595

7615

7626

7639

7652

7661

7680

7685

7700

7708

7720

7729

7743

7749

7759

7774

7783

7793

7802

7811

7822

7845

7857

7858

7871

7872

7883

7889

7909

7920

7933

7946

7957

7966

7971

7986

8001

8003

8019

8034

8041

8058

8072

8076

8087

8098

8103

8127

8135

8142

8155

8158

8176

8188

8193

8222

8216

8231

8238

8252

8260

8271

8286

8295

8305

8307

8328

8326

8344

8360

8367

8380

8398

8403

8406

8422

8435

8446

8461

8461

8467

8486

8486

8496

8518

8528

8534

8547

8560

8568

8586

8591

8605

8611

8625

8633

8641

8667

8663

8675

8688

8696

8708

8722

8743

8735

8750

8766

8789

8794

8790

8811

8818

8820

8841

8844

8864

8873

8886

8893

8898

8918

8924

8939

8947

8950

8968

8985

8989

9006

9015

9023

9044

9043

9053

9067

9069

9093

9083

9105

9120

9123

9147

9154

9166

9167

9187

9204

9214

9218

9227

9236

9249

9270

9273

9286

9311

9299

9322

9333

9334

9349

9351

9372

9373

9390

9398

9414

9418

9431

9450

9453

9469

9474

9487

9495

9511

9521

9534

9537

9544

9560

9580

9581

9610

9611

9611

9632

9640

9640

9659

9674

9688

9685

9704

9707

9712

9730

9756

9748

9775

9785

9788

9794

9807

9820

9834

9849

9854

9856

9877

9885

9891

9902

9913

9913

9943

9957

9964

9975

9979

10000

9998

10016

10028

10035

10052

10050

10072

10067

10095

10096

10106

10123

10132

10144

10159

10162

10175

10197

10195

10207

10218

10245

10242

10251

10265

10270

10285

10299

10311

10317

10335

10339

10343

10347

10375

10393

10391

10404

10414

10422

10425

10446

10455

10462

10472

10488

10491

10513

10526

10537

10547

10555

10562

10581

10592

10603

10608

10625

10629

10642

10663

10669

10661

10687

10696

10710

10719

10725

10725

10743

10753

10768

10783

10791

10806

10814

10829

10839

10848

10848

10872

10875

10877

10903

10899

10918

10929

10947

10954

10957

10972

10982

10996

11002

11008

11028

11040

11053

11058

11079

11084

11091

11109

11127

11135

11136

11139

11148

11158

11179

11201

11200

11203

11219

11228

11236

11256

11261

11274

11287

11303

11307

11319

11326

11338

11359

11360

11371

11388

11393

11406

11415

11439

11442

11451

11461

11473

11483

11496

11504

11511

11525

11531

11548

11557

11574

11583

11584

11607

11610

11599

11632

11636

11654

11658

11673

11677

11688

11702

11723

11728

11740

11754

11757

11770

11787

11796

11803

11814

11825

11836

11849

11856

11873

11891

11896

11907

11909

11926

11945

11942

11950

11963

11986

11976

12010

12018

12021

12024

12048

12064

12070

12076

12086

12107

12109

12131

12140

12144

12152

12153

12186

12191

12196

12209

12233

12227

12253

12263

12256

12285

12292

12301

12308

12308

12317

12340

12354

12353

12376

12379

12392

12403

12412

12430

12432

12447

12447

12463

12487

12498

12492

12510

12516

12534

12537

12553

12562

12578

12582

12594

12608

12616

12629

12643

12646

12657

12672

12688

12693

12711

12721

12727

12746

12753

12767

12771

12777

12791

12805

12819

12833

12839

12856

12863

12870

12877

12888

12905

12909

12918

12929

12943

12959

12962

12978

12988

13004

13010

13025

13022

13044

13067

13070

13078

13087

13093

13108

13114

13129

13142

13155

13163

13172

13185

13202

13205

13226

13238

13242

13256

13258

13273

13288

13288

13301

13308

13330

13326

13349

13358

13358

13370

13386

13400

13405

13435

13439

13458

13461

13472

13483

13489

13498

13519

13526

13533

13537

13562

13565

13567

13586

13595

13610

13620

13634

13647

13652

13663

13674

13690

13688

13710

13717

13728

13746

13755

13759

13775

13771

13791

13802

13809

13821

13836

13852

13861

13864

13874

13892

13900

13915

13927

13930

13951

13959

13971

13975

13990

14003

14010

14016

14035

14051

14058

14077

14083

14087

14106

14123

14126

14133

14130

14148

14161

14168

14194

14186

14215

14218

14219

14245

14247

14257

14273

14267

14296

14306

14316

14329

14337

14348

14362

14370

14379

14396

14403

14424

14432

14444

14445

14451

14474

14485

14501

14507

14509

14520

14529

14545

14567

14570

14581

14577

14595

14609

14630

14625

14642

14651

14667

14673

14679

14698

14709

14724

14718

14743

14752

14752

14764

14786

14797

14805

14811

14820

14842

14857

14857

14879

14895

14907

14908

14917

14931

14937

14948

14955

14970

14992

14997

14999

15019

15028

15028

15051

15062

15065

15073

15078

15093

15118

15133

15134

15140

15152

15163

15182

15184

15205

15209

15221

15235

15235

15244

15261

15269

15282

15301

15308

15318

15335

15338

15344

15361

15372

15373

15389

15408

15414

15432

15426

15442

15456

15465

15485

15489

15498

15511

15521

15530

15543

15548

15566

15565

15588

15592

15605

15624

15643

15637

15649

15650

15672

15686

15695

15706

15727

15731

15743

15751

15762

15773

15791

15801

15803

15813

15817

15838

15842

15862

15867

15875

15888

15909

15916

15933

15931

15944

15956

15971

15971

15988

15998

16005

16016

16033

16036

16046

16069

16088

16077

16092

16117

16123

16127

16149

16153

16155

16165

16175

16201

16209

16126

16217

16248

16246

16256

16271

16285

16303

16304

16313

16322

16344

16350

16348

16374

16374

16391

16402

16404

16426

16440

16442

16462

16464

16477

16492

16487

16487

16502

16526

16530

16499

16549

16578

16579

16485

16550

16601

16633

16642

16643

16663

16680

16694

16694

16708

16721

16727

16742

16753

16763

16773

16787

16800

16808

16821

16826

16840

16853

16860

16864

16874

16875

16905

16918

16928

16937

16955

16963

16971

16981

16993

17003

17016

17022

17037

17043

17053

17070

17084

17094

17110

17118

17109

17119

17136

17160

17162

17176

17194

17195

17203

17219

17237

17235

17256

17267

17274

17275

17287

17300

17318

17328

17331

17341

17351

17372

17396

17391

17403

17419

17418

17436

17448

17455

17478

17480

17496

17499

17510

17515

17544

17544

17548

17570

17583

17581

17601

17595

17612

17630

17638

17644

17667

17679

17680

17705

17707

17715

17732

17741

17744

17761

17766

17776

17788

17802

17822

17831

17841

17839

17858

17876

17883

17884

17897

17898

17924

17937

17957

17963

17964

17978

17994

18002

18012

18014

18025

18033

18050

18067

18070

18082

18096

18099

18131

18118

18137

18143

18160

18173

18176

18194

18195

18214

18237

17931

18194

18250

18261

18264

18297

18302

18311

18293

18311

18333

18366

18373

18374

18385

18389

18401

18359

18417

18426

18448

18460

18471

18484

18498

18269

18481

18478

18526

18552

18567

18570

18575

18587

18605

18617

18631

18639

18660

18655

18671

18672

18695

18701

18725

18724

18733

18733

18766

18779

18785

18782

18801

18814

18817

18832

18854

18862

18869

18876

18856

18898

18912

18907

18931

18946

18953

18959

18978

18982

18995

19007

19027

19027

19036

19054

19046

19036

19078

19088

19099

19113

19130

19110

19155

19166

19178

19183

19192

19199

19197

19226

19239

19235

19252

19260

19269

19295

19307

19310

19320

19338

19344

19353

19375

19370

19388

19397

19417

19426

19431

19449

19446

19456

19468

19478

19495

19506

19523

19525

19542

19547

19575

19570

19575

19594

19606

19616

19623

19633

19644

19653

19661

19671

19688

19691

19710

19728

19732

19742

19754

19765

19783

19789

19794

19810

19816

19835

19845

19845

19857

19876

19871

19889

19904

19919

19931

19939

19961

19947

19970

19984

19999

19998

20017

20023

20039

20044

20062

20068

20052

20080

20101

20112

20119

20136

20143

20153

20158

20168

20182

20199

20197

20216

20231

20229

20244

20254

20262

20283

20284

20306

20312

20328

20338

20344

20371

20368

20376

20380

20399

20413

20424

20432

20442

20451

20468

20467

20489

20502

20512

20525

20528

20539

20548

20556

20570

20582

20593

20605

20616

20627

20628

20651

20665

20673

20684

20690

20700

20723

20728

20722

20725

20747

20776

20773

20780

20792

20815

20825

20834

20842

20851

20861

20862

20885

20889

20899

20919

20921

20932

20945

20962

20973

20984

20995

20997

21018

21029

21034

20731

21035

21054

21089

21104

21102

21112

21129

21144

21155

21157

21163

21186

21191

21207

21221

21224

21240

21250

21261

21270

21284

21291

21299

21318

21326

21339

21348

21358

21369

21377

21384

21398

21408

21409

21433

21447

21450

21447

21473

21486

21485

21501

21512

21516

21535

21563

21551

21566

21577

21588

21599

21608

21621

21633

21630

21662

21669

21678

21694

21698

21701

21716

21726

21746

21758

21766

21778

21792

21799

21801

21811

21832

21857

21862

21855

21865

21879

21898

21899

21909

21917

21942

21946

21957

21968

21976

21989

22001

22012

22030

22030

22041

22050

22062

22075

22096

22094

22105

22115

22128

22146

22157

22159

22172

22183

22188

22194

22214

22226

22238

22248

22271

22271

22274

22286

22297

22312

22323

22345

22346

22355

22352

22382

22394

22401

22415

22430

22436

22439

22459

22466

22469

22494

22509

22500

22523

22530

22546

22544

22559

22562

22583

22593

22616

22625

22621

22636

22660

22662

22660

22687

22688

22696

22717

22720

22736

22754

22766

22758

22784

22792

22794

22811

22829

22839

22831

22858

22860

22887

22884

22894

22909

22922

22935

22943

22951

22960

22978

22992

23000

23003

23025

23030

23034

23046

23067

23079

23086

23095

23099

23112

23134

23126

23142

23158

23174

23174

23196

23200

23209

23210

23225

23235

23261

23265

23279

23281

23300

23326

23322

23331

23340

23349

23367

23374

23387

23400

23407

23426

23429

23443

23446

23464

23475

23487

23493

23511

23529

23524

23539

23555

23566

23558

23581

23587

23610

23615

23619

23633

23639

23664

23661

23684

23688

23703

23718

23735

23741

23743

23754

23766

23767

23785

23799

23805

23815

23831

23851

23853

23858

23880

23883

23887

23900

23918

23931

23925

23940

23954

23973

23970

23987

23997

24005

24023

24038

24044

24066

24070

24076

24083

24103

24112

24132

24133

24145

24154

24164

24169

24182

24192

24199

24221

24224

24238

24253

24257

24269

23638

24191

24296

24303

24325

24354

24353

24363

24373

24392

24398

24405

24416

24428

24439

24445

24463

24463

24478

24490

24502

24522

24536

24531

24543

24561

24578

24569

24592

24609

24630

24622

24629

24643

24659

24666

24677

24677

24705

24706

24723

24731

24752

24747

24766

24772

24785

24791

24812

24816

24830

24843

24856

24853

24869

24875

24894

24907

24885

24923

24935

24941

24954

24969

24985

24998

25000

25014

25018

25036

25037

25049

25068

25074

25094

25103

25114

25125

25131

25148

25147

25170

25182

25190

25196

25200

25217

25230

25243

25250

25264

25272

25280

25284

25306

25310

25329

25346

25346

25338

25375

25379

25391

25415

25407

25430

25434

25442

25454

25463

25478

25487

25508

25514

25530

25532

25543

25544

25570

25585

25584

25591

25611

25621

25624

25646

25660

25656

25676

25687

25697

25704

25717

25727

25733

25742

25770

25762

25782

25794

25809

25813

25820

25821

25841

25861

25868

25880

25887

25900

25914

25923

25930

25936

25961

25969

25978

25984

25998

26011

26017

26030

26042

26049

26070

26075

26087

26094

26110

26116

26126

26136

26048

26146

26166

26183

26190

26202

26232

26229

26232

26242

26249

26267

26277

26296

26306

26313

26308

26339

26355

26365

26375

26383

26381

26400

26411

26425

26438

26445

26452

26458

26474

26479

26497

26496

26521

26530

26544

26547

26557

26574

26587

26603

26605

26610

26628

26637

26644

26652

26667

26691

26687

26700

26714

26722

26743

26739

26760

26770

26774

26789

26804

26815

26821

26828

26844

26853

26867

26874

26880

26901

26901

26925

26931

26947

26948

26964

26974

26981

26997

27004

27003

27038

27041

27050

27051

27063

27071

27095

27104

27113

27131

27121

27140

27166

27176

27179

27192

27187

27210

27226

27233

27247

27247

27272

27275

27296

27295

27310

27321

27324

27333

27353

27362

27360

27388

27382

27397

27421

27432

27439

27453

27462

27479

27480

27490

27497

27515

27528

27535

27548

27545

27555

27563

27589

27600

27611

27631

27636

27644

27653

27666

27679

27693

27695

27706

27721

27734

27740

27753

27758

27782

27782

27785

27807

27810

27832

27830

27863

27872

27867

27875

27885

27901

27903

27930

27928

27943

27950

27979

27977

27990

27988

28008

28026

28037

28056

28049

28062

28058

28088

28086

28109

28122

28124

28133

28146

28159

28169

28178

28201

28203

28217

28225

28240

28246

28263

28267

28276

28298

28293

28311

28330

28336

28356

28359

28372

28377

28388

28389

28407

28422

28437

28442

28455

28470

28472

28483

28501

28499

28522

28531

28546

28544

28565

28576

28587

28602

28613

28617

28622

28646

28648

28655

28675

28668

28682

28701

28700

28723

28733

28752

28749

28766

28778

28793

28800

28816

28840

28830

28843

28856

28868

28877

28896

28887

28909

28920

28925

28936

28945

28957

28960

28989

28995

29006

29013

29023

29032

29053

29042

29073

29079

29080

29097

29105

29119

29125

29148

29160

29168

29174

29184

29196

29215

29228

29234

29244

29254

29274

29274

29286

29306

29309

29330

29329

29342

29349

29367

29389

29380

29393

29416

29409

29428

29448

29452

29458

29466

29472

29490

29497

29519

29513

29537

29544

29548

29570

29576

29587

29594

29612

29639

29632

29648

29664

29669

29668

29683

29693

29706

29713

29729

29739

29759

29765

29782

29794

29801

29802

29812

29827

29842

29838

29858

29870

29891

29883

29907

29909

29935

29931

29938

29950

29965

29983

30007

30000

30012

30028

30038

30041

30053

30063

30076

30075

30092

30117

30117

30140

30140

30154

30170

30173

30179

30198

30213

30219

30237

30239

30241

30269

30278

30283

30292

30312

30322

30336

30327

30344

30360

30370

30373

30396

30401

30414

30424

30433

30438

30456

30465

30486

30492

30512

30518

30531

30531

30546

30558

30569

30585

30587

30589

30605

30619

30621

30637

30660

30657

30672

30692

30707

30702

30724

30726

30737

30754

30772

30783

30789

30798

30815

30816

30814

30830

30844

30861

30871

30885

30905

30900

30899

30924

30938

30951

30963

30975

30985

30989

31001

31017

31024

31042

31040

31052

31059

31082

31085

31100

31115

31116

31129

31146

31159

31163

31180

31191

31188

31198

31227

31232

31246

31246

31255

31265

31274

31301

31311

31323

31332

31346

31361

31365

31376

31382

31388

31419

31414

31427

31446

31446

31464

31462

31475

31493

31503

31509

31521

31539

31545

31546

31572

31581

31594

31608

31617

31613

31630

31642

31659

31662

31683

31683

31692

31703

31726

31726

31739

31748

31758

31775

31781

31800

31813

31815

31839

31842

31852

31865

31876

31885

31891

31913

31910

31920

31940

31944

31965

31968

31972

31983

31988

32010

32033

32042

32048

32052

32071

32058

32081

32111

32100

32121

32126

32147

32153

30216

31691

32132

32181

32224

32246

32235

32241

32260

32271

32273

32295

32297

32317

32322

32335

32348

32351

32371

32379

32391

32403

32418

32429

32438

32434

32449

32470

32476

32490

32502

32512

32521

32532

32548

32559

32561

32577

32577

32603

32596

32612

32628

32645

32654

32661

32680

32681

32687

32707

32712

32728

32746

32748

32759

32771

32784

32796

32792

32815

32826

32840

32845

32859

32872

32874

32886

32898

32912

32926

32935

32955

32951

32961

32988

32950

32992

33002

33022

33022

33039

33051

33060

33077

33090

33097

33107

33119

33131

33125

33152

33165

33166

33197

33189

33191

33217

33228

33240

33246

33257

33262

33281

33292

33293

33307

33318

33323

33335

33352

33345

33376

33370

33395

33428

33421

33424

33441

33447

33457

33470

33477

33491

33494

33515

33524

33540

33540

33550

33564

33575

33592

33592

33611

33627

33627

33638

33647

33660

33677

33689

33688

33705

33716

33728

33734

33743

33750

33763

33782

33798

33800

33819

33833

33824

33855

33853

33864

33873

33884

33902

33904

33920

33920

33944

33950

33973

33981

33989

33997

34011

34016

34027

34037

34042

34061

34071

34081

34096

34111

34124

34120

34128

34132

34146

34168

34182

34192

34200

34218

34221

34233

34257

34256

34271

34275

34278

34292

34307

34310

34327

34340

34366

34359

34375

34372

34385

34397

34404

34423

34429

34436

34447

34456

34471

34482

34503

34505

34522

34531

34545

34552

34569

34578

34588

34596

34594

34613

34630

34626

34649

34655

34677

34675

34687

34696

34709

34715

34734

34744

34757

34768

34778

34792

34787

34806

34818

34823

34839

34860

34862

34876

34887

34887

34904

34913

34934

34939

34949

34955

34975

34975

34984

35003

35015

35013

35032

35047

35051

35059

35071

35074

35101

35107

35121

35124

35129

35142

35157

35172

35172

35185

35204

35208

35218

35219

35236

35248

35262

35277

35288

35300

35308

35324

35331

35335

35349

35360

35382

35383

35402

35410

35423

35427

35433

35451

35464

35475

35483

35498

35500

35521

35515

35538

35540

35548

35580

35581

35594

35606

35616

35619

35635

35640

35650

35670

35676

35692

35700

35707

35722

35724

35741

35747

35765

35775

35783

35794

35808

35819

35825

35838

35844

35855

35865

35883

35899

35904

35919

35938

35935

35952

35957

35966

35973

35989

35997

36014

36018

36035

36048

36057

36073

36076

36093

36102

36109

36128

36134

36140

36159

36164

36180

36190

36196

36203

36231

36240

36238

36257

36266

36271

36279

36287

36302

36324

36326

36340

36350

36363

36373

36373

36386

36399

36418

36416

36435

36445

36457

36470

36485

36489

36505

36508

36520

36530

36551

36563

36553

36577

36587

36603

36611

36614

36629

36645

36657

36668

36676

36675

36688

36707

36721

36723

36742

32603

34262

35956

36630

36750

36799

36827

36837

36829

30968

14106

5180

7411

2837

3295

2967

2817

2528

3372

3219

2576

3739

2979

2556

3444

2688

3872

2987

2703

3343

2737

2640

2507

2428

2467

2556

2652

3092

2580

2596

2415

2815

1699

1131

794

566

402

292

234

177

157

143

125

102

93

91

85

85

78

70

75

68

69

67

60

60

60

54

57

53

52

52

47

48

50

45

47

43

42

42

45

47

53

59

70

79

91

97

105

119

130

135

153

163

176

182

195

198

199

203

204

208

222

234

244

258

268

278

288

295

309

324

330

340

353

368

375

383

395

405

418

427

437

446

458

468

480

496

508

516

524

536

546

556

564

574

585

604

612

625

635

643

656

661

675

682

693

706

717

736

741

757

762

773

775

789

801

817

827

844

856

862

874

882

893

903

922

926

942

951

955

967

979

991

1004

1012

1021

1033

1043

1058

1068

1082

1090

1098

1110

1122

1136

1146

1155

1165

1177

1187

1197

1210

1220

1233

1239

1253

1262

1271

1284

1295

1313

1326

1334

1345

1355

1365

1375

1385

1396

1407

1414

1425

1437

1452

1464

1471

1479

1490

1502

1516

1524

1530

1545

1555

1573

1579

1600

1603

1614

1619

1635

1647

1657

1664

1671

1691

1700

1709

1717

1730

1741

1755

1767

1775

1784

1794

1804

1820

1826

1838

1849

1864

1878

1888

1893

1907

1906

1926

1939

1951

1965

1967

1985

1994

2009

2015

2033

2035

2051

2061

2070

2080

2090

2096

2106

2120

2133

2140

2152

2157

2169

2183

2196

2208

2215

2225

2244

2246

2258

2273

2280

2296

2309

2313

2328

2331

2352

2360

2370

2380

2388

2402

2410

2418

2436

2446

2456

2466

2477

2489

2502

2515

2517

2526

2538

2550

2563

2578

2580

2596

2605

2612

2622

2638

2647

2652

2663

2676

2689

2697

2706

2718

2737

2744

2757

2767

2783

2795

2804

2810

2820

2828

2841

2852

2868

2878

2890

2898

2907

2920

2931

2932

2940

2956

2965

2976

3000

3001

3016

3027

3034

3040

3053

3058

3079

3090

3099

3098

3113

3131

3151

3154

3163

3179

3191

3201

3204

3214

3226

3237

3247

3255

3269

3280

3286

3298

3308

3314

3324

3343

3356

3368

3381

3388

3406

3404

3421

3432

3443

3449

3459

3468

3481

3489

3505

3519

3525

3530

3540

3553

3569

3577

3585

3600

3612

3621

3637

3646

3656

3665

3672

3683

3704

3704

3717

3727

3746

3756

3763

3773

3786

3801

3810

3822

3828

3834

3843

3862

3867

3879

3887

3904

3920

3931

3936

3949

3959

3966

3971

3981

4000

4007

4020

4033

4038

4052

4058

4077

4084

4089

4099

4115

4123

4127

4145

4152

4171

4187

4198

4208

4220

4221

4233

4244

4262

4268

4279

4290

4297

4310

4326

4333

4343

4345

4366

4371

4384

4388

4410

4423

4422

4434

4443

4454

4468

4484

4487

4504

4515

4528

4539

4561

4561

4574

4590

4584

4610

4620

4629

4636

4642

4655

4667

4685

4694

4703

4713

4716

4725

4740

4755

4762

4772

4782

4790

4810

4819

4829

4834

4851

4858

4866

4880

4892

4903

4915

4925

4938

4951

4955

4969

4983

4998

5003

5013

5023

5032

5044

5055

5064

5078

5088

5101

5106

5125

5134

5145

5153

5166

5172

5186

5203

5215

5223

5234

5235

5244

5266

5276

5294

5296

5306

5318

5333

5348

5345

5360

5371

5383

5403

2634

2480

2257

2363

2167

2887

2316

2365

2747

2440

2604

2237

2747

2600

2456

2381

2827

2478

2586

2505

3059

2365

2770

2433

3057

2269

2336

2747

2136

2661

3041

2246

2772

2126

2515

3035

2096

2532

2348

2365

2302

2113

2528

2080

2559

3015

2201

2644

2032

2395

2655

2205

2796

2177

2750

2152

2080

2518

2022

2043

2467

2703

2161

2650

2052

2493

2942

2046

2481

2005

2421

2268

2232

2722

2282

2212

2027

2315

2040

2476

2070

2573

2077

2542

1961

2389

1942

2351

2826

1907

2308

1872

2212

2608

3034

1795

2132

2548

2286

1966

2417

2793

1909

2054

2267

2030

1822

2247

2677

1845

2231

2610

3091

1796

2197

2605

1810

1998

2438

1880

2254

1986

1843

2101

2493

2924

1916

2322

1856

2103

2502

1826

2122

2520

2940

1858

2259

1946

2360

2411

2020

2412

2283

2035

2500

1875

2236

2575

1977

2371

2808

1941

2345

2736

2449

1948

2330

1755

1780

2035

2450

2818

1741

2133

1757

2096

2459

1745

1968

1727

2051

1697

2038

2481

1835

2212

2550

1729

2098

2501

1919

2284

1742

2070

1987

1916

2083

1945

2342

1747

2062

2440

2834

1816

2269

1842

2191

2614

1760

2103

1870

2032

1847

2289

2003

2336

2701

2056

2032

2363

2782

1793

2174

1774

2088

2318

1916

2314

1880

2256

1771

2058

1765

2078

2424

2781

1841

2206

2622

1732

2044

2437

2027

1941

1945

1504

1184

944

752

611

491

386

311

249

207

182

166

145

132

126

115

108

98

91

86

85

79

75

72

69

68

68

64

60

60

56

55

54

56

55

48

46

44

45

44

41

40

40

41

38

42

37

37

35

36

38

37

34

34

34

36

34

36

31

30

31



T vs t #8flanged

		0.004266

		0.005886

		0.007548

		0.009216

		0.010884

		0.012552

		0.014214

		0.015882

		0.01755

		0.019218

		0.020886

		0.022548

		0.024216

		0.025884

		0.027552

		0.029214

		0.030882

		0.03255

		0.034218

		0.035886

		0.037548

		0.039216

		0.040884

		0.042552

		0.044214

		0.045882

		0.04755

		0.049218

		0.050886

		0.052548

		0.054216

		0.055884

		0.057552

		0.059214

		0.060882

		0.06255

		0.064218

		0.065886

		0.067548

		0.069216

		0.070884

		0.072552

		0.074214

		0.075882

		0.07755

		0.079218

		0.080886

		0.082548

		0.084216

		0.085884

		0.087552

		0.089214

		0.090882

		0.09255

		0.094218

		0.095886

		0.097548

		0.099216

		0.100884

		0.102552

		0.104214

		0.105882

		0.10755

		0.109218

		0.110886

		0.112548

		0.114216

		0.115884

		0.117552

		0.119214

		0.120882

		0.12255

		0.124218

		0.125886

		0.127548

		0.129216

		0.130884

		0.132552

		0.134214

		0.135882

		0.13755

		0.139218

		0.140886

		0.142548

		0.144216

		0.145884

		0.147552

		0.149214

		0.150882

		0.15255

		0.154218

		0.155886

		0.157548

		0.159216

		0.160884

		0.162552

		0.164214

		0.165882

		0.16755

		0.169218

		0.170886

		0.172548

		0.174216

		0.175884

		0.177552

		0.179214

		0.180882

		0.18255

		0.184218

		0.185886

		0.187548

		0.189216

		0.190884

		0.192552

		0.194214

		0.195882

		0.19755

		0.199218

		0.200886

		0.202548

		0.204216

		0.205884

		0.207552

		0.209214

		0.210882

		0.21255

		0.214218

		0.215886

		0.217548

		0.219216

		0.220884

		0.222552

		0.224214

		0.225882

		0.22755

		0.229218

		0.230886

		0.232548

		0.234216

		0.235884

		0.237552

		0.239214

		0.240882

		0.24255

		0.244218

		0.245886

		0.247548

		0.249216

		0.250884

		0.252552

		0.254214

		0.255882

		0.25755

		0.259218

		0.260886

		0.262548

		0.264216

		0.265884

		0.267552

		0.269214

		0.270882

		0.27255

		0.274218

		0.275886

		0.277548

		0.279216

		0.280884

		0.282552

		0.284214

		0.285882

		0.28755

		0.289218

		0.290886

		0.292548

		0.294216

		0.295884

		0.297552

		0.299214

		0.300882

		0.30255

		0.304218

		0.305886

		0.307548

		0.309216

		0.310884

		0.312552

		0.314214

		0.315882
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		2.35755

		2.359218

		2.360886

		2.362548

		2.364216

		2.365884

		2.367552

		2.369214

		2.370882

		2.37255

		2.374218

		2.375886

		2.377548

		2.379216

		2.380884

		2.382552

		2.384214

		2.385882

		2.38755

		2.389218

		2.390886

		2.392548

		2.394216

		2.395884

		2.397552

		2.399214

		2.400882

		2.40255

		2.404218

		2.405886

		2.407548

		2.409216

		2.410884

		2.412552

		2.414214

		2.415882

		2.41755

		2.419218

		2.420886

		2.422548

		2.424216

		2.425884

		2.427552

		2.429214

		2.430882

		2.43255

		2.434218

		2.435886

		2.437548

		2.439216

		2.440884

		2.442552

		2.444214

		2.445882

		2.44755

		2.449218

		2.450886

		2.452548

		2.454216

		2.455884

		2.457552

		2.459214

		2.460882

		2.46255

		2.464218

		2.465886

		2.467548

		2.469216

		2.470884

		2.472552

		2.474214

		2.475882

		2.47755

		2.479218

		2.480886

		2.482548

		2.484216

		2.485884

		2.487552

		2.489214

		2.490882

		2.49255

		2.494218

		2.495886

		2.497548

		2.499216

		2.500884

		2.502552

		2.504214

		2.505882

		2.50755

		2.509218

		2.510886

		2.512548

		2.514216

		2.515884

		2.517552

		2.519214

		2.520882

		2.52255

		2.524218

		2.525886

		2.527548

		2.529216

		2.530884

		2.532552

		2.534214

		2.535882

		2.53755

		2.539218

		2.540886

		2.542548

		2.544216

		2.545884

		2.547552

		2.549214

		2.550882

		2.55255

		2.554218

		2.555886

		2.557548

		2.559216

		2.560884

		2.562552

		2.564214

		2.565882

		2.56755

		2.569218

		2.570886

		2.572548

		2.574216

		2.575884

		2.577552

		2.579214

		2.580882

		2.58255

		2.584218

		2.585886

		2.587548

		2.589216

		2.590884

		2.592552

		2.594214

		2.595882

		2.59755

		2.599218

		2.600886

		2.602548

		2.604216

		2.605884

		2.607552

		2.609214

		2.610882

		2.61255

		2.614218

		2.615886

		2.617548

		2.619216

		2.620884

		2.622552

		2.624214

		2.625882

		2.62755

		2.629218

		2.630886

		2.632548

		2.634216

		2.635884

		2.637552

		2.639214

		2.640882

		2.64255

		2.644218

		2.645886

		2.647548

		2.649216

		2.650884

		2.652552

		2.654214

		2.655882

		2.65755

		2.659218

		2.660886

		2.662548

		2.664216

		2.665884

		2.667552

		2.669214

		2.670882

		2.67255

		2.674218

		2.675886

		2.677548

		2.679216

		2.680884

		2.682552

		2.684214

		2.685882

		2.68755

		2.689218

		2.690886

		2.692548

		2.694216

		2.695884

		2.697552

		2.699214

		2.700882

		2.70255

		2.704218

		2.705886

		2.707548

		2.709216

		2.710884

		2.712552

		2.714214

		2.715882

		2.71755

		2.719218

		2.720886

		2.722548

		2.724216

		2.725884

		2.727552

		2.729214

		2.730882

		2.73255

		2.734218

		2.735886

		2.737548

		2.739216

		2.740884

		2.742552

		2.744214

		2.745882

		2.74755

		2.749218

		2.750886

		2.752548

		2.754216

		2.755884

		2.757552

		2.759214

		2.760882

		2.76255

		2.764218

		2.765886

		2.767548

		2.769216

		2.770884

		2.772552

		2.774214

		2.775882

		2.77755

		2.779218

		2.780886

		2.782548

		2.784216

		2.785884

		2.787552

		2.789214

		2.790882

		2.79255

		2.794218

		2.795886

		2.797548

		2.799216

		2.800884

		2.802552

		2.804214

		2.805882

		2.80755

		2.809218

		2.810886

		2.812548

		2.814216

		2.815884

		2.817552

		2.819214

		2.820882

		2.82255

		2.824218

		2.825886

		2.827548

		2.829216

		2.830884

		2.832552

		2.834214

		2.835882

		2.83755

		2.839218

		2.840886

		2.842548

		2.844216

		2.845884

		2.847552

		2.849214

		2.850882

		2.85255

		2.854218

		2.855886

		2.857548

		2.859216

		2.860884

		2.862552

		2.864214

		2.865882

		2.86755

		2.869218

		2.870886

		2.872548

		2.874216

		2.875884

		2.877552

		2.879214

		2.880882

		2.88255

		2.884218

		2.885886

		2.887548

		2.889216

		2.890884

		2.892552

		2.894214

		2.895882

		2.89755

		2.899218

		2.900886

		2.902548

		2.904216

		2.905884

		2.907552

		2.909214

		2.910882

		2.91255

		2.914218

		2.915886

		2.917548

		2.919216

		2.920884

		2.922552

		2.924214

		2.925882

		2.92755

		2.929218

		2.930886

		2.932548

		2.934216

		2.935884

		2.937552

		2.939214

		2.940882

		2.94255

		2.944218

		2.945886

		2.947548

		2.949216

		2.950884

		2.952552

		2.954214

		2.955882

		2.95755

		2.959218

		2.960886

		2.962548

		2.964216

		2.965884

		2.967552

		2.969214

		2.970882

		2.97255

		2.974218

		2.975886

		2.977548

		2.979216

		2.980884

		2.982552

		2.984214

		2.985882

		2.98755

		2.989218

		2.990886

		2.992548

		2.994216

		2.995884

		2.997552

		2.999214

		3.000882

		3.00255

		3.004218

		3.005886

		3.007548

		3.009216

		3.010884

		3.012552

		3.014214

		3.015882

		3.01755

		3.019218

		3.020886

		3.022548

		3.024216

		3.025884

		3.027552

		3.029214

		3.030882

		3.03255

		3.034218

		3.035886

		3.037548

		3.039216

		3.040884

		3.042552

		3.044214

		3.045882

		3.04755

		3.049218

		3.050886

		3.052548

		3.054216

		3.055884

		3.057552

		3.059214

		3.060882

		3.06255

		3.064218

		3.065886

		3.067548

		3.069216

		3.070884

		3.072552

		3.074214

		3.075882

		3.07755

		3.079218

		3.080886

		3.082548

		3.084216

		3.085884

		3.087552

		3.089214

		3.090882

		3.09255

		3.094218

		3.095886

		3.097548

		3.099216

		3.100884

		3.102552

		3.104214

		3.105882

		3.10755

		3.109218

		3.110886

		3.112548

		3.114216

		3.115884

		3.117552

		3.119214

		3.120882

		3.12255

		3.124218

		3.125886

		3.127548

		3.129216

		3.130884

		3.132552

		3.134214

		3.135882

		3.13755

		3.139218

		3.140886

		3.142548

		3.144216

		3.145884

		3.147552

		3.149214

		3.150882

		3.15255

		3.154218

		3.155886

		3.157548

		3.159216

		3.160884

		3.162552

		3.164214

		3.165882

		3.16755

		3.169218

		3.170886

		3.172548

		3.174216

		3.175884

		3.177552

		3.179214

		3.180882

		3.18255

		3.184218

		3.185886

		3.187548

		3.189216

		3.190884

		3.192552

		3.194214

		3.195882

		3.19755

		3.199218

		3.200886

		3.202548

		3.204216

		3.205884

		3.207552

		3.209214

		3.210882

		3.21255

		3.214218

		3.215886

		3.217548

		3.219216

		3.220884

		3.222552

		3.224214

		3.225882

		3.22755

		3.229218

		3.230886

		3.232548

		3.234216

		3.235884

		3.237552

		3.239214

		3.240882

		3.24255

		3.244218

		3.245886

		3.247548

		3.249216

		3.250884

		3.252552

		3.254214

		3.255882

		3.25755

		3.259218

		3.260886

		3.262548

		3.264216

		3.265884

		3.267552

		3.269214

		3.270882

		3.27255

		3.274218

		3.275886

		3.277548

		3.279216

		3.280884

		3.282552

		3.284214

		3.285882

		3.28755

		3.289218

		3.290886

		3.292548

		3.294216

		3.295884

		3.297552

		3.299214

		3.300882

		3.30255

		3.304218

		3.305886

		3.307548

		3.309216

		3.310884

		3.312552

		3.314214

		3.315882

		3.31755

		3.319218

		3.320886

		3.322548

		3.324216

		3.325884

		3.327552

		3.329214

		3.330882

		3.33255

		3.334218

		3.335886

		3.337548

		3.339216

		3.340884

		3.342552

		3.344214

		3.345882

		3.34755

		3.349218

		3.350886

		3.352548

		3.354216

		3.355884

		3.357552

		3.359214

		3.360882

		3.36255

		3.364218

		3.365886

		3.367548

		3.369216

		3.370884

		3.372552

		3.374214

		3.375882

		3.37755

		3.379218

		3.380886

		3.382548

		3.384216

		3.385884

		3.387552

		3.389214

		3.390882

		3.39255

		3.394218

		3.395886

		3.397548

		3.399216

		3.400884

		3.402552

		3.404214

		3.405882

		3.40755

		3.409218

		3.410886

		3.412548

		3.414216

		3.415884

		3.417552

		3.419214

		3.420882

		3.42255

		3.424218

		3.425886

		3.427548

		3.429216

		3.430884

		3.432552

		3.434214

		3.435882

		3.43755

		3.439218

		3.440886

		3.442548

		3.444216

		3.445884

		3.447552

		3.449214

		3.450882

		3.45255

		3.454218

		3.455886

		3.457548

		3.459216

		3.460884

		3.462552

		3.464214

		3.465882

		3.46755

		3.469218

		3.470886

		3.472548

		3.474216

		3.475884

		3.477552

		3.479214

		3.480882

		3.48255

		3.484218

		3.485886

		3.487548

		3.489216

		3.490884

		3.492552

		3.494214

		3.495882

		3.49755

		3.499218

		3.500886

		3.502548

		3.504216

		3.505884

		3.507552

		3.509214

		3.510882

		3.51255

		3.514218

		3.515886

		3.517548

		3.519216

		3.520884

		3.522552

		3.524214

		3.525882

		3.52755

		3.529218

		3.530886

		3.532548

		3.534216

		3.535884

		3.537552

		3.539214

		3.540882

		3.54255

		3.544218

		3.545886

		3.547548

		3.549216

		3.550884

		3.552552

		3.554214

		3.555882

		3.55755

		3.559218

		3.560886

		3.562548

		3.564216

		3.565884

		3.567552

		3.569214

		3.570882

		3.57255

		3.574218

		3.575886

		3.577548

		3.579216

		3.580884

		3.582552

		3.584214

		3.585882

		3.58755

		3.589218

		3.590886

		3.592548

		3.594216

		3.595884

		3.597552

		3.599214

		3.600882

		3.60255

		3.604218

		3.605886

		3.607548

		3.609216

		3.610884

		3.612552

		3.614214

		3.615882

		3.61755

		3.619218

		3.620886

		3.622548

		3.624216

		3.625884

		3.627552

		3.629214

		3.630882

		3.63255

		3.634218

		3.635886

		3.637548

		3.639216

		3.640884

		3.642552

		3.644214

		3.645882

		3.64755

		3.649218

		3.650886

		3.652548

		3.654216

		3.655884

		3.657552

		3.659214

		3.660882

		3.66255

		3.664218

		3.665886

		3.667548

		3.669216

		3.670884

		3.672552

		3.674214

		3.675882

		3.67755

		3.679218

		3.680886

		3.682548

		3.684216

		3.685884

		3.687552

		3.689214

		3.690882

		3.69255

		3.694218

		3.695886

		3.697548

		3.699216

		3.700884

		3.702552

		3.704214

		3.705882

		3.70755

		3.709218

		3.710886

		3.712548

		3.714216

		3.715884

		3.717552

		3.719214

		3.720882

		3.72255

		3.724218

		3.725886

		3.727548

		3.729216

		3.730884

		3.732552

		3.734214

		3.735882

		3.73755

		3.739218

		3.740886

		3.742548

		3.744216

		3.745884

		3.747552

		3.749214

		3.750882

		3.75255

		3.754218

		3.755886

		3.757548

		3.759216

		3.760884

		3.762552

		3.764214

		3.765882

		3.76755

		3.769218

		3.770886

		3.772548

		3.774216

		3.775884

		3.777552

		3.779214

		3.780882

		3.78255

		3.784218

		3.785886

		3.787548

		3.789216

		3.790884

		3.792552

		3.794214

		3.795882

		3.79755

		3.799218

		3.800886

		3.802548

		3.804216

		3.805884

		3.807552

		3.809214

		3.810882

		3.81255

		3.814218

		3.815886

		3.817548

		3.819216

		3.820884

		3.822552

		3.824214

		3.825882

		3.82755

		3.829218

		3.830886

		3.832548

		3.834216

		3.835884

		3.837552

		3.839214

		3.840882

		3.84255

		3.844218

		3.845886

		3.847548

		3.849216

		3.850884

		3.852552

		3.854214

		3.855882

		3.85755

		3.859218

		3.860886

		3.862548

		3.864216

		3.865884

		3.867552

		3.869214

		3.870882

		3.87255

		3.874218

		3.875886

		3.877548

		3.879216

		3.880884

		3.882552

		3.884214

		3.885882

		3.88755

		3.889218

		3.890886

		3.892548

		3.894216

		3.895884

		3.897552

		3.899214

		3.900882

		3.90255

		3.904218

		3.905886

		3.907548

		3.909216

		3.910884

		3.912552

		3.914214

		3.915882

		3.91755

		3.919218

		3.920886

		3.922548

		3.924216

		3.925884

		3.927552

		3.929214

		3.930882

		3.93255

		3.934218

		3.935886

		3.937548

		3.939216

		3.940884

		3.942552

		3.944214

		3.945882

		3.94755

		3.949218

		3.950886

		3.952548

		3.954216

		3.955884

		3.957552

		3.959214

		3.960882

		3.96255

		3.964218

		3.965886

		3.967548

		3.969216

		3.970884

		3.972552

		3.974214

		3.975882

		3.97755

		3.979218

		3.980886

		3.982548

		3.984216

		3.985884

		3.987552

		3.989214

		3.990882

		3.99255

		3.994218

		3.995886

		3.997548

		3.999216

		4.000884

		4.002552

		4.004214

		4.005882

		4.00755

		4.009218

		4.010886

		4.012548

		4.014216

		4.015884

		4.017552

		4.019214

		4.020882

		4.02255

		4.024218

		4.025886

		4.027548

		4.029216

		4.030884

		4.032552

		4.034214

		4.035882

		4.03755

		4.039218

		4.040886

		4.042548

		4.044216

		4.045884

		4.047552

		4.049214

		4.050882

		4.05255

		4.054218
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Peak Load at Break = 15,300 lbf
Following 10 Cycles to 1,000 lbf
Specimen broke 7.5" from the Nose of the Flanged Socket

Time, minutes

Tension, lbf

Specimen 2949F - #8flanged 
Tension versus Time
Cycle 11
1 Sept 2005
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Peak Load at Break = 36,800 lbf
Following 10 Cycles to 1,000 lbf
Specimen broke 14" from the Nose of the Socket

Time, minutes

Tension, lbf

Specimen 2949F - #8 
Tension versus Time
Cycle 11
1 Sept 2005
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6255

6267

6270

6289

6300

6301

6324

6322

6334

6348

6369

6376

6385

6402

6413

6419

6434

6437

6451

6464

6467

6481

6487

6509

6518

6528

6538

6553

6562

6569

6585

6597

6614

6614

6620

6634

6655

6656

6672

6684

6689

6698

6706

6726

6736

6747

6757

6761

6778

6785

6798

6804

6825

6840

6842

6862

6872

6872

6880

6891

6907

6925

6928

6935

6954

6972

6975

6975

6997

7004

7007

7030

7043

7051

7054

7060

7085

7096

7099

7110

7126

7130

7142

7159

7177

7174

7183

7199

7213

7220

7225

7237

7249

7263

7275

7293

7303

7305

7320

7320

7334

7350

7362

7377

7378

7382

7409

7416

7423

7439

7445

7456

7478

7488

7494

7494

7511

7535

7538

7548

7555

7568

7581

7584

7598

7595

7615

7626

7639

7652

7661

7680

7685

7700

7708

7720

7729

7743

7749

7759

7774

7783

7793

7802

7811

7822

7845

7857

7858

7871

7872

7883

7889

7909

7920

7933

7946

7957

7966

7971

7986

8001

8003

8019

8034

8041

8058

8072

8076

8087

8098

8103

8127

8135

8142

8155

8158

8176

8188

8193

8222

8216

8231

8238

8252

8260

8271

8286

8295

8305

8307

8328

8326

8344

8360

8367

8380

8398

8403

8406

8422

8435

8446

8461

8461

8467

8486

8486

8496

8518

8528

8534

8547

8560

8568

8586

8591

8605

8611

8625

8633

8641

8667

8663

8675

8688

8696

8708

8722

8743

8735

8750

8766

8789

8794

8790

8811

8818

8820

8841

8844

8864

8873

8886

8893

8898

8918

8924

8939

8947

8950

8968

8985

8989

9006

9015

9023

9044

9043

9053

9067

9069

9093

9083

9105

9120

9123

9147

9154

9166

9167

9187

9204

9214

9218

9227

9236

9249

9270

9273

9286

9311

9299

9322

9333

9334

9349

9351

9372

9373

9390

9398

9414

9418

9431

9450

9453

9469

9474

9487

9495

9511

9521

9534

9537

9544

9560

9580

9581

9610

9611

9611

9632

9640

9640

9659

9674

9688

9685

9704

9707

9712

9730

9756

9748

9775

9785

9788

9794

9807

9820

9834

9849

9854

9856

9877

9885

9891

9902

9913

9913

9943

9957

9964

9975

9979

10000

9998

10016

10028

10035

10052

10050

10072

10067

10095

10096

10106

10123

10132

10144

10159

10162

10175

10197

10195

10207

10218

10245

10242

10251

10265

10270

10285

10299

10311

10317

10335

10339

10343

10347

10375

10393

10391

10404

10414

10422

10425

10446

10455

10462

10472

10488

10491

10513

10526

10537

10547

10555

10562

10581

10592

10603

10608

10625

10629

10642

10663

10669

10661

10687

10696

10710

10719

10725

10725

10743

10753

10768

10783

10791

10806

10814

10829

10839

10848

10848

10872

10875

10877

10903

10899

10918

10929

10947

10954

10957

10972

10982

10996

11002

11008

11028

11040

11053

11058

11079

11084

11091

11109

11127

11135

11136

11139

11148

11158

11179

11201

11200

11203

11219

11228

11236

11256

11261

11274

11287

11303

11307

11319

11326

11338

11359

11360

11371

11388

11393

11406

11415

11439

11442

11451

11461

11473

11483

11496

11504

11511

11525

11531

11548

11557

11574

11583

11584

11607

11610

11599

11632

11636

11654

11658

11673

11677

11688

11702

11723

11728

11740

11754

11757

11770

11787

11796

11803

11814

11825

11836

11849

11856

11873

11891

11896

11907

11909

11926

11945

11942

11950

11963

11986

11976

12010

12018

12021

12024

12048

12064

12070

12076

12086

12107

12109

12131

12140

12144

12152

12153

12186

12191

12196

12209

12233

12227

12253

12263

12256

12285

12292

12301

12308

12308

12317

12340

12354

12353

12376

12379

12392

12403

12412

12430

12432

12447

12447

12463

12487

12498

12492

12510

12516

12534

12537

12553

12562

12578

12582

12594

12608

12616

12629

12643

12646

12657

12672

12688

12693

12711

12721

12727

12746

12753

12767

12771

12777

12791

12805

12819

12833

12839

12856

12863

12870

12877

12888

12905

12909

12918

12929

12943

12959

12962

12978

12988

13004

13010

13025

13022

13044

13067

13070

13078

13087

13093

13108

13114

13129

13142

13155

13163

13172

13185

13202

13205

13226

13238

13242

13256

13258

13273

13288

13288

13301

13308

13330

13326

13349

13358

13358

13370

13386

13400

13405

13435

13439

13458

13461

13472

13483

13489

13498

13519

13526

13533

13537

13562

13565

13567

13586

13595

13610

13620

13634

13647

13652

13663

13674

13690

13688

13710

13717

13728

13746

13755

13759

13775

13771

13791

13802

13809

13821

13836

13852

13861

13864

13874

13892

13900

13915

13927

13930

13951

13959

13971

13975

13990

14003

14010

14016

14035

14051

14058

14077

14083

14087

14106

14123

14126

14133

14130

14148

14161

14168

14194

14186

14215

14218

14219

14245

14247

14257

14273

14267

14296

14306

14316

14329

14337

14348

14362

14370

14379

14396

14403

14424

14432

14444

14445

14451

14474

14485

14501

14507

14509

14520

14529

14545

14567

14570

14581

14577

14595

14609

14630

14625

14642

14651

14667

14673

14679

14698

14709

14724

14718

14743

14752

14752

14764

14786

14797

14805

14811

14820

14842

14857

14857

14879

14895

14907

14908

14917

14931

14937

14948

14955

14970

14992

14997

14999

15019

15028

15028

15051

15062

15065

15073

15078

15093

15118

15133

15134

15140

15152

15163

15182

15184

15205

15209

15221

15235

15235

15244

15261

15269

15282

15301

15308

15318

15335

15338

15344

15361

15372

15373

15389

15408

15414

15432

15426

15442

15456

15465

15485

15489

15498

15511

15521

15530

15543

15548

15566

15565

15588

15592

15605

15624

15643

15637

15649

15650

15672

15686

15695

15706

15727

15731

15743

15751

15762

15773

15791

15801

15803

15813

15817

15838

15842

15862

15867

15875

15888

15909

15916

15933

15931

15944

15956

15971

15971

15988

15998

16005

16016

16033

16036

16046

16069

16088

16077

16092

16117

16123

16127

16149

16153

16155

16165

16175

16201

16209

16126

16217

16248

16246

16256

16271

16285

16303

16304

16313

16322

16344

16350

16348

16374

16374

16391

16402

16404

16426

16440

16442

16462

16464

16477

16492

16487

16487

16502

16526

16530

16499

16549

16578

16579

16485

16550

16601

16633

16642

16643

16663

16680

16694

16694

16708

16721

16727

16742

16753

16763

16773

16787

16800

16808

16821

16826

16840

16853

16860

16864

16874

16875

16905

16918

16928

16937

16955

16963

16971

16981

16993

17003

17016

17022

17037

17043

17053

17070

17084

17094

17110

17118

17109

17119

17136

17160

17162

17176

17194

17195

17203

17219

17237

17235

17256

17267

17274

17275

17287

17300

17318

17328

17331

17341

17351

17372

17396

17391

17403

17419

17418

17436

17448

17455

17478

17480

17496

17499

17510

17515

17544

17544

17548

17570

17583

17581

17601

17595

17612

17630

17638

17644

17667

17679

17680

17705

17707

17715

17732

17741

17744

17761

17766

17776

17788

17802

17822

17831

17841

17839

17858

17876

17883

17884

17897

17898

17924

17937

17957

17963

17964

17978

17994

18002

18012

18014

18025

18033

18050

18067

18070

18082

18096

18099

18131

18118

18137

18143

18160

18173

18176

18194

18195

18214

18237

17931

18194

18250

18261

18264

18297

18302

18311

18293

18311

18333

18366

18373

18374

18385

18389

18401

18359

18417

18426

18448

18460

18471

18484

18498

18269

18481

18478

18526

18552

18567

18570

18575

18587

18605

18617

18631

18639

18660

18655

18671

18672

18695

18701

18725

18724

18733

18733

18766

18779

18785

18782

18801

18814

18817

18832

18854

18862

18869

18876

18856

18898

18912

18907

18931

18946

18953

18959

18978

18982

18995

19007

19027

19027

19036

19054

19046

19036

19078

19088

19099

19113

19130

19110

19155

19166

19178

19183

19192

19199

19197

19226

19239

19235

19252

19260

19269

19295

19307

19310

19320

19338

19344

19353

19375

19370

19388

19397

19417

19426

19431

19449

19446

19456

19468

19478

19495

19506

19523

19525

19542

19547

19575

19570

19575

19594

19606

19616

19623

19633

19644

19653

19661

19671

19688

19691

19710

19728

19732

19742

19754

19765

19783

19789

19794

19810

19816

19835

19845

19845

19857

19876

19871

19889

19904

19919

19931

19939

19961

19947

19970

19984

19999

19998

20017

20023

20039

20044

20062

20068

20052

20080

20101

20112

20119

20136

20143

20153

20158

20168

20182

20199

20197

20216

20231

20229

20244

20254

20262

20283

20284

20306

20312

20328

20338

20344

20371

20368

20376

20380

20399

20413

20424

20432

20442

20451

20468

20467

20489

20502

20512

20525

20528

20539

20548

20556

20570

20582

20593

20605

20616

20627

20628

20651

20665

20673

20684

20690

20700

20723

20728

20722

20725

20747

20776

20773

20780

20792

20815

20825

20834

20842

20851

20861

20862

20885

20889

20899

20919

20921

20932

20945

20962

20973

20984

20995

20997

21018

21029

21034

20731

21035

21054

21089

21104

21102

21112

21129

21144

21155

21157

21163

21186

21191

21207

21221

21224

21240

21250

21261

21270

21284

21291

21299

21318

21326

21339

21348

21358

21369

21377

21384

21398

21408

21409

21433

21447

21450

21447

21473

21486

21485

21501

21512

21516

21535

21563

21551

21566

21577

21588

21599

21608

21621

21633

21630

21662

21669

21678

21694

21698

21701

21716

21726

21746

21758

21766

21778

21792

21799

21801

21811

21832

21857

21862

21855

21865

21879

21898

21899

21909

21917

21942

21946

21957

21968

21976

21989

22001

22012

22030

22030

22041

22050

22062

22075

22096

22094

22105

22115

22128

22146

22157

22159

22172

22183

22188

22194

22214

22226

22238

22248

22271

22271

22274

22286

22297

22312

22323

22345

22346

22355

22352

22382

22394

22401

22415

22430

22436

22439

22459

22466

22469

22494

22509

22500

22523

22530

22546

22544

22559

22562

22583

22593

22616

22625

22621

22636

22660

22662

22660

22687

22688

22696

22717

22720

22736

22754

22766

22758

22784

22792

22794

22811

22829

22839

22831

22858

22860

22887

22884

22894

22909

22922

22935

22943

22951

22960

22978

22992

23000

23003

23025

23030

23034

23046

23067

23079

23086

23095

23099

23112

23134

23126

23142

23158

23174

23174

23196

23200

23209

23210

23225

23235

23261

23265

23279

23281

23300

23326

23322

23331

23340

23349

23367

23374

23387

23400

23407

23426

23429

23443

23446

23464

23475

23487

23493

23511

23529

23524

23539

23555

23566

23558

23581

23587

23610

23615

23619

23633

23639

23664

23661

23684

23688

23703

23718

23735

23741

23743

23754

23766

23767

23785

23799

23805

23815

23831

23851

23853

23858

23880

23883

23887

23900

23918

23931

23925

23940

23954

23973

23970

23987

23997

24005

24023

24038

24044

24066

24070

24076

24083

24103

24112

24132

24133

24145

24154

24164

24169

24182

24192

24199

24221

24224

24238

24253

24257

24269

23638

24191

24296

24303
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24354

24353

24363

24373

24392

24398

24405

24416

24428

24439

24445

24463

24463

24478

24490

24502

24522

24536

24531

24543

24561

24578

24569

24592

24609

24630

24622

24629

24643

24659

24666

24677

24677

24705

24706

24723

24731

24752

24747

24766

24772

24785

24791

24812

24816

24830

24843

24856

24853

24869

24875

24894

24907

24885

24923
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24941

24954

24969

24985

24998

25000

25014

25018

25036
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25049

25068

25074

25094

25103

25114

25125

25131

25148

25147

25170

25182

25190

25196

25200

25217

25230

25243

25250

25264

25272

25280

25284

25306

25310

25329

25346

25346

25338

25375

25379

25391

25415

25407

25430

25434

25442

25454

25463

25478
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25508
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25544

25570

25585

25584
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25611

25621

25624

25646
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25676
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25704

25717
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25733

25742
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25782

25794

25809

25813
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25841

25861

25868

25880
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25914
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25930

25936
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25969

25978

25984
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26011
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26030
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26049

26070

26075
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26094

26110

26116

26126

26136

26048

26146

26166

26183

26190

26202

26232

26229

26232

26242

26249
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26277

26296

26306

26313

26308

26339

26355
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26375

26383
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26400

26411
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26438
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26452

26458

26474

26479

26497
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26521

26530
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26574

26587
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26605

26610

26628
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26644
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26667

26691
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26700

26714

26722

26743

26739

26760

26770

26774

26789

26804

26815

26821
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26853

26867

26874

26880

26901

26901

26925

26931

26947

26948

26964

26974

26981

26997

27004

27003

27038

27041

27050

27051

27063

27071

27095

27104

27113

27131

27121

27140

27166

27176

27179

27192

27187

27210

27226

27233

27247
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27272

27275

27296

27295

27310

27321

27324

27333

27353

27362

27360

27388

27382

27397
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27432

27439

27453

27462

27479

27480

27490

27497

27515
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27548

27545

27555

27563

27589

27600

27611

27631

27636

27644

27653

27666

27679

27693

27695

27706

27721

27734

27740

27753

27758

27782

27782

27785

27807

27810

27832

27830

27863

27872

27867

27875

27885

27901

27903

27930

27928

27943

27950

27979

27977

27990

27988

28008

28026

28037

28056

28049

28062

28058

28088

28086

28109

28122

28124

28133

28146

28159

28169

28178

28201

28203

28217

28225

28240

28246

28263

28267

28276

28298

28293

28311

28330

28336

28356

28359

28372

28377

28388

28389

28407

28422

28437

28442

28455

28470

28472

28483

28501

28499

28522

28531

28546

28544

28565

28576

28587

28602

28613

28617

28622

28646

28648

28655

28675

28668

28682

28701

28700

28723

28733

28752

28749

28766

28778

28793

28800

28816

28840

28830

28843

28856

28868

28877

28896

28887

28909

28920

28925

28936

28945

28957

28960

28989

28995

29006

29013

29023

29032

29053

29042

29073

29079

29080

29097

29105

29119

29125

29148

29160

29168

29174

29184

29196

29215

29228

29234

29244

29254

29274

29274

29286

29306

29309

29330

29329

29342

29349

29367

29389

29380

29393

29416

29409

29428

29448

29452

29458

29466

29472

29490

29497

29519

29513

29537

29544

29548

29570

29576

29587

29594

29612

29639

29632

29648

29664

29669

29668

29683

29693

29706

29713

29729

29739

29759

29765

29782

29794

29801

29802

29812

29827

29842

29838

29858

29870

29891

29883

29907

29909

29935

29931

29938

29950

29965

29983

30007

30000

30012

30028

30038

30041

30053

30063

30076

30075

30092

30117

30117

30140

30140

30154

30170

30173

30179

30198

30213

30219

30237

30239

30241

30269

30278

30283

30292

30312

30322

30336

30327

30344

30360

30370

30373

30396

30401

30414

30424

30433

30438

30456

30465

30486

30492

30512

30518

30531

30531

30546

30558

30569

30585

30587

30589

30605

30619

30621

30637

30660

30657

30672

30692

30707

30702

30724

30726

30737

30754

30772

30783

30789

30798

30815

30816

30814

30830

30844

30861

30871

30885

30905

30900

30899

30924

30938

30951

30963

30975

30985

30989

31001

31017

31024

31042

31040

31052

31059

31082

31085

31100

31115

31116

31129

31146

31159

31163

31180

31191

31188

31198

31227

31232

31246

31246

31255

31265

31274

31301

31311

31323

31332

31346

31361

31365

31376

31382

31388

31419

31414

31427

31446

31446

31464

31462

31475

31493

31503

31509

31521

31539

31545

31546

31572

31581

31594

31608

31617

31613

31630

31642

31659

31662

31683

31683

31692

31703

31726

31726

31739

31748

31758

31775

31781

31800

31813

31815

31839

31842

31852

31865

31876

31885

31891

31913

31910

31920

31940

31944

31965

31968

31972

31983

31988

32010

32033

32042

32048

32052

32071

32058

32081

32111

32100

32121

32126

32147

32153

30216

31691

32132

32181

32224

32246

32235

32241

32260

32271

32273

32295

32297

32317

32322

32335

32348

32351

32371

32379

32391

32403

32418

32429

32438

32434

32449

32470

32476

32490

32502

32512

32521

32532

32548

32559

32561

32577

32577

32603

32596

32612

32628

32645

32654

32661

32680

32681

32687

32707

32712

32728

32746

32748

32759

32771

32784

32796

32792

32815

32826

32840

32845

32859

32872

32874

32886

32898

32912

32926

32935

32955

32951

32961

32988

32950

32992

33002

33022

33022

33039

33051

33060

33077

33090

33097

33107

33119

33131

33125

33152

33165

33166

33197

33189

33191

33217

33228

33240

33246

33257

33262

33281

33292

33293

33307

33318

33323

33335

33352

33345

33376

33370

33395

33428

33421

33424

33441

33447

33457

33470

33477

33491

33494

33515

33524

33540

33540

33550

33564

33575

33592

33592

33611

33627

33627

33638

33647

33660

33677

33689

33688

33705

33716

33728

33734

33743

33750

33763

33782

33798

33800

33819

33833

33824

33855

33853

33864

33873

33884

33902

33904

33920

33920

33944

33950

33973

33981

33989

33997

34011

34016

34027

34037

34042

34061

34071

34081

34096

34111

34124

34120

34128

34132

34146

34168

34182

34192

34200

34218

34221

34233

34257

34256

34271

34275

34278

34292

34307

34310

34327

34340

34366

34359

34375

34372

34385

34397

34404

34423

34429

34436

34447

34456

34471

34482

34503

34505

34522

34531

34545

34552

34569

34578

34588

34596

34594

34613

34630

34626

34649

34655

34677

34675

34687

34696

34709

34715

34734

34744

34757

34768

34778

34792

34787

34806

34818

34823

34839

34860

34862

34876

34887

34887

34904

34913

34934

34939

34949

34955

34975

34975

34984

35003

35015

35013

35032

35047

35051

35059

35071

35074

35101

35107

35121

35124

35129

35142

35157

35172

35172

35185

35204

35208

35218

35219

35236

35248

35262

35277

35288

35300

35308

35324

35331

35335

35349

35360

35382

35383

35402

35410

35423

35427

35433

35451

35464

35475

35483

35498

35500

35521

35515

35538

35540

35548

35580

35581

35594

35606

35616

35619

35635

35640

35650

35670

35676

35692

35700

35707

35722

35724

35741

35747

35765

35775

35783

35794

35808

35819

35825

35838

35844

35855

35865

35883

35899

35904

35919

35938

35935

35952

35957

35966

35973

35989

35997

36014

36018

36035

36048

36057

36073

36076

36093

36102

36109

36128

36134

36140

36159

36164

36180

36190

36196

36203

36231

36240

36238

36257

36266

36271

36279

36287

36302

36324

36326

36340

36350

36363

36373

36373

36386

36399

36418

36416

36435

36445

36457

36470

36485

36489

36505

36508

36520

36530

36551

36563

36553

36577

36587

36603

36611

36614

36629

36645

36657

36668

36676

36675

36688

36707

36721

36723

36742

32603

34262

35956

36630

36750

36799

36827

36837

36829

30968

14106

5180

7411

2837

3295

2967

2817

2528

3372

3219

2576

3739

2979

2556

3444

2688

3872

2987

2703

3343

2737

2640

2507

2428

2467

2556

2652

3092

2580

2596

2415

2815

1699

1131

794

566

402

292

234

177

157

143

125

102

93

91

85

85

78

70

75

68

69

67

60

60

60

54

57

53

52

52

47

48

50

45

47

43

42

42

45

47

53

59

70

79

91

97

105

119

130

135

153

163

176

182

195

198

199

203

204

208

222

234

244

258

268

278

288

295

309

324

330

340

353

368

375

383

395

405

418

427

437

446

458

468

480

496

508

516

524

536

546

556

564

574

585

604

612

625

635

643

656

661

675

682

693

706

717

736

741

757

762

773

775

789

801

817

827

844

856

862

874

882

893

903

922

926

942

951

955

967

979

991

1004

1012

1021

1033

1043

1058

1068

1082

1090

1098

1110

1122

1136

1146

1155

1165

1177

1187

1197

1210

1220

1233

1239

1253

1262

1271

1284

1295

1313

1326

1334

1345

1355

1365

1375

1385

1396

1407

1414

1425

1437

1452

1464

1471

1479

1490

1502

1516

1524

1530

1545

1555

1573

1579

1600

1603

1614

1619

1635

1647

1657

1664

1671

1691

1700

1709

1717

1730

1741

1755

1767

1775

1784

1794

1804

1820

1826

1838

1849

1864

1878

1888

1893

1907

1906

1926

1939

1951

1965

1967

1985

1994

2009

2015

2033

2035

2051

2061

2070

2080

2090

2096

2106

2120

2133

2140

2152

2157

2169

2183

2196

2208

2215

2225

2244

2246

2258

2273

2280

2296

2309

2313

2328

2331

2352

2360

2370

2380

2388

2402

2410

2418

2436

2446

2456

2466

2477

2489

2502

2515

2517

2526

2538

2550

2563

2578

2580

2596

2605

2612

2622

2638

2647

2652

2663

2676

2689

2697

2706

2718

2737

2744

2757

2767

2783

2795

2804

2810

2820

2828

2841

2852

2868

2878

2890

2898

2907

2920

2931

2932

2940

2956

2965

2976

3000

3001

3016

3027

3034

3040

3053

3058

3079

3090

3099

3098

3113

3131

3151

3154

3163

3179

3191

3201

3204

3214

3226

3237

3247

3255

3269

3280

3286

3298

3308

3314

3324

3343

3356

3368

3381

3388

3406

3404

3421

3432

3443

3449

3459

3468

3481

3489

3505

3519

3525

3530

3540

3553

3569

3577

3585

3600

3612

3621

3637

3646

3656

3665

3672

3683

3704

3704

3717

3727

3746

3756

3763

3773

3786

3801

3810

3822

3828

3834

3843

3862

3867

3879

3887

3904

3920

3931

3936

3949

3959

3966

3971

3981

4000

4007

4020

4033

4038

4052

4058

4077

4084

4089

4099

4115

4123

4127

4145

4152

4171

4187

4198

4208

4220

4221

4233

4244

4262

4268

4279

4290

4297

4310

4326

4333

4343

4345

4366

4371

4384

4388

4410

4423

4422

4434

4443

4454

4468

4484

4487

4504

4515

4528

4539

4561

4561

4574

4590

4584

4610

4620

4629

4636

4642

4655

4667

4685

4694

4703

4713

4716

4725

4740

4755

4762

4772

4782

4790

4810

4819

4829

4834

4851

4858

4866

4880

4892

4903

4915

4925

4938

4951

4955

4969

4983

4998

5003

5013

5023

5032

5044

5055

5064

5078

5088

5101

5106

5125

5134

5145

5153

5166

5172

5186

5203

5215

5223

5234

5235

5244

5266

5276

5294

5296

5306

5318

5333

5348

5345

5360

5371

5383

5403

2634

2480

2257

2363

2167

2887

2316

2365

2747

2440

2604

2237

2747

2600

2456

2381

2827

2478

2586

2505

3059

2365

2770

2433

3057

2269

2336

2747

2136

2661

3041

2246

2772

2126

2515

3035

2096

2532

2348

2365

2302

2113

2528

2080

2559

3015

2201

2644

2032

2395

2655

2205

2796

2177

2750

2152

2080

2518

2022

2043

2467

2703

2161

2650

2052

2493

2942

2046

2481

2005

2421

2268

2232

2722

2282

2212

2027

2315

2040

2476

2070

2573

2077

2542

1961

2389

1942

2351

2826

1907

2308

1872

2212

2608

3034

1795

2132

2548

2286

1966

2417

2793

1909

2054

2267

2030

1822

2247

2677

1845

2231

2610

3091

1796

2197

2605

1810

1998

2438

1880

2254

1986

1843

2101

2493

2924

1916

2322

1856

2103

2502

1826

2122

2520

2940

1858

2259

1946

2360

2411

2020

2412

2283

2035

2500

1875

2236

2575

1977

2371

2808

1941

2345

2736

2449

1948

2330

1755

1780

2035

2450

2818

1741

2133

1757

2096

2459

1745

1968

1727

2051

1697

2038

2481

1835

2212

2550

1729

2098

2501

1919

2284

1742

2070

1987

1916

2083

1945

2342

1747

2062

2440

2834

1816

2269

1842

2191

2614

1760

2103

1870

2032

1847

2289

2003

2336

2701

2056

2032

2363

2782

1793

2174

1774

2088

2318

1916

2314

1880

2256

1771

2058

1765

2078

2424

2781

1841

2206

2622

1732

2044

2437

2027

1941

1945

1504

1184

944

752

611

491

386

311

249

207

182

166

145

132

126

115

108

98

91

86

85

79

75

72

69

68

68

64

60

60

56

55

54

56

55

48

46

44

45

44

41

40

40

41

38

42

37

37

35

36

38

37

34

34

34

36

34

36

31

30

31



T vs t #8flanged

		0.004266

		0.005886

		0.007548

		0.009216

		0.010884

		0.012552

		0.014214

		0.015882

		0.01755

		0.019218

		0.020886

		0.022548

		0.024216

		0.025884

		0.027552

		0.029214

		0.030882

		0.03255

		0.034218

		0.035886

		0.037548

		0.039216

		0.040884

		0.042552

		0.044214

		0.045882

		0.04755

		0.049218

		0.050886

		0.052548

		0.054216

		0.055884

		0.057552

		0.059214

		0.060882

		0.06255

		0.064218

		0.065886

		0.067548

		0.069216

		0.070884

		0.072552

		0.074214

		0.075882

		0.07755

		0.079218

		0.080886

		0.082548

		0.084216

		0.085884

		0.087552

		0.089214

		0.090882

		0.09255

		0.094218

		0.095886

		0.097548

		0.099216

		0.100884

		0.102552

		0.104214

		0.105882

		0.10755

		0.109218

		0.110886

		0.112548

		0.114216

		0.115884

		0.117552

		0.119214

		0.120882

		0.12255

		0.124218

		0.125886

		0.127548

		0.129216

		0.130884

		0.132552

		0.134214

		0.135882

		0.13755

		0.139218

		0.140886

		0.142548

		0.144216

		0.145884

		0.147552

		0.149214

		0.150882

		0.15255

		0.154218

		0.155886

		0.157548

		0.159216

		0.160884

		0.162552

		0.164214

		0.165882

		0.16755

		0.169218

		0.170886

		0.172548

		0.174216

		0.175884

		0.177552

		0.179214

		0.180882

		0.18255

		0.184218

		0.185886

		0.187548

		0.189216

		0.190884

		0.192552

		0.194214

		0.195882

		0.19755

		0.199218

		0.200886

		0.202548

		0.204216

		0.205884

		0.207552

		0.209214

		0.210882

		0.21255

		0.214218

		0.215886

		0.217548

		0.219216

		0.220884

		0.222552

		0.224214

		0.225882

		0.22755

		0.229218

		0.230886

		0.232548

		0.234216

		0.235884

		0.237552

		0.239214

		0.240882

		0.24255

		0.244218

		0.245886

		0.247548

		0.249216

		0.250884

		0.252552

		0.254214

		0.255882

		0.25755

		0.259218

		0.260886

		0.262548

		0.264216

		0.265884

		0.267552

		0.269214

		0.270882

		0.27255

		0.274218

		0.275886

		0.277548

		0.279216

		0.280884

		0.282552

		0.284214

		0.285882

		0.28755

		0.289218

		0.290886

		0.292548

		0.294216

		0.295884

		0.297552

		0.299214

		0.300882

		0.30255

		0.304218

		0.305886

		0.307548

		0.309216

		0.310884

		0.312552

		0.314214

		0.315882

		0.31755

		0.319218

		0.320886

		0.322548

		0.324216

		0.325884

		0.327552

		0.329214

		0.330882

		0.33255

		0.334218

		0.335886
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		2.377548

		2.379216

		2.380884

		2.382552

		2.384214

		2.385882

		2.38755

		2.389218

		2.390886

		2.392548

		2.394216

		2.395884

		2.397552

		2.399214

		2.400882

		2.40255

		2.404218

		2.405886

		2.407548

		2.409216

		2.410884

		2.412552

		2.414214

		2.415882

		2.41755

		2.419218

		2.420886

		2.422548

		2.424216

		2.425884

		2.427552

		2.429214

		2.430882

		2.43255

		2.434218

		2.435886

		2.437548

		2.439216

		2.440884

		2.442552

		2.444214

		2.445882

		2.44755

		2.449218

		2.450886

		2.452548

		2.454216

		2.455884

		2.457552

		2.459214

		2.460882

		2.46255

		2.464218

		2.465886

		2.467548

		2.469216

		2.470884

		2.472552

		2.474214

		2.475882

		2.47755

		2.479218

		2.480886

		2.482548

		2.484216

		2.485884

		2.487552

		2.489214

		2.490882

		2.49255

		2.494218

		2.495886

		2.497548

		2.499216

		2.500884

		2.502552

		2.504214

		2.505882

		2.50755

		2.509218

		2.510886

		2.512548

		2.514216

		2.515884

		2.517552

		2.519214

		2.520882

		2.52255

		2.524218

		2.525886

		2.527548

		2.529216

		2.530884

		2.532552

		2.534214

		2.535882

		2.53755

		2.539218

		2.540886

		2.542548

		2.544216

		2.545884

		2.547552

		2.549214

		2.550882

		2.55255

		2.554218

		2.555886

		2.557548

		2.559216

		2.560884

		2.562552

		2.564214

		2.565882

		2.56755

		2.569218

		2.570886

		2.572548

		2.574216

		2.575884

		2.577552

		2.579214

		2.580882

		2.58255

		2.584218

		2.585886

		2.587548

		2.589216

		2.590884

		2.592552

		2.594214

		2.595882

		2.59755

		2.599218

		2.600886

		2.602548

		2.604216

		2.605884

		2.607552

		2.609214

		2.610882

		2.61255

		2.614218

		2.615886

		2.617548

		2.619216

		2.620884

		2.622552

		2.624214

		2.625882

		2.62755

		2.629218

		2.630886

		2.632548

		2.634216

		2.635884

		2.637552

		2.639214

		2.640882

		2.64255

		2.644218

		2.645886

		2.647548

		2.649216

		2.650884

		2.652552

		2.654214

		2.655882

		2.65755

		2.659218

		2.660886

		2.662548

		2.664216

		2.665884

		2.667552

		2.669214

		2.670882

		2.67255

		2.674218

		2.675886

		2.677548

		2.679216

		2.680884

		2.682552

		2.684214

		2.685882

		2.68755

		2.689218

		2.690886

		2.692548

		2.694216

		2.695884

		2.697552

		2.699214

		2.700882

		2.70255

		2.704218

		2.705886

		2.707548

		2.709216

		2.710884

		2.712552

		2.714214

		2.715882

		2.71755

		2.719218

		2.720886

		2.722548

		2.724216

		2.725884

		2.727552

		2.729214

		2.730882

		2.73255

		2.734218

		2.735886

		2.737548

		2.739216

		2.740884

		2.742552

		2.744214

		2.745882

		2.74755

		2.749218

		2.750886

		2.752548

		2.754216

		2.755884

		2.757552

		2.759214

		2.760882

		2.76255

		2.764218

		2.765886

		2.767548

		2.769216

		2.770884

		2.772552

		2.774214

		2.775882

		2.77755

		2.779218

		2.780886

		2.782548

		2.784216

		2.785884

		2.787552

		2.789214

		2.790882

		2.79255

		2.794218

		2.795886

		2.797548

		2.799216

		2.800884

		2.802552

		2.804214

		2.805882

		2.80755

		2.809218

		2.810886

		2.812548

		2.814216

		2.815884

		2.817552

		2.819214

		2.820882

		2.82255

		2.824218

		2.825886

		2.827548

		2.829216

		2.830884

		2.832552

		2.834214

		2.835882

		2.83755

		2.839218

		2.840886

		2.842548

		2.844216

		2.845884

		2.847552

		2.849214

		2.850882

		2.85255

		2.854218

		2.855886

		2.857548

		2.859216

		2.860884

		2.862552

		2.864214

		2.865882

		2.86755

		2.869218

		2.870886

		2.872548

		2.874216

		2.875884

		2.877552

		2.879214

		2.880882

		2.88255

		2.884218

		2.885886

		2.887548

		2.889216

		2.890884

		2.892552

		2.894214

		2.895882

		2.89755

		2.899218

		2.900886

		2.902548

		2.904216

		2.905884

		2.907552

		2.909214

		2.910882

		2.91255

		2.914218

		2.915886

		2.917548

		2.919216

		2.920884

		2.922552

		2.924214

		2.925882

		2.92755

		2.929218

		2.930886

		2.932548

		2.934216

		2.935884

		2.937552

		2.939214

		2.940882

		2.94255

		2.944218

		2.945886

		2.947548

		2.949216

		2.950884

		2.952552

		2.954214

		2.955882

		2.95755

		2.959218

		2.960886

		2.962548

		2.964216

		2.965884

		2.967552

		2.969214

		2.970882

		2.97255

		2.974218

		2.975886

		2.977548

		2.979216

		2.980884

		2.982552

		2.984214

		2.985882

		2.98755

		2.989218

		2.990886

		2.992548

		2.994216

		2.995884

		2.997552

		2.999214

		3.000882

		3.00255

		3.004218

		3.005886

		3.007548

		3.009216

		3.010884

		3.012552

		3.014214

		3.015882

		3.01755

		3.019218

		3.020886

		3.022548

		3.024216

		3.025884

		3.027552

		3.029214

		3.030882

		3.03255

		3.034218

		3.035886

		3.037548

		3.039216

		3.040884

		3.042552

		3.044214

		3.045882

		3.04755

		3.049218

		3.050886

		3.052548

		3.054216

		3.055884

		3.057552

		3.059214

		3.060882

		3.06255

		3.064218

		3.065886

		3.067548

		3.069216

		3.070884

		3.072552

		3.074214

		3.075882

		3.07755

		3.079218

		3.080886

		3.082548

		3.084216

		3.085884

		3.087552

		3.089214

		3.090882

		3.09255

		3.094218

		3.095886

		3.097548

		3.099216

		3.100884

		3.102552

		3.104214

		3.105882

		3.10755

		3.109218

		3.110886

		3.112548

		3.114216

		3.115884

		3.117552

		3.119214

		3.120882

		3.12255

		3.124218

		3.125886

		3.127548

		3.129216

		3.130884

		3.132552

		3.134214

		3.135882

		3.13755

		3.139218

		3.140886

		3.142548

		3.144216

		3.145884

		3.147552

		3.149214

		3.150882

		3.15255

		3.154218

		3.155886

		3.157548

		3.159216

		3.160884

		3.162552

		3.164214

		3.165882

		3.16755

		3.169218

		3.170886

		3.172548

		3.174216

		3.175884

		3.177552

		3.179214

		3.180882

		3.18255

		3.184218

		3.185886

		3.187548

		3.189216

		3.190884

		3.192552

		3.194214

		3.195882

		3.19755

		3.199218

		3.200886

		3.202548

		3.204216

		3.205884

		3.207552

		3.209214

		3.210882

		3.21255

		3.214218

		3.215886

		3.217548

		3.219216

		3.220884

		3.222552

		3.224214

		3.225882

		3.22755

		3.229218

		3.230886

		3.232548

		3.234216

		3.235884

		3.237552

		3.239214

		3.240882

		3.24255

		3.244218

		3.245886

		3.247548

		3.249216

		3.250884

		3.252552

		3.254214

		3.255882

		3.25755

		3.259218

		3.260886

		3.262548

		3.264216

		3.265884

		3.267552

		3.269214

		3.270882

		3.27255

		3.274218

		3.275886

		3.277548

		3.279216

		3.280884

		3.282552

		3.284214

		3.285882

		3.28755

		3.289218

		3.290886

		3.292548

		3.294216

		3.295884

		3.297552

		3.299214

		3.300882

		3.30255

		3.304218

		3.305886

		3.307548

		3.309216

		3.310884

		3.312552

		3.314214

		3.315882

		3.31755

		3.319218

		3.320886

		3.322548

		3.324216

		3.325884

		3.327552

		3.329214

		3.330882

		3.33255

		3.334218

		3.335886

		3.337548

		3.339216

		3.340884

		3.342552

		3.344214

		3.345882

		3.34755

		3.349218

		3.350886

		3.352548

		3.354216

		3.355884

		3.357552

		3.359214

		3.360882

		3.36255

		3.364218

		3.365886

		3.367548

		3.369216

		3.370884

		3.372552

		3.374214

		3.375882

		3.37755

		3.379218

		3.380886

		3.382548

		3.384216

		3.385884

		3.387552

		3.389214

		3.390882

		3.39255

		3.394218

		3.395886

		3.397548

		3.399216

		3.400884

		3.402552

		3.404214

		3.405882

		3.40755

		3.409218

		3.410886

		3.412548

		3.414216

		3.415884

		3.417552

		3.419214

		3.420882

		3.42255

		3.424218

		3.425886

		3.427548

		3.429216

		3.430884

		3.432552

		3.434214

		3.435882

		3.43755

		3.439218

		3.440886

		3.442548

		3.444216

		3.445884

		3.447552

		3.449214

		3.450882

		3.45255

		3.454218

		3.455886

		3.457548

		3.459216

		3.460884

		3.462552

		3.464214

		3.465882

		3.46755

		3.469218

		3.470886

		3.472548

		3.474216

		3.475884

		3.477552

		3.479214

		3.480882

		3.48255

		3.484218

		3.485886

		3.487548

		3.489216

		3.490884

		3.492552

		3.494214

		3.495882

		3.49755

		3.499218

		3.500886

		3.502548

		3.504216

		3.505884

		3.507552

		3.509214

		3.510882

		3.51255

		3.514218

		3.515886

		3.517548

		3.519216

		3.520884

		3.522552

		3.524214

		3.525882

		3.52755

		3.529218

		3.530886

		3.532548

		3.534216

		3.535884

		3.537552

		3.539214

		3.540882

		3.54255

		3.544218

		3.545886

		3.547548

		3.549216

		3.550884

		3.552552

		3.554214

		3.555882

		3.55755

		3.559218

		3.560886

		3.562548

		3.564216

		3.565884

		3.567552

		3.569214

		3.570882

		3.57255

		3.574218

		3.575886

		3.577548

		3.579216

		3.580884

		3.582552

		3.584214

		3.585882

		3.58755

		3.589218

		3.590886

		3.592548

		3.594216

		3.595884

		3.597552

		3.599214

		3.600882

		3.60255

		3.604218

		3.605886

		3.607548

		3.609216

		3.610884

		3.612552

		3.614214

		3.615882

		3.61755

		3.619218

		3.620886

		3.622548

		3.624216

		3.625884

		3.627552

		3.629214

		3.630882

		3.63255

		3.634218

		3.635886

		3.637548

		3.639216

		3.640884

		3.642552

		3.644214

		3.645882

		3.64755

		3.649218

		3.650886

		3.652548

		3.654216

		3.655884

		3.657552

		3.659214

		3.660882

		3.66255

		3.664218

		3.665886

		3.667548

		3.669216

		3.670884

		3.672552

		3.674214

		3.675882

		3.67755

		3.679218

		3.680886

		3.682548

		3.684216

		3.685884

		3.687552

		3.689214

		3.690882

		3.69255

		3.694218

		3.695886

		3.697548

		3.699216

		3.700884

		3.702552

		3.704214

		3.705882

		3.70755

		3.709218

		3.710886

		3.712548

		3.714216

		3.715884

		3.717552

		3.719214

		3.720882

		3.72255

		3.724218

		3.725886

		3.727548

		3.729216

		3.730884

		3.732552

		3.734214

		3.735882

		3.73755

		3.739218

		3.740886

		3.742548

		3.744216

		3.745884

		3.747552

		3.749214

		3.750882

		3.75255

		3.754218

		3.755886

		3.757548

		3.759216

		3.760884

		3.762552

		3.764214

		3.765882

		3.76755

		3.769218

		3.770886

		3.772548

		3.774216

		3.775884

		3.777552

		3.779214

		3.780882

		3.78255

		3.784218

		3.785886

		3.787548

		3.789216

		3.790884

		3.792552

		3.794214

		3.795882

		3.79755

		3.799218

		3.800886

		3.802548

		3.804216

		3.805884

		3.807552

		3.809214

		3.810882

		3.81255

		3.814218

		3.815886

		3.817548

		3.819216

		3.820884

		3.822552

		3.824214

		3.825882

		3.82755

		3.829218

		3.830886

		3.832548

		3.834216

		3.835884

		3.837552

		3.839214

		3.840882

		3.84255

		3.844218

		3.845886

		3.847548

		3.849216

		3.850884

		3.852552

		3.854214

		3.855882

		3.85755

		3.859218

		3.860886

		3.862548

		3.864216

		3.865884

		3.867552

		3.869214

		3.870882

		3.87255

		3.874218

		3.875886

		3.877548

		3.879216

		3.880884

		3.882552

		3.884214

		3.885882

		3.88755

		3.889218

		3.890886

		3.892548

		3.894216

		3.895884

		3.897552

		3.899214

		3.900882

		3.90255

		3.904218

		3.905886

		3.907548

		3.909216

		3.910884

		3.912552

		3.914214

		3.915882

		3.91755

		3.919218

		3.920886

		3.922548

		3.924216

		3.925884

		3.927552

		3.929214

		3.930882

		3.93255

		3.934218

		3.935886

		3.937548

		3.939216

		3.940884

		3.942552

		3.944214

		3.945882

		3.94755

		3.949218

		3.950886

		3.952548

		3.954216

		3.955884

		3.957552

		3.959214

		3.960882

		3.96255

		3.964218

		3.965886

		3.967548

		3.969216

		3.970884

		3.972552

		3.974214

		3.975882

		3.97755

		3.979218

		3.980886

		3.982548

		3.984216

		3.985884

		3.987552

		3.989214

		3.990882

		3.99255

		3.994218

		3.995886

		3.997548

		3.999216

		4.000884

		4.002552

		4.004214

		4.005882

		4.00755

		4.009218

		4.010886

		4.012548

		4.014216

		4.015884

		4.017552

		4.019214

		4.020882

		4.02255

		4.024218

		4.025886

		4.027548

		4.029216

		4.030884

		4.032552

		4.034214

		4.035882

		4.03755

		4.039218

		4.040886

		4.042548

		4.044216

		4.045884

		4.047552

		4.049214

		4.050882

		4.05255

		4.054218



&L




&C&14TMT Laboratories&10
&9Tension Member Technology
5721 Research Drive
Huntington Beach, CA  92649-1616
714-898-5641    Fax: 714-893-1925
www.tmtlabs.com

Peak Load at Break = 15,300 lbf
Following 10 Cycles to 1,000 lbf
Specimen broke 7.5" from the Nose of the Flanged Socket

Time, minutes

Tension, lbf

Specimen 2949F - #8flanged 
Tension versus Time
Cycle 11
1 Sept 2005

186

190

206

192

209

185

185

218

188

215

211

198

212

187

207

205

185

214

204

180

225

190

201

191

211

212

179

213

206

185

214

191

213

195

198

204

208

224

226

239

239

238

250

277

272

268

274

286

302

312

308

307

308

326

343

344

342

340

355

369

385

377

385

398

399

410

429

418

427

453

448

443

445

491

489

479

484

502

497

495

527

528

524

525

551

547

564

573

559

558

578

591

598

599

603

619

622

636

653

647

643

646

673

667

680

686

704

701

709

729

722

717

730

758

756

752

776

769

765

783

801

810

804

808

833

823

824

858

847

845

877

872

867

883

891

905

896

914

917

920

914

931

930

952

972

959

965

980

997

981

984

1006

1002

1034

1029

1017

1059

1059

1048

1058

1070

1068

1078

1095

1092

1084

1107

1104

1122

1131

1139

1155

1146

1155

1165

1158

1175

1184

1191

1195

1204

1221

1226

1228

1230

1238

1246

1253

1252

1268

1262

1288

1284

1303

1305

1306

1320

1320

1326

1331

1345

1348

1361

1371

1369

1375

1394

1390

1403

1410

1410

1424

1414

1436

1452

1453

1463

1443

1484

1481

1485

1484

1505

1505

1514

1536

1532

1529

1561

1535

1546

1572

1564

1584

1587

1571

1591

1593

1613

1623

1623

1633

1637

1644

1652

1642

1661

1694

1678

1697

1693

1700

1699

1718

1728

1724

1742

1742

1744

1763

1745

1771

1764

1790

1778

1796

1800

1822

1804

1842

1827

1819

1846

1850

1852

1874

1864

1885

1890

1877

1481

1874

1922

1926

1963

1938

1961

1964

1990

1967

1986

2009

1990

2003

2002

2016

2017

2029

2038

2056

2059

2054

2056

2086

2084

2092

2093

2108

2102

2136

2112

2150

2133

2133

2151

2161

2161

2166

2175

2198

2195

2201

2202

2222

2205

2238

2253

2234

2237

2257

2265

2262

2287

2283

2291

2288

2313

2307

2307

2330

2343

2326

2351

2351

2360

2367

2376

2386

2370

2417

2399

2418

2417

2403

2441

2429

2464

2446

2443

2480

2469

2470

2492

2487

2480

2505

2531

2513

2527

2526

2544

2564

2560

2560

2570

2574

2585

2590

2602

2584

2614

2614

2629

2622

2651

2630

2661

2663

2656

2694

2670

2688

2683

2693

2705

2732

2708

2746

2716

2747

2744

2743

2764

2750

2777

2783

2770

2804

2789

2827

2808

2823

2834

2831

2850

2846

2846

2866

2892

2883

2874

2903

2892

2908

2899

2929

2926

2945

2930

2940

2963

2966

2966

2988

2976

2991

2986

3015

2999

3031

3032

3018

3034

3049

3048

3066

3049

3065

3092

3076

3105

3094

3128

3108

3098

3137

3147

3134

3166

3153

3153

3192

3167

3189

3212

3195

3187

3227

3207

3246

3230

3245

3228

3250

3247

3274

3276

3282

3279

3311

3296

3298

3324

3311

3321

3361

3331

3369

3358

3344

3384

3377

3392

3395

3398

3387

3416

3412

3425

3440

3446

3443

3459

3482

3472

3485

3468

3488

3503

3487

3528

3509

3546

3520

3520

3546

3553

3550

3558

3579

3585

3575

3607

3583

3608

3623

3623

3624

3636

3662

3646

3640

3662

3679

3675

3670

3698

3692

3707

3714

3720

3704

3730

3756

3733

3746

3763

3766

3783

3764

3797

3785

3795

3804

3842

3820

3807

3849

3848

3836

3869

3855

3883

3864

3888

3909

3904

3881

3930

3910

3903

3958

3936

3927

3964

3950

3939

3972

3991

3978

4004

3991

4027

4008

4011

4045

4024

4044

4059

4046

4070

4058

4097

4060

4088

4107

4091

4121

4110

4126

4133

4122

4155

4137

4158

4171

4178

4160

4201

4190

4175

4230

4213

4204

4232

4229

4239

4229

4247

4257

4263

4275

4285

4304

4294

4281

4311

4342

4296

4333

4331

4332

4370

4359

4345

4387

4377

4374

4387

4388

4400

4404

4421

4421

4420

4452

4438

4428

4483

4449

4474

4492

4494

4477

4508

4513

4527

4511

4510

4549

4531

4566

4564

4551

4583

4571

4586

4587

4592

4614

4603

4621

4619

4637

4644

4627

4655

4659

4679

4677

4668

4683

4718

4687

4699

4742

4712

4722

4749

4728

4755

4776

4753

4778

4780

4770

4804

4799

4830

4806

4803

4851

4832

4822

4871

4845

4835

4879

4870

4890

4879

4906

4907

4906

4925

4929

4916

4950

4933

4949

4951

4986

4984

4977

4963

5022

4995

4988

5025

5007

5045

5034

5038

5053

5058

5068

5078

5080

5084

5087

5100

5103

5113

5110

5142

5122

5153

5138

5177

5153

5150

5194

5176

5173

5213

5180

5222

5215

5241

5226

5229

5268

5251

5280

5258

5293

5278

5273

5305

5293

5315

5306

5335

5323

5348

5340

5328

5367

5356

5386

5374

5362

5415

5398

5396

5423

5424

5437

5428

5442

5431

5457

5450

5464

5476

5494

5476

5498

5508

5492

5522

5509

5546

5534

5538

5545

5563

5592

5574

5563

5625

5604

5592

5611

5616

5604

5632

5627

5655

5639

5638

5670

5660

5704

5668

5667

5711

5702

5728

5721

5711

5769

5727

5736

5769

5757

5799

5776

5762

5815

5773

5811

5806

5815

5825

5824

5858

5839

5862

5856

5850

5869

5896

5882

5915

5905

5890

5928

5921

5952

5934

5945

5963

5935

5957

5970

5972

6005

5983

5979

6020

6007

6002

6041

6025

6044

6031

6054

6047

6098

6063

6063

6098

6085

6097

6107

6100

6137

6132

6129

6150

6135

6164

6153

6191

6160

6193

6198

6173

6211

6198

6213

6234

6229

6218

6263

6256

6252

6247

6292

6279

6300

6314

6289

6311

6311

6338

6319

6324

6354

6333

6340

6369

6366

6373

6359

6396

6414

6415

6400

6430

6423

6425

6443

6424

6483

6450

6452

6479

6477

6500

6492

6495

6508

6497

6535

6521

6553

6537

6582

6548

6558

6580

6547

6598

6585

6620

6593

6594

6633

6622

6621

6650

6636

6646

6669

6661

6673

6688

6675

6704

6692

6708

6721

6705

6740

6729

6746

6736

6763

6752

6793

6762

6782

6804

6804

6802

6829

6809

6818

6857

6836

6845

6858

6879

6864

6887

6886

6880

6892

6922

6900

6910

6936

6917

6945

6926

6972

6956

6956

6986

6980

6979

7004

6990

7012

7026

7014

7036

7023

7036

7043

7078

7058

7081

7091

7079

7104

7089

7094

7115

7110

7133

7115

7158

7143

7133

7167

7158

7175

7192

7178

7210

7192

7223

7220

7208

7239

7226

7238

7248

7241

7263

7284

7283

7285

7294

7284

7304

7322

7307

7332

7320

7347

7345

7359

7348

7379

7365

7391

7370

7405

7404

7398

7415

7405

7427

7437

7436

7459

7453

7461

7448

7500

7478

7471

7505

7485

7520

7506

7545

7519

7552

7546

7547

7563

7570

7562

7585

7615

7587

7584

7619

7600

7623

7632

7623

7643

7668

7652

7656

7664

7667

7697

7682

7698

7714

7684

7732

7728

7716

7727

7765

7753

7786

7771

7761

7798

7788

7768

7815

7803

7821

7819

7836

7848

7829

7846

7852

7876

7892

7871

7850

7901

7888

7895

7927

7917

7948

7921

7928

7936

7955

7963

7964

7940

8009

7984

7969

8013

8024

8014

8002

8061

8032

8006

8056

8061

8073

8058

8095

8071

8093

8103

8121

8100

8096

8140

8112

8146

8143

8145

8159

8155

8168

8174

8203

8186

8203

8202

8218

8211

8225

8230

8225

8266

8254

8255

8257

8265

8294

8274

8281

8317

8300

8315

8335

8313

8350

8335

8335

8359

8348

8382

8365

8380

8402

8380

8415

8402

8411

8431

8419

8460

8427

8450

8482

8461

8458

8494

8480

8496

8489

8515

8509

8515

8522

8540

8523

8549

8560

8583

8566

8557

8607

8580

8583

8582

8605

8600

8619

8621

8624

8671

8637

8633

8673

8665

8673

8690

8683

8693

8680

8723

8722

8709

8725

8734

8737

8748

8776

8756

8761

8774

8789

8779

8787

8808

8832

8811

8817

8834

8863

8841

8831

8867

8868

8866

8880

8887

8875

8903

8893

8918

8912

8923

8939

8928

8954

8968

8942

8989

8966

8966

9001

9023

8992

9025

9011

9008

9038

9026

9046

9061

9050

9060

9069

9081

9111

9086

9078

9121

9102

9121

9139

9131

9132

9159

9169

9152

9180

9178

9173

9192

9189

9213

9195

9231

9219

9222

9239

9234

9266

9247

9277

9266

9271

9292

9277

9308

9292

9307

9317

9322

9337

9335

9343

9356

9347

9373

9375

9360

9392

9395

9385

9405

9420

9411

9450

9427

9424

9456

9455

9458

9460

9475

9511

9489

9480

9538

9499

9511

9535

9511

9549

9530

9569

9559

9555

9566

9585

9580

9609

9603

9611

9646

9600

9630

9650

9623

9681

9654

9653

9676

9670

9698

9674

9709

9689

9737

9720

9752

9717

9732

9740

9749

9752

9785

9764

9802

9783

9775

9804

9818

9782

9820

9847

9823

9836

9852

9859

9855

9874

9875

9876

9898

9895

9898

9907

9901

9926

9936

9943

9943

9952

9965

9978

9955

9986

10001

10007

10000

10025

10002

10008

10038

10034

10021

10060

10053

10058

10075

10069

10113

10091

10083

10116

10098

10119

10130

10129

10131

10144

10150

10162

10166

10181

10187

10173

10210

10192

10203

10212

10210

10233

10250

10241

10239

10276

10265

10276

10271

10265

10297

10281

10320

10305

10329

10313

10331

10348

10323

10379

10358

10345

10384

10387

10368

10391

10405

10412

10424

10426

10419

10432

10437

10450

10455

10440

10483

10475

10473

10503

10487

10501

10516

10505

10530

10529

10549

10532

10553

10557

10578

10562

10586

10590

10594

10604

10616

10599

10631

10612

10645

10629

10654

10649

10653

10680

10705

10679

10669

10708

10724

10706

10708

10742

10724

10761

10735

10738

10775

10761

10754

10573

10783

10797

10783

10807

10817

10828

10822

10848

10829

10824

10871

10851

10879

10868

10898

10883

10890

10914

10926

10926

10949

10920

10907

10967

10948

10952

10985

10964

10977

11003

10983

11019

11003

10996

11051

11025

11032

11049

11048

11074

11058

11092

11075

11066

11093

11099

11111

11093

11119

11106

11135

11172

11147

11150

11166

11162

11168

11180

11187

11218

11187

11192

11231

11204

11232

11229

11265

11247

11238

11278

11280

11265

11298

11282

11316

11299

11316

11324

11310

11348

11347

11333

11368

11354

11389

11380

11369

11393

11380

11407

11422

11407

11412

11448

11442

11451

11445

11467

11472

11463

11494

11492

11489

11506

11517

11508

11528

11535

11540

11531

11560

11551

11570

11553

11580

11591

11579

11593

11631

11587

11648

11618

11620

11654

11629

11656

11678

11658

11684

11690

11674

11703

11695

11715

11715

11709

11737

11723

11739

11760

11751

11756

11780

11764

11787

11792

11824

11805

11792

11822

11813

11842

11825

11853

11853

11868

11869

11870

11890

11871

11925

11890

11892

11925

11912

11947

11933

11924

11955

11940

11988

11961

11972

11992

12021

11983

12000

12011

12012

12051

12043

12052

12038

12037

12083

12056

12085

12079

12100

12088

12121

12099

12115

12117

12139

12121

12162

12144

12156

12024

12158

12178

12198

12175

12211

12210

12199

12242

12216

12218

12240

12244

12245

12272

12267

12283

12266

12307

12294

12307

12313

12303

12326

12344

12337

12360

12347

12365

12360

12366

12392

12378

12392

12421

12408

12424

12433

12433

12450

12436

12446

12461

12450

12468

12476

12501

12484

12475

12505

12521

12519

12521

12537

12553

12538

12563

12569

12561

12610

12589

12578

12611

12603

12598

12646

12625

12616

12647

12680

12653

12672

12654

12680

12680

12695

12691

12706

12700

12726

12714

12730

12766

12740

12737

12764

12769

12761

12784

12805

12779

12817

12804

12804

12828

12836

12832

12863

12846

12870

12885

12844

12895

12886

12896

12902

12895

12921

12913

12936

12930

12969

12946

12978

12974

12963

13001

12989

12984

13016

13035

13023

13003

13032

13043

13027

13092

13014

13078

13057

13093

13078

13086

13104

13117

13127

13121

13124

13150

13138

13153

13152

13157

13176

13173

13205

13194

13183

13211

13207

13224

13239

13222

13247

13236

13265

13266

13254

13291

13268

13283

13315

13319

13303

13330

13310

13323

13329

13368

13346

13339

13367

13375

13420

13381

13375

13416

13406

13399

13449

13418

13429

13460

13434

13465

13459

13477

13478

13478

13486

13486

13500

13529

13496

13526

13531

13556

13543

13552

13580

13574

13565

13587

13589

13608

13619

13623

13613

13652

13620

13621

13657

13645

13674

13654

13692

13691

13675

13706

13713

13719

13703

13744

13727

13720

13763

13750

13738

13777

13759

13779

13805

13794

13786

13817

13806

13848

13835

13823

13843

13844

13861

13858

13872

13870

13886

13876

13893

13890

13924

13913

13945

13931

13921

13961

13946

13949

13981

13971

13961

13991

14000

13999

13987

14026

14002

14019

14042

14055

14038

14066

14057

14084

14058

14063

14106

14080

14116

14110

14103

14138

14129

14115

14166

14154

14143

14176

14177

14162

14187

14194

14203

14206

14218

14211

14236

14227

14241

14251

14258

14251

14262

14290

14280

14297

14303

14290

14327

14326

14304

14323

14342

14334

14370

14357

14363

14377

14373

14396

14380

14390

14412

14400

14428

14424

14448

14433

14454

14444

14484

14493

14475

14474

14512

14490

14488

14519

14522

14559

14532

14525

14566

14554

14567

14579

14556

14573

14609

14583

14592

14620

14609

14629

14627

14646

14639

14633

14660

14669

14667

14696

14683

14674

14696

14707

14709

14722

14715

14747

14734

14722

14776

14757

14765

14772

14803

14790

14784

14800

14817

14805

14837

14831

14854

14844

14837

14847

14858

14861

14895

14874

14893

14896

14895

14906

14919

14925

14923

14937

14950

14956

14969

14965

14957

14982

14983

15005

14996

15013

15001

15022

15042

15032

15037

15034

15062

15060

15082

15054

15109

15087

15079

15113

15100

15102

15138

15118

15158

15152

15144

15182

15168

15144

15177

15184

15212

15195

15225

15208

15198

15204

15239

15228

15257

15244

15272

15256

15292

15272

15285

15294

15303

15325

15305

14890

15335

7967

5705

2932

2199

2043

2090

1381

1430

1404

1195

1128

1095

1195

1336

1080

1120

1225

1124

1083

1080

1113

1115

945

881

805

901

807

769

714

705

744

638

594

650

633

714

624

578

605

585

598

539

533

515

517

442

423

401

366

375

358

351

349

324

308

324

308

306

307

288

279

270

277

269

210

185

159

138

131

112

104

94

85

82

79

73

71

70

67

66

65

64

66

66

66

65

69

68

70

69

69

68

57

56

58

59

59

56

57

58

56

50

47

44

42

42

43

40

42

40

40

42

43

45

44

44

46

47

44

46

48

47

47

48

47

47

45

46

41

37

33

31

31

31

29

27

27

27

27

27

27

23

20

22

21

21

21

21

17

18

22

20

21

18

20

20

20

18

16

16

16

18

18

18

16

15

17

18

17

15

14

15

16

14

17

14

14

15

18

17

16

15

13

17

14

16

12

12

15

17

16

13

15

13

14

15

15

13

11

15

15

16

17

14

13

13

15

17

15

10

13




