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TECHNICAL DATA SHEET 

TO B009 D5

CORNING SINGLE MODE OPTICAL FIBRE 

FOR SUBMARINE CABLES  

REFERENCE SMF / LS 1 585 for WDM system

( unspliced fiber and low PMD)

( THIS TECHNICAL DATA SHEET COMPLETE THE SPECIFICATION B009 D5 )

	REDACTOR
	CHECKED BY
	APPROBATOR
	APPROBATOR

	J.L LANG
 ASN DT-CSM  Optical transmission  Manager 
	L. WEENS

ASN  

Cable Coordination Manager
	JF. LIBERT
ASN - STI 

  DTCM Manager 
	C.LENGLET
ASN  SACM 

 fibre manager

	
	
	
	


	performances
	limits 
	NORMES

	- Batch 

- Delivery batch

-
	1 000  km

N batch (N ( 1)
	)

)

)

))

	- Mode field diameter at 1 550 nm

   . For individual fiber

   . Length weighted average for a batch


	8.40 -0.50 / +0.30 µm

( 8.1 µm
	)

)

)

) ( refer to  (1))

)

)

	- Fibre Cut-off wavelength (c


	1 050 to 1 650 nm
	)

) ( refer to  (1))

)

	- Dual requirement in MFD and (c
	


	)MFD in µm

)(c in µm

	- Chromatic dispersion (o in vacuum at 20° C:

      (o for individual fiber 

      Slope at o for individual fiber

   . 

       (o length weighted for a batch

      Slope at  length weighted for a batch

 
	1 585 ( 10  nm

0.060  to  0.080  ps/nm²/km 

1585 ( 1nm

0.066 ( X ( 0.074 ps/nm²/km

X ( 0.070ps/ nm2 /km


	)

)

)

)

)

) ( refer to  (1))

)

)

)

)

	- Polarisation Mode Dispersion at 1550nm:

     for individual fibre

     for each delivery batch

     
	( 0.15 ps/(km

( 0.08 ps/(km


	l

( refer to  (1))

length weighted quadratic average



	- Attenuation at 1 560 nm:

     -  for Individual fiber

     -  Length weighted average for a batch


	( 0.220 dB / km

( 0.203 dB / km


	) 

)

) ( refer to  (1)

)


	- Mini fiber length

- Average fiber length per batch 


	5 km

( 15 km
	)

)

)

)

	- Proof test


	( 1.8 % for 1 s or equivalent
	)

) ( refer to  (1))

)


Temperature test 23 ( 5°C 

(1) following the methods defined in the G650 and G655 

FORMAT FOR DATA SUBMISSION

The following detail the format of the data which shall be delivered with each fibre delivery.

Each field shall be TAB or COMMA delimited.

	
	REFERENCE
	NUMBER OF CHAR.
	OBSERVATIONS

	A
	Mode flag
	X
	S for singlemode

	f
	Template ID
	XXXXXXXX
	DLELSSB1

	B
	Fiber ID
	12
	

	C
	Shipment date
	YYYYMMDD
	

	D
	Corning order number
	12
	

	E
	Shipment item number
	XXXX
	

	F
	Corning product descr (glass)
	20
	SMF- LS

	f
	Corning product descr (coating)
	10
	CPC6

	G
	Color
	3
	NAT

	g
	Actual length
	XXXXXXX
	In meters

	H
	Att. loss at 1 540 nm
	X.XXX
	In dB / km

	I
	Att. loss at 1 550 nm
	X.XXX
	In dB / km

	J
	Att. loss at 1 560 nm
	X.XXX
	In dB / km

	j
	Max attenuation 1475-1600
	-XX.XX
	

	K
	MFD at 1 550 nm OSE
	XX.XX
	In mic

	L
	Fiber cutoff
	XXXX
	In nm

	M
	Cable cutoff
	XXXX
	In nm

	N
	Clad diameter
	XXX.X
	In mic

	O
	Clad non circularity
	X.X
	In %

	P
	Core/Clad concentricity
	X.X
	In mic

	Q
	Coating diameter
	XXX
	In mic

	R
	Zero dispersion slope
	X.XXX
	In ps / nm²/km

	S
	Zero dispersion wavelength
	XXXX.X
	In nm

	T
	Dispersion @ 1 530 nm
	X.X
	Including the sign in ps / nm.km

	t
	Dispersion @ 1 550 nm
	X.X
	Including the sign in ps / nm.km

	U
	Dispersion @ 1 560 nm
	X.X
	Including the sign in ps / nm.km

	V
	Box number
	XXXXX
	

	W
	Customer order number
	20
	

	X
	Customer part number
	25
	

	Y
	Ordered proof test
	XXXX
	kpsi

	Z
	Ordered atten 1550nm
	X.XX
	

	a
	Orderd atten 1310nm
	-X.XX
	

	b
	PMD at 1 550 nm
	X.XX
	In ps / (km

	c
	MFD at 1550 nm ISE
	XX.XX
	In mic


EDITIONS  SUCCESSIVES

CONSTITUTION  DU  DOSSIER  -  MODIFICATIONS

	Edition
	Date
	Position des modifications
	Motif de la mise à jour
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FICHE DE DIFFUSION CONTROLEE


Le  Document                    B 009 D5D - ISSUE 1

- sera disponible à partir du :

. :  10 Mars 1999


SERA OPERATIONNEL A PARTIR DU    :         12 mars 99


Il est à votre disposition au SQ-CSM en échange d'une signature et des exemplaires de l'ancienne édition (si celui-ci existe) voir QA O5.OO. 

- BUREAU DES OPERATIONS
Mme DEMAZEUX.
N° 6



Nombre d'emplaire reçu (1 )

- SYSTEMES
Mr. BOUCHEZ
N° 7 



Nombre d'exemplaire  reçu (1)

- AFFAIRES
Mme MULARD
N° 8  



Nombre d'exemplaire reçu  (1)

- QUALITE
Mme DEWITTE
N° 9



Nombre d'exemplaire reçu  (2 )

- Direction TECHNIQUE
Mme HERNAULT
N° 10 


Nombre d'exemplaire reçu  (2 )

- S A C M 
Mme JOAN

N° 16 


Nombre d'exemplaire reçu  (2) + 3 non contrôlés

- PORTLAND
Duane PRATT  - 1 E-Mail + 1 Contrôlé

- VILLARCEAUX
Mr. BRZOZOWSKI   1 E-Mail + 1 Contrôlé

- BOTANY
Sylvain KERSHAW    1 E-Mail + 1 Contrôlé



S Q C - Gestion documents : le 12/05/04
ASN Proprietary – Not  to be disclosed , duplicated or used without prior written permission of Alcatel
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