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Glass Type: Borosiicate

Description

Duran® 8330 glass is manufactured by Schott Glass. Ifs 3 chemically
‘and thermally highly resistant borosilicate glass available in tubes,
capilaries, and rods. It comes standard in many sizes and is frequently
used in place of Coming Pyrex® 7740 material. SGP can cut, shapes,
centerless grind, and hot work Duran material in many sizes and shapes,

Thermal P

‘Thermal Coefiicient of Expansion  (0/300°C) 33X 10 7/°C

Annealing Point §60°C11040 °F
Softening Point 825°C11817°F
‘Strain Point §25°C1977F

Density 223giem®
Knoop Hardness NA
Young's Modulus NA
Poisson's Ratio 020

Optical Properti

Refractive Index 1473

(Click Here for Optical Transmission Chart)

Chemical Pr

Hydrolytic Resistance dass 1

Acid Resistance dass 1

Alkali Resistance dass2
trical Properti

Dielectric Constant 46

Resistivty A

Dielectric Strength A
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