1. Part number: 10020895-MOB2  
2. Revision: Rev0, initial release
3. Contact information: Denis Klimov, MBARI, 7700 Sandholdt Rd, Moss Landing, CA 95039;    
a. Phone: 831-775-1914, 
b. After hours: 831-235-6515
c. Email: Klimov@mbari.org
4. Dimensions: 3.000”x 6.000” with 6 mounting holes - see drawing 2nd page.
5. Material:  FR4 0.062” thick

6. Trace width/Space: 0.010”/0.007”

7. Smallest hole size: 0.014”

8. Copper Layers: 4 layers, Top, Ground, Power, Bottom
9. Plating: Hot Air Solder Level (HASL), Leaded

10. Copper weight: 1oz (outer), 0.5 oz (inner)
11. Solder Mask: Solder Mask Top (Green), Solder Mask Bottom (Green)
12. Legend:  1 layer Silk Screen Top (White).

13. Holes plating: all holes plated thru

14.  Boards to be panelized 2-up (2 per panel), with standard rail (0.5”), scoring edge-to-edge
Table 1. Layers position in the board (also indicated in right upper part of the board)/ ORCAD CONVENTION
	Layer number
	Extended Gerber Filename
	Layer position, type, name
	Layer function

	1
	*.SST
	Silk Screen Top
	Annotation layer

	2
	*.SMT
	Solder Mask Top
	Solder mask

	3
	*.TOP
	Top Layer 
	Routing layer

	4
	*.GND
	Ground Layer
	Plane Layer

	5
	*.PWR
	Power layer
	Plane Layer

	6
	*.BOT
	Bottom Layer
	Routing layer

	7
	*.SMB
	Solder mask Bottom
	Solder mask

	
	
	
	

	
	
	
	


Table 2. Other files included (ORCAD 16 CONVENTION):

	*.DRD
	Drill file

	*.FAB
	Fabrication file with dimensions

	THRUHOLE.tap
	Drill file. 

	*.DTS
	Drill Tape Summary Report

	*.GTD
	Gerber Design File

	*.LIS
	Post processor report

	*.SPT
	Solder Paste Top

	
	


Total: 15 files, including Read_me.doc file

Mechanical Drawing
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Solder paste layer
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