## Slide 1: Optical Dome Reliability Analysis Monterey Bay Aquarium Research Institute (MBARI)
Eric H. Baker
Connecticut Reserve Technologies, Inc.
October 2016
PRELIMINARY ANALYSIS: Provided for demonstration of progress. Not intended to be a complete or final analysis.

## Slide 2: Outline
Perform Brittle Material Reliability Predictions on the Deep Water Camera Port of MBARI’s Autonomous Underwater Vehicle (AUV)
Acquire Dome and Dome Support geometry from MBARI
Generate finite element analyses of 3 Dome Configurations and calibrate models to MBARI FEA as well as Pressure Test Measurements
Estimate Weibull Material Properties from provided specimen failure data
Apply the Ceramics Analysis and Reliability Evaluation of Structures (CARES) program to predict the Brittle Material Reliability of the Dome Configurations
Establish a Proof Test Protocol to improve the Reliability
8/2/16

## Slide 3: CARES with ABAQUS Flowchart
8/15/16
CARES predicts the brittle material reliability of a component by post-processing finite element analysis stress results.
CARES requires region based Weibull material properties, Volume and/or Surface, where different Surface conditions are characterized by different parameter sets.

## Slide 4: Dome Configurations
8/2/16
#2
#3
#1
Kapton
0.005”
Kapton
0.020”
Groove
Added Bevel
Dome Restricted from Moving Radially
Dome Free to Move Radially
Dome Free to Move Radially
Dome
Support

## Slide 5: Boundary Conditions
Pressure
BC Axial: Fixed
Radial: Free
7/27/16
Per MBARI

## Slide 6: Material Properties: Mechanical
10/14/16
Configuration #3 Resin vs. Epoxy Material Trade-study
Configuration #3 Dome Support Material Trade-study

## Slide 7: Material Properties: Weibull
WeibPar (Weibull parameter estimation program) is used for the WM and WCS calculations of the failure specimen data as well as calculating the Effective Area from a FEA of the R-o-R specimen
9/22/16
2D Axisymmetric Model of the Ring-on-Ring Specimen
WM = 13.6 [-]
Aeff = 0.229 [in^2]
WCS = 22,714 [psi]
WSP = 20,386 [psi*in^(2/13.6)]
Ground Inert
Where WM & WSP are used in CARES
Flaws were all assumed to originate on the Surface of the Failure Specimens
Weibull Characteristic Strength (WCS)
Weibull Modulus (WM)
Weibull Material Scale Parameter (WSP)
Weibull Effective Area (Aeff)

## Slide 8: Material Properties: Weibull – Ground, Inert
9/22/16
Censor Outlier
# of Specimens 19 & 1
WM 13.628
WCS 156.6 MPa (22.71 ksi)
Includes Potential Outlier
# of Specimens 20
WM 11.375
WCS 155.0 MPa (22.48 ksi)
Censored
Excludes Outlier
# of Specimens 19
WM 13.626 [-]
WCS 22,714 [psi]
Aeff 0.229 [in^2]
WSP 20,386 [psi*in^(2/13.626)]
Outlier ?
MLE2B Estimation
90% Confidence Bounds

## Slide 9: Material Properties: Time Dependent (SCG) – Ground
9/20/16
Ground in Water
Time Dependent (SCG)
# of Specimens 26
WM 13.626 [-]
WSP 20,386 [psi*in^(2/13.63)]
N 14.7413 [-]
D 7,648 [psi]
WM2 15.765 [-]
Aeff 0.2197 [in^2]
B_Dynamic 36,437 [psi^2*sec]
B_Static 2,315 [psi^2*sec]
LIN2 Estimation

## Slide 10: Material Properties: Weibull – Polished, Inert
9/22/16
Polished Inert
# of Specimens 19
WM 4.346 [-]
WCS 47,304 [psi]
Aeff 0.353 [in^2]
WSP 37,235 [psi*in^(2/4.346)]
MLE2B Estimation
90% Confidence Bounds
low

## Slide 11: Material Properties: Time Dependent (SCG) – Polished
9/22/16
Polished (Water)
Time Dependent (SCG)
# of Specimens 0 (simulated)
WM 4.346 [-]
WSP 37,235 [psi*in^(2/4.346)]
N 14.74 [-]
D 14,310 [psi]
WM2 5.028 [-]
Aeff 0.3311 [in^2]
B_Dynamic 109,202 [psi^2*sec]
B_Static 6,938 [psi^2*sec]
LIN2 Estimation
Simulated from Ground

## Slide 12
Dome Configuration #3
Design
7/27/16
Titanium Ring prevents Radial Displacement of Dome

## Slide 13: Dome Configuration #3
10/14/16
Dome
H-K9L
Dome Support
Actual: Ti-6Al-4V
Test: 6061-T6
Trade Study
Resin or Epoxy
0.030”
Dome Coupler Ring
Ti-6Al-4V
Frictionless
Kapton 0.020”
Bonded
Axial = fixed
Radial = free
Model v15

## Slide 14: Dome Configuration #3
10/14/16
Load Step #4 includes DT and 2750 psi
Resin/Epoxy and Kapton Parts Hidden
Frictionless: Dome-2-Kapton, Ring-2-Resin
All the Rest Tied
Resin Model
Epoxy Model
Tensile Stresses
Compressive Stresses
Model v15
Resin vs. Epoxy Trade Study

## Slide 15: Dome Configuration #3
Load Steps
Resin allows more Radial Displacement than Epoxy
Greater Radial Displacement leads to Greater Hoop and Tangential Stresses (and therefore Max Principal Stresses)
10/14/16
Displacements
Maximum Principal Stress
Model v15
Max Stress found anywhere in Dome
Resin vs. Epoxy Trade Study
Axial @ Dome Center
Radial @ Dome Rim

## Slide 16: Dome Configuration #3
10/17/16
Model v15
CARES Output Example
2750 psi for 60 hrs
One Ground
Polished
Polished
Counterclockwise from Dome Inner to Dome Outer
Overall Reliability
Max Stress
Lowest Individual Surface Reliability
Epoxy Model

## Slide 17: Dome Configuration #3
10/17/16
Model v15
Resin Model
Epoxy Model
FEA Stress Solution @ 2750 psi
Assumes Stresses Scale Linearly with Pressure
Assumes other parts of Assembly can handle the increased Applied Pressure
Resin vs. Epoxy Trade Study
Reliability as a Function of Service Pressure
where Service Time is 60 hrs.

## Slide 18: Dome Configuration #3
10/17/16
Model v15
Resin Model
Epoxy Model
Reliability as a Function of Service Time
@ Applied Pressure 2750 psi
60 hrs.
Pf = 0.73%
Resin vs. Epoxy Trade Study

## Slide 19: Dome Configuration #3
10/17/16
Model v15
Epoxy Model
60 hrs. Service @ 2750 psi
with no Proof Test
Pf = 0.73%
Failure Rate = 1 out of 137
60 hrs. Service @ 2750 psi
with 10 sec Proof Test @ 4950 psi
Pf = 0.33%
Failure Rate = 1 out of 306
Risk of Failing the 10 sec Proof Test @ 4950 psi
Pf = 0.47%
Failure Rate = 1 out of 214
FEA Stress Solution @ 2750 psi
Assumes Stresses Scale Linearly with Pressure
Assumes other parts of Assembly can handle the increased Applied Pressure
Base Ground / Rest Polished
Proof Test