## Slide 1: Optical Dome Reliability Analysis Monterey Bay Aquarium Research Institute (MBARI)
Eric H. Baker
Connecticut Reserve Technologies, Inc.
August 2016
PRELIMINARY ANALYSIS: Provided for demonstration of progress. Not intended to be a complete or final analysis.

## Slide 2: Outline
Perform Brittle Material Reliability Predictions on the Deep Water Camera Port of MBARI’s Autonomous Underwater Vehicle (AUV)
Acquire Dome and Dome Support geometry from MBARI
Generate finite element analyses of 3 Dome Configurations and calibrate models to MBARI FEA as well as Pressure Test Measurements
  Challenge: Coefficient of Friction of Kapton Gasket unknown
Estimate Weibull Material Properties from provided specimen failure data
Establish a Proof Test Protocol to improve the Reliability
8/2/16

## Slide 3: CARES with ABAQUS Flowchart
8/15/16
CARES predicts the brittle material reliability of a component by post-processing finite element analysis stress results.
CARES requires region based Weibull material properties, Volume and/or Surface, where different Surface conditions are characterized by different parameter sets.

## Slide 4: Dome Configurations
8/2/16
#2
#3
#1
Kapton
0.005”
Kapton
0.020”
Groove
Added Bevel
Dome Restricted from Moving Radially
Dome Free to Move Radially
Dome Free to Move Radially
Dome
Support

## Slide 5: Boundary Conditions
Pressure
BC Axial: Fixed
Radial: Free
7/27/16
Per MBARI

## Slide 6: Material Properties
Weibull
Mechanical
8/5/16
Configuration #3 Dome Support Material Trade-study
Values needed
Waiting for Material Testing…

## Slide 7
Dome Configuration #1

## Slide 8
Dome Configuration #1
Failure During External Pressure Test 2,750 psi
Design
7/27/16
Kapton
0.005”
Dome Free to Move Radially
Dome
Support

## Slide 9: 2D Axisymmetric Model: Configuration #1
External Pressure Load
Mesh
8/2/16
Partition Line for Mesh
Dome
Support
BC: Radial = free, Axial = fixed
Configuration #1
Kapton
Dome is free to move Radially

## Slide 10: Dome Mesh Refinements on Bevels
7/28/16
Dome
Support
Kapton 0.005”
Configuration #1
Analyses will study Bonded and Frictionless Interfaces between Dome and Kapton
Bevels

## Slide 11: Displacements: External Pressure 2,750 psi
Dome-2-Kapton – Frictionless
Kapton-2-Support – Bonded
Dome-2-Kapton – Bonded
Kapton-2-Support – Bonded
Configuration #1 @ 2750 psi
0.0134 in
0.0095 in
8/2/16
Deformation Scale: 20x
v07

## Slide 12: Maximum Principal Stress & Volume Reliability (example)
Dome-2-Kapton – Frictionless
Kapton-2-Support – Bonded
Dome-2-Kapton – Bonded
Kapton-2-Support – Bonded
11,090 psi
2,183 psi
Configuration #1 @ 2750 psi
8/15/16
v07

## Slide 13: Solidworks FEA (provided results)
Pressure: unknown Coefficient of Friction: 0.5 (arbitrary)
8/5/16
von Mises Stress
Scale: 0 to 15 ksi
Displacement
Scale: 0.006 to 0.218 mm
0.00024 to 0.0086 in
Geometry Different!
Can not compare to ABAQUS
Solidworks
ABAQUS
Solidworks

## Slide 14
Dome Configuration #2

## Slide 15
Dome Configuration #2
Failure During External Pressure Test
Design
7/27/16
Added Groove to Support

## Slide 16: Displacements: External Pressure 2,750 psi
Dome-2-Kapton – Frictionless
Kapton-2-Support – Bonded
Dome-2-Kapton – Bonded
Kapton-2-Support – Bonded
Configuration #2 @ 2750 psi
0.0196 in
0.0124 in
8/15/16
Deformation Scale: 5x
v08

## Slide 17: Maximum Principal Stress & Volume Reliability (example)
Dome-2-Kapton – Frictionless
Kapton-2-Support – Bonded
Dome-2-Kapton – Bonded
Kapton-2-Support – Bonded
20,050 psi
1,260 psi
Configuration #2 @ 2750 psi
8/15/16
v08

## Slide 18
Dome Configuration #3

## Slide 19
Dome Configuration #3
External Pressure Test:
to be performed
Design
7/27/16
Titanium Ring prevents Radial Displacement of Dome

## Slide 20: Dome Configuration #3
8/5/16
Dome
H-K9L
Dome Support
Actual: Ti-6Al-4V
Test: 6061-T6
Resin 0.030”
Crystal Clear #200
Dome Coupler Ring
Ti-6Al-4V
Frictionless – free to separate
Kapton 0.020”
bonded
Axial = fixed
Radial = free

## Slide 21: Displacements: External Pressure 2,750 psi
Titanium Coupler Ring
Configuration #3 @ 2750 psi
0.0138 in
0.0131 in
8/15/16
Deformation Scale: 1x
v10
Aluminum Coupler Ring

## Slide 22: Maximum Principal Stress & Volume Reliability (example)
7,617 psi
7,778 psi
Configuration #3 @ 2750 psi
8/15/16
v10
Titanium Dome Support
Aluminum Dome Support

## Slide 23: Dome Support Material Trade Study
8/5/16
Dome Support
Ti-6Al-4V
Dome Support
6061-T6
55.10 ksi > 40 ksi (yield)
55.97 ksi < 120 ksi (yield)

## Slide 24: Dome Support – Aluminum
8/5/16
Colors Scaled 40 ksi to 55.1 ksi
Dome (glass) stresses are very similar whether the Support is Titanium or Aluminum.
A very small region of the Aluminum Support exceeds the Aluminum yield strength – potentially due to the Boundary Condition

## Slide 25: Dome Configuration #3 Test Measurment
8/25/16
Based on Chart 1500 psi would be ~0.0062” displacement …
REF: DescriptionOfPressureTestsOfDomePort.docx

## Slide 26
RESULTS

## Slide 27: COMPARSION of FEA’s & Test Measurements
8/25/16
Read from Chart – different than text…

## Slide 28: SUMMARY OF RESULTS
Arbitrary Weibull Parameters
10 & 9,000
8/25/16
PRELIMINARY

## Slide 29
BACKUP

## Slide 30: Local Coordinate System
Local Coordinate System
Global X-direction Stresses
Normal (Radial) Stresses
Tangential Stresses
Configuration #1
7/27/16

## Slide 31
8/5/16