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The dome of the I2map camera housing must be maintained carefully so that the optical quality does not degrade over time. The coating on the glass can easily be damaged. Below are some recommendations:

· To clean the dome, spray with optical cleaner (e.g. Purosol) and wipe gently with polyester wipes (e.g. mcmaster #98465T61). Then pat dry with kimwipes. Avoid using kimwipes to wipe the dome as they are slightly abrasive.

· Do not clean the dome unless necessary. Check that the dome is clean before every dive but only clean it if it’s dirty.

· Never wipe the dome when it’s dry. Small particles on the lens or the wipe will scratch the coating.

· Do not let water dry on the dome (after a dive, after going in the test tank, after rinsing with freshwater). Seawater and tap water will leave a mineral deposit that cannot be removed without damaging the coating. Rinse the dome with distilled or RO filtered water (available in the wet lab on the boat). If no RO water is available, use tap water and pat dry with kimwipes.

· Always keep a cover on the dome.

· [bookmark: _GoBack]When deploying the AUV, make sure deckhands are aware of the dome (one could easily put dirty fingers on the dome when handling the AUV).
