

Recommendations from Glenn McDonald (WHOI) during meeting at WHOI in May 2015.
High stresses in the glass should be centered. Avoid higher stress near edge.
Machine seat of glass at an angle, have the seat inspected and measure using a FARO arm, and machine the titanium seat to match.
Fluoride etch the base of the glass.
[bookmark: _GoBack]Use sapphire (hard to find in large sizes).
When doing the FEA, use the first principle stress. It makes it easier to stress tension in the glass, which is usually the reason for facture.



Recommendations from optical technician at Myriad Imaging to clean the glass
First, use lens cleaner (Purosol). Use berkshire clean room wipes and swabs for wiping
After dive, rinse lens with RO water, then pat dry. Never let water dry on a lens.
Never wipe a lens dry
Use .3 micron filter on compressed air and nitrogen.
Use nitrogen for last blow off (cleaner, heavier)
For last cleaning, use acetone with queue tip


