## Slide 1
Design and testing of a large sub-hemispherical glass port for a deep-sea camera
Francois Cazenave1; Eric H. Baker2
Nathan D. Card3; George D. Quinn4
Paul Remijan5; Jonathan Salem6
Arun K. Varshneya3
1. Monterey Bay Aquariun Research Institute, Moss Landing, CA
2. Connecticut Reserve Technologies, Gates Mills, OH
3. Saxon Glass technologies, Alfred, NY
4. National institute of Standard and Technology, Gaithersburg, MD
5. Fathom Imaging Inc., Brimfield, MA
6. NASA Glenn Research Center, Cleveland, OH

## Slide 2: Outline
Introduction
  Optical design
Experimental procedure
  Early design and failure
  Fractography
  Modified design
  Chemical strengthening
Testing and reliability analysis
  Glass testing procedure and results
  Reliability analysis
  Proof testing
Conclusion

## Slide 3: Introduction
  MBARI operates an autonomous underwater vehicle to carry out video surveys in Monterey Bay from 50m to 1500m depth.
  A new camera system was designed with the goal of achieving the highest image quality.
  A glass dome port was designed, built and tested.
Notes: The dome can be see in the front of the vehicle, protected by a black plastic shield.
The 4 appendages near the front are LED lights.

## Slide 4: Optical design
  Typical camera dome port
  Shape is optimized to resist hydrostatic pressure
  Small diameter (<200mm)
  Hemispherical shape
  Even and easy to predict stress and strain.
  High distortion
  BK-7 glass
  New camera dome port
  Shape is optimized for high optical quality
  Large diameter (250mm)
  Flattened hemispherical shape
  Uneven and hard to predict stress and strain.
  H-K9L glass (Chinese equivalent to BK-7)

## Slide 5: Early design of dome
Dome sits on kapton gasket
Dome is held with plastic retainer.
O-ring around dome

## Slide 6: FEA of early design: 2D Axisymmetric Model
External Pressure Load
8/2/16
Glass dome
Titanium support
BC: Radial = free, Axial = fixed
Kapton gasket
Dome is free to move Radially

## Slide 7: FEA results at 2750 PSI
Displacements
First principal (max tensile) Stress
11,090 psi

## Slide 8: Failure of early design
Two domes failed during external pressure test:
The first dome failed after numerous cycles to 2750 PSI.
The second dome failed at 800PSI during first pressure cycle.
Notes: The second dome failed at much lower pressure because the dome support was modified in a way that made things even worse. It was a design mistake basically. We could omit the second dome altogether for the sake of clarity if needed.

## Slide 9
The first generation domes were fractographically analyzed by G. Quinn
using a WILD stereo optical microscope with a digital camera.
(Blue tape with small paper inserts between the fracture surfaces held the pieces together during shipment.)
Notes: Notes for Francois
This slide shows the two broken domes.
It also is summarizes the experimental procedure.

## Slide 10
The fractographic analysis included study of the
crack patterns and the fracture surfaces.
How to look
Patterns of breakage
What to look for and how to interpret it.

## Slide 11
The directions of crack propagation were then marked on the assembly.
There were 4 crack systems. All 4 had the same type origins and same stresses driving them.
Fractographic analysis Dome 1
1
2
3
4

## Slide 12
All four origins were contact crack damage at the outer rim area.
Origin 4 was the first to start the overall fracture.
All flaws and initial crack propagation were driven by circumferential hoop tensile stresses.
By the time the cracks propagated towards the middle, the stress changed to bending with tension on the inner dome surface. This suggest that the external pressure caused “splaying” of the dome.
There were no fracture mirror boundary features, nor did any of the cracks branch. This means tensile stresses were low,
less than 1,500 psi = 10 MPa.
Fractographic analysis Dome 1
4
1
2
3

## Slide 13
2 views with different lighting at same magnification
The origin is a contact damage crack on the bottom ground surface.
It is about 1 mm in from the unbeveled edge.
Fractographic analysis Dome 1
Example: One of the rim contact damage cracks
Fracture surface
Fracture surface
Dome ground base
Dome ground base
Inner dome surface
Inner dome surface

## Slide 14
This dome broke at a higher stress.
This caused more extensive crack branching.
There was only one origin site, on the right side. It was a bevel grinding crack.
Origin
Fractographic analysis Dome 2

## Slide 15
Ground
outer
surface
Polished base
Fractographic analysis Dome 2
A fracture mechanics analysis of the flaw itself indicated the stress at fracture was: 39 to 46 MPa (5,600 to 6,600 psi).
A fracture mirror size analysis gave estimates of:
40 to 47 MPa (5,000 to 6,800 psi).
These estimates match.
Grinding crack at the outer bevel.

## Slide 16: Modified design
Dome was bonded to titanium ring with epoxy to prevent lateral motion of dome seat
Edges were beveled and polished
Seat was polished and flatness tolerance was decreased
Thicker kapton ring
Dome Support
Ti-6Al-4V
Dome Coupler Ring
Ti-6Al-4V

## Slide 17: FEA of Modified design
Axial displacement unchanged
Tensile stress reduced 30%
Axial displacement at 2750 PSI
Max = 0.013”
First principal stress at 2750 PSI
Max = 7779 PSI (30% decrease)
Notes: There is a 30% decrease in tensile stress compared to the first design

## Slide 18
Chemical Strengthening of glass
How it works:
Original surface
Surface in compression
Na+ (0.95 Å)
K+ (1.33 Å)
Submerge in a bath of molten KNO3
Ion Size
*Not drawn to scale, demonstration only
Notes: Transition: In addition making modification to the design, we hired Saxon G. T. to strengthen the domes.

## Slide 19
C = concentration of the invading ion
H = plate width ; d = case-depth = DOL
E = Young’s modulus; n = Poisson’s ratio
B = linear network dilation coefficient ( = “Cooper Coefficient”)
In-plane stresses
The Math…
= CS
perpendicular stress

## Slide 20
Glass composition and physical properties
Type: H-K9L (similar to Schott BK7)
Nominal composition (wt%):
69.13 SiO2; 10.75 B2O3;3.07 CaO; 10.40 Na2O; 6.29 K2O; 0.36 As2O3
Density = 2.55 g/cm3
Tg = 550°C
TEC = 70x10-7/°C
E = 71.GPa
n = 0.219
nd = 1.523

## Slide 21
Four domes
15 witness disk samples 2” dia x 2 mm thick,
(for subsequent biaxial testing and CS/DOL measurement)
Hold domes in a stainless steel wire cage
Immerse in electrically heated steel tank containing molten KNO3 salt.
Ion exchange at 450 °C for 24 hrs.
After extraction, carefully cool, wash and dry.
Compression layer (case depth “DOL”) = 45 m.
Compression (“CS”) = - 430 MPa
(measured by FSM-6000LE)
Chemical strengthening of the domes

## Slide 22
Fracture strength, slow crack growth parameters and fracture toughness are needed for the reliability analysis but are not published by the manufacturers.
MBARI hired Jon Salem to measure these parameters for BK-& and HK-9L (HK-9L is marketed as equal to BK7 but is much cheaper)
Chemically strengthened BK7 and HK-9L were also tested.
Ring-on-ring and four-point bar tests were performed in accordance with ASTM International test methods on a large number of samples
Material testing

## Slide 23
Results: Comparison of plain and strengthened glass

## Slide 24
Results: crack growth behavior
Crack velocity as a function of stress intensity.
BK7 and HK-9L exhibit similar crack growth behavior.

## Slide 25: Reliability analysis
MBARI hired Eric Baker of Connecticut Reserve Technology to perform brittle material reliability predictions on the camera port:
Generated finite element analyses of dome configurations and calibrated models to MBARI FEA as well as pressure test measurements
Estimated Weibull Material Properties from provided test data using WeibPar program
Applied the Ceramics Analysis and Reliability Evaluation of Structures (CARES) program to predict the brittle material reliability of the dome configurations
Established a proof test protocol to improve the reliability
This analysis was performed for unstrengthened and strengthened glass.

## Slide 26: CARES with ABAQUS Flowchart
CARES predicts the brittle material reliability of a component by post-processing finite element analysis stress results.
CARES requires region based Weibull material properties, Volume and/or Surface, where different Surface conditions are characterized by different parameter sets.
Notes: ABAQUS is FEA software.

## Slide 27: Material Properties: Weibull
WeibPar (Weibull parameter estimation program) is used for the WM and WCS calculations of the failure specimen data as well as calculating the Effective Area from a FEA of the R-o-R specimen
2D Axisymmetric Model of the Ring-on-Ring Specimen
m = 13.6 [-]
AE = 0.229 [in2]
σ̑­­θ= 22,714 [psi]
σ̑­­o = 20,386 [psi*in^(2/13.6)]
Ground Inert
Where m & σ̑­­o are used in CARES
Flaws were all assumed to originate on the Surface of the Failure Specimens
Weibull Characteristic Strength (σ̑­­θ)
Weibull Modulus (m)
Weibull Material Scale Parameter (σ̑­­o)
Weibull Effective Area (AE)
m = Weibull Modulus
σ̑­­θ = Weibull Characteristic Strength
AE = Weibull Effective Area
σ̑­­o = Weibull Material Scale Parameter

## Slide 28: Material Properties: Weibull – Inert
Strengthened Inert
# of Specimens 15
m 8.460 [-]
σ̑­­θ 111,565 [psi]
AE 1.2122 [in^2]
σ̑­­o 114,132 [psi*in^(2/8.460)]
MLE2B Estimation
90% Confidence Bounds
Polished Inert
# of Specimens 19
m 4.346 [-]
σ̑­­θ 47,304 [psi]
AE 0.353 [in^2]
σ̑­­o 37,235 [psi*in^(2/4.346)]
m = Weibull Modulus
σ̑­­θ = Weibull Characteristic Strength
AE = Weibull Effective Area
σ̑­­o = Weibull Material Scale Parameter
Notes: WM = weibull modulus
WCS = Weibull Characteristic Strength
WSP = Weibull Material Scale Parameter

## Slide 29: Material Properties: Time Dependent (SCG) – Polished
Strengthened (Water)
Time Dependent (SCG)
# of Specimens 0 (simulated)
m 8.460 [-]
σ̑­­o 114,132 [psi*in^(2/8.460)]
N 14.74 [-]
D 29,620 [psi]
WM2 9.788 [-]
AE 1.1558 [in^2]
B_Dynamic 122,443 [psi^2*sec]
B_Static 7,778 [psi^2*sec]
LIN2 Estimation
Simulated from Ground
Polished (Water)
Time Dependent (SCG)
# of Specimens 0 (simulated)
m 4.346 [-]
σ̑­­o 37,235 [psi*in^(2/4.346)]
N 14.74 [-]
D 14,310 [psi]
WM2 5.028 [-]
AE 0.3311 [in^2]
B_Dynamic 109,202 [psi^2*sec]
B_Static 6,938 [psi^2*sec]
Simulated from Ground
Notes: SCG: slow crack growth

## Slide 30: Example of CARES output Unstrengthened H-K9L glass
Pressure: 2750 psi
Duration: 60 hrs
One Ground
Polished
Polished
Counterclockwise from Dome Inner to Dome Outer
Overall Reliability
Max Stress
Lowest Individual Surface Reliability
Notes: Numbers 201 to 207 represent the different surfaces of the domes (inside, outside, 3 edge beveled, base, and perimeter)

## Slide 31
Reliability as a Function of Service Pressure
where Service Time is 60 hrs.
FEA Stress Solution @ 2750 psi
Assumes Stresses Scale Linearly with Pressure
Assumes other parts of Assembly can handle the increased Applied Pressure
Reliability as a Function of Service Time
@ Applied Pressure 2750 psi
Example of CARES output Unstrengthened H-K9L glass
Chart: Pressure (psi)
| 550 | 1100 | 1650 | 2200 | 2750 | 3300 | 3849.9999999999995 | 4400 | 4950 | 5500 | 6050.0000000000009 | 6600 | 7150 | 7699.9999999999991 | 8250
All Polished | 1 | 0.99992 | 0.99941 | 0.9975 | 0.99235 | 0.98098 | 0.95917 | 0.92166 | 0.86287 | 0.7784 | 0.66728 | 0.53441 | 0.39177 | 0.2566 | 0.14598
Chart: Time (hrs)
| 2.7777777777777776E-7 | 2.7777777777777779E-6 | 2.7777777777777779E-5 | 2.7777777777777778E-4 | 2.7777777777777779E-3 | 2.7777777777777776E-2 | 0.27777777777777779 | 2.7777777777777777 | 8.3333333333333339 | 13.888888888888889 | 27.777777777777779 | 60 | 111.11111111111111 | 277.77777777777777 | 416.66666666666669 | 833.33333333333337
All Polished | 1.6352e-05 | 2.5935e-05 | 5.3427e-05 | 0.00011635 | 0.00025501 | 0.00055922 | 0.0012262 | 0.0026877 | 0.0039073 | 0.0046493 | 0.0058859 | 0.0076475 | 0.009428 | 0.012865 | 0.014759 | 0.018659

## Slide 32: Example of proof test
No Proof Test
Pf = 0.73%
Failure Rate = 1 out of 137
10 sec Proof Test @ 4950 psi
Pf = 0.33%
Failure Rate = 1 out of 306
10 sec Proof Test @ 4950 psi
Pf = 0.47%
Failure Rate = 1 out of 214
The dome is subjected to a high pressure for a short time to decrease its probability of failure during service.
Blue line shows probably of failure during 10s proof test.
Red line shows probably of failure during 60-hour service life of proof-tested dome

## Slide 33: Reliability of chemically strengthened dome
Predicted reliability of strengthened dome is very high even without proof test.
Pf = probability of failure

## Slide 34: Proof testing
Domes were proof tested following the protocol determined by Eric Baker.
Pressure and axial displacement of glass port were logged. Displacement matched FEA prediction.
2 strengthened domes were tested to 3000 PSI.
1 strengthened dome was tested to 5000 PSI.
Notes: The photo shows the dome mounted on a test housing (the real camera housing is much longer), about to be lower in the pressure at the Navy’s pressure testing facility is Port Hueneme. A LVDT sensor was placed inside the housing to measure the axial displacement of the glass. Pressure was also measured and logged.

## Slide 35: Conclusion
After the failure of an early design, several steps were taken to improve the reliability of the glass port:
The edges and the base of the dome were polished, the flatness of the base was controlled.
The dome was bonded to a titanium ring to prevent hoop tensile stress from appearing.
Chemical strengthening greatly improved the strength of the glass.
Reliability was predicted using CARES software.
The camera housing can now be operated at 2000m with very low probability of failure, which exceed our goal.
Using this method, deep sea cameras are no longer limited to small hemispherical domes. Sub-hemispheres with large radii with better optical performance can be used and their reliability can be predicted.
More research is needed on life prediction for strengthened glass. The residual stress field should be incorporated into the model for a better prediction.