## Slide 1
Design and testing of a large sub-hemispherical glass port for a deep-sea camera
Francois Cazenave1; Eric H. Baker2
Nathan D. Card3; George D. Quinn4
Paul Remijan5; Jonathan Salem6
Arun K. Varshneya3
1. Monterey Bay Aquarium Research Institute, Moss Landing, CA
2. Connecticut Reserve Technologies, Gates Mills, OH
3. Saxon Glass technologies, Alfred, NY
4. National institute of Standard and Technology, Gaithersburg, MD
5. Fathom Imaging Inc., Brimfield, MA
6. NASA Glenn Research Center, Cleveland, OH

## Slide 2: Outline
  Optical design
  First structural design and failure
  Fractography
  Modified design
  Material testing
  Reliability analysis
  Chemical strengthening
  Proof testing

## Slide 3: Introduction
  MBARI operates an autonomous underwater vehicle to carry out video surveys in Monterey Bay from 50m to 1000m depth.
  A new camera system was designed with the goal of achieving the highest image quality and a depth rating of 1500m.
  A glass dome port was designed, built and tested.
Notes: The dome can be see in the front of the vehicle, protected by a black plastic shield.
The 4 appendages near the front are LED lights.

## Slide 4: Optical design
  Typical COTS dome port
  Shape is optimized to resist hydrostatic pressure
  Small diameter (<200mm)
  Hemispherical shape
  Even and easy to predict stress and strain.
  Poor optical performance
  BK-7 glass
  I2map dome port
  Shape is optimized for high optical quality
  Large diameter (250mm)
  Flattened hemispherical shape
  Uneven and hard to predict stress and strain.
  H-K9L glass (Chinese equivalent to BK-7)
Notes: A field curvature aberration decreases with larger optical surface radius.
Field curvature aberration is worse with large sensors
such that an image formed by a wide angle lens located behind the dome port is not focused on a flat surface, but rather focused onto a curved surface.
A camera image sensor is flat, so if the center of the image is focused at the center of the sensor, outer portions of the image will be focused behind the image sensor and become blurred.
Small diameter concentric dome ports with smaller optical surface radii produce a large field curvature aberration.
In addition, the field curvature aberration associated with a specific concentric port increases substantially as the size of image sensor is increased.
The “Corrector Group” has the additional feature of correcting port aberrations for any size image sensor.
could use any high resolution camera / sensor combination with field of view up to ~ 98 degrees, corner to corner

## Slide 5
Could use any high resolution camera / sensor combination with field of view up to ~ 98 degrees, corner to corner

## Slide 6: Early design of dome
Dome sits on kapton gasket
Dome is held with plastic retainer.
O-ring around dome

## Slide 7: FEA of early design: 2D Axisymmetric Model
External Pressure Load
8/2/16
Glass dome
Titanium support
BC: Radial = free, Axial = fixed
Kapton gasket
Dome is free to move Radially

## Slide 8: FEA results at 2750 PSI (19MPa)
Displacements
First principal (max tensile) Stress
11,090 psi
Maximum axial displacement 0.0134” (0.34mm)
Maximum first principal stress
11090 PSI (76.5MPa)
Notes: 2750PSI is the pressure at the rated depth (1500m) + 25%
25% is a safety margin that I chose somewhat arbitrarily at the time I started working on this.

## Slide 9: Failure of early design
Dome failed during external pressure test after numerous cycles to 2750 PSI (19MPa)
Notes: The second dome failed at much lower pressure because the dome support was modified in a way that made things even worse. It was a design mistake basically. We could omit the second dome altogether for the sake of clarity if needed.

## Slide 10
The broken dome was fractographically analyzed by G. Quinn
using a WILD stereo optical microscope with a digital camera.
The fractographic analysis included study of the
crack patterns and the fracture surfaces.
How to look
Patterns of breakage
What to look for and how to interpret it.

## Slide 11
George Quinn fractographer, performed an analysis of the broke dome.
There were 4 crack systems. All 4 had the same type origins and same stresses driving them.
Fractographic analysis
1
2
3
4

## Slide 12
All four origins were contact crack damage at the outer rim area.
Origin 4 was the first to start the overall fracture.
All flaws and initial crack propagation were driven by circumferential hoop tensile stresses.
By the time the cracks propagated towards the middle, the stress changed to bending with tension on the inner dome surface. This suggest that the external pressure caused “splaying” of the dome.
There were no fracture mirror boundary features, nor did any of the cracks branch.
Fractographic analysis
4
1
2
3

## Slide 13
2 views with different lighting at same magnification
The origin is a contact damage crack on the bottom ground surface.
It is about 1 mm in from the unbeveled edge.
Fractographic analysis
Example: One of the rim contact damage cracks
Fracture surface
Fracture surface
Dome ground base
Dome ground base
Inner dome surface
Inner dome surface
Notes: Summary of fractography: dome failed because of tensile hoop stress, and because of manufacturing defect.
George Quinn recommend that we hire Eric Baker to perform the reliability analysis

## Slide 14: Modified design
Dome was bonded to titanium ring with epoxy to prevent lateral motion of dome seat
Edges were beveled and polished
Seat was polished and flatness tolerance was decreased
Thicker kapton ring
Dome Support
Ti-6Al-4V
Dome Coupler Ring
Ti-6Al-4V

## Slide 15: FEA of Modified design
Axial displacement unchanged
Tensile stress reduced 30%
Axial displacement at 2750 PSI
Max = 0.013” (0.33mm)
First principal stress at 2750 PSI
Max = 7779 PSI (5.37MPa) (30% decrease)
Notes: There is a 30% decrease in tensile stress compared to the first design

## Slide 16
MBARI hired Eric Baker, ceramics reliability expert (CRT), to perform an analysis of the glass dome
MBARI hired Jon Salem, material scientist (NASA) to measure the mechanical properties of H-K9L glass and BK-7, and of chemically strengthened glass
MBARI hired Arun Varshneya (Saxon Glass Technology) to perform the chemical strengthening of the glass
External consultants

## Slide 17
Fracture strength, slow crack growth parameters and fracture toughness are needed for the reliability analysis but are not published by the manufacturers.
MBARI hired Jon Salem to measure these parameters for HK9-L (HK9-L is marketed as equal to BK-7 but is much cheaper) and BK-7.
Chemically strengthened HK9-L was also tested.
Material testing
ASTM C1499
Si
B
So
ASTM C1421

## Slide 18
Results: Comparison of plain and strengthened glass
Eta = Weibull Modulus
Beta = Characteristic strength
n = number of specimens
s = number of censored specimens
Notes: Strength distribution of plain and strengthened glass.
Strength more than doubled for strengthened glass.
BK7 was slightly stronger that HK9L

## Slide 19
Chemical Strengthening of glass
How it works:
Original surface
Surface in compression
Na+ (0.95 Å)
K+ (1.33 Å)
Submerge in a bath of molten KNO3
Ion Size
*Not drawn to scale, demonstration only
Notes: Bath of molten Potassium nitrate.
Exchange of ion between the glass and the salt solution
K potassium enter the glass and replace Sodium ion.

## Slide 20
C = concentration of the invading ion
H = plate width ; d = case-depth = DOL
E = Young’s modulus; n = Poisson’s ratio
B = linear network dilation coefficient ( = “Cooper Coefficient”)
In-plane stresses
The Math…
= CS
perpendicular stress

## Slide 21
Glass composition and physical properties
Type: H-K9L (similar to Schott BK7)
Nominal composition (wt%):
69.13 SiO2; 10.75 B2O3;3.07 CaO; 10.40 Na2O; 6.29 K2O; 0.36 As2O3
Density = 2.55 g/cm3
Tg = 550°C
TEC = 70x10-7/°C
E = 71.GPa
n = 0.219
nd = 1.523

## Slide 22
Four domes
15 witness disk samples 2” dia x 2 mm thick,
(for subsequent biaxial testing and CS/DOL measurement)
Hold domes in a stainless steel wire cage
Immerse in electrically heated steel tank containing molten KNO3 salt.
Ion exchange at 450 °C for 24 hrs.
After extraction, carefully cool, wash and dry.
Compression layer (case depth “DOL”) = 45 m.
Compression (“CS”) = - 430 MPa
(measured by FSM-6000LE)
Chemical strengthening of the domes

## Slide 23: Reliability analysis
MBARI hired Eric Baker of Connecticut Reserve Technology to perform brittle material reliability predictions on the camera port:
Generated finite element analyses of dome configurations and calibrated models to MBARI FEA as well as pressure test measurements
Estimated Weibull Material Properties from provided test data using WeibPar program
Applied the Ceramics Analysis and Reliability Evaluation of Structures (CARES) program to predict the brittle material reliability of the dome configurations
Established a proof test protocol to improve the reliability
This analysis was performed for unstrengthened and strengthened glass.

## Slide 24: CARES with ABAQUS Flowchart
CARES predicts the brittle material reliability of a component by post-processing finite element analysis stress results.
CARES requires region based Weibull material properties, Volume and/or Surface, where different Surface conditions are characterized by different parameter sets.
Notes: ABAQUS is FEA software.

## Slide 25: Material Properties: Weibull
WeibPar (Weibull parameter estimation program) is used for the WM and WCS calculations of the failure specimen data as well as calculating the Effective Area from a FEA of the R-o-R specimen
2D Axisymmetric Model of the Ring-on-Ring Specimen
m = 13.6 [-]
AE = 0.229 [in2]
σ̑­­θ= 22,714 [psi]
σ̑­­o = 20,386 [psi*in^(2/13.6)]
Ground Inert
Where m & σ̑­­o are used in CARES
Flaws were all assumed to originate on the Surface of the Failure Specimens
Weibull Characteristic Strength (σ̑­­θ)
Weibull Modulus (m)
Weibull Material Scale Parameter (σ̑­­o)
Weibull Effective Area (AE)
m = Weibull Modulus
σ̑­­θ = Weibull Characteristic Strength
AE = Weibull Effective Area
σ̑­­o = Weibull Material Scale Parameter

## Slide 26: Example of CARES output Unstrengthened H-K9L glass
Pressure: 2750 psi
Duration: 60 hrs
One Ground
Polished
Polished
Counterclockwise from Dome Inner to Dome Outer
Overall Reliability
Max Stress
Lowest Individual Surface Reliability
Notes: Numbers 201 to 207 represent the different surfaces of the domes (inside, outside, 3 edge beveled, base, and perimeter)

## Slide 27
Reliability as a Function of Service Pressure
where Service Time is 60 hrs.
FEA Stress Solution @ 2750 psi (19MPa)
Assumes Stresses Scale Linearly with Pressure
Assumes other parts of Assembly can handle the increased Applied Pressure
Reliability as a Function of Service Time
@ Applied Pressure 2750 psi
Example of CARES output Unstrengthened H-K9L glass
Chart: Pressure (psi)
| 550 | 1100 | 1650 | 2200 | 2750 | 3300 | 3849.9999999999995 | 4400 | 4950 | 5500 | 6050.0000000000009 | 6600 | 7150 | 7699.9999999999991 | 8250
All Polished | 1 | 0.99992 | 0.99941 | 0.9975 | 0.99235 | 0.98098 | 0.95917 | 0.92166 | 0.86287 | 0.7784 | 0.66728 | 0.53441 | 0.39177 | 0.2566 | 0.14598
Chart: Time (hrs)
| 2.7777777777777776E-7 | 2.7777777777777779E-6 | 2.7777777777777779E-5 | 2.7777777777777778E-4 | 2.7777777777777779E-3 | 2.7777777777777776E-2 | 0.27777777777777779 | 2.7777777777777777 | 8.3333333333333339 | 13.888888888888889 | 27.777777777777779 | 60 | 111.11111111111111 | 277.77777777777777 | 416.66666666666669 | 833.33333333333337
All Polished | 1.6352e-05 | 2.5935e-05 | 5.3427e-05 | 0.00011635 | 0.00025501 | 0.00055922 | 0.0012262 | 0.0026877 | 0.0039073 | 0.0046493 | 0.0058859 | 0.0076475 | 0.009428 | 0.012865 | 0.014759 | 0.018659

## Slide 28: Example of proof test
No Proof Test
Pf = 0.73%
Failure Rate = 1 out of 137
10 sec Proof Test @ 4950 psi
Pf = 0.33%
Failure Rate = 1 out of 306
10 sec Proof Test @ 4950 psi
Pf = 0.47%
Failure Rate = 1 out of 214
The dome is subjected to a high pressure for a short time to decrease its probability of failure during service.
Blue line shows probably of failure during 10s proof test.
Red line shows probably of failure during 60-hour service life of proof-tested dome

## Slide 29: Reliability of chemically strengthened dome
Predicted reliability of strengthened dome is very high even without proof test.
Pf = probability of failure

## Slide 30: Proof testing
Domes were proof tested following the protocol determined by Eric Baker.
Pressure and axial displacement of glass port were logged. Displacement matched FEA prediction.
2 strengthened domes were tested to 3000 PSI (20.7MPa).
1 strengthened dome was tested to 5000 PSI (34.5MPa).
Notes: The photo shows the dome mounted on a test housing (the real camera housing is much longer), about to be lower in the pressure at the Navy’s pressure testing facility is Port Hueneme. A LVDT sensor was placed inside the housing to measure the axial displacement of the glass. Pressure was also measured and logged.

## Slide 31
Dome port: $1500-$2000
Adapter lens set: $1200-$1500
Chemical strengthening: $4000 per batch
Mounting parts: $2500 materials, 3 weeks of machine shop time.
Cost of components

## Slide 32: Conclusion
After the failure of an early design, several steps were taken to improve the reliability of the glass port:
The edges and the base of the dome were polished, the flatness of the base was controlled.
The dome was bonded to a titanium ring to prevent hoop tensile stress from appearing.
Chemical strengthening greatly improved the strength of the glass.
Reliability was predicted using CARES software.
The camera housing can now be operated at 1500m with very low probability of failure.
Using this method, deep sea cameras are no longer limited to small hemispherical domes. Sub-hemispheres with large radii with better optical performance can be used and their reliability can be predicted.
More research is needed on life prediction for strengthened glass. The residual stress field should be incorporated into the model for a better prediction.

## Slide 33: Conclusion
MBARI owns what may be the highest quality deep sea optical system in existence.
The I2map dome can be operated at 2000m with very low probability of failure.
Deeper operation is possible, with some modifications.
It’s currently only used for one application (I2map). Let’s use it for other applications!