Talking Points – RP_Pressure Cases

· Added as Characterization of CAMTAG failure. (Pic’s and Sample)
· Ppt. table of failure pressures(3350psi test v.s. 1967psi. calc’d)
· Possible Build Direction differences (Horiz= X-Y, Vert.=Z).
· Definite Build Resolution differences (HD, UHD, XHD)
· Currently – Dogbone Tensile tests (6,121 psi. as advertized)
· Vertical UHD build 3,492 psi.
· Horizontal UHD build 4,343 psi.
· Horizontal XHD build 5,375 psi.
· Currently – Compression Test Coupons.
· Currently – building repeat test cases – test to failure
· Horiz. Build Dir. & Vert. Build Dir.
· Future - Build Double Size Cases (Same R/t ratio)
· [bookmark: _GoBack]Why?  H.S / College student with access to a “MakerBot” could produce pressure cases to experiment with.


