Prep:

-Clean SS insert and bonding surface with soapy water. Rinse parts multiple times with water(just water, no soap). Dry parts.

-Rough up outside surface of SS insert and also the bonding surface on endcap with sand paper or Dremel. If using a Dremel be very careful not got too deep, there is not much material behind the endcap insert hole;)

-Remove any debris. Clean SS insert and bonding surface with soapy water. Rinse parts multiple times with water(just water, no soap). Dry parts.

-Clean surfaces thoroughly with iso, dry parts with Kimwipe and then allow parts to air dry completely.

-Super glue spacer to SS insert and let glue dry.

Install:

-screw in a SS socket cap bolt for installation, be careful to not bottom out the bolt.

-apply 3M DP460NS epoxy to all surfaces of insert hole in endcap. Also apply 3M DP460NS epoxy to outside of SS insert.

-install insert assembly, during installation epoxy should push out of the hole around the edge of the insert.

-clean up any excess epoxy with qtips.

-use electrical tape to align and center the bolt/insert. Also make sure that the electrical tape applies some force to keep the insert pressed into the hole.

-using a multimeter, check to make sure SS installation screw is NOT in contact with endcap

-adjust tape as needed to isolate insert from endcap

-clean up any excess epoxy with qtips.

Insert isolation check (roughly 1 hour after install):

-using a multimeter, check to make sure SS installation screw is NOT in contact with endcap.

-adjust tape as needed to isolate insert from endcap.

Clean up (after 24 hrs)

-carefully remove electrical tape.

-carefully remove installation bolt.

-confirm that the insert is recessed or flush with the outside of the endcap so that the nose/tail shell goes on easily

-using a multimeter, check to make sure the SS insert is NOT in contact with endcap.

-using a razor blade carefully clean up any excess epoxy.