LRAUV Antenna Assembly Procedure

Rev4

- Parts required:               Devcon Flexane 94   Casting Polyurethane

  - Antenna PCB

  - (2) rigid coax cable

  - (2) Rigid coax cable SMA

- Attach SMA to two XX” long rigid coax, then solder to PCB.

- Craig: Electrical test with VNA

- Send to Schmidt Prototypes for encapsulation with clear urethane filled with milled fibers

- Craig: Electrical test with VNA

- Prep  and attach DGO/SMA cables as describe below:

  - Compressed air shall not be used for any operation described below.

  - De-grease LRAUV antenna potting cup and connectors with alcohol and lint free wipes.

  - Prepare LRAUV antenna potting cup internal surface and antenna cables by sanding the internal surface and edges with 80-100 grit sandpaper to promote urethane bonding. Be careful not to break through the p/u jacket of cables and use new sandpaper for each cable.

  - Wash the sanded surface with detergent and hot water, oven dry 100f overnight. (check the threads to insure that they are dry)

  - Do not touch the cleaned surfaces from this point on.

  - Apply Devcon Flexane FL-10 under fume hood

  - Air dry for a min of 60 minutes

  - Second primer coat, apply Devcon Flexane FL-20 under fume hood

  - Air dry for a min of 60 minutes

  - Install the RF cables and tighten SMA connectors with torque wrench to 7 inch/lbs (gloved hands, keep clean)

  - Craig: Check the SMA connectors for tightness. No touch clean surfaces!

  - Craig: Electrical test with VNA. No touch clean surfaces!

  - If any surface is touched even with gloved hands you must go to wash again from step 4.

  - If 2+ hrs have elapsed since Applying FL-20,  reapply, dry min 30 minutes

  - Position antenna cables in their final layback position

  - Mix 200 cc of polyurethane potting compound per instruction sheet in a large bucket that provides lots of surface area.

  - De-gas mixed urethane in vacuum chamber

  - Top off urethane to level fill

  - Place in pressure chamber to squeeze bubbles

- Pressure test to 500 psi cured assembly inside sealed bag filled with saltwater

- Craig: Electrical test with VNA

- Record final resistance and capacitance values in log and release assembly for installation and deployment