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Cell Description
The primary batteries used for future Coastal Profiler Floats (CPF) are comprised of 3B0036 High Rate DD Cell from Battery Specialties. This is their CSC93 series which has a Lithium Sulfuryl Chloride chemistry.  


	Chemistry
	Sulfuryl Chloride

	Construction
	Spiral

	Cell Size
	DD

	Length
	111.5 mm

	Diameter
	33.5 mm

	Cell Weight
	213.0 grams

	Lithium Weight
	9.9 grams

	Integrated Safety Fuse
	Yes


Table One: Physical characteristics of the 3B0036 cell.


	Cell Type
	Primary

	Open Circuit Voltage (25 degC)
	3.93V

	Nominal Voltage
	3.40V

	Nominal Capacity
	26Ah

	Maximum Continuous Current
	4000mA

	Operating Temperature
	-20 degC to +93 degC

	Self-Discharge Rate
	<3% per year

	Storage Temperature
	25 degC

	Discharge Condition
	1000mA @ 23 degC


Table Two: Electrical characteristics of the 3B0036 cell.


Battery Description
Each battery pack is comprised of four 3B0036 cells in series. This gives an open circuit voltage of ~15.72Vdc and a nominal output voltage of ~13.6Vdc. The MBARI drawing number (and part number) for these quad cell batteries is 100221761. Each battery has 16AWG, 300V Teflon insulated leads with a length of 18 inches. The four cells are spot welded to each other and have been shrink wrapped together.



Load Testing
A single four cell battery was load tested using an electronic dummy load. The dummy load was set in constant resistance mode with a value of 12.8 ohms. For safety reasons, the test was paused whenever I was not present in the room. As a result, the test was completed over six individual periods ranging from three to five hours each. This resulted in some real-world variance in the terminal voltage between testing periods. Integrating the area under the discharge curve found the cells to have a 26.9Ah capacity. Derating this value for the CPF’s operating depth due to decreased temperature translates to ~26Ah, the stated capacity. The temperature of the battery was recorded throughout the testing.




Figure One: Discharge curve of the four cell 3B0036 battery. The labeled data points (in blue) represent the voltage at the start of each separate testing period. The red data curve is the battery temperature in degrees Celsius.


Equipment Used
BK Precision 8500 Programmable DC Electronic Load
Fluke 87 Multimeter
Fluke 80TK Thermocouple Module




Constant Current Tests
A series of constant current tests were performed on a second, fresh battery. These were performed to capture the terminal voltage of the battery pack under differing load conditions. Table three displays the battery terminal voltages under six separate load conditions. 


	Discharge Rate (A)
	Vbatt
	Vcell

	0.004
	15.45
	3.86

	0.3
	14.43
	3.61

	1
	13.71
	3.43

	2
	13.20
	3.30

	3
	12.76
	3.19

	4
	12.33
	3.08


Table Three: Measured battery voltages at various load conditions.


Equipment Used
BK Precision 8500 Programmable DC Electronic Load


System Capacity
The total energy capacity of the CPF was calculated by piece meal integration of the discharge curve. This resulted in 359.1Wh (1.29MJ) for a single 4S battery. Doubling the voltages and rerunning the numbers gave 718.1Wh (2.59MJ) for a single 8S battery. Multiplying the 8S capacity by four gave 2872.5Wh (10.4MJ). This number corresponds to roughly the quick calculation using an average terminal voltage over the same period. 
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Discharge of a Quad Cell Battery (3B0036)
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