4k Deep ESP Sphere Strain gage sites:

There are locations on the top half of the sphere that did not make design shape during machining due to casting/annealing deformation.

These locations are as follows:
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Top Outside:
TOF-1: Flaw-1 outside strain; The “peninsula” cast surface area in the spherical shell section of the dome. 3.5x6” max 0.045” deep from spherical ideal.
TOF-2: Flaw-2 outside strain; a 2.5x4.5”, max 0.030” deep spot
TON: Top nominal spherical strain (About halfway up on sphere, away from all visible flaws.)
Top Inside:
TIF-1: Flaw-1 inside strain; inside surface directly underneath TOF-1

TIF-2: Flaw-2 inside strain; inside surface directly underneath TOF-2

TIN: Nominal spherical strain, inside surface directly underneath TON

Bottom Outside:

BON: Bottom outside nominal spherical strain (About halfway up on sphere.)
