ESP  GG  EM  CABLE  FABRICATION/TERMINATION                                                          2/1/12
\\Tornado\projectlibrary\ESP\TopLevelAssy\ShallowWaterMooring/EM Term March 09
This shallow water version started with a supplied cable cut to 16 meters, finished length to be about 15 meters.      Typically- Rochester Wireline   3/8” 7-H-375A.
Drawings and parts:  Connector Plate-100894,  Wire Centalizer-100895,  Connector Spacer-100896, EM Cable Termination housing- 100897 –Rev. B   DWG, Molded Silicon Wire Morrison Seal (molded here),  Bending Strain relief - PMI EVERFLEX #1).
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MATERIALS AND TOOLS

ESCO SocketFast Resin for wire rope socketing,  300gms BC Wire (usually case of 24) , 
( Alt.-CROSBY W416-7, 250cc)
Silastic J from Dow Corning or Smooth-Sil 950 from Smooth-On for Morrison seal molding

Seizing Wire, .025-0.035 dia.,  Galvanized and Annealed

0.50 “ Diameter  Heat shrink

Bead Blaster that has good control of stream

DMM to check for electrical isolation between housing and cable

Lineman’s, Round Nose and Needle nose pliers

Electrical Tape

6-32 socket head screws, 6 x 3/8” and 6 x  3 “,shorten to 2.9” and bevel  threaded  end
2-131 O’ring
Food grade Silicon spray Lube
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PRELIMINARIES:








Bore out Housings to 0.430 Diameter to clear cable .368” plus 1st layer of heat shrink insulation

Confirm or Fabricate locking grooves in cone area.  ¼”  x 0.1”  ~0.5”  below lip,  see photo
Clean grease etc. off inside of Housing

Chase 6-32 threads at inside bottom of Termination Body to confirm 0.6 depth, run screw or tap

Morrison Seal cut to  0.70”  length, See end of document for details.
Chamfer lead-in edge of Morrison Seal Cavity in Connector Block

MinK10FCR from Sea-Con,     sometimes long lead time.
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INITIAL  PROCEDURE:

Slide Strain Relief and Housing down cable

Apply 6- 10 wraps seizing wire about 20” down cable, make sure locking twist will be in coned section of Housing and not jammed in entrance area.

Slip a 3” piece of heat shrink down the cable,  shrink into place with upper end just covering the seizing.

Slip a ½” section down and shrink into position just covering the bump made by the seizing.  This becomes the seating point and extra electrical isolation (corrosion) for the Housing. See p.4 picture.
Wrap a few turns of electrical tape around the heat shrink then gently tighten a small worm clamp around the heat shrink at the seize wire location to temporarily protect it from damage while we are “brooming” the cable’s strength wires.

BROOMING PROCEDURE:

The max width of the spread out wires must be less than 1 ½” at the top.

Work methodically and carefully

Start with the outer layer, unraveling the strands, do not bend outward too much, hard to bend back to 1 ½”

Cut these off at about 4” to make it easier to handle and do the straightening process.

Reasonably straighten the outer larger wires avoiding kinks and nicks,  round nose pliers help
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Mark at  2.9” length from the bottom of the seizing (seating point in the cone)

Cut off at 2.9”, looping the top later will bring finished length to ~2 .7” so clears centralizing ring
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Leave the black covering on the Copper wires as protection for now











                Continue the Brooming with the thinner inner layer, be especially careful to not damage the wires
Use the same procedure, access to base is more difficult for straighting, OK if not perfect

Cut off at 2.9” and spread all wires somewhat evenly noting 1 1/2” dia. Max.

Carefully put a small loop (round nose) bringing tip back under slightly on all cable wires

Sand blast carefully, avoiding damage to Copper wires and Heat Shrink,  this will clean and abrade the cable wires for better resin adhesion. (Alt. procedure is to solvent clean and sand each one)

 Blow-out  and chase 6-32   threads to clean out grit  
Remove the black covering from the Cu wires down to ~ 1/2 ”  below the level of the loops.

The insulation over the wires is often rough and needs to be sanded relatively smooth in the area of the Morrison Seal.  Use 250 grit to smooth  the insulation 2-3 Inches above the broomed solid wires.

Separate and solvent clean the Copper wires, black in the middle.  NOTE twist direction.
This cleaned section and the loops will lock into the socketing resin

Now fit check the broomed ass’y ,  remove temp. clamp, check for about ¼”  clearance beneath centralizer mounting lip and no electrical contact of the cable to the alum housing, use a DVM
Adjust cable wires as req’d.  When potted,  loops must be covered and resin  still be below centralizer

Solvent clean all parts again, fingerprints, etc.  See images  below .
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p.6
Carefully slide the centralizer part way down the wire loom maintaining the sequence as they exit the covered portion.  This will make final connector wiring easier. Use a DVM,  clocking from red wire, one end will be clockwise, the other CCW to follow the twist direction.
Slide loom into the housing, recheck clearances and isolation, fix cable below the housing so is stabile.

Seal exit so resin will not leak out or foul threads of strain relief, electrical tape  work well

THE OTHER END

Repeat all the above making sure to slide strain relief and housing onto cable before starting brooming

POURING RESIN 
Get 6 x  6-32 x 3/8 screws, allen drive, gloves, ventilation on, and potting resin on hand
We won’t use much of the 250/300 grms, need to use whole thing since catalyst volume is pre-measured  for  the can-full.  Mix very thoroughly, scaping edges and bottom.   Total of ~110 CC.  
Thoroughly mix resin, scraping settled contents off bottom of can

Open catalyst and mix all of it into the can,  mix well, you have about 15 minutes working time.

Degas if sufficient working time available.
Avoiding the Copper wires, pour  mixed resin slowly so air bubbles leave and wires are fully covered.  Stop when about 1/8” below the level of the screw holes (bottom of centralizer)
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Slide centralizer into position, temporarily hold down with short 6-32’s

Quickly check for resin on wire insulation, clean off, this is the watertight seal area and must be smooth

Resin will set up in about an hour at RT, let sit several hours before moving however.

FINISHING THE WATERTIGHT SEALS

Check all remaining parts for cleanliness and burrs

Check Cu wires for rough spots and resin drops, clean as necessary

Spray with Silicon Lube all sides of wires
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Slide Morrison seal onto wires part way noting sequence , note photos
Coat Seal and Recess with Silicon Lube

Slide Wiring Cavity  onto wires noting sequence, respray wires and seal with silicon lube
Carefully aligning wires to holes, slide Morrison seal partway into cavity.  The lead-in chamfer will help.
Guide seal partway into cavity, then slide fully down to centralizer.  

Pulling wires taut in turn will eliminate possibility of  kinks as slide assembly down, check alignment again   to avoid damage to insulation as seal fully enters the cavity, 

2-131 oring will seal connector area, be careful with oring recess area on top of wiring cavity 
6-6-32 x 2.9” screws will do final seating/alignment of the Morrison seal,  be careful screws do not bottom out.

Ready for MinK connector wiring.
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Soldering to pins is in a very tight space.   Let Electronics techs do it.    

MORRISON SEAL FABRICATION
Clean all parts of mold and pins.

Assemble mold, insert pins, typically 0.062 for .056wires, smaller tan .070 need to be held in place with red molding compatible clay.  Green clay is incompatible.
Coat mold surfaces with suitable release agent,  silicon spray or Ease Release 200 from Smooth-On

Check mat’l for shelf life.  Use either Silastic J from Dow Corning (preferred due to Shore 56A) or Smooth-Sil 950, (Shore 50A) from Smooth-On. (SmoothSil shone.)
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Follow mixing instructions after carefully cleaning mix cups and strirers.  40 grams total  is plenty.

Mix thoroughly, degas 29”Hg for at least a minute, pour smoothly into mold avoiding bubbles.

Smooth-Sil 950 requires a post-cure of 80 deg. C for 2 hrs.  to guarantee a full cure.

You have about an hour of working time. Let cure overnight and do post-cure heat treatment  before demold. Pull pins first.

Cut off square ended cylinder 0.70 “ long.    
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