ESP E/M Cable Tear-down,  2/16/12    J.Scholfield      			2/28/12
In recovering a couple of the cone pieces, maybe more, of a well used E/M cable, I documented what I found as I disassembled the parts.  This was the B end. Wiring cavity looked dry with a slight amount of corrosion in the o’ring areas.  Note the darkened Cu wires (2) .
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I checked the wires 14” down the wire, only 1 was dark , same as very dark one above.  No shorts to housing.  3”x6-32 removed easily, aqua lube works.  
[image: C:\Users\scji\Pictures\mbari photos\ESP\Cone teardownFeb12\endB4.JPG]
[image: C:\Users\scji\Pictures\mbari photos\ESP\Cone teardownFeb12\endB5.JPG]
Plenty of water below Morrison as expected.   Still B end.








 Slight amount above where shouldn’t be. See below.
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FYI- wire hole diameters in installed Morrison approx. .058.  Cast as .070.
B end.
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Dark wire, 14” down.  Right of Red. 


[image: C:\Users\scji\Pictures\mbari photos\ESP\Cone teardownFeb12\endAgritty.JPG]
A end, “gritty” oring and land.   Sl. Corrosion in cavity.  3 of the 3” 6-32’s were frozen in, used Kroil to tease them out the next day.
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Big BSR  cable,  Dry!   3 of the long 6-32’s broke off, even after soak overnite in Kroil.  
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