              PRESSURE    TEST    RECORD

Test Date:  6/16/06
Item Description :  Small titanium housings for Benthic Rover Motor Controllers
Item S/N:  MC -1,  MC- 2
Tested For: MBARI at our own Pressure Test Facilities
Test Pressure:  8750
8750  psi / 1.5 S.F = 5833 psi    5833 / 1.487 psi/meter S.W. = 3923 meters water depth.
Gauge:  Autoclave  Pressure Transducer
Gauge S/N:  95104916
Calibration Date:  6/15/06 with a PSI-Tronixs digital gage calibrated by 


Precision Measurements  on 3/2/05,  Report # 1138295

Gauge Range:  0-15000 psi
The test articles were subjected to the implodable items alternative procedure stipulating 10 cycles to maximum allowed pressure.  A 1 minute hold at 0 and 8750 psi on cycles 
1-9 and a 60 minute hold at 8750 psi on the 10th cycle. 
Results:     No evidence of leaks or damage was noted.  
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