                                                                                                                           6/19/06
              PRESSURE    TEST    RECORD

Test Date:  6/8-9/06

Item Description :  18” Titanium Housings Benthic Rover/BIN Batteries and  Controller

Item S/N:  204T/303B; 301T/301B; 302T/302B
Tested For: MBARI Benthic Rover 
Test Pressure:  8750 PSI

8750 psi / 1.5 S.F = 5833 psi     5833 / 1.487 psi/meter S.W. = 3923 meters water depth.
Gauge:                         Tests performed at Port Hueneme Deep Ocean Simulation  



Facility by Mark Wells.  See attached report.
Gauge S/N:
Calibration Date:  

Gauge Range:  

The test articles were subjected to the implodable items alternative procedure stipulating 10 cycles to maximum allowed pressure.  A 1 minute hold at 0 and 8750 psi on cycles 
1-9 and a 60 minute hold at 8750 psi on the 10th cycle. 
 No evidence of leaks or damage was noted.  
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