Shrink Compensation Manual for ProJet Materials

Introduction:

Material shrinkage occurs in thermoplastics as they transition from liquid state to solid (change in density). In the case of photopolymers used in the Multi-Jet Modeling process, this shrinkage can occur during the curing stage of printing.

The ProJet Accelerator Client Software has features built in to allow a user to compensate for the natural shrinkage of the material and also fine tune the accuracy of a part.

The instructions below will explain the process for entering shrink compensation and fine tuning part accuracy using scaling factors.

SHRINK COMPENSATION VALUES FOR VISIJET MATERIALS

| Material | X value | Y value | Z value |
| --- | --- | --- | --- |
| SR200 | 1.01% | 1.01% | 0.00% |
| HR200 | 1.01% | 1.01% | 0.00% |
| EX200 | 1.02 | 0.75 | 0.00 |
| MX | 0.60 | 0.60 | 0.00 |
| DP200 | 1.01% | 1.01% | 0.00% |
| MP200 | 1.02 | 0.75 | 0.00 |

- Enter Standard Shrink Compensation Values for the material

• Open ProJet Accelerator Client software and select the desired printer.

• Select the model to print

• Select the “Options…” button as indicated below:

Within the Options panel, enter shrink compensations values for X or Y. Z compensation is rarely necessary.  SEE TABLE ABOVE FOR SHRINK COMP VALUES FOR THE MATERIAL BEING USED.

- Identify the exact X and Y dimensions of the part using a CAD program.

- Most CAD programs and simple stl file viewers will provide a way to view a part with its dimensions.

- Make note of the actual X and Y dimensions as XCAD and YCAD.

- Build and clean the part and take measurements of the finished part.

- It is recommended to measure along the critical dimensions of the geometry, take measurements in multiple areas and take an average of the values.

- Measurements can be made using calipers or more advanced metrology methods.

- Make note of the X and Y dimensions of the printed part and mark them as XPART and YPART

If the measurement of the finished part is different from the measurements of the CAD model, fine tune the accuracy using scaling factors.

- Determine “Scaling Factor” to use for the next build

- Use the following formula calculate the scaling percentage to be used on the “fine tuning” build:

X Scaling Factor = (XCAD  -  XPART)/ XCAD * 100 (answer will be as a percentage)

Y Scaling Factor = (YCAD  -  YPART)/ YCAD * 100 (answer will be as a percentage)

EXAMPLE:

X measurement of CAD model = 3.000”

Y measurement of CAD model  = 5.000”

X measurement of printed part = 2.998”

Y measurement of printed part  = 4.989”

X Scaling Factor = (3.000 – 2.998)/3.000 *100 = 0.067%

Y Scaling Factor = (5.000 – 4.989)/5.000 * 100 = 0.22%

- Enter “Scaling Factor” for adjustment build

- Open ProJet Accelerator Client software and select the desired printer.

- Select the model to print

• Open Print Preview to view the model. Select the model (color should be yellow)

- Select the “Scale” Icon  and enter the dialog box to enter the above scaling factors.

- Uncheck the “Isometric Scale” button. This allows user to make individual x and y adjustments.

- In the example above the x scaling factor should be 100% + 0.067% = 100.067%

- The y scaling factor should be 100% + 0.22% = 100.22%

- Enter these two numbers in the corresponding scaling boxes for x and y.

- Build Part with Scaling Factors and measure

  - Additional iterations of adjusting scaling factors and taking measurements may be necessary with certain geometries.