AUX-CIR_10020119 SPECIFICATION READ-ME
File Name:  AUR-CIR_10020119.MAX
QTY: 10



Turn Time: 3 Days 

Layers: 2 

Layer Orientation:


1: TOP


2: GND

Thickness:  0.062 "" FR4 

Dimensions: 2.5" x 3.5" 

Plating: SMOBC (HASL)
Cu Weight: 2oz on ALL LAYERS. 

Trace width/space: >(0.010”/0.010”)
Smallest hole size: 0.010"
Drill Tolerance: +/- 0.003” Finished hole 

Sides to solder mask: Both Sides (RED)

Sides to silk screen:  Both Sides (WHITE) 

IPC-356 included for test (AUX-CIR_10020119.net)
